+ Supplementary Material (B): Raw dataset for the model development of DtMG catalysts and systems.

Table B1. Compilation of the experimental dataset for the establishment of various ML models of the DtMG catalysts.												Page S1-S25

Table B2. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 99.83. 			Page S26-S74

Table B3. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 130.01. 			Page S75-S119

Table B4. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 247.87. 			Page S120-S164

Table B5. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 377.48. 			Page S165-S207

Table B6. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 477.29. 			Page S208-S249

Table B1. Compilation of the experimental dataset for the establishment of various ML models of the DtMG catalysts.

| V1 | Rcov1 | Ea1 | IE1 | λ1 | C1 | V2 | Rcov2 | Ea2 | IE2 | λ2 | C2 | CR | TC | TR | P | H | W | CDMO | SMG |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 14 | 130 | 0 | 737.7 | 156 | 4 | ZnO | 673 | 493 | 2.5 | 100 | 2 | 100 | 97.31 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 4.6 | 82 | 26.7 | 800.6 | 27 | 5 | SiO2 | 773 | 453 | 0.5 | 150 | 0.2 | 98.9 | 96.13 |
| 10.2 | 144 | 222.8 | 890.1 | 317 | 8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.75 | SBA-15 | 773 | 418 | 3 | 100 | 0.6 | 97.2 | 96.13 |
| 10.2 | 144 | 222.8 | 890.1 | 317 | 8 | 10.3 | 153 | 125.6 | 731 | 429 | 1.5 | SBA-15 | 773 | 418 | 3 | 100 | 0.6 | 99.5 | 93.73 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 10 | 118 | 42.5 | 577.5 | 237 | 4 | ZnO | 673 | 493 | 2.5 | 100 | 2 | 99.74 | 93.12 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 1.75 | 98.52 | 92.89 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.2 | 100 | 92.42 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.25 | 96.1 | 92.35 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.78 | 10.3 | 153 | 125.6 | 731 | 429 | 2.82 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 97.17 | 92.28 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.25 | 100 | 91.99 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.3 | 100 | 91.5 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 478 | 2.5 | 300 | 0.3 | 95.48 | 91.36 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 1 | 96.83 | 91.26 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 1.5 | 97.51 | 91.25 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.35 | 100 | 91.12 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.3 | 94.86 | 90.82 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 1.5 | 96.37 | 90.72 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.4 | 100 | 90.69 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 488 | 2.5 | 300 | 0.3 | 94.88 | 90.62 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 493 | 2.5 | 300 | 0.25 | 96.1 | 90.58 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 1 | 97.6 | 90.57 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 1.25 | 97.93 | 90.26 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 493 | 2.5 | 300 | 0.3 | 94.63 | 89.89 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.45 | 99.89 | 89.88 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 473 | 2.5 | 300 | 0.25 | 95.71 | 89.78 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 1 | 99.77 | 89.72 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.87 | 10.3 | 153 | 125.6 | 731 | 429 | 1.98 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 98.27 | 89.47 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 503 | 2.5 | 300 | 0.25 | 96.25 | 89.41 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 513 | 2.5 | 300 | 0.25 | 96.95 | 89.39 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 468 | 2.5 | 300 | 0.3 | 93.25 | 89.35 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.5 | 99.95 | 89.24 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 498 | 2.5 | 300 | 0.3 | 94.29 | 89.14 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 1.5 | 99.89 | 89.06 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 503 | 2.5 | 300 | 0.3 | 94.78 | 88.99 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 473 | 2.5 | 300 | 0.3 | 93.08 | 88.73 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.225 | 96.46 | 88.69 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 1.25 | 98.32 | 88.46 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.55 | 99.78 | 88.28 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 1.75 | 90.73 | 87.84 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 478 | 2.5 | 300 | 0.25 | 94.57 | 87.77 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.2 | 95.83 | 87.77 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 1.75 | 89.84 | 87.71 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 2 | 91.5 | 87.66 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 508 | 2.5 | 300 | 0.3 | 94.04 | 87.61 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 488 | 2.5 | 300 | 0.25 | 94.09 | 87.48 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 513 | 2.5 | 300 | 0.3 | 94.39 | 87.45 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 463 | 2.5 | 300 | 0.3 | 91.22 | 87.33 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.6 | 99.62 | 87.33 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.175 | 95.81 | 86.86 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 463 | 2.5 | 300 | 0.25 | 93.39 | 86.54 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 350 | 0.25 | 88.89 | 86.29 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.65 | 99.24 | 86.02 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 1 | 99.99 | 85.94 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 460.5 | 2 | 100 | 1 | 95.55 | 85.44 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.15 | 94.1 | 85.24 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 518 | 2.5 | 300 | 0.3 | 95.58 | 85.17 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 468 | 2.5 | 300 | 0.25 | 93.77 | 85.08 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 400 | 0.25 | 89.12 | 85.07 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 2.25 | 86.49 | 84.79 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 463 | 2 | 100 | 1 | 99.56 | 84.78 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 1.25 | 99.9 | 84.59 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.7 | 98.81 | 84.58 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 498 | 2.5 | 300 | 0.25 | 92.33 | 84.21 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.125 | 95.01 | 84.15 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 523 | 2.5 | 300 | 0.25 | 97.18 | 83.79 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 14.1 | 148 | 41.1 | 640.1 | 22.7 | 4 | ZnO | 673 | 493 | 2.5 | 100 | 2 | 96.53 | 83.5 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.75 | 98.43 | 83.35 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.99 | 10.3 | 153 | 125.6 | 731 | 429 | 1.39 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 98.74 | 83.06 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.46 | 38.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 70 | 0.02 | 94.38 | 82.8 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 1.25 | 85.31 | 82.73 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.1 | 94.68 | 82.41 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.15 | 7.235 | 5 | None | 773 | 483 | 3 | 300 | 0.1 | 93 | 81.84 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.8 | 97.94 | 81.77 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 508 | 2.5 | 300 | 0.25 | 91.05 | 81.74 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.16 | 8.235 | 5 | None | 773 | 493 | 3 | 300 | 0.1 | 97.3 | 81.73 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 465.5 | 2 | 100 | 1 | 99.85 | 81.48 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 503 | 2.5 | 300 | 0.3 | 87.28 | 81.29 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.4 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 523 | 2.5 | 300 | 0.3 | 94.39 | 81.18 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 0.75 | 98.32 | 80.92 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 498 | 2.5 | 300 | 0.3 | 86.82 | 80.79 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 2.5 | 81.63 | 80.72 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 250 | 0.25 | 87.65 | 80.48 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 508 | 2.5 | 300 | 0.3 | 88.23 | 80.43 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 488 | 2.5 | 300 | 0.3 | 85.23 | 80.35 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 493 | 2.5 | 300 | 0.3 | 85.5 | 80.34 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 518 | 2.5 | 300 | 0.3 | 92.23 | 80.3 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.75 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.05 | SBA-15 | 693 | 473 | 3 | 80 | 1 | 82.9 | 79.83 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 1 | 99.66 | 79.49 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 513 | 2.5 | 300 | 0.3 | 88.67 | 79.24 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.275 | 95.01 | 78.94 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.47 | 39.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 70 | 0.04 | 87.29 | 78.67 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 523 | 2.5 | 300 | 0.3 | 92.69 | 78.63 |
| 10.2 | 144 | 222.8 | 890.1 | 317 | 8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.5 | SBA-15 | 773 | 418 | 3 | 100 | 0.6 | 78.4 | 78.32 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 468 | 2 | 100 | 1 | 99.63 | 77.69 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 518 | 2.5 | 300 | 0.25 | 90.1 | 77.58 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 478 | 2.5 | 300 | 0.3 | 81.89 | 77.48 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 450 | 0.25 | 82.65 | 77.42 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.85 | 96.59 | 77.35 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.3 | 81.95 | 77.22 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 0.6 | 99.24 | 76.82 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 4.6 | 82 | 26.7 | 800.6 | 27 | 5 | SiO2 | 773 | 448 | 0.5 | 150 | 0.2 | 78.5 | 76.54 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 1.5 | 76.87 | 76.45 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 473 | 2.5 | 300 | 0.3 | 80.79 | 76.41 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 493 | 2.5 | 300 | 0.3 | 82.1 | 76.3 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 498 | 2.5 | 300 | 0.3 | 82.71 | 76.19 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 97.74 | 76.02 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.17 | 9.235 | 5 | None | 773 | 503 | 3 | 300 | 0.1 | 100 | 76 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 45 | 0.8 | 84.64 | 75.85 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 508 | 2.5 | 300 | 0.3 | 84.43 | 75.75 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 1.5 | 79.74 | 75.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 488 | 2.5 | 300 | 0.3 | 80.93 | 75.66 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.14 | 6.235 | 5 | None | 773 | 473 | 3 | 300 | 0.1 | 84.2 | 75.53 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.3 | 80.78 | 75.51 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 513 | 2.5 | 300 | 0.3 | 85.5 | 75.46 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 500 | 0.25 | 83.16 | 75.45 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 200 | 0.25 | 87.49 | 75.44 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.87 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.28 | SBA-15 | 693 | 473 | 3 | 80 | 1 | 77.9 | 75.33 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 503 | 2.5 | 300 | 0.3 | 82.41 | 75.28 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 4.6 | 82 | 26.7 | 800.6 | 27 | 6 | SiO2 | 773 | 423 | 0.5 | 150 | 0.2 | 75.9 | 75.14 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 0.75 | 99 | 75.1 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 468 | 2.5 | 300 | 0.3 | 79.04 | 75.03 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 25 | 0.8 | 87.38 | 74.94 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.25 | 300 | 0.25 | 83.39 | 74.79 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 518 | 2.5 | 300 | 0.3 | 86.77 | 74.7 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.48 | 40.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 70 | 0.06 | 82.45 | 74.16 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 458 | 2 | 100 | 1 | 80.45 | 74.12 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 2.75 | 74.16 | 74.1 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 479 | 2.5 | 300 | 0.3 | 78.88 | 73.93 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 0.5 | 99.89 | 73.37 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.9 | 95.67 | 73.29 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 468 | 3 | 80 | 0.6 | 84.77 | 73.14 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 2 | 73.7 | 73.13 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 523 | 2.5 | 300 | 0.3 | 86.82 | 72.82 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.75 | 300 | 0.25 | 88.29 | 72.24 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 470.5 | 2 | 100 | 1 | 99.56 | 71.77 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.10 | 2.235 | 5 | TiO2 | 773 | 503 | 3 | 300 | 0.1 | 81.6 | 71.64 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 473 | 2.5 | 300 | 0.3 | 76.07 | 71.42 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 1.75 | 30 | 0.8 | 84.05 | 71.41 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.18 | 10.235 | 5 | None | 773 | 503 | 4 | 300 | 0.1 | 100 | 71.2 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.8 | 85.1 | 71.06 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2 | 300 | 0.25 | 83.12 | 71.05 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 19.7 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 463 | 2.5 | 300 | 0.3 | 74.68 | 70.78 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 0.75 | 99 | 70.6 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 78.12 | 70.56 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 503 | 2.5 | 200 | 0.257 | 94.51 | 70.5 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 2 | 70.63 | 70.32 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.3 | 92.59 | 70.29 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.8 | 84.81 | 70.04 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2.25 | 30 | 0.8 | 86.16 | 69.94 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 468 | 2.5 | 300 | 0.3 | 74.42 | 69.93 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.8 | 83.36 | 69.86 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.9 | 82.38 | 69.56 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 4.6 | 82 | 26.7 | 800.6 | 27 | 2 | SiO2 | 773 | 423 | 0.5 | 150 | 0.2 | 69.8 | 69.52 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 0.95 | 94.48 | 68.96 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 1.5 | 30 | 0.8 | 81.34 | 68.84 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.11 | 3.235 | 5 | TiO2 | 773 | 513 | 3 | 300 | 0.1 | 82.3 | 68.8 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 1.1 | 79.77 | 68.47 |
| 10.2 | 144 | 222.8 | 890.1 | 317 | 8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.5 | SBA-15 | 773 | 508 | 3 | 100 | 0.6 | 99.9 | 68.33 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.7 | 84.28 | 68.22 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 0.75 | 100 | 68.11 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.8 | 82.28 | 67.7 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 1 | 79.48 | 67.24 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 478 | 3 | 80 | 0.6 | 99.81 | 67.16 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 498 | 2 | 30 | 0.8 | 81.78 | 66.95 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.49 | 41.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 70 | 0.12 | 74.96 | 66.92 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.78 | 10.3 | 153 | 125.6 | 731 | 429 | 2.82 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 96.97 | 66.66 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 3 | 66.89 | 66.6 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 508 | 2 | 30 | 0.8 | 86.3 | 66.31 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 463 | 3 | 80 | 0.6 | 69.29 | 66.3 |
| 10.2 | 144 | 222.8 | 890.1 | 317 | 8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.75 | SBA-15 | 773 | 508 | 3 | 100 | 0.6 | 99.9 | 66.23 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 2.25 | 66.27 | 66.22 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 1.25 | 30 | 0.8 | 77.2 | 65.98 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2.5 | 30 | 0.8 | 86.15 | 65.79 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 473 | 2 | 100 | 1 | 99.73 | 65.66 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.8 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 463 | 2.5 | 300 | 0.3 | 69.73 | 65.57 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 503 | 2 | 100 | 1 | 81.95 | 65.36 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 3 | 300 | 0.25 | 91.87 | 65.2 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 498 | 2.5 | 200 | 0.257 | 81.37 | 65.1 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 1.2 | 75.92 | 64.98 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.1 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.25 | 98.3 | 64.88 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 1.75 | 64.99 | 64.7 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.12 | 4.235 | 5 | TiO2 | 773 | 533 | 3 | 300 | 0.1 | 87.3 | 64.51 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.87 | 10.3 | 153 | 125.6 | 731 | 429 | 1.98 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 98.09 | 64.45 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 20 | 0.8 | 75.19 | 64.28 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.14 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.98 | SiO2 | 873 | 673 | 2.5 | 120 | 1 | 93.29 | 64.2 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.6 | 84.12 | 64.15 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.19 | 11.235 | 5 | None | 773 | 503 | 5 | 300 | 0.1 | 100 | 64.1 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 1.3 | 73.46 | 63.7 |
| 10.2 | 144 | 222.8 | 890.1 | 317 | 8 | 10.3 | 153 | 125.6 | 731 | 429 | 4.5 | SBA-15 | 773 | 418 | 3 | 100 | 0.6 | 63.6 | 63.28 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.5 | 85.33 | 63.11 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.50 | 42.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 70 | 0.18 | 69.85 | 62.95 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 493 | 2.5 | 200 | 0.257 | 73.06 | 62.8 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 500.5 | 2 | 100 | 1 | 75.94 | 62.42 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 508 | 2.5 | 200 | 0.257 | 96.17 | 62.35 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 0.5 | 99 | 62.09 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.42 | 34.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 220 | 0.28 | 68.79 | 62.08 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 2.25 | 62.13 | 62.03 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 2 | 61.9 | 61.83 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 40 | 0.8 | 87.84 | 61.81 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.22 | 14.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 70 | 0.28 | 67.69 | 61.7 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.51 | 43.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 70 | 0.58 | 67.92 | 61.6 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 150 | 0.25 | 78.86 | 61.58 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.33 | 25.235 | 2.25 | SiO2 | 723 | 573 | 2.5 | 70 | 0.28 | 74.2 | 61.53 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 488 | 2.5 | 200 | 0.257 | 70.56 | 61.41 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 513 | 2 | 30 | 0.8 | 87.23 | 61.31 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 493 | 2 | 30 | 0.8 | 76.57 | 61.08 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.8 | 22.5 | 169 | 48 | 538.1 | 13.5 | 2.5 | SiO2 | 623 | 453 | 3 | 80 | 1.5 | 79.5 | 60.98 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.32 | 24.235 | 2.25 | SiO2 | 723 | 563 | 2.5 | 70 | 0.28 | 69.4 | 60.51 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 483 | 2.5 | 200 | 0.257 | 68.23 | 60.49 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 27.1 | 10.3 | 153 | 125.6 | 731 | 429 | 2 | SiO2 | 773 | 473 | 2 | 100 | 1.8 | 83.68 | 60.43 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 443 | 2 | 50 | 0.2 | 80.37 | 60.43 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 473 | 2.5 | 200 | 0.257 | 63.08 | 60.18 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 478 | 2.5 | 200 | 0.257 | 65.41 | 60.09 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2.75 | 30 | 0.8 | 87.25 | 60.04 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 2 | 62.27 | 59.84 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.43 | 35.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 240 | 0.28 | 69.5 | 59.76 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 505.5 | 2 | 100 | 1 | 89.06 | 59.7 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 1 | 30 | 0.8 | 69.25 | 59.49 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.41 | 33.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 200 | 0.28 | 67.73 | 59.45 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.45 | 37.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 300 | 0.28 | 69.15 | 59.22 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.31 | 23.235 | 2.25 | SiO2 | 723 | 553 | 2.5 | 70 | 0.28 | 64.77 | 59.01 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 3.7 | 9.1 | 128 | 205.3 | 870 | 71.6 | 2.2 | SBA-15 | 773 | 463 | 3 | 80 | 0.6 | 78.5 | 58.88 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 2.5 | 58.96 | 58.64 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.40 | 32.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 160 | 0.28 | 64.18 | 58.6 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 453 | 2.4 | 60 | 0.5 | 63.75 | 58.59 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.31 | 10.3 | 153 | 125.6 | 731 | 429 | 0.29 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 97.96 | 58.53 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 498 | 2 | 100 | 1 | 68.54 | 57.84 |
| 10.3 | 153 | 125.6 | 731 | 429 | 12 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 773 | 423 | 0.5 | 150 | 0.2 | 57.9 | 57.78 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.4 | 76.44 | 57.69 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 2.25 | 57.5 | 57.32 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 475.5 | 2 | 100 | 1 | 99.56 | 57.27 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.44 | 36.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 280 | 0.28 | 67.2 | 57.07 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.57 | KCC-1 | 673 | 473 | 3 | 100 | 0.5 | 99.77 | 56.95 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 1.4 | 65.6 | 56.67 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 483 | 3 | 80 | 0.6 | 100 | 56.6 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 0.75 | 30 | 0.8 | 65.11 | 56.52 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 30 | 0.4 | 84.94 | 56.42 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.20 | 12.235 | 5 | None | 773 | 503 | 6 | 300 | 0.1 | 100 | 56.3 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.3 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 1.18 | KCC-1 | 673 | 473 | 3 | 100 | 0.5 | 99 | 56.26 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.5 | 70.67 | 56.14 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 100 | 0.25 | 78.7 | 56 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.9 | 1.235 | 5 | TiO2 | 773 | 493 | 3 | 300 | 0.1 | 62.8 | 55.77 |
| 7.1 | 125 | 15.7 | 762.5 | 80.2 | 5 | 10.2 | 144 | 222.8 | 890.1 | 317 | 5 | ZrO2 | 673 | 513 | 2.5 | 200 | 0.257 | 99.99 | 55.67 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.6 | 67.7 | 55.41 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.39 | 31.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 140 | 0.28 | 61.7 | 55.02 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.2 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.25 | 98.1 | 54.35 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 773 | 423 | 0.5 | 150 | 0.2 | 54.4 | 54.29 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 488 | 2 | 30 | 0.8 | 71.18 | 54.13 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.23 | 15.235 | 3.6 | SiO2 | 723 | 513 | 2.5 | 70 | 0.28 | 61.15 | 54.09 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.2 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 0.79 | KCC-1 | 673 | 473 | 3 | 100 | 2.5 | 53.74 | 53.56 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 3.25 | 300 | 0.25 | 85.49 | 53.35 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 27.6 | 10.3 | 153 | 125.6 | 731 | 429 | 1.7 | SiO2 | 773 | 473 | 2 | 100 | 1.8 | 87.24 | 53.13 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10.1 | 10.6 | 136 | 7.6 | 658.8 | 21.9 | 2.33 | KCC-1 | 673 | 473 | 3 | 100 | 2.5 | 52.95 | 52.83 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.3 | 79.26 | 52.67 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.30 | 22.235 | 2.25 | SiO2 | 723 | 543 | 2.5 | 70 | 0.28 | 58.9 | 52.19 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 26.4 | 10.3 | 153 | 125.6 | 731 | 429 | 2.3 | SiO2 | 773 | 473 | 2 | 100 | 1.8 | 80.15 | 51.92 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.12 | 10.3 | 153 | 125.6 | 731 | 429 | 0.83 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 99.06 | 51.71 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.38 | 30.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 120 | 0.28 | 56.91 | 51.56 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.21 | 13.235 | 2 | SiO2 | 723 | 513 | 2.5 | 70 | 0.28 | 57.88 | 51.43 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 2.5 | 52.16 | 51.38 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 518 | 2 | 30 | 0.8 | 87.97 | 51.35 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 443 | 3 | 80 | 0.6 | 91.5 | 51.28 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.76 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.16 | SBA-15 | 693 | 473 | 3 | 80 | 1 | 52.1 | 51.21 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 10 | 0.8 | 57.05 | 51 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 15 | 0.8 | 66.05 | 50.67 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 50 | 0.8 | 91.31 | 50.67 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.2 | 10.3 | 153 | 125.6 | 731 | 429 | 0.5 | SiO2 | 773 | 473 | 2 | 100 | 1.8 | 92.73 | 50.63 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.13 | 5.235 | 5 | TiO2 | 773 | 553 | 3 | 300 | 0.1 | 98.4 | 50.18 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.52 | 44.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 70 | 0.7 | 54.68 | 49.84 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 2 | 35 | 0.8 | 79.26 | 49.78 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 458 | 3 | 80 | 0.6 | 51.88 | 49.34 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.3 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 3.5 | 300 | 0.25 | 87.72 | 49.32 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 0.9 | SBA-15 | 873 | 453 | 3 | 80 | 0.6 | 84.7 | 49.3 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 623 | 453 | 3 | 80 | 3.5 | 69.18 | 49.23 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.37 | 29.235 | 2.25 | SiO2 | 723 | 513 | 2.5 | 100 | 0.28 | 54.61 | 49.19 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 3 | 30 | 0.8 | 87.01 | 49.08 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 443 | 2 | 50 | 0.2 | 60.49 | 49.03 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 508 | 2 | 100 | 1 | 97.56 | 47.59 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 533 | 2.4 | 60 | 0.5 | 100 | 46.98 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 483 | 2 | 30 | 0.8 | 64.31 | 46.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 478 | 2 | 100 | 1 | 99.65 | 46.58 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.29 | 21.235 | 2.25 | SiO2 | 723 | 533 | 2.5 | 70 | 0.28 | 53.56 | 46.51 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 503 | 0.5 | 30 | 0.8 | 53.67 | 46.48 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 488 | 3 | 80 | 0.6 | 100 | 46.24 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.24 | 16.235 | 6.3 | SiO2 | 723 | 513 | 2.5 | 70 | 0.28 | 51.35 | 46.12 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.2 | 82.81 | 45.22 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.20 | 12.235 | 1.34 | SiO2 | 723 | 513 | 2.5 | 70 | 0.28 | 49.81 | 45.21 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.99 | 10.3 | 153 | 125.6 | 731 | 429 | 1.39 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 98.88 | 44.32 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 493 | 2 | 100 | 1 | 50.98 | 44.27 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 3 | 43.8 | 43.36 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 46.7 | 43.21 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.28 | 20.235 | 2.25 | SiO2 | 723 | 523 | 2.5 | 70 | 0.28 | 46.98 | 42.47 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 463 | 2.4 | 60 | 0.5 | 72.66 | 42.25 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 433 | 2 | 50 | 0.2 | 48.29 | 41.71 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.36 | 28.235 | 2.25 | SiO2 | 723 | 513 | 4 | 70 | 0.28 | 45.89 | 41.09 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 523 | 2 | 30 | 0.8 | 88.19 | 40.44 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 4.6 | 82 | 26.7 | 800.6 | 27 | 5 | SiO2 | 773 | 443 | 0.5 | 150 | 0.2 | 41.2 | 40.25 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 4 | 9.1 | 128 | 205.3 | 870 | 71.6 | 1.9 | SBA-15 | 773 | 463 | 3 | 80 | 0.6 | 94.4 | 39.84 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.34 | 26.235 | 2.25 | SiO2 | 723 | 513 | 3 | 70 | 0.28 | 44.52 | 39.79 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.6 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.07 | SiO2 | 623 | 453 | 3 | 80 | 1.5 | 97.4 | 38.47 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 3.5 | 38.07 | 38 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.35 | 27.235 | 2.25 | SiO2 | 723 | 513 | 3.5 | 70 | 0.28 | 42.81 | 37.97 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 623 | 453 | 3 | 80 | 3 | 73.86 | 37.55 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 478 | 2 | 30 | 0.8 | 54.93 | 36.82 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 6 | 95.58 | 36.8 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 100 | 35.59 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 100 | 35.53 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 493 | 3 | 80 | 0.6 | 99.75 | 35.44 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 58 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 80 | 5 | 56.1 | 35.4 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 453 | 2 | 50 | 0.2 | 90.2 | 35.27 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 510.5 | 2 | 100 | 1 | 97.97 | 34.59 |
| 6.6 | 121 | 112 | 737.1 | 90.7 | 8 | 17 | 106 | 72 | 1011.8 | 0.235 | 5 | TiO2 | 773 | 473 | 3 | 300 | 0.1 | 38.2 | 34.57 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 488 | 2 | 100 | 1 | 40.31 | 34.52 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.2 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.92 | SiO2 | 623 | 453 | 3 | 80 | 1.5 | 96.6 | 32.65 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 480.5 | 2 | 100 | 1 | 99.44 | 32.18 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 483 | 2.5 | 200 | 0.257 | 73.82 | 32.08 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.6 | 68.89 | 31.96 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28.1 | 10.3 | 153 | 125.6 | 731 | 429 | 0.4 | Ni-foam | 573 | 483 | 2.5 | 300 | 0.25 | 90.6 | 31.89 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 4 | 31.93 | 31.87 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 453 | 3 | 80 | 0.6 | 33.25 | 31.56 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 623 | 453 | 3 | 80 | 2.5 | 82.81 | 30.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 723 | 453 | 3 | 80 | 1.5 | 96.9 | 30.23 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.27 | 19.235 | 2.25 | SiO2 | 723 | 503 | 2.5 | 70 | 0.28 | 32.74 | 30.18 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.5 | 70.22 | 30.1 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 4.5 | 30.02 | 29.96 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | SiO2 | 723 | 473 | 2 | 30 | 0.8 | 47.89 | 29.93 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 5.7 | 96.01 | 29.3 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 498 | 3 | 80 | 0.6 | 100 | 28.95 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.1 | 9.1 | 128 | 205.3 | 870 | 71.6 | 0.8 | SBA-15 | 773 | 463 | 3 | 80 | 0.6 | 99.5 | 28.95 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.25 | 17.235 | 20 | SiO2 | 723 | 513 | 2.5 | 70 | 0.28 | 34.04 | 28.93 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 523 | 2.4 | 60 | 0.5 | 99.69 | 28.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.4 | 74.96 | 28.6 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 5 | 28.23 | 28.17 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.2 | 73.78 | 28.11 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.1 | 85.93 | 27.86 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 433 | 2 | 50 | 0.2 | 30.12 | 27.56 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 10 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 80 | 5 | 42.2 | 26.84 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 478 | 2.5 | 200 | 0.257 | 64.27 | 26.24 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 26.5 | 10 | 118 | 42.5 | 577.5 | 237 | 2 | SiO2 | 723 | 553 | 2.5 | 200 | 0.2 | 100 | 25.9 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 5.5 | 25.89 | 25.84 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 483 | 2 | 100 | 1 | 30.01 | 25.54 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 80 | 5 | 34 | 25.53 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 27.6 | 25.14 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.2 | 49.78 | 25.04 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.3 | 51.41 | 24.62 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.4 | 40 | 23.88 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 623 | 453 | 3 | 80 | 2 | 93.31 | 23.59 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 6 | 23.48 | 23.43 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 20 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 80 | 5 | 45.2 | 23.32 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.75 | 6.6 | 121 | 112 | 737.1 | 90.7 | 1.05 | SBA-15 | 693 | 473 | 3 | 80 | 5 | 23.3 | 23.28 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 473 | 3 | 80 | 6 | 23.1 | 23.08 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.2 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.92 | SiO2 | 623 | 453 | 3 | 80 | 4 | 26.5 | 23.06 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.76 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.16 | SBA-15 | 693 | 473 | 3 | 80 | 3 | 22.9 | 22.85 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.12 | 10.3 | 153 | 125.6 | 731 | 429 | 0.83 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 25.2 | 22.83 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.3 | 80 | 22.81 |
| 6.7 | 126 | 63.7 | 760.4 | 100 | 20 | 17 | 106 | 72 | 1011.26 | 18.235 | 2.25 | SiO2 | 723 | 493 | 2.5 | 70 | 0.28 | 24.91 | 22.78 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 503 | 3 | 80 | 0.6 | 99.75 | 22.28 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 453 | 2 | 50 | 0.2 | 95.24 | 22.28 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 473 | 2.5 | 200 | 0.257 | 56.01 | 22.01 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 623 | 453 | 3 | 80 | 6 | 28.5 | 22 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.3 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.38 | SiO2 | 623 | 453 | 3 | 80 | 1.5 | 97.9 | 21.93 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.31 | 10.3 | 153 | 125.6 | 731 | 429 | 0.29 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 24.3 | 21.92 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 27.1 | 10 | 118 | 42.5 | 577.5 | 237 | 1.75 | SiO2 | 723 | 553 | 2.5 | 200 | 0.2 | 100 | 21.3 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 723 | 453 | 3 | 80 | 4.5 | 24.9 | 20.89 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.87 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.28 | SBA-15 | 693 | 473 | 3 | 80 | 4 | 20.9 | 20.88 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 488 | 2.5 | 200 | 0.257 | 86.22 | 20.78 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.1 | 73.48 | 20.5 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 1 | 91.41 | 20.17 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 5.4 | 98.34 | 20.1 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.3 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.38 | SiO2 | 623 | 453 | 3 | 80 | 5 | 23.6 | 20.01 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 478 | 2 | 100 | 1 | 23.28 | 19.93 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.6 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.07 | SiO2 | 623 | 453 | 3 | 80 | 4 | 22.3 | 19.78 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 9.2 | 131 | 0 | 906.4 | 116 | 3 | SiO2 | 623 | 483 | 2 | 100 | 1 | 99.56 | 18.8 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 513 | 2 | 100 | 1 | 99.02 | 18.36 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 508 | 3 | 80 | 0.6 | 100 | 18.23 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.5 | 29.78 | 18.07 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.5 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.86 | SiO2 | 623 | 453 | 3 | 80 | 1.5 | 25.9 | 18 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 4.6 | 82 | 26.7 | 800.6 | 27 | 5 | SiO2 | 773 | 433 | 0.5 | 150 | 0.2 | 18.1 | 17.97 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 5.1 | 98.74 | 17.87 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.3 | 29.48 | 17.67 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 623 | 453 | 3 | 80 | 1.5 | 98.5 | 17.34 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 39 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 80 | 5 | 69.2 | 16.88 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.1 | 80 | 16.72 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.99 | 10.3 | 153 | 125.6 | 731 | 429 | 1.39 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 18.9 | 16.71 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.2 | 82.96 | 16.68 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 27.8 | 10 | 118 | 42.5 | 577.5 | 237 | 1.5 | SiO2 | 723 | 553 | 2.5 | 200 | 0.2 | 100 | 16.6 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 94.61 | 16.29 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 4.8 | 99.57 | 15.95 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 100 | 14.58 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 513 | 3 | 80 | 0.6 | 100 | 14.21 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 4.5 | 100 | 13.96 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 30 | 1.2 | 98.17 | 13.79 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 473 | 2 | 100 | 1 | 15.37 | 13.16 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.1 | 87.56 | 13.04 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.6 | 20 | 13.02 |
| 10.3 | 153 | 125.6 | 731 | 429 | 5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 773 | 423 | 0.5 | 150 | 0.2 | 12.6 | 12.6 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 4.2 | 100 | 12.15 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.9 | 95.41 | 10.93 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 518 | 3 | 80 | 0.6 | 100 | 10.53 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 1 | 80 | 10.47 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 26.8 | 10 | 118 | 42.5 | 577.5 | 237 | 1.25 | SiO2 | 723 | 553 | 2.5 | 200 | 0.2 | 100 | 10.46 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 513 | 2.4 | 60 | 0.5 | 99.52 | 10.46 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 448 | 3 | 80 | 0.6 | 99.85 | 10.38 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 468 | 2 | 100 | 1 | 11.56 | 10.19 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 97.04 | 9.94 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 1 | 85.33 | 9.91 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 97.22 | 9.76 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 40 | 1.2 | 97.87 | 9.62 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 10 | 38.22 | 9.57 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 3.9 | 100 | 8.44 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 9 | 40.33 | 8.31 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 1 | 100 | 8.03 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.9 | 100 | 7.98 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.1 | 10 | 118 | 42.5 | 577.5 | 237 | 0.25 | SiO2 | 723 | 553 | 2.5 | 200 | 0.2 | 100 | 7.95 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 1 | 89.78 | 7.67 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.8 | 98.96 | 7.59 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.9 | 84.89 | 7.54 |
| 10.3 | 153 | 125.6 | 731 | 429 | 4.72 | 6.6 | 121 | 112 | 737.1 | 90.7 | 0.54 | SBA-15 | 693 | 523 | 3 | 80 | 0.6 | 99.75 | 7.09 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.4 | 10.37 | 6.99 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.4 | 99.56 | 6.85 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 8 | 42.9 | 6.68 |
| 10.3 | 153 | 125.6 | 731 | 429 | 10 | 4.6 | 82 | 26.7 | 800.6 | 27 | 5 | SiO2 | 773 | 423 | 0.5 | 150 | 0.2 | 6.7 | 6.61 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.6 | 98.67 | 6.31 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.8 | 89.48 | 6.25 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.23 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0.6 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 99.07 | 6.12 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.4 | 96.89 | 6.08 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.7 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0.8 | CNT | 773 | 573 | 2.5 | 200 | 0.4 | 99.9 | 5.99 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 7 | 45.47 | 5.98 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.8 | 100 | 5.96 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 30 | 7.39 | 139 | 0 | 717.3 | 7.82 | 3 | SiO2 | 623 | 463 | 2 | 100 | 1 | 6.59 | 5.92 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.7 | 100 | 5.87 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.6 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.1 | CNT | 773 | 573 | 2.5 | 200 | 0.4 | 100 | 5.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.5 | 94.81 | 5.61 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 3.6 | 100 | 5.52 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.3 | 99.11 | 5.46 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.5 | 99.85 | 5.2 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 483 | 2 | 50 | 0.2 | 100 | 5.14 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 50 | 1.2 | 97.62 | 5.09 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.15 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.4 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 99.58 | 4.97 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.9 | 93.48 | 4.97 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.3 | 97.33 | 4.8 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.8 | 10 | 118 | 42.5 | 577.5 | 237 | 1 | SiO2 | 723 | 553 | 2.5 | 200 | 0.2 | 100 | 4.77 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 25.2 | 10 | 118 | 42.5 | 577.5 | 237 | 0.75 | SiO2 | 723 | 553 | 2.5 | 200 | 0.2 | 100 | 4.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.6 | 92.89 | 4.57 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.7 | 90.81 | 4.52 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.4 | 10 | 118 | 42.5 | 577.5 | 237 | 7.1 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.7 | 99.41 | 4.51 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 24.3 | 10 | 118 | 42.5 | 577.5 | 237 | 0.5 | SiO2 | 723 | 553 | 2.5 | 200 | 0.2 | 100 | 4.14 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.6 | 100 | 4.11 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 6 | 48.19 | 4.02 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 503 | 2.4 | 60 | 0.5 | 99.53 | 3.96 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.8 | 96.44 | 3.87 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 3.3 | 100 | 3.83 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.5 | 100 | 3.75 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 5 | 57.7 | 3.73 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.4 | 100 | 3.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.5 | 5.04 | 3.67 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.8 | 22.5 | 169 | 48 | 538.1 | 13.5 | 2.5 | SiO2 | 623 | 453 | 3 | 80 | 4 | 3.6 | 3.52 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 100 | 3.51 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.6 | 96.89 | 3.45 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.7 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.4 | SBA-15 | 873 | 453 | 3 | 80 | 0.6 | 96.6 | 3.38 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 623 | 453 | 3 | 80 | 1 | 98.72 | 3.37 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.06 | 4.6 | 82 | 26.7 | 800.6 | 27 | 2.38 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 99.92 | 3.3 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 60 | 0.5 | 94.69 | 3.21 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.4 | 99.11 | 3.08 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 60 | 1.2 | 97.87 | 3.05 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.88 | 4.6 | 82 | 26.7 | 800.6 | 27 | 7.11 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 99.75 | 2.78 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.5 | 98.52 | 2.74 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 4 | 69.79 | 2.69 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.9 | 95.7 | 2.52 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 3 | 82.18 | 2.45 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.9 | 4.6 | 82 | 26.7 | 800.6 | 27 | 5.91 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 99.75 | 2.44 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 80 | 5 | 76.3 | 2.37 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.7 | 96.15 | 2.3 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.02 | 4.6 | 82 | 26.7 | 800.6 | 27 | 3.5 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 99.92 | 2.28 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17 | 10 | 118 | 42.5 | 577.5 | 237 | 0 | ZrO2 | 673 | 493 | 2.5 | 120 | 1.6 | 2.96 | 2.26 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 17.2 | 10 | 118 | 42.5 | 577.5 | 237 | 2.7 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.3 | 99.7 | 2.05 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 28 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 80 | 5 | 64.3 | 1.86 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 4.5 | 9.1 | 128 | 205.3 | 870 | 71.6 | 1.4 | SBA-15 | 773 | 463 | 3 | 80 | 0.6 | 100 | 1.8 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 100 | 1.78 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.12 | 10.3 | 153 | 125.6 | 731 | 429 | 0.83 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 99.68 | 1.74 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 100 | 1.74 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 1.71 |
| 10.2 | 144 | 222.8 | 890.1 | 317 | 8 | 10.3 | 153 | 125.6 | 731 | 429 | 4.5 | SBA-15 | 773 | 508 | 3 | 100 | 0.6 | 99.8 | 1.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 3 | 100 | 1.66 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 60 | 0.5 | 88.44 | 1.64 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 2 | 91.69 | 1.52 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.7 | 99.56 | 1.51 |
| 10.2 | 144 | 222.8 | 890.1 | 317 | 8 | 10.3 | 153 | 125.6 | 731 | 429 | 1.5 | SBA-15 | 773 | 508 | 3 | 100 | 0.6 | 99.8 | 1.4 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.4 | 100 | 1.21 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 6.1 | 10.2 | 144 | 222.8 | 890.1 | 317 | 3.7 | SBA-15 | 873 | 453 | 3 | 80 | 0.6 | 100 | 1.2 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.6 | 99.41 | 1.18 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 2.7 | 100 | 1.07 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 0.6 | 99.24 | 1 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.26 | 10.3 | 153 | 125.6 | 731 | 429 | 0.56 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 100 | 0.96 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.5 | 99.11 | 0.95 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 473 | 2.4 | 60 | 0.5 | 82.81 | 0.89 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 483 | 2.4 | 80 | 1 | 99.4 | 0.89 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 473 | 2 | 50 | 0.2 | 100 | 0.84 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 483 | 2 | 50 | 0.2 | 100 | 0.84 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 15.1 | 22.5 | 169 | 48 | 538.1 | 13.5 | 0.77 | SiO2 | 623 | 453 | 3 | 80 | 0.5 | 99 | 0.7 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0.5 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.31 | 10.3 | 153 | 125.6 | 731 | 429 | 0.29 | SiO2 | 573 | 463 | 2 | 50 | 0.2 | 99.68 | 0.48 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.8 | 99.56 | 0.36 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.3 | 100 | 0.23 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.3 | 99.7 | 0.2 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 503 | 2 | 50 | 0.2 | 100 | 0.17 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 16.8 | 10 | 118 | 42.5 | 577.5 | 237 | 4.5 | ZrO2 | 673 | 493 | 2.5 | 120 | 0.4 | 99.7 | 0.16 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 493 | 2.5 | 200 | 0.257 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 498 | 2.5 | 200 | 0.257 | 99.82 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 503 | 2.5 | 200 | 0.257 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 508 | 2.5 | 200 | 0.257 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 50 | 9.2 | 131 | 0 | 906.4 | 116 | 16.6 | MgO | 673 | 513 | 2.5 | 200 | 0.257 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 453 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 453 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 463 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 483 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 493 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 498 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 503 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 508 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 513 | 3 | 80 | 0.6 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 0.3 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 1.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 1.8 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 5.6 | 10.2 | 144 | 222.8 | 890.1 | 317 | 1.9 | SBA-15 | 873 | 473 | 3 | 80 | 2.4 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.23 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0.6 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.15 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.4 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.06 | 4.6 | 82 | 26.7 | 800.6 | 27 | 2.38 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.02 | 4.6 | 82 | 26.7 | 800.6 | 27 | 3.5 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.9 | 4.6 | 82 | 26.7 | 800.6 | 27 | 5.91 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.88 | 4.6 | 82 | 26.7 | 800.6 | 27 | 7.11 | SiO2 | 573 | 493 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 503 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 513 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 523 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 533 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 543 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.34 | 4.6 | 82 | 26.7 | 800.6 | 27 | 0 | SiO2 | 573 | 553 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 513 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 523 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 533 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 13.94 | 4.6 | 82 | 26.7 | 800.6 | 27 | 4.72 | SiO2 | 573 | 543 | 2 | 50 | 0.2 | 100 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 70 | 1.2 | 97.8 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 80 | 1.2 | 97.99 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 90 | 1.2 | 97.93 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 33 | 22.5 | 169 | 48 | 538.1 | 13.5 | 1.5 | ZrO2 | 1023 | 493 | 2.4 | 100 | 1.2 | 98.05 | 0 |
| 7.1 | 138 | 118.4 | 745.5 | 401 | 14.5 | 4.6 | 82 | 26.7 | 800.6 | 27 | 1.8 | CNT | 773 | 573 | 2.5 | 200 | 0.2 | 100 | 0 |

Table B2. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 99.83.

| X1 | X2 | X3 | X4 | X5 | X6 | X7 | X8 | X9 | X10 | X11 | X12 | X13 | X14 | X15 | X16 | UED | UPC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9898.14 | 25 | 0.95 | 100 | 1.1 | 0.4 | 0.482 | 110 | 0.6 | 0.895 | 130 | 30.9048 | 0.939426 | 100 | 100 | 100 | 22.93119 | 1978.587 |
| 20997.2 | 24.2378 | 0.869208 | 161.428 | 1.43871 | 46.5224 | 0.522082 | 443.634 | 84.1421 | 0.721371 | 496.941 | 48.7487 | 0.771661 | 43.1812 | 203.073 | 214.59 | 67.6987 | 4989.317 |
| 17956.7 | 20.3828 | 0.891337 | 86.3214 | 0.723023 | 13.8243 | 0.353691 | 302.497 | 75.2522 | 0.879275 | 484.189 | 97.1708 | 0.812812 | 8.0219 | 174.7 | 181.588 | 60.33499 | 4300.001 |
| 26888.3 | 19.7192 | 0.826323 | 171.916 | 3.75302 | 53.5755 | 0.383748 | 408.908 | 37.8351 | 0.808762 | 216.448 | 32.2446 | 0.808122 | 134.758 | 197.256 | 210.014 | 75.54589 | 5703.67 |
| 20616 | 32.841 | 0.871992 | 37.3904 | 1.50499 | 42.9581 | 0.5314 | 363.241 | 57.8923 | 0.846898 | 171.691 | 6.64137 | 0.618173 | 91.2008 | 230.403 | 163.447 | 61.34436 | 4546.74 |
| 9889.61 | 31.1775 | 0.950069 | 148.799 | 0.403384 | 72.6672 | 0.568407 | 121.402 | 90.4712 | 0.616633 | 84.2014 | 91.3457 | 0.653034 | 1.2097 | 115.988 | 77.1354 | 79.00911 | 6687.828 |
| 25617.2 | 17.8601 | 0.835575 | 170.3 | 0.711252 | 23.1573 | 0.494554 | 145.572 | 92.1661 | 0.620266 | 498.372 | 28.1722 | 0.861596 | 25.5029 | 97.9626 | 441.659 | 84.86071 | 5640.421 |
| 21196.2 | 16.4945 | 0.867754 | 20.1626 | 0.920437 | 13.5282 | 0.345965 | 394.275 | 81.5373 | 0.486198 | 490.359 | 2.93383 | 0.896738 | 19.691 | 213.586 | 424.823 | 87.22805 | 6170.075 |
| 25317.9 | 27.5222 | 0.83776 | 70.4129 | 2.39622 | 82.5357 | 0.548489 | 213.389 | 6.93241 | 0.931471 | 369.392 | 0.217765 | 0.462788 | 18.0123 | 159.282 | 340.216 | 85.20938 | 6734.67 |
| 10466.9 | 18.1095 | 0.945854 | 71.8066 | 0.523587 | 80.3274 | 0.442659 | 347.1 | 49.4944 | 0.553479 | 71.143 | 88.8438 | 0.73571 | 11.1414 | 74.1503 | 53.9875 | 73.41126 | 7111.924 |
| 12055.1 | 28.0029 | 0.934303 | 81.4726 | 0.940334 | 85.3208 | 0.415693 | 301.156 | 18.1723 | 0.528516 | 198.397 | 86.2361 | 0.767686 | 32.4997 | 81.2178 | 187.365 | 76.83245 | 7664.898 |
| 17093.9 | 27.1294 | 0.897623 | 83.4318 | 3.54174 | 87.4169 | 0.467226 | 250.776 | 94.1644 | 0.687123 | 152.953 | 85.0918 | 0.792925 | 131.298 | 127.56 | 113.141 | 63.0133 | 5392.544 |
| 18397.4 | 19.9957 | 0.888129 | 39.2059 | 0.299682 | 20.6463 | 0.436156 | 375.231 | 61.6916 | 0.711921 | 488.554 | 75.4831 | 0.932288 | 29.5805 | 133.623 | 309.866 | 48.22971 | 3578.201 |
| 26642.1 | 19.5305 | 0.828115 | 152.773 | 3.7571 | 76.6103 | 0.344697 | 411.724 | 77.9057 | 0.89387 | 339.048 | 77.4814 | 0.912873 | 153.455 | 73.7962 | 325.449 | 75.91922 | 6070.618 |
| 20623.4 | 23.6592 | 0.871928 | 141.754 | 1.73223 | 15.6171 | 0.623872 | 190.295 | 74.0791 | 0.558992 | 403.793 | 88.4112 | 0.748764 | 128.117 | 175.947 | 289.8 | 87.45732 | 5767.118 |
| 29096.6 | 26.0413 | 0.810253 | 36.485 | 1.89031 | 31.9153 | 0.397408 | 277.096 | 68.548 | 0.876352 | 212.143 | 55.8805 | 0.851799 | 125.55 | 106.346 | 164.458 | 57.96003 | 4050.004 |
| 20915.1 | 19.514 | 0.869802 | 113.975 | 2.02957 | 89.5923 | 0.304423 | 354.238 | 31.8735 | 0.94872 | 47.4194 | 69.9558 | 0.741579 | 30.989 | 56.9774 | 45.1041 | 77.30642 | 7190.392 |
| 26390.5 | 21.6717 | 0.829948 | 124.639 | 0.461113 | 74.5442 | 0.343085 | 396.721 | 6.35683 | 0.636715 | 229.581 | 47.9862 | 0.963346 | 33.9473 | 300.799 | 80.0627 | 92.89035 | 7532.59 |
| 27794.5 | 14.3498 | 0.819724 | 115.734 | 1.28668 | 9.156 | 0.362381 | 239.418 | 2.81846 | 0.953784 | 462.616 | 26.2749 | 0.642617 | 26.7278 | 113.06 | 234.239 | 69.24296 | 4560.13 |
| 20373.3 | 28.5359 | 0.873754 | 94.3845 | 1.64764 | 64.3733 | 0.486982 | 410.39 | 29.2626 | 0.749231 | 154.533 | 90.2899 | 0.403318 | 131.474 | 375.52 | 147.93 | 99.77503 | 7715.356 |
| 16472.1 | 28.7939 | 0.902151 | 122.407 | 1.08134 | 28.5355 | 0.35292 | 296.987 | 90.1635 | 0.849973 | 169.85 | 19.1069 | 0.954633 | 23.2962 | 42.9613 | 162.556 | 56.44098 | 4422.233 |
| 18632.5 | 27.9502 | 0.886424 | 109.53 | 3.23998 | 49.0123 | 0.5294 | 314.514 | 69.6651 | 0.39224 | 328.274 | 52.3746 | 0.903118 | 117.834 | 237.762 | 311.167 | 97.60698 | 7339.567 |
| 21681.2 | 32.5218 | 0.864238 | 97.9627 | 0.539948 | 52.1725 | 0.381106 | 276.833 | 14.0641 | 0.806593 | 289.924 | 61.3654 | 0.964068 | 34.5005 | 261.586 | 253.596 | 54.68112 | 4462.91 |
| 27604 | 13.1568 | 0.821111 | 116.45 | 0.784815 | 50.2071 | 0.471172 | 393.914 | 99.9341 | 0.797016 | 205.736 | 0.960382 | 0.717689 | 25.2866 | 229.91 | 193.477 | 72.89665 | 5250.095 |
| 20842.7 | 24.7508 | 0.870333 | 124.62 | 1.68805 | 56.3367 | 0.417533 | 274.944 | 41.3698 | 0.597115 | 326.775 | 92.0635 | 0.785277 | 142.516 | 76.5501 | 192.368 | 83.80903 | 6674.118 |
| 22682.3 | 28.1183 | 0.856945 | 169.62 | 2.39439 | 4.39858 | 0.355456 | 126.315 | 43.5608 | 0.75447 | 387.421 | 52.7375 | 0.797563 | 120.196 | 78.8062 | 173.572 | 82.48069 | 5440.273 |
| 16981.8 | 19.4911 | 0.898433 | 94.593 | 0.845242 | 83.6742 | 0.391343 | 411.906 | 46.6623 | 0.655753 | 259.964 | 3.10966 | 0.864594 | 17.4258 | 397.859 | 120.733 | 64.86465 | 6217.675 |
| 24706.7 | 15.3197 | 0.8422 | 122.093 | 3.78323 | 85.6785 | 0.314569 | 403.819 | 81.9486 | 0.859562 | 288.897 | 60.3706 | 0.853767 | 31.1887 | 369.748 | 132.41 | 76.00715 | 6666.743 |
| 19549.6 | 30.5171 | 0.879751 | 83.7113 | 2.44005 | 88.4629 | 0.482732 | 133.303 | 61.0646 | 0.950925 | 141.786 | 60.8944 | 0.800723 | 9.81661 | 42.2759 | 79.8017 | 44.01688 | 3743.605 |
| 13200.3 | 25.5963 | 0.925964 | 135.208 | 0.841212 | 19.2704 | 0.452536 | 450.911 | 88.4125 | 0.758339 | 325.182 | 22.4627 | 0.606031 | 3.92156 | 164.393 | 133.315 | 73.41424 | 5577.202 |
| 15872 | 20.8272 | 0.906512 | 169.301 | 2.24672 | 0.364159 | 0.558023 | 227.135 | 62.5113 | 0.682521 | 411.143 | 9.84075 | 0.909154 | 102.047 | 117.808 | 234.342 | 43.43763 | 3150.473 |
| 13699.6 | 26.3951 | 0.92233 | 118.81 | 0.31393 | 22.9507 | 0.454294 | 251.134 | 40.7156 | 0.411258 | 132.321 | 79.6952 | 0.909046 | 0.964357 | 121.158 | 125.906 | 87.66712 | 6773.618 |
| 15525.7 | 18.0064 | 0.909031 | 92.7789 | 1.80857 | 7.42784 | 0.415629 | 310.792 | 97.7363 | 0.737408 | 320.782 | 43.0122 | 0.432146 | 108.464 | 269.453 | 298.524 | 99.40249 | 6939.375 |
| 14035.6 | 19.9746 | 0.919879 | 40.2739 | 0.817584 | 52.1853 | 0.448793 | 146.721 | 91.376 | 0.921714 | 183.88 | 80.6713 | 0.429131 | 3.80319 | 131.301 | 167.656 | 85.18337 | 6902.507 |
| 16157.2 | 31.6395 | 0.904447 | 133.775 | 0.546339 | 59.8459 | 0.596732 | 434.449 | 79.3854 | 0.944712 | 304.135 | 3.88398 | 0.924078 | 39.0345 | 171.989 | 227.259 | 33.95832 | 2796.539 |
| 12224.3 | 23.7959 | 0.933066 | 66.9235 | 0.522207 | 1.75346 | 0.367804 | 92.261 | 6.2124 | 0.959678 | 427.652 | 66.2098 | 0.810515 | 36.1819 | 45.1775 | 381.066 | 37.05831 | 2879.844 |
| 13860.9 | 15.9614 | 0.921148 | 160.621 | 0.216767 | 4.80689 | 0.528306 | 335.871 | 2.54824 | 0.746413 | 508.333 | 55.0867 | 0.592772 | 14.3184 | 137.717 | 274.805 | 72.29448 | 5344.554 |
| 14753.2 | 20.7668 | 0.914656 | 125.626 | 0.30362 | 0.768519 | 0.622304 | 149.132 | 47.2743 | 0.522447 | 366.398 | 43.8906 | 0.598039 | 27.5932 | 86.4936 | 135.451 | 78.20817 | 5528.839 |
| 14659.8 | 13.2225 | 0.915331 | 56.146 | 1.08649 | 13.0878 | 0.41835 | 238.772 | 74.3657 | 0.965292 | 293.805 | 8.2478 | 0.378616 | 31.7301 | 74.9512 | 256.899 | 85.16441 | 6212.8 |
| 15739.5 | 18.1301 | 0.907475 | 88.8004 | 0.164591 | 49.2591 | 0.515147 | 305.745 | 16.0167 | 0.691287 | 384.307 | 66.7092 | 0.805549 | 13.0025 | 297.551 | 148.398 | 52.29567 | 4330.042 |
| 15721.1 | 34.5155 | 0.907625 | 147.985 | 0.144091 | 36.0649 | 0.636372 | 196.758 | 9.34376 | 0.616091 | 208.494 | 29.8338 | 0.716076 | 1.00676 | 68.0757 | 165.214 | 62.31041 | 4819.482 |
| 13455.7 | 21.7918 | 0.924101 | 137.929 | 1.60491 | 15.1604 | 0.399489 | 323.874 | 14.966 | 0.788185 | 154.272 | 36.1153 | 0.976071 | 158.048 | 219.652 | 78.8952 | 41.04303 | 3323.675 |
| 16262.5 | 27.4906 | 0.903676 | 87.9994 | 2.93722 | 29.1448 | 0.349212 | 361.23 | 87.0145 | 0.755149 | 321.623 | 6.31169 | 0.885121 | 98.0125 | 57.0649 | 244.343 | 55.24347 | 4465.229 |
| 15248 | 13.8826 | 0.91105 | 145.715 | 0.885098 | 47.2292 | 0.611135 | 279.449 | 25.1823 | 0.651424 | 206.303 | 30.3246 | 0.961352 | 38.7055 | 273.644 | 60.7241 | 38.38317 | 3119.053 |
| 12676.2 | 21.3828 | 0.929775 | 97.9067 | 1.50476 | 73.7013 | 0.457564 | 209.292 | 16.8313 | 0.480571 | 361.215 | 88.5133 | 0.870894 | 89.0992 | 175.189 | 52.5175 | 66.62632 | 6242.149 |
| 14968.1 | 28.6574 | 0.913099 | 112.285 | 1.01039 | 7.52141 | 0.522005 | 372.174 | 95.5359 | 0.609604 | 258.797 | 52.4424 | 0.858471 | 75.1769 | 359.513 | 182.66 | 52.99541 | 3804.293 |
| 11394.8 | 30.7988 | 0.939113 | 96.4437 | 0.610503 | 86.9288 | 0.55534 | 375.844 | 51.6917 | 0.597214 | 239.968 | 82.717 | 0.865152 | 30.8213 | 339.958 | 201.956 | 54.43152 | 4770.556 |
| 14184.1 | 29.1388 | 0.918807 | 171.676 | 2.06505 | 60.0272 | 0.532769 | 308.264 | 47.012 | 0.900474 | 159.528 | 38.8746 | 0.559166 | 5.64194 | 296.275 | 71.2704 | 62.87635 | 5228.258 |
| 13760.3 | 34.0365 | 0.921898 | 56.0106 | 1.8898 | 39.9978 | 0.472191 | 289.629 | 31.2826 | 0.796196 | 322.225 | 86.7809 | 0.81062 | 18.0542 | 270.403 | 96.8599 | 42.49277 | 3535.401 |
| 11498.1 | 27.5435 | 0.938357 | 160.121 | 2.38424 | 51.7863 | 0.454452 | 432.593 | 22.5612 | 0.892082 | 518.518 | 61.7421 | 0.461786 | 129.254 | 359.517 | 445.391 | 76.14348 | 6669.362 |
| 13879.6 | 33.3 | 0.921029 | 104.108 | 3.06918 | 29.4645 | 0.433173 | 293.279 | 57.2459 | 0.888427 | 92.0924 | 73.2483 | 0.55046 | 129.293 | 93.2639 | 79.3381 | 62.55683 | 4928.053 |
| 10557.9 | 30.2041 | 0.945204 | 119.401 | 0.375482 | 40.412 | 0.57923 | 364.232 | 97.6763 | 0.470471 | 336.329 | 64.5739 | 0.882545 | 27.5627 | 193.314 | 257.899 | 63.11766 | 5111.9 |
| 9372.25 | 34.7193 | 0.953841 | 157.513 | 2.36964 | 13.9056 | 0.567955 | 334.645 | 15.9538 | 0.553404 | 437.648 | 60.496 | 0.93692 | 30.1376 | 141.298 | 56.3028 | 41.40291 | 3410.576 |
| 15108.2 | 32.841 | 0.912084 | 69.9525 | 3.70436 | 47.3892 | 0.482096 | 403.996 | 17.5415 | 0.422182 | 238.434 | 20.3164 | 0.844135 | 170.911 | 251.051 | 233.287 | 66.02755 | 5518.322 |
| 16239.6 | 16.6733 | 0.903834 | 45.8294 | 1.25619 | 18.6746 | 0.470522 | 286.541 | 20.1878 | 0.774121 | 398.089 | 7.49916 | 0.664114 | 21.3773 | 184.12 | 389.501 | 45.7533 | 3609.843 |
| 14253.1 | 20.0454 | 0.918295 | 120.843 | 2.28628 | 43.3766 | 0.441343 | 289.884 | 53.4908 | 0.740911 | 335.615 | 9.39283 | 0.83941 | 71.702 | 132.944 | 137.733 | 45.99694 | 4004.92 |
| 11786.8 | 31.4832 | 0.93626 | 123.855 | 0.600824 | 11.586 | 0.457974 | 274.299 | 89.8183 | 0.441959 | 173.438 | 76.5107 | 0.858762 | 30.3797 | 51.0939 | 52.2839 | 82.29046 | 6182.796 |
| 15079.7 | 16.0231 | 0.912276 | 97.4456 | 1.60662 | 25.5272 | 0.47866 | 425.869 | 95.1389 | 0.641174 | 505.59 | 4.14293 | 0.692688 | 59.2323 | 136.736 | 131.197 | 60.62941 | 4647.282 |
| 11950.7 | 30.2095 | 0.935065 | 51.7843 | 2.02298 | 88.1398 | 0.357291 | 148.386 | 33.8224 | 0.928609 | 285.151 | 7.5035 | 0.915237 | 51.7623 | 53.6882 | 48.0712 | 42.88359 | 4674.742 |
| 9971.36 | 19.7892 | 0.949462 | 64.3086 | 2.1737 | 27.9039 | 0.483253 | 342.022 | 95.3662 | 0.435322 | 311.83 | 3.50369 | 0.639743 | 96.1229 | 223.546 | 165.373 | 85.59274 | 6938.619 |
| 10843.6 | 26.7924 | 0.943119 | 54.9245 | 0.957022 | 23.107 | 0.449787 | 382.626 | 10.7334 | 0.750159 | 235.102 | 92.7352 | 0.567188 | 48.0703 | 213.506 | 132.685 | 57.41777 | 4756.627 |
| 10671.7 | 30.3081 | 0.944375 | 165.731 | 1.70197 | 83.6389 | 0.622473 | 306.821 | 64.1238 | 0.901782 | 348.296 | 83.7629 | 0.407668 | 137.802 | 172.014 | 193.655 | 76.69153 | 6192.339 |
| 16097.1 | 17.2988 | 0.904871 | 118.169 | 2.42285 | 36.6158 | 0.600531 | 289.514 | 74.007 | 0.795346 | 408.017 | 27.1353 | 0.805718 | 65.0557 | 198.304 | 396.987 | 51.03431 | 3802.346 |
| 12127.9 | 28.6738 | 0.933773 | 48.8285 | 2.18595 | 52.2063 | 0.335962 | 97.953 | 21.7411 | 0.618264 | 145.326 | 42.9026 | 0.882382 | 35.2444 | 71.1444 | 125.087 | 63.5296 | 6060.932 |
| 9650.9 | 15.79 | 0.951792 | 132.324 | 1.98107 | 11.4819 | 0.474365 | 241.157 | 86.9615 | 0.691596 | 184.088 | 7.26049 | 0.83973 | 26.0975 | 228.487 | 123.206 | 43.69629 | 3527.118 |
| 14893.2 | 25.4892 | 0.913641 | 75.041 | 3.72615 | 80.4858 | 0.567122 | 406.651 | 26.0549 | 0.679384 | 310.171 | 70.3279 | 0.965919 | 72.6946 | 254.192 | 267.823 | 47.41052 | 4022.958 |
| 15267.5 | 14.4512 | 0.910908 | 161.312 | 1.61836 | 65.4335 | 0.585734 | 365.63 | 33.4382 | 0.664001 | 322.044 | 42.4603 | 0.59685 | 138.029 | 76.1207 | 166.132 | 69.05851 | 5663.585 |
| 13842.1 | 31.5213 | 0.921299 | 106.222 | 1.64709 | 70.7519 | 0.334441 | 84.6221 | 47.9307 | 0.783767 | 398.757 | 68.4898 | 0.872526 | 24.8056 | 59.9474 | 321.439 | 62.04562 | 5892.854 |
| 15145 | 31.9407 | 0.911815 | 165.659 | 1.63025 | 92.2856 | 0.450298 | 170.265 | 65.8832 | 0.657727 | 437.798 | 67.5562 | 0.876517 | 70.6116 | 57.8432 | 140.929 | 71.3035 | 6351.07 |
| 14173.7 | 17.3403 | 0.918872 | 121.207 | 1.4608 | 8.30121 | 0.360389 | 369.597 | 88.7426 | 0.716947 | 124.034 | 28.5533 | 0.573393 | 12.9522 | 104.524 | 100.339 | 91.03686 | 6613.073 |
| 12156.6 | 15.4844 | 0.933553 | 70.1124 | 1.42824 | 66.5982 | 0.358001 | 418.586 | 29.6426 | 0.836309 | 303.706 | 7.36003 | 0.804133 | 38.2926 | 76.5901 | 217.34 | 48.80028 | 4979.18 |
| 12323.9 | 21.3731 | 0.932339 | 81.4347 | 0.433814 | 12.2237 | 0.343121 | 364.244 | 6.9637 | 0.989566 | 221.89 | 40.6095 | 0.737509 | 8.22083 | 108.734 | 142.684 | 44.8122 | 3660.916 |
| 14029.9 | 18.5645 | 0.919919 | 117.789 | 1.37578 | 13.9318 | 0.316926 | 185.313 | 92.1256 | 0.865933 | 284.001 | 98.5146 | 0.978389 | 4.8108 | 116.995 | 216.887 | 64.09772 | 4715.809 |
| 15328.3 | 25.583 | 0.910474 | 132.422 | 1.14641 | 33.2731 | 0.507674 | 294.898 | 15.4392 | 0.520265 | 369.166 | 3.40226 | 0.754281 | 55.9631 | 70.173 | 193.005 | 66.71842 | 5415.878 |
| 12881.1 | 23.5604 | 0.928285 | 96.9152 | 3.27368 | 58.1152 | 0.439055 | 221.581 | 92.3832 | 0.870377 | 417.485 | 78.3687 | 0.614247 | 68.189 | 201.23 | 320.17 | 62.5949 | 5311.665 |
| 9470.45 | 22.7114 | 0.953111 | 36.7888 | 2.63669 | 67.8118 | 0.600707 | 352.224 | 96.9875 | 0.893796 | 363.419 | 98.4283 | 0.885525 | 208.918 | 266.232 | 309.982 | 47.21577 | 3669.993 |
| 13569.6 | 22.7464 | 0.923273 | 117.979 | 1.31332 | 4.40804 | 0.391439 | 448.33 | 5.75874 | 0.707058 | 62.4156 | 83.3124 | 0.571386 | 68.7339 | 329.129 | 59.6573 | 76.72634 | 5669.398 |
| 16564.5 | 32.4706 | 0.901484 | 126.294 | 0.179248 | 21.1752 | 0.420276 | 290.268 | 41.8997 | 0.955807 | 311.487 | 45.3145 | 0.988271 | 7.4699 | 155.882 | 188.682 | 55.49255 | 4154.958 |
| 15057.7 | 23.1169 | 0.912441 | 25.9657 | 0.331471 | 86.6482 | 0.560179 | 218.578 | 50.5544 | 0.787287 | 190.043 | 21.818 | 0.936583 | 31.9309 | 181.552 | 180.563 | 39.54668 | 3505.307 |
| 15748.8 | 29.9558 | 0.907417 | 39.1761 | 1.62222 | 7.36072 | 0.480536 | 92.1978 | 20.0232 | 0.849412 | 269.406 | 28.2109 | 0.610772 | 61.3244 | 80.0293 | 150.221 | 44.87118 | 3358.409 |
| 14612.9 | 19.3008 | 0.915676 | 58.858 | 1.82352 | 58.3656 | 0.395691 | 319.749 | 49.1665 | 0.948143 | 394.741 | 66.8288 | 0.669053 | 58.2185 | 202.06 | 325.782 | 54.98136 | 4873.91 |
| 13437.9 | 26.8457 | 0.924236 | 80.96 | 1.5382 | 25.6214 | 0.394644 | 136.606 | 53.0215 | 0.410712 | 186.303 | 28.281 | 0.876158 | 99.1963 | 45.0434 | 91.9594 | 79.66934 | 6518.111 |
| 10243 | 16.3842 | 0.947483 | 44.2175 | 2.76361 | 96.9081 | 0.480069 | 244.125 | 24.5137 | 0.51595 | 242.339 | 76.315 | 0.996286 | 90.6155 | 199.957 | 193.435 | 49.77595 | 4869.524 |
| 14373.5 | 21.4334 | 0.91742 | 50.9698 | 0.348487 | 1.26269 | 0.487558 | 289.47 | 18.774 | 0.409266 | 121.075 | 89.8789 | 0.741867 | 24.9073 | 232.418 | 110.74 | 81.01501 | 5762.936 |
| 14150.5 | 30.394 | 0.919052 | 112.587 | 0.768289 | 11.6504 | 0.536071 | 205.192 | 22.5347 | 0.564769 | 305.014 | 23.2714 | 0.66409 | 20.0857 | 145.972 | 117.137 | 61.91039 | 4711.604 |
| 15247.1 | 16.003 | 0.911057 | 141.653 | 0.947407 | 65.5583 | 0.399302 | 84.3209 | 47.4209 | 0.777601 | 312.296 | 93.5175 | 0.751483 | 88.6096 | 77.2885 | 119.514 | 74.15817 | 6333.191 |
| 9947.76 | 18.2215 | 0.949633 | 81.2497 | 0.995308 | 27.4067 | 0.464078 | 396.97 | 76.6721 | 0.956809 | 488.976 | 6.5746 | 0.378699 | 37.9271 | 367.696 | 433.436 | 73.05903 | 5910.189 |
| 12415.3 | 16.971 | 0.931671 | 144.24 | 3.34708 | 57.599 | 0.501759 | 477.562 | 33.1907 | 0.780886 | 483.822 | 8.67875 | 0.825325 | 23.7987 | 99.0403 | 434.102 | 37.73063 | 3525 |
| 14197 | 18.5499 | 0.918703 | 49.2782 | 2.03726 | 65.1362 | 0.496725 | 391.729 | 27.845 | 0.817727 | 518.667 | 55.2514 | 0.952221 | 39.5208 | 328.838 | 179.207 | 34.14482 | 3027.782 |
| 14095.7 | 28.0996 | 0.919449 | 56.6522 | 2.12631 | 85.9937 | 0.4957 | 277.682 | 65.535 | 0.789501 | 87.6624 | 23.1605 | 0.765303 | 34.4914 | 152.733 | 86.8476 | 47.00503 | 4228.425 |
| 12583.8 | 14.4078 | 0.930443 | 17.6768 | 2.59748 | 17.4092 | 0.522697 | 291.405 | 69.0121 | 0.833112 | 448.351 | 73.9465 | 0.870379 | 151.854 | 182.214 | 384.313 | 40.61941 | 3037.3 |
| 15949.9 | 27.1715 | 0.905951 | 154.916 | 2.46714 | 1.19163 | 0.492327 | 459.458 | 79.3877 | 0.705294 | 283.609 | 34.9077 | 0.654344 | 14.8587 | 67.962 | 51.4616 | 66.61171 | 4623.184 |
| 13191.1 | 15.3729 | 0.926023 | 19.8036 | 2.67182 | 46.2643 | 0.472483 | 186.087 | 27.4556 | 0.669348 | 515.657 | 42.9904 | 0.863928 | 168.127 | 85.3318 | 355.405 | 41.78305 | 3645.215 |
| 14571.8 | 24.9597 | 0.91598 | 157.19 | 3.04755 | 60.7008 | 0.562678 | 58.5947 | 40.0539 | 0.962091 | 408.071 | 45.8745 | 0.33904 | 137.808 | 47.9486 | 272.81 | 84.21797 | 6621.843 |
| 11262 | 14.3711 | 0.940064 | 155.724 | 2.16215 | 96.1827 | 0.538728 | 173.452 | 29.9475 | 0.887949 | 263.046 | 32.7055 | 0.653387 | 45.1017 | 141.566 | 145.694 | 46.59442 | 4523.554 |
| 12049.3 | 31.6661 | 0.934349 | 74.4035 | 1.9655 | 89.1524 | 0.450934 | 264.342 | 85.3154 | 0.70955 | 510.813 | 53.1195 | 0.561087 | 36.7227 | 170.254 | 281.346 | 78.69691 | 7428.068 |
| 10489.7 | 21.8378 | 0.945691 | 163.796 | 2.94996 | 21.5652 | 0.545697 | 161.683 | 34.4284 | 0.778594 | 515.093 | 45.1338 | 0.991044 | 139.233 | 96.5302 | 112.28 | 31.2596 | 2629.198 |
| 14929.8 | 31.1798 | 0.913381 | 149.123 | 2.7655 | 17.8151 | 0.541337 | 149.688 | 69.024 | 0.754927 | 514.164 | 45.1292 | 0.777352 | 111.668 | 71.9736 | 415.454 | 46.37242 | 3463.524 |
| 13955 | 13.1398 | 0.920461 | 170.002 | 0.513516 | 16.2949 | 0.520965 | 321.352 | 67.8269 | 0.530287 | 159.078 | 45.941 | 0.86026 | 29.5628 | 310.292 | 105.984 | 75.08518 | 5591.786 |
| 12476.3 | 23.2387 | 0.931232 | 43.8167 | 0.303202 | 39.7017 | 0.397527 | 421.829 | 33.5646 | 0.866187 | 162.921 | 78.6373 | 0.88637 | 16.3781 | 182.247 | 56.5191 | 41.14963 | 3597.158 |
| 11392.1 | 30.4572 | 0.939131 | 75.6285 | 3.3863 | 59.0813 | 0.475654 | 92.8537 | 35.4034 | 0.574353 | 75.0896 | 63.2441 | 0.742197 | 149.178 | 58.3183 | 55.946 | 57.87904 | 5156.511 |
| 16273.7 | 19.8838 | 0.903587 | 100.641 | 0.36318 | 90.6164 | 0.572765 | 394.291 | 17.9752 | 0.469854 | 223.829 | 38.8861 | 0.899813 | 28.762 | 70.5278 | 93.2219 | 61.96976 | 5313.499 |
| 12257.4 | 16.374 | 0.93282 | 132.752 | 0.346999 | 43.0538 | 0.527001 | 105.38 | 32.8393 | 0.901356 | 65.0379 | 34.635 | 0.502238 | 23.4637 | 54.9434 | 58.5931 | 64.4643 | 5344.485 |
| 9795.55 | 24.9458 | 0.950747 | 145.709 | 2.12074 | 37.1322 | 0.52597 | 390.567 | 78.8392 | 0.59731 | 434.674 | 82.9959 | 0.658239 | 62.5009 | 173.535 | 95.9221 | 68.86317 | 5619.928 |
| 9296.38 | 20.2079 | 0.954376 | 94.2984 | 3.29507 | 64.3384 | 0.45875 | 177.636 | 24.9095 | 0.507455 | 65.8745 | 95.1706 | 0.698451 | 156.624 | 112.147 | 53.9398 | 70.80323 | 6671.654 |
| 13536.3 | 16.6421 | 0.923511 | 103.526 | 0.799676 | 49.5714 | 0.534265 | 355.03 | 11.4765 | 0.591085 | 313.19 | 44.9026 | 0.44767 | 64.8046 | 58.2918 | 182.463 | 90.51801 | 7431.031 |
| 11662 | 21.3094 | 0.937157 | 120.525 | 3.10826 | 96.0834 | 0.523949 | 343.299 | 83.8428 | 0.821944 | 399.551 | 90.8299 | 0.837679 | 112.477 | 129.921 | 226.166 | 48.5797 | 4157.887 |
| 15062.5 | 33.075 | 0.912417 | 70.102 | 3.3755 | 80.7713 | 0.359309 | 343.023 | 33.9295 | 0.801258 | 400.166 | 82.7111 | 0.851274 | 58.8902 | 65.8778 | 283.572 | 58.33634 | 5611.679 |
| 13737.3 | 33.3647 | 0.922064 | 117.466 | 1.93595 | 93.8983 | 0.461885 | 427.884 | 41.1609 | 0.850863 | 493.928 | 93.5313 | 0.695265 | 154.961 | 114.536 | 297.075 | 56.14475 | 5239.412 |
| 12462.9 | 28.3375 | 0.931334 | 45.3447 | 1.7959 | 97.2415 | 0.471958 | 198.854 | 52.2241 | 0.560471 | 475.107 | 72.0402 | 0.676131 | 138.719 | 97.2634 | 473.607 | 73.79921 | 7003.14 |
| 12751.6 | 27.66 | 0.929232 | 32.9477 | 1.18273 | 43.1982 | 0.425739 | 347.979 | 82.5687 | 0.477432 | 143.963 | 39.4324 | 0.962152 | 22.6094 | 309.039 | 139.485 | 62.58963 | 5429.725 |
| 11415.8 | 34.9021 | 0.938966 | 139.234 | 0.964481 | 18.3077 | 0.336788 | 178.88 | 14.6825 | 0.632882 | 350.319 | 22.7522 | 0.688103 | 59.0019 | 45.3785 | 186.854 | 87.40411 | 7151.061 |
| 14414.1 | 20.3574 | 0.917124 | 141.626 | 3.25303 | 38.859 | 0.448885 | 499.08 | 16.4776 | 0.67142 | 350.591 | 88.6661 | 0.649967 | 55.2486 | 355.442 | 117.232 | 68.40867 | 5637.564 |
| 13704.4 | 22.5698 | 0.922291 | 66.301 | 1.9113 | 87.8431 | 0.451087 | 73.6995 | 62.9557 | 0.740591 | 243.038 | 8.56582 | 0.813196 | 172.856 | 58.606 | 170.345 | 47.88229 | 4668.548 |
| 10585.3 | 32.6717 | 0.945008 | 151.25 | 1.54466 | 16.1962 | 0.315895 | 146.92 | 45.7425 | 0.660252 | 235.939 | 8.31492 | 0.891466 | 93.3313 | 55.9876 | 222.198 | 68.63452 | 5667.261 |
| 15298.8 | 34.0562 | 0.910699 | 70.8759 | 2.63728 | 40.9211 | 0.521117 | 437.988 | 5.06023 | 0.80678 | 434.482 | 24.031 | 0.94227 | 181.665 | 353.931 | 261.416 | 30.26218 | 2608.644 |
| 16073 | 27.2763 | 0.905055 | 158.482 | 3.47374 | 72.7441 | 0.51831 | 194.521 | 36.8257 | 0.697078 | 135.787 | 90.4105 | 0.729187 | 4.15373 | 90.5265 | 107.853 | 61.56115 | 5212.271 |
| 16645.1 | 16.5253 | 0.900882 | 130.744 | 3.08314 | 41.9535 | 0.334442 | 402.344 | 11.4774 | 0.827249 | 306.667 | 73.1336 | 0.960804 | 59.9557 | 190.572 | 301.097 | 52.32776 | 4466.366 |
| 11226.2 | 25.0994 | 0.940333 | 107.441 | 3.44192 | 43.2258 | 0.316918 | 226.601 | 32.7786 | 0.752006 | 290.741 | 80.9846 | 0.959371 | 34.0434 | 45.0251 | 97.7951 | 52.93266 | 4848.989 |
| 10212.7 | 23.3979 | 0.947709 | 116.325 | 1.6032 | 38.2152 | 0.513043 | 376.77 | 51.976 | 0.973749 | 225.067 | 68.2385 | 0.358042 | 142.454 | 218.714 | 51.5031 | 74.27134 | 5974.711 |
| 10858.5 | 30.7102 | 0.943016 | 150.026 | 1.37583 | 95.469 | 0.555168 | 175.837 | 78.8698 | 0.776762 | 491.568 | 24.6533 | 0.773469 | 94.8456 | 67.9998 | 413.184 | 48.01202 | 4450.112 |
| 15698.4 | 21.5701 | 0.907776 | 103.496 | 0.879965 | 51.5664 | 0.467771 | 99.5552 | 87.697 | 0.973429 | 231.378 | 85.3672 | 0.380026 | 55.9549 | 72.4659 | 69.8312 | 98.34926 | 7628.105 |
| 11922.4 | 21.2403 | 0.935261 | 134.997 | 0.489445 | 80.693 | 0.506972 | 454.427 | 56.5169 | 0.616688 | 474.302 | 39.4967 | 0.839206 | 39.8738 | 220.518 | 384.998 | 60.58032 | 5538.657 |
| 12087.9 | 23.4148 | 0.934059 | 95.2879 | 3.12741 | 95.9855 | 0.468609 | 492.137 | 10.2913 | 0.692167 | 425.854 | 4.58493 | 0.608648 | 171.912 | 313.206 | 101.39 | 57.5782 | 5935.117 |
| 16570.3 | 29.324 | 0.901437 | 142.545 | 0.469151 | 70.0255 | 0.566656 | 411.452 | 5.48824 | 0.717724 | 179.326 | 5.47018 | 0.689072 | 10.6507 | 221.629 | 74.8506 | 56.67943 | 4874.961 |
| 13943.2 | 28.8983 | 0.92056 | 109.597 | 2.95079 | 4.10976 | 0.606467 | 480.813 | 10.9055 | 0.78554 | 456.44 | 97.3042 | 0.897003 | 123.892 | 398.367 | 372.336 | 42.78304 | 3081.413 |
| 11425.1 | 28.8053 | 0.93889 | 117.394 | 1.04267 | 82.2309 | 0.479578 | 472.138 | 14.6495 | 0.509371 | 288.368 | 87.0543 | 0.948814 | 46.1988 | 414.846 | 280.237 | 59.92061 | 5743.636 |
| 11326 | 24.208 | 0.939606 | 143.894 | 3.71406 | 54.6581 | 0.438876 | 347.76 | 12.8978 | 0.767503 | 286.288 | 46.0825 | 0.851162 | 132.322 | 283.942 | 86.2218 | 42.10836 | 3988.36 |
| 14327.3 | 26.7361 | 0.917761 | 113.852 | 1.0311 | 10.348 | 0.47328 | 270.092 | 55.8357 | 0.685186 | 278.803 | 49.544 | 0.77585 | 76.3879 | 109.614 | 96.5865 | 53.53351 | 3990.408 |
| 15650.8 | 31.0014 | 0.908132 | 44.9224 | 1.20636 | 48.3898 | 0.353722 | 469.582 | 21.2141 | 0.867363 | 431.639 | 30.0926 | 0.801847 | 87.274 | 274.356 | 148.439 | 50.11058 | 4533.075 |
| 12608.4 | 28.466 | 0.930275 | 42.3167 | 1.32192 | 47.877 | 0.501363 | 326.389 | 39.8905 | 0.629372 | 517.857 | 82.557 | 0.856343 | 125.099 | 289.985 | 192.613 | 50.60532 | 4166.782 |
| 9380.69 | 20.4364 | 0.953762 | 51.5556 | 3.1236 | 55.285 | 0.389996 | 315.876 | 22.8253 | 0.69614 | 438.76 | 5.25319 | 0.856797 | 137.214 | 179.851 | 436.973 | 44.26239 | 4551.941 |
| 10699 | 14.6863 | 0.944163 | 22.6338 | 0.585977 | 34.1746 | 0.475471 | 371.158 | 44.1447 | 0.868894 | 451.408 | 25.5958 | 0.708283 | 50.5876 | 191.862 | 262.639 | 37.39198 | 3242.973 |
| 10270.2 | 32.1529 | 0.9473 | 152.622 | 0.37159 | 38.9287 | 0.611067 | 227.393 | 74.4815 | 0.785947 | 393.507 | 72.4353 | 0.584821 | 14.3943 | 194.695 | 209.736 | 63.72232 | 5028.774 |
| 10464.1 | 19.0338 | 0.945875 | 160.703 | 2.80936 | 43.3419 | 0.590335 | 112.079 | 89.5403 | 0.72238 | 445.497 | 54.8802 | 0.689366 | 133.509 | 74.8919 | 93.5589 | 56.36845 | 4413.534 |
| 16401.1 | 25.8717 | 0.902665 | 70.5748 | 2.24554 | 67.1819 | 0.33752 | 221.045 | 86.0893 | 0.851839 | 83.7362 | 9.66087 | 0.956159 | 161.633 | 123.019 | 48.255 | 52.41514 | 4853.532 |
| 12379.1 | 32.6641 | 0.93195 | 37.6003 | 3.15572 | 58.7311 | 0.355418 | 314.702 | 69.1429 | 0.81996 | 407.933 | 82.66 | 0.609818 | 57.5143 | 82.2717 | 93.7234 | 77.11876 | 6954.627 |
| 16611.9 | 32.3358 | 0.901138 | 162.518 | 0.837135 | 91.6115 | 0.355338 | 239.295 | 40.034 | 0.958045 | 416.569 | 81.1728 | 0.68426 | 36.489 | 118.246 | 369.445 | 86.55484 | 7711.027 |
| 15581.6 | 28.1567 | 0.908633 | 61.3437 | 0.105956 | 66.9869 | 0.325145 | 270.343 | 19.8698 | 0.833245 | 511.033 | 65.5781 | 0.978208 | 3.36622 | 129.855 | 325.954 | 62.63962 | 5760.642 |
| 13070.6 | 19.56 | 0.926902 | 86.192 | 0.764463 | 43.2683 | 0.444789 | 487.618 | 14.2669 | 0.971656 | 187.95 | 53.0977 | 0.334913 | 24.5214 | 104.622 | 74.8743 | 84.89613 | 7295.857 |
| 13061.8 | 22.758 | 0.926969 | 141.27 | 0.388827 | 20.418 | 0.33239 | 233.24 | 27.7699 | 0.697795 | 381.358 | 74.1246 | 0.98153 | 38.023 | 51.181 | 261.214 | 69.86849 | 5510.143 |
| 16690.8 | 20.3026 | 0.900551 | 157.361 | 2.08605 | 48.0576 | 0.46296 | 201.371 | 30.8147 | 0.829977 | 363.501 | 18.0069 | 0.707988 | 27.1555 | 184.978 | 351.344 | 56.0358 | 4663.445 |
| 16298.4 | 17.5075 | 0.903406 | 154.46 | 0.510588 | 83.7472 | 0.58633 | 468.603 | 20.598 | 0.453129 | 223.723 | 79.9601 | 0.762106 | 29.3438 | 433.928 | 146.764 | 89.78217 | 7431.711 |
| 16736.9 | 28.5672 | 0.900223 | 163.857 | 3.24097 | 44.8871 | 0.458704 | 218.319 | 69.9354 | 0.803364 | 491.549 | 14.472 | 0.699452 | 60.3616 | 145.28 | 152.485 | 61.88787 | 4973.548 |
| 15192.4 | 19.8799 | 0.911458 | 153.174 | 3.3021 | 2.73597 | 0.332201 | 136.254 | 18.2657 | 0.975282 | 454.958 | 91.6952 | 0.890007 | 5.64989 | 90.3911 | 284.164 | 55.81685 | 3997.802 |
| 13608.8 | 21.1648 | 0.922986 | 172.01 | 0.261332 | 91.9427 | 0.56405 | 189.827 | 19.6491 | 0.644899 | 161.006 | 73.9319 | 0.809192 | 20.9676 | 84.4305 | 125.199 | 68.3812 | 5892.204 |
| 11757.1 | 26.0758 | 0.93647 | 84.408 | 0.853166 | 55.0641 | 0.550492 | 417.654 | 98.0356 | 0.778246 | 355.264 | 85.601 | 0.85075 | 71.0484 | 302.076 | 216.549 | 50.62389 | 3960.8 |
| 12355.2 | 28.7583 | 0.932119 | 88.0309 | 3.08035 | 71.7571 | 0.566961 | 491.796 | 42.4868 | 0.840394 | 423.347 | 79.6039 | 0.723605 | 252.846 | 273.907 | 334.409 | 53.32583 | 4393.849 |
| 12173.4 | 28.9982 | 0.933443 | 171.751 | 1.75945 | 17.9361 | 0.447199 | 230.764 | 66.796 | 0.975899 | 350.991 | 26.4909 | 0.599773 | 160.804 | 84.2774 | 136.712 | 61.711 | 4750.524 |
| 15631.6 | 31.8207 | 0.908273 | 86.0091 | 2.06332 | 94.4263 | 0.43953 | 71.0318 | 70.2492 | 0.476106 | 132.423 | 17.3681 | 0.792638 | 100.506 | 62.5431 | 64.4235 | 83.09406 | 7970.847 |
| 9642.4 | 25.359 | 0.951862 | 139.204 | 1.38581 | 78.5528 | 0.452449 | 375.684 | 3.66418 | 0.970349 | 108.659 | 16.2174 | 0.764508 | 59.9312 | 132.929 | 47.9073 | 36.72703 | 3895.42 |
| 9704.02 | 32.0623 | 0.951422 | 146.586 | 1.15801 | 40.4186 | 0.598524 | 205.06 | 81.6631 | 0.437891 | 84.7021 | 65.7017 | 0.599996 | 21.7292 | 70.6367 | 51.3764 | 91.26148 | 7283.127 |
| 13588.9 | 33.4881 | 0.923145 | 154.649 | 0.520734 | 12.6337 | 0.660389 | 385.392 | 95.1296 | 0.755194 | 245.591 | 44.6341 | 0.390585 | 38.5809 | 165.747 | 163.116 | 96.39822 | 6760.975 |
| 14980.1 | 20.7156 | 0.913004 | 126.986 | 0.818935 | 21.0909 | 0.466819 | 393.401 | 45.4307 | 0.696919 | 403.364 | 86.0998 | 0.870366 | 44.3117 | 153.43 | 398.434 | 54.00191 | 4103.324 |
| 13872.5 | 31.4365 | 0.921078 | 76.1786 | 2.68213 | 48.1367 | 0.409101 | 164.15 | 73.6207 | 0.70516 | 71.565 | 66.7371 | 0.673345 | 45.6506 | 128.45 | 68.8803 | 69.58088 | 5905.836 |
| 13653.2 | 24.9003 | 0.922667 | 99.9685 | 0.412491 | 7.09149 | 0.414369 | 382.429 | 50.317 | 0.688344 | 331.736 | 0.187497 | 0.524764 | 9.68371 | 118.045 | 319.098 | 87.40343 | 6484.563 |
| 9876.66 | 24.8284 | 0.950156 | 61.8228 | 2.85877 | 21.5237 | 0.491643 | 380.116 | 29.5119 | 0.814344 | 278.96 | 79.1164 | 0.633927 | 187.27 | 339.113 | 133.57 | 46.78908 | 3769.621 |
| 11358.2 | 29.7033 | 0.939378 | 119.457 | 2.95976 | 39.3228 | 0.369566 | 159.864 | 25.0917 | 0.589401 | 371.647 | 14.981 | 0.829175 | 132.058 | 88.7489 | 293.451 | 60.4987 | 5562.09 |
| 13176.6 | 13.9313 | 0.926128 | 84.5647 | 1.88999 | 27.4549 | 0.379853 | 479.344 | 22.5539 | 0.931801 | 142.397 | 77.0445 | 0.75993 | 134.21 | 216.785 | 69.4456 | 44.67793 | 3724.249 |
| 9403.19 | 17.2831 | 0.953596 | 57.8174 | 0.759788 | 29.5865 | 0.304557 | 271.525 | 97.9253 | 0.769191 | 113.327 | 62.5284 | 0.956681 | 55.4173 | 136.049 | 46.5424 | 53.86679 | 4660.378 |
| 11911.4 | 14.318 | 0.935337 | 162.06 | 0.376466 | 68.0027 | 0.558598 | 490.447 | 16.7251 | 0.659816 | 134.048 | 60.4563 | 0.917385 | 28.8299 | 412.726 | 54.3829 | 50.75444 | 4444.6 |
| 16025 | 18.8862 | 0.905397 | 104.153 | 1.30388 | 65.8574 | 0.53968 | 270.476 | 34.8458 | 0.389949 | 337.817 | 29.1841 | 0.953213 | 50.5485 | 163.182 | 211.318 | 76.88834 | 6370.942 |
| 13358.9 | 17.6676 | 0.924803 | 41.481 | 1.67858 | 5.44595 | 0.447576 | 403.256 | 57.8893 | 0.420973 | 150.072 | 47.1927 | 0.642627 | 54.2791 | 303.23 | 124.788 | 91.61221 | 6712.766 |
| 14284.2 | 20.8643 | 0.91807 | 93.4334 | 0.51356 | 46.468 | 0.489767 | 446.965 | 75.7455 | 0.483913 | 209.059 | 7.14054 | 0.755734 | 36.8335 | 249.978 | 133.582 | 75.75684 | 6324.12 |
| 13112.2 | 17.9121 | 0.926599 | 65.4972 | 1.61739 | 95.1932 | 0.541105 | 373.895 | 8.23154 | 0.541722 | 419.009 | 6.44933 | 0.690625 | 45.1378 | 354.79 | 243.092 | 81.7994 | 7725.12 |
| 13981.6 | 29.936 | 0.920281 | 142.67 | 1.96014 | 15.1236 | 0.330223 | 285.492 | 11.9158 | 0.951555 | 67.997 | 3.27218 | 0.832348 | 20.4118 | 105.635 | 66.9442 | 49.15738 | 3999.871 |
| 11503.9 | 23.768 | 0.938311 | 152.238 | 0.474429 | 93.6336 | 0.413578 | 262.07 | 23.5911 | 0.924514 | 321.481 | 83.5287 | 0.746453 | 18.7972 | 160.811 | 321.005 | 62.61687 | 5964.335 |
| 10302.5 | 20.3473 | 0.947052 | 30.4755 | 0.590947 | 62.566 | 0.358106 | 390.823 | 54.8797 | 0.73272 | 470.108 | 79.4696 | 0.82099 | 11.1002 | 320.44 | 352.911 | 58.92632 | 5679.43 |
| 15241.8 | 27.8537 | 0.911106 | 165.127 | 1.58517 | 70.0219 | 0.424765 | 251.852 | 88.283 | 0.697062 | 491.052 | 62.9841 | 0.785987 | 119.841 | 232.494 | 238.22 | 79.13606 | 6678.918 |
| 16581.2 | 34.4238 | 0.901364 | 71.2603 | 3.63005 | 88.4427 | 0.545127 | 471.123 | 85.4566 | 0.742906 | 314.632 | 35.4053 | 0.832304 | 114.377 | 240.085 | 277.179 | 54.621 | 4500.002 |
| 9664.17 | 14.1679 | 0.951695 | 23.5679 | 1.68824 | 26.1239 | 0.408389 | 382.388 | 56.3468 | 0.309945 | 307.17 | 21.9028 | 0.955521 | 37.216 | 220.911 | 127.295 | 84.20731 | 7313.833 |
| 10317 | 13.9572 | 0.946943 | 35.2266 | 3.55162 | 10.3865 | 0.547694 | 183.124 | 30.4275 | 0.933588 | 290.036 | 14.6997 | 0.835745 | 239.915 | 168.575 | 252.402 | 27.89796 | 2327.956 |
| 14525.3 | 14.1694 | 0.91631 | 22.5621 | 1.34621 | 70.1336 | 0.43123 | 105.211 | 92.5117 | 0.745477 | 185.293 | 96.0736 | 0.701736 | 66.3716 | 74.4322 | 62.5838 | 67.86474 | 5857.479 |
| 14462.4 | 19.1869 | 0.916772 | 63.4403 | 2.34935 | 12.0421 | 0.317912 | 279.988 | 8.67132 | 0.765633 | 399.903 | 9.83509 | 0.657586 | 28.5888 | 51.5217 | 105.393 | 65.84968 | 5201.51 |
| 13849.4 | 24.9512 | 0.921238 | 103.401 | 0.557466 | 33.5282 | 0.556654 | 158.904 | 57.6501 | 0.764518 | 366.662 | 49.8501 | 0.590071 | 42.8083 | 117.726 | 351.952 | 59.0184 | 4524.687 |
| 16657.4 | 24.2158 | 0.900798 | 132.004 | 2.76618 | 14.5293 | 0.513328 | 306.158 | 58.1989 | 0.754663 | 272.579 | 90.1228 | 0.927864 | 80.3387 | 51.2143 | 199.15 | 41.93622 | 3029.869 |
| 11081.1 | 23.7608 | 0.941388 | 159.332 | 0.896695 | 2.63964 | 0.652698 | 328.077 | 61.597 | 0.686736 | 276.938 | 37.432 | 0.381149 | 85.1321 | 63.537 | 127.155 | 96.30038 | 6979.081 |
| 12995.9 | 16.7744 | 0.927444 | 172.671 | 0.807253 | 78.7746 | 0.593336 | 316.878 | 63.6466 | 0.666921 | 449.213 | 99.5578 | 0.655336 | 8.95068 | 96.8223 | 188.264 | 75.82911 | 6216.589 |
| 13287.5 | 33.3627 | 0.925339 | 56.7659 | 2.34467 | 8.21997 | 0.543656 | 369.984 | 1.46236 | 0.663654 | 307.33 | 85.1237 | 0.804584 | 155.458 | 186.961 | 241.865 | 50.27275 | 3755.362 |
| 10956.3 | 19.909 | 0.942293 | 29.3952 | 2.96284 | 48.0133 | 0.440865 | 90.223 | 92.411 | 0.780843 | 342.015 | 22.8253 | 0.733279 | 164.041 | 70.0103 | 216.479 | 50.08446 | 4391.556 |
| 12140.1 | 31.231 | 0.933688 | 78.5239 | 3.10167 | 65.6231 | 0.393934 | 71.0151 | 49.1414 | 0.922107 | 402.024 | 14.0237 | 0.783924 | 166.31 | 51.0024 | 193.271 | 43.32245 | 4231.314 |
| 13502.5 | 14.6698 | 0.923756 | 150.42 | 0.216357 | 10.6201 | 0.445841 | 312.854 | 39.7157 | 0.781665 | 302.295 | 36.409 | 0.528619 | 12.8448 | 160.984 | 179.524 | 91.81104 | 6810.789 |
| 10019.8 | 25.1109 | 0.949115 | 162.132 | 1.7159 | 32.4122 | 0.427632 | 117.755 | 13.6821 | 0.460454 | 176.443 | 42.4589 | 0.944987 | 4.11353 | 94.8058 | 56.5334 | 70.8907 | 6151.974 |
| 9533.58 | 34.6018 | 0.952666 | 98.7313 | 1.17388 | 30.0766 | 0.466908 | 127.262 | 98.751 | 0.747603 | 318.98 | 90.1812 | 0.576855 | 20.5575 | 84.0293 | 158.946 | 68.72339 | 5483.99 |
| 12317.9 | 13.7089 | 0.932378 | 166.885 | 1.25569 | 83.4144 | 0.602931 | 183.87 | 39.7547 | 0.957071 | 371.37 | 97.6015 | 0.539227 | 40.7978 | 154.438 | 159.251 | 58.86304 | 4955.484 |
| 13027.1 | 16.9368 | 0.927217 | 129.124 | 1.85818 | 61.0784 | 0.515758 | 212.007 | 15.7652 | 0.793286 | 387.093 | 26.0512 | 0.96421 | 148.498 | 117.182 | 279.661 | 30.9147 | 2904.473 |
| 12323.4 | 34.0498 | 0.932357 | 129.457 | 2.5436 | 76.0564 | 0.526494 | 254.473 | 45.0442 | 0.902052 | 237.775 | 57.0143 | 0.454264 | 132.511 | 112.5 | 126.56 | 67.25057 | 5718.924 |
| 14411.4 | 13.5171 | 0.917139 | 164.626 | 2.68333 | 66.152 | 0.331078 | 476.759 | 50.5368 | 0.969724 | 403.582 | 33.1212 | 0.661849 | 66.5746 | 133.097 | 274.235 | 76.15561 | 6865.85 |
| 13680.1 | 23.2088 | 0.922469 | 34.5974 | 1.03927 | 36.7296 | 0.44398 | 476.447 | 6.22194 | 0.967699 | 401.922 | 66.3975 | 0.429445 | 70.265 | 77.758 | 121.209 | 62.84956 | 5325.463 |
| 13488.8 | 14.7502 | 0.923856 | 62.907 | 3.36919 | 93.4231 | 0.561564 | 421.145 | 14.0984 | 0.713525 | 418.655 | 74.8225 | 0.97364 | 220.168 | 268.356 | 348.73 | 42.52349 | 3776.175 |
| 10320.7 | 16.3377 | 0.946917 | 42.3919 | 3.67213 | 94.5411 | 0.387632 | 315.847 | 17.9358 | 0.735519 | 383.177 | 66.4663 | 0.653641 | 13.1786 | 269.633 | 251.383 | 67.21582 | 7224.806 |
| 9620.21 | 30.157 | 0.952029 | 35.5339 | 1.69462 | 96.5168 | 0.424717 | 430.922 | 66.4368 | 0.941144 | 332.908 | 95.496 | 0.900004 | 45.6391 | 65.827 | 215.135 | 42.73835 | 4226.433 |
| 10270.8 | 15.8637 | 0.94728 | 138.774 | 0.699872 | 30.2512 | 0.529852 | 127.148 | 91.2652 | 0.794017 | 512.613 | 58.6635 | 0.92676 | 61.1449 | 105.032 | 121.561 | 41.39081 | 3335.302 |
| 16764.7 | 32.993 | 0.900027 | 102.44 | 3.55455 | 54.8919 | 0.33864 | 320.135 | 2.35003 | 0.797598 | 298.602 | 2.8128 | 0.628911 | 88.6563 | 62.1053 | 175.701 | 73.07925 | 6736.7 |
| 16427 | 13.8267 | 0.902468 | 90.7373 | 1.95568 | 51.0643 | 0.353882 | 443.881 | 74.7806 | 0.813805 | 293.612 | 15.8503 | 0.815005 | 152.141 | 391.597 | 212.943 | 57.04807 | 4989.236 |
| 13905.8 | 32.2731 | 0.920836 | 71.6624 | 0.548903 | 24.1064 | 0.325071 | 341.131 | 6.73267 | 0.461931 | 509.162 | 30.0859 | 0.999586 | 7.32512 | 196.236 | 248.099 | 77.01044 | 6412.346 |
| 9604.77 | 32.6156 | 0.952145 | 168.831 | 1.5262 | 19.4021 | 0.399548 | 126.582 | 59.5845 | 0.779382 | 149.521 | 52.0218 | 0.747004 | 103.916 | 80.3454 | 124.779 | 63.73008 | 5169.828 |
| 15444.2 | 34.1037 | 0.90964 | 172.209 | 3.41691 | 39.1718 | 0.384078 | 463.581 | 2.53397 | 0.463176 | 225.312 | 30.3992 | 0.925247 | 143.833 | 235.857 | 72.4097 | 87.68853 | 7272.124 |
| 12508.4 | 28.1241 | 0.931003 | 152.853 | 2.15678 | 21.6165 | 0.558923 | 288.262 | 72.2275 | 0.636027 | 457.572 | 10.7692 | 0.901034 | 62.0064 | 259.766 | 409.895 | 42.40513 | 3385.454 |
| 13159.9 | 18.2824 | 0.926251 | 51.8793 | 2.92829 | 10.2754 | 0.352204 | 314.133 | 66.664 | 0.484148 | 334.017 | 71.2434 | 0.683299 | 134.322 | 270.117 | 290.965 | 98.31786 | 7383.051 |
| 13922 | 34.4765 | 0.920722 | 91.8359 | 3.17161 | 48.0544 | 0.361048 | 197.361 | 33.4625 | 0.746843 | 518.565 | 24.8359 | 0.780828 | 159.061 | 60.7316 | 502.32 | 56.89823 | 5179.121 |
| 15465.9 | 24.1761 | 0.909471 | 124.182 | 2.68786 | 10.7651 | 0.707425 | 462.87 | 94.7097 | 0.996102 | 434.622 | 31.9238 | 0.643899 | 19.6138 | 271.232 | 376.716 | 68.93681 | 4588.735 |
| 10356.5 | 14.4815 | 0.946655 | 68.4542 | 2.12556 | 0.059006 | 0.427689 | 438.726 | 87.1031 | 0.635553 | 439.062 | 51.1454 | 0.64299 | 96.4638 | 320.513 | 144.742 | 64.18185 | 4720.156 |
| 12222.2 | 23.1481 | 0.933081 | 69.7782 | 1.42767 | 32.152 | 0.409005 | 221.663 | 92.1391 | 0.562325 | 498.852 | 73.9656 | 0.948392 | 89.9902 | 115.965 | 426.152 | 58.29642 | 4796.114 |
| 16693.8 | 31.8892 | 0.900541 | 162.591 | 0.351099 | 10.4557 | 0.693675 | 241.889 | 17.5818 | 0.778708 | 286.794 | 7.58679 | 0.388158 | 4.97884 | 205.309 | 147.436 | 84.36902 | 6009.967 |
| 9636.68 | 33.357 | 0.951914 | 167.333 | 0.176575 | 87.2891 | 0.524949 | 403.785 | 74.5891 | 0.577069 | 390.045 | 71.9155 | 0.82135 | 16.9558 | 298.494 | 85.1157 | 79.39351 | 7055.731 |
| 10801.8 | 13.1773 | 0.943414 | 57.2451 | 2.60608 | 82.7872 | 0.546962 | 271.226 | 30.7424 | 0.52122 | 388.684 | 42.1341 | 0.940991 | 97.7371 | 253.697 | 269.786 | 58.36512 | 5365.449 |
| 15217.4 | 17.5799 | 0.911274 | 148.766 | 2.36231 | 92.7692 | 0.657385 | 451.279 | 75.9396 | 0.960225 | 488.42 | 57.5892 | 0.556174 | 18.4707 | 184.217 | 485.312 | 73.40021 | 5621.64 |
| 9524.95 | 16.9936 | 0.95271 | 69.9102 | 2.77089 | 49.3712 | 0.602015 | 415.736 | 20.9954 | 0.90967 | 327.643 | 44.0479 | 0.628754 | 273.03 | 290.323 | 294.077 | 50.7039 | 4303.532 |
| 10917.1 | 20.4864 | 0.942579 | 165.835 | 1.93063 | 84.9934 | 0.387733 | 148.031 | 60.6852 | 0.702627 | 428.077 | 12.2439 | 0.82949 | 22.105 | 108.545 | 92.5368 | 68.99904 | 6782.098 |
| 16521.9 | 24.7452 | 0.901785 | 27.5573 | 0.313011 | 49.0356 | 0.351059 | 408.992 | 33.3114 | 0.922234 | 416.371 | 70.8281 | 0.514481 | 9.23775 | 233.041 | 45.1955 | 81.39275 | 6949.678 |
| 14617.9 | 31.4301 | 0.915652 | 143.101 | 2.24936 | 2.33532 | 0.500904 | 204.38 | 25.2691 | 0.969028 | 298.049 | 30.7215 | 0.698501 | 15.2971 | 167.748 | 197.137 | 37.83951 | 2848.46 |
| 11344.5 | 33.8227 | 0.939483 | 105.041 | 0.29823 | 42.4658 | 0.487999 | 386.158 | 0.20208 | 0.476684 | 513.94 | 75.7099 | 0.960928 | 14.5462 | 135.148 | 350.206 | 60.36004 | 5248.047 |
| 15758.7 | 18.7025 | 0.907335 | 85.0661 | 3.6554 | 79.506 | 0.537032 | 309.102 | 8.10563 | 0.491263 | 233.41 | 29.1568 | 0.801119 | 45.9256 | 248.86 | 225.034 | 78.95804 | 6897.109 |
| 13066.8 | 16.5219 | 0.926928 | 68.0083 | 0.709526 | 47.5314 | 0.40304 | 311.943 | 73.2512 | 0.743469 | 446.229 | 33.5037 | 0.886078 | 21.0367 | 305.498 | 60.6748 | 47.53514 | 4228.138 |
| 12183.6 | 33.3881 | 0.933374 | 72.093 | 1.22357 | 72.9346 | 0.408401 | 97.0576 | 17.6813 | 0.804808 | 71.6519 | 39.5703 | 0.974094 | 73.2505 | 52.1279 | 63.0541 | 37.2907 | 3807.074 |
| 11114 | 34.2163 | 0.941161 | 97.9647 | 1.77132 | 94.9198 | 0.344242 | 451.468 | 50.679 | 0.637307 | 440.196 | 28.4895 | 0.909322 | 121.971 | 149.339 | 166.662 | 64.88369 | 7005.697 |
| 10308.4 | 28.6061 | 0.947018 | 84.4734 | 2.9707 | 13.6998 | 0.390944 | 280.467 | 37.9465 | 0.836634 | 399.743 | 26.4471 | 0.406113 | 26.904 | 216.843 | 235.905 | 79.60817 | 6408.097 |
| 16610.3 | 26.4446 | 0.901143 | 149.658 | 0.697761 | 64.0107 | 0.592306 | 249.091 | 14.4938 | 0.911208 | 221.161 | 11.9934 | 0.961724 | 46.6262 | 79.0957 | 128.17 | 30.97317 | 2717.102 |
| 9796.92 | 28.0934 | 0.95074 | 124.657 | 1.3791 | 73.7657 | 0.56437 | 302.079 | 24.9092 | 0.890464 | 451.731 | 24.1379 | 0.747913 | 32.8119 | 120.541 | 280.23 | 34.18352 | 3234.724 |
| 12361.2 | 31.7849 | 0.932079 | 153.82 | 2.32465 | 43.6658 | 0.41157 | 151.387 | 43.963 | 0.967844 | 513.506 | 20.262 | 0.503895 | 150.287 | 113.938 | 115.969 | 71.51364 | 6111.166 |
| 15508.1 | 23.0446 | 0.909162 | 118.159 | 3.63025 | 65.6057 | 0.427687 | 190.941 | 20.9303 | 0.755832 | 181.273 | 66.0881 | 0.755737 | 90.3419 | 105.115 | 132.26 | 53.74047 | 4889.381 |
| 12750.8 | 32.3215 | 0.929244 | 51.5049 | 0.236767 | 19.2398 | 0.361966 | 84.7905 | 35.8652 | 0.704933 | 75.2688 | 38.5019 | 0.522175 | 2.18829 | 45.0229 | 45.5849 | 86.61159 | 6927.171 |
| 9525.96 | 22.9358 | 0.952707 | 158.693 | 0.156976 | 85.5453 | 0.715103 | 230.06 | 40.5602 | 0.87361 | 301.189 | 51.0927 | 0.920137 | 4.93312 | 68.6379 | 99.563 | 31.69418 | 2801.377 |
| 12290.7 | 23.4111 | 0.932582 | 98.3703 | 3.48183 | 2.97791 | 0.426273 | 346.008 | 34.765 | 0.881913 | 512.04 | 11.3848 | 0.539628 | 167.576 | 252.266 | 220.447 | 51.67291 | 3944.563 |
| 15473.3 | 30.9003 | 0.909424 | 59.1875 | 0.857439 | 88.4054 | 0.325115 | 251.389 | 43.9107 | 0.86264 | 81.6242 | 17.4253 | 0.843194 | 78.1409 | 42.467 | 79.3393 | 58.54466 | 5975.058 |
| 10082.9 | 28.5595 | 0.948659 | 60.1736 | 3.49181 | 2.62188 | 0.485114 | 401.75 | 7.9061 | 0.677123 | 203.767 | 36.6856 | 0.864942 | 58.4775 | 157.479 | 63.9671 | 33.50443 | 2745.422 |
| 15328.6 | 17.2682 | 0.910465 | 27.3626 | 1.63638 | 49.9763 | 0.503035 | 211.195 | 37.6111 | 0.896525 | 459.903 | 83.2844 | 0.932039 | 75.2027 | 188.531 | 303.051 | 35.4221 | 2870.517 |
| 11233.7 | 21.4864 | 0.940275 | 134.16 | 2.07902 | 98.8833 | 0.583827 | 211.106 | 12.964 | 0.988377 | 474.171 | 61.6656 | 0.797005 | 206.228 | 137.457 | 441.514 | 32.53292 | 3018.483 |
| 12676.6 | 30.0589 | 0.929781 | 99.6615 | 2.933 | 5.64509 | 0.55948 | 491.091 | 2.85286 | 0.819348 | 509.594 | 92.5354 | 0.83881 | 128.269 | 471.059 | 334.544 | 38.77179 | 2910.759 |
| 10277.5 | 23.3305 | 0.947237 | 46.9828 | 1.11217 | 72.579 | 0.424354 | 187.292 | 30.8103 | 0.808676 | 479.537 | 9.62167 | 0.873971 | 51.9938 | 47.9686 | 373.324 | 36.88731 | 3901.434 |
| 11016.4 | 30.4119 | 0.941867 | 96.1 | 0.918091 | 42.9111 | 0.319639 | 416.608 | 52.2146 | 0.797767 | 83.9201 | 36.8027 | 0.981445 | 61.7409 | 348.418 | 45.0798 | 50.90018 | 4692.12 |
| 16294.9 | 34.4461 | 0.903449 | 59.3491 | 0.80541 | 52.4032 | 0.448178 | 177.224 | 65.087 | 0.597192 | 244.327 | 4.45818 | 0.866293 | 7.91494 | 96.8854 | 131.185 | 55.58728 | 4825.726 |
| 10185.2 | 25.1088 | 0.94791 | 84.0157 | 2.55718 | 48.0571 | 0.335702 | 400.482 | 84.2366 | 0.703978 | 147.418 | 20.2364 | 0.908245 | 11.6776 | 196.982 | 115.896 | 55.16183 | 5210.432 |
| 14112.9 | 15.9253 | 0.919313 | 124.068 | 1.16642 | 2.80602 | 0.453228 | 444.099 | 73.3491 | 0.939259 | 232.756 | 27.8042 | 0.635963 | 43.2396 | 260.614 | 78.1847 | 52.36914 | 3772.992 |
| 9596.04 | 20.385 | 0.952195 | 102.776 | 3.05603 | 31.3041 | 0.45552 | 243.61 | 84.9921 | 0.828169 | 388.734 | 64.089 | 0.91144 | 74.2083 | 87.4139 | 133.75 | 37.19379 | 3114.379 |
| 16006 | 27.8369 | 0.905543 | 151.39 | 3.23715 | 90.7852 | 0.337334 | 204.42 | 60.6139 | 0.817007 | 314.772 | 79.4967 | 0.774637 | 40.5683 | 140.995 | 60.4619 | 79.5909 | 7458.977 |
| 15952.2 | 21.0141 | 0.905928 | 117.357 | 1.80872 | 1.72066 | 0.481394 | 184.715 | 39.3269 | 0.943966 | 230.621 | 47.9043 | 0.908864 | 89.3598 | 142.945 | 146.923 | 32.28101 | 2378.896 |
| 10418.1 | 29.3585 | 0.94622 | 74.2674 | 0.385372 | 38.4212 | 0.511724 | 426.218 | 75.0973 | 0.738667 | 486.326 | 84.9745 | 0.644601 | 20.8987 | 367.53 | 229.481 | 56.1097 | 4535.327 |
| 14658.2 | 34.6027 | 0.915363 | 46.7382 | 1.24674 | 29.1507 | 0.493024 | 411.06 | 36.0535 | 0.66915 | 385.805 | 80.7468 | 0.965084 | 89.0132 | 275.145 | 304.968 | 41.41671 | 3240.214 |
| 15334.5 | 16.9324 | 0.910422 | 33.7164 | 3.7533 | 2.36157 | 0.441305 | 364.977 | 72.9538 | 0.984523 | 376.326 | 82.7579 | 0.945032 | 105 | 265.132 | 251.995 | 39.07471 | 2744.741 |
| 13016.6 | 17.8586 | 0.927295 | 86.3248 | 0.756156 | 74.9497 | 0.339049 | 68.4171 | 33.7856 | 0.936529 | 209.77 | 20.7728 | 0.865282 | 15.9648 | 62.3872 | 195.811 | 49.65317 | 5025.817 |
| 9631.25 | 30.1081 | 0.951949 | 73.0427 | 2.26756 | 68.9383 | 0.435321 | 170.011 | 54.4657 | 0.871962 | 498.481 | 72.1393 | 0.665284 | 160.287 | 160.909 | 402.404 | 50.92667 | 4825.613 |
| 12685.4 | 21.9654 | 0.929708 | 171.63 | 1.1825 | 41.6532 | 0.481263 | 345.011 | 15.8376 | 0.811965 | 415.489 | 96.9334 | 0.591382 | 95.7591 | 208.244 | 212.564 | 72.374 | 5901.436 |
| 15501.9 | 30.1892 | 0.909215 | 159.133 | 0.85668 | 5.52407 | 0.642364 | 486.884 | 6.0102 | 0.877405 | 199.404 | 8.21461 | 0.76052 | 19.3801 | 173.35 | 144.272 | 33.01077 | 2569.255 |
| 11584.8 | 15.7423 | 0.937715 | 163.688 | 1.52928 | 68.4682 | 0.689707 | 239.114 | 79.8875 | 0.867074 | 477.957 | 90.5239 | 0.613529 | 131.836 | 147.132 | 456.269 | 64.51888 | 4850.955 |
| 10577.9 | 18.8215 | 0.945046 | 150.495 | 1.92876 | 57.6181 | 0.421858 | 353.191 | 46.4823 | 0.67695 | 433.221 | 23.5718 | 0.927313 | 160.512 | 306.039 | 417.417 | 50.92251 | 4780.894 |
| 9531.75 | 25.5785 | 0.952668 | 145.797 | 1.00294 | 21.3965 | 0.567866 | 169.636 | 16.6537 | 0.937504 | 281.606 | 46.3718 | 0.96583 | 59.2918 | 112.859 | 87.1831 | 27.35437 | 2368.391 |
| 14591 | 34.9524 | 0.915852 | 117.377 | 1.5451 | 39.7557 | 0.397073 | 414.033 | 42.7551 | 0.481278 | 495.61 | 69.5049 | 0.793585 | 69.952 | 211.641 | 102.617 | 89.2124 | 7394.581 |
| 17254.2 | 33.1346 | 0.896463 | 166.458 | 2.09712 | 64.1689 | 0.657384 | 462.967 | 15.9105 | 0.664511 | 508.127 | 8.06063 | 0.512018 | 208.983 | 451.637 | 198.41 | 87.03684 | 6668.706 |
| 14806.8 | 34.7202 | 0.914281 | 65.0832 | 1.25447 | 24.1281 | 0.342235 | 147.564 | 43.8092 | 0.708218 | 422.733 | 47.5326 | 0.556107 | 51.6361 | 134.181 | 239.821 | 90.17614 | 7165.326 |
| 22781.4 | 26.8108 | 0.856223 | 87.6888 | 1.5039 | 54.513 | 0.505279 | 337.283 | 44.8723 | 0.944077 | 477.635 | 71.4183 | 0.73583 | 125.234 | 115.315 | 452.396 | 48.27903 | 3595.843 |
| 29759.8 | 17.0381 | 0.80542 | 102.72 | 0.102536 | 82.1735 | 0.470854 | 256.52 | 31.7699 | 0.642496 | 516.304 | 42.804 | 0.8534 | 5.66777 | 209.762 | 286.592 | 84.11002 | 6377.87 |
| 27554.5 | 22.1856 | 0.821476 | 145.198 | 2.60362 | 45.3333 | 0.536059 | 89.2023 | 54.8315 | 0.946853 | 272.158 | 80.4714 | 0.722995 | 164.121 | 58.2627 | 256.705 | 54.22648 | 3755.573 |
| 19961.1 | 20.7747 | 0.876747 | 135.748 | 3.47107 | 41.3985 | 0.457607 | 343.735 | 57.9398 | 0.828366 | 303.263 | 43.3703 | 0.717903 | 31.8275 | 236.692 | 285.652 | 55.6964 | 4334.592 |
| 25740.1 | 30.2006 | 0.834689 | 168.949 | 0.778278 | 98.2371 | 0.741049 | 280.627 | 73.7651 | 0.615392 | 430.631 | 83.1793 | 0.879199 | 60.0864 | 174.355 | 326.182 | 71.66488 | 4861.476 |
| 26749.4 | 18.31 | 0.827334 | 143.819 | 2.62002 | 95.0053 | 0.546628 | 323.693 | 36.785 | 0.876876 | 460.558 | 2.34435 | 0.42397 | 107.005 | 136.048 | 321.243 | 89.73587 | 6782.697 |
| 30230.1 | 33.0176 | 0.802009 | 157.428 | 0.354644 | 74.2276 | 0.625383 | 316.991 | 16.5928 | 0.786466 | 199.021 | 64.8084 | 0.722371 | 5.80612 | 91.1626 | 172.528 | 69.29607 | 4821.051 |
| 17237.2 | 34.897 | 0.89659 | 61.9119 | 1.06311 | 32.0583 | 0.340776 | 423.254 | 69.9415 | 0.593273 | 449.8 | 38.1439 | 0.802818 | 65.6988 | 293.131 | 219.216 | 81.00192 | 6468.4 |
| 17426.1 | 21.2518 | 0.8952 | 97.2898 | 0.821192 | 14.4899 | 0.528628 | 249.16 | 98.8788 | 0.936145 | 324.097 | 3.5483 | 0.585023 | 30.8951 | 63.0713 | 269.637 | 56.33427 | 3936.855 |
| 27883.1 | 15.7552 | 0.81908 | 159.024 | 0.224299 | 87.0242 | 0.660957 | 160.906 | 28.401 | 0.678901 | 290.045 | 7.69148 | 0.621874 | 12.4194 | 79.614 | 241.484 | 84.59267 | 6042.097 |
| 12741.6 | 13.9016 | 0.929294 | 168.101 | 0.246804 | 8.25695 | 0.413831 | 242.435 | 70.3057 | 0.979835 | 163.784 | 85.5115 | 0.70059 | 16.7214 | 163.738 | 99.1094 | 70.77863 | 5143.501 |
| 29134.1 | 14.3451 | 0.809973 | 47.7408 | 0.544983 | 69.0579 | 0.325483 | 391.458 | 75.9458 | 0.868911 | 189.648 | 6.91824 | 0.87087 | 40.8292 | 180.186 | 67.8668 | 70.30188 | 5753.662 |
| 13523.4 | 28.0896 | 0.923614 | 86.8434 | 1.95774 | 26.7427 | 0.376552 | 211.063 | 39.7608 | 0.72258 | 148.271 | 38.0329 | 0.453175 | 140.878 | 94.025 | 73.4491 | 95.09807 | 7711.236 |
| 24029.4 | 14.3646 | 0.84713 | 78.1384 | 0.583059 | 98.7389 | 0.423556 | 142.264 | 34.1451 | 0.90916 | 264.134 | 46.6617 | 0.711413 | 23.4764 | 100.875 | 197.653 | 62.04402 | 5539.352 |
| 23585.7 | 29.9577 | 0.850372 | 65.9314 | 2.6495 | 22.6638 | 0.534452 | 419.468 | 79.0779 | 0.802365 | 344.018 | 80.1715 | 0.622996 | 93.9509 | 135.418 | 341.149 | 77.26691 | 5083.465 |
| 21968.7 | 21.6538 | 0.862134 | 149.332 | 1.8773 | 69.4677 | 0.601971 | 471.763 | 73.8483 | 0.810098 | 192.392 | 0.326864 | 0.927547 | 16.7344 | 124.751 | 79.2857 | 41.29966 | 3177.02 |
| 25611.2 | 22.0623 | 0.835621 | 167.004 | 1.73576 | 59.5274 | 0.476555 | 213.862 | 59.7884 | 0.744599 | 229.114 | 97.0161 | 0.906724 | 102.456 | 203.29 | 83.4829 | 68.71778 | 5014.828 |
| 17491.2 | 19.4606 | 0.894725 | 37.5532 | 0.586873 | 34.0836 | 0.444646 | 348.993 | 10.6552 | 0.721184 | 178.613 | 66.0416 | 0.918398 | 31.8358 | 340.899 | 159.856 | 42.76568 | 3490.097 |
| 11367.2 | 27.1477 | 0.939309 | 164.946 | 2.19947 | 8.5622 | 0.693992 | 485.501 | 53.0695 | 0.871797 | 360.729 | 93.9783 | 0.862519 | 161.768 | 258.264 | 283.935 | 40.84703 | 2970.094 |
| 24329.6 | 18.6532 | 0.844947 | 52.6109 | 2.37311 | 31.2435 | 0.422208 | 141.381 | 12.8691 | 0.734751 | 286.972 | 32.4955 | 0.888021 | 14.3115 | 51.9415 | 90.332 | 49.50888 | 3757.856 |
| 27199.1 | 30.4642 | 0.824069 | 171.49 | 0.944531 | 81.5123 | 0.4468 | 299.896 | 10.6864 | 0.520861 | 148.664 | 14.8819 | 0.986302 | 17.0105 | 278.2 | 87.4812 | 96.84355 | 7496.603 |
| 27829.1 | 28.7964 | 0.819482 | 172.257 | 2.20646 | 48.2857 | 0.597323 | 116.141 | 6.72818 | 0.591162 | 284.88 | 80.2476 | 0.983436 | 111.975 | 74.9722 | 182.441 | 59.23647 | 4121.803 |
| 17654.9 | 31.7989 | 0.893545 | 132.642 | 3.34957 | 37.9335 | 0.355826 | 463.932 | 20.6315 | 0.91111 | 381.536 | 2.49026 | 0.543624 | 109.748 | 45.2088 | 265.541 | 75.9349 | 6290.095 |
| 12734.7 | 31.2297 | 0.929359 | 153.891 | 3.18272 | 36.6622 | 0.461221 | 390.434 | 96.3814 | 0.393316 | 338.898 | 96.6805 | 0.848465 | 23.6759 | 104.002 | 282.988 | 94.40669 | 7565.756 |
| 11110.4 | 17.06 | 0.941169 | 88.3805 | 3.3027 | 87.3965 | 0.375698 | 195.104 | 91.7499 | 0.97517 | 429.159 | 38.6883 | 0.811298 | 92.7558 | 47.4363 | 72.2933 | 48.9432 | 4838.297 |
| 17549.1 | 30.8801 | 0.894314 | 38.655 | 2.72669 | 15.5094 | 0.396899 | 342.252 | 70.0332 | 0.616954 | 362.002 | 43.6548 | 0.946573 | 119.184 | 261.361 | 253.915 | 55.68835 | 4135.603 |
| 20601.5 | 30.8434 | 0.872095 | 62.7976 | 0.131034 | 77.5028 | 0.483476 | 467.867 | 86.8165 | 0.61401 | 203.516 | 35.2151 | 0.769875 | 9.02493 | 103.535 | 182.646 | 75.51782 | 6227.093 |
| 25882.4 | 27.8376 | 0.833651 | 150.309 | 3.24522 | 83.3885 | 0.421382 | 125.895 | 19.1049 | 0.679024 | 78.4115 | 76.3962 | 0.832736 | 124.672 | 47.7876 | 78.2641 | 77.22228 | 6334.215 |
| 14378.6 | 16.4977 | 0.917379 | 167.959 | 2.70087 | 3.23789 | 0.512003 | 352.763 | 11.5032 | 0.664349 | 429.757 | 13.1207 | 0.720867 | 138.557 | 217.968 | 64.1429 | 52.81444 | 3976.323 |
| 16733.4 | 13.4073 | 0.900237 | 77.6981 | 0.35771 | 12.5219 | 0.475008 | 180.079 | 84.8957 | 0.499041 | 120.151 | 83.5533 | 0.776688 | 4.32676 | 93.563 | 50.4995 | 78.38955 | 5556.428 |
| 21510 | 23.8554 | 0.865475 | 153.401 | 1.88711 | 86.3998 | 0.53228 | 388.726 | 72.6251 | 0.840561 | 514.323 | 75.3852 | 0.815025 | 88.515 | 292.488 | 415.815 | 55.29272 | 4411.288 |
| 12145.5 | 17.3869 | 0.933635 | 133.483 | 2.28172 | 48.9279 | 0.419402 | 454.186 | 41.8346 | 0.918127 | 300.723 | 49.8964 | 0.879218 | 10.3173 | 182.048 | 189.806 | 40.049 | 3605.007 |
| 21642.1 | 20.9749 | 0.864511 | 119.496 | 1.55625 | 17.9827 | 0.341048 | 274.942 | 56.4369 | 0.992636 | 107.012 | 7.23237 | 0.871859 | 32.066 | 234.976 | 52.7228 | 56.46018 | 4099.337 |
| 30271.2 | 25.1169 | 0.801702 | 130.205 | 2.96168 | 18.0058 | 0.443977 | 410.806 | 93.9524 | 0.891636 | 136.724 | 35.2577 | 0.855761 | 55.2123 | 238.266 | 67.5347 | 54.67949 | 3566.853 |
| 17157.3 | 13.758 | 0.897152 | 156.883 | 2.73288 | 84.0797 | 0.408455 | 283.589 | 36.7486 | 0.529878 | 156.348 | 30.8964 | 0.839797 | 66.3349 | 108.813 | 77.4616 | 87.64814 | 7986.803 |
| 11178 | 18.3172 | 0.940678 | 85.9312 | 0.254029 | 24.6985 | 0.352543 | 338.854 | 50.3456 | 0.987682 | 245.819 | 66.052 | 0.502923 | 8.91267 | 227.715 | 150.588 | 77.96524 | 6315.223 |
| 24259.6 | 16.8134 | 0.845456 | 47.7051 | 1.31187 | 73.2272 | 0.347861 | 238.864 | 32.4426 | 0.891761 | 515.548 | 14.6271 | 0.721192 | 116.057 | 114.988 | 190.863 | 68.4335 | 5992.157 |
| 22927.6 | 20.8345 | 0.855154 | 115.047 | 0.987378 | 71.5599 | 0.384025 | 404.349 | 70.0851 | 0.578234 | 436.828 | 41.5521 | 0.944986 | 89.0513 | 158.976 | 226.386 | 83.03834 | 6873.175 |
| 14164.4 | 15.9124 | 0.918939 | 20.9751 | 0.969159 | 22.5611 | 0.387358 | 331.862 | 87.9093 | 0.527233 | 261.709 | 38.5754 | 0.897046 | 66.4595 | 244.735 | 193.308 | 66.4229 | 5248.948 |
| 16334.9 | 16.912 | 0.90314 | 36.7875 | 1.80219 | 75.2901 | 0.683752 | 449.633 | 48.7606 | 0.973268 | 518.509 | 1.40038 | 0.653216 | 25.3765 | 284.613 | 388.506 | 60.64565 | 4766.938 |
| 29302.5 | 17.6924 | 0.808749 | 141.105 | 0.579904 | 3.75997 | 0.459618 | 119.241 | 8.75957 | 0.557101 | 403.383 | 96.0586 | 0.816322 | 18.8725 | 104.773 | 178.274 | 96.27644 | 5911.357 |
| 15780 | 21.3146 | 0.907182 | 130.918 | 2.26388 | 26.651 | 0.539974 | 176.762 | 88.749 | 0.695235 | 146.166 | 96.4254 | 0.641308 | 87.8294 | 106.771 | 130.947 | 70.78879 | 5039.464 |
| 12295.4 | 28.6492 | 0.932554 | 155.919 | 3.14935 | 37.771 | 0.340062 | 130.394 | 91.6302 | 0.963224 | 147.352 | 24.7334 | 0.488419 | 41.1089 | 88.8983 | 86.9219 | 94.90494 | 7794.537 |
| 20727 | 23.2437 | 0.871174 | 124.549 | 1.42832 | 0.402922 | 0.493347 | 375.954 | 9.62982 | 0.632866 | 105.412 | 46.0386 | 0.726675 | 25.051 | 116.735 | 53.234 | 61.27655 | 4148.954 |
| 30212 | 33.9799 | 0.802142 | 163.909 | 0.174959 | 43.5879 | 0.736547 | 347.163 | 80.3317 | 0.420409 | 230.952 | 76.985 | 0.976535 | 2.33617 | 281.864 | 149.259 | 91.6664 | 5777.878 |
| 24001 | 26.241 | 0.847344 | 61.1721 | 2.65054 | 25.2522 | 0.358434 | 496.184 | 79.498 | 0.636779 | 254.218 | 23.5937 | 0.967844 | 116.441 | 294.231 | 145.504 | 66.19914 | 4801.624 |
| 17724.6 | 21.7783 | 0.893028 | 117.796 | 0.389059 | 15.4975 | 0.323233 | 347.917 | 55.9889 | 0.987316 | 236.821 | 0.43498 | 0.750138 | 35.7646 | 112.863 | 194.353 | 68.01553 | 5030.973 |
| 16977.7 | 28.0609 | 0.89847 | 161.23 | 3.26789 | 91.7363 | 0.513106 | 188.921 | 7.32437 | 0.859075 | 517.069 | 68.6061 | 0.478304 | 31.6657 | 78.9644 | 113.159 | 75.50456 | 6734.16 |
| 22590.4 | 30.2492 | 0.857617 | 68.2021 | 1.38804 | 80.2221 | 0.632553 | 495.718 | 82.7889 | 0.901468 | 323.723 | 94.8545 | 0.626062 | 131.766 | 388.277 | 309.523 | 91.36815 | 6364.889 |
| 22132.3 | 34.4428 | 0.860956 | 121.786 | 1.66631 | 53.3911 | 0.437212 | 262.928 | 68.5907 | 0.738911 | 444.179 | 1.05897 | 0.959371 | 153.916 | 115.434 | 147.567 | 51.69196 | 4165.558 |
| 22145.4 | 29.6678 | 0.860855 | 57.2739 | 1.08605 | 3.07684 | 0.312358 | 485.691 | 34.5077 | 0.90602 | 109.754 | 4.24215 | 0.501174 | 44.279 | 354.859 | 108.753 | 93.19725 | 6190.389 |
| 15298.4 | 19.5107 | 0.910686 | 44.0785 | 1.74436 | 98.1023 | 0.471842 | 311.141 | 66.0294 | 0.880287 | 187.196 | 42.8369 | 0.792708 | 108.528 | 298.417 | 57.5889 | 43.91748 | 4068.904 |
| 23911.6 | 14.4604 | 0.847988 | 112.849 | 0.995979 | 93.1304 | 0.300501 | 60.6406 | 26.1175 | 0.991443 | 287.752 | 12.8306 | 0.900679 | 56.7208 | 45.3342 | 215.01 | 78.83791 | 7237.963 |
| 20072.4 | 25.9809 | 0.875941 | 159.838 | 0.930549 | 46.6764 | 0.674041 | 301.239 | 20.506 | 0.825773 | 343.911 | 3.76024 | 0.668542 | 14.725 | 126.307 | 130.568 | 49.24751 | 3675.431 |
| 16731.7 | 30.8798 | 0.900264 | 148.939 | 2.22516 | 13.1008 | 0.394778 | 389.351 | 38.8149 | 0.704244 | 474.323 | 19.5265 | 0.928845 | 54.6556 | 101.735 | 217.048 | 53.76386 | 4051.977 |
| 29855.9 | 31.8536 | 0.804731 | 148.491 | 2.88064 | 53.8854 | 0.586564 | 471.543 | 58.3967 | 0.732718 | 277.037 | 72.4248 | 0.941245 | 238.66 | 234.113 | 88.8121 | 54.60484 | 3663.473 |
| 29903.6 | 19.7581 | 0.804374 | 109.986 | 2.19903 | 87.2727 | 0.459565 | 323.446 | 66.9355 | 0.938303 | 217.329 | 39.3868 | 0.926534 | 104.684 | 166.326 | 184.553 | 48.56866 | 3887.814 |
| 29881.4 | 30.6601 | 0.804545 | 141.949 | 1.23216 | 59.1822 | 0.633472 | 152.489 | 9.13827 | 0.929068 | 161.773 | 63.2026 | 0.885715 | 64.7368 | 113.794 | 112.915 | 41.46263 | 2879.639 |
| 28916.7 | 15.0755 | 0.811556 | 84.3317 | 0.977724 | 86.5876 | 0.473673 | 356.231 | 8.21318 | 0.778194 | 508.735 | 43.6452 | 0.853127 | 79.523 | 190.194 | 406.095 | 51.57148 | 4255.881 |
| 14249.4 | 34.5083 | 0.918338 | 55.3491 | 2.51788 | 99.6323 | 0.416928 | 328.952 | 39.2815 | 0.994389 | 90.8195 | 2.29255 | 0.508517 | 4.40569 | 144.647 | 69.5574 | 66.09237 | 6744.062 |
| 14489.2 | 13.285 | 0.916573 | 146.053 | 3.0504 | 87.268 | 0.527188 | 281.283 | 1.16416 | 0.692886 | 246.1 | 63.1495 | 0.783356 | 140.623 | 151.117 | 61.0314 | 47.65104 | 4362.786 |
| 13310.3 | 19.3186 | 0.925157 | 120.188 | 1.24339 | 16.3218 | 0.534744 | 384.93 | 81.1518 | 0.940468 | 423.427 | 48.0035 | 0.580598 | 78.2932 | 198.749 | 111.599 | 51.67139 | 3797.734 |
| 25074.8 | 28.0393 | 0.83953 | 66.5675 | 3.61719 | 43.5195 | 0.569815 | 366.405 | 16.9082 | 0.973998 | 470.302 | 39.9661 | 0.807882 | 131.843 | 310.512 | 283.764 | 40.18021 | 2935.218 |
| 15419.4 | 22.2675 | 0.909808 | 62.1112 | 1.15927 | 96.3658 | 0.484915 | 429.187 | 50.2677 | 0.505035 | 270.987 | 40.6064 | 0.871595 | 104.905 | 59.2503 | 250.08 | 63.21115 | 5720.121 |
| 11414.2 | 29.8859 | 0.93897 | 98.0967 | 2.48403 | 2.06375 | 0.423074 | 297.293 | 49.7004 | 0.951875 | 449.75 | 78.3215 | 0.356087 | 20.9618 | 123.235 | 114.351 | 82.16063 | 5935.437 |
| 23083.5 | 32.2164 | 0.854029 | 39.0743 | 0.834477 | 98.8447 | 0.47487 | 325.061 | 55.5571 | 0.677099 | 516.278 | 37.0294 | 0.769985 | 17.3385 | 249.659 | 266.916 | 64.80699 | 5649.698 |
| 26934.7 | 28.2916 | 0.825992 | 126.203 | 0.965816 | 98.556 | 0.519212 | 497.152 | 65.226 | 0.782721 | 447.303 | 31.6568 | 0.958397 | 91.254 | 132.614 | 174.803 | 51.37709 | 4154.132 |
| 23225 | 18.316 | 0.852987 | 79.4423 | 3.49131 | 59.2409 | 0.361511 | 280.871 | 92.2249 | 0.699664 | 511.32 | 20.5507 | 0.912546 | 84.2759 | 169.237 | 180.294 | 67.71464 | 5566.325 |
| 14850 | 15.7504 | 0.913948 | 44.1777 | 2.69355 | 49.4896 | 0.462407 | 353.149 | 82.5685 | 0.408903 | 426.488 | 46.4165 | 0.774837 | 160.106 | 227.848 | 291.636 | 86.70542 | 7182.69 |
| 14453.8 | 21.425 | 0.916836 | 80.2924 | 0.510027 | 97.7575 | 0.528013 | 303.024 | 54.4848 | 0.749705 | 450.898 | 2.21777 | 0.752749 | 48.4174 | 157.317 | 121.578 | 48.17727 | 4410.258 |
| 13897.3 | 13.1048 | 0.920881 | 99.7915 | 0.453144 | 46.0674 | 0.337801 | 353.396 | 60.827 | 0.883768 | 122.748 | 4.43997 | 0.920662 | 39.4859 | 57.1237 | 70.3643 | 54.28439 | 4806.939 |
| 23120.2 | 21.5969 | 0.853753 | 75.2001 | 3.19955 | 31.7487 | 0.433755 | 406.72 | 25.3722 | 0.446656 | 377.735 | 18.5351 | 0.721628 | 119.18 | 233.152 | 234.51 | 96.43186 | 7141.105 |
| 11902.7 | 14.8306 | 0.935401 | 69.8203 | 1.43946 | 38.6415 | 0.316707 | 129.314 | 97.1449 | 0.845492 | 364.359 | 9.07495 | 0.923022 | 134.129 | 50.2955 | 206.049 | 50.1859 | 4462.473 |
| 16267.9 | 19.7064 | 0.903629 | 58.5274 | 3.20552 | 22.1634 | 0.396076 | 330.979 | 40.6088 | 0.843959 | 138.853 | 95.7904 | 0.5546 | 122.211 | 115.69 | 60.1748 | 71.33875 | 5388.159 |
| 22789 | 33.9098 | 0.856175 | 122.846 | 0.38382 | 35.7318 | 0.522867 | 369.416 | 20.7395 | 0.843205 | 452.255 | 28.3095 | 0.61573 | 34.2411 | 175.402 | 405.25 | 64.45699 | 4712.338 |
| 28813.3 | 31.6863 | 0.81232 | 91.6315 | 1.491 | 69.8613 | 0.456787 | 208.266 | 64.5382 | 0.656754 | 418.247 | 77.8049 | 0.852176 | 132.223 | 202.376 | 357.836 | 70.17441 | 5334.407 |
| 20351.9 | 13.5046 | 0.873898 | 154.033 | 2.22303 | 77.9078 | 0.653066 | 332.124 | 18.1752 | 0.889144 | 433.017 | 49.6334 | 0.75176 | 194.566 | 149.474 | 251.028 | 46.60491 | 3568.163 |
| 20722.7 | 16.9039 | 0.871201 | 164.823 | 1.11801 | 46.6365 | 0.654029 | 136.988 | 87.3118 | 0.803263 | 116.567 | 4.53849 | 0.68719 | 90.8728 | 105.343 | 90.8056 | 56.62411 | 4006.352 |
| 26447.6 | 27.8425 | 0.829537 | 113.019 | 1.44103 | 85.5534 | 0.421913 | 348.014 | 83.4321 | 0.564954 | 158.805 | 48.5411 | 0.83088 | 12.7887 | 184.584 | 128.857 | 93.61738 | 7635.99 |
| 15681.2 | 30.3189 | 0.90791 | 136.23 | 1.97295 | 7.64363 | 0.334307 | 142.415 | 86.6051 | 0.561606 | 294.942 | 30.1175 | 0.881062 | 156.587 | 92.8067 | 45.0707 | 82.83956 | 5983.626 |
| 17090.9 | 26.1751 | 0.897644 | 29.8164 | 3.20319 | 19.5693 | 0.356004 | 380.954 | 33.2488 | 0.965664 | 161.995 | 0.557078 | 0.478601 | 78.9999 | 241.145 | 134.078 | 75.91101 | 5838.656 |
| 14935.8 | 20.9937 | 0.913327 | 68.2747 | 1.70847 | 37.7621 | 0.348533 | 321.908 | 89.3119 | 0.863964 | 234.569 | 99.4663 | 0.708313 | 169.261 | 242.051 | 106.494 | 68.39698 | 5474.631 |
| 23603.4 | 21.1025 | 0.850235 | 140.013 | 1.75327 | 15.4562 | 0.40559 | 403.269 | 2.63497 | 0.668956 | 180.639 | 83.3376 | 0.743837 | 162.175 | 246.483 | 112.634 | 80.04574 | 5488.924 |
| 22329.5 | 26.1784 | 0.859512 | 30.9179 | 2.26453 | 35.0028 | 0.418053 | 362.126 | 14.731 | 0.979882 | 379.003 | 78.6305 | 0.350716 | 20.1394 | 43.3465 | 95.8222 | 99.55994 | 7438.73 |
| 13683 | 15.8794 | 0.922443 | 52.6731 | 1.92919 | 45.4332 | 0.322261 | 457.848 | 29.8699 | 0.955463 | 171.157 | 6.67114 | 0.709959 | 93.8872 | 326.353 | 106.831 | 53.66465 | 4981.282 |
| 10716 | 34.9387 | 0.94406 | 127.405 | 3.14503 | 56.1995 | 0.378834 | 415.869 | 76.953 | 0.558655 | 494.999 | 37.5251 | 0.945656 | 35.3597 | 110.727 | 81.1322 | 62.98247 | 5911.501 |
| 9425.37 | 24.6998 | 0.953441 | 110.657 | 0.365693 | 95.1584 | 0.567554 | 166.873 | 76.9307 | 0.412797 | 401.189 | 43.4218 | 0.813348 | 8.25074 | 82.2808 | 114.282 | 75.77554 | 7140.057 |
| 13724.1 | 31.4363 | 0.922158 | 161.651 | 3.57146 | 94.8268 | 0.523792 | 198.83 | 3.66462 | 0.565949 | 275.296 | 4.27868 | 0.853577 | 39.3679 | 88.7463 | 149.204 | 53.2376 | 5254.393 |
| 17584 | 20.143 | 0.89405 | 123.625 | 0.645455 | 50.1638 | 0.526573 | 290.269 | 80.0217 | 0.726086 | 219.013 | 87.8633 | 0.758897 | 18.6869 | 251.996 | 112.205 | 62.52598 | 4785.536 |
| 10800 | 19.9151 | 0.943431 | 137.072 | 3.72771 | 47.4596 | 0.487669 | 494.452 | 13.8376 | 0.64941 | 188.872 | 50.4144 | 0.962869 | 145.519 | 346.258 | 89.5444 | 37.21935 | 3420.632 |
| 28933.9 | 26.2837 | 0.811437 | 91.136 | 0.346884 | 0.389577 | 0.333323 | 357.543 | 94.2777 | 0.97449 | 285.917 | 63.99 | 0.930577 | 1.16169 | 218.873 | 193.568 | 78.33947 | 4739.368 |
| 21137.7 | 26.9831 | 0.868188 | 40.46 | 0.400392 | 52.7396 | 0.47275 | 261.495 | 34.1121 | 0.758719 | 146.714 | 18.744 | 0.723284 | 30.5224 | 98.6582 | 74.3946 | 52.61325 | 4275.696 |
| 29825.2 | 32.2708 | 0.804956 | 115.85 | 1.978 | 61.2186 | 0.529537 | 209.162 | 98.7308 | 0.666283 | 433.006 | 91.623 | 0.98437 | 163.862 | 70.7225 | 286.185 | 60.87299 | 4146.051 |
| 22013.1 | 18.2228 | 0.861809 | 30.1295 | 0.459831 | 94.033 | 0.440459 | 465.593 | 3.48705 | 0.716128 | 277.289 | 30.7716 | 0.875033 | 42.3911 | 291.659 | 168.157 | 51.58991 | 4853.483 |
| 30374.7 | 26.1952 | 0.80095 | 114.821 | 1.68633 | 97.3657 | 0.386498 | 249.876 | 99.3674 | 0.64262 | 338.323 | 67.5749 | 0.972807 | 82.0163 | 64.8679 | 283.48 | 85.46356 | 6952.203 |
| 22407.9 | 27.3318 | 0.858942 | 168.403 | 1.32179 | 78.4336 | 0.460684 | 481.387 | 19.8105 | 0.812431 | 336.284 | 40.0583 | 0.764336 | 40.2281 | 340.305 | 192.039 | 69.19623 | 5635.804 |
| 22201.7 | 30.8738 | 0.860447 | 51.6806 | 1.59437 | 35.7787 | 0.48909 | 246.274 | 13.9156 | 0.903406 | 402.043 | 39.6705 | 0.34579 | 44.9614 | 216.602 | 284.347 | 91.03578 | 6612.002 |
| 26119.1 | 17.6238 | 0.831921 | 71.1955 | 1.59192 | 92.3878 | 0.458782 | 98.4326 | 43.2897 | 0.855716 | 104.454 | 15.2757 | 0.787891 | 111.606 | 47.4298 | 45.3667 | 51.4757 | 4424.91 |
| 27737.7 | 19.3649 | 0.82014 | 112.911 | 1.1288 | 61.642 | 0.451957 | 472.218 | 14.6007 | 0.959213 | 413.965 | 48.4895 | 0.86867 | 12.4916 | 284.044 | 320.574 | 46.7151 | 3675.251 |
| 27246.8 | 17.4369 | 0.823713 | 44.8652 | 2.48729 | 50.0132 | 0.469268 | 186.603 | 12.0858 | 0.524548 | 439.868 | 38.994 | 0.722754 | 142.334 | 129.279 | 364.48 | 82.91987 | 6147.393 |
| 13331.9 | 18.3112 | 0.925 | 62.072 | 1.10999 | 72.36 | 0.463619 | 171.215 | 33.8015 | 0.751071 | 135.308 | 87.6468 | 0.675803 | 90.4718 | 167.272 | 100.333 | 56.39244 | 5092.869 |
| 27156.4 | 31.3512 | 0.824381 | 125.611 | 1.8476 | 28.3418 | 0.363851 | 266.825 | 88.6619 | 0.919847 | 243.984 | 62.5972 | 0.717575 | 108.939 | 46.0603 | 234.565 | 79.03941 | 5400.482 |
| 20477.2 | 17.6587 | 0.872989 | 172.944 | 1.02753 | 77.0385 | 0.480076 | 242.014 | 95.1788 | 0.781142 | 514.586 | 12.3823 | 0.608236 | 68.3745 | 161.11 | 57.4535 | 95.1133 | 7463.872 |
| 27055 | 17.909 | 0.825109 | 46.692 | 2.87105 | 14.976 | 0.329501 | 472.239 | 48.7966 | 0.710615 | 266.883 | 81.2561 | 0.785135 | 117.847 | 216.094 | 218.333 | 83.85745 | 5583.131 |
| 15230.4 | 20.1779 | 0.911182 | 59.812 | 0.404478 | 71.6547 | 0.360991 | 362.4 | 80.8788 | 0.827535 | 482.372 | 45.4837 | 0.768153 | 15.4973 | 188.322 | 459.824 | 63.6188 | 5857.821 |
| 25488.5 | 18.1146 | 0.836511 | 126.05 | 2.54135 | 15.5961 | 0.481506 | 241.675 | 9.79842 | 0.747058 | 192.73 | 86.552 | 0.821059 | 33.1312 | 163.522 | 132.161 | 52.83279 | 3598.183 |
| 10196.3 | 30.4735 | 0.947836 | 113.731 | 2.47588 | 90.7594 | 0.30526 | 69.3869 | 87.9677 | 0.958777 | 204.673 | 95.6564 | 0.970849 | 149.853 | 39.6577 | 41.9243 | 68.47756 | 6724.777 |
| 15706.1 | 30.0781 | 0.907729 | 75.4645 | 2.5385 | 30.8497 | 0.409726 | 499.411 | 23.034 | 0.495941 | 259.829 | 47.5044 | 0.63539 | 21.0017 | 243.286 | 148.353 | 92.65663 | 7488.826 |
| 12600.3 | 16.9831 | 0.930324 | 72.9401 | 2.65043 | 5.67855 | 0.43912 | 407.537 | 4.31469 | 0.86778 | 288.031 | 64.7084 | 0.792903 | 143.762 | 398.606 | 197.465 | 34.76056 | 2747.561 |
| 23357.3 | 26.748 | 0.852031 | 85.807 | 3.57665 | 47.7238 | 0.508619 | 271.224 | 25.0927 | 0.846049 | 388.913 | 16.8053 | 0.394045 | 189.748 | 159.132 | 377.412 | 97.47622 | 7091.557 |
| 27575.6 | 14.4401 | 0.821317 | 76.5598 | 1.35164 | 65.4208 | 0.351081 | 147.753 | 37.8306 | 0.776763 | 439.221 | 96.2469 | 0.70222 | 37.7619 | 105.696 | 120.692 | 89.39042 | 7119.693 |
| 19338.9 | 28.8585 | 0.881283 | 172.692 | 1.17202 | 92.1308 | 0.557358 | 291.746 | 41.8467 | 0.52153 | 262.331 | 8.56679 | 0.731272 | 74.5893 | 128.316 | 239.952 | 90.38183 | 7465.809 |
| 15116.6 | 33.2674 | 0.912024 | 115.147 | 2.1001 | 63.8213 | 0.381497 | 472.973 | 93.9472 | 0.784648 | 230.215 | 44.9266 | 0.922003 | 60.4614 | 86.8446 | 159.931 | 54.6673 | 4845.016 |
| 19789.5 | 22.4454 | 0.877997 | 54.7072 | 1.46673 | 21.1211 | 0.544669 | 401.53 | 51.7058 | 0.882807 | 490.145 | 61.461 | 0.577341 | 48.5845 | 389.422 | 365.915 | 68.58575 | 4743.659 |
| 11654.4 | 13.8369 | 0.937207 | 141.241 | 1.4408 | 27.9384 | 0.511305 | 168.663 | 83.3358 | 0.883942 | 251.357 | 72.7663 | 0.664881 | 46.7259 | 161.39 | 213.756 | 53.18192 | 4125.891 |
| 10055.3 | 18.5947 | 0.94885 | 143.553 | 2.30497 | 10.0515 | 0.579989 | 443.157 | 61.209 | 0.600194 | 171.234 | 79.6508 | 0.77023 | 76.2954 | 299.3 | 140.164 | 57.47021 | 4323.453 |
| 23069.5 | 15.052 | 0.854118 | 76.5628 | 1.17981 | 35.6736 | 0.396143 | 486.687 | 82.0586 | 0.414093 | 111.228 | 88.1721 | 0.971332 | 25.9146 | 252.228 | 47.6313 | 94.53341 | 6989.106 |
| 13340.5 | 19.3529 | 0.924938 | 146.045 | 2.18815 | 29.7815 | 0.347682 | 474.771 | 89.842 | 0.655788 | 455.008 | 4.14222 | 0.964969 | 136.951 | 376.379 | 357.842 | 62.63444 | 5187.242 |
| 20932.3 | 20.297 | 0.869677 | 166.39 | 1.40441 | 35.0305 | 0.434181 | 177.885 | 87.6315 | 0.719206 | 177.769 | 25.7381 | 0.647416 | 60.5601 | 159.221 | 120.317 | 95.75866 | 6931.977 |
| 25919.5 | 33.7082 | 0.833387 | 118.872 | 2.80947 | 66.6417 | 0.354642 | 209.815 | 53.9572 | 0.755756 | 137.769 | 27.9855 | 0.704613 | 47.7076 | 127.468 | 125.18 | 88.43159 | 7216.244 |
| 20857.5 | 24.1846 | 0.870225 | 83.794 | 0.391163 | 90.522 | 0.341299 | 129.798 | 8.69845 | 0.905761 | 309.38 | 94.9498 | 0.903708 | 6.29042 | 81.8092 | 194.439 | 66.6258 | 6074.598 |
| 20441.1 | 30.8682 | 0.873263 | 153.947 | 3.31317 | 42.8576 | 0.323672 | 305.401 | 59.6911 | 0.562088 | 137.875 | 86.4837 | 0.91201 | 154.815 | 105.83 | 60.5384 | 99.9899 | 7775.17 |
| 11885.9 | 20.6257 | 0.935527 | 129.239 | 0.409355 | 51.416 | 0.365509 | 216.554 | 57.005 | 0.985943 | 404.021 | 16.566 | 0.735889 | 34.6157 | 196.923 | 47.4893 | 58.27141 | 5186.935 |
| 24096.2 | 16.9677 | 0.846645 | 33.3012 | 0.25806 | 16.0176 | 0.479386 | 441.522 | 42.1362 | 0.76069 | 182.737 | 21.4408 | 0.859692 | 11.5751 | 143.666 | 46.9144 | 43.48515 | 3057.394 |
| 23846.4 | 18.3082 | 0.848465 | 154.884 | 3.41415 | 46.7041 | 0.574349 | 333.4 | 63.365 | 0.952075 | 243.278 | 54.6015 | 0.970703 | 136.646 | 177.129 | 108.777 | 40.68257 | 2887.077 |
| 28664.8 | 26.7423 | 0.813397 | 143.733 | 1.50769 | 92.431 | 0.463613 | 180.625 | 82.6195 | 0.949513 | 81.0844 | 65.2722 | 0.933846 | 5.49379 | 173.763 | 59.2558 | 62.12791 | 4792.769 |
| 21121.1 | 34.4695 | 0.868317 | 131.086 | 2.12543 | 46.3722 | 0.516206 | 93.7323 | 58.438 | 0.994302 | 444.04 | 15.0242 | 0.524762 | 136.409 | 89.0762 | 155.971 | 61.41775 | 4612.101 |
| 10959 | 17.2312 | 0.942271 | 160.433 | 0.21375 | 30.5571 | 0.526221 | 349.978 | 30.2916 | 0.859387 | 59.3567 | 46.5363 | 0.455916 | 9.20501 | 263.956 | 48.744 | 83.27415 | 6675.822 |
| 23325.3 | 22.2124 | 0.85226 | 34.9966 | 1.37999 | 64.118 | 0.382161 | 292.945 | 94.1448 | 0.825315 | 188.458 | 50.2045 | 0.659022 | 45.1194 | 262.833 | 129.987 | 80.81052 | 6508.215 |
| 29113.1 | 15.6458 | 0.810126 | 26.9993 | 1.3544 | 65.906 | 0.424023 | 314.214 | 94.0294 | 0.862221 | 296.423 | 59.3051 | 0.821223 | 18.0476 | 304.26 | 51.9285 | 62.1247 | 4730.904 |
| 14584.7 | 16.7315 | 0.91588 | 67.7606 | 2.19294 | 11.958 | 0.579534 | 367.523 | 6.80869 | 0.978194 | 282.434 | 69.4174 | 0.924043 | 184.458 | 252.39 | 220.448 | 30.15817 | 2300.857 |
| 22409.3 | 25.86 | 0.858931 | 108.617 | 1.50874 | 83.6965 | 0.423115 | 213.205 | 26.4066 | 0.489113 | 255.177 | 17.4674 | 0.820042 | 86.7049 | 156.86 | 162.206 | 91.10407 | 7998.581 |
| 15446.8 | 26.6324 | 0.909612 | 123.952 | 1.51437 | 2.60496 | 0.424246 | 367.259 | 46.1687 | 0.68016 | 115.931 | 82.9856 | 0.99205 | 94.0404 | 326.179 | 90.6317 | 49.25943 | 3524.94 |
| 20061.6 | 27.2488 | 0.876021 | 126.532 | 0.940494 | 52.9649 | 0.37251 | 461.166 | 11.0343 | 0.989801 | 261.505 | 3.11658 | 0.643681 | 4.13162 | 78.0482 | 202.436 | 66.32211 | 5577.996 |
| 15106.8 | 29.0051 | 0.91209 | 68.2627 | 0.219415 | 93.4904 | 0.44033 | 478.603 | 63.2167 | 0.68113 | 272.932 | 69.1063 | 0.824364 | 12.3066 | 372.925 | 57.8533 | 64.26458 | 5993.184 |
| 26232.6 | 17.3259 | 0.831094 | 170.531 | 0.54401 | 76.5981 | 0.649196 | 182.538 | 27.7607 | 0.91149 | 212.421 | 20.0746 | 0.645473 | 25.4667 | 60.5379 | 186.05 | 59.43813 | 4328.203 |
| 12667.1 | 19.9097 | 0.92984 | 107.667 | 1.80639 | 35.3001 | 0.4872 | 288.512 | 58.8487 | 0.914783 | 337.768 | 47.037 | 0.513885 | 149.255 | 53.9632 | 323.479 | 57.52142 | 4600.568 |
| 25461.2 | 29.8301 | 0.836719 | 123.947 | 2.52049 | 1.3696 | 0.375995 | 487.92 | 78.5344 | 0.620465 | 246.945 | 94.2228 | 0.886646 | 91.4186 | 461.72 | 70.4676 | 79.11806 | 4966.587 |
| 29745.6 | 30.6783 | 0.805533 | 149.678 | 1.03352 | 54.8212 | 0.429959 | 351.628 | 20.3487 | 0.876411 | 335.512 | 10.4594 | 0.588024 | 58.3299 | 166.399 | 85.6704 | 93.35751 | 6741.89 |
| 27211.2 | 22.1503 | 0.823975 | 133.276 | 2.01706 | 94.751 | 0.646129 | 444.259 | 39.2139 | 0.755001 | 419.603 | 9.42684 | 0.707827 | 199.097 | 336.768 | 383.942 | 72.80968 | 5284.989 |
| 30404.2 | 21.6995 | 0.800732 | 114.149 | 3.03655 | 68.4597 | 0.5257 | 281.109 | 49.6919 | 0.545832 | 466.428 | 46.6465 | 0.86351 | 81.1129 | 192.595 | 215.515 | 81.87695 | 5809.93 |
| 15905.2 | 28.8726 | 0.906278 | 83.7348 | 0.311501 | 37.0444 | 0.324522 | 413.379 | 48.134 | 0.64307 | 216.503 | 54.5096 | 0.998775 | 12.3979 | 72.0324 | 182.445 | 70.3396 | 5800.748 |
| 15103.5 | 16.3153 | 0.912103 | 127.864 | 1.77561 | 18.1854 | 0.466571 | 218.905 | 70.1732 | 0.97389 | 444.752 | 42.4557 | 0.490114 | 19.6877 | 116.652 | 407.87 | 66.94718 | 4929.238 |
| 21559.5 | 16.9948 | 0.86511 | 26.4153 | 3.36053 | 79.21 | 0.428467 | 361.439 | 55.0299 | 0.816162 | 134.741 | 71.5693 | 0.909263 | 26.9909 | 201.856 | 121.328 | 50.9485 | 4395.839 |
| 24118.8 | 32.0085 | 0.846493 | 55.9411 | 1.88015 | 14.0206 | 0.394969 | 306.69 | 17.5871 | 0.493692 | 265.274 | 77.1556 | 0.810299 | 56.8953 | 282.951 | 166.977 | 88.94289 | 6064.074 |
| 25629.2 | 31.2021 | 0.835498 | 61.565 | 0.736866 | 34.3714 | 0.506083 | 458.296 | 19.2386 | 0.806277 | 406.062 | 69.3637 | 0.817477 | 48.034 | 218.95 | 183.142 | 48.29933 | 3424.206 |
| 20277.1 | 15.3225 | 0.874444 | 86.0945 | 0.300678 | 16.1633 | 0.482807 | 474.498 | 83.1238 | 0.34621 | 380.188 | 55.0783 | 0.917105 | 27.6502 | 312.345 | 156.848 | 99.06587 | 6893.008 |
| 20751.8 | 26.1057 | 0.870996 | 166.639 | 1.3086 | 65.7586 | 0.424964 | 174.239 | 29.8871 | 0.747807 | 265.696 | 86.2627 | 0.949323 | 64.7478 | 63.5471 | 119.242 | 66.58129 | 5315.121 |
| 24309.5 | 21.0148 | 0.845095 | 172.824 | 3.15019 | 57.4263 | 0.359235 | 337.27 | 55.7244 | 0.998999 | 176.084 | 24.9729 | 0.558231 | 107.339 | 214.673 | 135.493 | 97.90721 | 7519.735 |
| 10662.8 | 25.7758 | 0.944435 | 156.615 | 3.26724 | 55.8227 | 0.567381 | 487.746 | 8.07124 | 0.592806 | 460.16 | 18.7257 | 0.660664 | 164.9 | 158.209 | 134.176 | 56.46041 | 4979.864 |
| 13547.6 | 23.4204 | 0.923434 | 138.014 | 2.60909 | 3.16011 | 0.558173 | 357.851 | 75.18 | 0.671599 | 332.264 | 17.6926 | 0.894732 | 239.694 | 188.264 | 179.662 | 42.38079 | 3129.924 |
| 17427.7 | 33.4368 | 0.895201 | 151.427 | 1.02344 | 3.93489 | 0.470924 | 467.79 | 65.1247 | 0.584227 | 225.676 | 82.985 | 0.670316 | 96.7369 | 223.815 | 46.9319 | 92.04295 | 6277.066 |
| 9148.89 | 33.4552 | 0.955465 | 81.6604 | 1.56194 | 71.6051 | 0.435471 | 321.051 | 46.9859 | 0.867693 | 277.293 | 54.3013 | 0.683882 | 155.764 | 305.19 | 47.1051 | 47.35834 | 4651.073 |
| 13783.8 | 25.1285 | 0.921716 | 32.5229 | 1.97727 | 84.3153 | 0.444761 | 218.291 | 62.2341 | 0.819079 | 270.334 | 32.5896 | 0.747095 | 147.008 | 87.3084 | 146.019 | 50.07627 | 4757.362 |
| 23576.7 | 32.3999 | 0.85044 | 76.4185 | 2.95466 | 79.9655 | 0.4104 | 289.039 | 62.5149 | 0.59379 | 220.104 | 81.9818 | 0.77999 | 79.203 | 188.915 | 192.691 | 87.52161 | 7337.554 |
| 19639.6 | 20.6527 | 0.879087 | 123.157 | 2.17372 | 29.3125 | 0.483784 | 239.894 | 56.7038 | 0.976598 | 312.403 | 17.3514 | 0.757228 | 111.635 | 191.083 | 197.586 | 40.89497 | 3120.365 |
| 21997.9 | 20.539 | 0.861921 | 167.672 | 0.932384 | 27.5188 | 0.607906 | 264.178 | 93.0666 | 0.876673 | 205.742 | 50.426 | 0.560576 | 59.5046 | 65.0941 | 53.6782 | 75.27942 | 5064.976 |
| 15013.1 | 24.935 | 0.912767 | 166.386 | 0.790195 | 33.0176 | 0.405733 | 334.219 | 76.2878 | 0.745166 | 369.436 | 5.87164 | 0.947374 | 4.26513 | 277.375 | 318.86 | 61.05502 | 4867.205 |
| 24438.5 | 19.808 | 0.844155 | 166.235 | 1.15544 | 19.8596 | 0.588417 | 210.811 | 12.3661 | 0.719606 | 518.528 | 88.5283 | 0.661416 | 23.9238 | 63.4651 | 223.474 | 70.93034 | 4754.035 |
| 17585.8 | 25.7234 | 0.894042 | 127.783 | 1.33984 | 51.6434 | 0.357046 | 304.649 | 78.0217 | 0.868585 | 387.217 | 58.3634 | 0.970574 | 129.323 | 209.147 | 342.765 | 60.8197 | 4991.828 |
| 24066.9 | 27.2903 | 0.846866 | 52.3423 | 0.86159 | 97.0312 | 0.457859 | 103.745 | 67.8217 | 0.965884 | 449.757 | 9.98417 | 0.560056 | 64.6772 | 43.7427 | 223.396 | 69.09041 | 5901.974 |
| 28347.4 | 33.0108 | 0.815714 | 137.316 | 0.484015 | 92.6278 | 0.42893 | 302.069 | 30.5733 | 0.875893 | 364.801 | 41.7905 | 0.715594 | 43.4142 | 264.632 | 264.312 | 82.67031 | 6552.973 |
| 17006.2 | 34.275 | 0.898271 | 165.883 | 3.09762 | 72.5422 | 0.571377 | 327.858 | 35.884 | 0.884928 | 101.297 | 19.8888 | 0.518454 | 170.014 | 130.387 | 99.1072 | 60.91689 | 4998.984 |
| 17082.9 | 15.8634 | 0.897695 | 102.778 | 1.54764 | 90.0763 | 0.399948 | 463.438 | 9.13921 | 0.950034 | 357.115 | 54.5542 | 0.510813 | 96.4107 | 103.936 | 216.731 | 73.45207 | 7068.132 |
| 29023.2 | 32.1232 | 0.810793 | 55.3798 | 2.07703 | 94.6648 | 0.552143 | 217.116 | 41.8533 | 0.92565 | 299.448 | 57.6241 | 0.777292 | 196.083 | 205.84 | 263.826 | 53.69949 | 3997.427 |
| 19470.1 | 13.0194 | 0.880317 | 113.599 | 0.280566 | 80.2437 | 0.606909 | 389.807 | 38.2021 | 0.976851 | 117.118 | 50.993 | 0.934961 | 16.0041 | 137.372 | 103.507 | 35.50528 | 2827.835 |
| 19064.4 | 19.5398 | 0.883273 | 83.2667 | 0.254499 | 46.1643 | 0.516717 | 452.6 | 69.3729 | 0.769956 | 401.928 | 89.4199 | 0.903891 | 14.1258 | 350.506 | 125.866 | 48.86251 | 3723.671 |
| 29830.1 | 25.3913 | 0.804914 | 171.797 | 1.75446 | 22.697 | 0.426268 | 235.91 | 84.1974 | 0.927275 | 472.124 | 8.47149 | 0.654318 | 1.43874 | 75.1579 | 383.882 | 88.23925 | 5698.778 |
| 15549.3 | 32.0844 | 0.908873 | 121.311 | 2.31451 | 95.199 | 0.428687 | 361.757 | 14.6804 | 0.788913 | 513.632 | 10.4725 | 0.786401 | 167.617 | 242.465 | 202.045 | 50.38077 | 5110.986 |
| 22532.2 | 18.6583 | 0.858031 | 123.882 | 2.39191 | 14.9156 | 0.330578 | 141.571 | 92.8404 | 0.923831 | 61.4036 | 58.9007 | 0.933924 | 98.5674 | 39.9391 | 45.5676 | 64.87528 | 4445.339 |
| 29471 | 26.3172 | 0.807528 | 113.045 | 2.77443 | 74.9382 | 0.354165 | 368.186 | 84.3375 | 0.993339 | 254.467 | 23.9811 | 0.863713 | 120.043 | 56.9872 | 109.082 | 65.99757 | 5295.958 |
| 24336.6 | 33.1597 | 0.844909 | 81.5791 | 1.78351 | 39.7695 | 0.459784 | 255.25 | 95.7105 | 0.578715 | 371.52 | 48.0341 | 0.62238 | 104.202 | 99.0552 | 297.753 | 96.8816 | 6947.946 |
| 23262.5 | 22.6121 | 0.852717 | 150.387 | 0.501667 | 26.9398 | 0.432409 | 450.344 | 62.0995 | 0.908853 | 394.755 | 25.0981 | 0.794326 | 15.102 | 225.168 | 287.63 | 64.79934 | 4570.71 |
| 21774.4 | 32.0324 | 0.863558 | 81.4853 | 1.48901 | 11.9595 | 0.499864 | 168.165 | 48.9047 | 0.639809 | 416.48 | 96.3294 | 0.968981 | 73.7703 | 75.3247 | 187.869 | 51.04873 | 3458.727 |
| 25522.1 | 17.7161 | 0.836266 | 150.963 | 0.876367 | 46.8499 | 0.40796 | 288.166 | 35.6869 | 0.948698 | 305.451 | 56.5692 | 0.98815 | 5.01943 | 69.9612 | 103.427 | 66.87323 | 4888.246 |
| 25720.6 | 26.0021 | 0.834827 | 153.535 | 0.637304 | 65.4636 | 0.556758 | 331.605 | 5.23121 | 0.990437 | 175.335 | 15.8458 | 0.685751 | 56.6451 | 282.638 | 136.68 | 51.4187 | 3938.848 |
| 24792 | 29.2479 | 0.84159 | 35.7354 | 2.93026 | 34.8962 | 0.352193 | 350.276 | 77.7278 | 0.566715 | 438.609 | 35.3326 | 0.939565 | 146.309 | 74.8829 | 217.729 | 81.13561 | 6010.772 |
| 23729.9 | 29.1962 | 0.849321 | 33.1157 | 3.01089 | 76.1913 | 0.452401 | 253.875 | 19.2272 | 0.416386 | 337.41 | 10.6069 | 0.910818 | 119.365 | 167.188 | 183.515 | 84.19653 | 7144.474 |
| 30291.5 | 23.5136 | 0.801553 | 169.473 | 3.0837 | 4.48507 | 0.486181 | 375.868 | 84.9528 | 0.651309 | 455.238 | 3.48795 | 0.933869 | 118.419 | 300.956 | 399.113 | 66.24207 | 4113.416 |
| 10921.6 | 21.717 | 0.942547 | 84.0723 | 0.608802 | 22.7216 | 0.35153 | 347.757 | 24.6455 | 0.9823 | 94.7864 | 43.6887 | 0.381349 | 20.6445 | 207 | 79.1476 | 87.92068 | 7310.339 |
| 25146.2 | 23.6207 | 0.839006 | 33.2039 | 0.659821 | 66.3005 | 0.482588 | 187.418 | 14.0013 | 0.765233 | 446.746 | 18.4772 | 0.510657 | 26.3929 | 148.177 | 384.834 | 76.44973 | 5994.07 |
| 14879.8 | 31.8875 | 0.913746 | 116.762 | 1.9452 | 89.3537 | 0.473569 | 236.189 | 37.8484 | 0.969782 | 112.149 | 14.7298 | 0.95138 | 131.022 | 197.997 | 64.7444 | 34.25355 | 3365.315 |
| 23133.1 | 16.9077 | 0.853656 | 110.226 | 1.75128 | 54.551 | 0.374326 | 174.296 | 43.7095 | 0.909368 | 518.33 | 89.1886 | 0.558942 | 68.2411 | 154.949 | 335.749 | 87.24874 | 6856.858 |
| 18394.9 | 21.0159 | 0.888148 | 27.9411 | 1.3867 | 58.4725 | 0.500455 | 436.916 | 22.5073 | 0.93491 | 219.017 | 89.9546 | 0.812075 | 92.7462 | 108.377 | 138.469 | 40.58063 | 3236.412 |
| 28654.3 | 17.4939 | 0.813467 | 90.4957 | 1.2765 | 44.3699 | 0.401149 | 317.244 | 36.3216 | 0.933932 | 81.4795 | 16.1338 | 0.601659 | 120.258 | 104.367 | 45.6228 | 70.9995 | 5258.739 |
| 19044.9 | 20.0002 | 0.883416 | 147.489 | 1.5747 | 9.6536 | 0.505046 | 191.825 | 34.3485 | 0.938633 | 474.357 | 23.9947 | 0.796898 | 54.0359 | 59.6634 | 348.331 | 40.22296 | 2928.18 |
| 27725.3 | 33.8707 | 0.820243 | 152.362 | 1.39157 | 68.8972 | 0.489292 | 496.98 | 22.3174 | 0.989966 | 248.891 | 90.8285 | 0.508856 | 45.644 | 72.5301 | 216.494 | 86.76254 | 6383.939 |
| 23230.6 | 20.1305 | 0.852948 | 129.526 | 0.50188 | 46.9205 | 0.328376 | 248.575 | 21.0722 | 0.758647 | 173.761 | 49.1201 | 0.971366 | 9.48777 | 122.004 | 138.268 | 78.06272 | 6046.956 |
| 27536.2 | 20.4423 | 0.821607 | 153.01 | 1.29749 | 1.06043 | 0.602337 | 95.5783 | 4.02404 | 0.980105 | 381.895 | 74.1652 | 0.630061 | 77.8657 | 79.6769 | 357.971 | 50.50362 | 3227.556 |
| 11770.1 | 16.9758 | 0.936368 | 133.777 | 3.12599 | 32.0479 | 0.451178 | 384.29 | 33.6749 | 0.973541 | 184.687 | 91.4149 | 0.358696 | 158.375 | 177.259 | 101.073 | 82.4747 | 6672.795 |
| 27451.6 | 14.5636 | 0.82222 | 49.6637 | 1.26457 | 46.0612 | 0.435112 | 90.1257 | 54.4752 | 0.996784 | 264.978 | 91.5437 | 0.792037 | 7.68892 | 62.212 | 54.0097 | 52.27324 | 3817.649 |
| 25115.7 | 34.991 | 0.83924 | 89.9556 | 1.08216 | 18.9773 | 0.355996 | 479.474 | 96.9641 | 0.688664 | 224.907 | 23.5163 | 0.941807 | 21.196 | 193.269 | 194.398 | 68.33048 | 4728.656 |
| 27212 | 14.3019 | 0.823964 | 143.877 | 3.3048 | 86.9762 | 0.39436 | 114.376 | 5.87719 | 0.78502 | 517.592 | 63.3248 | 0.690501 | 147.122 | 110.319 | 356.046 | 83.09679 | 6976.837 |
| 14332 | 19.1334 | 0.917721 | 69.1101 | 1.32955 | 92.409 | 0.300972 | 449.332 | 38.2833 | 0.796145 | 438.618 | 48.6742 | 0.782528 | 8.71222 | 200.293 | 191.694 | 74.45302 | 7744.893 |
| 13002.9 | 24.617 | 0.9274 | 74.8461 | 2.4057 | 44.764 | 0.384375 | 129.05 | 73.7317 | 0.757189 | 249.887 | 91.9132 | 0.959198 | 149.868 | 110.731 | 205.972 | 49.63528 | 4222.87 |
| 21681.2 | 28.5285 | 0.864233 | 74.8816 | 0.559819 | 49.4717 | 0.424667 | 403.555 | 79.8061 | 0.83353 | 284.919 | 24.4666 | 0.861165 | 13.3109 | 214.617 | 175.426 | 51.70661 | 4116.674 |
| 23635.9 | 32.1164 | 0.850009 | 167.805 | 2.12567 | 95.1449 | 0.663304 | 264.971 | 1.37541 | 0.786246 | 178.517 | 71.4827 | 0.686225 | 29.9765 | 236.367 | 169.362 | 60.88431 | 4552.084 |
| 26506.5 | 25.4948 | 0.829106 | 55.7609 | 2.94671 | 19.0058 | 0.385117 | 298.072 | 95.3197 | 0.591568 | 285.951 | 97.5788 | 0.729798 | 66.0968 | 116.859 | 47.2937 | 98.99742 | 6559.981 |
| 19642.7 | 26.2192 | 0.87907 | 45.0209 | 1.49695 | 29.7028 | 0.351687 | 346.397 | 9.80584 | 0.895725 | 166.967 | 51.9478 | 0.90204 | 98.2187 | 172.26 | 156.865 | 46.03624 | 3690.461 |
| 11332.9 | 23.9282 | 0.939555 | 59.3571 | 0.862359 | 4.19933 | 0.36305 | 254.452 | 28.8597 | 0.94654 | 502.982 | 42.7168 | 0.555153 | 64.6589 | 85.496 | 215.426 | 55.15091 | 4251.209 |
| 14057.7 | 33.18 | 0.919732 | 134.404 | 0.415137 | 91.9919 | 0.701135 | 479.385 | 70.0956 | 0.759504 | 500.979 | 32.563 | 0.65785 | 19.605 | 258.296 | 198.421 | 63.45813 | 4993.334 |
| 12368.8 | 33.585 | 0.932026 | 171.714 | 0.626684 | 52.3168 | 0.654487 | 254.653 | 79.02 | 0.60259 | 339.295 | 0.585528 | 0.887748 | 18.1085 | 154.011 | 281.481 | 50.06073 | 4105.082 |
| 19276.8 | 32.8698 | 0.88174 | 143.715 | 0.543228 | 22.7636 | 0.436699 | 416.713 | 32.6217 | 0.678946 | 460.515 | 23.6019 | 0.970957 | 52.8688 | 124.403 | 300.228 | 58.59043 | 4360.599 |
| 28980.5 | 15.957 | 0.811092 | 145.91 | 1.00634 | 8.45858 | 0.511025 | 81.6574 | 59.7494 | 0.931352 | 75.8084 | 42.2384 | 0.939571 | 36.9206 | 59.0615 | 45.2813 | 49.34818 | 3158.881 |
| 17236.4 | 20.2191 | 0.89658 | 113.797 | 1.43385 | 47.5179 | 0.428173 | 112.293 | 35.2104 | 0.946358 | 139.442 | 9.07834 | 0.373392 | 129.208 | 82.018 | 49.622 | 94.02168 | 7691.188 |
| 29730.4 | 16.5874 | 0.805634 | 113.799 | 1.87066 | 26.2903 | 0.487847 | 318.893 | 80.828 | 0.466276 | 288.916 | 92.3024 | 0.937205 | 148.804 | 232.289 | 250.114 | 83.62686 | 5461.075 |
| 27138.9 | 22.6688 | 0.824501 | 107.58 | 0.606614 | 43.2354 | 0.357805 | 77.8386 | 60.6492 | 0.87183 | 432.502 | 90.3395 | 0.672654 | 56.9736 | 55.1079 | 320.127 | 92.78111 | 6656.045 |
| 21584.9 | 20.6167 | 0.864927 | 171.37 | 2.07223 | 42.9642 | 0.653987 | 222.99 | 97.1553 | 0.823033 | 254.983 | 72.9082 | 0.890233 | 156.878 | 206.238 | 164.32 | 49.70327 | 3399.182 |
| 27897.6 | 24.0892 | 0.818979 | 55.1574 | 2.56727 | 41.7398 | 0.421325 | 351.868 | 71.0742 | 0.519668 | 221.338 | 25.7681 | 0.881896 | 118.421 | 328.402 | 171.509 | 81.8817 | 5957.494 |
| 11733.8 | 25.3436 | 0.936638 | 139.893 | 1.24787 | 91.7761 | 0.638896 | 428.419 | 96.0946 | 0.936994 | 327.736 | 12.8802 | 0.741841 | 14.684 | 266.809 | 215.403 | 44.3436 | 3691.797 |
| 10370.6 | 30.815 | 0.946567 | 56.0376 | 2.27269 | 14.3371 | 0.487939 | 186.442 | 74.4739 | 0.605976 | 331.788 | 89.0844 | 0.800201 | 56.9166 | 136.364 | 110.863 | 53.77536 | 4096.211 |
| 16031.7 | 19.931 | 0.905349 | 157.473 | 0.82862 | 14.9046 | 0.500054 | 274.824 | 58.4177 | 0.969088 | 323.832 | 6.85733 | 0.666804 | 13.3821 | 40.7827 | 127.067 | 52.83278 | 3908.099 |
| 21284.6 | 15.9208 | 0.867111 | 102.859 | 0.135607 | 10.8234 | 0.484159 | 282.041 | 29.3815 | 0.979539 | 160.139 | 2.32499 | 0.456483 | 1.95103 | 133.478 | 157.836 | 78.80646 | 5411.744 |
| 24542.4 | 27.0524 | 0.843404 | 133.687 | 2.18779 | 4.42421 | 0.503144 | 478.662 | 38.1067 | 0.946414 | 490.639 | 47.8715 | 0.81604 | 149.783 | 154.016 | 440.278 | 41.51355 | 2781.769 |
| 27825.8 | 21.6671 | 0.8195 | 129.01 | 2.44981 | 70.1996 | 0.53643 | 441.219 | 47.8067 | 0.614717 | 517.498 | 5.08487 | 0.756519 | 175.245 | 123.618 | 445.291 | 70.96617 | 5173.365 |
| 17718.6 | 19.7166 | 0.893069 | 67.2582 | 0.590939 | 82.0433 | 0.492167 | 449.605 | 10.0268 | 0.752771 | 371.297 | 69.2901 | 0.539851 | 33.0797 | 205.761 | 85.5 | 70.25655 | 6037.797 |
| 11515.7 | 31.1217 | 0.938233 | 89.662 | 1.24714 | 44.3072 | 0.458168 | 392.627 | 17.9533 | 0.811117 | 502.375 | 24.7599 | 0.781594 | 62.4674 | 340.655 | 113.834 | 37.16703 | 3472.441 |
| 17145.5 | 18.3906 | 0.89724 | 67.1375 | 3.12144 | 48.9915 | 0.466834 | 461.247 | 81.9563 | 0.547777 | 250.728 | 13.371 | 0.58439 | 12.0242 | 233.58 | 125 | 89.89277 | 7275.658 |
| 13541.5 | 24.7321 | 0.92348 | 150.151 | 2.89899 | 10.7568 | 0.482504 | 103.379 | 46.5112 | 0.637355 | 99.5817 | 54.2581 | 0.700621 | 87.2672 | 90.9989 | 59.5317 | 61.82183 | 4637.539 |
| 13569.4 | 29.026 | 0.92328 | 159.292 | 1.82818 | 55.4673 | 0.471363 | 430.928 | 79.4722 | 0.536289 | 55.9597 | 76.5046 | 0.75872 | 118.339 | 220.294 | 46.0762 | 85.71359 | 7089.807 |
| 22494.7 | 15.0833 | 0.858301 | 138.213 | 0.875002 | 73.6155 | 0.522113 | 161.712 | 71.794 | 0.990905 | 201.617 | 37.2275 | 0.399873 | 34.2301 | 99.5069 | 72.3808 | 98.67115 | 7476.526 |
| 25742.2 | 27.4279 | 0.834672 | 154.323 | 0.899227 | 41.229 | 0.555407 | 270.328 | 79.2349 | 0.829809 | 326.902 | 3.78813 | 0.932866 | 28.111 | 84.8544 | 148.377 | 48.23325 | 3441.832 |
| 19667.8 | 15.3858 | 0.878879 | 119.529 | 0.691524 | 54.7342 | 0.333394 | 379.586 | 37.4209 | 0.625386 | 493.348 | 87.2209 | 0.89955 | 38.5753 | 141.671 | 356.907 | 90.05256 | 7370.577 |
| 18966.2 | 16.0826 | 0.883986 | 67.2037 | 0.910221 | 45.8397 | 0.409447 | 483.083 | 8.586 | 0.998591 | 426.604 | 9.79732 | 0.583547 | 9.61445 | 332.922 | 97.4526 | 51.90729 | 4474.747 |
| 18811.6 | 14.4578 | 0.885111 | 132.93 | 3.19143 | 15.2131 | 0.555613 | 217.602 | 22.8006 | 0.87296 | 349.065 | 92.6406 | 0.719467 | 118.792 | 198.968 | 271.389 | 49.23478 | 3453.766 |
| 12396.3 | 22.5963 | 0.931813 | 104.529 | 0.690183 | 20.2682 | 0.418322 | 205.678 | 17.4226 | 0.880306 | 153.505 | 30.1171 | 0.659344 | 61.9439 | 73.5205 | 116.309 | 49.43455 | 4087.92 |
| 16685.4 | 23.9313 | 0.900594 | 120.429 | 3.02734 | 42.7588 | 0.485445 | 143.428 | 14.8838 | 0.915825 | 470.208 | 1.69144 | 0.683216 | 21.2668 | 99.94 | 359.536 | 38.87032 | 3350.058 |
| 13257.3 | 19.6969 | 0.925544 | 156.437 | 3.28938 | 28.5001 | 0.448698 | 479.955 | 50.819 | 0.65791 | 117.866 | 94.0409 | 0.655593 | 149.939 | 297.002 | 58.8622 | 74.46058 | 5841.356 |
| 20698.1 | 20.6727 | 0.871382 | 71.7682 | 3.76115 | 60.7914 | 0.338335 | 327.304 | 66.5309 | 0.769283 | 448.247 | 0.155041 | 0.846502 | 137.006 | 131.485 | 226.46 | 66.48704 | 5786.511 |
| 24259.6 | 17.426 | 0.845456 | 98.6087 | 3.56513 | 32.6369 | 0.396788 | 123.704 | 90.6874 | 0.655848 | 362.159 | 38.5477 | 0.959418 | 54.8021 | 72.4984 | 103.998 | 61.78003 | 4531.822 |
| 20135.1 | 14.0527 | 0.875477 | 107.858 | 0.162912 | 18.0817 | 0.309654 | 209.083 | 37.0264 | 0.924787 | 83.0824 | 4.93763 | 0.908593 | 5.62237 | 144.126 | 62.2982 | 75.65184 | 5513.231 |
| 10789.4 | 16.4841 | 0.943506 | 77.8042 | 2.70494 | 37.3448 | 0.366903 | 122.24 | 22.0848 | 0.848225 | 365.073 | 35.4041 | 0.836009 | 152.315 | 70.132 | 249.803 | 41.30528 | 3848.466 |
| 11756.8 | 34.6099 | 0.936483 | 133.792 | 0.627993 | 29.5044 | 0.438519 | 89.521 | 90.869 | 0.743126 | 161.653 | 97.8757 | 0.572007 | 10.7944 | 76.4097 | 156.849 | 88.53314 | 6866.48 |
| 11805.5 | 26.2734 | 0.936117 | 147.765 | 2.10609 | 93.0032 | 0.484261 | 323.972 | 4.81777 | 0.976074 | 400.8 | 93.4767 | 0.471338 | 125.752 | 194.731 | 152.55 | 66.29748 | 6367.166 |
| 13773.6 | 20.0368 | 0.921786 | 120.009 | 1.58396 | 20.6622 | 0.32501 | 381.58 | 66.396 | 0.508928 | 420.826 | 32.2622 | 0.989516 | 98.2764 | 164.704 | 218.417 | 77.66136 | 6187.69 |
| 16340.6 | 14.9367 | 0.903097 | 123.379 | 0.192791 | 16.8322 | 0.453959 | 307.362 | 1.17063 | 0.62836 | 392.952 | 41.4576 | 0.974202 | 17.4757 | 180.232 | 354.442 | 55.39856 | 4225.831 |
| 14704.1 | 21.8495 | 0.915014 | 152.371 | 2.44823 | 37.3706 | 0.46333 | 289.528 | 59.8426 | 0.930247 | 208.06 | 55.864 | 0.382087 | 82.6034 | 268.201 | 117.94 | 95.50243 | 7427.279 |
| 20617.2 | 18.4045 | 0.87197 | 75.9777 | 1.76944 | 9.91219 | 0.457239 | 223.475 | 16.2117 | 0.878339 | 130.961 | 32.2271 | 0.350042 | 172.222 | 203.642 | 123.226 | 89.72266 | 6199.907 |
| 23852.1 | 25.9483 | 0.848428 | 107.409 | 0.910328 | 59.3332 | 0.49512 | 267.938 | 28.9099 | 0.908453 | 395.493 | 98.5936 | 0.483401 | 9.28196 | 84.6229 | 219.221 | 81.25614 | 6156.678 |
| 22142 | 17.1198 | 0.86087 | 111.538 | 2.3131 | 19.5471 | 0.32552 | 440.346 | 54.6081 | 0.716032 | 496.061 | 56.7003 | 0.893713 | 110.485 | 435.513 | 89.0362 | 68.80535 | 4956.235 |
| 15423.8 | 25.0513 | 0.909778 | 145.366 | 0.888334 | 74.0528 | 0.474795 | 284.641 | 5.02402 | 0.702935 | 379.109 | 36.6002 | 0.737135 | 31.1377 | 239.698 | 210.772 | 63.49027 | 5697.837 |
| 21766 | 34.2556 | 0.863623 | 91.179 | 3.58783 | 30.5804 | 0.544035 | 470.809 | 66.7208 | 0.909696 | 378.074 | 5.44117 | 0.829697 | 257.849 | 246.462 | 283.684 | 41.17218 | 2982.712 |
| 25178.4 | 29.9916 | 0.838778 | 140.914 | 1.81851 | 41.8513 | 0.606193 | 396.27 | 33.7005 | 0.552127 | 449.228 | 96.004 | 0.730199 | 178.059 | 190.266 | 420.276 | 89.1478 | 5986.344 |
| 30366.1 | 18.3069 | 0.801008 | 158.846 | 0.51308 | 92.9407 | 0.676515 | 493.223 | 66.7527 | 0.808651 | 367.368 | 23.0531 | 0.606247 | 19.8752 | 287.842 | 227.397 | 74.77622 | 5142.458 |
| 10150.2 | 13.5336 | 0.948157 | 131.239 | 1.19419 | 95.1079 | 0.451937 | 266.764 | 11.7905 | 0.919629 | 301.096 | 64.5905 | 0.687072 | 68.5772 | 78.8625 | 149.515 | 49.56528 | 5071.683 |
| 10725.5 | 22.9096 | 0.943976 | 170.764 | 2.59653 | 23.6385 | 0.596696 | 408.281 | 25.8303 | 0.416565 | 407.254 | 85.7742 | 0.997218 | 170.475 | 82.2803 | 327.12 | 56.43246 | 4475.607 |
| 29077.7 | 20.2642 | 0.810387 | 159.118 | 2.16849 | 26.2093 | 0.554882 | 361.443 | 4.93446 | 0.970829 | 180.484 | 92.4149 | 0.78633 | 86.3383 | 172.653 | 127.322 | 47.073 | 3161.144 |
| 12790.4 | 20.2117 | 0.928943 | 161.859 | 2.6816 | 65.4818 | 0.567603 | 101.132 | 40.519 | 0.894315 | 138.097 | 73.8059 | 0.363785 | 6.12732 | 94.2673 | 81.9762 | 84.86115 | 7038.467 |
| 24812.7 | 26.1669 | 0.841436 | 71.5884 | 1.24413 | 59.5074 | 0.37086 | 388.216 | 85.483 | 0.92576 | 137.717 | 20.6041 | 0.804808 | 16.6733 | 284.393 | 47.1324 | 59.91255 | 4828.218 |
| 9813.65 | 34.0854 | 0.950627 | 116.341 | 0.363319 | 10.2937 | 0.300934 | 307.571 | 7.9265 | 0.877499 | 193.893 | 88.7221 | 0.81937 | 11.9179 | 146.925 | 92.6965 | 61.51809 | 4945.403 |
| 26138.7 | 23.4371 | 0.831782 | 142.244 | 2.07097 | 22.0833 | 0.420273 | 315.543 | 39.9089 | 0.659868 | 170.696 | 59.6341 | 0.837109 | 62.4169 | 82.372 | 141.095 | 74.99589 | 5120.55 |
| 20795 | 13.4679 | 0.870673 | 21.204 | 2.07112 | 97.1948 | 0.375191 | 481.131 | 1.87752 | 0.760219 | 263.807 | 72.9165 | 0.972552 | 112.622 | 75.6793 | 242.655 | 54.74338 | 5270.584 |
| 25126.8 | 26.8361 | 0.83915 | 157.699 | 0.753397 | 80.2412 | 0.481349 | 436.519 | 29.6038 | 0.625934 | 57.2709 | 69.9643 | 0.995154 | 2.97747 | 149.177 | 55.9584 | 73.77172 | 5722.388 |
| 22623 | 31.7144 | 0.857381 | 58.9223 | 0.894222 | 78.6489 | 0.482367 | 191.736 | 50.3889 | 0.783173 | 295.629 | 22.3874 | 0.526998 | 79.165 | 179.472 | 233.046 | 76.69602 | 6217.07 |
| 29560.8 | 14.1972 | 0.806867 | 166.247 | 1.27013 | 73.6331 | 0.641073 | 469.76 | 17.6761 | 0.730495 | 296.82 | 72.9766 | 0.997388 | 31.741 | 351.465 | 164.616 | 48.35476 | 3390.595 |
| 28221.3 | 24.2548 | 0.816623 | 78.4588 | 0.943125 | 29.8704 | 0.39203 | 272.118 | 45.1264 | 0.924083 | 314.249 | 46.7729 | 0.743906 | 23.3626 | 180.937 | 160.461 | 59.96339 | 4240.747 |
| 28030.9 | 29.126 | 0.818013 | 91.3217 | 0.463758 | 9.94149 | 0.360545 | 230.802 | 6.40838 | 0.687725 | 492.834 | 58.693 | 0.96321 | 38.9904 | 107.752 | 241.025 | 68.73834 | 4497.823 |
| 23807.1 | 23.7239 | 0.848754 | 167.672 | 1.09149 | 31.6651 | 0.465129 | 334.501 | 83.8197 | 0.976754 | 364.294 | 3.17637 | 0.545809 | 43.1317 | 91.6355 | 189.434 | 88.85702 | 6125.263 |
| 20183.5 | 21.1896 | 0.875129 | 34.3682 | 1.74766 | 22.2422 | 0.372502 | 334.26 | 46.4959 | 0.933117 | 353.431 | 14.7025 | 0.653307 | 92.0514 | 258.819 | 54.9998 | 58.33748 | 4387.057 |
| 16855.4 | 24.2487 | 0.899356 | 28.322 | 0.626382 | 42.4164 | 0.315902 | 296.488 | 54.9746 | 0.839802 | 401.682 | 52.3331 | 0.769045 | 11.7687 | 72.6839 | 310.118 | 66.58939 | 5614.465 |
| 24433.1 | 30.5813 | 0.844204 | 98.6356 | 2.87538 | 79.1018 | 0.475105 | 174.091 | 68.4399 | 0.500785 | 131.346 | 8.91518 | 0.954955 | 101.653 | 115.052 | 102.073 | 67.49801 | 5542.471 |
| 16115.6 | 27.1528 | 0.904745 | 164.907 | 2.80626 | 57.6146 | 0.502399 | 200.015 | 72.9438 | 0.969395 | 286.162 | 75.771 | 0.860128 | 146.882 | 165.178 | 69.8213 | 45.03681 | 3600.072 |
| 30407.6 | 19.135 | 0.800705 | 41.4575 | 1.52478 | 98.6037 | 0.355095 | 406.375 | 79.339 | 0.952712 | 161.305 | 68.1644 | 0.966289 | 106.387 | 263.455 | 139.459 | 71.04522 | 5928.95 |
| 11365.9 | 34.2923 | 0.939328 | 165.142 | 1.66053 | 76.7764 | 0.315756 | 443.289 | 74.9627 | 0.783185 | 129.164 | 73.2103 | 0.99693 | 22.2964 | 375.89 | 94.9983 | 78.32524 | 7326.153 |
| 9348.94 | 15.9967 | 0.95399 | 111.406 | 0.712693 | 74.7023 | 0.363354 | 347.687 | 25.3839 | 0.602585 | 207.308 | 83.6349 | 0.994899 | 71.2203 | 274.139 | 48.8483 | 64.17417 | 6410.121 |
| 16421.6 | 28.8574 | 0.902519 | 134.215 | 0.644946 | 80.0763 | 0.668848 | 363.269 | 36.7165 | 0.938876 | 496.178 | 69.9832 | 0.56197 | 58.2906 | 141.466 | 237.931 | 61.44355 | 4697.377 |
| 24828.6 | 28.2884 | 0.841323 | 109.668 | 2.86538 | 72.3923 | 0.479694 | 276.333 | 25.4524 | 0.871786 | 106.047 | 57.2809 | 0.920903 | 148.172 | 131.51 | 54.7954 | 40.43145 | 3269.384 |
| 26814.9 | 14.2208 | 0.826854 | 37.5248 | 1.85346 | 38.5438 | 0.41929 | 174.855 | 9.72699 | 0.732028 | 190.247 | 40.7297 | 0.527245 | 18.2254 | 100.63 | 80.8791 | 90.54328 | 6672.482 |
| 18617.6 | 28.1983 | 0.886533 | 172.396 | 1.27115 | 59.46 | 0.363666 | 210.697 | 25.7617 | 0.616887 | 491.766 | 94.1581 | 0.894628 | 64.3951 | 68.0674 | 443.765 | 96.44949 | 7808.304 |
| 24245.4 | 29.1079 | 0.845568 | 35.8761 | 1.97333 | 87.4674 | 0.401494 | 265.632 | 49.1461 | 0.973057 | 459.834 | 8.88284 | 0.690591 | 123.143 | 114.948 | 388.558 | 60.00623 | 5301.574 |
| 14094.5 | 29.4567 | 0.919459 | 131.851 | 0.378297 | 95.8256 | 0.478097 | 469.651 | 66.5163 | 0.540024 | 247.209 | 93.8615 | 0.84168 | 24.3818 | 182.973 | 228.237 | 83.96299 | 7495.714 |
| 21197.7 | 31.1859 | 0.867756 | 116.316 | 2.06459 | 56.4544 | 0.372086 | 493.931 | 58.1585 | 0.822473 | 104.579 | 18.6338 | 0.885081 | 16.9021 | 188.303 | 93.9502 | 56.58915 | 4751.006 |
| 12797.9 | 24.2176 | 0.928892 | 82.4918 | 0.891182 | 82.0303 | 0.422711 | 339.546 | 72.6698 | 0.990468 | 198.536 | 42.0285 | 0.694279 | 74.5382 | 240.641 | 120.343 | 50.34339 | 4750.473 |
| 23158.8 | 26.1875 | 0.853475 | 44.7743 | 1.23471 | 66.4137 | 0.480131 | 397.461 | 84.2329 | 0.734743 | 78.758 | 21.2127 | 0.7116 | 87.881 | 287.558 | 66.4463 | 62.56015 | 4871.589 |
| 16029.5 | 29.3893 | 0.905374 | 67.8082 | 2.2821 | 86.1874 | 0.514676 | 466.111 | 46.9479 | 0.837137 | 442.284 | 17.3741 | 0.852946 | 160.632 | 464.998 | 183.549 | 38.81905 | 3464.233 |
| 17773.3 | 27.627 | 0.892678 | 139.566 | 2.37032 | 29.1947 | 0.412009 | 179.096 | 26.2997 | 0.802059 | 369.359 | 60.149 | 0.442315 | 119.58 | 45.5202 | 74.0688 | 99.36502 | 7556.149 |
| 10677.1 | 14.9459 | 0.944322 | 145.718 | 2.934 | 32.9874 | 0.476299 | 443.546 | 88.8633 | 0.774932 | 504.867 | 85.5391 | 0.618482 | 166.183 | 166.093 | 78.1589 | 64.55548 | 5135.505 |
| 19033.3 | 33.5309 | 0.883513 | 106.34 | 0.143776 | 42.897 | 0.572583 | 494.367 | 1.32593 | 0.575016 | 243.885 | 74.2613 | 0.976298 | 13.6681 | 405.875 | 103.954 | 52.88682 | 4065.595 |
| 18661.3 | 22.1403 | 0.886209 | 22.8537 | 3.20673 | 71.222 | 0.53293 | 378.223 | 81.1049 | 0.81812 | 510.667 | 10.153 | 0.751818 | 222.25 | 224.06 | 389.332 | 53.27757 | 4224.778 |
| 16834.5 | 33.2826 | 0.899519 | 170.951 | 1.55881 | 78.182 | 0.557424 | 160.737 | 20.0617 | 0.700147 | 241.9 | 98.5736 | 0.533037 | 32.2965 | 77.115 | 83.1875 | 88.67936 | 7241.438 |
| 23529.8 | 19.9871 | 0.85077 | 67.8944 | 2.17787 | 62.1116 | 0.486591 | 401.684 | 69.7062 | 0.868047 | 434.632 | 44.3412 | 0.939498 | 22.6789 | 312.158 | 189.296 | 40.74118 | 3163.239 |
| 13189.3 | 29.5728 | 0.926048 | 117.015 | 2.37646 | 98.2699 | 0.382439 | 231.723 | 69.7502 | 0.847526 | 448.831 | 50.7177 | 0.575085 | 85.5135 | 163.096 | 307.6 | 80.78707 | 7980.787 |
| 13493.3 | 20.4709 | 0.923826 | 124.725 | 2.63981 | 37.5653 | 0.519132 | 428.72 | 30.526 | 0.445746 | 153.201 | 74.9591 | 0.619353 | 185.92 | 399.968 | 140.233 | 95.71899 | 7511.517 |
| 11035.1 | 33.7309 | 0.941735 | 110.852 | 2.02949 | 60.0496 | 0.469741 | 213.842 | 67.5221 | 0.627957 | 398.866 | 89.9192 | 0.93132 | 115.566 | 70.4035 | 122.433 | 49.96148 | 4414.15 |
| 19452.1 | 28.3029 | 0.880459 | 52.0501 | 0.922831 | 35.5733 | 0.534877 | 264.632 | 4.45325 | 0.863849 | 404.805 | 43.6776 | 0.785548 | 42.3046 | 184.04 | 359.742 | 40.22003 | 3128.425 |
| 23174.8 | 22.2226 | 0.853355 | 162.674 | 0.128577 | 24.5148 | 0.366833 | 495.401 | 55.2689 | 0.971747 | 404.944 | 10.0558 | 0.921422 | 10.2153 | 168.991 | 161.544 | 94.77627 | 6541.153 |
| 24676.7 | 24.0015 | 0.842424 | 163.796 | 0.305156 | 26.8661 | 0.593431 | 259.11 | 46.3421 | 0.965663 | 396.31 | 83.1969 | 0.734235 | 10.5707 | 56.5202 | 241.613 | 58.58983 | 3926.26 |
| 23560.1 | 26.3541 | 0.850554 | 132.858 | 0.411626 | 61.405 | 0.305189 | 151.786 | 36.3447 | 0.81004 | 205.895 | 23.8883 | 0.993576 | 39.3019 | 67.6932 | 69.3884 | 92.21642 | 7390.713 |
| 21094.3 | 29.2628 | 0.868506 | 57.0719 | 0.730365 | 52.4467 | 0.530337 | 398.204 | 49.4415 | 0.834762 | 518.5 | 18.5828 | 0.821121 | 35.6764 | 369.607 | 123.62 | 44.41563 | 3451.178 |
| 23937.1 | 24.032 | 0.847808 | 47.7393 | 0.147195 | 61.4928 | 0.336334 | 232.863 | 34.2371 | 0.822493 | 441.503 | 78.5595 | 0.876019 | 1.4989 | 155.957 | 144.104 | 69.16058 | 5680.63 |
| 15955.8 | 23.8921 | 0.905904 | 107.907 | 1.14731 | 41.6603 | 0.516473 | 144.43 | 3.40203 | 0.839297 | 293.642 | 48.6052 | 0.338284 | 46.5809 | 56.6651 | 57.8078 | 87.1802 | 6980.932 |
| 26541.9 | 31.4229 | 0.828855 | 87.0777 | 2.48093 | 29.2363 | 0.469779 | 176.371 | 84.3652 | 0.890951 | 398.079 | 41.5415 | 0.447579 | 14.3661 | 49.252 | 394.264 | 91.72517 | 6193.278 |
| 11632.3 | 27.377 | 0.937379 | 142.161 | 2.22258 | 28.1385 | 0.548351 | 302.715 | 46.2179 | 0.79389 | 147.479 | 54.0373 | 0.952472 | 80.7193 | 106.05 | 133.733 | 32.36773 | 2641.233 |
| 20775.2 | 18.1807 | 0.87082 | 50.7806 | 3.43658 | 85.4538 | 0.540848 | 194.116 | 21.7995 | 0.827412 | 494.827 | 26.7045 | 0.963807 | 237.008 | 172.323 | 236.142 | 36.42431 | 3092.835 |
| 13610.6 | 13.9971 | 0.922969 | 159.819 | 2.09133 | 53.8463 | 0.647536 | 305.043 | 43.3385 | 0.833481 | 512.023 | 97.3595 | 0.469194 | 195.198 | 158.956 | 295.934 | 85.74473 | 6404.4 |
| 12339.8 | 22.1103 | 0.932224 | 134.786 | 1.68599 | 80.6052 | 0.522103 | 373.812 | 73.2173 | 0.851695 | 214.913 | 32.7171 | 0.98776 | 121.454 | 68.2185 | 170.049 | 34.9518 | 3211.761 |
| 23313.5 | 32.8979 | 0.852356 | 109.765 | 0.39239 | 11.4814 | 0.366756 | 449.358 | 97.857 | 0.936018 | 443.422 | 70.9548 | 0.726691 | 29.0774 | 61.4262 | 181.418 | 77.90019 | 5132.392 |
| 9488.86 | 34.3266 | 0.952991 | 42.9667 | 1.01186 | 11.6022 | 0.338572 | 118.126 | 59.0041 | 0.399806 | 382.986 | 83.1451 | 0.901046 | 90.3915 | 102.291 | 236.719 | 86.12223 | 6910.698 |
| 26275.7 | 26.777 | 0.830788 | 169.326 | 1.69358 | 93.0629 | 0.585683 | 144.3 | 34.1549 | 0.928058 | 335.159 | 52.8772 | 0.772409 | 141.234 | 129.308 | 229.387 | 51.71565 | 3971.774 |
| 30394.4 | 33.5153 | 0.800813 | 152.888 | 1.73493 | 85.465 | 0.475842 | 488.559 | 40.5419 | 0.739635 | 183.811 | 18.9548 | 0.909517 | 158.801 | 386.099 | 175.296 | 65.09446 | 5033.072 |
| 17037.5 | 19.7883 | 0.898027 | 143.287 | 1.63341 | 4.94749 | 0.538963 | 366.093 | 85.2345 | 0.884842 | 452.15 | 53.4207 | 0.644068 | 77.5456 | 364.033 | 239.904 | 54.61415 | 3765.612 |
| 11054.4 | 24.7211 | 0.941583 | 96.1257 | 2.70812 | 2.15746 | 0.307332 | 203.932 | 85.4858 | 0.488863 | 283.554 | 11.6437 | 0.815658 | 146.605 | 158.687 | 113.264 | 84.33467 | 6352.372 |
| 24300.3 | 33.4322 | 0.845174 | 159.789 | 1.93779 | 42.6617 | 0.46901 | 201.218 | 19.6605 | 0.734311 | 360.376 | 14.2554 | 0.532038 | 61.7676 | 188.72 | 238.841 | 97.8514 | 7160.326 |
| 18465.7 | 34.2631 | 0.887646 | 135.037 | 3.66101 | 14.8904 | 0.57317 | 356.276 | 87.5073 | 0.976767 | 491.912 | 69.3806 | 0.523932 | 251.536 | 223.688 | 368.005 | 75.84974 | 5022.928 |
| 16324.2 | 22.9286 | 0.903222 | 148.653 | 2.22182 | 42.6603 | 0.449472 | 90.4939 | 14.6529 | 0.714375 | 502.923 | 62.7235 | 0.815949 | 50.5741 | 61.0611 | 432.666 | 55.9225 | 4605.157 |
| 26116.8 | 13.1374 | 0.831935 | 45.0138 | 2.54513 | 31.8792 | 0.371134 | 352.691 | 22.8178 | 0.544877 | 428.106 | 61.7927 | 0.909505 | 164.55 | 345.378 | 260.641 | 80.0143 | 5825.014 |
| 11532.5 | 17.7919 | 0.938097 | 80.4663 | 2.40542 | 42.9019 | 0.353605 | 347.079 | 57.5197 | 0.55942 | 142.467 | 38.7969 | 0.968921 | 169.336 | 270.993 | 130.835 | 60.44501 | 5499.078 |
| 16088.5 | 16.3415 | 0.904933 | 91.6488 | 3.3263 | 71.0088 | 0.457993 | 376.827 | 43.0298 | 0.801127 | 466.818 | 47.1333 | 0.874291 | 170.922 | 221.017 | 362.91 | 41.81548 | 3767.874 |
| 19316.5 | 29.3964 | 0.881447 | 128.512 | 1.75635 | 53.3922 | 0.476687 | 392.082 | 47.0977 | 0.456296 | 381.283 | 73.6507 | 0.861601 | 116.245 | 128.448 | 373.004 | 83.24041 | 6602.134 |
| 10951 | 21.7412 | 0.942333 | 36.3871 | 3.44994 | 59.7253 | 0.502263 | 211.399 | 0.125564 | 0.387866 | 313.398 | 97.3042 | 0.847407 | 103.07 | 170.511 | 170.029 | 80.4712 | 7053.237 |
| 10231.9 | 30.3257 | 0.947577 | 101.711 | 0.562205 | 7.40113 | 0.350628 | 328.72 | 85.6731 | 0.937082 | 358.359 | 24.3655 | 0.465682 | 11.7298 | 148.024 | 323.913 | 86.24291 | 6505.656 |
| 13574.5 | 19.1538 | 0.923234 | 65.297 | 2.39534 | 20.4087 | 0.488527 | 226.669 | 61.4545 | 0.741536 | 342.932 | 8.48528 | 0.810314 | 115.103 | 204.077 | 77.4225 | 40.29855 | 3189.793 |
| 18183.4 | 13.548 | 0.889683 | 35.7935 | 0.839227 | 65.3057 | 0.417791 | 128.425 | 33.575 | 0.863987 | 491.636 | 22.0254 | 0.869754 | 6.56813 | 110.886 | 290.841 | 42.32428 | 3881.232 |
| 30231.3 | 33.9197 | 0.802001 | 153.236 | 0.452261 | 60.3896 | 0.69367 | 480.575 | 3.24804 | 0.699996 | 457.078 | 5.35796 | 0.67884 | 38.4516 | 82.7566 | 292.878 | 66.05427 | 4429.703 |
| 20990.3 | 28.3781 | 0.869262 | 135.914 | 0.765053 | 5.1438 | 0.394541 | 301.529 | 64.6217 | 0.471737 | 173.52 | 18.2036 | 0.982466 | 54.5664 | 188.677 | 50.3453 | 88.68432 | 5981.073 |
| 16570.8 | 30.9156 | 0.901435 | 160.44 | 3.32301 | 26.141 | 0.457662 | 474.374 | 69.5274 | 0.692734 | 464.02 | 28.2482 | 0.703957 | 171.559 | 403.124 | 409.21 | 67.6176 | 5132.088 |
| 27511.6 | 16.722 | 0.821784 | 31.1996 | 1.37211 | 22.4017 | 0.462513 | 364.41 | 66.2238 | 0.822688 | 315.217 | 16.9047 | 0.93685 | 66.4929 | 206.707 | 173.791 | 42.85983 | 2991.773 |
| 25644.2 | 19.9428 | 0.835379 | 123.511 | 0.277163 | 15.29 | 0.34926 | 257.261 | 97.5022 | 0.839688 | 215.238 | 57.3281 | 0.798601 | 10.3313 | 137.363 | 89.7851 | 88.6604 | 5815.291 |
| 19194.9 | 20.9025 | 0.882325 | 47.0983 | 1.72474 | 94.5075 | 0.451223 | 296.176 | 72.7957 | 0.69387 | 323.863 | 48.9153 | 0.834639 | 84.732 | 191.322 | 187.324 | 59.42979 | 5349.404 |
| 26799.5 | 19.4235 | 0.826969 | 22.7326 | 2.57457 | 20.2838 | 0.507265 | 332.927 | 35.6346 | 0.855656 | 483.28 | 65.0026 | 0.600148 | 93.6525 | 165.076 | 165.164 | 66.39454 | 4375.199 |
| 16606.6 | 27.8907 | 0.901171 | 170.01 | 1.05993 | 65.2694 | 0.530967 | 361.572 | 26.148 | 0.690708 | 167.851 | 25.9874 | 0.839734 | 61.0427 | 117.741 | 161.308 | 56.84142 | 4751.752 |
| 27524.5 | 23.7461 | 0.821695 | 86.1831 | 0.949052 | 31.6142 | 0.482002 | 276.249 | 27.964 | 0.810258 | 254.701 | 85.1565 | 0.821333 | 73.0768 | 151.39 | 243.449 | 51.78562 | 3615.041 |
| 28791.7 | 28.7641 | 0.812475 | 109.365 | 2.14576 | 32.3397 | 0.450273 | 400.409 | 14.1317 | 0.468209 | 264.92 | 18.4784 | 0.982472 | 104.006 | 275.153 | 61.6697 | 72.90301 | 5154.607 |
| 14609.2 | 28.833 | 0.915712 | 105.351 | 2.46628 | 3.84111 | 0.330743 | 145.968 | 84.391 | 0.93548 | 517.198 | 44.9749 | 0.706748 | 158.991 | 39.6093 | 423.486 | 58.4149 | 4174.585 |
| 20766.8 | 30.7345 | 0.870891 | 96.0687 | 1.35754 | 26.4951 | 0.395787 | 308.21 | 13.6587 | 0.767906 | 363.831 | 79.9256 | 0.502319 | 121.879 | 304.471 | 202.94 | 91.05625 | 6742.221 |
| 12248.2 | 28.408 | 0.932897 | 137.416 | 2.6453 | 1.43135 | 0.345863 | 368.786 | 3.53804 | 0.991336 | 327.175 | 4.89633 | 0.399892 | 20.5336 | 291.742 | 312.432 | 79.89236 | 6066.679 |
| 9383.51 | 20.2857 | 0.953742 | 157.607 | 0.22238 | 88.1301 | 0.704021 | 255.427 | 10.1502 | 0.552861 | 350.455 | 42.8824 | 0.544658 | 18.9773 | 179.676 | 138.301 | 74.8181 | 6622.355 |
| 29476.7 | 34.7079 | 0.807495 | 63.3511 | 1.81918 | 35.578 | 0.405369 | 229.252 | 8.99985 | 0.877564 | 304.561 | 75.0226 | 0.502448 | 30.2757 | 110.39 | 120.553 | 90.63132 | 6387.03 |
| 11962.5 | 34.3603 | 0.934985 | 166.718 | 2.21753 | 76.7885 | 0.642081 | 312.665 | 18.2169 | 0.775246 | 317.953 | 34.2627 | 0.644649 | 45.4923 | 260.213 | 298.1 | 50.16498 | 4313.224 |
| 17252.2 | 16.7765 | 0.896463 | 22.0995 | 2.2415 | 50.3902 | 0.512368 | 403.221 | 95.5245 | 0.788068 | 473.303 | 89.1791 | 0.754045 | 152.243 | 148.399 | 290.994 | 59.74714 | 4423.86 |
| 27284.6 | 17.8622 | 0.823437 | 86.5531 | 0.199629 | 81.3877 | 0.357435 | 372.979 | 20.9137 | 0.967041 | 216.323 | 39.3841 | 0.987528 | 6.64719 | 220.882 | 193.662 | 71.1711 | 5884.822 |
| 16884.6 | 33.483 | 0.899155 | 98.4965 | 2.27322 | 48.0319 | 0.486825 | 458.364 | 1.68663 | 0.522803 | 470.401 | 42.6906 | 0.97672 | 174.542 | 222.123 | 249.414 | 48.20087 | 3988.032 |
| 19029.8 | 19.3317 | 0.883525 | 77.8427 | 1.10215 | 46.8018 | 0.385697 | 357.63 | 76.3324 | 0.780225 | 372.263 | 92.0591 | 0.658135 | 46.5306 | 352.885 | 227.069 | 77.01203 | 6111.174 |
| 29045.7 | 13.4439 | 0.810616 | 149.246 | 1.54087 | 99.0811 | 0.430597 | 430.61 | 98.1881 | 0.904997 | 451.569 | 97.0495 | 0.791995 | 64.3002 | 49.2252 | 152.461 | 79.49381 | 6134.598 |
| 15647 | 30.8365 | 0.90816 | 162.105 | 1.51358 | 59.724 | 0.303061 | 209.844 | 39.133 | 0.954131 | 329.766 | 68.6574 | 0.729809 | 22.7037 | 95.4311 | 79.9848 | 84.14733 | 7248.261 |
| 25138.5 | 25.5553 | 0.839064 | 165.419 | 3.40187 | 71.8167 | 0.387509 | 285.082 | 99.4761 | 0.983672 | 503.715 | 22.74 | 0.614208 | 33.8689 | 180.731 | 249.677 | 89.1815 | 6934.18 |
| 15482.3 | 30.3145 | 0.909358 | 154.531 | 0.949193 | 2.65819 | 0.423125 | 482.624 | 48.3264 | 0.650515 | 189.762 | 52.2188 | 0.712836 | 15.971 | 299.901 | 131.345 | 80.35672 | 5685.516 |
| 22377.9 | 21.2449 | 0.859155 | 162 | 2.28379 | 91.7568 | 0.578024 | 446.463 | 41.1183 | 0.858119 | 431.438 | 11.9797 | 0.845987 | 104.179 | 327.604 | 163.306 | 42.21419 | 3492.165 |
| 29528 | 23.8297 | 0.807111 | 135.038 | 1.17386 | 92.5008 | 0.561571 | 398.295 | 73.4337 | 0.958156 | 126.744 | 60.7867 | 0.528305 | 110.619 | 370.921 | 49.0222 | 79.05993 | 5732.619 |
| 24627.4 | 21.5433 | 0.842782 | 130.314 | 2.1252 | 54.484 | 0.391723 | 256.163 | 40.3038 | 0.858983 | 348.406 | 20.5868 | 0.746459 | 150.297 | 56.8451 | 181.773 | 66.02719 | 5216.921 |
| 25474.8 | 17.9804 | 0.836611 | 117.858 | 1.65827 | 31.903 | 0.662066 | 233.235 | 8.64852 | 0.96667 | 344.16 | 87.9461 | 0.844687 | 41.778 | 228.083 | 278.929 | 43.74602 | 2968.975 |
| 11859.1 | 13.9545 | 0.935718 | 157.228 | 0.478573 | 6.03697 | 0.467507 | 172.635 | 39.4985 | 0.915015 | 321.494 | 38.6924 | 0.804185 | 5.12797 | 113.259 | 269.239 | 45.59916 | 3515.787 |
| 13538.6 | 16.0441 | 0.923494 | 56.0393 | 3.11961 | 41.6091 | 0.450133 | 467.243 | 71.41 | 0.642128 | 361.794 | 46.2257 | 0.610673 | 59.5708 | 392.822 | 157.645 | 71.70638 | 5951.9 |
| 19686.4 | 15.6591 | 0.878743 | 162.825 | 0.543439 | 16.6132 | 0.5851 | 387.445 | 13.2862 | 0.633372 | 293.084 | 36.0801 | 0.959917 | 15.3368 | 78.4518 | 110.239 | 50.303 | 3631.474 |
| 11599.2 | 14.7203 | 0.93761 | 74.048 | 2.94531 | 43.976 | 0.458881 | 385.535 | 8.66903 | 0.586761 | 477.436 | 66.7693 | 0.879781 | 97.1291 | 295.466 | 172.504 | 46.83157 | 4204.165 |
| 27006.9 | 29.3908 | 0.825468 | 96.88 | 3.4668 | 33.7926 | 0.419011 | 132.757 | 9.14933 | 0.910744 | 395.241 | 39.7543 | 0.732771 | 55.9957 | 106.402 | 173.36 | 52.66071 | 3898.03 |
| 9451.2 | 32.9672 | 0.953263 | 43.2864 | 0.689815 | 25.7119 | 0.410367 | 478.436 | 27.7676 | 0.61016 | 291.512 | 85.7181 | 0.82967 | 36.4475 | 431.994 | 291.477 | 52.56935 | 4530.969 |
| 15679.5 | 25.5579 | 0.907918 | 161.486 | 3.57481 | 61.901 | 0.431265 | 75.0018 | 84.0069 | 0.848249 | 156.848 | 33.5127 | 0.532187 | 166.358 | 67.557 | 80.8487 | 85.35837 | 7096.197 |
| 11971.7 | 24.8135 | 0.934906 | 88.5176 | 1.64304 | 46.9043 | 0.354545 | 323.769 | 78.9252 | 0.602895 | 192.056 | 30.9279 | 0.900404 | 69.5244 | 152.325 | 161.036 | 63.28204 | 5741.809 |
| 16199 | 26.669 | 0.904137 | 58.9187 | 0.99085 | 18.8026 | 0.432534 | 418.049 | 10.7813 | 0.777125 | 263.273 | 99.2361 | 0.492826 | 28.438 | 241.668 | 187.456 | 74.28697 | 5611.985 |
| 11747.1 | 32.9344 | 0.936551 | 90.1126 | 0.592786 | 65.2205 | 0.345693 | 420.099 | 41.9626 | 0.774002 | 322.149 | 36.9444 | 0.900804 | 26.9912 | 226.885 | 230.026 | 54.97396 | 5362.026 |
| 27064.4 | 20.5394 | 0.825042 | 171.979 | 3.28725 | 26.4508 | 0.457333 | 349.08 | 98.8027 | 0.717 | 324.006 | 5.67041 | 0.682078 | 125.004 | 50.7619 | 223.667 | 88.95733 | 5950.006 |
| 22563.9 | 31.415 | 0.857811 | 75.5211 | 0.633357 | 9.5414 | 0.348407 | 67.5583 | 88.326 | 0.998684 | 246.325 | 18.2009 | 0.677563 | 39.1991 | 57.5327 | 178.553 | 65.84154 | 4443.486 |
| 17074.3 | 27.8186 | 0.897767 | 165.437 | 2.85381 | 60.4003 | 0.407765 | 201.584 | 50.3879 | 0.919529 | 421.968 | 34.4966 | 0.973927 | 73.1737 | 72.703 | 289.78 | 52.54285 | 4468.624 |
| 14308.5 | 19.2475 | 0.917892 | 62.4253 | 1.48959 | 6.81053 | 0.3047 | 472.725 | 66.104 | 0.552827 | 125.139 | 54.7887 | 0.92827 | 63.8772 | 324.834 | 103.936 | 73.69269 | 5453.451 |
| 20405.8 | 26.2858 | 0.873515 | 167.37 | 1.18758 | 62.3958 | 0.533442 | 465.069 | 12.5874 | 0.744963 | 354.047 | 49.1993 | 0.555981 | 85.7341 | 220.809 | 149.806 | 84.23556 | 6562.451 |
| 21129.5 | 26.9337 | 0.868247 | 145.477 | 0.385718 | 36.6807 | 0.659975 | 235.977 | 34.7929 | 0.817958 | 367.289 | 48.8666 | 0.835773 | 23.887 | 177.765 | 150.433 | 42.66776 | 3086.746 |
| 20066.8 | 31.2554 | 0.875988 | 150.012 | 1.27381 | 76.7741 | 0.416306 | 257.854 | 2.19273 | 0.869746 | 500.648 | 70.3865 | 0.559611 | 3.98591 | 203.095 | 116.975 | 87.95166 | 7467.848 |
| 22908.9 | 28.3468 | 0.855296 | 63.8399 | 1.59807 | 40.2317 | 0.460502 | 172.893 | 89.1328 | 0.73121 | 270.714 | 25.0245 | 0.883685 | 148.821 | 80.3091 | 136.239 | 51.62029 | 3869.14 |
| 16495.1 | 33.2767 | 0.90199 | 56.133 | 3.2956 | 83.5699 | 0.389445 | 416.113 | 60.9503 | 0.699418 | 273.553 | 42.3783 | 0.659838 | 22.8993 | 293.965 | 121.642 | 80.54964 | 7555.299 |
| 12980.7 | 26.7634 | 0.927564 | 97.4633 | 2.56979 | 52.763 | 0.402582 | 285.893 | 55.7371 | 0.588863 | 261.737 | 22.2486 | 0.762417 | 49.8278 | 100.479 | 70.0772 | 66.97378 | 6095.804 |
| 23959 | 27.0821 | 0.847651 | 133.527 | 1.97081 | 33.7892 | 0.484819 | 79.7868 | 9.98632 | 0.908787 | 269.319 | 64.7022 | 0.982156 | 103.954 | 45.778 | 205.145 | 40.70114 | 3026.555 |
| 27579.1 | 15.9618 | 0.821292 | 55.0825 | 3.12792 | 43.6964 | 0.384245 | 171.165 | 25.0243 | 0.82552 | 442.698 | 23.2985 | 0.901844 | 40.8021 | 166.505 | 114.232 | 52.31924 | 4044.041 |
| 13023.3 | 18.2722 | 0.927246 | 26.4299 | 1.59318 | 7.4809 | 0.391909 | 358.863 | 79.4159 | 0.872984 | 513.492 | 71.3656 | 0.77533 | 94.2778 | 354.576 | 275.104 | 48.14507 | 3563.615 |
| 26246.1 | 15.6296 | 0.830996 | 77.8385 | 0.171171 | 97.606 | 0.590561 | 282.044 | 62.4942 | 0.854767 | 337.738 | 69.2624 | 0.585818 | 16.2856 | 126.674 | 187.143 | 77.27973 | 5656.836 |
| 27182.2 | 16.409 | 0.824182 | 59.5052 | 1.37248 | 92.0059 | 0.36372 | 470.125 | 35.3769 | 0.727366 | 330.035 | 87.5143 | 0.867583 | 22.1443 | 350.281 | 51.4021 | 76.66055 | 6639.19 |
| 15387.1 | 27.7707 | 0.910048 | 124.328 | 3.6325 | 28.9446 | 0.455753 | 217.77 | 59.4092 | 0.822669 | 199.703 | 29.5466 | 0.792525 | 139.271 | 145.754 | 83.2446 | 42.95879 | 3442.641 |
| 18616.8 | 30.0563 | 0.886541 | 140.738 | 1.60251 | 52.8703 | 0.330977 | 171.891 | 98.126 | 0.723842 | 324.658 | 78.965 | 0.96119 | 48.3148 | 75.9986 | 49.369 | 77.65609 | 6256.521 |
| 30478 | 25.5596 | 0.800198 | 154.908 | 2.74782 | 61.5524 | 0.456635 | 113.74 | 26.9045 | 0.778412 | 302.408 | 37.7861 | 0.555952 | 136.084 | 66.1127 | 284.869 | 98.87431 | 7190.647 |
| 11962.8 | 30.5641 | 0.934977 | 35.5698 | 3.06972 | 4.17817 | 0.383133 | 279.318 | 34.1755 | 0.995552 | 394.967 | 85.1149 | 0.757832 | 13.2707 | 175.93 | 315.013 | 40.74978 | 3088.801 |
| 9821.5 | 34.8625 | 0.950571 | 124.053 | 1.87212 | 71.9119 | 0.395724 | 322.944 | 48.5281 | 0.6478 | 338.745 | 76.157 | 0.767992 | 122.866 | 274.797 | 330.637 | 68.44003 | 6633.25 |
| 11652.6 | 20.2485 | 0.937225 | 159.879 | 1.50343 | 51.5462 | 0.674628 | 309.991 | 48.1098 | 0.875922 | 373.358 | 38.8799 | 0.945388 | 111.063 | 230.266 | 338.575 | 31.13835 | 2561.85 |
| 11498.2 | 22.0039 | 0.93835 | 52.3505 | 1.2358 | 97.9964 | 0.316115 | 280.455 | 54.1648 | 0.973505 | 485.652 | 12.8099 | 0.672684 | 8.73627 | 131.467 | 360.537 | 65.51604 | 7135.64 |
| 27466.4 | 21.1228 | 0.822116 | 43.0322 | 0.921199 | 98.6435 | 0.529726 | 164.85 | 83.8325 | 0.6621 | 204.828 | 47.2464 | 0.950856 | 44.3135 | 140.594 | 180.036 | 62.46796 | 4788.266 |
| 12682.4 | 20.1557 | 0.929729 | 149.239 | 0.529464 | 65.4692 | 0.640967 | 376.524 | 38.5434 | 0.50706 | 147.803 | 5.61769 | 0.924675 | 18.2389 | 152.458 | 81.0146 | 49.89873 | 4297.436 |
| 16432 | 20.492 | 0.902435 | 82.407 | 0.732027 | 58.3674 | 0.482026 | 353.106 | 36.6328 | 0.719479 | 312.293 | 76.7479 | 0.434884 | 9.13861 | 74.9255 | 148.27 | 93.17363 | 7728.107 |
| 16637.3 | 28.1977 | 0.900948 | 67.2012 | 2.16906 | 17.0571 | 0.32958 | 355.88 | 91.5964 | 0.542624 | 97.6933 | 1.58915 | 0.85734 | 70.6002 | 81.8224 | 80.1867 | 80.94504 | 6130.532 |
| 14049 | 34.7679 | 0.919798 | 123.335 | 1.85688 | 27.1143 | 0.474951 | 219.641 | 13.2594 | 0.404962 | 215.514 | 15.6384 | 0.809128 | 161.431 | 195.663 | 155.35 | 76.27721 | 6194.392 |
| 16062.3 | 16.7587 | 0.905124 | 73.8655 | 0.720211 | 24.4045 | 0.400107 | 75.2276 | 85.711 | 0.403918 | 513.843 | 41.5839 | 0.897982 | 38.0314 | 62.9292 | 270.456 | 87.00621 | 6718.35 |
| 20559.9 | 20.5578 | 0.872388 | 110.621 | 3.40048 | 27.6561 | 0.476516 | 71.0393 | 30.8596 | 0.551125 | 225.406 | 38.5835 | 0.511974 | 110.604 | 56.4025 | 218.282 | 97.03429 | 7032.881 |
| 27038.2 | 22.7439 | 0.825234 | 27.5899 | 1.82879 | 19.4752 | 0.496763 | 451.819 | 8.44303 | 0.475587 | 249.242 | 79.46 | 0.743201 | 132.179 | 423.887 | 107.141 | 90.13084 | 5912.532 |
| 13071.7 | 28.3453 | 0.926903 | 110.153 | 3.61953 | 83.869 | 0.320141 | 265.62 | 27.4708 | 0.729243 | 460.918 | 53.3092 | 0.779669 | 17.7475 | 168.116 | 446.765 | 72.15672 | 7448.321 |
| 26762.4 | 17.3111 | 0.827238 | 166.224 | 0.15523 | 73.4135 | 0.727342 | 209.269 | 87.6789 | 0.916006 | 235.242 | 38.3409 | 0.472814 | 8.39754 | 172.937 | 122.357 | 90.93503 | 6021.921 |
| 23127.1 | 23.4829 | 0.853704 | 132.802 | 1.61689 | 11.6349 | 0.538193 | 337.672 | 61.8091 | 0.960416 | 231.071 | 66.6693 | 0.975392 | 101.562 | 331.399 | 60.1753 | 40.50091 | 2738.899 |
| 22275.4 | 21.687 | 0.859902 | 138.271 | 2.43142 | 87.0887 | 0.423846 | 400.276 | 8.92971 | 0.60915 | 382.908 | 5.6224 | 0.73142 | 83.3088 | 273.033 | 308.756 | 84.18952 | 7489.472 |
| 28588.6 | 15.1419 | 0.813944 | 111.104 | 0.308197 | 28.7182 | 0.438396 | 47.4351 | 62.5241 | 0.871227 | 275.784 | 15.1714 | 0.613577 | 30.4694 | 42.536 | 224.116 | 84.90527 | 5707.476 |
| 9995.27 | 20.3075 | 0.949289 | 128.098 | 1.04959 | 4.10522 | 0.304364 | 241.338 | 67.0642 | 0.877498 | 189.517 | 49.9714 | 0.984125 | 102.538 | 159.53 | 128.755 | 57.93478 | 4441.283 |
| 10947.9 | 17.4481 | 0.942352 | 143.657 | 1.22903 | 91.779 | 0.641331 | 481.512 | 67.0041 | 0.643224 | 369.912 | 86.4635 | 0.784619 | 52.3661 | 468.722 | 301.805 | 61.24564 | 5053.842 |
| 10908 | 18.2565 | 0.942643 | 37.7759 | 0.449807 | 53.0688 | 0.518628 | 400.052 | 25.5117 | 0.51283 | 481.995 | 68.1818 | 0.884385 | 21.6869 | 256.518 | 227.537 | 59.36041 | 5148.867 |
| 27614.9 | 34.7459 | 0.821048 | 162.671 | 2.45209 | 31.5847 | 0.417913 | 199.979 | 42.9576 | 0.641574 | 262.164 | 5.82236 | 0.845599 | 52.7215 | 172.568 | 99.3116 | 82.73426 | 5757.084 |
| 15453.2 | 17.7772 | 0.909559 | 117.204 | 2.56111 | 72.9761 | 0.398118 | 236.028 | 3.17199 | 0.823475 | 262.438 | 68.0478 | 0.477046 | 128.839 | 148.52 | 121.29 | 84.80089 | 7930.418 |
| 10673 | 28.7578 | 0.944364 | 151.801 | 1.61614 | 70.1802 | 0.542664 | 252.423 | 30.2002 | 0.752875 | 230.854 | 9.05707 | 0.757041 | 49.4378 | 210.445 | 165.374 | 43.29508 | 4114.767 |
| 24814 | 16.4922 | 0.84142 | 172.171 | 2.02212 | 72.2421 | 0.469847 | 284.814 | 47.8839 | 0.534651 | 339.208 | 86.6565 | 0.923041 | 80.9873 | 229.481 | 270.724 | 90.30906 | 6887.744 |
| 12616.3 | 13.5326 | 0.930206 | 142.005 | 1.36808 | 29.5488 | 0.550855 | 202.854 | 22.1737 | 0.68519 | 496.858 | 56.0519 | 0.761769 | 38.3034 | 50.0092 | 177.233 | 47.24424 | 3846.602 |
| 22275.4 | 20.1668 | 0.859901 | 168.714 | 0.302399 | 78.3453 | 0.601424 | 146.196 | 85.4477 | 0.678731 | 162.154 | 4.08395 | 0.629305 | 7.87262 | 127.335 | 117.259 | 92.66707 | 6855.706 |
| 24920.6 | 27.3034 | 0.840652 | 110.563 | 1.6591 | 42.8051 | 0.378594 | 110.034 | 49.0973 | 0.931334 | 111.592 | 56.3238 | 0.663245 | 23.9971 | 86.1098 | 47.072 | 71.68441 | 5374.974 |
| 21580.9 | 15.3492 | 0.864953 | 94.122 | 2.21366 | 51.8141 | 0.490468 | 326.032 | 94.5888 | 0.709405 | 217.932 | 11.0643 | 0.492622 | 88.7544 | 270.441 | 190.554 | 95.3989 | 6992.713 |
| 28182.5 | 21.5 | 0.816904 | 31.0991 | 0.694817 | 43.7603 | 0.505707 | 398.273 | 58.4049 | 0.495392 | 315.454 | 77.3147 | 0.864003 | 66.9066 | 232.522 | 189.048 | 84.72038 | 5786.993 |
| 15314.9 | 29.7342 | 0.910576 | 162.165 | 2.36287 | 80.376 | 0.597313 | 121.594 | 91.8776 | 0.749613 | 165.312 | 1.15094 | 0.43641 | 73.4529 | 102.982 | 65.558 | 92.4161 | 7220.829 |
| 25304.8 | 17.0355 | 0.837848 | 25.3897 | 2.03705 | 2.89699 | 0.484675 | 192.126 | 93.5399 | 0.439789 | 240.798 | 32.1215 | 0.782559 | 77.69 | 123.623 | 212.065 | 89.66799 | 5650.643 |
| 21322.3 | 20.0574 | 0.866838 | 74.6311 | 1.4996 | 78.6134 | 0.446338 | 495.922 | 30.6993 | 0.80531 | 433.975 | 8.12158 | 0.740609 | 85.3871 | 455.195 | 70.761 | 52.61667 | 4713.877 |
| 14451.3 | 25.4327 | 0.916858 | 118.708 | 3.0044 | 20.0435 | 0.397372 | 165.3 | 94.9414 | 0.816795 | 195.662 | 93.5742 | 0.910047 | 91.8294 | 161.482 | 79.5372 | 49.45992 | 3719.332 |
| 9541.63 | 24.9309 | 0.952595 | 39.8199 | 3.31201 | 84.0915 | 0.57303 | 494.811 | 48.7956 | 0.934552 | 432.619 | 19.6912 | 0.777493 | 330.986 | 363.22 | 231.949 | 37.22169 | 3428.176 |
| 20524.1 | 29.4582 | 0.872657 | 33.9109 | 2.20361 | 16.6304 | 0.441928 | 139.696 | 88.8142 | 0.68827 | 94.1298 | 0.837724 | 0.591527 | 124.808 | 47.5454 | 75.0106 | 78.37553 | 5500.743 |
| 12290.6 | 25.4266 | 0.932585 | 29.4091 | 2.55205 | 9.76197 | 0.440516 | 233.058 | 54.1596 | 0.852889 | 52.7078 | 69.3304 | 0.690746 | 140.82 | 207.713 | 45.5543 | 46.60117 | 3538.954 |
| 19545 | 18.7939 | 0.879775 | 126.913 | 3.05398 | 24.5788 | 0.451611 | 260.901 | 45.4486 | 0.71838 | 362.625 | 97.1479 | 0.657465 | 131.459 | 220.065 | 197.305 | 69.30203 | 5032.047 |
| 20709.6 | 21.8842 | 0.8713 | 133.727 | 1.50446 | 60.4494 | 0.425324 | 349.976 | 78.8449 | 0.816142 | 295.599 | 86.1235 | 0.529376 | 84.8649 | 327.743 | 277.852 | 99.73108 | 7773.464 |
| 21526.3 | 21.1562 | 0.865355 | 90.4099 | 2.80042 | 10.1625 | 0.384324 | 463.431 | 15.8034 | 0.680711 | 493.205 | 1.39864 | 0.555059 | 20.2832 | 206.468 | 274.553 | 86.18006 | 6037.718 |
| 11827.1 | 18.5264 | 0.935953 | 117.337 | 0.207215 | 98.0855 | 0.634445 | 217.102 | 4.12402 | 0.42855 | 358.313 | 68.9653 | 0.9654 | 18.2422 | 201.571 | 352.312 | 58.53684 | 5179.022 |
| 19631.8 | 14.2618 | 0.879141 | 160.145 | 1.88495 | 30.017 | 0.666302 | 297.274 | 60.1922 | 0.474236 | 347.333 | 22.6493 | 0.768021 | 26.4756 | 227.474 | 345.828 | 95.77689 | 6650.559 |
| 15868.7 | 28.9776 | 0.906543 | 156.625 | 2.41551 | 77.3214 | 0.448045 | 79.7966 | 79.7172 | 0.705934 | 79.7075 | 93.5747 | 0.908736 | 4.47385 | 50.5879 | 60.1352 | 63.24309 | 5389.612 |
| 14014.6 | 19.4022 | 0.920031 | 125.586 | 2.46135 | 41.2416 | 0.5246 | 418.583 | 35.7721 | 0.570516 | 459.688 | 35.4018 | 0.663981 | 189.122 | 132.916 | 283.053 | 67.28844 | 5381.694 |
| 10350.9 | 24.5915 | 0.946704 | 158.565 | 2.4107 | 63.7198 | 0.338622 | 289.869 | 14.9152 | 0.707986 | 374.16 | 21.7206 | 0.879183 | 114.903 | 213.639 | 150.143 | 63.22765 | 6265.406 |
| 26405.1 | 26.4804 | 0.829845 | 151.118 | 0.335716 | 60.5038 | 0.666381 | 172.287 | 18.7951 | 0.677129 | 358.743 | 5.79425 | 0.922269 | 4.36735 | 104.312 | 140.865 | 48.75815 | 3546.056 |
| 19450.1 | 29.7896 | 0.880475 | 118.536 | 2.84487 | 39.2485 | 0.517308 | 288.582 | 40.6983 | 0.933347 | 206.378 | 88.359 | 0.458027 | 135.589 | 273.318 | 193.902 | 76.35767 | 5510.442 |
| 22673.4 | 16.9546 | 0.857002 | 162.263 | 2.13051 | 87.068 | 0.387057 | 403.167 | 88.3792 | 0.705638 | 452.235 | 62.1713 | 0.839087 | 43.1423 | 59.5256 | 231.337 | 89.47399 | 7403.259 |
| 18264.5 | 29.9071 | 0.889105 | 143.854 | 0.748583 | 16.031 | 0.557993 | 280.004 | 23.6659 | 0.87215 | 477.359 | 4.82817 | 0.961917 | 16.9654 | 111.152 | 443.749 | 31.96865 | 2477.64 |
| 18256.2 | 32.9699 | 0.88917 | 85.5141 | 0.176474 | 91.3946 | 0.357951 | 205.637 | 70.1741 | 0.764974 | 131.297 | 86.9663 | 0.82503 | 12.1764 | 73.6549 | 79.4689 | 82.43501 | 7357.466 |
| 13933.7 | 17.6956 | 0.920619 | 164.033 | 0.340749 | 47.1633 | 0.573224 | 493.079 | 54.2125 | 0.582413 | 194.326 | 5.60458 | 0.92717 | 21.7899 | 416.641 | 118.053 | 56.61657 | 4624.514 |
| 11166.2 | 29.3983 | 0.940775 | 169.333 | 2.11121 | 29.2976 | 0.401515 | 121.929 | 99.3951 | 0.473427 | 380.426 | 57.3016 | 0.837408 | 151.126 | 114.257 | 251.245 | 95.23232 | 7684.633 |
| 18384.7 | 27.4834 | 0.888228 | 77.5157 | 2.80471 | 57.4736 | 0.317933 | 441.087 | 22.9773 | 0.793867 | 213.047 | 66.2234 | 0.813141 | 12.2884 | 236.153 | 140.285 | 67.93675 | 6016.914 |
| 29272.2 | 17.6929 | 0.808969 | 99.5352 | 2.90276 | 73.3615 | 0.492203 | 381.34 | 73.8374 | 0.710163 | 433.983 | 76.8208 | 0.753147 | 103.614 | 254.751 | 197.158 | 71.26708 | 5129.928 |
| 25084.6 | 15.8095 | 0.83945 | 44.115 | 2.99853 | 55.8017 | 0.338356 | 247.199 | 68.2244 | 0.93983 | 257.821 | 74.7378 | 0.70484 | 95.8852 | 215.701 | 104.596 | 75.63973 | 5940.256 |
| 30089.9 | 22.9465 | 0.80302 | 131.757 | 3.45813 | 74.3626 | 0.511684 | 124.763 | 95.026 | 0.936669 | 311.149 | 14.8616 | 0.69671 | 161.531 | 58.3235 | 280.566 | 58.91944 | 4188.744 |
| 26861.3 | 19.1727 | 0.826519 | 46.3198 | 3.55163 | 21.7189 | 0.435818 | 94.3343 | 53.3788 | 0.722744 | 379.752 | 29.2009 | 0.578362 | 10.0467 | 83.0296 | 308.736 | 83.41589 | 5672.925 |
| 14048.5 | 15.4023 | 0.919782 | 117.818 | 3.61368 | 49.4534 | 0.391752 | 253.764 | 93.5908 | 0.711231 | 467.879 | 10.5062 | 0.697763 | 101.142 | 72.9921 | 297.571 | 67.54682 | 5857.158 |
| 18219.7 | 23.2744 | 0.889425 | 146.056 | 1.00413 | 93.3429 | 0.482518 | 237.046 | 76.2383 | 0.997226 | 222.624 | 45.3886 | 0.464871 | 83.6831 | 83.8441 | 104.03 | 89.67978 | 7459.94 |
| 9793.7 | 15.7622 | 0.950753 | 148.658 | 0.775895 | 71.346 | 0.37169 | 282.824 | 63.7289 | 0.912459 | 85.8472 | 60.0415 | 0.689542 | 64.9732 | 234.16 | 77.9356 | 70.27738 | 6544.088 |
| 17356.1 | 16.3595 | 0.895706 | 155.666 | 2.37852 | 35.2376 | 0.485747 | 236.581 | 77.4081 | 0.972541 | 63.7426 | 87.3857 | 0.973351 | 164.044 | 99.4678 | 45.2229 | 48.23484 | 3561.023 |
| 11606.8 | 13.1095 | 0.937553 | 75.36 | 3.09569 | 25.3581 | 0.438211 | 436.592 | 77.7335 | 0.710534 | 288.93 | 8.56959 | 0.992592 | 144.539 | 269.822 | 63.8355 | 36.29961 | 3097.351 |
| 14087.4 | 15.8524 | 0.919499 | 118.057 | 1.10625 | 7.05862 | 0.47032 | 344.996 | 25.2152 | 0.90169 | 131.542 | 39.2348 | 0.512911 | 40.1693 | 55.8211 | 62.194 | 58.36223 | 4354.982 |
| 10918.2 | 29.1 | 0.942579 | 150.633 | 1.16354 | 52.011 | 0.45338 | 317.668 | 59.3965 | 0.687911 | 393.687 | 67.9084 | 0.879976 | 106.613 | 106.06 | 56.6998 | 56.66534 | 4917.166 |
| 26129.7 | 18.8927 | 0.831844 | 130.762 | 1.50841 | 7.01495 | 0.443597 | 278.706 | 65.2499 | 0.948218 | 403.804 | 91.0286 | 0.729307 | 131.212 | 115.104 | 168.495 | 62.01042 | 3961.713 |
| 13910.8 | 15.6006 | 0.920785 | 49.8142 | 2.42475 | 82.1572 | 0.439967 | 220.265 | 97.4038 | 0.535562 | 233.814 | 62.8817 | 0.770895 | 120.123 | 48.0432 | 203.193 | 78.10323 | 7139.094 |
| 28839.8 | 16.4308 | 0.812116 | 17.2709 | 1.94442 | 75.9078 | 0.479628 | 407.441 | 77.049 | 0.979062 | 447.919 | 22.9272 | 0.584996 | 146.449 | 220.129 | 133.382 | 65.00836 | 4815.676 |
| 24708.1 | 26.2793 | 0.842197 | 140.633 | 2.12976 | 98.0455 | 0.591645 | 263.689 | 86.3515 | 0.993634 | 456.323 | 35.9799 | 0.787856 | 120.498 | 257.039 | 129.675 | 48.17659 | 3586.747 |
| 22320 | 18.5877 | 0.859575 | 157.361 | 0.485625 | 21.9403 | 0.360584 | 137.328 | 79.7273 | 0.810721 | 191.544 | 24.6269 | 0.93663 | 5.58475 | 83.7083 | 87.0789 | 79.84316 | 5577.03 |
| 16581.2 | 16.6022 | 0.901347 | 57.6726 | 3.69258 | 4.51292 | 0.362481 | 383.276 | 12.3509 | 0.980563 | 493.865 | 13.947 | 0.847198 | 55.51 | 356.82 | 58.1724 | 36.14751 | 2765.915 |
| 16612 | 20.1511 | 0.901125 | 98.7155 | 0.277615 | 74.8879 | 0.598634 | 291.114 | 96.8743 | 0.793227 | 448.498 | 66.6912 | 0.893462 | 22.3608 | 244.283 | 393.58 | 46.59744 | 3602.508 |
| 20184.5 | 29.1811 | 0.875128 | 155.51 | 0.923774 | 73.3124 | 0.452285 | 485.925 | 50.9708 | 0.990833 | 344.533 | 69.6159 | 0.941789 | 42.0215 | 97.3467 | 190.17 | 59.41057 | 4750.371 |
| 16162.2 | 31.4548 | 0.90441 | 118.567 | 1.43706 | 1.96695 | 0.554907 | 366.978 | 13.9844 | 0.76279 | 285.012 | 66.0556 | 0.560723 | 103.587 | 278.072 | 181.058 | 61.10584 | 4317.219 |
| 10746.3 | 20.5287 | 0.943822 | 64.9727 | 0.585668 | 22.1314 | 0.382166 | 220.059 | 23.881 | 0.701511 | 71.7237 | 1.34854 | 0.880736 | 6.78064 | 167.797 | 58.2865 | 41.66541 | 3729.768 |
| 11794.3 | 17.6913 | 0.936192 | 117.058 | 1.62907 | 88.3006 | 0.442461 | 117.899 | 42.198 | 0.960585 | 499.693 | 84.2607 | 0.845095 | 72.2264 | 70.7758 | 287.137 | 42.27374 | 4063.463 |
| 11665 | 15.1998 | 0.937131 | 58.1708 | 2.37286 | 11.4777 | 0.5149 | 411.478 | 34.6963 | 0.967122 | 313.941 | 63.1363 | 0.353109 | 182.064 | 353.676 | 294.808 | 85.13863 | 6290.451 |
| 15768.5 | 31.1855 | 0.907276 | 158.547 | 1.04022 | 53.588 | 0.562858 | 84.2966 | 10.7274 | 0.852333 | 114.287 | 73.7904 | 0.359489 | 6.98696 | 65.1395 | 100.717 | 96.83125 | 7705.253 |
| 12242.2 | 30.2552 | 0.932943 | 59.3961 | 0.29581 | 59.4588 | 0.367559 | 105.015 | 69.0984 | 0.890871 | 452.35 | 47.507 | 0.656439 | 8.97074 | 70.5326 | 318.787 | 64.39756 | 5874.756 |
| 21246.5 | 29.5441 | 0.867398 | 131.15 | 2.80606 | 60.4818 | 0.724969 | 494.298 | 87.2618 | 0.911381 | 499.982 | 69.5012 | 0.906004 | 45.6895 | 357.027 | 293.322 | 51.33744 | 3512.158 |
| 22753.2 | 33.4883 | 0.856435 | 107.988 | 0.328719 | 18.3074 | 0.651262 | 202.322 | 37.8211 | 0.928495 | 298.342 | 55.2472 | 0.68919 | 18.9184 | 184.797 | 191.431 | 51.10196 | 3447.13 |
| 11040.9 | 34.5948 | 0.941694 | 115.109 | 0.314918 | 42.8569 | 0.32755 | 210.525 | 71.3832 | 0.671674 | 229.27 | 87.5444 | 0.816969 | 21.77 | 55.4947 | 102.397 | 85.51301 | 7331.51 |
| 14316.4 | 27.7986 | 0.917842 | 105.128 | 0.481864 | 12.3973 | 0.354376 | 335.397 | 62.8875 | 0.683226 | 515.501 | 57.2519 | 0.843704 | 24.3881 | 261.577 | 379.578 | 68.37155 | 5139.451 |
| 21100.5 | 27.4662 | 0.868459 | 166.071 | 3.58584 | 16.4521 | 0.570966 | 144.617 | 88.1929 | 0.531908 | 88.7163 | 51.795 | 0.956264 | 95.8714 | 95.7381 | 68.7549 | 59.14737 | 4032.277 |
| 18685.5 | 17.8243 | 0.88603 | 135.386 | 1.33845 | 6.74306 | 0.354282 | 404.928 | 58.9814 | 0.709695 | 366.74 | 42.0843 | 0.91713 | 67.2833 | 376.544 | 95.074 | 65.04318 | 4569.408 |
| 25211 | 22.3796 | 0.838534 | 94.7396 | 1.56717 | 36.5196 | 0.433952 | 365.036 | 56.5407 | 0.964146 | 468.787 | 99.4391 | 0.575125 | 108.879 | 116.69 | 371.057 | 70.91016 | 5038.418 |
| 29006.3 | 21.8837 | 0.810908 | 44.4165 | 1.31893 | 14.1813 | 0.548638 | 495.56 | 27.6456 | 0.578539 | 281.399 | 53.9572 | 0.993572 | 104.627 | 304.101 | 210.066 | 62.16668 | 3985.489 |
| 21379.2 | 32.6805 | 0.866436 | 151.643 | 1.67024 | 97.7471 | 0.337181 | 337.671 | 97.57 | 0.852763 | 220.541 | 60.6534 | 0.846354 | 151.851 | 133.182 | 88.829 | 85.67537 | 7428.788 |
| 23100.8 | 14.8532 | 0.85389 | 65.2143 | 0.230788 | 10.475 | 0.417845 | 471.878 | 41.5092 | 0.80347 | 488.609 | 52.1159 | 0.6186 | 16.802 | 322.302 | 376.154 | 72.67867 | 4915 |
| 24538.1 | 27.4327 | 0.843436 | 94.4607 | 1.9249 | 42.7939 | 0.499353 | 386.637 | 43.3956 | 0.751222 | 485.548 | 53.0892 | 0.527609 | 113.864 | 129.23 | 374.846 | 82.88827 | 5860.793 |
| 30473.6 | 34.1559 | 0.800238 | 121.743 | 0.488129 | 45.4726 | 0.581076 | 236.53 | 23.0356 | 0.635149 | 504.593 | 73.4915 | 0.724852 | 37.8247 | 93.1763 | 146.837 | 77.06607 | 5182.81 |
| 25112.2 | 32.4018 | 0.839263 | 166.964 | 1.5307 | 37.7319 | 0.623919 | 137.681 | 0.111058 | 0.864598 | 487.236 | 15.8894 | 0.766135 | 14.6266 | 107.282 | 317.711 | 42.86792 | 3124.136 |
| 24753.9 | 23.8803 | 0.841862 | 164.693 | 1.09964 | 94.4734 | 0.429775 | 212.85 | 95.3855 | 0.850383 | 280.256 | 9.18063 | 0.781884 | 106.557 | 59.4382 | 62.5527 | 80.30638 | 6451.608 |
| 18477.3 | 33.7753 | 0.887561 | 165.005 | 0.278159 | 24.1334 | 0.641781 | 279.703 | 1.77569 | 0.544603 | 110.98 | 30.3784 | 0.611881 | 23.8297 | 178.88 | 60.2384 | 88.07682 | 6332.484 |
| 17801.3 | 20.9971 | 0.892469 | 84.7939 | 3.26466 | 38.0212 | 0.473365 | 424.502 | 45.004 | 0.70759 | 327.557 | 99.0272 | 0.817681 | 104.984 | 313.513 | 180.135 | 51.86126 | 3980.677 |
| 17856.7 | 26.2273 | 0.89207 | 164.073 | 1.22964 | 56.0269 | 0.670368 | 298.562 | 80.7851 | 0.680947 | 506.401 | 59.1311 | 0.50818 | 88.6368 | 214.848 | 265.76 | 97.43743 | 6908.211 |
| 14665.9 | 16.0725 | 0.915288 | 43.2197 | 0.815363 | 22.3956 | 0.4629 | 235.675 | 22.8218 | 0.721573 | 113.148 | 3.33995 | 0.860214 | 19.7838 | 116.181 | 89.3062 | 36.76541 | 3083.255 |
| 19830.3 | 32.64 | 0.877711 | 108.955 | 1.55859 | 54.1199 | 0.418382 | 472.896 | 93.1921 | 0.894418 | 336.405 | 94.0857 | 0.587896 | 149.213 | 203.32 | 197.534 | 80.04368 | 6182.009 |
| 20534.2 | 14.2811 | 0.872572 | 47.155 | 1.9427 | 13.0322 | 0.407636 | 119.394 | 5.20281 | 0.347552 | 271.387 | 50.0913 | 0.952203 | 131.227 | 107.832 | 73.4325 | 91.46795 | 6494.433 |
| 11920 | 19.5257 | 0.935278 | 153.031 | 2.03384 | 12.6837 | 0.551307 | 145.255 | 64.1342 | 0.946915 | 500.07 | 91.4727 | 0.421078 | 107.92 | 92.1066 | 286.635 | 71.99219 | 5236.198 |
| 10266.4 | 23.8831 | 0.947318 | 149.552 | 0.195833 | 58.4596 | 0.67193 | 437.831 | 42.1936 | 0.562771 | 491.555 | 76.3646 | 0.634942 | 10.9309 | 435.536 | 301.223 | 70.84013 | 5840.906 |
| 18060.1 | 13.6989 | 0.89058 | 26.4185 | 0.567215 | 67.6422 | 0.399074 | 217.249 | 72.7115 | 0.519266 | 444.995 | 16.9936 | 0.900591 | 51.9742 | 45.726 | 401.372 | 73.87756 | 6591.72 |
| 29670.3 | 21.551 | 0.806074 | 44.3155 | 1.47002 | 61.9915 | 0.464361 | 277.021 | 20.2712 | 0.634713 | 126.337 | 67.3754 | 0.786779 | 24.8773 | 209.267 | 119.712 | 71.22622 | 5381.461 |
| 29917.5 | 31.3537 | 0.804282 | 95.9841 | 1.80398 | 56.5954 | 0.510329 | 267.897 | 36.0622 | 0.506618 | 179.209 | 54.246 | 0.745992 | 31.4419 | 216.386 | 127.266 | 95.16784 | 6658.497 |
| 11250.5 | 26.5459 | 0.940157 | 115.962 | 0.592927 | 40.4692 | 0.543255 | 462.309 | 82.3343 | 0.909241 | 370.725 | 14.6758 | 0.999415 | 38.5129 | 319.565 | 343.492 | 31.28717 | 2683.098 |
| 15826.1 | 31.8722 | 0.906857 | 63.8416 | 0.462177 | 14.3218 | 0.480151 | 373.556 | 21.9971 | 0.935328 | 463.04 | 9.18989 | 0.842803 | 23.565 | 242.634 | 329.142 | 28.97767 | 2356.123 |
| 14368.7 | 20.1544 | 0.917454 | 119.667 | 2.28868 | 62.952 | 0.47686 | 415.897 | 32.3507 | 0.582376 | 160.65 | 51.7481 | 0.597212 | 26.4689 | 275 | 153.255 | 79.22029 | 6989.675 |
| 23654.8 | 28.0851 | 0.849866 | 43.1342 | 1.57613 | 1.11813 | 0.345301 | 408.875 | 44.863 | 0.880181 | 424.417 | 59.6105 | 0.488416 | 26.4355 | 171.549 | 277.579 | 95.59744 | 6098.617 |
| 16874.8 | 32.2251 | 0.899224 | 71.061 | 1.87811 | 70.6563 | 0.402765 | 276.829 | 34.8977 | 0.822965 | 364.781 | 71.2995 | 0.512438 | 125.137 | 232.119 | 94.1815 | 83.37502 | 7425.331 |
| 12243 | 31.5715 | 0.932939 | 145.466 | 1.75664 | 78.0458 | 0.395214 | 159.521 | 28.6304 | 0.792531 | 461.671 | 38.0031 | 0.620699 | 3.70012 | 118.834 | 190.612 | 75.62217 | 7266.233 |
| 25931.7 | 17.366 | 0.833285 | 110.424 | 0.650147 | 73.0086 | 0.463713 | 221.309 | 14.7362 | 0.89338 | 462.94 | 78.5256 | 0.905117 | 22.8803 | 53.7281 | 432.317 | 49.55956 | 3968.026 |
| 11914.3 | 27.7915 | 0.935327 | 30.6151 | 2.183 | 28.8007 | 0.433344 | 210.341 | 72.8339 | 0.919966 | 191.571 | 70.2193 | 0.85178 | 164.8 | 41.7311 | 61.0232 | 39.50627 | 3198.88 |
| 29948.5 | 28.1931 | 0.804054 | 140.206 | 0.916524 | 63.0009 | 0.560921 | 262.107 | 3.51346 | 0.861631 | 270.93 | 75.9158 | 0.890275 | 27.1173 | 239.294 | 115.348 | 48.20438 | 3497.506 |
| 29907.8 | 15.3479 | 0.804342 | 91.9694 | 2.7013 | 56.2264 | 0.4985 | 266.956 | 75.7649 | 0.891527 | 145.58 | 27.1672 | 0.617801 | 27.6508 | 93.0024 | 129.314 | 68.84288 | 4808.618 |
| 17756.7 | 13.5015 | 0.892789 | 15.7766 | 1.23484 | 36.6021 | 0.325892 | 450.951 | 69.8755 | 0.801926 | 428.848 | 48.3475 | 0.673479 | 49.2818 | 136.934 | 286.585 | 78.1836 | 6287.227 |
| 20467.2 | 15.5706 | 0.87306 | 106.849 | 3.55018 | 20.1308 | 0.485688 | 381.082 | 23.5693 | 0.656133 | 377.848 | 69.1458 | 0.492823 | 39.4878 | 173.994 | 314.45 | 87.3959 | 6142.536 |
| 16955.2 | 16.4745 | 0.898624 | 119.446 | 0.2139 | 64.8027 | 0.389681 | 324.063 | 32.2803 | 0.997592 | 411.145 | 8.39832 | 0.561 | 15.1926 | 272.091 | 392.075 | 78.89187 | 6792.874 |
| 21518.9 | 19.2829 | 0.865407 | 153.754 | 2.25046 | 97.2544 | 0.560598 | 237.148 | 0.580631 | 0.513615 | 210.239 | 30.0491 | 0.980458 | 173.719 | 53.5402 | 199.553 | 57.64711 | 4886.472 |
| 13943.5 | 30.9764 | 0.92056 | 126.023 | 1.88118 | 95.4868 | 0.70317 | 413.152 | 33.1252 | 0.987321 | 333.966 | 39.0858 | 0.942592 | 176.482 | 332.642 | 226.967 | 32.51833 | 2718.489 |
| 13135.6 | 33.2846 | 0.926445 | 155.938 | 0.314448 | 71.4849 | 0.661499 | 139.471 | 57.3476 | 0.429588 | 231.015 | 33.9658 | 0.72406 | 6.29665 | 124.689 | 80.4673 | 85.62539 | 6993.703 |
| 9986.13 | 27.0024 | 0.949362 | 124.695 | 3.76966 | 83.765 | 0.532834 | 334.77 | 8.55149 | 0.798947 | 379.618 | 76.9144 | 0.480416 | 208.839 | 206.214 | 363.255 | 75.2143 | 6884.566 |
| 16461.2 | 13.1302 | 0.902219 | 149.177 | 1.17669 | 62.7042 | 0.366651 | 320.113 | 13.1151 | 0.919016 | 195.818 | 95.9043 | 0.795349 | 77.0132 | 252.607 | 71.3117 | 64.19279 | 5512.933 |
| 26905.9 | 16.7014 | 0.826193 | 71.251 | 1.52089 | 11.1785 | 0.382714 | 365.625 | 46.0938 | 0.899957 | 440.211 | 37.1327 | 0.718248 | 106.744 | 200.537 | 316.698 | 60.3259 | 4013.896 |
| 14621.5 | 21.062 | 0.915615 | 72.4984 | 3.50466 | 55.8633 | 0.399563 | 195.897 | 58.5549 | 0.677265 | 405.893 | 58.5359 | 0.918638 | 3.30437 | 49.0225 | 238.327 | 53.70346 | 4785.89 |
| 18446.1 | 15.9783 | 0.887772 | 95.2886 | 1.86875 | 0.856248 | 0.358533 | 208.575 | 58.0152 | 0.780498 | 96.5043 | 87.3883 | 0.917387 | 42.8317 | 151.84 | 69.0965 | 52.48202 | 3575.631 |
| 15093.6 | 21.1036 | 0.912178 | 33.6515 | 2.80599 | 84.5568 | 0.448078 | 329.608 | 60.7908 | 0.475286 | 512.427 | 74.3853 | 0.764087 | 154.348 | 176.942 | 122.881 | 84.91761 | 7781.507 |
| 13352.2 | 27.0527 | 0.92486 | 103.997 | 0.285989 | 31.4338 | 0.319197 | 362.585 | 79.5376 | 0.902322 | 363.851 | 43.6403 | 0.905286 | 13.9902 | 103.272 | 273.628 | 66.8325 | 5413.97 |
| 25265.5 | 22.3698 | 0.838137 | 132.375 | 0.500252 | 3.02763 | 0.369314 | 330.998 | 13.1694 | 0.752495 | 155.282 | 37.582 | 0.938524 | 9.45467 | 198.792 | 48.5728 | 67.00969 | 4369.418 |
| 22102.7 | 15.0686 | 0.861155 | 142.137 | 0.459801 | 7.87744 | 0.394118 | 208.573 | 60.5942 | 0.66894 | 460.013 | 86.749 | 0.810634 | 28.4073 | 177.256 | 431.857 | 89.3413 | 5918.064 |
| 15082.8 | 18.4206 | 0.912255 | 55.5006 | 2.67733 | 34.7369 | 0.413659 | 269.006 | 96.3685 | 0.657694 | 263.078 | 69.8881 | 0.662256 | 136.356 | 202.942 | 108.196 | 76.50187 | 6015.022 |
| 15711.7 | 27.8398 | 0.907685 | 98.2428 | 1.99083 | 31.7897 | 0.422742 | 424.307 | 91.4462 | 0.458132 | 281.469 | 20.2307 | 0.72286 | 118.098 | 60.4572 | 56.8109 | 90.50593 | 7150.054 |
| 10213.8 | 18.8658 | 0.947697 | 106.768 | 1.13715 | 58.5985 | 0.502918 | 355.467 | 90.6504 | 0.898054 | 263.9 | 15.8397 | 0.716101 | 104.396 | 177.288 | 122.031 | 42.71332 | 3770.686 |
| 28812.2 | 29.7941 | 0.812327 | 79.109 | 2.36355 | 34.6545 | 0.440125 | 348.193 | 79.4825 | 0.719458 | 367.507 | 82.9059 | 0.815483 | 34.3702 | 346.098 | 286.03 | 68.5064 | 4728.828 |
| 29508.5 | 16.1303 | 0.807249 | 16.372 | 1.27452 | 88.6175 | 0.468948 | 436.565 | 36.8093 | 0.537107 | 238.17 | 32.995 | 0.75122 | 84.7134 | 208.601 | 156.513 | 87.54142 | 6994.174 |
| 27122.9 | 18.0759 | 0.824615 | 126.492 | 2.92645 | 62.0074 | 0.347858 | 382.967 | 76.406 | 0.516171 | 161.539 | 42.1599 | 0.980062 | 72.8857 | 326.583 | 83.2778 | 97.24654 | 7688.555 |
| 19822.3 | 25.8482 | 0.877762 | 87.7463 | 3.30179 | 35.3066 | 0.512827 | 379.591 | 25.386 | 0.353546 | 386.119 | 45.125 | 0.944499 | 276.316 | 252.967 | 373.322 | 91.51521 | 6723.265 |
| 16981.1 | 15.3844 | 0.898435 | 115.571 | 3.36355 | 20.1809 | 0.305302 | 139.724 | 40.5263 | 0.861859 | 372.008 | 5.32285 | 0.697125 | 164.887 | 67.0314 | 319.792 | 66.22619 | 5194.269 |
| 27081.1 | 28.6211 | 0.824926 | 166.392 | 3.00267 | 21.8579 | 0.516047 | 192.68 | 40.5073 | 0.594826 | 219.303 | 88.5201 | 0.745465 | 7.87395 | 187.91 | 171.782 | 84.38135 | 5554.099 |
| 19984.4 | 28.2733 | 0.876584 | 67.9718 | 1.61076 | 92.366 | 0.457763 | 164.765 | 52.3734 | 0.923452 | 272.63 | 67.4671 | 0.9462 | 120.161 | 124.339 | 202.802 | 42.27383 | 3740.929 |
| 18883.7 | 33.9056 | 0.884603 | 108.404 | 0.683923 | 72.2068 | 0.349694 | 387.785 | 65.1081 | 0.936575 | 256.327 | 16.2653 | 0.855808 | 42.4226 | 233.564 | 98.4964 | 62.30984 | 5503.102 |
| 26515.4 | 21.6153 | 0.829039 | 161.243 | 2.02675 | 2.77279 | 0.422759 | 57.738 | 23.6137 | 0.743805 | 364.018 | 80.9077 | 0.655888 | 154.883 | 50.2492 | 361.657 | 89.68208 | 5637.885 |
| 10751.4 | 31.7253 | 0.943797 | 118.202 | 3.58089 | 91.8916 | 0.50969 | 465.779 | 96.7865 | 0.847049 | 210.868 | 41.4181 | 0.996667 | 87.6941 | 344.709 | 151.508 | 36.19508 | 3280.899 |
| 14540.8 | 27.7391 | 0.916208 | 161.726 | 3.54826 | 28.3999 | 0.365779 | 418.531 | 20.0503 | 0.978242 | 190.267 | 43.5398 | 0.750511 | 158.297 | 239.697 | 148.844 | 51.23535 | 4213.482 |
| 21076.5 | 33.0339 | 0.86864 | 145.841 | 3.38046 | 44.8955 | 0.42993 | 269.519 | 89.504 | 0.989185 | 370.783 | 91.5689 | 0.83005 | 89.7968 | 148.489 | 99.4907 | 54.77214 | 4077.503 |
| 22157.4 | 18.5185 | 0.860758 | 46.4401 | 0.31367 | 51.9543 | 0.421409 | 302.487 | 24.1749 | 0.506013 | 160.194 | 78.1861 | 0.732299 | 29.8576 | 189.615 | 72.8482 | 92.45536 | 7373.052 |
| 20043.9 | 27.0009 | 0.87615 | 56.9646 | 3.60095 | 44.9461 | 0.4302 | 70.5811 | 8.24511 | 0.396415 | 271.2 | 24.9808 | 0.858731 | 97.4652 | 66.1174 | 143.913 | 87.72078 | 7128.967 |
| 16478.3 | 33.9724 | 0.902113 | 76.6393 | 2.28019 | 8.1728 | 0.333845 | 289.917 | 22.7818 | 0.922607 | 180.156 | 29.2899 | 0.526892 | 23.8808 | 175.292 | 155.815 | 72.0968 | 5302.881 |
| 26303.4 | 20.3885 | 0.830581 | 23.2951 | 1.26338 | 55.0285 | 0.426389 | 103.282 | 58.9442 | 0.977396 | 200.874 | 44.7027 | 0.825841 | 20.7355 | 86.7367 | 174.24 | 48.73451 | 3787.498 |
| 16641.1 | 14.5791 | 0.90091 | 28.9522 | 1.11083 | 25.9597 | 0.394582 | 121.554 | 35.8217 | 0.876822 | 512.688 | 96.9405 | 0.964055 | 74.3601 | 47.7833 | 45.3545 | 43.02245 | 3344.166 |
| 29714.1 | 19.0382 | 0.805753 | 163.935 | 1.88664 | 79.3626 | 0.637502 | 213.736 | 2.74398 | 0.747512 | 329.996 | 1.70912 | 0.957325 | 168.614 | 110.112 | 89.7682 | 42.71787 | 3118.832 |
| 22704.7 | 33.9258 | 0.856789 | 51.8308 | 2.04621 | 48.8312 | 0.376808 | 435.421 | 34.1305 | 0.734091 | 356.12 | 25.2516 | 0.592986 | 23.5799 | 366.223 | 94.1866 | 88.47224 | 7092.033 |
| 12196.5 | 34.4813 | 0.933282 | 155.338 | 0.581891 | 2.87102 | 0.628499 | 402.639 | 12.5915 | 0.535933 | 379.849 | 28.7032 | 0.436575 | 16.1733 | 206.815 | 95.4727 | 98.13669 | 7301.148 |
| 14406.3 | 23.3242 | 0.917183 | 158.039 | 1.85676 | 98.8846 | 0.58856 | 344.601 | 49.6198 | 0.80751 | 236.167 | 52.1971 | 0.445159 | 112.104 | 235.302 | 227.856 | 79.27635 | 6718.424 |
| 28843.7 | 28.048 | 0.812096 | 128.922 | 1.95379 | 85.5271 | 0.558842 | 268.13 | 61.6331 | 0.970704 | 503.13 | 78.4017 | 0.788094 | 92.3123 | 210.093 | 328.416 | 51.36782 | 3685.732 |
| 26114.8 | 17.5061 | 0.831952 | 159.199 | 2.4401 | 48.9538 | 0.444967 | 184.401 | 13.0111 | 0.451692 | 211.546 | 15.9505 | 0.941227 | 48.6529 | 84.1421 | 156.746 | 92.73354 | 6909.866 |
| 28576.6 | 18.6807 | 0.814033 | 128.291 | 1.70854 | 58.0226 | 0.743574 | 480.475 | 3.39294 | 0.742063 | 504.769 | 79.309 | 0.93186 | 76.2998 | 382.412 | 355.996 | 59.36625 | 3937.735 |
| 20797.9 | 26.234 | 0.870661 | 147.636 | 0.142629 | 72.07 | 0.602997 | 382.322 | 31.0486 | 0.549198 | 486.059 | 8.51264 | 0.692458 | 1.89329 | 323.11 | 132.676 | 89.07617 | 6831.218 |
| 14637.5 | 25.1503 | 0.915502 | 103.82 | 3.39544 | 76.6553 | 0.509945 | 478.987 | 16.7842 | 0.995393 | 469.173 | 94.6788 | 0.644677 | 260.268 | 281.577 | 412.71 | 45.90057 | 3901.83 |
| 14059.8 | 29.8005 | 0.919712 | 88.6336 | 1.76387 | 54.9664 | 0.502474 | 498.823 | 34.2128 | 0.681777 | 206.89 | 30.5896 | 0.673121 | 165.272 | 117.785 | 111.933 | 57.24061 | 4813.042 |
| 21239.1 | 25.1859 | 0.867448 | 161.302 | 0.216744 | 56.6695 | 0.772088 | 288.253 | 82.5956 | 0.708111 | 493.697 | 70.7007 | 0.993685 | 15.8632 | 190.456 | 481.431 | 49.54609 | 3407.719 |
| 27737.6 | 18.0274 | 0.82014 | 111.264 | 1.80916 | 0.299061 | 0.488934 | 391.073 | 51.7406 | 0.550971 | 330.181 | 21.5437 | 0.748728 | 84.1049 | 131.371 | 319.391 | 75.45164 | 4694.353 |
| 23670.3 | 13.733 | 0.849744 | 117.965 | 0.946721 | 43.0932 | 0.503353 | 243.055 | 31.8954 | 0.960868 | 274.213 | 28.4567 | 0.951909 | 47.6594 | 165.078 | 79.73 | 38.81764 | 2983.326 |
| 29546.2 | 29.0172 | 0.806983 | 129.85 | 2.38548 | 22.924 | 0.469122 | 428.896 | 10.3856 | 0.622622 | 360.442 | 19.0449 | 0.598083 | 94.687 | 406.623 | 92.4083 | 92.69724 | 6171.198 |
| 22689.3 | 30.288 | 0.856897 | 39.5974 | 0.461741 | 22.2096 | 0.393989 | 375.059 | 27.5908 | 0.961499 | 414.792 | 34.9881 | 0.477243 | 1.5018 | 356.557 | 101.596 | 77.22472 | 5570.074 |
| 14210.3 | 30.7833 | 0.918617 | 161.612 | 3.31409 | 59.4807 | 0.508661 | 370.174 | 22.2905 | 0.984917 | 279.393 | 20.8698 | 0.490023 | 73.0638 | 154.982 | 180.842 | 58.02798 | 5062.056 |
| 11765.6 | 28.9905 | 0.936411 | 80.775 | 0.439151 | 42.641 | 0.405176 | 244.186 | 19.897 | 0.567644 | 346.815 | 41.5784 | 0.629615 | 8.74373 | 202.838 | 99.6421 | 83.26317 | 7403.31 |
| 23044.4 | 26.67 | 0.854308 | 104.763 | 1.85147 | 71.108 | 0.459565 | 468.283 | 18.8115 | 0.976385 | 456.349 | 4.65577 | 0.377587 | 28.342 | 241.514 | 427.297 | 88.78371 | 7406.523 |
| 10532.5 | 26.6018 | 0.945384 | 59.969 | 3.11144 | 61.1157 | 0.309797 | 87.7191 | 36.3549 | 0.917782 | 346.582 | 36.7409 | 0.73924 | 45.6315 | 70.2885 | 184.293 | 57.04483 | 5724.635 |
| 28796.9 | 33.5755 | 0.812442 | 42.0881 | 2.76451 | 61.5279 | 0.402821 | 355.13 | 97.3786 | 0.836369 | 180.407 | 3.54247 | 0.658662 | 99.2362 | 166.497 | 71.7678 | 81.44133 | 6187.86 |
| 10733.5 | 22.478 | 0.943917 | 138.378 | 0.521795 | 92.6973 | 0.633865 | 467.216 | 57.6264 | 0.858154 | 371.151 | 48.2905 | 0.490662 | 30.5632 | 109.619 | 202.246 | 64.04444 | 5397.49 |
| 10457.5 | 34.8354 | 0.945941 | 93.811 | 1.24615 | 34.6117 | 0.350798 | 313.955 | 68.6195 | 0.752946 | 447.496 | 8.26469 | 0.969417 | 85.2055 | 226.102 | 66.4923 | 44.39491 | 4047.979 |
| 28219.5 | 30.7986 | 0.816642 | 87.7032 | 1.31443 | 33.6857 | 0.482811 | 372.06 | 92.6071 | 0.61432 | 244.49 | 68.4944 | 0.735171 | 60.7201 | 289.114 | 89.5198 | 79.27867 | 5340.528 |
| 13882 | 25.0717 | 0.921001 | 171.932 | 2.53038 | 32.191 | 0.412317 | 399.177 | 25.2221 | 0.873738 | 76.8833 | 60.5756 | 0.437679 | 62.905 | 213.315 | 52.5962 | 97.03564 | 7736.251 |
| 13607.8 | 14.0771 | 0.922989 | 43.8818 | 1.67602 | 31.0732 | 0.465375 | 436 | 33.3139 | 0.873703 | 409.032 | 6.5662 | 0.344468 | 18.4136 | 105.678 | 106.617 | 83.24616 | 6760.742 |
| 16687.1 | 17.7332 | 0.900577 | 153.183 | 2.2096 | 45.803 | 0.577801 | 392.658 | 34.3645 | 0.989575 | 108.492 | 75.0279 | 0.958393 | 163.951 | 81.422 | 51.4941 | 35.39138 | 2703.097 |
| 12203.5 | 33.2543 | 0.933229 | 137.38 | 3.36783 | 37.4779 | 0.44858 | 195.704 | 17.5942 | 0.655283 | 445.569 | 18.8171 | 0.474322 | 77.2264 | 91.2255 | 363.438 | 83.90217 | 7240.675 |
| 12675.2 | 34.4771 | 0.929797 | 70.7064 | 3.66465 | 31.7276 | 0.467588 | 433.551 | 78.2824 | 0.758377 | 206.029 | 88.159 | 0.586331 | 43.6141 | 70.5455 | 177.556 | 65.27867 | 5105.916 |
| 20849.5 | 24.9044 | 0.870284 | 131.673 | 1.01405 | 55.1629 | 0.562424 | 249.69 | 14.8412 | 0.566519 | 304.404 | 83.2935 | 0.589211 | 59.6287 | 208.695 | 248.341 | 88.30097 | 6675.361 |
| 29847.6 | 30.6557 | 0.804791 | 100.683 | 2.18067 | 36.5677 | 0.381188 | 496.865 | 22.1986 | 0.665279 | 370.315 | 41.6426 | 0.866996 | 48.6579 | 121.224 | 48.0825 | 72.16334 | 5192.184 |
| 23449.8 | 28.5458 | 0.851359 | 129.668 | 3.7528 | 90.9198 | 0.475324 | 411.296 | 70.5755 | 0.655664 | 189.784 | 69.5732 | 0.900248 | 174.279 | 93.8458 | 57.983 | 61.49667 | 5080.286 |
| 16190.9 | 19.635 | 0.90419 | 74.1722 | 0.757896 | 38.7734 | 0.485561 | 291.247 | 79.0913 | 0.537671 | 447.269 | 20.1049 | 0.711873 | 39.8629 | 85.4967 | 353.218 | 70.0065 | 5444.7 |
| 12732.3 | 28.845 | 0.929374 | 36.7222 | 0.32373 | 60.218 | 0.304282 | 454.585 | 99.9013 | 0.770311 | 226.366 | 89.2697 | 0.864303 | 20.6713 | 103.859 | 126.081 | 70.95913 | 6448.267 |
| 21248.6 | 25.3407 | 0.867379 | 115.201 | 1.84664 | 72.3183 | 0.328487 | 395.1 | 35.6131 | 0.922614 | 288.005 | 79.8781 | 0.844865 | 81.3257 | 189.819 | 258.366 | 65.72637 | 5714.585 |
| 23994.1 | 24.8437 | 0.847394 | 117.53 | 1.03487 | 69.6432 | 0.500336 | 227.38 | 91.2369 | 0.831116 | 461.96 | 33.294 | 0.55175 | 26.9384 | 52.1248 | 280.79 | 83.44159 | 6345.126 |
| 15714.1 | 25.6089 | 0.907666 | 44.3006 | 1.67411 | 60.1795 | 0.436799 | 97.1076 | 39.4883 | 0.837331 | 282.389 | 4.37314 | 0.858529 | 118.383 | 73.0493 | 49.814 | 39.18004 | 3634.678 |
| 18305.6 | 13.6957 | 0.888793 | 59.9332 | 0.361277 | 24.6805 | 0.475512 | 253.238 | 34.9784 | 0.556851 | 263.828 | 24.2039 | 0.988859 | 16.4036 | 56.6619 | 226.506 | 47.42605 | 3680.255 |
| 22104.1 | 28.3919 | 0.861155 | 42.7465 | 2.55539 | 92.5985 | 0.362801 | 425.191 | 97.7096 | 0.760703 | 415.209 | 88.6785 | 0.869281 | 16.1046 | 115.272 | 171.605 | 74.78023 | 6577.734 |
| 11619.6 | 18.0575 | 0.937463 | 139.25 | 2.20798 | 49.0814 | 0.360062 | 498.645 | 85.9805 | 0.888521 | 368.567 | 12.6073 | 0.567132 | 131.627 | 369.873 | 278.249 | 79.08769 | 6934.31 |
| 22426.8 | 32.5872 | 0.85881 | 120.299 | 2.43972 | 9.61942 | 0.370733 | 283.393 | 98.3257 | 0.874186 | 266.957 | 57.0233 | 0.867893 | 55.7246 | 48.4571 | 79.5604 | 58.10814 | 3911.994 |
| 10408.2 | 30.3104 | 0.946294 | 105.428 | 0.780219 | 53.3394 | 0.510832 | 80.3921 | 67.121 | 0.968645 | 174.859 | 35.8675 | 0.41393 | 7.80408 | 74.3125 | 124.373 | 70.44237 | 5979.702 |
| 29898 | 31.5145 | 0.804425 | 167.582 | 0.980724 | 47.4628 | 0.483028 | 310.515 | 27.9003 | 0.959976 | 322.084 | 69.4908 | 0.771378 | 88.6192 | 239.313 | 262.727 | 66.33582 | 4571.353 |
| 25319.6 | 23.2169 | 0.837744 | 75.7966 | 2.06806 | 34.5745 | 0.627633 | 485.346 | 45.13 | 0.685418 | 399.664 | 13.8332 | 0.95517 | 193.461 | 415.3 | 329.957 | 54.6833 | 3775.986 |
| 11251.6 | 19.9753 | 0.940143 | 66.5781 | 1.97585 | 77.1598 | 0.412296 | 162.872 | 4.37716 | 0.952639 | 518.196 | 48.7709 | 0.763136 | 123.996 | 133.955 | 173.374 | 38.78247 | 4052.908 |
| 12115.6 | 33.7322 | 0.93387 | 113.139 | 0.632858 | 54.6289 | 0.553693 | 139.904 | 14.654 | 0.977331 | 287.472 | 65.4625 | 0.517655 | 8.0486 | 102.098 | 69.7585 | 49.17518 | 4248.371 |
| 21716.7 | 26.7341 | 0.863973 | 136.771 | 0.809267 | 47.1405 | 0.622828 | 239.478 | 5.48797 | 0.834225 | 226.884 | 62.5875 | 0.427744 | 56.4357 | 134.018 | 195.886 | 84.00916 | 5994.882 |
| 13017.4 | 24.0144 | 0.927294 | 59.0538 | 1.33771 | 6.83133 | 0.419209 | 289.896 | 83.1756 | 0.903603 | 485.457 | 57.0661 | 0.565206 | 74.5322 | 69.2237 | 266.178 | 60.57441 | 4387.568 |
| 15477.3 | 33.7203 | 0.909399 | 131.936 | 0.503937 | 5.67747 | 0.381535 | 293.6 | 97.5017 | 0.685582 | 329.401 | 62.7751 | 0.8909 | 12.6922 | 111.027 | 317.946 | 70.92551 | 5015.938 |
| 18959.6 | 32.2638 | 0.884049 | 79.6947 | 3.08358 | 58.8034 | 0.345776 | 391.633 | 12.8618 | 0.815079 | 338.211 | 51.886 | 0.93772 | 67.644 | 358.507 | 318.793 | 51.70545 | 4635.366 |
| 19254.9 | 19.8425 | 0.881887 | 73.6392 | 0.74504 | 84.3224 | 0.352233 | 423.182 | 57.329 | 0.683114 | 412.916 | 24.9066 | 0.730113 | 41.5923 | 199.383 | 367.38 | 84.85359 | 7923.489 |
| 11110.2 | 16.425 | 0.94117 | 59.4491 | 2.40219 | 0.357816 | 0.491996 | 198.441 | 59.4258 | 0.845824 | 327.2 | 65.3598 | 0.470638 | 63.6564 | 109.044 | 252.45 | 66.08559 | 4757.473 |
| 22341.8 | 31.3007 | 0.859427 | 138.184 | 1.95315 | 35.8531 | 0.547196 | 333.549 | 66.0763 | 0.881006 | 389.265 | 31.7004 | 0.382871 | 106.237 | 192.077 | 188.247 | 95.33267 | 6628.26 |
| 26041.7 | 26.8105 | 0.832491 | 130.848 | 3.77014 | 88.7494 | 0.444287 | 439.27 | 33.489 | 0.555708 | 218.552 | 70.0391 | 0.718598 | 128.911 | 355.337 | 196.733 | 95.41854 | 7925.265 |
| 11386.6 | 31.1556 | 0.939172 | 77.3397 | 1.65436 | 67.7066 | 0.420534 | 436.337 | 74.8029 | 0.804686 | 236.151 | 82.779 | 0.500269 | 49.063 | 241.862 | 48.8866 | 81.58996 | 7388.797 |
| 19273.1 | 33.5865 | 0.881768 | 48.4906 | 1.27291 | 28.1106 | 0.332463 | 175.088 | 49.8288 | 0.872817 | 309.63 | 30.0987 | 0.680237 | 125.622 | 90.4688 | 163.193 | 68.72303 | 5318.465 |
| 29538.6 | 16.738 | 0.80703 | 76.5537 | 0.642923 | 88.4193 | 0.537341 | 235.896 | 72.1299 | 0.872045 | 494.6 | 41.6942 | 0.872821 | 43.7734 | 128.626 | 231.15 | 50.97833 | 3785.708 |
| 9460.22 | 14.9182 | 0.95318 | 94.6148 | 1.11877 | 15.2127 | 0.412598 | 349.027 | 95.3965 | 0.418653 | 88.9889 | 88.6979 | 0.883345 | 23.3996 | 147.935 | 45.54 | 76.9544 | 6098.073 |
| 21178.5 | 18.8227 | 0.867884 | 128.062 | 0.451959 | 53.7266 | 0.569279 | 213.121 | 3.36844 | 0.583189 | 325.646 | 86.1252 | 0.62453 | 42.3735 | 57.3791 | 224.998 | 84.2293 | 6345.596 |
| 29134.1 | 25.8417 | 0.80998 | 164.92 | 2.23449 | 50.7425 | 0.611426 | 164.697 | 60.0047 | 0.707453 | 389.285 | 69.4773 | 0.942333 | 65.0886 | 84.6122 | 117.86 | 54.11823 | 3624.422 |
| 18496.3 | 32.3815 | 0.887421 | 159.512 | 1.75628 | 12.2079 | 0.45564 | 182.664 | 12.8519 | 0.715681 | 458.901 | 97.5343 | 0.726403 | 166.038 | 116.251 | 132.79 | 69.58659 | 4925.396 |
| 20919.6 | 27.5404 | 0.869776 | 41.0937 | 1.26114 | 16.2659 | 0.319233 | 122.083 | 13.4664 | 0.963251 | 146.851 | 90.8343 | 0.603286 | 24.8399 | 54.9944 | 89.6359 | 73.47545 | 5285.285 |
| 21507.3 | 32.8736 | 0.865504 | 134.011 | 0.497166 | 71.2745 | 0.575618 | 385.845 | 63.5844 | 0.914686 | 170.964 | 30.4944 | 0.68204 | 20.6293 | 306.211 | 57.1843 | 55.09332 | 4257.339 |
| 16078.3 | 31.0669 | 0.905021 | 102.714 | 2.48868 | 42.1126 | 0.325607 | 245.628 | 50.4282 | 0.668896 | 218.963 | 48.2133 | 0.685649 | 54.8274 | 148.426 | 134.186 | 87.24585 | 7385.55 |
| 18245.9 | 28.5547 | 0.889239 | 92.6986 | 1.8699 | 9.9094 | 0.451768 | 308.887 | 10.4097 | 0.936855 | 133.638 | 44.1606 | 0.419543 | 41.5498 | 74.0502 | 79.3642 | 67.72351 | 4880.738 |
| 24960.6 | 17.6372 | 0.840354 | 167.361 | 0.243744 | 26.1664 | 0.656684 | 279.676 | 7.12184 | 0.587718 | 234.202 | 24.4438 | 0.739357 | 23.6724 | 165.177 | 210.194 | 76.23133 | 5137.741 |
| 15581.9 | 15.5515 | 0.90862 | 151.304 | 0.769984 | 11.3849 | 0.684458 | 434.992 | 8.92354 | 0.95442 | 184.453 | 79.0333 | 0.564654 | 51.6689 | 96.0878 | 130.299 | 51.70497 | 3725.203 |
| 21317.6 | 33.1119 | 0.866885 | 155.447 | 2.127 | 59.8702 | 0.528445 | 489.549 | 48.0374 | 0.540496 | 285.53 | 54.8828 | 0.945866 | 74.7556 | 104.009 | 207.773 | 65.41348 | 5077.117 |
| 11231 | 13.2573 | 0.940289 | 85.3225 | 0.301594 | 5.92376 | 0.410489 | 274.9 | 11.2849 | 0.75347 | 470.148 | 78.5154 | 0.63708 | 13.5046 | 154.965 | 172.716 | 60.30571 | 4660.42 |
| 22800.6 | 23.6514 | 0.85608 | 96.4539 | 0.362004 | 30.9404 | 0.483235 | 293.502 | 65.5817 | 0.697927 | 137.252 | 52.8086 | 0.663858 | 10.5144 | 109.762 | 98.7032 | 77.34869 | 5487.924 |
| 13502.7 | 32.2649 | 0.92377 | 150.994 | 1.21131 | 45.9482 | 0.569085 | 196.635 | 60.3581 | 0.941721 | 310.191 | 62.3734 | 0.323133 | 85.0639 | 71.8554 | 250.422 | 98.93174 | 7624.823 |
| 11635.2 | 14.0988 | 0.937348 | 150.26 | 0.856684 | 33.8322 | 0.442522 | 235.735 | 63.3346 | 0.642178 | 357.502 | 11.9831 | 0.859411 | 26.3131 | 122.767 | 192.802 | 59.98448 | 5037.756 |
| 22098.8 | 13.0423 | 0.861183 | 59.2683 | 0.149944 | 29.8763 | 0.507692 | 444.922 | 41.4701 | 0.426566 | 67.8941 | 21.4657 | 0.869423 | 11.1598 | 376.756 | 51.9887 | 77.04918 | 5617.311 |
| 17648.5 | 34.6027 | 0.893596 | 124.504 | 3.76252 | 79.7733 | 0.559781 | 463.26 | 23.6429 | 0.713259 | 365.023 | 83.3455 | 0.749557 | 224.239 | 200.841 | 238.304 | 63.34967 | 5078.157 |
| 13242.4 | 28.3773 | 0.92566 | 137.036 | 3.48756 | 83.6013 | 0.544792 | 467.782 | 53.6616 | 0.631449 | 186.585 | 84.1346 | 0.718203 | 89.0944 | 181.262 | 185.977 | 68.06845 | 5727.088 |
| 12285.5 | 20.2167 | 0.932618 | 34.3694 | 2.23032 | 6.8332 | 0.469898 | 197.758 | 50.5807 | 0.696849 | 259.441 | 94.5755 | 0.752741 | 103.366 | 70.6293 | 85.3217 | 49.41216 | 3663.511 |
| 12582.2 | 17.6801 | 0.930456 | 161.418 | 2.72528 | 75.5711 | 0.489492 | 198.586 | 88.325 | 0.499204 | 215.749 | 11.2682 | 0.886904 | 46.0018 | 170.595 | 199.297 | 69.45047 | 6306.97 |
| 14627.5 | 23.156 | 0.915573 | 122.768 | 1.19951 | 74.0876 | 0.497646 | 173.612 | 99.56 | 0.740281 | 371.189 | 80.1547 | 0.546152 | 18.1184 | 118.127 | 339.493 | 85.0038 | 7077.108 |
| 10804.3 | 18.8614 | 0.943399 | 149.165 | 2.52979 | 76.7455 | 0.523301 | 93.7988 | 18.8666 | 0.697367 | 488.469 | 65.1601 | 0.545355 | 9.01526 | 74.1136 | 203.481 | 68.18522 | 6370.394 |
| 20691 | 20.5888 | 0.871434 | 68.9941 | 0.178088 | 99.9151 | 0.449378 | 128.739 | 78.9591 | 0.570303 | 472.052 | 34.7014 | 0.847277 | 14.151 | 103.615 | 116.902 | 79.93583 | 7093.133 |
| 25090.8 | 23.9097 | 0.83941 | 64.5688 | 1.74942 | 2.30722 | 0.366704 | 287.673 | 57.7508 | 0.568315 | 301.969 | 71.2986 | 0.722411 | 96.0481 | 92.5544 | 296.541 | 96.08954 | 6084.124 |
| 26615.6 | 27.6954 | 0.828314 | 115.13 | 0.229857 | 91.134 | 0.445119 | 403.109 | 76.6725 | 0.980202 | 418.402 | 53.8259 | 0.959971 | 17.7597 | 91.9335 | 204.491 | 67.02266 | 5230.753 |
| 13489.9 | 26.2568 | 0.923857 | 123.375 | 3.60269 | 19.4259 | 0.48597 | 451.422 | 99.0338 | 0.433833 | 511.161 | 67.6844 | 0.640201 | 160.712 | 389.996 | 103.637 | 93.30565 | 6892.933 |
| 25472.5 | 30.4192 | 0.836638 | 146.924 | 1.28348 | 92.3145 | 0.705623 | 496.393 | 42.1886 | 0.967598 | 218.721 | 5.19186 | 0.769408 | 63.3619 | 207.461 | 206.997 | 45.33959 | 3323.346 |
| 13129.3 | 14.0232 | 0.926472 | 66.3184 | 2.59284 | 78.1684 | 0.525962 | 183.576 | 60.1833 | 0.970705 | 490.027 | 25.3891 | 0.636335 | 60.822 | 129.53 | 302.599 | 49.15248 | 4245.733 |
| 10470 | 29.3399 | 0.945843 | 67.4915 | 2.64127 | 25.9444 | 0.306107 | 268.355 | 55.5866 | 0.867339 | 92.9497 | 92.9792 | 0.576207 | 28.0722 | 78.6838 | 58.0471 | 78.49428 | 6543.05 |
| 20036.8 | 33.7509 | 0.87621 | 153.578 | 1.8025 | 74.5526 | 0.385913 | 320.37 | 63.6441 | 0.921753 | 200.019 | 96.0883 | 0.989206 | 57.2211 | 290.874 | 50.3032 | 69.3672 | 5639.645 |
| 18536.9 | 20.9385 | 0.887114 | 171.03 | 1.17159 | 45.2735 | 0.441647 | 424.176 | 1.80261 | 0.674246 | 184.725 | 14.8059 | 0.871641 | 85.5652 | 205.435 | 90.1411 | 65.66572 | 5280.623 |
| 23017.6 | 25.1182 | 0.854502 | 169.338 | 2.88641 | 48.6626 | 0.400906 | 414.194 | 63.2775 | 0.887329 | 426.258 | 89.0208 | 0.615979 | 45.7063 | 215.538 | 270.734 | 90.89486 | 6732.518 |
| 18968.1 | 16.9328 | 0.883973 | 115.771 | 1.04086 | 9.07696 | 0.443382 | 194.194 | 94.3082 | 0.574162 | 277.861 | 49.2565 | 0.993228 | 26.3823 | 65.5155 | 127.273 | 60.97597 | 4245.785 |
| 24084.1 | 25.5486 | 0.846739 | 33.5072 | 2.19973 | 31.9476 | 0.498866 | 336.68 | 37.4463 | 0.97672 | 394.06 | 18.6573 | 0.55295 | 197.288 | 311.59 | 193.747 | 56.69828 | 4017.7 |
| 28223.3 | 19.0572 | 0.816605 | 127.234 | 0.308234 | 45.1313 | 0.442799 | 264.147 | 2.2774 | 0.62346 | 421.475 | 77.0477 | 0.890212 | 26.2688 | 257.021 | 292.605 | 83.00546 | 5884.852 |
| 16603.8 | 13.5577 | 0.901181 | 168.206 | 1.72559 | 19.2662 | 0.306793 | 284.784 | 95.6316 | 0.707248 | 343.856 | 2.47827 | 0.878088 | 40.4537 | 93.3516 | 332.476 | 88.36745 | 6603.691 |
| 14381.1 | 14.3287 | 0.91736 | 172.396 | 1.28323 | 45.6874 | 0.562603 | 343.626 | 15.9306 | 0.898638 | 148.961 | 64.2929 | 0.899143 | 13.6417 | 224.974 | 80.6769 | 37.26292 | 3078.216 |
| 16696 | 22.669 | 0.900515 | 57.5632 | 0.350337 | 75.031 | 0.51671 | 320.642 | 26.5489 | 0.437012 | 483.869 | 11.6018 | 0.957787 | 16.3537 | 231.684 | 166.777 | 66.15689 | 5768.453 |
| 21841.3 | 34.2018 | 0.863074 | 66.036 | 3.58521 | 43.2827 | 0.383443 | 389.813 | 9.11076 | 0.903519 | 168.98 | 96.0792 | 0.639914 | 87.9923 | 98.3333 | 55.1859 | 66.44561 | 5228.847 |
| 10331.9 | 17.909 | 0.946837 | 149.989 | 1.68972 | 44.9991 | 0.397229 | 214.731 | 87.122 | 0.824236 | 354.145 | 27.5153 | 0.66612 | 162.518 | 72.8926 | 58.4295 | 67.94462 | 5871.571 |
| 18289 | 15.3368 | 0.888915 | 146.007 | 0.729995 | 4.6138 | 0.638595 | 477.255 | 64.0761 | 0.441306 | 265.113 | 59.6781 | 0.822706 | 70.7227 | 253.823 | 205.356 | 78.29491 | 5309.57 |
| 10794.8 | 18.797 | 0.943468 | 140.978 | 0.79296 | 11.3999 | 0.437446 | 141.773 | 52.224 | 0.903376 | 220.729 | 83.1211 | 0.85885 | 61.3629 | 97.4084 | 86.497 | 44.94463 | 3477.326 |
| 28840.7 | 21.3755 | 0.812113 | 135.93 | 1.92081 | 70.9356 | 0.394671 | 341.707 | 65.2762 | 0.934995 | 490.817 | 59.6193 | 0.809738 | 14.8469 | 194.875 | 462.31 | 68.09789 | 5249.608 |
| 13612.9 | 20.1761 | 0.922956 | 77.5062 | 0.986474 | 34.2672 | 0.504231 | 305.642 | 35.487 | 0.964352 | 515.216 | 66.721 | 0.78748 | 54.7397 | 132.567 | 115.755 | 36.10754 | 2897.266 |
| 14728 | 34.5509 | 0.914854 | 143.147 | 2.55718 | 58.7035 | 0.450201 | 336.939 | 46.7792 | 0.982442 | 361.702 | 93.2421 | 0.372242 | 124.348 | 210.644 | 300.99 | 96.20592 | 7968.445 |
| 21204 | 33.4147 | 0.867713 | 73.7655 | 0.998858 | 50.8194 | 0.407907 | 193.096 | 25.9195 | 0.870604 | 142.498 | 52.7752 | 0.542231 | 41.2934 | 44.5174 | 47.9786 | 74.98598 | 6070.095 |
| 28714.6 | 20.1599 | 0.81303 | 154.838 | 2.48428 | 27.9874 | 0.524638 | 71.4414 | 71.1084 | 0.824435 | 365.625 | 69.161 | 0.803921 | 112.621 | 47.6159 | 304.681 | 59.14189 | 3918.478 |
| 29405.4 | 28.9957 | 0.808008 | 155.988 | 2.95493 | 33.0523 | 0.328787 | 362.677 | 65.9157 | 0.700249 | 503.715 | 75.9292 | 0.979074 | 160.981 | 316.778 | 362.115 | 88.04797 | 6056.393 |
| 9634.14 | 25.3656 | 0.951922 | 132.303 | 3.27033 | 14.0522 | 0.45198 | 176.127 | 65.7615 | 0.897419 | 310.939 | 97.9451 | 0.85822 | 153.262 | 48.0971 | 46.0201 | 39.04191 | 3042.536 |
| 16430.6 | 24.4773 | 0.902449 | 134.346 | 2.31561 | 86.9755 | 0.312924 | 468.497 | 74.3604 | 0.791785 | 422.63 | 37.704 | 0.997555 | 5.12237 | 359.871 | 295.593 | 69.47167 | 6650.312 |
| 20120.7 | 17.9644 | 0.875584 | 82.7042 | 1.56466 | 64.5732 | 0.411991 | 391.928 | 54.17 | 0.606712 | 509.2 | 83.6352 | 0.771977 | 49.0033 | 140.906 | 392.024 | 77.87094 | 6535.316 |
| 19741.8 | 28.8939 | 0.878351 | 85.2897 | 2.95181 | 37.2931 | 0.620989 | 302.315 | 42.9571 | 0.742733 | 491.09 | 64.4423 | 0.980225 | 105.179 | 255.683 | 423.644 | 47.52983 | 3422.91 |
| 15759.1 | 25.4945 | 0.907338 | 72.5274 | 1.73833 | 43.1466 | 0.338669 | 170.833 | 43.074 | 0.501153 | 272.965 | 3.13313 | 0.913495 | 110.337 | 61.8425 | 126.082 | 78.27648 | 6851.983 |
| 24444.2 | 31.6915 | 0.844124 | 112.882 | 2.21899 | 47.1571 | 0.470537 | 428.355 | 14.4099 | 0.995306 | 148.757 | 98.0318 | 0.408309 | 147.162 | 342.926 | 81.1412 | 83.32222 | 6169.998 |
| 18887.3 | 31.2005 | 0.884573 | 84.0725 | 2.80854 | 5.82019 | 0.312769 | 492.904 | 81.0878 | 0.746144 | 422.081 | 13.6658 | 0.874655 | 112.41 | 197.154 | 332.517 | 62.70361 | 4411.245 |
| 13013.2 | 29.8589 | 0.92733 | 62.6179 | 0.866593 | 37.2221 | 0.440803 | 248.707 | 65.3438 | 0.940657 | 505.419 | 77.8492 | 0.94701 | 85.9768 | 146.477 | 198.753 | 38.24346 | 3139.271 |
| 24880.5 | 15.6015 | 0.840935 | 18.7685 | 3.20064 | 15.2865 | 0.372094 | 338.192 | 16.7376 | 0.534821 | 506.25 | 46.7248 | 0.833739 | 67.0299 | 49.5218 | 493.992 | 82.30102 | 5676.476 |
| 11576.7 | 15.4757 | 0.937774 | 133.607 | 2.49474 | 67.8216 | 0.365581 | 454.306 | 43.5763 | 0.833832 | 177.864 | 24.5565 | 0.907038 | 134.944 | 83.1404 | 149.526 | 47.50866 | 4688.312 |
| 18010.9 | 23.2397 | 0.890945 | 129.36 | 3.21367 | 0.283269 | 0.358461 | 135.057 | 76.4055 | 0.997672 | 291.405 | 87.8072 | 0.622792 | 44.0653 | 128.249 | 208.762 | 67.09215 | 4464.108 |
| 13384.7 | 23.2853 | 0.92462 | 56.4143 | 2.55722 | 90.8657 | 0.474728 | 212.691 | 84.3187 | 0.737736 | 81.157 | 71.6021 | 0.488509 | 67.3506 | 106.874 | 69.2273 | 85.16938 | 7528.378 |
| 15096.2 | 22.1078 | 0.91216 | 127.093 | 3.26185 | 78.9969 | 0.445659 | 179.749 | 93.8059 | 0.995721 | 309.937 | 81.989 | 0.782 | 64.0073 | 53.3619 | 273.562 | 49.8187 | 4286.842 |
| 12451 | 20.8795 | 0.931414 | 168.213 | 2.25916 | 85.1285 | 0.540991 | 375.839 | 75.0079 | 0.846249 | 305.743 | 84.1023 | 0.812396 | 44.647 | 369.744 | 285.78 | 49.08613 | 4253.465 |
| 24426.6 | 22.8536 | 0.844244 | 171.763 | 1.55811 | 98.6476 | 0.661676 | 369.36 | 65.6096 | 0.638625 | 411.331 | 0.889027 | 0.788702 | 148.984 | 212.507 | 297.711 | 64.6741 | 4737.871 |
| 11188.6 | 26.6201 | 0.940609 | 35.7213 | 0.986291 | 63.9402 | 0.514481 | 445.136 | 81.1721 | 0.745121 | 234.019 | 40.7135 | 0.975598 | 93.9826 | 375.924 | 204.867 | 38.42928 | 3338.471 |
| 22747.6 | 24.1693 | 0.856466 | 151.237 | 0.210639 | 25.194 | 0.631975 | 129.423 | 34.3107 | 0.764845 | 487.67 | 92.8555 | 0.683354 | 15.8769 | 64.978 | 178.254 | 67.46736 | 4566.109 |
| 21172 | 31.1174 | 0.867943 | 45.9373 | 1.66892 | 30.2338 | 0.400541 | 412.4 | 15.3602 | 0.77919 | 455.199 | 22.1297 | 0.493386 | 60.1169 | 220.356 | 355.784 | 85.39876 | 6515.101 |
| 22978.9 | 22.3161 | 0.854781 | 168.59 | 0.37122 | 50.2843 | 0.625814 | 360.353 | 12.8231 | 0.945587 | 231.908 | 37.8347 | 0.971266 | 23.3823 | 197.143 | 71.6661 | 41.77845 | 3097.578 |
| 19824.8 | 31.218 | 0.877749 | 92.8462 | 1.55319 | 57.8927 | 0.480884 | 191.283 | 33.5176 | 0.852374 | 166.693 | 32.0294 | 0.645789 | 67.5472 | 187.485 | 105.602 | 52.03348 | 4253.107 |
| 18442.1 | 16.615 | 0.887801 | 66.4498 | 2.01076 | 15.5939 | 0.44807 | 367.776 | 24.8507 | 0.788106 | 441.11 | 19.9588 | 0.684388 | 172.94 | 87.3709 | 262.616 | 49.2314 | 3699.699 |
| 10034.4 | 17.2458 | 0.949002 | 80.9344 | 2.29147 | 20.9484 | 0.485532 | 138.227 | 91.2742 | 0.569766 | 228.041 | 60.0905 | 0.993531 | 85.1074 | 127.781 | 101.49 | 45.27468 | 3584.208 |
| 16909.4 | 13.0837 | 0.898956 | 115.536 | 0.678934 | 70.7823 | 0.515869 | 151.915 | 59.3988 | 0.888298 | 122.58 | 18.1956 | 0.753949 | 9.06382 | 91.4815 | 48.2228 | 46.2006 | 3967.558 |
| 15052.7 | 15.9364 | 0.912473 | 110.78 | 3.49794 | 29.4179 | 0.35113 | 271.408 | 28.7624 | 0.809722 | 322.578 | 15.8791 | 0.83594 | 43.656 | 232.974 | 201.309 | 48.13527 | 4109.955 |
| 25330.5 | 18.9387 | 0.837662 | 153.591 | 2.73631 | 55.9449 | 0.469757 | 223.509 | 54.8764 | 0.842864 | 82.4832 | 12.2644 | 0.750228 | 92.8645 | 118.148 | 48.9101 | 60.24862 | 4597.984 |
| 19657.2 | 16.7884 | 0.878957 | 116.575 | 2.83166 | 21.4812 | 0.404056 | 160.374 | 40.2613 | 0.549961 | 142.433 | 4.5821 | 0.623492 | 32.118 | 94.9732 | 61.475 | 92.50475 | 6867.838 |
| 28646.2 | 31.3128 | 0.813536 | 69.3742 | 0.430121 | 89.1093 | 0.310418 | 68.4902 | 60.9562 | 0.811625 | 202.729 | 66.2154 | 0.898688 | 30.7374 | 50.0745 | 147.94 | 84.88652 | 7197.066 |
| 11811.5 | 25.1991 | 0.936073 | 116.312 | 0.112767 | 72.0838 | 0.436077 | 474.51 | 98.7572 | 0.709126 | 296.883 | 32.9009 | 0.805972 | 4.53334 | 93.6341 | 145.158 | 70.75974 | 6263.653 |
| 27603.4 | 22.8861 | 0.82112 | 164.409 | 0.96739 | 29.6529 | 0.647305 | 108.215 | 24.2843 | 0.39201 | 424.745 | 65.3144 | 0.83754 | 53.6914 | 95.0827 | 205.681 | 98.05126 | 6375.819 |
| 16431.5 | 13.2765 | 0.902435 | 74.6926 | 1.63003 | 57.1386 | 0.432224 | 179.117 | 37.0566 | 0.435424 | 342.498 | 7.18943 | 0.751995 | 40.7752 | 116.52 | 156.596 | 87.77937 | 7738.784 |
| 22322.1 | 34.8097 | 0.859575 | 114.847 | 0.354837 | 42.3365 | 0.38757 | 335.571 | 82.6471 | 0.828719 | 160.267 | 96.9046 | 0.908573 | 17.4964 | 327.513 | 122.227 | 69.43049 | 5105.177 |
| 26335.6 | 31.1613 | 0.830356 | 162.862 | 3.69674 | 19.761 | 0.642099 | 361.161 | 51.9181 | 0.759671 | 462.43 | 51.4539 | 0.972628 | 339.092 | 290.854 | 414.387 | 47.28402 | 3110.805 |
| 26952.5 | 32.531 | 0.825867 | 94.4122 | 0.459043 | 52.8748 | 0.310289 | 441.792 | 25.9801 | 0.713036 | 177.974 | 17.8892 | 0.994094 | 13.6017 | 261.828 | 122.278 | 81.17273 | 6362.764 |
| 12425.8 | 17.6266 | 0.931595 | 47.9934 | 3.54633 | 27.5484 | 0.370005 | 441.053 | 25.3047 | 0.655308 | 152.502 | 66.8349 | 0.508899 | 14.7236 | 179.669 | 60.2012 | 91.80138 | 7643.561 |
| 14843.1 | 25.3843 | 0.914005 | 126.039 | 0.673322 | 56.2626 | 0.576619 | 182.592 | 25.2707 | 0.933609 | 82.5397 | 51.1159 | 0.605881 | 44.9815 | 44.2978 | 58.5726 | 46.62987 | 3843.559 |
| 12077.9 | 26.3811 | 0.934135 | 123.659 | 3.61577 | 92.1474 | 0.447332 | 262.484 | 61.7826 | 0.957669 | 101.896 | 33.24 | 0.637435 | 100.67 | 61.1786 | 97.3551 | 51.1939 | 4985.683 |
| 27736.4 | 24.4606 | 0.820153 | 164.42 | 2.35152 | 90.7439 | 0.61602 | 485.443 | 43.1175 | 0.62113 | 471.294 | 53.5524 | 0.824959 | 38.169 | 75.9468 | 279.495 | 68.10742 | 4899.585 |
| 19856.6 | 15.8041 | 0.877504 | 139.728 | 1.70564 | 87.7111 | 0.631306 | 314.064 | 73.6971 | 0.704175 | 414.38 | 80.1679 | 0.731488 | 146.158 | 217.824 | 189.321 | 74.19784 | 5472.55 |
| 11431.5 | 16.352 | 0.938832 | 127.937 | 1.6885 | 43.6882 | 0.316763 | 431.239 | 30.6764 | 0.747879 | 97.4968 | 21.9991 | 0.728858 | 31.8096 | 251.819 | 60.7522 | 72.30909 | 6636.089 |
| 16955.2 | 14.3049 | 0.898623 | 140.757 | 0.103319 | 79.385 | 0.603688 | 200.013 | 6.01591 | 0.865164 | 382.503 | 39.6612 | 0.657277 | 4.75494 | 54.7334 | 244.835 | 54.38252 | 4531.469 |
| 27065.7 | 15.7364 | 0.82503 | 97.2737 | 3.09017 | 0.559658 | 0.474905 | 378.251 | 15.1322 | 0.38649 | 144.898 | 7.39272 | 0.996789 | 153.075 | 321.676 | 65.319 | 73.00415 | 4632.307 |
| 12993.9 | 32.136 | 0.927474 | 130.564 | 1.22815 | 43.078 | 0.527108 | 407.353 | 17.1426 | 0.656088 | 319.269 | 55.4505 | 0.491321 | 46.8235 | 287.654 | 83.8372 | 79.10695 | 6576.391 |
| 25164.4 | 22.1701 | 0.838873 | 152.534 | 2.35766 | 35.0547 | 0.555426 | 241.759 | 59.2633 | 0.432516 | 270.774 | 83.9388 | 0.77123 | 57.7827 | 93.5573 | 189.576 | 98.14565 | 6696.383 |
| 17049.4 | 15.7767 | 0.897938 | 125.723 | 1.38687 | 0.777457 | 0.571282 | 416.06 | 61.0417 | 0.912803 | 221.678 | 65.1856 | 0.701565 | 119.456 | 187.451 | 164.438 | 47.17923 | 3234.929 |
| 14422 | 34.5063 | 0.917082 | 83.02 | 3.36803 | 16.3978 | 0.437104 | 200.029 | 51.4877 | 0.452715 | 497.326 | 57.6409 | 0.977442 | 105.358 | 80.8546 | 132.196 | 61.18377 | 4705.904 |
| 18440.4 | 21.9324 | 0.887818 | 152.465 | 2.44462 | 33.7942 | 0.332087 | 387.159 | 12.3488 | 0.793123 | 480.544 | 18.6918 | 0.915338 | 79.275 | 257.3 | 85.7387 | 60.16611 | 4882.1 |
| 13127.1 | 16.9897 | 0.92649 | 106.807 | 3.66416 | 9.70766 | 0.46555 | 114.394 | 95.3421 | 0.842945 | 433.875 | 82.1006 | 0.93048 | 131.258 | 80.3613 | 153.577 | 38.74428 | 2837.785 |
| 11080.8 | 27.3416 | 0.941394 | 159.329 | 1.66152 | 76.6423 | 0.498629 | 58.5708 | 7.93405 | 0.749132 | 444.919 | 57.2493 | 0.734274 | 70.24 | 51.0023 | 83.3371 | 53.08271 | 5020.15 |
| 14214 | 26.0585 | 0.918585 | 41.9665 | 0.875001 | 3.18349 | 0.49802 | 234.849 | 5.40382 | 0.710185 | 293.982 | 65.7848 | 0.941556 | 20.94 | 190.42 | 83.8414 | 35.2715 | 2670.778 |
| 10725.5 | 22.6449 | 0.943975 | 165.547 | 1.76635 | 48.0015 | 0.507679 | 205.568 | 87.2991 | 0.946551 | 481.961 | 63.5215 | 0.413448 | 106.511 | 102.583 | 90.331 | 88.00834 | 7050.393 |
| 10453 | 27.5963 | 0.945964 | 148.787 | 0.616533 | 93.1922 | 0.59167 | 129.977 | 96.7667 | 0.982845 | 176.275 | 21.7999 | 0.529968 | 43.3354 | 68.7691 | 150.543 | 61.38403 | 5275.31 |
| 20712.9 | 20.893 | 0.871275 | 65.5742 | 2.59235 | 50.9397 | 0.630226 | 345.27 | 49.545 | 0.958484 | 335.176 | 8.96843 | 0.967684 | 157.23 | 324.415 | 214.135 | 33.96043 | 2600.311 |
| 13561.1 | 30.4021 | 0.923343 | 107.031 | 1.16259 | 5.71464 | 0.327464 | 365.977 | 54.6343 | 0.66161 | 147.039 | 68.7945 | 0.871597 | 84.8157 | 144.442 | 125.806 | 66.6003 | 4924.992 |
| 18314.1 | 28.7419 | 0.888743 | 53.5327 | 0.275844 | 0.637678 | 0.490165 | 255.713 | 52.9335 | 0.384106 | 272.266 | 38.7569 | 0.787835 | 11.003 | 177.126 | 108.964 | 83.89591 | 5702.539 |
| 11711 | 31.225 | 0.936811 | 164.985 | 1.37801 | 30.7716 | 0.390625 | 375.732 | 82.0103 | 0.731822 | 415.452 | 27.1989 | 0.777472 | 31.6711 | 60.6206 | 390.989 | 70.80144 | 5778.822 |
| 11186.1 | 18.8474 | 0.940619 | 53.9945 | 0.854344 | 40.4282 | 0.382324 | 468.857 | 67.9938 | 0.435568 | 396.514 | 25.0584 | 0.863576 | 54.8645 | 453.043 | 165.955 | 78.34394 | 7025.932 |
| 11457.4 | 16.9031 | 0.938643 | 110.503 | 2.74127 | 20.6495 | 0.406681 | 405.476 | 6.81581 | 0.987149 | 126.818 | 41.1705 | 0.385079 | 164.36 | 154.899 | 76.7927 | 66.98159 | 5593.253 |
| 16323.3 | 19.408 | 0.903226 | 127.531 | 3.64903 | 85.3339 | 0.367725 | 431.126 | 95.8105 | 0.978965 | 494.966 | 85.6269 | 0.629138 | 44.5531 | 324.778 | 50.3341 | 75.00372 | 6709.193 |
| 10696.3 | 20.6782 | 0.944186 | 162.44 | 1.10318 | 57.1692 | 0.582687 | 302.735 | 80.9046 | 0.668138 | 451.302 | 65.8165 | 0.465747 | 96.6376 | 280.62 | 283.388 | 93.11512 | 7602.238 |
| 10565.3 | 15.2203 | 0.945136 | 98.4191 | 0.734993 | 97.2911 | 0.329557 | 419.667 | 0.32982 | 0.878136 | 260.562 | 36.9526 | 0.705153 | 23.3498 | 162.943 | 116.868 | 64.44626 | 7173.3 |
| 19890.3 | 21.5973 | 0.877263 | 140.758 | 1.31259 | 81.574 | 0.594195 | 376.642 | 11.1906 | 0.616442 | 197.479 | 76.0799 | 0.523929 | 100.285 | 227.991 | 182.315 | 92.6598 | 7144.547 |
| 24187.7 | 19.2106 | 0.845981 | 153.164 | 2.02637 | 17.6354 | 0.543715 | 305.806 | 77.4813 | 0.978096 | 330.986 | 31.264 | 0.604261 | 85.9532 | 287.44 | 202.554 | 59.73938 | 3988.718 |
| 29500.7 | 14.2438 | 0.807304 | 41.8623 | 1.84145 | 76.1603 | 0.577836 | 314.062 | 2.98915 | 0.609534 | 445.646 | 35.2561 | 0.986692 | 152.929 | 250.868 | 401.339 | 61.21887 | 4503.976 |
| 23954.1 | 17.8126 | 0.84768 | 133.424 | 3.68927 | 83.7753 | 0.397948 | 113.175 | 93.5637 | 0.787058 | 349.856 | 21.9486 | 0.817461 | 93.6949 | 46.1433 | 68.0876 | 68.09597 | 5779.906 |
| 12684.8 | 20.739 | 0.929712 | 134.43 | 0.917802 | 13.202 | 0.379656 | 489.29 | 30.2849 | 0.560966 | 203.961 | 17.4484 | 0.993301 | 79.4791 | 440.91 | 85.1902 | 60.94245 | 4845.555 |
| 13343.2 | 17.1679 | 0.924917 | 161.296 | 1.79315 | 14.1002 | 0.52196 | 322.486 | 54.9535 | 0.386544 | 230.485 | 77.8462 | 0.825175 | 112.04 | 111.768 | 94.6205 | 88.69247 | 6604.58 |
| 23499.8 | 18.425 | 0.850987 | 132.147 | 3.01187 | 75.1357 | 0.50177 | 306.04 | 9.26587 | 0.89914 | 223.12 | 98.572 | 0.498208 | 162.155 | 302.638 | 97.5971 | 72.36193 | 5703.481 |
| 15771.2 | 26.9603 | 0.907251 | 164.242 | 1.5446 | 3.38738 | 0.360511 | 377.176 | 32.7175 | 0.849274 | 400.478 | 83.0345 | 0.710331 | 68.6284 | 203.213 | 329.215 | 73.73434 | 5218.109 |
| 18332.9 | 30.7255 | 0.888608 | 79.9445 | 2.46865 | 0.179771 | 0.36884 | 454.921 | 57.3366 | 0.626799 | 214.102 | 41.5569 | 0.701688 | 137.056 | 158.527 | 176.747 | 76.83696 | 5210.898 |
| 21090.5 | 23.5674 | 0.868528 | 78.6738 | 0.527733 | 9.1317 | 0.346742 | 409.378 | 37.1171 | 0.646872 | 383.392 | 77.2528 | 0.924776 | 41.0035 | 315.45 | 137.5 | 68.82548 | 4757.972 |
| 22822.2 | 26.0646 | 0.855925 | 124.394 | 1.05675 | 77.3719 | 0.441746 | 199.843 | 19.3619 | 0.875317 | 191.152 | 16.3136 | 0.468365 | 58.3825 | 122.317 | 166.427 | 94.29964 | 7863.697 |
| 20628.3 | 29.9831 | 0.871898 | 42.891 | 1.71809 | 9.62035 | 0.44744 | 140.378 | 78.9234 | 0.857387 | 403.564 | 92.3485 | 0.971766 | 100.441 | 60.8233 | 136.072 | 43.03154 | 2950.206 |
| 14277.7 | 30.9904 | 0.918127 | 158.836 | 0.572872 | 48.7415 | 0.577475 | 381.432 | 30.8376 | 0.998274 | 114.322 | 37.6611 | 0.878738 | 38.4273 | 89.4024 | 100.744 | 36.48668 | 3025.305 |
| 18381.4 | 29.6317 | 0.888254 | 31.5084 | 1.26132 | 42.1139 | 0.402918 | 143.414 | 92.7126 | 0.954863 | 343.759 | 13.7717 | 0.683099 | 3.47677 | 100.583 | 124.446 | 56.97117 | 4539.532 |
| 25492.4 | 32.7271 | 0.836495 | 157.766 | 3.5822 | 80.0398 | 0.481578 | 392.444 | 71.1376 | 0.933659 | 102.29 | 28.7414 | 0.551219 | 94.6208 | 155.818 | 53.129 | 79.58019 | 6188.64 |
| 13419.7 | 27.0977 | 0.924368 | 125.485 | 1.11549 | 44.0096 | 0.516638 | 289.291 | 61.9871 | 0.832477 | 218.728 | 72.6002 | 0.394082 | 84.6231 | 208.922 | 52.8997 | 90.44764 | 7148.896 |
| 15868.7 | 27.1429 | 0.906542 | 71.9964 | 0.931194 | 60.6555 | 0.511177 | 354.151 | 29.9699 | 0.992742 | 429.294 | 11.8836 | 0.705577 | 71.9882 | 249.743 | 363.815 | 37.15003 | 3223.906 |
| 16084.4 | 27.2264 | 0.904972 | 167.888 | 1.58017 | 33.7157 | 0.587066 | 386.254 | 70.8618 | 0.508559 | 238.904 | 41.6691 | 0.880219 | 153.637 | 283.254 | 60.1046 | 64.42161 | 4862.315 |
| 12029.3 | 23.8781 | 0.934486 | 158.151 | 1.96786 | 59.8044 | 0.543029 | 457.454 | 53.8513 | 0.517275 | 233.101 | 3.39684 | 0.760753 | 146.323 | 113.61 | 110.897 | 66.18926 | 5799.136 |
| 16680.3 | 31.9299 | 0.90064 | 113.097 | 0.530347 | 92.9001 | 0.3674 | 283.523 | 78.8531 | 0.881444 | 491.919 | 0.462322 | 0.716733 | 9.32638 | 152.175 | 81.1807 | 77.93237 | 7259.4 |
| 17100.3 | 31.0209 | 0.897581 | 137.456 | 0.118564 | 9.42147 | 0.652055 | 460.409 | 57.8195 | 0.426796 | 134.512 | 3.97129 | 0.868225 | 3.90899 | 243.782 | 125.315 | 73.19135 | 5200.771 |
| 24474.2 | 28.2912 | 0.843902 | 59.1168 | 1.57045 | 33.6968 | 0.405898 | 125.941 | 76.8894 | 0.64567 | 300.671 | 85.7994 | 0.919047 | 124.557 | 52.6304 | 243.679 | 67.35833 | 4858.477 |
| 24454.1 | 26.3492 | 0.844047 | 151.903 | 1.94839 | 94.821 | 0.632373 | 439.923 | 45.6087 | 0.559034 | 397.074 | 92.8751 | 0.730673 | 29.8659 | 431.374 | 328.285 | 94.01494 | 6826.906 |
| 9424.06 | 15.2992 | 0.953443 | 122.966 | 0.283595 | 46.6211 | 0.402942 | 287.836 | 48.8866 | 0.878975 | 498.857 | 37.0864 | 0.608134 | 28.08 | 262.958 | 412.076 | 67.87146 | 6057.199 |
| 10894.1 | 26.4549 | 0.942752 | 135.289 | 1.05914 | 80.2852 | 0.593588 | 343.071 | 28.1192 | 0.997446 | 382.485 | 54.9381 | 0.649677 | 33.1591 | 200.492 | 267.526 | 39.1409 | 3463.842 |
| 26092.5 | 17.7142 | 0.832114 | 162.893 | 2.00856 | 11.2766 | 0.373285 | 307.518 | 64.7723 | 0.88 | 474.324 | 88.2677 | 0.76804 | 120.228 | 227.155 | 391.753 | 79.64746 | 5154.563 |
| 29856.6 | 26.7133 | 0.804722 | 105.651 | 2.49843 | 13.981 | 0.586497 | 186.948 | 20.4288 | 0.998122 | 477.967 | 84.3261 | 0.855138 | 28.6723 | 181.136 | 245.794 | 43.78907 | 2807.748 |
| 19078.8 | 20.8449 | 0.88317 | 171.849 | 2.35368 | 61.0907 | 0.626858 | 478.103 | 87.5051 | 0.766341 | 191.753 | 34.2828 | 0.445896 | 46.3414 | 108.712 | 188.653 | 97.02557 | 6944.109 |
| 13131.9 | 19.2858 | 0.926456 | 106.769 | 0.341669 | 76.938 | 0.525693 | 431.061 | 68.3089 | 0.902764 | 399.599 | 88.0035 | 0.921211 | 30.7122 | 92.3867 | 75.7494 | 41.00667 | 3518.488 |
| 9441.77 | 33.9637 | 0.953334 | 131.488 | 2.18892 | 75.2906 | 0.533832 | 425.02 | 36.5486 | 0.363839 | 351.893 | 62.1097 | 0.972432 | 134.007 | 384.725 | 348.642 | 65.98155 | 6017.671 |
| 29870.5 | 14.0695 | 0.804613 | 101.704 | 3.30002 | 76.1369 | 0.46651 | 148.104 | 57.0854 | 0.724383 | 314.424 | 59.8288 | 0.534153 | 163.413 | 60.7906 | 93.3999 | 97.32529 | 7301.873 |
| 30348.5 | 24.3257 | 0.801139 | 131.418 | 1.32948 | 70.4476 | 0.373664 | 115.38 | 54.8316 | 0.739519 | 453.651 | 6.94086 | 0.959838 | 112.261 | 85.3501 | 118.609 | 73.95225 | 5756.023 |
| 18600.5 | 22.41 | 0.886652 | 149.071 | 1.75519 | 43.5189 | 0.61649 | 312.4 | 99.0056 | 0.687486 | 324.941 | 82.6921 | 0.563747 | 80.1343 | 276.115 | 310.262 | 93.63147 | 6497.4 |
| 28504.4 | 13.2157 | 0.814556 | 72.4147 | 1.14791 | 36.733 | 0.380724 | 486.114 | 10.4655 | 0.697188 | 340.304 | 46.8351 | 0.757257 | 81.4997 | 70.9224 | 302.944 | 75.08706 | 5491.102 |
| 30086.3 | 31.3865 | 0.803054 | 98.9521 | 0.443595 | 49.6918 | 0.385812 | 378.912 | 45.4044 | 0.804726 | 375.004 | 65.4669 | 0.86876 | 40.7858 | 339.545 | 160.124 | 73.47611 | 5310.29 |
| 13585.9 | 24.9868 | 0.923157 | 85.4613 | 3.14102 | 80.1904 | 0.396236 | 430.01 | 39.1309 | 0.569857 | 486.18 | 27.1898 | 0.829653 | 91.7445 | 172.554 | 403.078 | 67.53479 | 6704.147 |
| 25353.7 | 14.7815 | 0.837491 | 118.104 | 1.91759 | 62.8289 | 0.478761 | 213.018 | 47.5891 | 0.575283 | 309.735 | 68.3797 | 0.942261 | 102.159 | 47.2285 | 289.729 | 65.08857 | 5019.256 |
| 13625.4 | 31.97 | 0.922877 | 139.266 | 2.97545 | 54.7292 | 0.541126 | 356.353 | 62.636 | 0.441812 | 322.451 | 21.7437 | 0.977306 | 116.907 | 210.015 | 106.649 | 59.10937 | 4897.118 |
| 21894 | 15.1605 | 0.862674 | 138.127 | 2.60457 | 38.8609 | 0.397282 | 254.242 | 4.50437 | 0.648545 | 81.4848 | 17.1905 | 0.934966 | 118.995 | 172.374 | 59.3071 | 59.19571 | 4698.243 |
| 23442.6 | 13.4768 | 0.851401 | 100.332 | 0.33122 | 74.1761 | 0.414147 | 385.671 | 13.7951 | 0.576519 | 459 | 34.0161 | 0.943155 | 8.91999 | 260.218 | 300.037 | 76.00794 | 6366.244 |
| 20406.8 | 15.2264 | 0.8735 | 149.648 | 0.521462 | 74.8877 | 0.78073 | 347.372 | 80.1989 | 0.836861 | 225.115 | 1.6691 | 0.83826 | 21.922 | 266.669 | 219.083 | 48.49895 | 3478.282 |
| 15918.6 | 17.0764 | 0.90617 | 81.4432 | 1.5401 | 69.3161 | 0.357948 | 283.789 | 87.5401 | 0.975959 | 60.1316 | 45.4358 | 0.732946 | 70.995 | 144.285 | 51.5105 | 59.32241 | 5306.146 |
| 13767 | 22.5283 | 0.921836 | 54.9397 | 0.893629 | 68.4912 | 0.455696 | 77.7481 | 18.8813 | 0.982324 | 212.97 | 78.8725 | 0.825947 | 32.2593 | 50.761 | 78.251 | 36.08792 | 3345.198 |
| 22079.4 | 33.2943 | 0.86134 | 169.779 | 0.809035 | 28.8604 | 0.457942 | 200.144 | 53.1381 | 0.801152 | 422.362 | 52.5381 | 0.991107 | 3.42006 | 81.4329 | 56.7144 | 60.46168 | 4304.737 |
| 29718.3 | 25.5315 | 0.805727 | 56.1116 | 1.32136 | 74.4235 | 0.447172 | 460.197 | 3.8013 | 0.907211 | 308.687 | 5.48363 | 0.921965 | 23.4532 | 213.51 | 58.9144 | 40.55529 | 3442.259 |
| 22191.4 | 23.1898 | 0.860514 | 113.446 | 2.13289 | 37.0931 | 0.34656 | 294.796 | 41.949 | 0.748544 | 502.114 | 53.6137 | 0.688191 | 163.831 | 53.6987 | 380.569 | 83.55268 | 6397.08 |
| 25772.1 | 25.9199 | 0.834453 | 34.7411 | 0.617998 | 44.4181 | 0.343538 | 249.112 | 99.0406 | 0.605277 | 246.499 | 78.5726 | 0.87558 | 54.422 | 123.485 | 220.246 | 91.88201 | 6860.313 |
| 21563 | 34.7508 | 0.865101 | 163.809 | 2.90588 | 18.5035 | 0.596533 | 248.349 | 38.8634 | 0.792495 | 213.56 | 34.7664 | 0.910667 | 67.3335 | 79.5321 | 172.514 | 39.45098 | 2798.211 |
| 19861.1 | 20.1819 | 0.877474 | 134.215 | 3.10003 | 76.8102 | 0.383345 | 102.034 | 23.9856 | 0.738133 | 334.549 | 55.5985 | 0.843995 | 129.97 | 45.8127 | 317.055 | 64.35377 | 5759.594 |
| 28749.3 | 33.4646 | 0.812788 | 112.777 | 1.113 | 66.7135 | 0.362574 | 68.0001 | 39.0905 | 0.923669 | 472.781 | 34.2216 | 0.988332 | 105.827 | 43.2928 | 287.509 | 66.65729 | 5240.75 |
| 16782.2 | 24.8292 | 0.89989 | 83.4712 | 3.73612 | 8.99981 | 0.355294 | 82.8704 | 41.2083 | 0.708226 | 428.931 | 59.8705 | 0.98875 | 15.3478 | 67.1545 | 305.614 | 49.91551 | 3685.666 |
| 14664.4 | 22.2039 | 0.915303 | 170.171 | 0.991207 | 92.0534 | 0.348287 | 94.7304 | 25.9462 | 0.945349 | 208.652 | 24.7627 | 0.904012 | 37.5686 | 76.5752 | 132.077 | 74.27133 | 7016.627 |
| 22777.1 | 29.2353 | 0.856257 | 82.5788 | 0.271138 | 41.8176 | 0.504729 | 441.329 | 91.9711 | 0.894157 | 446.267 | 17.5846 | 0.574988 | 4.02024 | 45.3074 | 128.685 | 70.51557 | 5095.186 |
| 30435.5 | 29.2575 | 0.80051 | 125.987 | 2.73834 | 89.2928 | 0.343733 | 192.022 | 39.6989 | 0.835666 | 328.971 | 50.3215 | 0.722298 | 81.9427 | 52.7667 | 113.993 | 92.14253 | 7642.537 |
| 24858.8 | 13.0844 | 0.841093 | 137.629 | 1.32191 | 97.3896 | 0.579099 | 103.736 | 68.0301 | 0.554561 | 424.603 | 99.2741 | 0.810998 | 53.5085 | 89.2682 | 174.984 | 79.0841 | 5850.723 |
| 11773.8 | 33.7508 | 0.936357 | 48.3395 | 3.05702 | 47.4992 | 0.360954 | 251.824 | 3.05537 | 0.890861 | 65.8784 | 54.1029 | 0.455466 | 94.6242 | 227.59 | 52.421 | 77.05959 | 7177.785 |
| 23613.2 | 18.5493 | 0.850162 | 109.091 | 1.78426 | 4.0742 | 0.521864 | 353.43 | 4.28488 | 0.807087 | 245.74 | 72.5847 | 0.927769 | 60.157 | 269.981 | 76.5407 | 38.71883 | 2627.981 |
| 10237.2 | 18.056 | 0.947526 | 135.219 | 3.13232 | 0.257082 | 0.492132 | 425.397 | 48.3654 | 0.49941 | 326.411 | 33.4203 | 0.696806 | 79.3018 | 189.388 | 64.8161 | 63.17315 | 4807.218 |
| 27365.1 | 30.2519 | 0.822861 | 136.377 | 1.45284 | 14.3328 | 0.534467 | 205.579 | 49.3281 | 0.419653 | 392.532 | 99.2686 | 0.962977 | 69.5727 | 115.509 | 145.093 | 86.10196 | 5516.443 |
| 14844.2 | 17.8963 | 0.913991 | 45.386 | 1.35547 | 17.6003 | 0.358938 | 429.607 | 61.588 | 0.772368 | 289.349 | 57.5343 | 0.882869 | 68.7707 | 120.982 | 113.885 | 51.06233 | 3960.396 |
| 10914.4 | 25.1977 | 0.942603 | 150.125 | 1.77833 | 71.283 | 0.516443 | 442.647 | 94.1067 | 0.807748 | 387.611 | 36.2769 | 0.425288 | 143.85 | 102.84 | 180.85 | 91.90913 | 7859.683 |
| 28572 | 27.772 | 0.814073 | 161.208 | 0.225932 | 99.3262 | 0.593958 | 310.054 | 80.8037 | 0.586825 | 403.174 | 43.1456 | 0.836973 | 18.9753 | 219.102 | 138.157 | 91.38664 | 6584.743 |
| 26230.6 | 31.7883 | 0.831121 | 91.9123 | 0.852407 | 51.3233 | 0.339003 | 231.612 | 54.7781 | 0.935873 | 239.924 | 69.4294 | 0.753677 | 33.4283 | 144.312 | 205.409 | 74.6253 | 5706.048 |
| 9974.76 | 30.3302 | 0.949449 | 103.587 | 1.31188 | 26.117 | 0.546984 | 398.025 | 62.702 | 0.775194 | 292.144 | 51.6164 | 0.613392 | 83.9451 | 137.981 | 291.149 | 57.90259 | 4536.885 |
| 29569.9 | 24.4384 | 0.806806 | 60.0038 | 1.87823 | 11.545 | 0.505466 | 229.77 | 56.8633 | 0.759588 | 370.517 | 31.8072 | 0.942106 | 182.267 | 200.761 | 251.519 | 46.38807 | 3000.197 |
| 12335.4 | 33.062 | 0.932269 | 151.717 | 0.780767 | 52.9535 | 0.552538 | 148.552 | 13.883 | 0.88062 | 308.005 | 87.8936 | 0.70954 | 58.9709 | 57.3023 | 296.984 | 46.84361 | 3960.48 |
| 14265.6 | 18.1656 | 0.918204 | 146.756 | 0.278883 | 5.08352 | 0.730151 | 452.969 | 62.5054 | 0.93137 | 491.6 | 17.4004 | 0.459223 | 16.4314 | 143.854 | 302.786 | 70.89728 | 4964.057 |
| 25521.8 | 30.9207 | 0.836279 | 68.0032 | 1.54649 | 63.4984 | 0.417645 | 259.005 | 5.22684 | 0.839508 | 198.118 | 0.075387 | 0.615707 | 51.4502 | 104.614 | 196.115 | 68.60009 | 5721.617 |
| 23130.8 | 15.7023 | 0.853672 | 30.605 | 2.14254 | 90.7481 | 0.555308 | 305.685 | 15.3411 | 0.896878 | 373.048 | 62.0812 | 0.798827 | 91.5298 | 248.426 | 349.101 | 47.26105 | 3804.254 |
| 13290 | 28.6186 | 0.925314 | 87.6402 | 0.803726 | 38.6658 | 0.301188 | 419.788 | 18.6185 | 0.571641 | 348.481 | 73.2808 | 0.814953 | 23.4996 | 364.951 | 275.609 | 88.50782 | 7738.198 |
| 24962.3 | 33.4795 | 0.840355 | 72.0568 | 3.46471 | 69.8585 | 0.31502 | 327.011 | 26.2956 | 0.893747 | 496.646 | 53.8895 | 0.743223 | 47.6 | 162.393 | 145.825 | 77.16744 | 6591.941 |
| 10860.2 | 32.415 | 0.943006 | 58.4878 | 3.26183 | 38.5654 | 0.381365 | 113.319 | 12.0081 | 0.957338 | 469.701 | 45.9092 | 0.929271 | 36.4896 | 103.404 | 313.843 | 35.27747 | 3314.308 |
| 12336.8 | 27.2847 | 0.932251 | 86.1934 | 3.38543 | 67.2856 | 0.527875 | 208.78 | 41.3663 | 0.670169 | 277.426 | 84.1484 | 0.55819 | 245.244 | 136.094 | 263.374 | 86.73206 | 7184.564 |
| 17967.6 | 31.0204 | 0.891268 | 47.882 | 2.03312 | 87.8126 | 0.376371 | 333.807 | 2.38265 | 0.69343 | 496.697 | 72.3004 | 0.883923 | 48.5687 | 101.749 | 280.608 | 61.66206 | 5967.028 |
| 23694 | 25.7098 | 0.849579 | 161.539 | 0.659862 | 87.9316 | 0.426022 | 117.663 | 19.2987 | 0.759416 | 135.063 | 93.1478 | 0.876447 | 50.1452 | 77.2405 | 125.78 | 79.13102 | 6358.835 |
| 11443.9 | 29.8873 | 0.938753 | 110.706 | 1.0372 | 89.4662 | 0.513484 | 369.472 | 60.0692 | 0.931621 | 302.937 | 45.6638 | 0.56241 | 84.1241 | 360.692 | 254.455 | 55.01697 | 5071.422 |
| 27828 | 25.6854 | 0.819487 | 59.853 | 1.20813 | 94.7051 | 0.322833 | 139.744 | 47.9037 | 0.719025 | 304.595 | 16.8257 | 0.941098 | 59.2967 | 78.4903 | 45.224 | 78.15397 | 7029.946 |
| 17899.1 | 14.6009 | 0.891753 | 158.091 | 2.99302 | 57.0049 | 0.458376 | 286.745 | 0.976714 | 0.927361 | 149.573 | 97.0882 | 0.813969 | 151.149 | 222 | 111.32 | 46.71227 | 3888.255 |
| 15322.1 | 18.1985 | 0.910513 | 20.1233 | 3.24635 | 66.0581 | 0.349423 | 296.982 | 50.7064 | 0.884552 | 57.1049 | 7.09372 | 0.916706 | 95.4217 | 213.584 | 49.6065 | 45.80347 | 4421.659 |
| 10482.1 | 15.5406 | 0.945742 | 46.8945 | 0.284236 | 23.4483 | 0.411481 | 436.39 | 40.8659 | 0.696091 | 347.765 | 71.7137 | 0.573109 | 4.81488 | 137.967 | 238.617 | 68.31695 | 5662.38 |
| 15164.8 | 27.8729 | 0.911666 | 88.9885 | 1.29396 | 31.8085 | 0.316553 | 58.0274 | 14.468 | 0.583932 | 464.079 | 86.2782 | 0.744667 | 113.128 | 50.9712 | 82.7265 | 89.445 | 7384.981 |
| 19106.4 | 29.8259 | 0.882977 | 97.0831 | 0.246982 | 56.5524 | 0.369371 | 196.24 | 19.7437 | 0.949595 | 114.531 | 65.7383 | 0.711128 | 19.9739 | 109.339 | 93.6529 | 67.1689 | 5582.542 |
| 16783.4 | 25.9664 | 0.899882 | 107.216 | 0.89825 | 95.1314 | 0.382794 | 169.786 | 20.5095 | 0.888644 | 268.459 | 32.0309 | 0.625164 | 28.3012 | 152.37 | 192.96 | 72.02294 | 7012.664 |
| 11086.1 | 33.817 | 0.941364 | 161.948 | 0.517865 | 84.323 | 0.522932 | 93.9406 | 65.9479 | 0.780856 | 161.001 | 21.1842 | 0.626444 | 14.7099 | 52.5504 | 64.8176 | 69.75064 | 6247.813 |
| 24648.7 | 29.1933 | 0.842633 | 99.4799 | 1.74385 | 64.3605 | 0.487313 | 142.053 | 51.3025 | 0.639934 | 383.946 | 87.294 | 0.936332 | 47.386 | 64.119 | 119.226 | 57.17768 | 4368.312 |
| 24156.9 | 25.0586 | 0.846209 | 148.399 | 3.04555 | 50.9929 | 0.458394 | 88.1412 | 42.9493 | 0.428421 | 330.918 | 47.0177 | 0.886104 | 7.40841 | 79.4577 | 206.882 | 95.96142 | 7268.98 |
| 22798.7 | 25.0209 | 0.856095 | 122.581 | 1.24522 | 74.8273 | 0.507529 | 358.264 | 20.5626 | 0.647027 | 232.341 | 87.0265 | 0.890298 | 83.9897 | 63.0512 | 157.994 | 59.5166 | 4782.391 |
| 11339.5 | 22.8226 | 0.939506 | 104.674 | 0.747532 | 23.7377 | 0.514794 | 448.055 | 34.1082 | 0.971106 | 134.727 | 32.6824 | 0.667725 | 21.5809 | 223.85 | 128.421 | 36.93369 | 3081.151 |
| 18816 | 13.0383 | 0.885078 | 131.678 | 2.7574 | 1.76648 | 0.318071 | 417.968 | 12.2097 | 0.794105 | 501.075 | 49.1925 | 0.762091 | 99.6572 | 388.067 | 397.029 | 66.14419 | 4598.014 |
| 26600.7 | 25.057 | 0.828421 | 55.8196 | 1.06617 | 88.1545 | 0.464893 | 77.6366 | 10.3247 | 0.931236 | 377.058 | 79.4786 | 0.575288 | 46.5464 | 71.318 | 162.732 | 66.30479 | 5497.504 |
| 20570.9 | 18.7826 | 0.872307 | 118.795 | 0.101889 | 46.9757 | 0.538195 | 207.3 | 39.0094 | 0.985279 | 481.285 | 95.8846 | 0.891463 | 4.02496 | 169.178 | 203.401 | 49.67231 | 3661.462 |
| 21944.3 | 26.343 | 0.862316 | 166.837 | 1.54057 | 23.3092 | 0.446869 | 187.083 | 13.3364 | 0.636536 | 511.587 | 14.7158 | 0.666463 | 99.5101 | 44.1068 | 149.573 | 91.39862 | 6508.469 |
| 13521.8 | 31.4684 | 0.92363 | 103.73 | 0.802754 | 84.1478 | 0.472415 | 183.998 | 23.1933 | 0.759499 | 452.889 | 52.3368 | 0.818449 | 17.1609 | 82.4255 | 250.429 | 47.94566 | 4602.029 |
| 21896 | 28.0092 | 0.862669 | 169.928 | 2.96388 | 2.36482 | 0.500643 | 312.262 | 54.7406 | 0.827743 | 56.0943 | 44.7153 | 0.854194 | 39.0647 | 70.2878 | 46.8385 | 49.31594 | 3309.524 |
| 21877.5 | 25.1875 | 0.862801 | 148.952 | 0.168191 | 30.5703 | 0.651675 | 119.998 | 66.4924 | 0.864843 | 411.836 | 38.2054 | 0.675025 | 7.58913 | 82.3762 | 172.18 | 59.04039 | 4075.254 |
| 29434.1 | 30.6924 | 0.807801 | 133.984 | 1.84314 | 51.3614 | 0.341722 | 184.601 | 58.8097 | 0.875967 | 394.398 | 77.0414 | 0.707289 | 57.4187 | 43.8428 | 382.137 | 94.61884 | 6882.343 |
| 17527.7 | 26.7483 | 0.894465 | 137.909 | 2.97639 | 8.43269 | 0.371761 | 472.396 | 54.4288 | 0.705592 | 228.503 | 85.6779 | 0.541397 | 143.167 | 460.717 | 209.419 | 99.32298 | 6936.669 |
| 23429.3 | 33.1969 | 0.851514 | 133.069 | 1.2573 | 10.8583 | 0.498234 | 304.533 | 4.64903 | 0.733397 | 299.473 | 13.2618 | 0.878682 | 1.74336 | 297 | 248.747 | 46.41473 | 3271.604 |
| 18970.7 | 28.2214 | 0.883963 | 133.321 | 0.684182 | 18.8067 | 0.637362 | 407.3 | 97.0582 | 0.725949 | 332.033 | 25.5356 | 0.925596 | 51.4362 | 115.829 | 276.408 | 45.91776 | 3211.006 |
| 29143.6 | 14.6939 | 0.809904 | 118.23 | 2.44043 | 86.7811 | 0.582656 | 458.893 | 1.7076 | 0.94197 | 356.304 | 25.9314 | 0.830018 | 143.671 | 217.481 | 278.463 | 41.44299 | 3199.62 |
| 15546.1 | 34.2903 | 0.908899 | 107.48 | 0.720073 | 29.4677 | 0.485183 | 266.326 | 27.8581 | 0.590489 | 112.841 | 2.85123 | 0.949826 | 41.5636 | 157.449 | 106.01 | 46.91884 | 3856.505 |
| 26146.1 | 18.3865 | 0.831725 | 134.286 | 3.38087 | 4.50947 | 0.433023 | 160.607 | 35.914 | 0.993361 | 121.72 | 36.1023 | 0.9326 | 104.653 | 113.917 | 81.8054 | 43.11175 | 2856.349 |
| 11816.4 | 29.1192 | 0.936042 | 35.0002 | 1.00739 | 4.7742 | 0.396257 | 437.685 | 80.6237 | 0.843957 | 480.429 | 93.2103 | 0.577542 | 17.2376 | 393.068 | 244.77 | 65.44489 | 4747.137 |
| 23470.9 | 27.8324 | 0.851205 | 168.813 | 2.23058 | 39.9031 | 0.548811 | 158.861 | 54.5531 | 0.629839 | 333.339 | 52.7117 | 0.70909 | 29.0526 | 45.4368 | 276.328 | 78.23251 | 5547.817 |
| 14471.2 | 14.0712 | 0.916704 | 171.76 | 1.72981 | 29.5752 | 0.511826 | 154.544 | 47.5705 | 0.775731 | 387.464 | 51.7648 | 0.474101 | 130.911 | 58.3867 | 255.238 | 88.09027 | 6711.796 |
| 29002 | 30.0846 | 0.810945 | 36.4813 | 0.8397 | 68.4583 | 0.426012 | 112.747 | 85.6931 | 0.815534 | 139.492 | 59.2905 | 0.550312 | 77.1158 | 84.762 | 92.1147 | 97.25136 | 7331.597 |
| 16625.6 | 14.4956 | 0.901023 | 44.4545 | 1.2612 | 10.1463 | 0.467382 | 326.266 | 35.8775 | 0.683755 | 458.167 | 57.2394 | 0.663307 | 37.792 | 101.98 | 317.956 | 57.36147 | 4176.107 |
| 23939.5 | 33.0086 | 0.8478 | 98.3882 | 1.96502 | 29.3298 | 0.508143 | 148.344 | 30.9378 | 0.982224 | 309.517 | 17.6038 | 0.411391 | 133.074 | 65.9505 | 216.557 | 78.32841 | 5428.983 |
| 24013.6 | 20.3893 | 0.847249 | 56.4511 | 2.89502 | 51.8391 | 0.540274 | 260.616 | 12.3222 | 0.99483 | 301.322 | 59.1181 | 0.752672 | 276.213 | 232.944 | 226.193 | 42.65169 | 3178.704 |
| 15284.3 | 17.4388 | 0.910787 | 68.0011 | 1.67034 | 11.0308 | 0.371798 | 320.433 | 53.3631 | 0.789079 | 167.912 | 10.8218 | 0.826525 | 106.427 | 283.443 | 160.846 | 47.18836 | 3633.018 |
| 19047.2 | 22.3873 | 0.883401 | 40.2665 | 1.09733 | 40.9175 | 0.434549 | 95.9971 | 55.337 | 0.821046 | 347.299 | 29.5987 | 0.455836 | 90.9584 | 53.6504 | 177.141 | 85.93998 | 6704.478 |
| 12002.5 | 24.5734 | 0.934682 | 111.067 | 1.89976 | 62.8403 | 0.395446 | 409.53 | 26.4432 | 0.58733 | 464.403 | 53.3904 | 0.856897 | 16.3669 | 188.917 | 228.704 | 62.7074 | 5997.313 |
| 18288.9 | 31.2398 | 0.888929 | 44.8491 | 3.29897 | 14.4891 | 0.49117 | 335.011 | 82.6981 | 0.788836 | 155.986 | 87.1997 | 0.893629 | 45.785 | 105.883 | 112.713 | 45.39312 | 3171.551 |
| 29049.8 | 25.2606 | 0.810593 | 33.836 | 0.764616 | 24.1603 | 0.30848 | 450.135 | 78.2962 | 0.873392 | 142.246 | 6.80857 | 0.985989 | 23.5267 | 282.326 | 76.2156 | 67.29709 | 4680.431 |
| 18237.7 | 32.419 | 0.889304 | 48.7642 | 2.72026 | 66.6272 | 0.354015 | 334.447 | 83.1559 | 0.586207 | 236.564 | 88.1718 | 0.808723 | 104.627 | 106.831 | 146.366 | 90.8694 | 7853.536 |
| 30204.9 | 28.6057 | 0.802188 | 150.723 | 1.41776 | 96.8624 | 0.430643 | 297.289 | 50.7089 | 0.963417 | 436.367 | 11.6755 | 0.654222 | 133.089 | 126.695 | 110.324 | 81.77514 | 6466.975 |
| 14243.3 | 31.4453 | 0.918379 | 92.9076 | 0.117981 | 45.9956 | 0.391901 | 347.169 | 53.1709 | 0.490546 | 224.305 | 52.1817 | 0.956352 | 5.03499 | 196.655 | 143.617 | 83.99793 | 7045.957 |
| 13696.9 | 22.9746 | 0.922347 | 55.8828 | 0.223206 | 29.8325 | 0.456134 | 449.613 | 44.6753 | 0.991097 | 361.518 | 74.248 | 0.658047 | 15.5266 | 258.682 | 218.802 | 46.05745 | 3690.463 |
| 21630 | 21.7682 | 0.8646 | 137.699 | 2.37419 | 16.489 | 0.304598 | 208.172 | 71.2 | 0.904292 | 263.906 | 69.5279 | 0.795867 | 127.158 | 139.159 | 162.013 | 74.927 | 5237.987 |
| 24188.8 | 19.732 | 0.845973 | 124.283 | 2.99249 | 59.2579 | 0.42104 | 233.52 | 84.5303 | 0.944127 | 213.025 | 21.169 | 0.763146 | 115.881 | 160.255 | 139.274 | 56.20304 | 4430.985 |
| 23905 | 22.517 | 0.84804 | 70.6025 | 1.83877 | 71.5303 | 0.373334 | 132.24 | 25.3416 | 0.982527 | 508.736 | 19.3337 | 0.669087 | 56.5284 | 75.326 | 219.741 | 61.57584 | 5364.733 |
| 21609 | 16.2196 | 0.864749 | 50.4544 | 0.185201 | 32.5024 | 0.440691 | 421.787 | 62.0532 | 0.670302 | 110.227 | 36.7444 | 0.897097 | 17.7826 | 194.253 | 48.697 | 55.61917 | 4191.896 |
| 13942.4 | 25.2186 | 0.920562 | 83.7443 | 0.484292 | 83.3875 | 0.435887 | 204.126 | 90.6598 | 0.566723 | 292.039 | 59.9184 | 0.765139 | 21.3468 | 147.902 | 284.466 | 80.58145 | 7391.912 |
| 11900.6 | 24.3745 | 0.935423 | 76.5105 | 1.61449 | 34.373 | 0.430664 | 464.39 | 10.9943 | 0.538237 | 176.875 | 60.4892 | 0.763389 | 99.4731 | 422.248 | 90.9511 | 61.87517 | 5378.046 |
| 24759.9 | 23.6073 | 0.841819 | 116.269 | 0.871596 | 66.746 | 0.412538 | 414.17 | 10.5107 | 0.75155 | 220.624 | 31.614 | 0.603663 | 34.0981 | 211.515 | 73.4876 | 90.77194 | 7328.214 |
| 12292.2 | 13.6815 | 0.932565 | 83.7962 | 2.26075 | 65.3703 | 0.38329 | 212.019 | 53.229 | 0.554992 | 423.854 | 57.413 | 0.795625 | 158.481 | 50.5473 | 300.798 | 74.18102 | 7012.572 |
| 14029.7 | 24.9482 | 0.919926 | 64.8436 | 0.646779 | 52.4278 | 0.600224 | 394.787 | 93.7256 | 0.91508 | 455.216 | 55.1719 | 0.85556 | 57.4371 | 223.558 | 259.728 | 45.83807 | 3466.812 |
| 11320.5 | 28.9216 | 0.939651 | 119.135 | 0.730806 | 17.5069 | 0.554416 | 384.788 | 90.99 | 0.888842 | 351.976 | 75.9605 | 0.56609 | 63.0675 | 85.2789 | 327.137 | 57.5529 | 4254.636 |
| 13565.7 | 17.0394 | 0.923297 | 55.8683 | 0.378019 | 5.19043 | 0.358327 | 283.532 | 99.7064 | 0.809626 | 69.4778 | 94.8473 | 0.584221 | 7.01323 | 164.036 | 51.3818 | 78.55476 | 5541.065 |
| 9636.26 | 29.1578 | 0.951911 | 100.75 | 0.30046 | 26.9968 | 0.551137 | 429.61 | 4.02135 | 0.603156 | 362.606 | 41.6943 | 0.865814 | 21.9659 | 49.5772 | 223.332 | 40.31853 | 3528.366 |
| 22231.5 | 28.467 | 0.860227 | 44.1766 | 1.35399 | 8.23459 | 0.388163 | 192.588 | 37.4108 | 0.902472 | 221.87 | 7.06609 | 0.732193 | 35.5719 | 69.0673 | 203.161 | 51.22862 | 3590.182 |
| 12285.5 | 29.6862 | 0.932627 | 148.099 | 3.57362 | 77.1026 | 0.521932 | 316.387 | 50.524 | 0.992044 | 457.985 | 66.0691 | 0.770773 | 93.409 | 227.403 | 269.098 | 37.75524 | 3350.698 |
| 27880.4 | 30.4513 | 0.81911 | 105.307 | 3.34713 | 30.2844 | 0.450052 | 413.212 | 28.3695 | 0.862218 | 179.998 | 29.923 | 0.935159 | 134.345 | 226.446 | 160.51 | 41.41249 | 3008.254 |
| 21059.2 | 26.3633 | 0.868759 | 77.1942 | 2.73896 | 88.3862 | 0.501432 | 104.011 | 15.5634 | 0.652402 | 347.441 | 30.1217 | 0.731606 | 212.378 | 80.0384 | 203.264 | 61.88085 | 5193.697 |
| 23771.3 | 25.4201 | 0.849016 | 145.172 | 3.143 | 69.5147 | 0.588812 | 395.961 | 66.8244 | 0.726406 | 332.032 | 87.6146 | 0.8524 | 285.94 | 316.211 | 172.344 | 60.95807 | 4331.912 |
| 10423.4 | 24.3612 | 0.946176 | 133.336 | 0.604976 | 22.1654 | 0.57707 | 139.407 | 76.2904 | 0.559074 | 468.487 | 47.7951 | 0.94717 | 53.214 | 99.2753 | 310.065 | 47.26916 | 3774.698 |
| 29451 | 23.4092 | 0.807671 | 138.826 | 0.200892 | 47.2957 | 0.346467 | 100.259 | 3.83456 | 0.884239 | 434.878 | 41.7315 | 0.809207 | 2.34732 | 41.3053 | 292.582 | 93.03207 | 6631.632 |
| 15543.6 | 17.7128 | 0.9089 | 124.258 | 1.58588 | 46.4222 | 0.446377 | 387.699 | 99.4976 | 0.802744 | 452.702 | 40.2187 | 0.727109 | 87.3839 | 369.28 | 190.619 | 60.22449 | 4856.014 |
| 21519.5 | 33.2328 | 0.865416 | 76.2445 | 1.62291 | 38.521 | 0.452113 | 375.017 | 2.35417 | 0.676588 | 428.687 | 85.5082 | 0.738795 | 109.596 | 321.998 | 408.253 | 61.45128 | 4735.28 |
| 28908.6 | 27.8666 | 0.811623 | 64.0065 | 2.0862 | 7.87567 | 0.553512 | 445.565 | 4.49433 | 0.674763 | 428.586 | 6.81711 | 0.675601 | 70.8829 | 270.131 | 386.265 | 75.15946 | 4777.78 |
| 25555.8 | 28.7709 | 0.836029 | 168.172 | 2.42534 | 47.5541 | 0.40147 | 472.858 | 73.9328 | 0.966707 | 515.867 | 19.5236 | 0.617399 | 124.632 | 365.414 | 397.375 | 85.367 | 6210.764 |
| 10330.4 | 22.0615 | 0.946851 | 127.777 | 2.01257 | 99.1304 | 0.650694 | 458.85 | 63.1885 | 0.898916 | 498.982 | 6.53921 | 0.76691 | 186.88 | 374.9 | 260.748 | 41.999 | 3713.055 |
| 23004.9 | 28.1549 | 0.854597 | 50.9961 | 0.255693 | 88.6149 | 0.399552 | 118.593 | 88.9661 | 0.783352 | 237.143 | 58.3967 | 0.951405 | 22.4173 | 80.1849 | 114.814 | 59.55886 | 5150.292 |
| 15045.8 | 15.5335 | 0.912523 | 77.2764 | 1.31084 | 96.5584 | 0.369409 | 294.049 | 44.0851 | 0.714276 | 418.143 | 60.7836 | 0.766755 | 39.6792 | 179.293 | 238.966 | 70.60197 | 7091.316 |
| 28186.5 | 34.0346 | 0.816886 | 164.224 | 0.343573 | 11.1667 | 0.455963 | 230.55 | 41.1703 | 0.584178 | 327.939 | 70.5681 | 0.939052 | 27.3281 | 161.907 | 304.054 | 95.55442 | 6028.239 |
| 26901.3 | 22.1851 | 0.82623 | 37.5958 | 1.3342 | 13.6804 | 0.514486 | 396.7 | 11.1384 | 0.766371 | 256.692 | 1.46819 | 0.754501 | 23.8177 | 372.509 | 226.957 | 50.22088 | 3412.336 |
| 18412.4 | 34.7217 | 0.888035 | 156.045 | 2.90496 | 33.1304 | 0.511738 | 296.485 | 76.304 | 0.952531 | 384.745 | 10.7288 | 0.731471 | 14.7103 | 253.534 | 298.72 | 46.36046 | 3526.652 |
| 22394.6 | 17.1291 | 0.859031 | 102.678 | 0.828021 | 24.7177 | 0.631277 | 428.828 | 63.8882 | 0.8195 | 412.118 | 54.3348 | 0.58807 | 16.2554 | 411.05 | 339.126 | 85.54918 | 5663.669 |
| 24321.6 | 25.5456 | 0.84501 | 155.222 | 0.428129 | 16.5019 | 0.413462 | 429.783 | 48.0855 | 0.929222 | 445.851 | 47.8857 | 0.560272 | 3.97444 | 349.101 | 82.4511 | 98.6059 | 6550.647 |
| 20984.5 | 27.3367 | 0.869304 | 64.4474 | 2.41769 | 14.2054 | 0.502537 | 135.454 | 29.7634 | 0.827894 | 349.707 | 45.8146 | 0.68108 | 188.12 | 127.916 | 347.089 | 50.5839 | 3547.041 |
| 28391.2 | 29.7725 | 0.815391 | 149.072 | 3.79518 | 31.7839 | 0.409222 | 356.149 | 87.0264 | 0.857569 | 393.013 | 40.8444 | 0.859126 | 104.937 | 310.077 | 280.938 | 62.18718 | 4304.5 |
| 21306.3 | 16.7655 | 0.866953 | 100.272 | 2.089 | 42.3834 | 0.401668 | 362.276 | 85.3737 | 0.98803 | 356.408 | 92.8101 | 0.595461 | 92.0009 | 245.238 | 227.42 | 71.17456 | 5318.469 |
| 25238.3 | 19.1917 | 0.838333 | 33.0523 | 2.01493 | 46.556 | 0.393665 | 409.583 | 44.6128 | 0.963095 | 485.872 | 51.2025 | 0.815953 | 3.62762 | 135.609 | 348.673 | 51.1676 | 3977.245 |
| 17959.2 | 33.1496 | 0.891332 | 42.3681 | 0.3457 | 2.49595 | 0.370341 | 54.4482 | 16.3078 | 0.935353 | 107.846 | 6.06052 | 0.565587 | 4.39502 | 40.2469 | 60.4199 | 58.64249 | 4186.874 |
| 10590.7 | 32.3587 | 0.944968 | 77.6986 | 1.50374 | 27.1282 | 0.332222 | 181.087 | 77.9044 | 0.999597 | 254.473 | 51.289 | 0.87987 | 64.7484 | 110.789 | 144.533 | 48.44188 | 4050.98 |
| 23854.9 | 33.4073 | 0.848416 | 164.907 | 2.91914 | 75.8972 | 0.473738 | 325.591 | 8.77276 | 0.579024 | 356.128 | 86.1554 | 0.802585 | 4.45517 | 225.353 | 183.122 | 85.04449 | 6777.013 |
| 28560.4 | 31.1163 | 0.814161 | 46.4316 | 1.30039 | 59.0639 | 0.453374 | 139.566 | 23.302 | 0.642224 | 130.983 | 62.5318 | 0.752698 | 17.4912 | 77.1152 | 57.2759 | 74.77301 | 5686.058 |
| 27362.2 | 18.3503 | 0.822872 | 140.003 | 1.85889 | 65.1569 | 0.540657 | 374.44 | 61.8689 | 0.954635 | 436.618 | 49.0454 | 0.908467 | 13.9516 | 362.111 | 258.216 | 43.56749 | 3249.104 |
| 10198 | 14.1213 | 0.947809 | 143.382 | 1.49082 | 14.5378 | 0.471762 | 245.013 | 99.235 | 0.5384 | 459.844 | 41.4148 | 0.692967 | 17.4933 | 175.137 | 405.956 | 77.6341 | 6022.159 |
| 18762.1 | 18.0497 | 0.885473 | 88.4438 | 1.12601 | 71.4281 | 0.532371 | 252.479 | 86.8986 | 0.937497 | 300.957 | 14.3092 | 0.449128 | 54.2374 | 115.948 | 258.471 | 89.91318 | 6853.835 |
| 30219 | 13.9196 | 0.802076 | 113.846 | 1.43114 | 8.70749 | 0.462256 | 251.771 | 17.5584 | 0.874214 | 394.058 | 40.4061 | 0.437842 | 118.784 | 189.681 | 370.594 | 92.92975 | 5810.061 |
| 25768.9 | 31.3153 | 0.834481 | 126.744 | 2.20729 | 2.29356 | 0.588066 | 326.88 | 47.6314 | 0.518853 | 484.543 | 95.9436 | 0.827383 | 82.3227 | 313.171 | 350.329 | 88.893 | 5517.737 |
| 12407.2 | 18.4509 | 0.931731 | 162.379 | 1.84553 | 71.3242 | 0.414991 | 357.375 | 50.3078 | 0.572225 | 397.348 | 42.0216 | 0.748712 | 115.376 | 100.076 | 205.921 | 87.72182 | 7995.725 |
| 9849.35 | 13.8758 | 0.950347 | 147.353 | 0.5487 | 94.4009 | 0.632495 | 341.616 | 57.8313 | 0.322328 | 256.135 | 2.74594 | 0.904663 | 19.4912 | 246.451 | 115.315 | 79.3506 | 7304.418 |
| 23022.2 | 30.0248 | 0.854474 | 83.3539 | 1.53905 | 30.6527 | 0.528861 | 369.063 | 57.4048 | 0.995484 | 301.385 | 11.4711 | 0.489 | 50.8701 | 177.94 | 187.813 | 71.71436 | 4964.761 |
| 15709.7 | 23.4939 | 0.907695 | 97.8173 | 2.03594 | 6.97508 | 0.481311 | 266.237 | 62.3625 | 0.817671 | 263.16 | 78.6202 | 0.381788 | 60.1552 | 138.749 | 63.8632 | 88.98147 | 6139.952 |
| 17234.4 | 34.7513 | 0.89661 | 45.0267 | 1.18512 | 70.561 | 0.486477 | 142.543 | 45.6078 | 0.572392 | 508.332 | 50.5499 | 0.751474 | 98.0117 | 79.3668 | 384.669 | 64.71888 | 5391.922 |
| 27383.2 | 30.4075 | 0.822729 | 49.9818 | 1.36329 | 99.4935 | 0.467475 | 134.43 | 35.3129 | 0.79363 | 438.089 | 21.6328 | 0.837947 | 117.512 | 65.3793 | 67.9547 | 52.69014 | 4523.508 |
| 25303.6 | 29.0758 | 0.837865 | 96.6133 | 1.77442 | 21.5665 | 0.519755 | 451.078 | 97.0126 | 0.53491 | 418.648 | 69.8691 | 0.777596 | 154.126 | 345.295 | 144.419 | 89.23917 | 5807.933 |
| 17990.1 | 34.8004 | 0.891109 | 52.4209 | 2.69927 | 2.45838 | 0.400916 | 87.1823 | 38.383 | 0.731154 | 110.607 | 47.8037 | 0.502507 | 85.9412 | 73.8829 | 79.1103 | 84.3985 | 5789.991 |
| 27711.4 | 28.2002 | 0.820338 | 71.2643 | 1.97091 | 68.5944 | 0.516673 | 495.679 | 57.4893 | 0.719597 | 185.198 | 83.0931 | 0.658036 | 137.236 | 341.859 | 142.492 | 81.49967 | 5799.258 |
| 14697.7 | 19.8422 | 0.915059 | 21.9558 | 1.35077 | 82.5856 | 0.346467 | 494.21 | 99.0351 | 0.863541 | 181.108 | 94.5283 | 0.631029 | 121.944 | 297.364 | 81.3227 | 83.86473 | 7696.062 |
| 21798.6 | 16.9701 | 0.863369 | 98.3492 | 0.499412 | 65.0021 | 0.336779 | 240.007 | 36.1455 | 0.849955 | 236.715 | 49.1774 | 0.873127 | 6.87679 | 80.8233 | 75.5873 | 67.51814 | 5708.609 |
| 13861.6 | 31.2843 | 0.921157 | 96.3256 | 1.56753 | 74.5631 | 0.479549 | 374.936 | 8.94915 | 0.974162 | 511.985 | 47.049 | 0.610301 | 125.111 | 154.845 | 139.675 | 42.8409 | 4019.894 |
| 13132.1 | 27.8262 | 0.926463 | 169.751 | 0.429085 | 38.2239 | 0.657085 | 430.882 | 88.3207 | 0.685079 | 519.806 | 83.9456 | 0.67546 | 7.42834 | 328.494 | 70.2489 | 67.71234 | 5053.536 |
| 24910.5 | 22.6552 | 0.840721 | 86.4011 | 1.41589 | 77.3282 | 0.448988 | 357.006 | 65.1099 | 0.844558 | 359.081 | 15.5303 | 0.939493 | 74.6028 | 347.062 | 161.091 | 44.57588 | 3774.402 |
| 12816.2 | 20.6935 | 0.928755 | 156.668 | 1.91217 | 7.66458 | 0.470756 | 287.125 | 85.563 | 0.451025 | 481.757 | 38.7419 | 0.902312 | 163.448 | 204.935 | 120.638 | 73.6696 | 5473.148 |
| 14076.3 | 20.9865 | 0.919583 | 25.3805 | 1.05425 | 72.7217 | 0.419198 | 330.577 | 7.36197 | 0.69672 | 242.051 | 98.4016 | 0.945539 | 3.62906 | 248.889 | 87.5591 | 48.48044 | 4592.347 |
| 21533.6 | 25.5251 | 0.865305 | 87.6918 | 0.866061 | 23.6485 | 0.583742 | 482.8 | 32.8385 | 0.938984 | 430.638 | 75.6436 | 0.701015 | 57.302 | 300.001 | 196.386 | 52.12653 | 3596.417 |
| 25270.8 | 33.1954 | 0.838109 | 157.863 | 1.88512 | 8.47466 | 0.461958 | 293.937 | 25.5253 | 0.763912 | 378.229 | 96.1972 | 0.966743 | 93.5362 | 212.529 | 281.647 | 56.1046 | 3690.21 |
| 20599.2 | 26.7158 | 0.872107 | 121.364 | 0.825018 | 50.4089 | 0.705742 | 193.524 | 13.587 | 0.895722 | 363.088 | 12.0712 | 0.765803 | 44.4658 | 184.037 | 341.46 | 42.57932 | 3205.071 |
| 18796.4 | 13.758 | 0.885221 | 39.7404 | 0.602549 | 1.26423 | 0.475935 | 274.821 | 77.5432 | 0.87999 | 182.639 | 54.5537 | 0.535923 | 40.6086 | 77.8449 | 129.887 | 63.41637 | 4217.292 |
| 16505.9 | 29.8128 | 0.901906 | 68.5518 | 1.61829 | 17.6008 | 0.440534 | 427.021 | 4.51117 | 0.975444 | 63.3073 | 56.4762 | 0.89268 | 45.2081 | 193.619 | 46.293 | 32.08243 | 2559.869 |
| 12029.1 | 32.9544 | 0.934498 | 84.2004 | 0.628796 | 139.514 | 0.538553 | 318.941 | 302.373 | 0.764299 | 205.177 | 66.1177 | 0.733349 | 57.672 | 269.084 | 150.686 | 84.88612 | 6719.506 |
| 15090.6 | 31.5933 | 0.912211 | 103.323 | 0.945278 | 38.0146 | 0.422543 | 201.545 | 285.33 | 0.970933 | 368.601 | 313.847 | 0.973921 | 4.38789 | 51.8308 | 300.435 | 91.85862 | 5979.73 |
| 15219.3 | 29.1133 | 0.911271 | 92.9621 | 1.5462 | 95.9021 | 0.446349 | 313.157 | 370.134 | 0.988961 | 114.134 | 262.865 | 0.894223 | 82.6834 | 191.407 | 102.979 | 89.1354 | 6297.391 |
| 26408 | 33.5174 | 0.829832 | 149.775 | 3.32975 | 174.543 | 0.542251 | 439.213 | 47.5172 | 0.952067 | 158.139 | 438.775 | 0.851781 | 59.1755 | 199.772 | 130.054 | 77.78568 | 5729.155 |
| 42362.2 | 30.834 | 0.713695 | 30.872 | 1.58665 | 11.3232 | 0.57463 | 259.569 | 219.781 | 0.752802 | 420.724 | 282.556 | 0.979513 | 127.322 | 192.255 | 169.795 | 99.82564 | 5460.139 |

Table B3. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 130.01.

| X1 | X2 | X3 | X4 | X5 | X6 | X7 | X8 | X9 | X10 | X11 | X12 | X13 | X14 | X15 | X16 | UED | UPC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 12018.2 | 25 | 0.95 | 100 | 1.1 | 0.4 | 0.482 | 110 | 0.6 | 0.895 | 130 | 30.9048 | 0.939426 | 100 | 100 | 100 | 26.35906 | 2182.015 |
| 50239.8 | 22.719 | 0.737455 | 47.5805 | 1.90224 | 28.4573 | 0.386536 | 242.014 | 20.1008 | 0.612276 | 373.92 | 24.9877 | 0.566169 | 104.496 | 210.307 | 319.394 | 161.7398 | 9572.361 |
| 42915.7 | 25.085 | 0.778184 | 155.369 | 1.37459 | 78.8287 | 0.258873 | 320.681 | 85.7076 | 0.982801 | 121.294 | 69.835 | 0.676153 | 44.2386 | 277.423 | 117.521 | 170.3231 | 11943.11 |
| 55078.5 | 19.2925 | 0.710546 | 109.644 | 1.5108 | 58.9027 | 0.383965 | 493.331 | 36.6614 | 0.305828 | 206.55 | 61.9703 | 0.941398 | 111.187 | 166.4 | 201.506 | 229.8262 | 14316.73 |
| 35388.4 | 23.2917 | 0.820041 | 136.598 | 0.220522 | 50.2781 | 0.653366 | 418.476 | 34.869 | 0.90443 | 136.001 | 36.8791 | 0.462072 | 8.35842 | 161.572 | 50.6812 | 95.80218 | 6115.854 |
| 50306.5 | 27.5809 | 0.737087 | 115.914 | 3.53456 | 30.9859 | 0.499135 | 389.507 | 83.7745 | 0.948165 | 291.671 | 21.161 | 0.515555 | 57.253 | 336.584 | 248.58 | 99.60402 | 5753.711 |
| 39936.9 | 25.5301 | 0.794749 | 28.2072 | 1.25156 | 99.8277 | 0.362869 | 184.61 | 80.7468 | 0.871322 | 367.711 | 95.5424 | 0.381511 | 89.4423 | 134.457 | 76.7328 | 193.766 | 14758.72 |
| 46189.8 | 25.685 | 0.759978 | 162.658 | 0.484342 | 59.6763 | 0.551358 | 291.382 | 69.7965 | 0.618716 | 377.156 | 33.9222 | 0.927436 | 23.7432 | 268.675 | 201.835 | 102.2841 | 6270.698 |
| 41749.4 | 14.5345 | 0.784664 | 90.4875 | 2.20383 | 83.7006 | 0.423068 | 216.707 | 41.1869 | 0.782578 | 234.03 | 48.5641 | 0.331575 | 52.6574 | 163.315 | 83.2807 | 195.1018 | 14097.69 |
| 45553.7 | 31.5703 | 0.763521 | 99.4934 | 1.26213 | 64.668 | 0.365303 | 363.961 | 51.326 | 0.879139 | 347.489 | 39.2032 | 0.657624 | 85.6401 | 292.092 | 144.392 | 112.801 | 7684.052 |
| 14537.1 | 34.6184 | 0.936005 | 157.037 | 1.87551 | 80.5558 | 0.40027 | 323.059 | 41.8003 | 0.441605 | 507.564 | 79.1583 | 0.752765 | 26.9644 | 178.395 | 368.519 | 130.4585 | 11753.53 |
| 34241.6 | 20.3881 | 0.826416 | 79.4512 | 1.24536 | 13.8574 | 0.368219 | 205.591 | 6.82467 | 0.728987 | 435.888 | 47.2624 | 0.934274 | 36.1717 | 136.104 | 76.1568 | 67.0978 | 4337.953 |
| 53102.5 | 27.7163 | 0.721539 | 150.182 | 2.0043 | 63.2711 | 0.338311 | 398.682 | 70.4339 | 0.916123 | 130.792 | 73.2044 | 0.945071 | 149.767 | 240.951 | 54.4517 | 119.3186 | 7522.201 |
| 30315.3 | 24.1728 | 0.848252 | 159.836 | 0.941021 | 38.2341 | 0.40316 | 235.704 | 88.2174 | 0.82067 | 315.987 | 90.2991 | 0.853888 | 76.5737 | 133.344 | 265.192 | 90.70796 | 6096.805 |
| 11805.5 | 23.6224 | 0.951181 | 140.277 | 1.30745 | 14.6936 | 0.317597 | 351.405 | 21.5401 | 0.571883 | 442.977 | 49.7968 | 0.401182 | 14.2353 | 266.009 | 116.95 | 188.8373 | 14809.34 |
| 11887.1 | 27.1006 | 0.950731 | 156.153 | 1.41436 | 54.3215 | 0.240213 | 416.48 | 22.1184 | 0.872808 | 352.09 | 97.1609 | 0.437619 | 72.9749 | 71.0442 | 206.734 | 179.4408 | 16122.92 |
| 18010.2 | 18.6042 | 0.916674 | 126.713 | 1.70359 | 73.254 | 0.335046 | 328.384 | 0.97121 | 0.583938 | 327.232 | 18.5344 | 0.462685 | 115.872 | 290.483 | 318.955 | 172.935 | 15649.27 |
| 34074 | 29.8337 | 0.827356 | 135.112 | 0.62292 | 57.973 | 0.553131 | 263.157 | 59.1365 | 0.55524 | 326.996 | 62.5581 | 0.612487 | 28.9304 | 120.223 | 224.379 | 128.6325 | 8584.814 |
| 44952.2 | 29.4587 | 0.766864 | 79.1579 | 1.49711 | 27.9037 | 0.561073 | 334.619 | 8.42046 | 0.985217 | 480.578 | 23.5664 | 0.995348 | 104.228 | 184.923 | 190.16 | 45.77615 | 2826.725 |
| 18078.6 | 27.5919 | 0.916302 | 153.035 | 2.80894 | 50.931 | 0.538998 | 274.092 | 18.3027 | 0.941058 | 330.969 | 93.3603 | 0.99611 | 137.427 | 88.8225 | 177.039 | 39.03883 | 3079.986 |
| 43434.2 | 22.4765 | 0.7753 | 96.4633 | 2.5583 | 27.8892 | 0.301927 | 409.035 | 69.1018 | 0.892553 | 378.926 | 2.03267 | 0.981443 | 160.446 | 359.868 | 115.416 | 85.84423 | 5455.556 |
| 35773.3 | 15.5143 | 0.817896 | 149.706 | 0.417459 | 5.09697 | 0.690686 | 390.902 | 32.6072 | 0.909138 | 475.755 | 85.2483 | 0.533323 | 36.4732 | 265.727 | 468.713 | 84.92021 | 5018.67 |
| 13320.2 | 32.9677 | 0.94277 | 47.5997 | 0.649727 | 97.0781 | 0.470028 | 337.38 | 5.77646 | 0.70965 | 168.898 | 84.934 | 0.741437 | 16.4609 | 159.27 | 128.7 | 56.27481 | 5512.375 |
| 23791.2 | 32.4613 | 0.88454 | 77.227 | 3.34471 | 44.7229 | 0.35391 | 454.097 | 57.2334 | 0.981995 | 270.198 | 56.447 | 0.38745 | 28.9242 | 331.369 | 154.808 | 125.2509 | 9516.303 |
| 27709.9 | 21.0098 | 0.862738 | 135.347 | 2.30358 | 92.0771 | 0.48784 | 156.701 | 66.9694 | 0.522139 | 336.791 | 65.8472 | 0.712454 | 56.4727 | 81.2369 | 250.239 | 110.4512 | 8708.328 |
| 14850.9 | 33.2643 | 0.934258 | 37.9661 | 0.674003 | 73.8788 | 0.495761 | 401.188 | 95.205 | 0.744167 | 459.913 | 76.4879 | 0.793726 | 14.4022 | 85.4586 | 237.957 | 57.84599 | 4756.685 |
| 26298.6 | 14.7002 | 0.870582 | 110.222 | 1.87586 | 55.4653 | 0.275331 | 483.598 | 36.2647 | 0.855729 | 310.928 | 64.34 | 0.672744 | 45.741 | 341.27 | 77.4369 | 110.4199 | 8803.582 |
| 24873.9 | 14.8417 | 0.878504 | 105.774 | 2.68598 | 72.8225 | 0.432895 | 468.8 | 67.1606 | 0.776228 | 470.463 | 68.4555 | 0.629045 | 90.2484 | 254.819 | 52.8548 | 83.46238 | 6682.555 |
| 16265.3 | 29.5985 | 0.926388 | 155.286 | 2.48233 | 92.7167 | 0.268975 | 350.019 | 42.9979 | 0.901207 | 126.974 | 32.8353 | 0.813073 | 53.6541 | 233.811 | 113.448 | 92.95778 | 8997.929 |
| 22038.6 | 16.7166 | 0.894272 | 83.1936 | 0.38825 | 27.786 | 0.417264 | 296.607 | 18.7485 | 0.210656 | 233.129 | 98.7816 | 0.799231 | 30.5496 | 50.0363 | 139.004 | 223.5697 | 16133.04 |
| 37072.1 | 17.6041 | 0.810675 | 102.407 | 3.05877 | 0.391138 | 0.429628 | 414.244 | 8.63762 | 0.184743 | 352.914 | 61.3741 | 0.887551 | 85.6086 | 345.298 | 137.208 | 244.3953 | 13966.31 |
| 16130.8 | 20.8921 | 0.927127 | 85.8368 | 1.92238 | 82.2188 | 0.229506 | 103.927 | 26.3534 | 0.595931 | 127.127 | 59.2198 | 0.665546 | 120.083 | 83.0873 | 47.7853 | 162.0028 | 16075.88 |
| 22056.9 | 25.3792 | 0.894177 | 90.1911 | 1.06856 | 43.2238 | 0.292184 | 334.695 | 73.4875 | 0.241583 | 108.586 | 91.7404 | 0.903828 | 42.4263 | 153.228 | 49.9512 | 245.2151 | 19248.85 |
| 11143.8 | 31.5454 | 0.95487 | 156.792 | 1.67911 | 95.4297 | 0.558241 | 136.019 | 92.1018 | 0.78327 | 113.16 | 34.5593 | 0.423091 | 156.341 | 95.5862 | 109.536 | 98.30719 | 8555.381 |
| 32192.3 | 20.0923 | 0.837812 | 169.028 | 0.768075 | 71.8955 | 0.598824 | 292.055 | 25.3295 | 0.544077 | 205.237 | 26.7542 | 0.449882 | 56.3853 | 99.4947 | 168.427 | 172.3516 | 11718.52 |
| 32344.8 | 27.7251 | 0.83697 | 61.816 | 2.04251 | 64.5387 | 0.186233 | 400.108 | 36.3434 | 0.911416 | 500.388 | 34.867 | 0.923577 | 51.2746 | 102.798 | 309.859 | 155.2862 | 12444.43 |
| 42616.5 | 32.4344 | 0.779855 | 45.6751 | 3.50928 | 76.915 | 0.219738 | 332.867 | 1.0834 | 0.583461 | 59.2131 | 57.2838 | 0.884637 | 79.6677 | 110.704 | 50.7096 | 192.6623 | 14639.63 |
| 19616.6 | 22.1162 | 0.907744 | 29.3666 | 1.34684 | 68.9778 | 0.485494 | 352.388 | 64.8399 | 0.598191 | 364.813 | 10.4618 | 0.311757 | 35.002 | 93.2526 | 118.776 | 174.17 | 13727.04 |
| 53804.5 | 21.844 | 0.717632 | 80.5153 | 2.72379 | 45.7186 | 0.42226 | 320.462 | 88.4154 | 0.608251 | 383.996 | 18.2069 | 0.821654 | 161.749 | 135.289 | 311.585 | 114.2613 | 6955.155 |
| 20281.4 | 18.8794 | 0.904045 | 166.902 | 0.396406 | 94.497 | 0.605877 | 373.546 | 53.569 | 0.618547 | 386.153 | 25.0568 | 0.364516 | 14.7419 | 80.727 | 215.506 | 168.8909 | 13063.32 |
| 24193.1 | 31.9792 | 0.882305 | 129.373 | 1.36061 | 79.7886 | 0.236003 | 232.03 | 80.0116 | 0.76481 | 180.654 | 87.0476 | 0.750577 | 87.4785 | 137.301 | 68.8429 | 151.1999 | 12792.85 |
| 15658.4 | 15.8068 | 0.92975 | 159.01 | 1.69102 | 85.2435 | 0.473823 | 172.387 | 0.043322 | 0.772121 | 173.076 | 99.084 | 0.260755 | 72.6358 | 168.825 | 75.3555 | 181.4275 | 15937.51 |
| 31386.7 | 21.0975 | 0.842292 | 77.8001 | 2.81703 | 49.3352 | 0.451983 | 466.503 | 86.437 | 0.230019 | 238.96 | 82.3985 | 0.946614 | 164.615 | 317.094 | 50.3116 | 179.7329 | 12602.79 |
| 35765.9 | 22.0779 | 0.817941 | 140.81 | 0.849903 | 36.6036 | 0.594292 | 366.273 | 19.2409 | 0.822345 | 363.732 | 37.9538 | 0.689009 | 26.4496 | 315.042 | 56.2955 | 67.13997 | 4346.039 |
| 39857.3 | 29.3884 | 0.795195 | 81.8624 | 1.78472 | 65.9357 | 0.427816 | 499.757 | 7.34745 | 0.4339 | 329.171 | 73.2751 | 0.99519 | 21.5151 | 203.59 | 161.445 | 111.1383 | 7899.521 |
| 47106.1 | 15.5926 | 0.754878 | 62.7607 | 0.627959 | 67.6044 | 0.157253 | 315.395 | 93.893 | 0.723193 | 304.755 | 84.2609 | 0.899012 | 38.0577 | 280.199 | 247.322 | 249.8274 | 18002.59 |
| 29403.7 | 20.7509 | 0.853319 | 168.616 | 2.31561 | 51.2245 | 0.517542 | 296.357 | 82.3338 | 0.41117 | 417.093 | 28.8391 | 0.433337 | 143.839 | 101.887 | 200.564 | 239.0452 | 16318.72 |
| 17002.6 | 28.747 | 0.922287 | 158.656 | 1.29549 | 51.3501 | 0.372379 | 259.404 | 81.8563 | 0.42403 | 191.111 | 39.9888 | 0.942356 | 1.97663 | 254.748 | 177.524 | 122.8821 | 9990.114 |
| 36855.7 | 20.4344 | 0.81188 | 112.28 | 0.440655 | 64.1336 | 0.434357 | 313.883 | 90.2119 | 0.777733 | 135.559 | 36.8462 | 0.6435 | 33.4085 | 280.147 | 101.255 | 113.1006 | 7788.276 |
| 47056.2 | 18.524 | 0.755156 | 21.2713 | 2.18643 | 73.3626 | 0.486933 | 474.302 | 98.4252 | 0.908662 | 365.818 | 66.889 | 0.609496 | 119.378 | 78.1886 | 344.789 | 92.35126 | 5909.057 |
| 42654.9 | 18.0298 | 0.77963 | 18.26 | 0.7275 | 15.9012 | 0.352466 | 485.489 | 44.8638 | 0.650177 | 510.656 | 70.0691 | 0.429349 | 8.66265 | 432.957 | 300.023 | 202.8181 | 11953.46 |
| 15833.6 | 33.9416 | 0.928794 | 91.6163 | 3.69819 | 89.9004 | 0.540701 | 462.462 | 33.9797 | 0.715269 | 441.654 | 84.3244 | 0.503108 | 287.011 | 226.565 | 294.604 | 107.5465 | 8850.83 |
| 21797.1 | 18.0231 | 0.895616 | 155.277 | 1.70566 | 49.974 | 0.308968 | 159.809 | 87.189 | 0.789684 | 412.671 | 21.2736 | 0.503218 | 5.32038 | 43.8736 | 328.382 | 161.7594 | 12493.9 |
| 18589.9 | 33.5166 | 0.913466 | 132.291 | 0.758575 | 55.6266 | 0.616956 | 219.564 | 95.1688 | 0.554936 | 463.366 | 24.9325 | 0.759231 | 59.5952 | 103.006 | 290.036 | 76.97871 | 5682.077 |
| 11931.4 | 18.1725 | 0.950477 | 37.9937 | 1.94223 | 21.6178 | 0.46732 | 264.947 | 49.69 | 0.592185 | 448.081 | 63.7309 | 0.512369 | 44.3165 | 131.955 | 148.209 | 86.46613 | 6810.673 |
| 13539 | 22.218 | 0.94154 | 130.358 | 1.39118 | 14.6769 | 0.596432 | 398.226 | 10.0522 | 0.719232 | 283.501 | 2.85277 | 0.400459 | 67.6274 | 145 | 241.5 | 102.42 | 7755.169 |
| 35692.6 | 21.7411 | 0.818348 | 154.512 | 1.35291 | 37.2457 | 0.314559 | 200.67 | 48.0869 | 0.435088 | 430.977 | 9.09754 | 0.877038 | 129.821 | 114.362 | 317.861 | 193.1862 | 12763.63 |
| 17675.8 | 32.3704 | 0.918548 | 60.4757 | 2.14216 | 5.34113 | 0.404548 | 470.653 | 79.6318 | 0.566762 | 477.723 | 29.9566 | 0.44366 | 26.3589 | 256.449 | 216.338 | 133.8339 | 9251.732 |
| 34858 | 32.1074 | 0.822999 | 82.9289 | 2.20838 | 24.9095 | 0.249733 | 287.357 | 8.92751 | 0.964798 | 82.1756 | 0.773628 | 0.968899 | 137.162 | 231.86 | 43.1206 | 93.31046 | 6330.485 |
| 22360.5 | 25.6887 | 0.892489 | 115.486 | 0.88609 | 52.3916 | 0.439685 | 130.022 | 21.6197 | 0.870393 | 473.356 | 42.4409 | 0.408297 | 73.9174 | 88.6947 | 69.5746 | 110.8327 | 8607.652 |
| 17550.9 | 18.7108 | 0.919228 | 49.2397 | 1.67312 | 40.8795 | 0.481174 | 347.23 | 31.0897 | 0.683033 | 179.83 | 54.7201 | 0.824627 | 52.8165 | 107.112 | 53.7746 | 50.36367 | 3989.726 |
| 24935.4 | 22.0434 | 0.878167 | 59.3527 | 2.47334 | 9.9832 | 0.280192 | 78.4408 | 27.1576 | 0.928197 | 402.181 | 68.6325 | 0.4972 | 69.8885 | 68.1318 | 384.319 | 116.6728 | 7828.396 |
| 16997.8 | 21.3034 | 0.922306 | 85.4103 | 1.22565 | 53.9436 | 0.376394 | 63.7465 | 37.11 | 0.899629 | 223.852 | 51.3269 | 0.846609 | 5.54507 | 47.9074 | 56.0248 | 50.28461 | 4408.16 |
| 21877.8 | 31.7114 | 0.89518 | 34.0441 | 1.88839 | 31.3325 | 0.175021 | 501.641 | 35.7764 | 0.954186 | 402.85 | 35.0923 | 0.794832 | 51.457 | 318.187 | 367.515 | 134.1015 | 10460.68 |
| 25916.5 | 20.2523 | 0.87271 | 114.445 | 2.21771 | 67.0334 | 0.306275 | 195.054 | 34.1049 | 0.790561 | 400.488 | 73.6226 | 0.48037 | 66.4328 | 158.667 | 212.492 | 152.0919 | 12431.04 |
| 16320.5 | 23.0292 | 0.926074 | 132.584 | 1.3257 | 78.1273 | 0.41344 | 422.807 | 64.3729 | 0.823873 | 299.759 | 12.0598 | 0.470299 | 76.9133 | 140.527 | 255.776 | 108.0451 | 9491.465 |
| 18955.1 | 28.5575 | 0.911429 | 29.3356 | 0.375222 | 92.6626 | 0.238277 | 504.145 | 40.7214 | 0.846835 | 261.026 | 63.2186 | 0.761949 | 19.9693 | 132.407 | 219.026 | 106.9618 | 10505.89 |
| 29908.4 | 15.605 | 0.850509 | 137.432 | 1.40995 | 12.706 | 0.174289 | 155.56 | 54.6478 | 0.822513 | 215.072 | 28.2393 | 0.553668 | 103.731 | 62.0092 | 59.2182 | 244.314 | 15670.68 |
| 12472.4 | 14.7183 | 0.947466 | 43.6676 | 1.77273 | 50.8951 | 0.39195 | 395.472 | 69.116 | 0.205819 | 270.572 | 8.1721 | 0.770173 | 11.5097 | 236.963 | 256.854 | 198.5288 | 17875.62 |
| 47146.9 | 25.1413 | 0.754656 | 64.4886 | 3.69392 | 47.0456 | 0.265886 | 289.689 | 10.6703 | 0.971479 | 370.355 | 87.3698 | 0.564891 | 45.6698 | 271.647 | 323.3 | 152.3745 | 10045 |
| 37063.6 | 31.7313 | 0.810733 | 142.888 | 2.7057 | 36.6654 | 0.507392 | 498.665 | 78.9288 | 0.641516 | 518.382 | 70.1307 | 0.41735 | 64.8039 | 65.9273 | 139.714 | 168.2607 | 10557.21 |
| 20870.2 | 30.7109 | 0.900782 | 140.585 | 3.12048 | 7.99107 | 0.144517 | 427.08 | 92.5628 | 0.786691 | 221.19 | 80.267 | 0.848738 | 2.25084 | 100.939 | 104.182 | 224.4768 | 15230.81 |
| 14663.3 | 22.0638 | 0.935288 | 34.3693 | 1.4735 | 27.2236 | 0.362105 | 210.516 | 81.6435 | 0.636504 | 294.994 | 72.053 | 0.441459 | 145.647 | 121.959 | 137.524 | 134.8621 | 10498.74 |
| 34894.9 | 28.9873 | 0.82279 | 146.393 | 3.32737 | 82.6894 | 0.304439 | 256.736 | 8.60901 | 0.800172 | 147.711 | 15.3088 | 0.804833 | 86.791 | 209.006 | 120.786 | 107.4198 | 8575.454 |
| 21882.1 | 34.6754 | 0.89516 | 153.203 | 2.84801 | 40.5394 | 0.263477 | 355.993 | 50.8939 | 0.309821 | 332.716 | 7.59145 | 0.990024 | 107.886 | 216.462 | 211.02 | 213.1495 | 16557.54 |
| 19434.3 | 15.5159 | 0.908753 | 117.438 | 0.109785 | 15.1781 | 0.553837 | 162.798 | 85.0888 | 0.727545 | 282.453 | 59.0102 | 0.317945 | 10.1892 | 79.2967 | 193.458 | 161.8717 | 10930.49 |
| 46236.8 | 27.5723 | 0.759718 | 167.397 | 1.15589 | 41.0338 | 0.370339 | 182.791 | 47.4516 | 0.451805 | 453.913 | 46.6339 | 0.727963 | 56.0626 | 118.675 | 125.742 | 243.7692 | 14706.26 |
| 36942.2 | 29.2645 | 0.811406 | 79.1474 | 2.32054 | 6.56275 | 0.655452 | 459.762 | 94.7772 | 0.739116 | 414.067 | 76.3482 | 0.956522 | 127.018 | 295.488 | 338.769 | 74.83402 | 4368.853 |
| 41159.1 | 24.4888 | 0.787952 | 36.5546 | 1.89076 | 92.6012 | 0.495732 | 423.407 | 24.502 | 0.941326 | 156.896 | 36.3746 | 0.511963 | 67.315 | 313.88 | 100.446 | 87.3673 | 6122.977 |
| 31072.2 | 19.1507 | 0.84404 | 26.0811 | 3.37978 | 88.6526 | 0.302182 | 175.689 | 58.6297 | 0.568984 | 318.956 | 63.7055 | 0.949212 | 104.373 | 85.3918 | 48.2963 | 117.395 | 9869.369 |
| 31857.6 | 32.921 | 0.839685 | 111.258 | 2.6217 | 72.4923 | 0.230464 | 338.327 | 73.3441 | 0.813292 | 222.931 | 92.2133 | 0.518519 | 119.267 | 222.674 | 112.747 | 206.6085 | 16414.6 |
| 45359.9 | 30.4441 | 0.764597 | 32.7707 | 2.78709 | 29.7573 | 0.242872 | 445.399 | 92.6528 | 0.580555 | 262.864 | 48.1264 | 0.91608 | 74.2158 | 281.187 | 175.303 | 169.108 | 10522.13 |
| 56229.4 | 24.3798 | 0.704149 | 73.6255 | 0.903074 | 79.4776 | 0.435774 | 148.274 | 8.1569 | 0.888787 | 192.505 | 23.812 | 0.497357 | 2.17842 | 144.378 | 191.051 | 127.256 | 8429.386 |
| 43073.1 | 23.1552 | 0.777308 | 92.2735 | 2.17821 | 28.3532 | 0.490047 | 483.08 | 50.0776 | 0.826507 | 391.504 | 87.4486 | 0.607543 | 75.9482 | 422.715 | 51.8178 | 87.73157 | 5282.181 |
| 12178.4 | 34.3034 | 0.949122 | 137.665 | 1.8004 | 34.5586 | 0.444687 | 498.5 | 6.84649 | 0.891249 | 354.977 | 82.0173 | 0.498305 | 13.7152 | 91.9488 | 86.8384 | 71.48483 | 5988.622 |
| 29286.7 | 32.4977 | 0.853981 | 160.653 | 1.23065 | 68.544 | 0.393929 | 300.903 | 73.0716 | 0.676122 | 268.349 | 73.5253 | 0.989699 | 41.0229 | 290.945 | 174.934 | 94.16502 | 6955.803 |
| 29320.9 | 21.3256 | 0.85378 | 81.3906 | 0.967073 | 44.4354 | 0.377214 | 399.953 | 84.5429 | 0.929151 | 415.087 | 1.22732 | 0.856482 | 33.7654 | 174.485 | 208.297 | 60.75682 | 4520.471 |
| 35984.8 | 14.1013 | 0.816719 | 129.661 | 1.83826 | 66.3918 | 0.304386 | 214.097 | 39.3043 | 0.494711 | 341.868 | 7.41791 | 0.802362 | 55.9746 | 196.226 | 72.5267 | 174.0525 | 12951.91 |
| 56111.9 | 23.1312 | 0.704802 | 89.3125 | 1.97038 | 36.9408 | 0.529407 | 291.323 | 84.674 | 0.623815 | 271.569 | 96.251 | 0.415106 | 170.044 | 187.609 | 256.626 | 245.5404 | 13435.69 |
| 15897.2 | 17.8993 | 0.928423 | 103.662 | 0.153647 | 51.2186 | 0.531484 | 343.652 | 9.47577 | 0.317202 | 82.6587 | 71.5543 | 0.784545 | 10.5733 | 324.393 | 59.0747 | 124.2057 | 9998.151 |
| 14944.9 | 30.7135 | 0.933732 | 90.5549 | 2.35989 | 22.1723 | 0.437763 | 282.891 | 92.7057 | 0.247931 | 318.67 | 95.0811 | 0.653733 | 43.2254 | 111.847 | 165.63 | 183.5022 | 13918.9 |
| 51409 | 22.4223 | 0.730953 | 93.0885 | 1.70867 | 95.6719 | 0.389779 | 347.824 | 65.1333 | 0.7266 | 472.121 | 26.1576 | 0.570655 | 138.584 | 249.52 | 420.484 | 153.1201 | 10825.31 |
| 17527.6 | 31.7171 | 0.919371 | 62.3679 | 0.14955 | 15.6517 | 0.330604 | 299.162 | 74.345 | 0.581744 | 321.226 | 69.6864 | 0.568946 | 9.91513 | 294.603 | 93.0958 | 139.7182 | 10131 |
| 19787.4 | 30.1903 | 0.906802 | 144.9 | 0.198033 | 87.4834 | 0.374194 | 442.795 | 96.2978 | 0.781434 | 287.277 | 82.2264 | 0.608697 | 12.5147 | 265.249 | 165.61 | 135.9603 | 11106.5 |
| 20003.7 | 14.7187 | 0.905586 | 80.9193 | 0.694607 | 10.5304 | 0.402147 | 240.799 | 17.9401 | 0.55793 | 102.298 | 48.8578 | 0.882852 | 67.2675 | 84.4737 | 88.5587 | 69.15744 | 4965.27 |
| 31919.6 | 32.8305 | 0.83934 | 129.796 | 0.366601 | 80.3317 | 0.551297 | 247.718 | 35.0538 | 0.488134 | 191.769 | 58.0955 | 0.83888 | 5.38458 | 191.847 | 178.218 | 105.5731 | 7560.995 |
| 11071.3 | 29.9352 | 0.955271 | 125.525 | 1.41124 | 60.7067 | 0.501644 | 413.901 | 3.73786 | 0.701629 | 85.2051 | 54.2139 | 0.618393 | 138.777 | 101.732 | 72.5427 | 61.20967 | 5613.871 |
| 35592.8 | 23.7287 | 0.818905 | 128.624 | 0.141042 | 61.1288 | 0.567216 | 314.336 | 55.7947 | 0.463432 | 425.349 | 49.9646 | 0.849594 | 9.18122 | 170.35 | 170.379 | 118.5977 | 7819.275 |
| 26014.2 | 28.31 | 0.872174 | 83.3101 | 0.513238 | 32.6524 | 0.483222 | 56.5518 | 17.2709 | 0.789588 | 187.358 | 56.1483 | 0.391461 | 19.9908 | 45.1789 | 103.506 | 112.9354 | 7953.086 |
| 41346.9 | 17.1503 | 0.786904 | 53.9372 | 2.67079 | 76.5596 | 0.428803 | 163.489 | 89.1934 | 0.909754 | 122.583 | 49.0487 | 0.802527 | 75.0682 | 63.7183 | 63.1793 | 73.00608 | 5209.325 |
| 28109.8 | 21.6339 | 0.860514 | 72.2524 | 1.17111 | 29.7702 | 0.467912 | 310.85 | 17.7137 | 0.654601 | 59.1485 | 96.5312 | 0.639173 | 59.8474 | 116.006 | 53.891 | 84.54713 | 5824.521 |
| 19718.7 | 13.9096 | 0.907171 | 57.9624 | 2.79357 | 2.56324 | 0.444702 | 496.036 | 11.0601 | 0.760653 | 212.272 | 31.85 | 0.50812 | 140.339 | 422.226 | 56.7016 | 73.39833 | 5107.281 |
| 26698.3 | 30.3693 | 0.868372 | 34.2881 | 3.39352 | 73.88 | 0.32787 | 172.469 | 73.3801 | 0.395697 | 219.235 | 3.93977 | 0.844261 | 28.1175 | 154.518 | 76.5849 | 157.382 | 13166.91 |
| 30587.1 | 19.0995 | 0.846737 | 101.59 | 0.534051 | 51.6165 | 0.522892 | 353.857 | 69.4715 | 0.872528 | 360.567 | 36.1818 | 0.716563 | 23.245 | 275.813 | 228.193 | 63.8519 | 4494.825 |
| 11530 | 16.3285 | 0.952708 | 149.622 | 1.4602 | 52.4308 | 0.422311 | 184.822 | 94.1671 | 0.612444 | 378.609 | 54.9132 | 0.88194 | 52.6195 | 101.907 | 270.822 | 72.49388 | 6225.824 |
| 45494.1 | 29.6646 | 0.76385 | 35.35 | 1.247 | 7.70603 | 0.443347 | 501.906 | 74.764 | 0.982376 | 465.369 | 40.7196 | 0.240369 | 3.69109 | 342.867 | 66.8173 | 216.5836 | 11961.05 |
| 22198.7 | 22.9469 | 0.893386 | 58.3351 | 1.35572 | 98.9455 | 0.277301 | 130.452 | 85.9013 | 0.786074 | 214.907 | 63.2056 | 0.444771 | 32.4025 | 90.6341 | 103.872 | 186.102 | 17222.67 |
| 57045.9 | 20.6103 | 0.699607 | 38.9702 | 0.236278 | 94.8526 | 0.486209 | 156.94 | 34.3254 | 0.637368 | 152.634 | 63.3452 | 0.959754 | 7.6231 | 149.04 | 68.4368 | 86.21853 | 5722.59 |
| 15340.4 | 25.1846 | 0.931526 | 125.199 | 2.7778 | 75.1861 | 0.297302 | 202.456 | 55.8774 | 0.756924 | 166.673 | 88.781 | 0.35908 | 96.3521 | 188.936 | 46.1838 | 193.7596 | 17873.8 |
| 21908.2 | 23.3833 | 0.895002 | 104.168 | 0.650739 | 36.4717 | 0.55145 | 418.905 | 27.2909 | 0.7816 | 129.071 | 83.7226 | 0.598159 | 16.496 | 214.939 | 91.5714 | 68.26074 | 4888.251 |
| 42805.3 | 27.9048 | 0.778801 | 157.099 | 0.168536 | 22.8497 | 0.29916 | 280.026 | 17.1744 | 0.859382 | 310.046 | 50.006 | 0.627765 | 1.91041 | 211.994 | 79.0397 | 196.4002 | 11575.21 |
| 27405.3 | 15.081 | 0.864428 | 38.5022 | 0.696627 | 26.2602 | 0.403864 | 207.202 | 12.6798 | 0.29986 | 254.843 | 20.8897 | 0.669913 | 67.7142 | 165.729 | 72.8424 | 186.6596 | 12984.05 |
| 29676.2 | 15.9025 | 0.851801 | 43.5134 | 0.825817 | 10.9965 | 0.354503 | 496.101 | 56.5403 | 0.753314 | 332.786 | 27.4081 | 0.860725 | 18.3307 | 252.501 | 271.685 | 70.37796 | 4622.62 |
| 45761.4 | 27.7678 | 0.762362 | 51.7624 | 2.38371 | 50.4731 | 0.44002 | 215.207 | 20.534 | 0.611272 | 445.653 | 98.114 | 0.844993 | 27.4945 | 54.7859 | 173.468 | 98.0186 | 6351.829 |
| 25249.9 | 20.0297 | 0.876417 | 155.514 | 0.537852 | 94.3507 | 0.23208 | 44.968 | 59.6934 | 0.889617 | 348.157 | 70.9648 | 0.768188 | 1.53521 | 36.1761 | 315.149 | 181.6497 | 15197.66 |
| 34065.4 | 24.7272 | 0.827399 | 62.0414 | 3.75647 | 32.6057 | 0.376513 | 358.176 | 25.6001 | 0.794485 | 260.831 | 71.1789 | 0.430055 | 59.1077 | 178.783 | 111.165 | 141.3111 | 9478.207 |
| 48522.6 | 19.2128 | 0.747002 | 86.273 | 1.4066 | 14.9468 | 0.336011 | 193.894 | 35.2905 | 0.798087 | 296.522 | 88.0713 | 0.326775 | 48.2034 | 146.969 | 96.4319 | 247.249 | 13964.63 |
| 19612.9 | 24.922 | 0.907767 | 104.473 | 0.498429 | 26.3435 | 0.452051 | 395.524 | 32.7482 | 0.769417 | 61.0665 | 92.6174 | 0.902881 | 11.7164 | 393.275 | 52.8161 | 55.04402 | 4086.304 |
| 45505.1 | 26.9307 | 0.763787 | 91.7011 | 2.2323 | 92.3781 | 0.374457 | 323.84 | 30.4057 | 0.950166 | 480.182 | 46.9123 | 0.29742 | 19.4241 | 193.09 | 139.92 | 219.3544 | 16060.18 |
| 31237.9 | 23.3484 | 0.843121 | 65.8714 | 0.805247 | 33.7168 | 0.44056 | 259.391 | 44.316 | 0.757854 | 409.12 | 71.0042 | 0.833749 | 38.4197 | 140.6 | 191.882 | 64.81424 | 4484.735 |
| 39669.3 | 16.4943 | 0.796232 | 103.653 | 3.46586 | 98.8203 | 0.488539 | 354.379 | 94.5747 | 0.919783 | 175.061 | 43.1127 | 0.218667 | 95.5017 | 294.953 | 90.5312 | 238.7755 | 16206.27 |
| 14521.8 | 20.2165 | 0.936074 | 158.65 | 2.2196 | 46.516 | 0.332013 | 408.086 | 36.5962 | 0.613372 | 477.702 | 0.89611 | 0.672109 | 57.9942 | 267.291 | 205.904 | 114.9739 | 9870.325 |
| 19471.9 | 14.3107 | 0.908544 | 96.517 | 1.96119 | 10.1185 | 0.562408 | 491.716 | 26.0961 | 0.66548 | 333.491 | 1.99785 | 0.727912 | 164.422 | 400.412 | 289.265 | 67.47142 | 4790.87 |
| 49067.1 | 21.2732 | 0.743976 | 60.4959 | 2.63178 | 95.509 | 0.453475 | 390.565 | 20.1945 | 0.766768 | 471.751 | 82.6998 | 0.441359 | 49.2201 | 293.017 | 444.76 | 153.1947 | 10734.06 |
| 28042.4 | 33.9628 | 0.860902 | 82.2121 | 0.601027 | 99.7141 | 0.485538 | 424.237 | 87.5639 | 0.690056 | 279.914 | 55.0307 | 0.793051 | 2.5796 | 182.119 | 112.482 | 77.46976 | 6238.587 |
| 41832 | 29.8192 | 0.784215 | 92.2135 | 0.840224 | 70.414 | 0.39953 | 243.419 | 35.0073 | 0.280284 | 293.766 | 55.9077 | 0.792083 | 4.64068 | 118.757 | 73.6999 | 249.8674 | 17423.35 |
| 45531 | 16.3399 | 0.763636 | 53.001 | 2.36969 | 40.2369 | 0.347922 | 313.278 | 73.9284 | 0.594926 | 290.499 | 35.7279 | 0.70953 | 51.027 | 263.303 | 236.333 | 146.0152 | 9325.082 |
| 50226 | 16.5173 | 0.737529 | 171.652 | 0.390394 | 39.319 | 0.525384 | 292.802 | 6.10032 | 0.888848 | 320.601 | 9.24461 | 0.769697 | 21.4971 | 187.295 | 170.359 | 92.78552 | 5425.199 |
| 36428.2 | 31.5861 | 0.814267 | 72.3628 | 1.27494 | 69.3172 | 0.415358 | 469.269 | 11.4469 | 0.83271 | 453.39 | 77.133 | 0.773081 | 27.0158 | 275.017 | 413.902 | 74.38621 | 5548.013 |
| 11859.6 | 14.0902 | 0.950873 | 149.552 | 0.668617 | 44.8408 | 0.650939 | 506.888 | 99.1411 | 0.900078 | 168.179 | 66.2472 | 0.362918 | 16.3582 | 138.95 | 151.618 | 102.6462 | 7533.143 |
| 20266.2 | 28.9454 | 0.904139 | 102.029 | 2.71238 | 9.79838 | 0.164211 | 146.986 | 32.3272 | 0.624443 | 250.657 | 93.907 | 0.683621 | 137.216 | 62.987 | 218.296 | 195.8625 | 13760 |
| 59045.8 | 19.8112 | 0.688486 | 74.1204 | 3.72824 | 67.0663 | 0.386457 | 447.342 | 91.0813 | 0.435395 | 352.359 | 47.1352 | 0.741946 | 142.506 | 137.891 | 343.622 | 208.0907 | 13030.86 |
| 28908.9 | 24.8737 | 0.856073 | 43.471 | 2.34785 | 20.9488 | 0.399897 | 311.075 | 44.0968 | 0.739821 | 163.751 | 26.5588 | 0.832308 | 87.238 | 307.821 | 80.3893 | 65.5212 | 4510.386 |
| 11786.4 | 32.1622 | 0.951298 | 140.83 | 1.4111 | 49.0497 | 0.456673 | 203.873 | 29.1644 | 0.739164 | 373.725 | 25.8859 | 0.215458 | 117.565 | 188.367 | 200.113 | 203.8267 | 17335.36 |
| 20874.7 | 31.4169 | 0.900758 | 37.1483 | 3.43946 | 43.1728 | 0.468438 | 383.139 | 85.4952 | 0.463519 | 178.6 | 57.5707 | 0.399229 | 145.42 | 270.359 | 178.34 | 178.2027 | 13251.3 |
| 16999 | 18.2139 | 0.922297 | 60.2505 | 0.523686 | 34.9103 | 0.298149 | 319.804 | 99.9691 | 0.362284 | 502.869 | 16.9722 | 0.712086 | 10.1091 | 173.133 | 78.5991 | 177.1395 | 14351.27 |
| 29596.9 | 18.0348 | 0.852243 | 49.7707 | 1.99636 | 20.2748 | 0.307885 | 135.045 | 43.7781 | 0.960899 | 349.263 | 39.9596 | 0.727208 | 152.873 | 117.401 | 187.345 | 77.51709 | 5289.397 |
| 18595 | 31.6135 | 0.913435 | 37.001 | 0.865775 | 14.386 | 0.244076 | 103.146 | 27.1965 | 0.365656 | 105.515 | 86.3008 | 0.650176 | 0.818322 | 45.2396 | 49.4652 | 228.6303 | 16688.46 |
| 14461.3 | 22.6836 | 0.936412 | 41.6328 | 0.943572 | 18.405 | 0.276827 | 314.273 | 69.2958 | 0.862733 | 188.095 | 26.673 | 0.888442 | 81.5014 | 311.404 | 142.438 | 60.32375 | 4813.511 |
| 15195.4 | 20.4568 | 0.932328 | 53.2124 | 1.46878 | 23.6583 | 0.308219 | 462.223 | 66.6204 | 0.483878 | 237.509 | 93.3707 | 0.785998 | 111.587 | 292.842 | 184.003 | 113.3663 | 8877.318 |
| 18721.7 | 18.9838 | 0.912718 | 94.0237 | 0.798764 | 58.8474 | 0.493214 | 331.199 | 75.2375 | 0.914533 | 441.399 | 71.1138 | 0.998627 | 20.9554 | 315.693 | 188.864 | 42.59263 | 3412.499 |
| 56783.2 | 20.9085 | 0.701068 | 71.3467 | 3.40051 | 71.941 | 0.437002 | 106.57 | 43.2463 | 0.437136 | 135.361 | 45.4406 | 0.899361 | 162.27 | 69.3957 | 127.932 | 144.1679 | 9186.024 |
| 30360.8 | 25.2229 | 0.848 | 133.921 | 2.50268 | 71.2417 | 0.479146 | 469.676 | 6.11324 | 0.473077 | 194.399 | 44.5004 | 0.900847 | 59.5999 | 281.673 | 172.712 | 91.35506 | 6965.621 |
| 39357.1 | 29.2389 | 0.797977 | 112.328 | 0.952641 | 14.1472 | 0.26632 | 466.694 | 46.9285 | 0.562669 | 55.446 | 83.9903 | 0.994356 | 61.0295 | 132.54 | 49.0897 | 148.9588 | 8960.939 |
| 36640.1 | 23.5686 | 0.813081 | 57.5059 | 2.31434 | 75.4854 | 0.33104 | 184.09 | 55.4546 | 0.508618 | 447.475 | 11.6294 | 0.609887 | 153.002 | 71.3445 | 168.082 | 192.6704 | 14709.1 |
| 39198.2 | 31.9575 | 0.798863 | 138.595 | 2.85129 | 50.6577 | 0.220721 | 249.542 | 69.398 | 0.973419 | 439.899 | 58.9295 | 0.716192 | 113.189 | 117.965 | 213.253 | 155.0974 | 10738.18 |
| 15373.9 | 28.7612 | 0.931344 | 62.5421 | 1.51444 | 41.692 | 0.35433 | 239.372 | 54.6336 | 0.757598 | 426.958 | 64.0488 | 0.497928 | 148.505 | 223.785 | 366.522 | 104.4985 | 8671.328 |
| 34504.2 | 31.4696 | 0.824966 | 98.3325 | 2.97999 | 55.5622 | 0.481012 | 348.878 | 86.1472 | 0.240833 | 188.138 | 7.85989 | 0.655789 | 109.011 | 178.7 | 78.4173 | 243.7964 | 16702.81 |
| 21098.5 | 17.485 | 0.8995 | 34.0962 | 1.2534 | 85.2445 | 0.171334 | 173.796 | 56.2961 | 0.987316 | 406.868 | 77.2637 | 0.494879 | 105.957 | 99.8597 | 59.7869 | 203.571 | 19208.5 |
| 20593.8 | 24.3928 | 0.902312 | 92.7706 | 3.16493 | 18.3422 | 0.394889 | 324.933 | 27.4706 | 0.72042 | 211.157 | 76.809 | 0.658152 | 88.17 | 74.8064 | 127.381 | 76.53732 | 5551.575 |
| 37994.4 | 34.3164 | 0.80556 | 73.4932 | 3.71087 | 81.5109 | 0.175049 | 51.9196 | 81.6839 | 0.963577 | 386.567 | 27.895 | 0.564864 | 12.4446 | 41.1077 | 146.231 | 233.0085 | 18526.85 |
| 34486.3 | 31.0223 | 0.825065 | 88.8375 | 2.80768 | 7.76 | 0.416069 | 342.575 | 46.274 | 0.719115 | 115.246 | 81.5535 | 0.722829 | 27.3423 | 262.968 | 68.7573 | 85.81632 | 5246.297 |
| 37146.2 | 17.8686 | 0.810263 | 53.849 | 2.00494 | 11.6261 | 0.278411 | 505.424 | 70.1661 | 0.297348 | 271.902 | 26.4073 | 0.937464 | 2.83493 | 406.925 | 263.317 | 229.4613 | 13906.66 |
| 23835.5 | 23.1177 | 0.884284 | 161.34 | 2.7082 | 24.0416 | 0.587117 | 496.021 | 71.2067 | 0.234767 | 220.386 | 39.0152 | 0.837466 | 181.68 | 71.7385 | 101.182 | 164.3593 | 10952.88 |
| 20066 | 28.9072 | 0.905252 | 133.818 | 1.43719 | 81.5885 | 0.246595 | 184.154 | 68.657 | 0.57198 | 500.31 | 22.3081 | 0.838489 | 103.633 | 113.26 | 190.314 | 154.7011 | 13963.49 |
| 32038.5 | 15.7876 | 0.838664 | 154.418 | 0.306041 | 66.9755 | 0.710739 | 400.512 | 64.807 | 0.777557 | 241.764 | 31.8256 | 0.45541 | 26.0716 | 191.993 | 95.3524 | 113.377 | 7231.371 |
| 28981.2 | 27.935 | 0.855674 | 146.307 | 1.98264 | 19.4199 | 0.653488 | 244.233 | 88.385 | 0.824903 | 293.492 | 32.636 | 0.860936 | 69.1361 | 160.847 | 152.369 | 57.14328 | 3657.531 |
| 29577.1 | 32.5015 | 0.852366 | 162.132 | 1.04041 | 96.6676 | 0.754291 | 421.721 | 89.1875 | 0.712406 | 293.705 | 43.7677 | 0.51399 | 44.7357 | 312.998 | 269.723 | 147.716 | 9568.528 |
| 29635.6 | 13.6687 | 0.852025 | 77.7883 | 0.715206 | 52.4194 | 0.304806 | 157.938 | 47.2215 | 0.338856 | 348.036 | 75.7866 | 0.687036 | 23.0697 | 106.75 | 188.831 | 248.3807 | 18752.96 |
| 40349.9 | 25.6216 | 0.792453 | 145.749 | 0.131692 | 62.0826 | 0.7133 | 475.323 | 52.7785 | 0.48395 | 219.576 | 93.5791 | 0.584287 | 7.27822 | 342.369 | 171.888 | 154.2136 | 9300.92 |
| 10869.5 | 32.644 | 0.956398 | 64.2121 | 3.27346 | 36.4884 | 0.29747 | 120.324 | 90.2719 | 0.336035 | 443.609 | 75.6159 | 0.547732 | 150.955 | 73.1272 | 72.4657 | 224.916 | 19573.66 |
| 25042.3 | 23.4266 | 0.877574 | 76.006 | 2.74221 | 15.0419 | 0.469885 | 445.414 | 44.8133 | 0.781596 | 464.137 | 55.0499 | 0.629159 | 109.923 | 117.614 | 173.517 | 67.90844 | 4605.348 |
| 42198.7 | 16.4322 | 0.782166 | 122.896 | 0.896832 | 41.1587 | 0.418377 | 515.097 | 94.6649 | 0.883827 | 500.133 | 28.8545 | 0.475308 | 19.4677 | 262.601 | 471.78 | 144.9274 | 9072.471 |
| 22813.8 | 27.1985 | 0.889969 | 169.371 | 0.461776 | 30.9753 | 0.710012 | 349.977 | 86.7283 | 0.702475 | 473.195 | 2.47533 | 0.429442 | 35.121 | 50.3544 | 376.01 | 113.9078 | 7585.617 |
| 41277.3 | 27.244 | 0.787297 | 147.911 | 2.92259 | 99.4029 | 0.541022 | 60.2109 | 68.5028 | 0.621683 | 261.374 | 59.4256 | 0.549786 | 113.925 | 51.0108 | 174.139 | 134.886 | 9249.195 |
| 21243.8 | 22.7897 | 0.898696 | 30.2404 | 0.724544 | 58.9608 | 0.314683 | 470.854 | 37.9388 | 0.53542 | 500.615 | 96.9885 | 0.661251 | 42.5949 | 338.807 | 421.428 | 140.3352 | 11786.64 |
| 16526.2 | 15.5125 | 0.924924 | 55.149 | 0.245101 | 99.0965 | 0.371936 | 235.956 | 36.4808 | 0.772281 | 278.035 | 71.4234 | 0.484278 | 5.11278 | 84.5572 | 204.571 | 115.2393 | 11110.09 |
| 22183.9 | 30.7704 | 0.893476 | 129.851 | 0.310139 | 84.5452 | 0.225913 | 84.3536 | 78.1531 | 0.98307 | 128.138 | 36.6084 | 0.865867 | 1.10603 | 34.2939 | 112.997 | 167.6535 | 14257.06 |
| 21382.5 | 15.3567 | 0.89792 | 164.307 | 3.55051 | 9.93045 | 0.354017 | 81.917 | 12.0063 | 0.887588 | 411.229 | 73.8096 | 0.453745 | 126.002 | 42.8288 | 276.292 | 115.8042 | 7972.457 |
| 31986.3 | 29.8002 | 0.838966 | 159.769 | 0.976663 | 40.3874 | 0.428313 | 132.656 | 1.58087 | 0.594194 | 472.492 | 59.6471 | 0.5859 | 20.9253 | 83.677 | 429.731 | 156.0966 | 10491.96 |
| 36121 | 31.7163 | 0.815975 | 149.616 | 1.88575 | 55.5501 | 0.534121 | 516.595 | 49.9629 | 0.308694 | 169.485 | 34.2832 | 0.607573 | 161.787 | 56.76 | 105.299 | 226.1328 | 14860.16 |
| 42665.5 | 20.9711 | 0.779573 | 54.898 | 2.43252 | 3.29382 | 0.46183 | 180.789 | 63.1741 | 0.661044 | 400.329 | 1.37092 | 0.638815 | 52.5332 | 148.849 | 380.766 | 100.9777 | 5735.195 |
| 39917.5 | 18.9338 | 0.794853 | 91.2712 | 0.334156 | 34.3194 | 0.407901 | 129.662 | 96.1788 | 0.350864 | 441.554 | 29.5269 | 0.807675 | 18.5423 | 49.2712 | 277.161 | 194.2844 | 12214.8 |
| 44258 | 33.8404 | 0.770729 | 94.8405 | 1.37649 | 73.2075 | 0.423304 | 251.023 | 94.905 | 0.733644 | 216.317 | 36.7642 | 0.888064 | 137.222 | 74.2298 | 54.1827 | 86.64524 | 5984.389 |
| 52163 | 18.8794 | 0.726759 | 119.774 | 1.8872 | 84.2367 | 0.32883 | 418.851 | 63.4875 | 0.945941 | 470.348 | 89.1856 | 0.739994 | 89.9516 | 83.2595 | 159.335 | 120.2221 | 8251.845 |
| 23568.3 | 22.3886 | 0.885769 | 111.474 | 1.34337 | 73.9306 | 0.467904 | 226.79 | 72.2273 | 0.900608 | 168.765 | 21.8641 | 0.994742 | 109.377 | 69.5769 | 154.264 | 45.52605 | 3749.98 |
| 15725.6 | 28.4811 | 0.929388 | 113.683 | 3.19717 | 25.8468 | 0.306588 | 203.816 | 8.76172 | 0.302475 | 256.262 | 1.56628 | 0.804715 | 61.5278 | 74.4622 | 58.4242 | 165.2317 | 13376.27 |
| 29416.7 | 22.7215 | 0.853248 | 64.6313 | 1.97242 | 1.3234 | 0.483309 | 322.79 | 73.5429 | 0.770801 | 281.392 | 43.5584 | 0.770337 | 100.746 | 116.717 | 148.04 | 59.81418 | 3747.35 |
| 20375.9 | 13.1675 | 0.903516 | 46.8646 | 0.582724 | 11.2536 | 0.368637 | 338.371 | 8.93218 | 0.46732 | 400.558 | 69.4889 | 0.699176 | 16.6577 | 136.761 | 311.997 | 110.3455 | 7819.025 |
| 36308.8 | 30.0754 | 0.814929 | 106.509 | 0.894504 | 92.2863 | 0.295282 | 250.487 | 43.504 | 0.946476 | 206.495 | 50.2538 | 0.43287 | 68.1085 | 191.596 | 155.607 | 191.4012 | 15016.41 |
| 21975.8 | 22.5936 | 0.894625 | 90.1932 | 0.811906 | 70.4572 | 0.31555 | 196.784 | 66.8007 | 0.388164 | 392.634 | 26.4646 | 0.808942 | 8.40933 | 122.022 | 269.821 | 167.5968 | 14421.7 |
| 12617.5 | 33.1317 | 0.946678 | 91.4653 | 1.31344 | 70.2762 | 0.418133 | 354.201 | 3.85981 | 0.5905 | 282.59 | 25.8409 | 0.451641 | 104.755 | 223.951 | 281.527 | 113.4306 | 10882.61 |
| 29101.8 | 32.745 | 0.855009 | 168.17 | 2.55626 | 18.8942 | 0.563963 | 291.528 | 34.9535 | 0.546817 | 417.019 | 74.5854 | 0.411994 | 146.747 | 282.062 | 254.88 | 165.5129 | 10521.13 |
| 38735.1 | 15.1711 | 0.801426 | 93.9642 | 1.19072 | 40.4076 | 0.289016 | 490.351 | 18.2037 | 0.866978 | 501.953 | 42.2321 | 0.999342 | 90.1481 | 112.103 | 63.8705 | 88.36442 | 6094.479 |
| 36268.5 | 14.151 | 0.815142 | 120.203 | 1.85998 | 70.6493 | 0.495419 | 442.893 | 39.621 | 0.660693 | 491.849 | 60.3223 | 0.537114 | 72.6429 | 104.808 | 109.416 | 118.6472 | 8333.402 |
| 23032.2 | 17.8239 | 0.888748 | 47.082 | 0.535465 | 13.0789 | 0.316197 | 497.21 | 70.3133 | 0.536947 | 457.504 | 55.5374 | 0.94197 | 8.28435 | 53.016 | 134.423 | 92.73722 | 6434.43 |
| 28995.4 | 15.7097 | 0.855586 | 163.391 | 2.04722 | 30.8935 | 0.613785 | 269.771 | 78.6869 | 0.79838 | 393.222 | 18.7411 | 0.235822 | 58.1129 | 175.995 | 342.437 | 215.453 | 13510.06 |
| 28145.7 | 24.2235 | 0.860317 | 26.5153 | 1.03494 | 22.6851 | 0.170118 | 287.06 | 19.4462 | 0.966897 | 428.197 | 52.7172 | 0.971353 | 49.3048 | 177.424 | 83.5165 | 152.9473 | 10706.59 |
| 12468.8 | 18.7538 | 0.947489 | 164.671 | 0.871467 | 20.7607 | 0.55465 | 388.208 | 22.0917 | 0.271552 | 517.667 | 94.0193 | 0.948058 | 57.6812 | 78.1962 | 509.435 | 115.7432 | 8902.6 |
| 16880.6 | 23.7521 | 0.92296 | 24.0265 | 2.30413 | 40.7787 | 0.496676 | 136.453 | 32.6171 | 0.841225 | 412.319 | 50.5937 | 0.691677 | 136.592 | 127.28 | 229.049 | 50.0675 | 3943.013 |
| 28969.8 | 27.4425 | 0.855737 | 157.543 | 0.323175 | 15.769 | 0.653654 | 486.968 | 76.7991 | 0.808958 | 248.324 | 96.6083 | 0.659433 | 29.1689 | 303.824 | 237.189 | 79.40826 | 4983.178 |
| 31112.9 | 22.5657 | 0.843816 | 112.87 | 0.549715 | 49.5795 | 0.565218 | 267.466 | 84.8499 | 0.281961 | 133.364 | 1.31754 | 0.717351 | 12.0738 | 51.7036 | 89.3204 | 177.8031 | 11960.65 |
| 46484.3 | 17.4282 | 0.758336 | 42.9986 | 1.84341 | 8.88363 | 0.298351 | 282.775 | 18.2033 | 0.507482 | 353.961 | 58.8493 | 0.832872 | 100.58 | 96.2287 | 295.117 | 159.5769 | 9020.143 |
| 16966 | 28.2286 | 0.922489 | 64.1712 | 2.79943 | 10.728 | 0.431345 | 398.426 | 80.1796 | 0.348696 | 243.377 | 84.2463 | 0.418673 | 5.32971 | 103.743 | 85.8458 | 212.0566 | 14985.13 |
| 17319.9 | 30.229 | 0.920524 | 130.662 | 0.899219 | 78.4054 | 0.427411 | 509.016 | 76.9485 | 0.511898 | 406.101 | 97.437 | 0.55678 | 81.5837 | 278.892 | 154.067 | 151.8327 | 12821.18 |
| 26914.3 | 28.6436 | 0.867169 | 43.3895 | 0.902015 | 43.3936 | 0.42611 | 457.74 | 72.3109 | 0.720913 | 492.218 | 86.0376 | 0.567263 | 56.022 | 400.241 | 86.6708 | 102.552 | 7386.965 |
| 44768 | 29.4115 | 0.767888 | 141.196 | 2.79746 | 66.4117 | 0.48971 | 350.82 | 21.9516 | 0.93707 | 104.38 | 15.2436 | 0.938358 | 144.555 | 232.648 | 99.1814 | 55.33571 | 3790.066 |
| 31247.7 | 24.8566 | 0.843068 | 153.177 | 0.734235 | 93.2349 | 0.483233 | 67.4424 | 71.0979 | 0.951237 | 459.587 | 64.2469 | 0.406663 | 61.7346 | 57.6269 | 211.918 | 143.5048 | 10433.83 |
| 44216.7 | 34.0965 | 0.770959 | 79.2715 | 0.326657 | 44.4539 | 0.259513 | 400.473 | 46.3749 | 0.864268 | 278.775 | 91.3962 | 0.779653 | 1.49499 | 191.101 | 76.8343 | 141.449 | 9208.809 |
| 48928.4 | 19.3714 | 0.744746 | 46.5492 | 3.18182 | 91.5734 | 0.406746 | 161.438 | 31.4593 | 0.516153 | 263.772 | 52.187 | 0.880177 | 152.738 | 90.6659 | 178.769 | 125.1569 | 8942.187 |
| 29417.2 | 34.7784 | 0.853258 | 142.48 | 1.74722 | 46.8255 | 0.413618 | 495.001 | 68.8691 | 0.545317 | 132.305 | 77.7308 | 0.773623 | 5.47496 | 271.603 | 126.836 | 121.7465 | 8576.449 |
| 51533.9 | 22.285 | 0.730259 | 143.866 | 2.86863 | 53.4524 | 0.291092 | 463.127 | 52.3821 | 0.502887 | 184.328 | 56.2763 | 0.726492 | 71.5818 | 443.318 | 77.4427 | 245.1304 | 15522.78 |
| 52375.7 | 21.1235 | 0.725577 | 115.382 | 1.34136 | 0.058684 | 0.229118 | 104.38 | 36.7017 | 0.98182 | 397.788 | 55.1779 | 0.978366 | 131.427 | 60.6074 | 336.656 | 149.428 | 7855.181 |
| 44762.1 | 22.24 | 0.767915 | 105.874 | 2.45272 | 72.8171 | 0.472588 | 123.544 | 81.1697 | 0.98938 | 52.3134 | 80.1262 | 0.552632 | 174.734 | 97.8739 | 50.473 | 95.00322 | 6267.281 |
| 20260.4 | 24.5025 | 0.904166 | 137.382 | 3.64944 | 47.4387 | 0.259999 | 351.004 | 12.4315 | 0.50358 | 185.557 | 8.7713 | 0.893078 | 147.452 | 102.237 | 109.517 | 127.7676 | 10738.91 |
| 14359.3 | 13.8302 | 0.936973 | 79.6012 | 0.187565 | 12.8261 | 0.170255 | 494.646 | 18.7946 | 0.908693 | 406.048 | 19.7298 | 0.863307 | 17.6832 | 119.786 | 81.6747 | 141.5558 | 10913.64 |
| 46596.9 | 26.7465 | 0.757715 | 86.4952 | 3.7534 | 32.9756 | 0.476294 | 482.957 | 80.6136 | 0.916537 | 496.68 | 38.3889 | 0.898807 | 62.4535 | 140.149 | 369.709 | 58.86326 | 3635.318 |
| 26089.2 | 14.827 | 0.871747 | 69.5696 | 2.16794 | 95.1499 | 0.266496 | 207.664 | 48.3993 | 0.943564 | 393.456 | 62.273 | 0.987768 | 19.3126 | 121.967 | 55.3805 | 93.3398 | 8421.607 |
| 38375.2 | 29.1795 | 0.803437 | 139.921 | 2.04062 | 30.024 | 0.205769 | 242.127 | 68.0945 | 0.65614 | 172.855 | 95.2889 | 0.824398 | 107.362 | 227.466 | 163.885 | 204.7587 | 13170.42 |
| 19478.6 | 13.2771 | 0.908506 | 64.7135 | 2.79052 | 59.9431 | 0.271493 | 451.211 | 16.7688 | 0.44418 | 441.778 | 33.0148 | 0.857382 | 124.304 | 412.396 | 126.354 | 139.1173 | 12373.77 |
| 29409.5 | 18.9502 | 0.853285 | 42.1223 | 1.53708 | 44.0993 | 0.334797 | 155.09 | 13.4678 | 0.786986 | 265.243 | 74.5369 | 0.470672 | 126.179 | 143.797 | 176.295 | 136.2355 | 10051.57 |
| 50584.8 | 21.1865 | 0.735536 | 89.4452 | 1.95309 | 60.0156 | 0.43032 | 508.164 | 79.823 | 0.476773 | 128.012 | 42.4043 | 0.938985 | 36.6935 | 356.58 | 62.7574 | 121.4689 | 7837.84 |
| 34367.2 | 27.5435 | 0.825723 | 81.0247 | 2.70071 | 8.5395 | 0.284865 | 388.729 | 29.3732 | 0.908206 | 332.407 | 7.64169 | 0.402319 | 118.462 | 217.55 | 116.802 | 167.7475 | 10270.86 |
| 22361.6 | 14.4272 | 0.892474 | 147.553 | 2.96982 | 45.9051 | 0.251519 | 482.125 | 6.22845 | 0.504263 | 219.678 | 3.2374 | 0.545891 | 15.2019 | 451.285 | 217.822 | 241.4754 | 19318.91 |
| 25788.9 | 32.3559 | 0.873432 | 128.858 | 0.130984 | 48.4358 | 0.295651 | 488.865 | 72.8523 | 0.655873 | 113.87 | 93.4147 | 0.869938 | 8.29133 | 140.679 | 77.5471 | 142.4667 | 10368.27 |
| 19684.5 | 34.3413 | 0.90738 | 70.5117 | 2.25255 | 95.371 | 0.424932 | 359.444 | 88.3994 | 0.658335 | 347.687 | 96.8264 | 0.357706 | 152.876 | 48.8761 | 285.847 | 174.1928 | 15086.98 |
| 32910.6 | 30.4672 | 0.833826 | 150.009 | 0.892564 | 30.2943 | 0.567325 | 423.956 | 6.41517 | 0.427024 | 276.502 | 35.9993 | 0.83759 | 69.1531 | 115.216 | 68.8422 | 109.1094 | 7036.515 |
| 19667 | 13.5352 | 0.907458 | 81.5895 | 2.14378 | 27.8977 | 0.283616 | 275.909 | 27.2528 | 0.678616 | 299.498 | 52.9273 | 0.82436 | 163.337 | 191.465 | 54.9341 | 87.01872 | 6794.942 |
| 44827.1 | 26.7535 | 0.767557 | 135.417 | 3.36056 | 64.6358 | 0.288275 | 200.779 | 28.9253 | 0.554384 | 321.153 | 45.387 | 0.799623 | 1.4386 | 78.3844 | 308.42 | 180.5778 | 12606.23 |
| 21914 | 19.7344 | 0.894967 | 45.4338 | 1.86201 | 63.7385 | 0.330977 | 107.077 | 2.46719 | 0.451393 | 320.488 | 18.3143 | 0.685714 | 4.18741 | 62.8378 | 97.6199 | 144.9139 | 12574.96 |
| 26417.7 | 28.9776 | 0.869931 | 61.6251 | 1.50167 | 30.9027 | 0.148636 | 273.614 | 1.82741 | 0.988373 | 366.705 | 92.3443 | 0.527683 | 24.9113 | 189.501 | 241.777 | 206.5242 | 15352.92 |
| 43000.9 | 23.1323 | 0.777709 | 48.7101 | 0.35628 | 86.2012 | 0.171316 | 437.312 | 20.3288 | 0.820243 | 223.717 | 84.0562 | 0.928081 | 26.496 | 139.07 | 108.025 | 214.6529 | 16912.42 |
| 10828.4 | 23.1692 | 0.956615 | 136.997 | 2.66999 | 41.8612 | 0.191539 | 327.633 | 39.7031 | 0.552113 | 360.405 | 72.1751 | 0.996064 | 24.6461 | 205.064 | 201.458 | 131.5816 | 12052.51 |
| 28015.9 | 26.5681 | 0.861041 | 73.2003 | 0.449386 | 3.90956 | 0.226567 | 146.474 | 66.5357 | 0.452965 | 375.222 | 49.746 | 0.85622 | 10.8266 | 128.93 | 163.957 | 186.473 | 11700.96 |
| 35504.6 | 14.5883 | 0.81939 | 166.367 | 0.431025 | 57.8345 | 0.612255 | 304.643 | 71.4463 | 0.913818 | 149.423 | 39.1557 | 0.239867 | 1.23685 | 61.9828 | 81.3802 | 225.2206 | 14126.95 |
| 37740.1 | 23.6376 | 0.806964 | 153.225 | 0.780308 | 23.9349 | 0.508085 | 168.446 | 22.7377 | 0.558879 | 185.619 | 49.1083 | 0.617282 | 22.2374 | 125.673 | 138.268 | 141.961 | 8652.549 |
| 16301.7 | 23.2214 | 0.926178 | 88.7775 | 2.39867 | 59.9077 | 0.442366 | 324.665 | 75.791 | 0.801342 | 214.695 | 16.5171 | 0.978003 | 39.3378 | 262.099 | 114.245 | 41.24868 | 3657.06 |
| 17567.2 | 25.3734 | 0.919143 | 134.091 | 0.301592 | 93.7726 | 0.55633 | 351.955 | 25.9384 | 0.612438 | 367.289 | 53.8389 | 0.657326 | 17.8046 | 208.341 | 108.227 | 85.91487 | 7276.644 |
| 16611.2 | 18.025 | 0.924454 | 90.9527 | 3.44598 | 61.3208 | 0.307817 | 302.749 | 14.3508 | 0.534066 | 183.275 | 44.0576 | 0.479573 | 114.08 | 272.571 | 173.428 | 174.6881 | 15851.9 |
| 39065.2 | 15.5679 | 0.799591 | 131.665 | 0.236572 | 68.5428 | 0.248737 | 195.292 | 86.0403 | 0.71591 | 382.044 | 40.5491 | 0.84573 | 8.20392 | 177.547 | 329.965 | 186.216 | 13080.86 |
| 59864.3 | 21.0918 | 0.683935 | 116.324 | 1.59824 | 93.7561 | 0.475764 | 347.158 | 23.211 | 0.29001 | 227.037 | 12.1055 | 0.925369 | 108.021 | 82.6713 | 188.153 | 214.2133 | 13699.06 |
| 14949.7 | 20.8317 | 0.933695 | 151.341 | 2.17336 | 60.9106 | 0.377212 | 96.2878 | 56.9547 | 0.908641 | 350.059 | 20.6289 | 0.237608 | 42.1611 | 43.3338 | 208.324 | 210.0849 | 17769.01 |
| 22282.1 | 21.2191 | 0.892921 | 128.337 | 0.214074 | 56.8373 | 0.510203 | 227.399 | 73.7547 | 0.382722 | 512.146 | 18.5198 | 0.45286 | 20.4584 | 125.193 | 219.261 | 233.2943 | 17268.7 |
| 30368.4 | 31.7707 | 0.847964 | 68.5911 | 0.930038 | 20.1354 | 0.363745 | 243.795 | 33.3369 | 0.576076 | 146.136 | 91.5099 | 0.647455 | 64.5375 | 47.171 | 81.506 | 126.7783 | 8365.079 |
| 16610.8 | 18.1687 | 0.924456 | 98.2106 | 0.908808 | 63.8715 | 0.298535 | 265.259 | 42.3911 | 0.72031 | 128.799 | 71.7678 | 0.505667 | 44.5813 | 154.303 | 76.0807 | 143.5199 | 12748.74 |
| 14053.6 | 34.4287 | 0.938694 | 64.2629 | 1.00873 | 64.4174 | 0.434196 | 321.75 | 20.2474 | 0.756556 | 479.816 | 52.1829 | 0.339371 | 24.4376 | 96.4615 | 349.169 | 119.9497 | 10827.61 |
| 35404.3 | 25.5698 | 0.819954 | 107.485 | 3.11476 | 90.7317 | 0.663442 | 516.993 | 72.7331 | 0.812839 | 422.14 | 33.9841 | 0.85981 | 157.469 | 381.929 | 371.402 | 71.98619 | 4816.489 |
| 22672.3 | 21.9338 | 0.890752 | 144.258 | 0.253056 | 57.8328 | 0.535764 | 278.399 | 43.1421 | 0.549361 | 318.209 | 37.1732 | 0.419165 | 20.8502 | 86.0023 | 133.6 | 176.053 | 12908.05 |
| 12850.4 | 22.4312 | 0.94537 | 130.208 | 3.48608 | 49.9332 | 0.328269 | 80.8989 | 15.3978 | 0.893438 | 295.043 | 19.5384 | 0.562167 | 62.8337 | 64.3663 | 167.22 | 77.75553 | 7210.165 |
| 44587.9 | 21.7444 | 0.768884 | 153.473 | 0.792954 | 28.1466 | 0.586998 | 401.616 | 73.8966 | 0.723984 | 164.436 | 27.1668 | 0.705013 | 40.7242 | 300.045 | 158.588 | 95.74482 | 5614.277 |
| 55362.6 | 18.7408 | 0.708966 | 104.868 | 1.13741 | 90.9424 | 0.48595 | 371.302 | 63.9127 | 0.82383 | 372.555 | 13.0697 | 0.357654 | 111.946 | 159.646 | 165.996 | 192.0644 | 12336.25 |
| 51470.9 | 27.3123 | 0.730612 | 103.136 | 2.0537 | 61.8429 | 0.352159 | 432.161 | 5.81177 | 0.900417 | 462.854 | 2.30828 | 0.968097 | 79.6338 | 252.627 | 328.776 | 78.15976 | 5325.43 |
| 48909.1 | 30.7768 | 0.744861 | 103.72 | 2.76305 | 63.5633 | 0.188538 | 238.237 | 58.0177 | 0.792337 | 140.02 | 64.0793 | 0.743929 | 116.558 | 161.755 | 132.753 | 216.5145 | 15022.07 |
| 31219 | 17.939 | 0.843222 | 37.6875 | 2.25833 | 28.855 | 0.270024 | 247.404 | 94.946 | 0.406288 | 461.453 | 4.09479 | 0.959675 | 160.624 | 127.296 | 448.849 | 161.6211 | 11170.86 |
| 37587 | 25.5883 | 0.807817 | 103.665 | 1.94847 | 13.8922 | 0.180496 | 500.319 | 86.0459 | 0.640139 | 102.875 | 93.5174 | 0.945039 | 118.796 | 409.711 | 81 | 177.0687 | 10861.51 |
| 28409.9 | 25.5372 | 0.858849 | 160.002 | 2.48434 | 96.9143 | 0.482661 | 459.663 | 98.9587 | 0.986229 | 216.448 | 59.08 | 0.501274 | 123.345 | 319.907 | 162.34 | 103.4137 | 7820.3 |
| 52588.1 | 22.5341 | 0.724396 | 140.487 | 0.963473 | 98.5988 | 0.378829 | 493.76 | 35.3178 | 0.87723 | 498.696 | 60.474 | 0.498933 | 5.84601 | 293.954 | 294.905 | 186.44 | 12589.63 |
| 24584.7 | 27.2061 | 0.880122 | 158.095 | 1.67875 | 73.7633 | 0.67244 | 394.989 | 81.7448 | 0.606266 | 489.936 | 63.4488 | 0.893901 | 93.4754 | 344.57 | 463.248 | 73.43742 | 5115.278 |
| 14855.4 | 16.0484 | 0.934216 | 62.1849 | 2.29483 | 94.1072 | 0.562084 | 416.371 | 94.2706 | 0.720706 | 395.569 | 50.4358 | 0.79503 | 49.6591 | 197.005 | 266.635 | 67.84347 | 5591.561 |
| 40469.8 | 16.3134 | 0.79178 | 19.0923 | 2.40328 | 22.4427 | 0.358173 | 224.814 | 91.3033 | 0.537138 | 210.944 | 30.801 | 0.600997 | 62.8101 | 158.555 | 181.671 | 171.2283 | 10510.6 |
| 27221.2 | 33.459 | 0.865468 | 160.616 | 1.95752 | 35.5613 | 0.509764 | 296.242 | 11.1039 | 0.636763 | 433.502 | 25.794 | 0.606341 | 167.585 | 146.658 | 257.52 | 99.56501 | 6939.351 |
| 40676.3 | 23.1922 | 0.790636 | 120.864 | 0.193149 | 10.1588 | 0.579615 | 209.647 | 38.9434 | 0.640718 | 234.649 | 54.143 | 0.918649 | 15.9873 | 147.766 | 178.665 | 76.3448 | 4486.638 |
| 36759.8 | 17.9964 | 0.812411 | 129.344 | 2.6898 | 69.0083 | 0.450464 | 384.76 | 3.18587 | 0.684953 | 397.507 | 56.7788 | 0.700208 | 144.215 | 65.0539 | 45.8128 | 92.61382 | 6717.706 |
| 36778.9 | 14.0783 | 0.812303 | 161.74 | 0.155894 | 23.2751 | 0.518836 | 226.903 | 75.3202 | 0.781169 | 462.181 | 27.4215 | 0.376423 | 1.88478 | 72.4726 | 106.785 | 203.092 | 12119.97 |
| 35118.9 | 34.0747 | 0.82155 | 35.5953 | 0.542521 | 12.2048 | 0.471204 | 460.519 | 57.7533 | 0.955254 | 446.015 | 65.7008 | 0.683297 | 26.2465 | 368.755 | 134.43 | 64.26882 | 3990.622 |
| 23165.6 | 33.4895 | 0.888021 | 141.156 | 0.112517 | 50.1269 | 0.637949 | 268.61 | 64.1033 | 0.50412 | 284.573 | 52.9199 | 0.659298 | 8.60089 | 220.543 | 117.258 | 111.3281 | 7800.402 |
| 15758.2 | 23.7711 | 0.929201 | 155.772 | 1.10528 | 4.12156 | 0.553403 | 433.539 | 50.956 | 0.749241 | 226.693 | 93.6909 | 0.805135 | 35.7494 | 203.543 | 162.421 | 55.01848 | 3907.388 |
| 41827.9 | 23.8048 | 0.784233 | 121.977 | 1.0379 | 48.9328 | 0.435312 | 465.208 | 4.58026 | 0.598988 | 461.301 | 91.1628 | 0.381651 | 72.6153 | 55.9965 | 290.573 | 232.866 | 14963.81 |
| 52106.9 | 28.3957 | 0.727076 | 38.1819 | 2.2371 | 61.169 | 0.554717 | 272.411 | 10.7653 | 0.650104 | 327.727 | 25.8831 | 0.834627 | 81.1628 | 245.569 | 254.745 | 90.07362 | 5462.069 |
| 55239.1 | 24.8574 | 0.709656 | 113.451 | 3.17688 | 2.79587 | 0.480981 | 259.153 | 19.9176 | 0.988578 | 236.152 | 40.5172 | 0.350604 | 19.742 | 59.7696 | 60.141 | 138.4897 | 7245.775 |
| 25743.8 | 27.3727 | 0.873676 | 121.194 | 1.81802 | 95.5031 | 0.486759 | 506.463 | 23.4297 | 0.580812 | 451.945 | 3.33266 | 0.676379 | 125.648 | 317.743 | 276.016 | 91.71557 | 7711.007 |
| 13089.7 | 23.8806 | 0.94404 | 142.7 | 0.241708 | 0.285585 | 0.664465 | 137.288 | 62.0651 | 0.357217 | 464.063 | 74.9983 | 0.657679 | 17.2857 | 119.853 | 220.991 | 111.6072 | 8003.968 |
| 27315.8 | 17.1047 | 0.864927 | 49.2297 | 1.30688 | 77.3636 | 0.425384 | 507.234 | 5.39575 | 0.365331 | 397.959 | 79.444 | 0.6206 | 115.243 | 363.555 | 240.927 | 172.939 | 13998.25 |
| 10903.5 | 25.4584 | 0.956199 | 27.9704 | 1.15674 | 15.3589 | 0.427874 | 257.866 | 24.0627 | 0.580079 | 236.732 | 57.9589 | 0.836348 | 85.4573 | 230.87 | 58.6116 | 54.27209 | 4443.028 |
| 15646.8 | 15.2125 | 0.929814 | 24.8765 | 0.957526 | 14.537 | 0.234072 | 506.347 | 16.5399 | 0.665534 | 294.527 | 36.2928 | 0.78024 | 53.6935 | 45.7907 | 228.414 | 99.371 | 7723.944 |
| 45175.2 | 20.8643 | 0.765617 | 59.2077 | 2.43779 | 14.6561 | 0.365413 | 186.37 | 66.3845 | 0.513562 | 230.122 | 43.2556 | 0.8504 | 128.873 | 90.6652 | 171.031 | 129.2442 | 7524.734 |
| 43891 | 20.5062 | 0.772758 | 81.4389 | 0.499386 | 74.995 | 0.461907 | 151.425 | 60.7459 | 0.622534 | 133.404 | 60.7937 | 0.760868 | 5.88975 | 86.145 | 119.004 | 108.3928 | 7426.515 |
| 10671.5 | 17.9379 | 0.957483 | 171.699 | 3.46863 | 21.3799 | 0.396674 | 377.678 | 26.1901 | 0.930203 | 275.549 | 57.3682 | 0.324586 | 63.2019 | 86.0034 | 71.1042 | 119.9529 | 9648.433 |
| 14173.5 | 24.3703 | 0.938014 | 33.4451 | 1.4958 | 30.0071 | 0.415995 | 334.956 | 80.7217 | 0.532223 | 84.9004 | 79.6127 | 0.542448 | 66.2749 | 199.862 | 84.0808 | 113.359 | 8916.183 |
| 28399.6 | 28.8125 | 0.858909 | 115.531 | 3.76642 | 58.932 | 0.236942 | 227.477 | 67.4576 | 0.955306 | 307.809 | 58.2022 | 0.407831 | 43.3541 | 81.244 | 281.905 | 200.0796 | 15724.17 |
| 45058.8 | 31.9712 | 0.766273 | 122.905 | 2.00451 | 21.766 | 0.37281 | 327.37 | 38.8561 | 0.640192 | 111.886 | 70.4214 | 0.70582 | 82.8214 | 277.77 | 53.458 | 136.579 | 8095.11 |
| 18372.4 | 20.8371 | 0.914662 | 73.0917 | 0.941846 | 3.88764 | 0.40536 | 202.35 | 35.2296 | 0.758518 | 385.975 | 87.361 | 0.284521 | 43.4516 | 116.372 | 325.119 | 154.0497 | 10491.8 |
| 16178.2 | 31.5146 | 0.926875 | 56.7988 | 1.02235 | 22.3001 | 0.169383 | 106.985 | 22.6419 | 0.798951 | 70.166 | 89.0157 | 0.531546 | 37.2043 | 53.0601 | 54.5451 | 182.3684 | 14417.49 |
| 40428.4 | 22.9014 | 0.792015 | 148.607 | 1.38801 | 58.4032 | 0.521827 | 350.616 | 41.3313 | 0.963478 | 501.054 | 86.3255 | 0.646378 | 105.661 | 175.688 | 341.056 | 81.78358 | 5322.126 |
| 13527.8 | 17.8948 | 0.9416 | 167.591 | 2.24039 | 31.518 | 0.309266 | 231.334 | 8.90699 | 0.660663 | 393.307 | 99.8997 | 0.62399 | 109.547 | 142.699 | 169.86 | 124.9571 | 10161.68 |
| 30851.6 | 34.5096 | 0.845281 | 78.0082 | 0.724578 | 59.827 | 0.266495 | 324.495 | 33.3738 | 0.346335 | 418.215 | 49.8512 | 0.907362 | 8.37582 | 136.169 | 390.65 | 220.2504 | 17079.87 |
| 34412.7 | 32.841 | 0.825476 | 156.025 | 2.61106 | 28.3852 | 0.466356 | 299.953 | 59.0722 | 0.38094 | 319.073 | 37.2551 | 0.488709 | 82.4258 | 260.836 | 50.9581 | 249.0622 | 15736.62 |
| 35546.5 | 16.4515 | 0.819158 | 151.23 | 0.199559 | 79.364 | 0.504711 | 231.74 | 20.5765 | 0.361392 | 505.025 | 26.8724 | 0.660977 | 8.35041 | 63.028 | 244.102 | 228.5826 | 15638.67 |
| 17643.6 | 32.6825 | 0.918728 | 137.144 | 1.36495 | 96.9914 | 0.19832 | 367.108 | 80.0971 | 0.646987 | 417.674 | 30.015 | 0.731526 | 22.5383 | 230.812 | 137.829 | 200.7947 | 19472.34 |
| 21532.9 | 28.4718 | 0.897094 | 109.992 | 1.61822 | 30.5879 | 0.285671 | 362.143 | 76.0907 | 0.542553 | 354.596 | 94.4093 | 0.797164 | 18.415 | 62.9246 | 107.272 | 131.9033 | 9841.829 |
| 11307.5 | 27.0215 | 0.953954 | 34.2902 | 1.88574 | 53.2263 | 0.347563 | 137.212 | 66.4387 | 0.956093 | 491.592 | 66.096 | 0.98267 | 119.803 | 69.2302 | 81.088 | 51.10417 | 4592.704 |
| 18733.3 | 17.7416 | 0.912653 | 142.639 | 2.67613 | 3.53843 | 0.386353 | 517.544 | 32.0347 | 0.740131 | 86.1735 | 83.1709 | 0.739997 | 73.7538 | 250.758 | 78.2331 | 72.4298 | 5023.392 |
| 25760.1 | 18.612 | 0.873579 | 138.268 | 0.835916 | 70.0408 | 0.339985 | 215.56 | 25.5111 | 0.922921 | 129.848 | 82.8792 | 0.48184 | 22.6356 | 168.867 | 65.4785 | 139.8724 | 11004.45 |
| 37947.1 | 34.2277 | 0.805823 | 88.3102 | 1.30181 | 66.1692 | 0.467683 | 357.967 | 77.2561 | 0.515774 | 379.477 | 84.2821 | 0.822963 | 85.6777 | 77.9042 | 214.001 | 107.7015 | 7464.251 |
| 27550.6 | 29.7877 | 0.863632 | 88.5646 | 0.461161 | 56.4054 | 0.33772 | 258.672 | 13.2139 | 0.887072 | 255.73 | 97.5303 | 0.437726 | 21.055 | 57.408 | 150.094 | 144.7808 | 11048.08 |
| 37290.9 | 27.4114 | 0.809465 | 30.1162 | 2.34109 | 63.1989 | 0.521644 | 419.432 | 82.4157 | 0.672781 | 250.617 | 20.1489 | 0.95211 | 25.9465 | 273.784 | 227.358 | 65.65218 | 4462.272 |
| 47687.2 | 19.8852 | 0.751648 | 147.707 | 3.29078 | 15.6507 | 0.549606 | 273.357 | 39.5803 | 0.599424 | 290.905 | 11.9602 | 0.575662 | 191.593 | 112.703 | 134.522 | 125.6118 | 7007.94 |
| 32665.4 | 31.376 | 0.835191 | 143.932 | 0.206483 | 10.0598 | 0.282282 | 346.463 | 18.4214 | 0.575147 | 453.511 | 17.8424 | 0.797833 | 15.4205 | 303.641 | 230.015 | 189.3807 | 11660.48 |
| 13833.7 | 25.6214 | 0.939905 | 148.389 | 3.69243 | 10.2581 | 0.287234 | 507.83 | 71.5878 | 0.758763 | 169.826 | 12.0904 | 0.614443 | 85.7052 | 180.856 | 163.249 | 101.8074 | 7684.749 |
| 15821.3 | 21.4339 | 0.928848 | 46.2708 | 1.9584 | 2.04939 | 0.437463 | 233.773 | 77.1452 | 0.723002 | 289.521 | 98.3107 | 0.505494 | 159.611 | 185.954 | 254.676 | 88.4109 | 6075.571 |
| 41679.4 | 18.8469 | 0.785056 | 41.0825 | 1.29273 | 78.4659 | 0.489892 | 218.308 | 69.8093 | 0.929286 | 451.217 | 81.0881 | 0.544999 | 93.4006 | 155.766 | 432.303 | 92.31305 | 6117.251 |
| 50600.6 | 16.5809 | 0.735446 | 122.813 | 1.81142 | 14.8299 | 0.476359 | 197.777 | 57.3804 | 0.79045 | 199.953 | 6.66253 | 0.722722 | 35.4223 | 94.104 | 141.899 | 87.84316 | 4968.162 |
| 30783.7 | 25.3598 | 0.845648 | 107.456 | 2.43351 | 38.5027 | 0.411323 | 158.651 | 53.823 | 0.280173 | 397.176 | 85.0015 | 0.837601 | 2.79724 | 108.889 | 366.679 | 179.5335 | 12503.29 |
| 43036.1 | 24.3059 | 0.777514 | 158.026 | 0.650743 | 32.4433 | 0.605532 | 225.92 | 22.3517 | 0.558439 | 373.361 | 6.74698 | 0.549853 | 41.8556 | 97.4651 | 233.289 | 148.4506 | 8755.616 |
| 16386 | 17.9299 | 0.925705 | 159.732 | 0.510483 | 15.6546 | 0.660135 | 438.422 | 27.627 | 0.798492 | 431.751 | 81.4643 | 0.971059 | 46.3929 | 304.546 | 263.045 | 38.76114 | 2871.835 |
| 18192.2 | 31.9493 | 0.915676 | 128.149 | 0.725754 | 98.5103 | 0.453962 | 108.747 | 88.4471 | 0.702948 | 317.762 | 91.0774 | 0.833953 | 55.5427 | 69.9085 | 164.423 | 77.7569 | 6663.899 |
| 32065.1 | 32.0754 | 0.83853 | 87.4672 | 3.36396 | 61.7521 | 0.193933 | 74.1267 | 24.1259 | 0.98618 | 256.403 | 44.9943 | 0.863734 | 29.1428 | 64.256 | 120.411 | 147.8402 | 11721.36 |
| 25458.7 | 16.0597 | 0.875253 | 58.7185 | 1.40469 | 25.7657 | 0.22722 | 465.947 | 32.266 | 0.40399 | 479.801 | 49.0866 | 0.900862 | 69.144 | 442.915 | 466.144 | 182.6592 | 13264.19 |
| 50832.7 | 16.131 | 0.734155 | 27.5273 | 0.878791 | 4.24201 | 0.34235 | 265.202 | 91.4078 | 0.876065 | 63.545 | 63.7809 | 0.974418 | 84.7186 | 81.8856 | 58.0983 | 84.38473 | 4634.642 |
| 29705.3 | 33.0153 | 0.851654 | 138.84 | 2.3308 | 71.4319 | 0.491896 | 225.412 | 87.8442 | 0.956024 | 507.046 | 83.4346 | 0.674021 | 87.1675 | 117.993 | 142.133 | 73.7349 | 5327.724 |
| 55015.8 | 20.2513 | 0.710896 | 128.782 | 2.78293 | 68.5621 | 0.599985 | 410.883 | 69.2187 | 0.843083 | 363.479 | 7.31292 | 0.930934 | 17.7028 | 408.478 | 212.553 | 65.92196 | 3975.306 |
| 23233.9 | 34.0794 | 0.887642 | 108.301 | 1.50287 | 15.981 | 0.283837 | 93.2493 | 46.2197 | 0.565081 | 468.699 | 75.3858 | 0.836046 | 64.1696 | 65.438 | 382.611 | 118.6505 | 8280.426 |
| 22221.7 | 31.7493 | 0.893268 | 140.354 | 1.69693 | 74.0782 | 0.433188 | 426.933 | 14.8564 | 0.561985 | 274.449 | 9.27153 | 0.78683 | 107.923 | 405.019 | 262.893 | 91.1299 | 7658.112 |
| 26738.7 | 17.3297 | 0.868136 | 97.1776 | 1.20593 | 8.53334 | 0.445311 | 417.106 | 90.6724 | 0.729987 | 414.252 | 61.6703 | 0.343795 | 20.2425 | 380.938 | 403.595 | 157.5342 | 9944.386 |
| 24235.1 | 16.0686 | 0.882057 | 42.9303 | 0.457617 | 90.8408 | 0.275785 | 475.172 | 18.6519 | 0.953006 | 92.8166 | 7.13854 | 0.375777 | 26.0614 | 96.3157 | 74.8087 | 171.7558 | 15890.02 |
| 41432.8 | 15.1208 | 0.786425 | 169.357 | 2.05337 | 41.9725 | 0.46084 | 329.389 | 50.4403 | 0.454865 | 287.264 | 64.1035 | 0.597358 | 96.056 | 180.938 | 89.1049 | 208.2497 | 12899.97 |
| 28752.7 | 21.5213 | 0.85694 | 53.7256 | 3.18147 | 19.3204 | 0.334384 | 366.378 | 28.9345 | 0.738274 | 249.646 | 38.8671 | 0.498327 | 31.4764 | 364.647 | 215.316 | 130.0207 | 8778.048 |
| 42937.3 | 24.5975 | 0.778064 | 35.228 | 0.873232 | 25.143 | 0.339488 | 87.6215 | 75.6118 | 0.991141 | 128.862 | 65.9435 | 0.473976 | 76.8731 | 80.85 | 97.2363 | 138.0619 | 8410.168 |
| 17403 | 34.6544 | 0.920069 | 135.73 | 1.45159 | 63.5247 | 0.256512 | 359.514 | 10.894 | 0.894562 | 154.824 | 96.6451 | 0.884923 | 28.7376 | 49.8667 | 89.0196 | 98.21806 | 8607.493 |
| 16768.4 | 17.956 | 0.923579 | 117.568 | 0.760626 | 82.3939 | 0.340311 | 352.451 | 14.623 | 0.923224 | 482.188 | 7.2611 | 0.675133 | 69.1011 | 128.817 | 264.23 | 76.56434 | 7287.935 |
| 15606.1 | 30.6477 | 0.930055 | 145.251 | 1.35723 | 94.0532 | 0.345543 | 437.093 | 43.3157 | 0.736768 | 146.027 | 59.8239 | 0.41005 | 43.4392 | 397.931 | 66.2847 | 173.6152 | 16145.82 |
| 23200.8 | 26.619 | 0.887817 | 111.664 | 1.72103 | 62.6118 | 0.240745 | 275.734 | 6.91985 | 0.389771 | 434.349 | 69.2803 | 0.926543 | 106.834 | 214.755 | 380.684 | 191.3426 | 16234.56 |
| 34394.5 | 33.2445 | 0.825578 | 86.1048 | 1.72752 | 88.1769 | 0.319481 | 342.828 | 73.9384 | 0.805711 | 211.437 | 59.7787 | 0.47603 | 121.572 | 315.716 | 99.2199 | 171.7789 | 13610.89 |
| 23584.3 | 31.1972 | 0.885689 | 98.0136 | 0.242473 | 27.4236 | 0.36261 | 406.824 | 93.6554 | 0.487365 | 505.642 | 30.8328 | 0.514456 | 21.5452 | 389.102 | 294.689 | 205.8896 | 14453.82 |
| 38366.3 | 15.6612 | 0.803477 | 166.434 | 2.20303 | 78.7754 | 0.408666 | 438.918 | 57.1903 | 0.776821 | 446.655 | 38.5715 | 0.47814 | 123.436 | 251.283 | 400.086 | 170.4196 | 11959.18 |
| 47815 | 16.5532 | 0.750936 | 46.8539 | 0.663117 | 46.49 | 0.47103 | 367.345 | 19.1559 | 0.609192 | 98.3582 | 34.0904 | 0.83176 | 46.4628 | 330.335 | 76.1021 | 87.8314 | 5564.665 |
| 23022 | 23.7998 | 0.888809 | 107.369 | 2.60628 | 3.04727 | 0.171684 | 114.134 | 27.0984 | 0.584505 | 362.832 | 94.2521 | 0.716218 | 79.6768 | 95.2093 | 134.51 | 196.1178 | 12853.76 |
| 38469.5 | 16.4893 | 0.802904 | 121.894 | 2.67292 | 67.3344 | 0.359112 | 189.648 | 74.2006 | 0.80738 | 310.041 | 25.4067 | 0.676875 | 158.647 | 72.7778 | 81.8768 | 109.1168 | 7895.432 |
| 39501.6 | 24.6429 | 0.797169 | 114.833 | 0.104842 | 35.8477 | 0.415569 | 432.444 | 68.3307 | 0.932085 | 218.938 | 26.4547 | 0.657226 | 5.15977 | 215.061 | 78.7338 | 108.777 | 6821.328 |
| 20729.4 | 28.6631 | 0.901563 | 57.5389 | 0.179895 | 48.1204 | 0.515385 | 445.356 | 95.1086 | 0.681484 | 479.405 | 45.0583 | 0.265673 | 13.4968 | 231.508 | 327.407 | 187.6325 | 13637.26 |
| 12534.3 | 23.08 | 0.947128 | 118.054 | 0.453694 | 40.3342 | 0.540802 | 446.395 | 9.79541 | 0.433982 | 452.299 | 84.9429 | 0.505908 | 35.4595 | 337.776 | 180.491 | 123.8957 | 10112.99 |
| 33088.5 | 28.123 | 0.832834 | 115.598 | 1.01463 | 32.3249 | 0.439421 | 104.598 | 85.1494 | 0.513912 | 237.396 | 62.0548 | 0.604347 | 4.64961 | 76.15 | 224.804 | 153.7348 | 10029.5 |
| 19306.8 | 13.3092 | 0.909461 | 23.7864 | 1.40378 | 57.9915 | 0.15878 | 97.8326 | 65.05 | 0.697542 | 417.58 | 99.524 | 0.963913 | 99.8179 | 83.3076 | 311.343 | 159.8314 | 14144.73 |
| 49011.8 | 21.0912 | 0.744283 | 132.88 | 1.0474 | 85.8046 | 0.582818 | 450.729 | 84.9405 | 0.364992 | 380.318 | 80.5527 | 0.988503 | 52.9568 | 156.205 | 251.883 | 133.3137 | 8277.599 |
| 49236.3 | 30.3923 | 0.743041 | 154.639 | 0.486042 | 5.42265 | 0.699832 | 84.2958 | 72.1788 | 0.964201 | 369.943 | 44.2233 | 0.736586 | 40.6391 | 73.7305 | 161.051 | 69.2586 | 3827.856 |
| 38295.6 | 33.1559 | 0.803884 | 83.9969 | 0.297529 | 46.407 | 0.339664 | 229.245 | 48.7079 | 0.358907 | 152.904 | 18.7421 | 0.953802 | 4.70988 | 195.468 | 68.8344 | 188.5821 | 12709.75 |
| 20679.7 | 31.3668 | 0.901842 | 125.123 | 0.510597 | 74.6738 | 0.593777 | 494.712 | 38.9676 | 0.576261 | 310.458 | 76.6995 | 0.768874 | 48.1913 | 458.518 | 139.608 | 72.85054 | 5640.179 |
| 19337.3 | 34.6358 | 0.909312 | 87.6696 | 0.897571 | 26.4565 | 0.309128 | 116.856 | 68.3741 | 0.64016 | 201.472 | 36.0762 | 0.487566 | 26.8991 | 94.6984 | 88.914 | 155.4226 | 11684.62 |
| 54437.4 | 18.4543 | 0.714111 | 166.246 | 0.418256 | 80.1836 | 0.681473 | 458.429 | 20.6425 | 0.969922 | 427.287 | 99.5965 | 0.737584 | 4.76021 | 344.386 | 265.653 | 77.45197 | 4544.096 |
| 36041.3 | 21.3499 | 0.816409 | 71.9413 | 0.446658 | 23.921 | 0.505603 | 452.66 | 47.2002 | 0.778099 | 402.507 | 14.5153 | 0.471178 | 25.059 | 312.746 | 58.4776 | 103.3205 | 6467.473 |
| 36583.3 | 32.5887 | 0.813405 | 104.248 | 0.407247 | 25.1977 | 0.512413 | 374.783 | 22.5141 | 0.732291 | 507.969 | 43.7534 | 0.270887 | 19.8238 | 352.634 | 388.763 | 215.5169 | 13252.38 |
| 22228.1 | 24.935 | 0.893224 | 83.0839 | 0.236458 | 61.712 | 0.238126 | 84.4512 | 26.935 | 0.386913 | 324.368 | 74.5806 | 0.814311 | 2.59565 | 53.0932 | 170.378 | 237.4116 | 19845.88 |
| 17190.5 | 26.3365 | 0.921239 | 87.6324 | 2.84242 | 26.567 | 0.210787 | 185.902 | 62.1922 | 0.772971 | 206.055 | 70.9183 | 0.987061 | 153.137 | 81.4796 | 68.3168 | 94.89559 | 7506.954 |
| 34394.8 | 17.47 | 0.825563 | 31.3299 | 0.314248 | 34.0052 | 0.496146 | 359.366 | 91.7895 | 0.697822 | 145.258 | 50.0178 | 0.384741 | 19.2919 | 125.423 | 110.129 | 160.9913 | 10126 |
| 19379.2 | 22.5906 | 0.909064 | 131.36 | 2.13127 | 43.0533 | 0.402032 | 367.483 | 59.6224 | 0.996991 | 235.545 | 9.00894 | 0.227504 | 154.928 | 235.457 | 98.0201 | 186.4205 | 14232.13 |
| 42358.4 | 21.2662 | 0.781281 | 163.448 | 1.14172 | 21.0855 | 0.334919 | 482.561 | 80.2452 | 0.610027 | 184.352 | 73.4026 | 0.655687 | 12.9892 | 119.772 | 131.495 | 208.0859 | 12242.94 |
| 40223.7 | 17.8917 | 0.79315 | 149.566 | 1.76761 | 5.12955 | 0.536108 | 155.777 | 21.5773 | 0.538819 | 500.552 | 84.4608 | 0.696543 | 134.582 | 95.3948 | 217.412 | 115.0415 | 6607.729 |
| 34421.5 | 20.173 | 0.825416 | 71.0363 | 2.15067 | 86.8402 | 0.412663 | 114.12 | 48.4326 | 0.295107 | 180.734 | 62.4996 | 0.960417 | 123.707 | 66.6615 | 138.822 | 164.1287 | 12783.17 |
| 29965.5 | 21.0868 | 0.850195 | 73.8197 | 3.31333 | 2.18408 | 0.469972 | 321.832 | 60.7379 | 0.372374 | 403.483 | 30.1787 | 0.714219 | 125.746 | 81.0102 | 193.043 | 127.6783 | 7826.56 |
| 42404.8 | 23.7588 | 0.781025 | 156.572 | 2.03725 | 40.707 | 0.557033 | 227.577 | 2.54462 | 0.342816 | 361.539 | 78.4974 | 0.865913 | 120.138 | 137.856 | 212.854 | 147.8943 | 9024.616 |
| 42475.4 | 21.6022 | 0.780631 | 135.725 | 1.67338 | 68.3082 | 0.363212 | 176.441 | 93.6271 | 0.491253 | 249.559 | 9.71611 | 0.565014 | 81.5826 | 158.192 | 219.88 | 245.3779 | 16742.71 |
| 44272 | 20.996 | 0.770639 | 136.863 | 1.10641 | 80.3809 | 0.475803 | 222.781 | 11.3249 | 0.34874 | 230.897 | 48.2061 | 0.99546 | 33.5688 | 183.308 | 46.6642 | 155.4916 | 10512.52 |
| 42400.1 | 31.0478 | 0.781057 | 98.3848 | 1.48943 | 39.341 | 0.472367 | 112.726 | 46.3462 | 0.673803 | 498.261 | 20.7145 | 0.298786 | 53.7566 | 106.345 | 243.211 | 224.7482 | 13974.04 |
| 38228.2 | 29.8719 | 0.804255 | 152.29 | 1.97432 | 36.1328 | 0.59288 | 312.739 | 53.0015 | 0.442825 | 457.96 | 50.1793 | 0.977379 | 151.887 | 184.379 | 306.153 | 90.97943 | 5609.011 |
| 13926.6 | 29.0922 | 0.939392 | 166.998 | 1.22093 | 50.3788 | 0.55896 | 68.6815 | 55.2104 | 0.796364 | 249.567 | 78.2974 | 0.192187 | 89.1195 | 44.3403 | 239.227 | 220.1645 | 17033.1 |
| 31872.9 | 18.3095 | 0.839587 | 158.695 | 0.838658 | 81.4252 | 0.4277 | 329.148 | 12.8308 | 0.863614 | 112.914 | 13.616 | 0.788581 | 63.6375 | 199.953 | 57.1653 | 81.31302 | 6184.699 |
| 29058.1 | 28.8058 | 0.855248 | 74.9181 | 1.02237 | 62.0258 | 0.52276 | 516.763 | 88.9494 | 0.97421 | 353.576 | 10.2106 | 0.293387 | 59.9897 | 371.54 | 309.676 | 169.2966 | 11513.73 |
| 41252.3 | 30.5332 | 0.787439 | 100.66 | 1.67742 | 28.2939 | 0.465279 | 205.929 | 73.2511 | 0.725917 | 162.064 | 54.8738 | 0.300452 | 12.1386 | 165.074 | 160.627 | 213.858 | 12929 |
| 17678.4 | 24.6551 | 0.918525 | 143.801 | 0.204229 | 37.7652 | 0.423654 | 387.322 | 18.5006 | 0.914158 | 397.26 | 34.939 | 0.454004 | 9.26037 | 304.908 | 390.388 | 110.74 | 8526.499 |
| 10892.6 | 27.0376 | 0.956262 | 149.599 | 1.47064 | 29.0556 | 0.353096 | 154.025 | 58.7512 | 0.968988 | 202.84 | 57.0944 | 0.26996 | 144.524 | 102.238 | 192.477 | 170.4915 | 13706.92 |
| 46000 | 24.6948 | 0.761033 | 42.4292 | 3.799 | 22.3734 | 0.6311 | 404.602 | 68.6357 | 0.946392 | 366.271 | 96.6133 | 0.855125 | 66.5782 | 315.95 | 332.595 | 68.84508 | 3953.466 |
| 28428.7 | 18.0152 | 0.858739 | 157.056 | 0.895679 | 12.8408 | 0.644208 | 240.744 | 62.289 | 0.685951 | 287.34 | 3.63602 | 0.804722 | 22.8353 | 226.451 | 108.814 | 60.92284 | 3949.407 |
| 43421.6 | 29.8486 | 0.775375 | 62.8029 | 0.148678 | 44.3211 | 0.504912 | 140.771 | 11.4117 | 0.406653 | 380.722 | 91.0458 | 0.808035 | 10.2356 | 53.9287 | 308.535 | 139.0118 | 8692.662 |
| 33616.6 | 18.7584 | 0.82989 | 162.668 | 2.37468 | 94.2268 | 0.536363 | 329.543 | 61.87 | 0.223182 | 78.8307 | 8.39551 | 0.897384 | 142.264 | 279.97 | 73.2091 | 209.9045 | 15276.91 |
| 18916 | 19.137 | 0.911637 | 26.6083 | 3.58419 | 41.2752 | 0.353588 | 513.403 | 66.8956 | 0.546991 | 113.775 | 49.1704 | 0.631037 | 19.9368 | 236.762 | 99.4402 | 119.1215 | 9555.668 |
| 23886.6 | 25.6615 | 0.884003 | 104.318 | 1.5064 | 48.4481 | 0.510485 | 121.149 | 4.59125 | 0.352398 | 356.134 | 28.2413 | 0.37779 | 90.8029 | 68.6064 | 298.904 | 237.781 | 17191.7 |
| 23319.4 | 33.6635 | 0.887166 | 77.0784 | 2.83141 | 95.7852 | 0.418623 | 198.761 | 87.5413 | 0.317533 | 465.175 | 36.9727 | 0.814612 | 36.4007 | 143.887 | 356.698 | 156.6608 | 13738.46 |
| 42677.2 | 16.5405 | 0.779506 | 144.699 | 0.773729 | 43.3946 | 0.673285 | 378.836 | 16.7998 | 0.774716 | 258.188 | 26.1915 | 0.793302 | 28.2894 | 349.228 | 139.929 | 68.53316 | 4158.973 |
| 48922.1 | 18.6597 | 0.744781 | 75.5268 | 0.2546 | 66.1659 | 0.299338 | 107.846 | 9.69178 | 0.938832 | 483.42 | 75.2118 | 0.386476 | 3.31664 | 55.0086 | 388.005 | 232.0228 | 15585.75 |
| 28655.8 | 32.5649 | 0.857489 | 51.113 | 3.64069 | 0.833793 | 0.424607 | 64.5328 | 31.9784 | 0.920118 | 146.19 | 70.0582 | 0.848032 | 12.4094 | 52.226 | 74.0988 | 50.51351 | 3230.13 |
| 18719.1 | 28.0774 | 0.91274 | 78.9445 | 1.41028 | 8.07694 | 0.356163 | 322.834 | 54.27 | 0.47489 | 422.823 | 25.8988 | 0.612601 | 123.141 | 93.5932 | 302.646 | 127.1463 | 8958.813 |
| 44332.4 | 23.4798 | 0.770305 | 117.208 | 0.112137 | 19.1336 | 0.497864 | 469.902 | 57.6825 | 0.89491 | 516.877 | 47.6512 | 0.460484 | 9.50193 | 106.254 | 278.438 | 143.3131 | 8215.837 |
| 49164.3 | 30.155 | 0.743441 | 123.044 | 1.6376 | 20.969 | 0.304194 | 514.786 | 64.1892 | 0.70221 | 333.745 | 92.8211 | 0.7353 | 153.428 | 376.784 | 120.499 | 161.5599 | 9308.78 |
| 49259 | 17.2617 | 0.742907 | 63.5731 | 0.436571 | 13.6673 | 0.441017 | 193.308 | 24.0843 | 0.763945 | 439.451 | 82.3358 | 0.713183 | 40.3694 | 56.6579 | 199.147 | 92.56446 | 5264.93 |
| 44226.3 | 25.8299 | 0.770897 | 34.9908 | 2.09123 | 37.9707 | 0.467908 | 314.131 | 79.9201 | 0.504585 | 400.029 | 46.8264 | 0.687505 | 128.353 | 161.824 | 304.48 | 132.5236 | 8175.518 |
| 55076.7 | 25.768 | 0.71056 | 63.1879 | 1.94199 | 61.2164 | 0.248273 | 187.812 | 89.0125 | 0.821776 | 82.9491 | 26.2013 | 0.567431 | 112.151 | 44.9449 | 58.5773 | 222.3955 | 14488.06 |
| 30196.6 | 28.2706 | 0.848916 | 30.7639 | 0.334522 | 94.1731 | 0.437673 | 447.846 | 68.3402 | 0.543801 | 196.083 | 65.8948 | 0.420749 | 3.58393 | 93.8286 | 126.451 | 192.2729 | 15420.37 |
| 17701.7 | 23.8551 | 0.918394 | 113.692 | 0.287815 | 91.4408 | 0.205031 | 92.038 | 50.0803 | 0.763825 | 497.998 | 40.347 | 0.641583 | 6.33066 | 86.1569 | 484.171 | 192.4436 | 18178.27 |
| 41180.4 | 31.6308 | 0.78784 | 128.096 | 2.4095 | 82.537 | 0.323085 | 286.339 | 16.7898 | 0.699696 | 277.706 | 1.21016 | 0.51728 | 121.754 | 123.718 | 48.1026 | 195.3861 | 14543.79 |
| 32182.7 | 33.3512 | 0.837877 | 135.442 | 0.984741 | 38.8692 | 0.549582 | 395.855 | 89.034 | 0.856471 | 366.703 | 3.46304 | 0.533036 | 77.7303 | 129.254 | 321.276 | 93.65213 | 6131.059 |
| 31285 | 26.2334 | 0.842862 | 121.92 | 3.44911 | 11.5059 | 0.351943 | 222.275 | 47.8993 | 0.934014 | 299.542 | 85.5586 | 0.38764 | 130.476 | 198.723 | 47.1422 | 140.2664 | 8788.376 |
| 32287.6 | 20.654 | 0.837282 | 86.8145 | 1.56868 | 24.5601 | 0.401298 | 261.279 | 59.4019 | 0.773164 | 505.465 | 12.0115 | 0.50711 | 95.1123 | 102.68 | 211.195 | 111.8363 | 7384.231 |
| 29250.7 | 28.4728 | 0.854176 | 94.3984 | 1.07749 | 15.0073 | 0.333885 | 439.133 | 16.0815 | 0.77088 | 356.767 | 64.0863 | 0.778145 | 22.4803 | 227.613 | 179.197 | 84.49859 | 5628.404 |
| 51243.5 | 27.4375 | 0.731877 | 31.6875 | 3.69001 | 67.1033 | 0.529344 | 250.299 | 36.653 | 0.861572 | 495.072 | 67.1059 | 0.544605 | 197.883 | 168.5 | 385.747 | 109.4742 | 6630.224 |
| 25808.3 | 25.9815 | 0.873316 | 120.953 | 1.32817 | 85.5998 | 0.367548 | 343.127 | 0.517733 | 0.981924 | 236.228 | 77.842 | 0.947936 | 88.6758 | 43.5131 | 139.233 | 66.2998 | 5616.279 |
| 27057.3 | 31.774 | 0.866377 | 146.277 | 1.69005 | 60.5789 | 0.558482 | 477.834 | 35.3371 | 0.785057 | 74.5637 | 5.54247 | 0.425316 | 65.3024 | 229.266 | 48.0569 | 105.9461 | 7674.667 |
| 54864.1 | 23.4718 | 0.711741 | 41.2352 | 3.34306 | 59.183 | 0.336694 | 404.873 | 28.5322 | 0.9342 | 366.134 | 34.6952 | 0.785206 | 13.8102 | 161.67 | 211.289 | 98.54428 | 6435.655 |
| 40980.4 | 14.0801 | 0.78894 | 66.753 | 2.763 | 98.2163 | 0.381838 | 444.153 | 6.41765 | 0.605548 | 453.145 | 80.4362 | 0.646745 | 122.452 | 167.348 | 340.002 | 140.8158 | 10944.1 |
| 37710.5 | 13.7459 | 0.807123 | 143.375 | 1.21693 | 82.508 | 0.540673 | 272.276 | 84.933 | 0.568835 | 388.525 | 67.3463 | 0.867106 | 76.2088 | 238.041 | 339.319 | 95.37487 | 6563.335 |
| 32637.4 | 20.6381 | 0.835337 | 81.7832 | 1.22294 | 26.4566 | 0.144402 | 262.863 | 49.8828 | 0.947135 | 250.843 | 24.1611 | 0.604356 | 6.05078 | 202.797 | 220.196 | 223.5345 | 15336.99 |
| 35796.4 | 34.0299 | 0.817783 | 165.645 | 2.22131 | 41.8627 | 0.412015 | 256.148 | 87.9549 | 0.726104 | 357.622 | 26.1605 | 0.717422 | 55.0458 | 139.431 | 341.069 | 116.2707 | 7631.47 |
| 50977.5 | 28.9046 | 0.733357 | 144.939 | 3.67629 | 43.1794 | 0.539029 | 251.124 | 33.9203 | 0.812506 | 290.2 | 45.2742 | 0.481967 | 146.753 | 217.115 | 110.989 | 118.7663 | 6917.144 |
| 16542.4 | 21.1025 | 0.924838 | 61.73 | 0.271025 | 18.1534 | 0.302545 | 211.983 | 35.0676 | 0.486005 | 208.62 | 27.7211 | 0.541079 | 26.1831 | 168.8 | 139.234 | 167.4403 | 12721.14 |
| 30009.4 | 28.6172 | 0.849958 | 100.853 | 1.05774 | 68.4545 | 0.516278 | 139.012 | 64.6111 | 0.67245 | 479.389 | 78.8528 | 0.805586 | 27.3939 | 100.61 | 370.286 | 72.20504 | 5231.158 |
| 40677.2 | 16.7211 | 0.790627 | 39.2116 | 1.64778 | 28.3205 | 0.345539 | 190.237 | 90.6322 | 0.581004 | 394.099 | 2.55405 | 0.698828 | 8.82594 | 166.269 | 255.296 | 142.1056 | 8996.669 |
| 58083.7 | 24.0834 | 0.693837 | 139.739 | 1.7453 | 46.9024 | 0.569092 | 181.055 | 32.9472 | 0.724455 | 291.53 | 2.17499 | 0.594793 | 145.204 | 55.7034 | 65.374 | 115.1996 | 6496.823 |
| 55457.6 | 22.2644 | 0.70844 | 147.81 | 3.11395 | 37.1006 | 0.490176 | 253.73 | 57.329 | 0.776304 | 299.453 | 65.065 | 0.565451 | 6.03851 | 48.3585 | 201.81 | 129.8917 | 7433.48 |
| 57342.5 | 19.2422 | 0.697957 | 157.168 | 1.55398 | 48.1119 | 0.274147 | 442.901 | 44.8556 | 0.756221 | 330.792 | 89.0032 | 0.965373 | 73.7227 | 319.247 | 108.758 | 167.6037 | 9976.839 |
| 46721 | 17.7419 | 0.75702 | 167.602 | 0.433719 | 27.5789 | 0.611194 | 102.248 | 52.1717 | 0.639315 | 459.376 | 92.3304 | 0.446586 | 31.4208 | 77.1048 | 202.445 | 191.0544 | 10730.43 |
| 45568.4 | 29.8945 | 0.763437 | 74.2748 | 1.5672 | 65.5629 | 0.323816 | 388.784 | 28.6749 | 0.538199 | 473.681 | 54.2899 | 0.673862 | 4.3421 | 197.916 | 118.798 | 189.4306 | 13167.79 |
| 41663.4 | 28.43 | 0.785151 | 168.519 | 1.60229 | 25.723 | 0.563468 | 116.15 | 25.7306 | 0.74952 | 188.936 | 2.69452 | 0.49206 | 34.2078 | 45.3158 | 94.811 | 126.0851 | 7496.634 |
| 28053.3 | 15.6372 | 0.860825 | 145.189 | 0.839368 | 38.045 | 0.28289 | 358.843 | 68.6766 | 0.863388 | 507.51 | 27.2397 | 0.563723 | 25.4848 | 104.679 | 316.045 | 158.7707 | 11198.96 |
| 10612.6 | 26.5047 | 0.957818 | 74.8428 | 1.87655 | 44.5931 | 0.282579 | 277.993 | 73.1212 | 0.760257 | 438.262 | 74.7183 | 0.708534 | 147.414 | 61.7059 | 257.788 | 86.65426 | 7806.9 |
| 46068.7 | 26.1131 | 0.760652 | 59.077 | 0.136622 | 45.2649 | 0.444951 | 133.584 | 44.066 | 0.551265 | 381.951 | 58.7278 | 0.849847 | 3.91002 | 97.3581 | 87.5736 | 115.0876 | 7229.106 |
| 27345.9 | 33.557 | 0.864775 | 85.1558 | 3.73162 | 93.9858 | 0.417418 | 448.76 | 67.9933 | 0.878549 | 208.267 | 27.4925 | 0.811869 | 113.1 | 65.8334 | 58.5165 | 62.72516 | 5316.71 |
| 45042.1 | 26.3125 | 0.766361 | 109.189 | 2.8254 | 60.5193 | 0.228402 | 153.364 | 94.4295 | 0.81245 | 274.285 | 53.4188 | 0.978246 | 103.588 | 81.4193 | 94.0872 | 141.8712 | 9921.33 |
| 26741.4 | 27.5151 | 0.868129 | 135.764 | 1.97373 | 31.5024 | 0.346227 | 421.676 | 82.4812 | 0.476317 | 349.625 | 76.9137 | 0.517358 | 99.0741 | 269.327 | 126.809 | 220.3492 | 15303 |
| 40759.3 | 27.2706 | 0.790178 | 90.0325 | 1.96066 | 42.5629 | 0.432501 | 98.6499 | 6.1754 | 0.800483 | 404.854 | 88.2715 | 0.816072 | 96.1128 | 85.8406 | 57.3587 | 72.11669 | 4791.543 |
| 48567.9 | 15.9416 | 0.746749 | 109.667 | 0.790024 | 83.4875 | 0.450961 | 407.665 | 46.0592 | 0.289122 | 66.1196 | 85.2625 | 0.997541 | 42.6597 | 188.066 | 51.3671 | 199.866 | 13365.45 |
| 14505.3 | 15.0693 | 0.936162 | 111.764 | 0.753079 | 4.23179 | 0.511644 | 457.325 | 63.2936 | 0.904892 | 445.053 | 28.5685 | 0.954912 | 74.4521 | 283.844 | 294.059 | 33.27522 | 2527.614 |
| 35587.9 | 17.8904 | 0.818929 | 137.613 | 2.38743 | 98.185 | 0.499185 | 306.951 | 26.8303 | 0.653025 | 337.238 | 35.4502 | 0.604076 | 138.045 | 165.122 | 318.595 | 108.1933 | 8152.181 |
| 41013.7 | 23.7467 | 0.78876 | 73.9144 | 1.42974 | 37.9253 | 0.430397 | 284.506 | 95.0943 | 0.840887 | 484.367 | 4.63007 | 0.598005 | 38.3843 | 212.731 | 335.38 | 98.90196 | 6352.585 |
| 43804.7 | 32.9001 | 0.773248 | 160.748 | 1.19147 | 75.3889 | 0.634708 | 135.073 | 41.6201 | 0.525073 | 168.618 | 59.1825 | 0.524986 | 108.188 | 61.473 | 79.3799 | 164.1184 | 10135.62 |
| 45426.1 | 34.4504 | 0.764233 | 166.246 | 3.43491 | 58.9006 | 0.445525 | 114.133 | 43.5914 | 0.991232 | 315.878 | 50.1141 | 0.423576 | 159.772 | 75.0907 | 313.159 | 146.5379 | 9304.952 |
| 33175.9 | 15.5177 | 0.83234 | 156.897 | 2.64712 | 93.7783 | 0.596896 | 399.245 | 30.2248 | 0.632168 | 461.513 | 87.9397 | 0.563598 | 236.784 | 283.283 | 304.637 | 118.3961 | 8072.589 |
| 31677.2 | 29.8027 | 0.840684 | 157.236 | 0.126778 | 43.2995 | 0.709715 | 491.24 | 36.4329 | 0.525626 | 245.589 | 86.121 | 0.912105 | 7.07507 | 165.894 | 117.692 | 84.67585 | 5413.839 |
| 26042 | 14.3771 | 0.872009 | 51.4068 | 1.00114 | 69.4715 | 0.487912 | 176.4 | 58.223 | 0.348326 | 347.689 | 29.8717 | 0.537661 | 21.0986 | 157.668 | 162.634 | 190.4034 | 14281.59 |
| 19030.9 | 32.902 | 0.911013 | 117.002 | 2.56372 | 86.1967 | 0.455189 | 455.279 | 24.1024 | 0.787435 | 453.249 | 15.2521 | 0.973377 | 55.747 | 401.706 | 289.482 | 41.88323 | 3962.26 |
| 32591.9 | 33.2327 | 0.835602 | 34.1778 | 1.78317 | 61.3709 | 0.483787 | 214.941 | 20.2758 | 0.650516 | 278.251 | 59.4967 | 0.719077 | 106.515 | 102.425 | 47.6033 | 80.36644 | 5805.493 |
| 25075.5 | 15.533 | 0.877384 | 39.7289 | 0.756284 | 29.4955 | 0.469279 | 290.731 | 37.1874 | 0.985715 | 225.535 | 49.1607 | 0.676695 | 65.9272 | 265.72 | 90.5992 | 50.68418 | 3655.88 |
| 49372.6 | 25.704 | 0.742279 | 43.3697 | 0.576755 | 63.9902 | 0.524374 | 118.345 | 79.1144 | 0.943254 | 430.855 | 38.7094 | 0.507932 | 28.9402 | 105.497 | 236.99 | 111.1798 | 6786.754 |
| 23892.5 | 21.9529 | 0.883967 | 123.907 | 0.669461 | 48.8337 | 0.522126 | 479.61 | 13.7401 | 0.717169 | 126.378 | 34.37 | 0.77874 | 63.9193 | 233.711 | 121.71 | 61.12618 | 4647.551 |
| 21921.5 | 34.1371 | 0.89494 | 43.2234 | 1.723 | 37.7637 | 0.499167 | 291.63 | 15.1556 | 0.817122 | 353.582 | 48.6932 | 0.838632 | 60.4331 | 75.2067 | 135.679 | 43.49901 | 3312.221 |
| 28209.6 | 21.9568 | 0.85996 | 168.183 | 0.397877 | 26.9485 | 0.371406 | 400.526 | 20.2122 | 0.391199 | 236.405 | 40.9989 | 0.673339 | 1.13916 | 277.23 | 223.463 | 249.6033 | 16548.05 |
| 31046.1 | 29.8628 | 0.844194 | 114.087 | 0.311477 | 36.5771 | 0.292658 | 322.353 | 91.0171 | 0.700082 | 298.797 | 66.5865 | 0.860081 | 6.69802 | 181.263 | 237.792 | 129.5794 | 8862.972 |
| 13583.2 | 34.6819 | 0.94131 | 137.675 | 2.41319 | 31.6674 | 0.200803 | 93.0842 | 36.8644 | 0.864158 | 131.563 | 16.4367 | 0.812849 | 77.3064 | 41.4652 | 59.1145 | 106.5772 | 9090.627 |
| 19106.8 | 20.417 | 0.910577 | 140.961 | 0.350094 | 67.0847 | 0.588672 | 282.076 | 26.8847 | 0.371686 | 298.632 | 92.0861 | 0.952256 | 3.04403 | 158.883 | 108.982 | 95.14877 | 7386.638 |
| 31232.7 | 31.3834 | 0.843158 | 77.0778 | 1.18583 | 54.1929 | 0.201956 | 98.3104 | 36.3 | 0.767485 | 368.421 | 45.7617 | 0.874277 | 116.939 | 69.8424 | 293.103 | 134.7377 | 10480.33 |
| 22992.8 | 25.5844 | 0.888973 | 69.2413 | 3.4336 | 69.8816 | 0.32328 | 443.522 | 28.732 | 0.860464 | 348.358 | 63.5468 | 0.997961 | 112.421 | 343.136 | 188.185 | 63.94492 | 5548.928 |
| 23009.6 | 19.7845 | 0.888874 | 146.816 | 0.463924 | 11.3461 | 0.322857 | 345.905 | 96.5865 | 0.939547 | 494.988 | 34.3974 | 0.554896 | 7.29018 | 200.33 | 364.185 | 128.3143 | 8528.868 |
| 13601 | 34.3405 | 0.941211 | 79.0718 | 1.34617 | 15.7419 | 0.373379 | 332.562 | 75.3899 | 0.535022 | 121.742 | 82.5247 | 0.844245 | 89.6 | 150.859 | 91.9479 | 77.93979 | 5961.218 |
| 16264.8 | 23.2106 | 0.926384 | 49.3477 | 1.24071 | 92.2115 | 0.333567 | 247.62 | 53.5765 | 0.645153 | 422.189 | 43.9341 | 0.754128 | 41.9773 | 150.142 | 389.397 | 93.63949 | 9204.081 |
| 32597 | 27.229 | 0.835567 | 132.718 | 3.36068 | 38.9586 | 0.378826 | 364.584 | 41.076 | 0.446249 | 436.047 | 29.4735 | 0.784503 | 71.6654 | 196.334 | 318.867 | 138.6423 | 9624.834 |
| 37117.9 | 20.7478 | 0.810422 | 144.821 | 2.56303 | 40.5626 | 0.277692 | 247.015 | 46.8996 | 0.783571 | 61.7031 | 47.1429 | 0.882471 | 77.785 | 75.7889 | 48.6908 | 113.6167 | 7725.813 |
| 34598.7 | 18.0365 | 0.824429 | 97.7765 | 0.512317 | 56.4953 | 0.3078 | 460.297 | 17.5126 | 0.943753 | 201.466 | 65.0385 | 0.696557 | 11.0268 | 374.059 | 67.1248 | 104.3349 | 7622.521 |
| 33999.6 | 34.4101 | 0.827775 | 105.539 | 1.68781 | 71.6353 | 0.310481 | 501.733 | 93.4976 | 0.991715 | 466.544 | 54.7445 | 0.890034 | 59.627 | 340.894 | 150.015 | 91.9218 | 6963.349 |
| 48213.7 | 16.5353 | 0.748719 | 91.7934 | 2.08489 | 33.3993 | 0.285482 | 189.158 | 35.9009 | 0.943603 | 307.385 | 23.6917 | 0.83547 | 10.6997 | 91.3869 | 157.776 | 97.80613 | 6174.814 |
| 26129.6 | 21.6847 | 0.871526 | 77.251 | 2.75237 | 75.3164 | 0.274465 | 111.442 | 38.2813 | 0.916302 | 475.971 | 87.4186 | 0.544682 | 82.4527 | 54.8149 | 208.054 | 130.7165 | 11071.45 |
| 39468.4 | 30.5405 | 0.797359 | 66.5326 | 1.83821 | 8.29154 | 0.323482 | 297.429 | 48.4079 | 0.717617 | 491.241 | 16.0586 | 0.575799 | 120.704 | 234.908 | 264.224 | 142.1695 | 8377.708 |
| 47270 | 31.7404 | 0.753977 | 44.1429 | 1.82882 | 16.7241 | 0.298855 | 393.425 | 79.8224 | 0.519679 | 248.991 | 18.3668 | 0.644779 | 148.465 | 354.366 | 49.2145 | 216.7458 | 12484.08 |
| 28883.9 | 26.56 | 0.856214 | 31.8792 | 3.76476 | 34.6939 | 0.5781 | 409.067 | 35.6689 | 0.577635 | 482.546 | 65.2596 | 0.919055 | 235.626 | 215.76 | 461.538 | 79.24275 | 5256.983 |
| 12296.8 | 16.0701 | 0.948443 | 87.8499 | 1.66255 | 11.8537 | 0.410155 | 445.187 | 64.7101 | 0.303471 | 486.108 | 48.1739 | 0.924157 | 92.6747 | 267.091 | 366.42 | 100.3709 | 7774.66 |
| 16351.1 | 16.4128 | 0.925899 | 118.83 | 2.08485 | 17.031 | 0.45873 | 238.294 | 51.7547 | 0.794573 | 350.307 | 23.7937 | 0.529984 | 87.6757 | 229.471 | 176.815 | 72.22141 | 5397.727 |
| 15351.2 | 13.4387 | 0.931457 | 121.102 | 2.80162 | 15.4823 | 0.42959 | 433.266 | 74.0658 | 0.900562 | 475.06 | 63.8864 | 0.497554 | 129.203 | 230.333 | 445.955 | 76.20801 | 5582.09 |
| 37916.1 | 14.3423 | 0.80598 | 67.7283 | 2.20422 | 60.2794 | 0.275652 | 467.705 | 5.45454 | 0.91399 | 462.206 | 73.1366 | 0.949184 | 114.435 | 297.04 | 337.874 | 93.40114 | 6970.194 |
| 56011.4 | 20.9415 | 0.705359 | 78.1552 | 0.154686 | 85.6069 | 0.370733 | 351.923 | 35.2056 | 0.528332 | 300.151 | 1.50873 | 0.601185 | 10.1655 | 215.585 | 174.852 | 246.7076 | 16187.76 |
| 11735 | 23.4868 | 0.951574 | 42.7264 | 0.627826 | 77.8433 | 0.168777 | 296.051 | 26.5073 | 0.987587 | 207.77 | 4.69923 | 0.869539 | 46.0674 | 292.185 | 158.901 | 126.3266 | 13566.52 |
| 27090.8 | 32.5439 | 0.866192 | 65.2182 | 3.38418 | 93.6949 | 0.207722 | 129.806 | 51.3909 | 0.980739 | 498.011 | 92.3963 | 0.8082 | 48.5947 | 101.089 | 205.756 | 137.6698 | 12310.45 |
| 28684.4 | 27.472 | 0.857324 | 156.067 | 1.3967 | 52.5624 | 0.463648 | 345.56 | 31.7171 | 0.687503 | 339.025 | 70.4625 | 0.56789 | 48.2167 | 255.664 | 217.468 | 121.2315 | 8602.335 |
| 59612.2 | 21.1387 | 0.685336 | 80.8009 | 1.87443 | 14.8939 | 0.39675 | 354.457 | 25.677 | 0.834542 | 381.779 | 73.5204 | 0.80909 | 60.7632 | 95.3548 | 374.623 | 92.44585 | 5040.557 |
| 23268.1 | 25.893 | 0.887442 | 27.8304 | 0.74304 | 17.5192 | 0.503785 | 491.324 | 46.1912 | 0.951736 | 121.905 | 4.94104 | 0.604065 | 46.2372 | 114.555 | 113.319 | 55.15436 | 3854.962 |
| 53637.2 | 20.2264 | 0.718562 | 116.786 | 3.15252 | 95.1772 | 0.429002 | 448.732 | 26.9172 | 0.978138 | 360.147 | 20.6474 | 0.949275 | 10.1625 | 364.864 | 304.284 | 66.53813 | 4771.061 |
| 22939.3 | 32.8275 | 0.889279 | 127.443 | 3.26777 | 30.2759 | 0.365787 | 292.644 | 10.7023 | 0.744694 | 156.115 | 95.2418 | 0.866648 | 150.317 | 104.268 | 54.7992 | 67.79574 | 5053.252 |
| 49480.1 | 25.8446 | 0.741682 | 26.0055 | 0.258509 | 29.5601 | 0.353256 | 361.028 | 42.5817 | 0.793426 | 244.328 | 79.2865 | 0.481426 | 12.5534 | 55.7607 | 101.066 | 169.4918 | 10093.79 |
| 20890.2 | 30.0676 | 0.90067 | 112.15 | 2.86625 | 3.91507 | 0.524034 | 469.16 | 70.808 | 0.604208 | 274.61 | 85.0474 | 0.909135 | 208.847 | 452.909 | 154.131 | 63.38539 | 4217.304 |
| 39388 | 30.6071 | 0.797806 | 125.258 | 1.48048 | 16.695 | 0.437174 | 149.705 | 58.9072 | 0.984158 | 139.438 | 32.3993 | 0.435663 | 6.51588 | 64.3015 | 126.142 | 122.4978 | 7325.285 |
| 54309.6 | 22.3021 | 0.714824 | 135.906 | 3.03216 | 69.5848 | 0.344487 | 378.146 | 50.5084 | 0.808679 | 102.794 | 7.10065 | 0.559733 | 138.893 | 145.095 | 89.3842 | 170.2207 | 11092.42 |
| 32171.4 | 24.4347 | 0.837931 | 73.1016 | 1.83725 | 42.25 | 0.243321 | 158.895 | 92.0324 | 0.454217 | 297.908 | 27.7317 | 0.703748 | 104.901 | 132.803 | 90.9017 | 231.6951 | 16707.47 |
| 23289.3 | 27.3441 | 0.887326 | 70.6379 | 1.78688 | 67.4711 | 0.327513 | 166.886 | 93.2983 | 0.443859 | 241.332 | 38.4902 | 0.683053 | 67.3264 | 123.282 | 134.834 | 167.034 | 13957.76 |
| 12466.9 | 14.2262 | 0.947496 | 94.0034 | 1.74387 | 24.7486 | 0.265605 | 328.601 | 75.8226 | 0.902001 | 63.2451 | 52.6874 | 0.262689 | 106.394 | 186.313 | 49.7264 | 207.6907 | 16625.65 |
| 31189.9 | 18.2263 | 0.843384 | 56.8164 | 1.85355 | 88.6555 | 0.200373 | 329.227 | 23.9302 | 0.753131 | 407.183 | 45.9947 | 0.704912 | 18.4516 | 125.603 | 260.56 | 178.782 | 15689.6 |
| 14248.9 | 31.8165 | 0.937604 | 146.729 | 0.407609 | 65.981 | 0.448291 | 510.602 | 23.2249 | 0.4771 | 345.691 | 72.6534 | 0.813866 | 10.8541 | 405.602 | 154.57 | 104.9997 | 8979.052 |
| 49187.8 | 24.9104 | 0.743306 | 50.6876 | 1.26162 | 23.0135 | 0.346411 | 109.508 | 26.6213 | 0.658827 | 223.183 | 56.9556 | 0.79457 | 86.7793 | 97.4665 | 211.382 | 120.3447 | 7107.897 |
| 17451.3 | 32.2771 | 0.919796 | 134.597 | 0.985045 | 59.685 | 0.519838 | 250.118 | 63.0876 | 0.8222 | 122.24 | 22.2186 | 0.218793 | 22.4841 | 102.937 | 88.3562 | 195.5324 | 15229.6 |
| 38669.9 | 14.5193 | 0.801789 | 57.1345 | 0.874557 | 45.7375 | 0.393201 | 116.778 | 81.3671 | 0.971882 | 116.899 | 1.78547 | 0.523684 | 60.7987 | 47.8934 | 63.2402 | 104.8672 | 7062.055 |
| 31330 | 14.0937 | 0.842603 | 138.41 | 2.71634 | 17.2411 | 0.426529 | 166.885 | 28.0434 | 0.910306 | 133.65 | 36.2479 | 0.415612 | 144.828 | 79.5015 | 87.6 | 114.5674 | 7367.644 |
| 19838.1 | 20.5531 | 0.906511 | 162.255 | 2.83408 | 55.6736 | 0.271071 | 340.762 | 15.8607 | 0.398913 | 327.687 | 14.0328 | 0.739038 | 117.831 | 100.114 | 257.189 | 216.0506 | 18012.79 |
| 31409 | 34.1651 | 0.842181 | 48.0988 | 1.83948 | 11.9946 | 0.387336 | 420.473 | 3.36806 | 0.239277 | 461.257 | 15.8393 | 0.854679 | 162.745 | 290.816 | 397.589 | 204.6562 | 12946.84 |
| 11427.5 | 14.5607 | 0.953276 | 167.77 | 0.188196 | 72.1113 | 0.362765 | 177.651 | 89.1266 | 0.940236 | 241.884 | 3.82273 | 0.729868 | 7.70068 | 75.0697 | 186.078 | 88.75898 | 7829.702 |
| 12320.4 | 21.4301 | 0.948316 | 152.166 | 0.634285 | 4.94606 | 0.643102 | 255.234 | 46.768 | 0.982213 | 455.256 | 30.1474 | 0.130649 | 26.7399 | 193.423 | 342.973 | 211.94 | 15029.94 |
| 30394.1 | 15.6423 | 0.847808 | 162.24 | 1.01295 | 89.0391 | 0.483158 | 331.096 | 4.93054 | 0.503841 | 85.2936 | 14.9534 | 0.623453 | 92.4095 | 66.9671 | 56.7549 | 151.994 | 11473.43 |
| 27948.4 | 23.6869 | 0.861414 | 106.36 | 2.29457 | 51.5757 | 0.448476 | 404.095 | 90.4909 | 0.521435 | 514.584 | 9.08774 | 0.927497 | 59.1217 | 47.0502 | 346.355 | 78.64328 | 5877.677 |
| 43241.4 | 13.717 | 0.776367 | 96.3883 | 0.363558 | 34.5461 | 0.44791 | 382.486 | 70.0071 | 0.859304 | 234.151 | 35.9929 | 0.76462 | 29.8367 | 68.9884 | 187.205 | 83.14678 | 5178.522 |
| 29872.6 | 31.9051 | 0.850722 | 65.335 | 0.349543 | 34.501 | 0.429698 | 436.622 | 66.9017 | 0.712043 | 316.404 | 64.9508 | 0.362482 | 16.9408 | 301.209 | 301.45 | 169.8877 | 11505.11 |
| 24593.8 | 21.1198 | 0.880066 | 143.874 | 0.679238 | 75.3169 | 0.554439 | 270.54 | 6.26818 | 0.25303 | 332.305 | 9.30627 | 0.761788 | 48.3129 | 59.865 | 194.472 | 185.0924 | 14097.03 |
| 21324.5 | 15.7228 | 0.898242 | 172.238 | 0.408984 | 72.8447 | 0.309024 | 244.819 | 52.2196 | 0.986982 | 496.914 | 72.7055 | 0.821044 | 11.5214 | 177.403 | 266.016 | 122.6574 | 9745.107 |
| 11495.7 | 17.3891 | 0.952899 | 24.7887 | 1.10254 | 53.1364 | 0.223074 | 420.222 | 90.8328 | 0.623946 | 386.29 | 68.138 | 0.634757 | 85.3083 | 139.387 | 116.216 | 151.6315 | 14168.98 |
| 12453.5 | 14.6214 | 0.947571 | 139.029 | 3.08106 | 9.97532 | 0.34298 | 490.731 | 66.2898 | 0.380765 | 107.073 | 72.2132 | 0.392965 | 139.809 | 467.811 | 65.1832 | 249.4606 | 18751.16 |
| 41006.1 | 15.2196 | 0.788797 | 59.1587 | 1.2458 | 98.3297 | 0.425573 | 96.1756 | 14.2332 | 0.293528 | 450.406 | 74.3826 | 0.709213 | 32.6292 | 89.1767 | 338.653 | 234.5929 | 17826.65 |
| 54637 | 21.6643 | 0.713003 | 48.0237 | 0.257675 | 97.7136 | 0.375071 | 180.977 | 56.1619 | 0.744506 | 494.426 | 21.8653 | 0.473846 | 22.8968 | 146.879 | 120.532 | 194.8691 | 13658.12 |
| 42177.5 | 24.3624 | 0.782289 | 140.942 | 0.847286 | 73.7517 | 0.555779 | 367.38 | 84.7407 | 0.289342 | 404.636 | 47.3514 | 0.857691 | 14.9957 | 180.944 | 234.081 | 191.5472 | 12390.96 |
| 29263.9 | 13.4093 | 0.854092 | 50.3656 | 2.75785 | 24.4833 | 0.552071 | 454.454 | 19.576 | 0.953769 | 518.11 | 43.6373 | 0.784113 | 232.147 | 307.499 | 236.003 | 47.46434 | 3206.784 |
| 11597.7 | 25.666 | 0.952339 | 156.633 | 1.97886 | 41.2563 | 0.255688 | 315.053 | 81.2599 | 0.643805 | 97.298 | 8.63148 | 0.428598 | 60.6255 | 231.669 | 71.93 | 220.4064 | 19003.51 |
| 35690.1 | 29.7665 | 0.818369 | 83.0492 | 2.8301 | 7.40202 | 0.304315 | 393.443 | 51.7419 | 0.790421 | 198.284 | 13.7916 | 0.583115 | 145.834 | 59.0629 | 89.4712 | 128.3193 | 7758.133 |
| 33259.1 | 16.2489 | 0.831877 | 144.098 | 3.13509 | 12.185 | 0.466344 | 447.161 | 28.3166 | 0.425795 | 151.59 | 2.83337 | 0.524968 | 108.583 | 154.402 | 104.98 | 176.6304 | 10894.69 |
| 11935.1 | 29.267 | 0.950467 | 111.835 | 1.27111 | 7.83608 | 0.498673 | 507.187 | 83.4163 | 0.456006 | 130.984 | 15.4145 | 0.276542 | 48.2209 | 75.2965 | 109.479 | 210.5155 | 15427.48 |
| 20605.7 | 24.4455 | 0.902246 | 172.919 | 1.74149 | 98.0535 | 0.57132 | 297.462 | 39.2045 | 0.758151 | 358.388 | 15.0065 | 0.763347 | 30.1636 | 216.919 | 87.9761 | 60.60257 | 5069.176 |
| 28430.6 | 32.6138 | 0.858742 | 171.528 | 0.677998 | 32.4911 | 0.513285 | 459.364 | 52.8143 | 0.304206 | 172.87 | 13.6889 | 0.956118 | 54.0176 | 344.816 | 158.425 | 160.9043 | 10688.52 |
| 39836.3 | 28.5119 | 0.795311 | 144.878 | 2.6013 | 9.91586 | 0.294923 | 447.299 | 84.1316 | 0.950486 | 124.057 | 55.2641 | 0.5799 | 84.6322 | 351.934 | 119.69 | 142.665 | 8352.932 |
| 38745.8 | 16.9365 | 0.801368 | 65.7526 | 0.863932 | 4.17783 | 0.303004 | 442.845 | 8.30956 | 0.834955 | 406.946 | 49.7559 | 0.980191 | 44.718 | 126.909 | 322.288 | 74.51733 | 4454.828 |
| 29013.5 | 23.1103 | 0.855491 | 117.575 | 1.95257 | 70.75 | 0.379815 | 280.817 | 22.6808 | 0.297774 | 508.907 | 2.66183 | 0.671854 | 143.233 | 188.236 | 329.366 | 237.4549 | 18695.56 |
| 15676.8 | 31.1627 | 0.929663 | 110.948 | 0.880366 | 79.1355 | 0.39257 | 195.75 | 4.77878 | 0.605154 | 463.905 | 1.4095 | 0.381607 | 60.9202 | 111.646 | 72.2241 | 168.9389 | 15686.11 |
| 43406.6 | 21.3189 | 0.775452 | 132.546 | 0.142625 | 76.1667 | 0.484574 | 430.002 | 74.0662 | 0.759349 | 440.368 | 45.7224 | 0.821668 | 6.74852 | 332.258 | 417.968 | 103.0839 | 6736.98 |
| 10727.7 | 28.5302 | 0.95718 | 128.203 | 1.64769 | 3.06966 | 0.172837 | 507.541 | 61.7824 | 0.605526 | 496.512 | 20.2701 | 0.838643 | 140.425 | 198.555 | 74.7077 | 139.1321 | 10639.24 |
| 17848.6 | 15.5876 | 0.917571 | 33.6772 | 2.50588 | 83.7459 | 0.2892 | 113.616 | 78.8911 | 0.861639 | 373.971 | 50.1801 | 0.479255 | 30.14 | 66.6158 | 309.615 | 137.0002 | 12736.16 |
| 52910.7 | 24.2551 | 0.722604 | 33.1161 | 3.68665 | 52.5465 | 0.527904 | 399.379 | 29.9816 | 0.728047 | 445.736 | 5.65945 | 0.441032 | 178.06 | 246.225 | 344.543 | 164.7637 | 9602.386 |
| 20067.1 | 23.9553 | 0.905241 | 154.203 | 1.06273 | 51.7766 | 0.302527 | 195.806 | 9.83238 | 0.881861 | 392.581 | 51.3327 | 0.432816 | 75.786 | 75.6741 | 58.6907 | 163.3776 | 13107.61 |
| 17365 | 26.2427 | 0.920269 | 135.707 | 1.87186 | 81.8462 | 0.433997 | 294.692 | 51.6539 | 0.870694 | 203.623 | 91.6157 | 0.411784 | 143.691 | 184.292 | 46.2402 | 115.3531 | 9854.329 |
| 25688.6 | 17.0487 | 0.873976 | 110.741 | 2.35917 | 58.8644 | 0.542006 | 368.936 | 47.6472 | 0.725835 | 411.095 | 81.7919 | 0.504926 | 80.5547 | 133.917 | 326.78 | 119.4159 | 8427.142 |
| 12284.2 | 32.3545 | 0.94853 | 164.298 | 0.156995 | 59.3225 | 0.893129 | 488.072 | 14.4471 | 0.997833 | 314.075 | 52.8642 | 0.650636 | 15.0173 | 223.841 | 268.044 | 45.45398 | 3500.503 |
| 38380.7 | 26.5433 | 0.803404 | 45.6353 | 3.53395 | 23.9582 | 0.503299 | 388.519 | 20.6785 | 0.773807 | 185.271 | 38.0928 | 0.443954 | 134.277 | 195.363 | 96.992 | 114.23 | 6964.767 |
| 33217.1 | 30.2119 | 0.832122 | 124.274 | 3.29722 | 81.8348 | 0.26907 | 161.075 | 33.0275 | 0.874121 | 395.362 | 40.9693 | 0.842699 | 42.8606 | 105.42 | 196.16 | 100.7088 | 8294.406 |
| 46327.4 | 14.5266 | 0.759207 | 84.2341 | 1.88848 | 45.5803 | 0.440818 | 231.663 | 80.5836 | 0.904145 | 159.536 | 44.4588 | 0.707056 | 128.274 | 114.09 | 125.443 | 81.51535 | 5176.129 |
| 15274.2 | 24.1345 | 0.931893 | 146.301 | 0.236683 | 30.4937 | 0.27725 | 231.308 | 31.887 | 0.882908 | 268.579 | 30.7487 | 0.859964 | 22.6532 | 122.009 | 164.081 | 101.7192 | 8075.237 |
| 25180.8 | 26.9522 | 0.876807 | 124.807 | 2.16646 | 1.28924 | 0.328893 | 449.817 | 30.2725 | 0.268189 | 412.96 | 52.9276 | 0.907068 | 58.6028 | 331.202 | 291.511 | 194.618 | 12370.22 |
| 24669.5 | 28.5553 | 0.879652 | 110.981 | 0.419288 | 59.8678 | 0.532895 | 312.455 | 28.8497 | 0.455007 | 192.517 | 74.4063 | 0.706242 | 4.99002 | 105.001 | 176.758 | 111.9186 | 8340.008 |
| 21780.9 | 26.5314 | 0.895713 | 148.882 | 3.63651 | 14.9378 | 0.295824 | 276.223 | 75.7932 | 0.901471 | 370.652 | 24.2822 | 0.947079 | 114.917 | 247.059 | 362.356 | 73.07102 | 5188.392 |
| 33794.4 | 32.2624 | 0.828914 | 139.647 | 3.61635 | 95.7183 | 0.4199 | 289.642 | 67.7147 | 0.561969 | 430.552 | 54.3646 | 0.803527 | 1.7186 | 209.262 | 74.8165 | 113.6856 | 8925.93 |
| 54973 | 22.6021 | 0.711135 | 23.1168 | 3.11388 | 99.0654 | 0.571353 | 269.885 | 96.1987 | 0.841754 | 343.608 | 49.3028 | 0.812869 | 131.19 | 244.435 | 186.636 | 87.0131 | 5367.688 |
| 18005.3 | 28.8498 | 0.916711 | 49.5167 | 2.46273 | 23.2079 | 0.372166 | 478.781 | 58.2946 | 0.267295 | 421.187 | 23.6905 | 0.678611 | 159.838 | 139.452 | 387.121 | 195.2666 | 14745.67 |
| 16780.8 | 24.5127 | 0.923516 | 100.445 | 1.85032 | 51.0293 | 0.311402 | 488.932 | 37.4573 | 0.646491 | 493.691 | 99.6899 | 0.307779 | 160.275 | 289.101 | 361.445 | 231.2628 | 19653.04 |
| 22639.5 | 32.0425 | 0.890945 | 61.9491 | 2.00178 | 67.079 | 0.306844 | 348.335 | 53.4037 | 0.272293 | 420.034 | 35.4792 | 0.943286 | 164.467 | 335.625 | 211.13 | 200.5256 | 17151.15 |
| 19847.4 | 16.9685 | 0.906457 | 77.6349 | 3.29228 | 26.0822 | 0.23338 | 402.958 | 10.3024 | 0.562943 | 259.286 | 56.5662 | 0.562192 | 10.1814 | 313.603 | 250.294 | 184.6133 | 14256.88 |
| 19608.5 | 20.2204 | 0.907788 | 154.367 | 1.25803 | 41.6403 | 0.533307 | 69.5948 | 45.3233 | 0.368179 | 126.417 | 63.8549 | 0.638634 | 1.62333 | 56.1364 | 116.381 | 144.9895 | 10775.26 |
| 47487.1 | 16.3286 | 0.752759 | 105.99 | 1.66697 | 59.8664 | 0.251099 | 330.239 | 26.6118 | 0.393738 | 518.725 | 38.3753 | 0.981942 | 25.9502 | 134.889 | 313.989 | 234.4352 | 16079.35 |
| 31759.2 | 18.3618 | 0.840219 | 141.287 | 0.44971 | 56.2624 | 0.439468 | 373 | 69.5561 | 0.504871 | 366.109 | 53.6983 | 0.657376 | 29.9576 | 74.4454 | 251.718 | 165.8797 | 11464.98 |
| 52849.9 | 18.6759 | 0.722939 | 151.888 | 3.16095 | 23.137 | 0.297089 | 390.59 | 42.3371 | 0.898226 | 429.248 | 83.0331 | 0.887192 | 104.4 | 305.053 | 150.982 | 120.3628 | 6910.402 |
| 41905.3 | 28.4658 | 0.783806 | 76.0907 | 1.67345 | 50.6852 | 0.327869 | 441.402 | 89.1419 | 0.692883 | 84.9408 | 63.6945 | 0.939482 | 127.965 | 341.472 | 71.937 | 103.0388 | 6990.431 |
| 14888.2 | 19.204 | 0.934035 | 46.3326 | 1.30391 | 31.5874 | 0.486019 | 462.972 | 41.4095 | 0.329926 | 404.86 | 52.7822 | 0.874164 | 119.677 | 217.647 | 365.914 | 93.28148 | 7270.819 |
| 13847.9 | 23.7167 | 0.939824 | 116.274 | 1.20695 | 72.4815 | 0.519819 | 286.39 | 65.6185 | 0.874141 | 413.378 | 45.6925 | 0.656308 | 55.4025 | 87.7561 | 273.047 | 53.99051 | 4639.338 |
| 52478.1 | 19.2323 | 0.725006 | 120.336 | 2.34862 | 27.3952 | 0.228448 | 435.912 | 2.48842 | 0.767141 | 93.8225 | 20.7102 | 0.878004 | 64.7841 | 115.219 | 90.1577 | 150.5146 | 8974.272 |
| 40614.1 | 27.4454 | 0.790985 | 167.929 | 2.29066 | 65.8654 | 0.395019 | 517.52 | 98.7277 | 0.949369 | 161.365 | 21.5897 | 0.313712 | 100.659 | 129.87 | 83.1695 | 242.9732 | 15984.63 |
| 39348.1 | 15.8011 | 0.798017 | 162.951 | 2.18551 | 19.1341 | 0.300995 | 226.055 | 72.5805 | 0.781992 | 99.4041 | 98.1421 | 0.5539 | 19.4502 | 157.926 | 74.87 | 191.8968 | 11535.76 |
| 45721.6 | 29.7449 | 0.762585 | 119.127 | 0.355447 | 58.3106 | 0.326064 | 260.129 | 31.0433 | 0.674823 | 516.135 | 67.5545 | 0.631812 | 22.0633 | 207.882 | 216.795 | 199.8313 | 12960.62 |
| 35474.7 | 33.0291 | 0.819571 | 88.0339 | 2.31678 | 0.730714 | 0.184427 | 508.745 | 8.05242 | 0.832088 | 518.547 | 70.2365 | 0.678654 | 25.6476 | 336.352 | 375.845 | 167.8409 | 9806.134 |
| 41579.9 | 20.1685 | 0.78561 | 111.854 | 1.57151 | 23.7213 | 0.530171 | 339.751 | 32.4601 | 0.98168 | 310.488 | 90.7386 | 0.38081 | 89.2803 | 329.972 | 119.377 | 117.1248 | 6886.653 |
| 24960 | 26.2853 | 0.878034 | 71.8413 | 3.38196 | 60.6274 | 0.480979 | 135.305 | 6.90924 | 0.450233 | 270.991 | 44.2718 | 0.834572 | 20.8018 | 89.1756 | 148.07 | 84.50573 | 6610.873 |
| 47315.7 | 22.0529 | 0.753715 | 35.0072 | 1.51789 | 31.6865 | 0.339581 | 324.005 | 77.0408 | 0.568868 | 474.439 | 18.6838 | 0.931796 | 98.9338 | 112.149 | 316.517 | 120.117 | 7413.948 |
| 59824.9 | 22.2719 | 0.684154 | 135.696 | 1.28326 | 80.3705 | 0.465093 | 263.052 | 94.1861 | 0.91613 | 366.814 | 50.7359 | 0.912476 | 60.7253 | 170.943 | 114.647 | 86.36103 | 5353.538 |
| 22445.5 | 30.2847 | 0.892021 | 163.843 | 3.04797 | 53.4769 | 0.449215 | 270.1 | 64.4145 | 0.510795 | 229.848 | 83.0269 | 0.494434 | 170.761 | 61.8562 | 148.911 | 169.2814 | 12691.6 |
| 50418.6 | 29.9712 | 0.736466 | 92.9754 | 0.942439 | 68.3176 | 0.610521 | 281.861 | 3.16773 | 0.84756 | 442.967 | 13.0718 | 0.912277 | 84.4239 | 144.068 | 390.805 | 57.15577 | 3572.818 |
| 14153.4 | 22.6428 | 0.938124 | 85.8588 | 0.474519 | 19.4361 | 0.515964 | 301.355 | 25.3487 | 0.769223 | 392.741 | 30.9127 | 0.742484 | 16.7793 | 244.634 | 322.508 | 43.89975 | 3506.872 |
| 31525.8 | 13.5182 | 0.841514 | 156.269 | 2.02297 | 4.66372 | 0.398104 | 202.707 | 59.1528 | 0.87359 | 514.396 | 44.2181 | 0.88772 | 31.2465 | 46.6139 | 493.93 | 68.2965 | 4264.125 |
| 36774.9 | 19.1772 | 0.812328 | 105.249 | 1.34955 | 91.8188 | 0.311262 | 213.061 | 11.9677 | 0.69228 | 299.025 | 43.1795 | 0.392397 | 70.1941 | 116.661 | 149.897 | 249.301 | 19858.59 |
| 31304.4 | 15.1658 | 0.842746 | 152.144 | 2.80091 | 12.773 | 0.459089 | 344.279 | 35.939 | 0.504121 | 420.125 | 71.7613 | 0.936767 | 167.386 | 210.116 | 158.785 | 90.15742 | 5719.028 |
| 44640.7 | 14.4919 | 0.768586 | 96.6171 | 1.34082 | 40.4086 | 0.271689 | 119.845 | 55.2711 | 0.65517 | 492.292 | 65.4773 | 0.556723 | 43.0244 | 49.1873 | 412.945 | 219.6074 | 14185.89 |
| 22589.9 | 32.7925 | 0.891222 | 34.9135 | 0.976018 | 78.6873 | 0.19284 | 472.719 | 60.379 | 0.76606 | 143.977 | 28.2626 | 0.929909 | 1.28965 | 368.871 | 49.471 | 134.8761 | 12442.99 |
| 16747 | 22.0919 | 0.923701 | 30.4048 | 1.58558 | 27.2651 | 0.388005 | 364.29 | 17.752 | 0.458543 | 260.994 | 1.39534 | 0.553841 | 127.759 | 154.633 | 198.786 | 127.4072 | 10109.45 |
| 21052.2 | 30.1078 | 0.899769 | 46.4202 | 1.8592 | 52.135 | 0.262402 | 286.97 | 67.3619 | 0.786161 | 343.884 | 32.7156 | 0.372989 | 128.015 | 148.733 | 285.157 | 205.8823 | 16940.35 |
| 28752.2 | 13.377 | 0.856937 | 162.187 | 2.12549 | 77.3277 | 0.386627 | 437.288 | 10.5771 | 0.276766 | 232.467 | 81.7666 | 0.866281 | 40.6771 | 369.633 | 187.68 | 230.6103 | 17802.44 |
| 13395.2 | 13.2723 | 0.942334 | 113.719 | 0.319834 | 82.1988 | 0.482418 | 255.51 | 18.7015 | 0.823371 | 477.754 | 73.9448 | 0.560788 | 23.4478 | 121.202 | 386.192 | 74.76848 | 6775.952 |
| 32955.6 | 20.8745 | 0.833568 | 30.4092 | 1.31268 | 43.6604 | 0.472044 | 163.715 | 73.488 | 0.241263 | 132.225 | 63.0176 | 0.805239 | 117.716 | 47.7956 | 46.8252 | 193.0113 | 13015.56 |
| 19758.7 | 21.8835 | 0.906954 | 126.511 | 1.56106 | 57.6153 | 0.220783 | 196.018 | 20.0399 | 0.759498 | 335.792 | 19.3541 | 0.855822 | 80.9877 | 122.705 | 86.958 | 113.8617 | 9949.421 |
| 50255.9 | 19.8656 | 0.737364 | 155.036 | 1.81905 | 13.0456 | 0.262956 | 507.79 | 10.413 | 0.881264 | 288.46 | 28.7397 | 0.478017 | 129.768 | 353.215 | 115.275 | 240.1358 | 13293.66 |
| 11491 | 18.663 | 0.952926 | 172.079 | 1.71883 | 17.4994 | 0.469569 | 222.549 | 20.9026 | 0.286925 | 269.676 | 87.8983 | 0.884627 | 59.6616 | 52.2664 | 241.735 | 129.5789 | 10115.81 |
| 17695.5 | 15.8793 | 0.918423 | 34.3348 | 2.42433 | 35.7322 | 0.493594 | 185.465 | 10.8331 | 0.40686 | 299.902 | 84.0955 | 0.470176 | 225.781 | 128.111 | 282.491 | 164.049 | 12290.49 |
| 19720.5 | 14.865 | 0.907161 | 148.733 | 2.7771 | 31.6582 | 0.241272 | 433.536 | 32.4637 | 0.70364 | 263.59 | 81.6905 | 0.982227 | 108.907 | 320.511 | 85.0183 | 100.64 | 7802.57 |
| 19817.2 | 24.5146 | 0.906631 | 83.7015 | 1.97669 | 61.8307 | 0.236349 | 455.056 | 85.6442 | 0.506617 | 446.044 | 61.1761 | 0.664241 | 100.859 | 380.948 | 329.04 | 195.5764 | 17100.4 |
| 39581.9 | 21.771 | 0.796721 | 133.016 | 1.72385 | 65.9399 | 0.426436 | 354.993 | 33.815 | 0.721312 | 137.825 | 64.1329 | 0.656707 | 56.753 | 278.24 | 87.493 | 114.795 | 7949.164 |
| 17233.3 | 25.2239 | 0.921 | 106.979 | 1.24827 | 83.4623 | 0.463518 | 286.475 | 48.9193 | 0.322368 | 156.101 | 7.56308 | 0.858234 | 122.341 | 125.641 | 47.4155 | 116.9935 | 10512.49 |
| 51302 | 23.8599 | 0.731549 | 99.0466 | 1.69169 | 92.9566 | 0.214511 | 268.186 | 97.3782 | 0.933848 | 263.634 | 82.2426 | 0.892711 | 124.521 | 69.6878 | 131.19 | 180.5664 | 13220.49 |
| 23154.3 | 29.6723 | 0.888079 | 96.8334 | 0.973845 | 20.2495 | 0.47122 | 234.901 | 58.3042 | 0.376213 | 131.239 | 27.6572 | 0.957194 | 31.332 | 163.518 | 61.3816 | 91.2648 | 6423.114 |
| 13927 | 15.0986 | 0.939378 | 154.255 | 2.57822 | 87.204 | 0.560191 | 392.702 | 57.6496 | 0.129738 | 458.994 | 89.7795 | 0.926469 | 34.7693 | 384.74 | 291.048 | 226.6823 | 19398.38 |
| 32164.7 | 24.0709 | 0.837968 | 81.4332 | 3.22022 | 87.1315 | 0.350592 | 333.925 | 40.9672 | 0.911902 | 241.137 | 8.11592 | 0.50321 | 118.412 | 55.6673 | 66.5347 | 118.9935 | 9755.609 |
| 43926.9 | 24.1131 | 0.772561 | 152.123 | 1.47384 | 71.3177 | 0.597855 | 135.125 | 92.8556 | 0.986233 | 472.35 | 16.0728 | 0.310098 | 18.3424 | 128.745 | 259.88 | 162.8788 | 10028.62 |
| 31406.8 | 31.1837 | 0.84219 | 159.143 | 3.389 | 96.5511 | 0.562479 | 170.38 | 63.9582 | 0.543933 | 328.412 | 14.9492 | 0.403834 | 39.8473 | 159.215 | 88.4798 | 175.2844 | 12707.08 |
| 35808.3 | 24.1638 | 0.817707 | 122.178 | 0.217706 | 94.7558 | 0.325741 | 400.759 | 20.5489 | 0.34476 | 367.527 | 89.5966 | 0.999128 | 5.38061 | 212.709 | 348.027 | 237.7106 | 18005.06 |
| 25654.8 | 20.1472 | 0.874165 | 50.9562 | 0.649197 | 34.0506 | 0.315308 | 213.328 | 35.2103 | 0.744105 | 466.222 | 66.7152 | 0.403665 | 59.24 | 204.574 | 281.239 | 168.3149 | 12332.25 |
| 39585.9 | 21.3604 | 0.796698 | 142.816 | 0.692199 | 23.3215 | 0.467462 | 479.915 | 42.7953 | 0.702639 | 390.703 | 31.5116 | 0.500726 | 23.5717 | 396.259 | 320.276 | 152.1545 | 9171.212 |
| 38324.3 | 25.3862 | 0.803717 | 84.1304 | 0.280704 | 84.0349 | 0.183512 | 86.2861 | 57.5459 | 0.802231 | 116.473 | 25.6334 | 0.700052 | 10.9941 | 79.8029 | 45.6842 | 231.5265 | 18115.05 |
| 12128.1 | 22.8829 | 0.949387 | 107.39 | 0.438574 | 22.6831 | 0.538663 | 189.111 | 16.5696 | 0.338157 | 71.919 | 91.6151 | 0.856798 | 39.8352 | 133.473 | 59.003 | 89.41591 | 7038.568 |
| 24962.2 | 28.8978 | 0.878025 | 65.542 | 2.2072 | 98.1377 | 0.488765 | 249.666 | 90.4369 | 0.486458 | 176.52 | 32.1125 | 0.585757 | 147.248 | 185.14 | 55.1586 | 124.2067 | 9742.996 |
| 23176 | 28.4603 | 0.887957 | 97.9996 | 0.164431 | 74.4012 | 0.58729 | 198.322 | 97.8609 | 0.913099 | 343.08 | 45.5633 | 0.634775 | 5.42934 | 82.776 | 177.275 | 66.45416 | 4919.104 |
| 53428.8 | 25.3772 | 0.719723 | 88.4774 | 2.592 | 31.6294 | 0.187874 | 173.756 | 65.5266 | 0.701925 | 314.697 | 55.2286 | 0.833709 | 143.838 | 67.2832 | 202.101 | 216.3095 | 12995.92 |
| 14876.2 | 27.1075 | 0.93411 | 55.2838 | 0.705175 | 34.0296 | 0.189941 | 408.793 | 43.9484 | 0.57586 | 180.844 | 64.5796 | 0.559236 | 10.0411 | 195.535 | 140.914 | 213.8048 | 18129.8 |
| 51928.3 | 17.2248 | 0.728063 | 74.0893 | 0.740036 | 38.4164 | 0.237267 | 276.64 | 19.9852 | 0.979996 | 123.691 | 56.3957 | 0.581978 | 72.8666 | 159.147 | 72.2092 | 169.9688 | 10588.6 |
| 11136.2 | 29.5861 | 0.95491 | 43.8613 | 2.61225 | 80.4122 | 0.446182 | 362.247 | 65.8506 | 0.226358 | 413.798 | 27.0092 | 0.787423 | 7.66775 | 169.319 | 291.742 | 160.0828 | 15634.68 |
| 19717.1 | 27.1272 | 0.90719 | 67.9841 | 1.92911 | 24.562 | 0.166785 | 171.889 | 18.8621 | 0.649638 | 163.822 | 45.2626 | 0.627042 | 36.5472 | 119.634 | 154.824 | 202.8742 | 15695.63 |
| 41953 | 22.8746 | 0.783536 | 131.635 | 2.82339 | 18.571 | 0.410163 | 239.544 | 23.9745 | 0.960993 | 351.86 | 13.3532 | 0.366019 | 109.534 | 50.0012 | 267.871 | 145.4237 | 8689.222 |
| 14966 | 18.0922 | 0.933602 | 62.6299 | 2.41099 | 21.7365 | 0.396762 | 342.976 | 78.0913 | 0.471535 | 195.443 | 17.5391 | 0.995095 | 20.5788 | 109.249 | 164.261 | 68.04421 | 5392.418 |
| 32965.2 | 34.4815 | 0.833528 | 48.3829 | 0.71317 | 57.8306 | 0.428248 | 468.777 | 72.3136 | 0.313662 | 459.62 | 56.2089 | 0.842132 | 12.243 | 72.5901 | 317.932 | 165.6703 | 11953.7 |
| 15451.4 | 30.5643 | 0.930915 | 75.9414 | 1.51738 | 29.6529 | 0.276924 | 151.756 | 13.2731 | 0.772563 | 465.189 | 56.7842 | 0.4847 | 11.8287 | 143.807 | 199.284 | 123.7451 | 10195.42 |
| 17313 | 19.9062 | 0.920552 | 87.4691 | 0.612884 | 84.8624 | 0.466682 | 509.157 | 6.5521 | 0.794178 | 338.139 | 93.0874 | 0.679129 | 7.02317 | 447.339 | 337.85 | 62.96153 | 5686.729 |
| 39836.1 | 14.4236 | 0.795303 | 58.8109 | 3.73932 | 1.98156 | 0.57883 | 280.92 | 50.5873 | 0.900219 | 471.529 | 73.0119 | 0.404749 | 227.039 | 246.482 | 427.801 | 177.1783 | 9896.166 |
| 26447 | 26.1498 | 0.869765 | 91.147 | 2.94596 | 90.1406 | 0.407991 | 352.924 | 60.4053 | 0.964781 | 209.908 | 37.7759 | 0.634163 | 159.784 | 151.802 | 105.784 | 73.86721 | 6207.21 |
| 38314 | 17.7808 | 0.803769 | 94.6606 | 2.23295 | 18.3559 | 0.450969 | 435.267 | 3.61695 | 0.824788 | 127.855 | 42.9778 | 0.607592 | 86.1279 | 269.63 | 47.9416 | 78.62338 | 4925.535 |
| 21105.4 | 16.2921 | 0.899461 | 28.8273 | 1.86605 | 86.9096 | 0.371676 | 458.999 | 28.8496 | 0.385501 | 347.109 | 82.3267 | 0.669014 | 114.188 | 445.39 | 179.137 | 164.8937 | 14842.78 |
| 23196.8 | 14.2488 | 0.88783 | 114.461 | 0.858177 | 4.37188 | 0.501649 | 362.092 | 74.8617 | 0.917444 | 493.806 | 55.9051 | 0.31067 | 4.86255 | 103.058 | 370.601 | 129.7132 | 8290.263 |
| 33699 | 33.1466 | 0.829445 | 113.944 | 2.44805 | 37.1777 | 0.351306 | 142.157 | 46.3303 | 0.65287 | 286.827 | 85.0854 | 0.779577 | 46.2355 | 126.539 | 282.101 | 108.2517 | 7420.384 |
| 34694.5 | 28.9816 | 0.823905 | 156.037 | 0.196735 | 35.6906 | 0.404418 | 130.331 | 77.6956 | 0.468983 | 162.1 | 62.1715 | 0.756905 | 11.3548 | 121.53 | 111.545 | 199.8789 | 12690.17 |
| 17667.8 | 16.7115 | 0.918577 | 85.6285 | 2.90798 | 14.5796 | 0.389248 | 287.667 | 48.5303 | 0.970467 | 200.685 | 11.1246 | 0.255317 | 34.2162 | 192.632 | 148.461 | 143.2869 | 10313.2 |
| 44927.8 | 18.5383 | 0.766992 | 152.998 | 0.222289 | 44.3008 | 0.597319 | 467.914 | 6.32299 | 0.59084 | 479.436 | 45.2211 | 0.797028 | 2.56983 | 115.403 | 81.9021 | 108.0405 | 6465.937 |
| 14220.2 | 26.4514 | 0.937756 | 30.0455 | 3.37711 | 66.6692 | 0.34401 | 273.303 | 44.5713 | 0.520561 | 177.772 | 77.4009 | 0.892779 | 135.447 | 257.079 | 172.305 | 87.79578 | 8153.485 |
| 10991.6 | 26.2402 | 0.95571 | 46.1638 | 1.16576 | 9.10782 | 0.23809 | 384.032 | 65.3779 | 0.572041 | 240.332 | 43.4478 | 0.824213 | 70.2494 | 359.6 | 144.424 | 100.7199 | 7938.621 |
| 58649.2 | 20.3175 | 0.690691 | 165.961 | 1.70822 | 8.84548 | 0.481949 | 507.42 | 31.3673 | 0.502056 | 472.582 | 65.4274 | 0.913704 | 109.804 | 437.309 | 102.911 | 142.9817 | 7457.016 |
| 40919.2 | 17.4857 | 0.789282 | 42.6915 | 3.20437 | 44.5527 | 0.206247 | 441.432 | 42.3277 | 0.727299 | 129.912 | 72.5996 | 0.60865 | 153.213 | 350.223 | 114.321 | 222.6061 | 15270.05 |
| 13250.5 | 20.2036 | 0.943143 | 142.922 | 2.9666 | 61.8254 | 0.23072 | 306.829 | 80.8223 | 0.549765 | 87.5131 | 57.7543 | 0.77204 | 133.125 | 44.6093 | 77.7182 | 155.1282 | 14380.69 |
| 20399.4 | 17.3272 | 0.903387 | 167.826 | 1.77906 | 42.9032 | 0.603399 | 503.103 | 48.7585 | 0.70235 | 421.952 | 0.879875 | 0.853409 | 126.866 | 250.959 | 105.251 | 50.24883 | 3816.978 |
| 20869.7 | 14.7776 | 0.900771 | 160.996 | 0.422684 | 79.3959 | 0.573922 | 405.461 | 92.8603 | 0.649455 | 67.9461 | 88.9742 | 0.317934 | 14.7293 | 193.685 | 48.6343 | 203.3347 | 15077.87 |
| 15773.4 | 33.0244 | 0.929128 | 170.979 | 1.91173 | 16.6207 | 0.600707 | 422.581 | 79.2688 | 0.323744 | 296.227 | 48.8114 | 0.481739 | 6.30759 | 376.335 | 49.2081 | 184.4312 | 13199.85 |
| 49938.8 | 29.9655 | 0.739134 | 81.6976 | 1.61575 | 74.4164 | 0.199062 | 179.058 | 46.5488 | 0.60982 | 220.553 | 11.0745 | 0.803164 | 51.9525 | 44.647 | 192.062 | 246.5367 | 17697.29 |
| 36724.7 | 14.7957 | 0.812605 | 153.528 | 2.59932 | 36.8141 | 0.562261 | 403.081 | 7.89976 | 0.798952 | 377.344 | 88.9013 | 0.639081 | 38.2207 | 328.18 | 267.605 | 76.27146 | 4866.238 |
| 29302.9 | 22.0012 | 0.85388 | 49.5998 | 0.261013 | 74.8521 | 0.53526 | 296.108 | 63.5906 | 0.392752 | 505.7 | 80.9724 | 0.824629 | 22.1587 | 290.59 | 280.897 | 140.4556 | 10054.27 |
| 33930 | 19.3693 | 0.828148 | 150.952 | 1.12067 | 87.6069 | 0.286106 | 385.879 | 70.5334 | 0.662783 | 179.347 | 70.6852 | 0.606307 | 46.0213 | 111.817 | 114.588 | 219.8901 | 16822.9 |
| 43146 | 24.7939 | 0.776903 | 72.3427 | 1.84946 | 37.3137 | 0.239898 | 453.675 | 17.8342 | 0.935164 | 503.198 | 47.6451 | 0.514168 | 24.6862 | 74.3873 | 238.752 | 178.6646 | 11727.99 |
| 11066.5 | 31.4173 | 0.9553 | 123.997 | 0.109798 | 67.7528 | 0.380992 | 277.06 | 87.064 | 0.882124 | 476.503 | 97.5136 | 0.508848 | 0.743822 | 139.846 | 189.092 | 116.9882 | 10078.42 |
| 22592.9 | 13.1607 | 0.891188 | 57.0496 | 1.15315 | 24.705 | 0.244342 | 429.764 | 40.5567 | 0.851434 | 176.24 | 71.1579 | 0.907234 | 19.1091 | 376.69 | 167.401 | 84.01802 | 6261.649 |
| 36010.1 | 21.7426 | 0.816583 | 127.144 | 2.1775 | 62.29 | 0.181014 | 96.6066 | 22.9815 | 0.993793 | 257.823 | 21.1076 | 0.859996 | 34.6212 | 60.8526 | 128.534 | 188.6896 | 14336.17 |
| 39433.2 | 14.612 | 0.797544 | 87.932 | 1.95086 | 53.2145 | 0.329821 | 479.235 | 59.2902 | 0.455645 | 437.463 | 64.0616 | 0.894714 | 55.1089 | 204.921 | 382.813 | 148.7087 | 10414.4 |
| 29695.7 | 20.3202 | 0.851695 | 125.567 | 0.662561 | 38.7816 | 0.302917 | 198.019 | 83.002 | 0.808484 | 172.231 | 51.1296 | 0.881747 | 30.4286 | 50.7136 | 45.5328 | 100.3825 | 7057.022 |
| 24314.1 | 29.7965 | 0.881629 | 73.127 | 2.01187 | 41.3929 | 0.445194 | 98.2619 | 81.8941 | 0.499977 | 496.054 | 5.57141 | 0.333834 | 140.466 | 56.8652 | 212.847 | 217.7728 | 15805.23 |
| 23922.9 | 34.7087 | 0.883811 | 74.9544 | 2.29055 | 44.247 | 0.216075 | 433.843 | 89.1785 | 0.543279 | 123.422 | 31.7658 | 0.982306 | 136.678 | 370.293 | 53.9941 | 139.7719 | 11105.81 |
| 25137.1 | 33.9145 | 0.877059 | 65.8354 | 1.79099 | 73.2645 | 0.434345 | 97.0976 | 16.5244 | 0.832214 | 269.537 | 6.62883 | 0.584067 | 91.4568 | 48.7026 | 176.041 | 75.27749 | 6327.349 |
| 42275.2 | 22.342 | 0.781744 | 61.4691 | 0.378208 | 24.1263 | 0.360386 | 270.812 | 1.80136 | 0.782655 | 327.091 | 79.3209 | 0.359652 | 30.1261 | 159.928 | 73.8545 | 197.7091 | 12086.07 |
| 24135.2 | 20.6808 | 0.882616 | 119.968 | 3.09772 | 1.30852 | 0.194087 | 186.16 | 37.9412 | 0.84154 | 308.051 | 71.1466 | 0.975511 | 16.1615 | 158.045 | 118.764 | 115.1879 | 7429.789 |
| 48210.8 | 32.3104 | 0.748746 | 161.373 | 1.94436 | 44.2771 | 0.363461 | 288.901 | 21.3402 | 0.651329 | 303.573 | 99.4825 | 0.507239 | 2.69461 | 172.438 | 101.103 | 238.4927 | 14466.49 |
| 30401.8 | 18.3385 | 0.847767 | 43.2061 | 1.97313 | 30.7621 | 0.501241 | 375.343 | 85.5768 | 0.803328 | 195.835 | 31.8001 | 0.815527 | 175.81 | 98.6594 | 161.291 | 58.52705 | 3886.296 |
| 42485.4 | 25.2376 | 0.780578 | 124.54 | 0.328072 | 25.1945 | 0.284061 | 116.867 | 70.9315 | 0.870194 | 516.633 | 96.8829 | 0.617978 | 21.5045 | 96.0714 | 111.226 | 180.4053 | 10831.7 |
| 44754.2 | 32.1173 | 0.767967 | 92.6223 | 0.817 | 32.7754 | 0.349951 | 185.354 | 20.1112 | 0.519832 | 72.137 | 27.9763 | 0.941384 | 38.8852 | 44.2348 | 55.6978 | 128.2066 | 8014.196 |
| 22832.4 | 32.8337 | 0.889873 | 142.096 | 1.54236 | 32.8553 | 0.313537 | 288.438 | 60.6743 | 0.494499 | 514.67 | 78.4033 | 0.627661 | 96.1486 | 285.344 | 508.486 | 188.6159 | 13755.31 |
| 20520.6 | 16.9661 | 0.902713 | 168.401 | 1.14936 | 74.6998 | 0.199298 | 297.198 | 58.7456 | 0.840969 | 96.387 | 62.2672 | 0.59172 | 10.7536 | 69.7685 | 45.0405 | 219.901 | 18678.69 |
| 36456.3 | 20.9083 | 0.814101 | 41.4919 | 1.26523 | 1.46852 | 0.352775 | 397.86 | 26.0589 | 0.415453 | 342.678 | 50.5836 | 0.804534 | 70.5559 | 104.058 | 293.648 | 146.9237 | 8563.674 |
| 15215.3 | 34.3858 | 0.932234 | 113.131 | 1.85357 | 42.6074 | 0.538689 | 393.051 | 97.5891 | 0.885942 | 300.417 | 66.3167 | 0.781925 | 171.412 | 95.7114 | 163.447 | 50.2365 | 3755.003 |
| 13857.9 | 19.8844 | 0.939765 | 142.755 | 0.158833 | 86.9318 | 0.542114 | 381.15 | 48.9657 | 0.371181 | 428.139 | 52.7676 | 0.985247 | 14.0619 | 114.327 | 380.842 | 97.71498 | 8440.685 |
| 24753 | 30.6104 | 0.87919 | 135.307 | 0.864742 | 45.5068 | 0.580502 | 472.444 | 99.4767 | 0.46291 | 221.258 | 25.1572 | 0.952769 | 7.43742 | 254.546 | 61.3031 | 78.08863 | 5555.715 |
| 10738.7 | 24.675 | 0.957115 | 123.97 | 2.58134 | 1.03938 | 0.355086 | 504.666 | 21.799 | 0.836714 | 99.2352 | 34.6528 | 0.240895 | 60.5957 | 139.748 | 46.9626 | 159.7046 | 11944.8 |
| 20477.2 | 23.4177 | 0.902959 | 147.985 | 0.249778 | 94.7883 | 0.535754 | 166.289 | 50.6126 | 0.647952 | 170.831 | 18.9285 | 0.883938 | 23.0956 | 52.4348 | 104.186 | 70.74304 | 5834.591 |
| 27934.5 | 20.123 | 0.861488 | 107.323 | 0.372643 | 70.187 | 0.23327 | 314.14 | 30.7768 | 0.955252 | 271.256 | 73.1198 | 0.9807 | 16.6922 | 44.5124 | 167.766 | 140.5516 | 11192.84 |
| 25179 | 32.6579 | 0.876824 | 155.611 | 0.159599 | 17.3447 | 0.419658 | 261.354 | 1.11221 | 0.473885 | 447.798 | 92.2962 | 0.966486 | 8.13531 | 103.847 | 148.087 | 125.1922 | 8345.552 |
| 41948.9 | 18.146 | 0.783556 | 93.3359 | 0.849392 | 4.9033 | 0.230515 | 188.373 | 84.061 | 0.630053 | 64.1956 | 85.2281 | 0.737214 | 56.5357 | 59.5479 | 46.2309 | 196.6945 | 11128.47 |
| 28080.8 | 17.9136 | 0.860674 | 22.1319 | 2.27525 | 78.3608 | 0.427282 | 384.228 | 72.6373 | 0.38335 | 436.842 | 99.1033 | 0.979875 | 52.4778 | 365.772 | 416.689 | 113.0129 | 8988.006 |
| 15227.6 | 20.6975 | 0.932149 | 116.773 | 1.42432 | 62.583 | 0.417734 | 120.188 | 81.4863 | 0.418253 | 425.559 | 23.5553 | 0.467185 | 107.298 | 101.442 | 417.218 | 186.0956 | 15991.07 |
| 29847.6 | 25.8727 | 0.850855 | 105.821 | 1.66309 | 78.0804 | 0.292922 | 167.397 | 22.4412 | 0.902778 | 196.48 | 10.3467 | 0.383093 | 164.756 | 50.4853 | 133.494 | 185.6923 | 15272.34 |
| 32211.8 | 17.4902 | 0.837702 | 125.296 | 1.04899 | 59.8356 | 0.189298 | 133.964 | 17.2564 | 0.935172 | 364.327 | 55.4972 | 0.734345 | 58.7835 | 47.9224 | 181.487 | 183.1446 | 13977.81 |
| 28367 | 22.3324 | 0.859085 | 45.6972 | 3.13993 | 40.831 | 0.524215 | 325.723 | 1.70739 | 0.547832 | 401.581 | 58.9228 | 0.856717 | 85.4864 | 282.888 | 287.789 | 76.61551 | 5342.741 |
| 15132.8 | 23.7254 | 0.932679 | 52.0181 | 2.40005 | 95.5568 | 0.194935 | 179.575 | 75.6005 | 0.68927 | 417.912 | 10.3804 | 0.847635 | 106.258 | 89.1498 | 203.779 | 134.9591 | 14227.82 |
| 16543.1 | 23.2152 | 0.924836 | 136.95 | 0.52138 | 54.1127 | 0.460992 | 417.837 | 5.56155 | 0.301711 | 395.616 | 8.40884 | 0.74388 | 5.96471 | 155.761 | 148.086 | 162.343 | 13351.44 |
| 28111.2 | 27.2838 | 0.860512 | 144.225 | 1.08096 | 36.9284 | 0.475586 | 307.174 | 30.3395 | 0.235837 | 344.82 | 32.5605 | 0.894489 | 13.9231 | 137.112 | 92.7451 | 198.9487 | 13655.59 |
| 54824.8 | 21.2043 | 0.711958 | 143.805 | 0.614998 | 4.08134 | 0.380397 | 347.609 | 42.2165 | 0.658778 | 189.391 | 68.8693 | 0.875921 | 49.1816 | 54.1973 | 96.461 | 140.1672 | 7375.872 |
| 48107.7 | 20.0088 | 0.74931 | 38.1602 | 0.285637 | 50.7516 | 0.282277 | 247.137 | 81.3168 | 0.670124 | 167.358 | 3.26508 | 0.493838 | 24.5376 | 159.787 | 142.887 | 245.0748 | 16059.79 |
| 51125.2 | 26.6906 | 0.732534 | 148.596 | 1.79716 | 27.0444 | 0.306102 | 232.999 | 90.9102 | 0.942001 | 369.785 | 99.4968 | 0.527652 | 11.8694 | 214.011 | 110.183 | 194.4084 | 11144.86 |
| 39696.3 | 13.9453 | 0.79608 | 151.497 | 0.802059 | 72.6874 | 0.480119 | 319.551 | 30.3147 | 0.789137 | 290.262 | 44.9672 | 0.532113 | 51.5193 | 315.668 | 114.509 | 131.4701 | 8871.983 |
| 40290.6 | 13.371 | 0.792775 | 170.371 | 2.06627 | 20.0369 | 0.250733 | 167.377 | 16.6341 | 0.990792 | 509.871 | 65.0654 | 0.564705 | 107.156 | 146.992 | 361.828 | 178.4602 | 10816.81 |
| 53936.7 | 18.016 | 0.716895 | 79.2658 | 0.797262 | 27.3566 | 0.473273 | 375.287 | 50.7839 | 0.675137 | 489.371 | 36.787 | 0.658922 | 59.6535 | 290.289 | 143.77 | 112.3067 | 6414.957 |
| 16756.3 | 14.2704 | 0.923644 | 134.903 | 0.477252 | 88.7486 | 0.595907 | 215.488 | 5.66873 | 0.505298 | 315.906 | 30.0782 | 0.911444 | 47.0363 | 69.51 | 161.905 | 61.42614 | 5322.486 |
| 30317.9 | 14.9422 | 0.848232 | 163.195 | 0.441706 | 81.535 | 0.557114 | 105.045 | 42.4111 | 0.22583 | 165.574 | 28.7274 | 0.883541 | 2.92784 | 96.4441 | 63.1399 | 226.293 | 16013.6 |
| 51707.7 | 25.9039 | 0.729295 | 95.1421 | 1.02713 | 57.2694 | 0.462972 | 396.182 | 76.6512 | 0.690986 | 280.946 | 22.8404 | 0.986396 | 21.1667 | 130.205 | 93.271 | 79.56307 | 5051.863 |
| 33131.7 | 33.4949 | 0.8326 | 137.089 | 1.97673 | 3.52974 | 0.314525 | 95.6379 | 64.7748 | 0.76867 | 288.896 | 46.2309 | 0.460913 | 154.147 | 59.5681 | 276.355 | 182.3833 | 10869.96 |
| 33875.7 | 26.2735 | 0.828455 | 167.404 | 0.864732 | 41.2213 | 0.342649 | 128.874 | 17.7176 | 0.844409 | 384.011 | 8.06482 | 0.828984 | 21.4492 | 103.274 | 50.0269 | 104.3768 | 7095.175 |
| 23225.8 | 26.5294 | 0.887678 | 157.286 | 1.97025 | 10.7565 | 0.415816 | 514.424 | 43.8247 | 0.6322 | 57.9317 | 8.61523 | 0.443918 | 34.7653 | 241.699 | 55.9781 | 154.2475 | 10330.21 |
| 18070.1 | 22.1598 | 0.916344 | 72.349 | 2.70655 | 21.1801 | 0.521479 | 163.363 | 14.5422 | 0.591823 | 234.543 | 0.231782 | 0.563366 | 241.777 | 147.7 | 214.212 | 93.67153 | 6907.558 |
| 17124.4 | 14.0567 | 0.921597 | 14.1638 | 0.875752 | 15.1527 | 0.230878 | 302.858 | 65.3689 | 0.540421 | 185.696 | 68.7934 | 0.449375 | 15.9689 | 260.617 | 138.173 | 234.3154 | 17352.43 |
| 45317 | 19.5185 | 0.764828 | 145.603 | 0.192669 | 17.5561 | 0.631548 | 455.162 | 19.8838 | 0.765197 | 117.553 | 47.7643 | 0.409387 | 6.43202 | 231.863 | 50.8451 | 152.2556 | 8553.876 |
| 41500.5 | 13.6573 | 0.786048 | 61.5193 | 0.111929 | 36.1987 | 0.448795 | 391.699 | 32.9713 | 0.351997 | 305.511 | 35.2879 | 0.897532 | 4.18499 | 48.8744 | 111.272 | 153.546 | 9652.804 |
| 20609.9 | 22.4212 | 0.902221 | 98.6131 | 1.62314 | 22.7331 | 0.444881 | 145.867 | 32.5986 | 0.449609 | 189.55 | 71.0168 | 0.663234 | 30.131 | 57.6581 | 137.247 | 108.0617 | 7849.271 |
| 22764.1 | 27.252 | 0.890246 | 169.426 | 2.09524 | 56.2291 | 0.328573 | 227.561 | 94.115 | 0.711248 | 354.056 | 82.6695 | 0.820105 | 139.081 | 95.0414 | 283.266 | 113.2957 | 8680.531 |
| 13020.3 | 21.9953 | 0.944425 | 122.978 | 1.84329 | 14.3517 | 0.531312 | 299.578 | 21.4627 | 0.779149 | 314.376 | 20.0184 | 0.974474 | 31.868 | 232.003 | 256.86 | 30.16123 | 2494.317 |
| 19211 | 33.4092 | 0.910012 | 126.959 | 1.42777 | 81.2324 | 0.429983 | 273.18 | 40.0393 | 0.225469 | 336.965 | 33.5911 | 0.906922 | 33.9464 | 184.243 | 148.541 | 190.1639 | 16518.41 |
| 34824.4 | 15.74 | 0.823173 | 50.7185 | 1.59321 | 51.6778 | 0.486087 | 475.375 | 82.4019 | 0.966479 | 277.362 | 89.6493 | 0.381783 | 118.362 | 87.5384 | 240 | 119.1484 | 7710.82 |
| 15994.5 | 34.2384 | 0.927901 | 164.224 | 0.309023 | 29.9125 | 0.183922 | 277.732 | 18.4484 | 0.756558 | 509.466 | 65.9014 | 0.625897 | 17.0861 | 140.952 | 203.162 | 241.7207 | 18803.44 |
| 16441.7 | 31.7311 | 0.92541 | 87.19 | 3.12248 | 18.4368 | 0.232539 | 202.717 | 43.7822 | 0.519726 | 347.302 | 33.6544 | 0.940657 | 57.9908 | 129.027 | 293.232 | 112.1814 | 8735.091 |
| 24891.1 | 17.4486 | 0.87841 | 106.687 | 0.549088 | 17.0472 | 0.347214 | 417.085 | 17.4585 | 0.646577 | 76.3509 | 37.0984 | 0.741336 | 5.44159 | 62.1745 | 74.251 | 101.5685 | 7030.39 |
| 24301.4 | 18.9695 | 0.88169 | 153.6 | 0.4018 | 4.74293 | 0.411247 | 425.455 | 28.4816 | 0.98932 | 315.025 | 81.8729 | 0.583233 | 27.3727 | 283.911 | 280.449 | 92.32741 | 6021.468 |
| 22657.3 | 31.3416 | 0.890845 | 146.42 | 1.54814 | 78.032 | 0.605504 | 423.135 | 26.5539 | 0.797181 | 415.924 | 31.642 | 0.64648 | 32.848 | 237.846 | 331.387 | 62.10268 | 4743.577 |
| 19586.4 | 24.9331 | 0.907914 | 166.142 | 0.928607 | 21.5913 | 0.375002 | 483.247 | 33.7589 | 0.848261 | 303.91 | 59.1629 | 0.333664 | 40.6437 | 218.582 | 84.9788 | 186.2539 | 13258.76 |
| 10691.3 | 24.1037 | 0.957378 | 89.8997 | 0.252763 | 1.99911 | 0.550827 | 507.077 | 61.323 | 0.183167 | 352.224 | 73.1762 | 0.660769 | 16.5808 | 194.11 | 134.058 | 192.0744 | 14288.68 |
| 26639 | 21.3456 | 0.868693 | 51.4111 | 0.268913 | 30.9692 | 0.271497 | 432.124 | 78.1078 | 0.55662 | 288.91 | 7.09293 | 0.674199 | 13.7937 | 350.161 | 239.174 | 160.3047 | 11619.6 |
| 50581.6 | 24.5676 | 0.735556 | 69.975 | 1.69759 | 7.09497 | 0.46825 | 404.517 | 65.0139 | 0.602487 | 242.307 | 85.9188 | 0.939089 | 8.43174 | 183.492 | 198.625 | 87.8933 | 4852.122 |
| 26101.9 | 29.3575 | 0.871687 | 51.2161 | 0.182649 | 46.4658 | 0.254658 | 147.27 | 89.4921 | 0.739903 | 324.84 | 18.1974 | 0.887314 | 4.50683 | 86.0693 | 127.249 | 105.8254 | 8202.824 |
| 52516.3 | 18.8387 | 0.724794 | 137.351 | 3.79248 | 93.7691 | 0.407252 | 471.939 | 16.2628 | 0.388998 | 289.4 | 65.5791 | 0.680312 | 121.695 | 425.089 | 91.5655 | 233.1003 | 16048.67 |
| 13300.1 | 22.6545 | 0.94287 | 72.0571 | 0.565196 | 61.3752 | 0.31072 | 393.955 | 99.5084 | 0.829482 | 242.794 | 77.621 | 0.534144 | 26.2211 | 312.007 | 148.315 | 112.2879 | 9999.369 |
| 17527.1 | 28.3982 | 0.91937 | 44.6918 | 0.163483 | 47.6306 | 0.31694 | 404.639 | 33.9169 | 0.306604 | 454.665 | 73.2858 | 0.840782 | 14.62 | 145.432 | 389.476 | 175.3123 | 14783.04 |
| 23044.2 | 26.9787 | 0.888689 | 149.882 | 2.00151 | 99.9061 | 0.500154 | 421.086 | 53.5361 | 0.623439 | 476.166 | 20.7502 | 0.325921 | 47.8422 | 316.849 | 211.266 | 194.4428 | 15966.53 |
| 14370.5 | 25.2807 | 0.936919 | 91.0245 | 2.56066 | 52.5564 | 0.474872 | 249.198 | 55.2144 | 0.454938 | 272.774 | 41.0236 | 0.554942 | 61.9542 | 72.0425 | 109.868 | 109.5333 | 9138.463 |
| 14777.2 | 32.9756 | 0.934668 | 157.711 | 2.02932 | 41.2072 | 0.257383 | 480.406 | 97.5372 | 0.67002 | 103.3 | 43.3654 | 0.672751 | 146.725 | 391.16 | 94.1044 | 146.0427 | 12024.98 |
| 25354.3 | 30.1064 | 0.875846 | 78.4013 | 0.147442 | 99.2709 | 0.480769 | 516.544 | 37.8305 | 0.493588 | 392.192 | 49.4771 | 0.547679 | 6.09469 | 385.383 | 130.847 | 152.2721 | 12507.44 |
| 19584.3 | 28.0333 | 0.90793 | 163.829 | 0.647727 | 5.93134 | 0.466748 | 338.685 | 11.9087 | 0.478712 | 268.013 | 59.1767 | 0.632211 | 32.2095 | 104.531 | 68.244 | 135.2051 | 9260.48 |
| 17151.7 | 17.9111 | 0.921448 | 160.235 | 0.537447 | 83.2058 | 0.555456 | 377.328 | 5.68309 | 0.29286 | 98.9842 | 42.1863 | 0.502556 | 2.52351 | 67.204 | 63.9633 | 235.7869 | 19379.83 |
| 27524 | 30.2029 | 0.86378 | 133.668 | 2.66832 | 27.1041 | 0.520083 | 316.3 | 88.0298 | 0.62488 | 250.651 | 62.955 | 0.973694 | 169.685 | 224.115 | 209.432 | 60.63494 | 4089.571 |
| 19749.5 | 31.4451 | 0.907015 | 136.074 | 3.75298 | 43.3888 | 0.170012 | 155.243 | 12.9028 | 0.933052 | 367.401 | 41.716 | 0.732215 | 14.1568 | 56.0131 | 57.9431 | 150.5702 | 12637.18 |
| 30259.5 | 31.1529 | 0.848569 | 45.4115 | 1.34472 | 31.8083 | 0.315666 | 306.34 | 33.5854 | 0.893939 | 477.361 | 82.4817 | 0.421616 | 38.6225 | 60.791 | 132.544 | 148.876 | 10327.7 |
| 49823.7 | 17.7583 | 0.739766 | 101.152 | 0.373723 | 80.0039 | 0.510505 | 155.636 | 73.6899 | 0.545878 | 463.004 | 77.7118 | 0.699245 | 34.3217 | 122.962 | 263.531 | 143.6117 | 9185.553 |
| 16535.1 | 32.3677 | 0.924891 | 156.926 | 3.2475 | 97.2258 | 0.384713 | 482.613 | 60.1214 | 0.953336 | 476.864 | 21.8953 | 0.345823 | 15.5553 | 357.841 | 245.876 | 143.9889 | 13184.38 |
| 23900.4 | 23.4615 | 0.883924 | 77.0678 | 2.5242 | 7.29961 | 0.323502 | 514.295 | 65.3885 | 0.817212 | 384.341 | 4.17612 | 0.251581 | 25.0269 | 385.068 | 162.229 | 230.5789 | 15068.47 |
| 12424.5 | 32.1478 | 0.94775 | 155.18 | 2.42834 | 55.8831 | 0.274754 | 160.367 | 2.55115 | 0.817264 | 467.557 | 93.195 | 0.763278 | 85.6702 | 83.8379 | 151.396 | 90.53083 | 8285.143 |
| 27887.8 | 31.9534 | 0.861759 | 82.0582 | 3.11678 | 18.3833 | 0.529613 | 252.882 | 59.5689 | 0.911539 | 464.802 | 79.3102 | 0.967975 | 82.1461 | 234.256 | 293.946 | 44.32629 | 2936.935 |
| 21809.1 | 34.82 | 0.895567 | 127.623 | 1.92539 | 38.8068 | 0.485563 | 96.4087 | 28.4131 | 0.720254 | 355.998 | 83.8461 | 0.881524 | 122.083 | 53.9502 | 78.5601 | 55.92767 | 4202.034 |
| 31701.1 | 14.572 | 0.84054 | 134.828 | 1.77845 | 66.8317 | 0.209731 | 165.527 | 38.5847 | 0.884139 | 510.984 | 85.5748 | 0.63346 | 127.332 | 67.7511 | 452.818 | 181.3854 | 14078.11 |
| 29037.7 | 20.3565 | 0.855354 | 49.0779 | 1.12361 | 89.2209 | 0.477788 | 330.174 | 30.4904 | 0.887936 | 509.898 | 23.355 | 0.59709 | 36.4054 | 53.6423 | 472.172 | 68.40209 | 5518.198 |
| 29548 | 16.197 | 0.852514 | 84.1418 | 1.7585 | 48.2532 | 0.246424 | 113.789 | 60.2734 | 0.63975 | 233.429 | 60.9741 | 0.859071 | 100.8 | 55.5089 | 199.404 | 129.4973 | 9859.096 |
| 15475.2 | 15.9619 | 0.930769 | 163.903 | 3.26283 | 38.3507 | 0.389932 | 306.902 | 48.9618 | 0.935762 | 187.556 | 99.7697 | 0.948595 | 86.638 | 115.297 | 161.145 | 57.5106 | 4545.735 |
| 42561.5 | 20.2935 | 0.780151 | 29.9274 | 2.20193 | 14.49 | 0.519722 | 144.606 | 1.15643 | 0.63392 | 292.165 | 11.2105 | 0.748777 | 128.57 | 109.509 | 230.083 | 84.40804 | 4980.044 |
| 33587.2 | 30.2986 | 0.830063 | 75.1636 | 0.833558 | 90.1051 | 0.369795 | 462.3 | 69.5298 | 0.5558 | 461.65 | 44.1328 | 0.778612 | 37.6857 | 77.4744 | 449.616 | 125.1036 | 10043.83 |
| 20669.5 | 28.0757 | 0.901895 | 59.0226 | 1.41893 | 62.199 | 0.276401 | 252.939 | 39.8076 | 0.505155 | 194.764 | 43.9186 | 0.98499 | 119.306 | 60.4032 | 191.088 | 111.0946 | 9739.853 |
| 47533.8 | 31.2707 | 0.752509 | 157.079 | 0.918925 | 34.133 | 0.513684 | 333.103 | 2.09897 | 0.730619 | 229.77 | 56.104 | 0.387992 | 59.6947 | 254.286 | 130.749 | 198.603 | 11511.48 |
| 40636.1 | 18.3 | 0.790856 | 143.732 | 1.30057 | 60.3604 | 0.446183 | 142.876 | 45.1995 | 0.683354 | 401.138 | 20.9956 | 0.585506 | 95.2217 | 75.8054 | 45.269 | 137.6141 | 9155.751 |
| 22896.7 | 18.6952 | 0.889501 | 78.2262 | 0.631833 | 18.9077 | 0.133161 | 436.818 | 96.5494 | 0.775965 | 212.931 | 58.0393 | 0.918957 | 51.1119 | 216.168 | 111.583 | 227.991 | 16224.6 |
| 56693.2 | 22.2885 | 0.701569 | 154.558 | 0.65128 | 30.6639 | 0.523341 | 248.941 | 46.1306 | 0.614759 | 486.47 | 73.6608 | 0.949627 | 59.7944 | 214.536 | 239.251 | 111.0398 | 6140.837 |
| 46651.3 | 22.5333 | 0.75741 | 85.295 | 3.57719 | 81.6685 | 0.317948 | 162.071 | 94.2774 | 0.76267 | 429.451 | 24.0642 | 0.886308 | 93.0166 | 45.038 | 391.271 | 109.8791 | 7983.706 |
| 29034.8 | 20.5087 | 0.85537 | 28.7123 | 0.224411 | 3.97019 | 0.328287 | 344.287 | 12.4479 | 0.817694 | 246.973 | 39.7592 | 0.75265 | 16.1949 | 185.521 | 188.019 | 75.46346 | 4846.29 |
| 48057.7 | 29.5953 | 0.749595 | 60.4741 | 0.673725 | 35.0824 | 0.233099 | 282.389 | 46.5856 | 0.929516 | 291.689 | 51.5393 | 0.973167 | 5.34634 | 230.158 | 187.291 | 139.5118 | 8771.205 |
| 20743.6 | 29.4688 | 0.901484 | 69.0984 | 3.64749 | 68.2826 | 0.441416 | 482.953 | 83.648 | 0.945357 | 387.757 | 63.0515 | 0.180643 | 88.6607 | 209.083 | 352.948 | 233.2657 | 18329.07 |
| 36867 | 15.7431 | 0.811814 | 94.5871 | 1.55362 | 53.2777 | 0.378803 | 156.155 | 36.5183 | 0.791759 | 325.336 | 98.7693 | 0.582275 | 151.043 | 128.686 | 90.5348 | 114.883 | 8034.684 |
| 23079.8 | 20.4587 | 0.888485 | 145.379 | 2.37271 | 86.3009 | 0.220512 | 221.857 | 80.2485 | 0.748483 | 374.379 | 94.1051 | 0.962468 | 4.78837 | 168.829 | 252.305 | 141.4322 | 12413.86 |
| 51045.9 | 28.9756 | 0.732977 | 162.143 | 0.433591 | 15.5692 | 0.684756 | 371.82 | 66.1503 | 0.883851 | 299.75 | 67.2734 | 0.429415 | 41.7655 | 226.067 | 99.6988 | 138.6562 | 7478.364 |
| 11924.6 | 20.6273 | 0.950517 | 154.046 | 0.313842 | 64.4306 | 0.466923 | 370.59 | 95.2383 | 0.861929 | 464.034 | 43.9268 | 0.799301 | 9.29813 | 174.988 | 364.525 | 63.35181 | 5358.542 |
| 45767.3 | 31.9562 | 0.762333 | 160.21 | 1.12527 | 9.19721 | 0.463265 | 471.348 | 35.5965 | 0.297084 | 296.196 | 79.4588 | 0.897361 | 80.5098 | 143.396 | 101.757 | 227.2024 | 12556.01 |
| 27349.4 | 15.9162 | 0.86474 | 164.681 | 0.946729 | 39.6648 | 0.570679 | 393.54 | 12.47 | 0.631122 | 211.634 | 85.6321 | 0.875209 | 57.9868 | 159.696 | 209.296 | 71.64156 | 4942.324 |
| 46514.6 | 27.9091 | 0.758174 | 59.726 | 3.15166 | 89.1222 | 0.264531 | 153.482 | 45.8692 | 0.869832 | 432.262 | 46.7463 | 0.653119 | 117.975 | 110.408 | 306.701 | 158.1105 | 11877.69 |
| 16227.3 | 15.2152 | 0.926586 | 102.864 | 2.55465 | 52.5687 | 0.178392 | 262.209 | 43.8551 | 0.542927 | 328.699 | 69.011 | 0.964503 | 120.636 | 97.7204 | 251.788 | 150.1303 | 13630.66 |
| 32691.4 | 22.7705 | 0.835038 | 79.6333 | 1.60914 | 73.0993 | 0.35908 | 404.911 | 93.5856 | 0.572885 | 500.706 | 22.8401 | 0.533476 | 43.361 | 112.883 | 246.831 | 176.9039 | 13593.1 |
| 52704.9 | 22.5656 | 0.723747 | 168.807 | 2.36895 | 35.4689 | 0.413036 | 277.375 | 50.053 | 0.322394 | 132.57 | 10.2287 | 0.94373 | 165.682 | 180.809 | 55.3924 | 229.7168 | 13190.33 |
| 21353.9 | 16.7631 | 0.898079 | 156.879 | 1.74139 | 20.9551 | 0.556414 | 271.072 | 21.9391 | 0.936696 | 324.15 | 22.6793 | 0.711658 | 51.3303 | 89.8496 | 76.8417 | 46.12507 | 3381.069 |
| 35194.2 | 23.7681 | 0.821121 | 35.6642 | 0.470205 | 24.7667 | 0.206405 | 364.387 | 74.2838 | 0.907627 | 315.137 | 89.8442 | 0.933793 | 3.75438 | 286.095 | 150.859 | 140.4897 | 9199.817 |
| 13257.9 | 17.4624 | 0.9431 | 64.2907 | 0.328718 | 29.3509 | 0.163657 | 436.751 | 25.7045 | 0.872756 | 335.616 | 66.2744 | 0.494534 | 20.3327 | 82.1528 | 61.4205 | 184.4953 | 15644.14 |
| 13210.3 | 29.6541 | 0.943376 | 66.9472 | 0.768689 | 78.4608 | 0.305134 | 159.362 | 37.6578 | 0.973557 | 377.746 | 25.7067 | 0.830869 | 18.1154 | 145.012 | 116.501 | 57.71127 | 5875.689 |
| 31846.9 | 18.1192 | 0.839731 | 161.465 | 1.95093 | 95.0001 | 0.601111 | 450.003 | 42.6831 | 0.990489 | 224.665 | 17.2404 | 0.378019 | 33.3383 | 334.6 | 184.491 | 103.3262 | 7303.711 |
| 27929.1 | 30.4082 | 0.861528 | 136.495 | 0.590172 | 79.9472 | 0.212159 | 238.014 | 20.3878 | 0.799471 | 394.58 | 56.616 | 0.757703 | 40.0373 | 124.622 | 64.7787 | 176.9867 | 14483.62 |
| 30822.4 | 27.7717 | 0.845435 | 95.7166 | 3.36578 | 49.6385 | 0.193531 | 475.464 | 42.0134 | 0.674656 | 443.96 | 49.0518 | 0.767847 | 28.9369 | 394.948 | 271.506 | 178.2632 | 13673.59 |
| 31674 | 18.535 | 0.840693 | 45.5337 | 1.26801 | 0.087475 | 0.14732 | 311.676 | 33.6798 | 0.947981 | 144.32 | 53.7912 | 0.855344 | 23.7694 | 82.3103 | 111.596 | 186.081 | 11085.19 |
| 36339.6 | 31.6491 | 0.814759 | 109.841 | 1.84367 | 14.5156 | 0.40418 | 436.367 | 18.8863 | 0.842112 | 73.1867 | 43.7791 | 0.598814 | 9.67287 | 48.4807 | 55.1942 | 92.42298 | 5753.819 |
| 23535.9 | 16.4041 | 0.885946 | 140.56 | 3.60853 | 72.0757 | 0.364927 | 144.87 | 32.2872 | 0.485386 | 51.6268 | 5.59726 | 0.455557 | 5.8101 | 115.958 | 48.0311 | 209.5102 | 17556.4 |
| 12850.3 | 32.5648 | 0.945382 | 49.0672 | 3.49333 | 39.3498 | 0.312161 | 494.598 | 61.3195 | 0.671782 | 189.666 | 67.9521 | 0.799166 | 84.8694 | 488.915 | 46.7906 | 79.09104 | 6846.437 |
| 34797.7 | 28.0348 | 0.82333 | 146.503 | 0.638236 | 50.8648 | 0.613787 | 496.35 | 89.0835 | 0.310942 | 367.546 | 15.759 | 0.729036 | 26.1054 | 457.997 | 93.9965 | 175.9822 | 11283.2 |
| 21409.5 | 16.5838 | 0.89777 | 99.7145 | 3.71662 | 21.0041 | 0.507696 | 203.222 | 83.2762 | 0.916751 | 296.739 | 33.6288 | 0.699478 | 232.932 | 194.459 | 187.458 | 54.29835 | 3771.442 |
| 33103.7 | 17.3028 | 0.832742 | 98.6181 | 2.5318 | 29.5956 | 0.413949 | 121.317 | 74.0953 | 0.436007 | 515.644 | 11.1261 | 0.79075 | 45.018 | 66.7711 | 369.278 | 122.0589 | 8161.013 |
| 30097.3 | 21.6313 | 0.849463 | 147.095 | 2.79752 | 34.2978 | 0.530514 | 378.467 | 67.7895 | 0.957829 | 62.8219 | 33.4989 | 0.240255 | 97.0428 | 324.444 | 51.7112 | 171.5378 | 11116.14 |
| 24900.6 | 28.9505 | 0.878367 | 38.3041 | 0.570455 | 63.7466 | 0.294207 | 437.931 | 14.5563 | 0.79498 | 409.176 | 67.1794 | 0.408745 | 28.1205 | 137.135 | 218.661 | 172.621 | 14360.39 |
| 11988.8 | 25.8847 | 0.950164 | 171.277 | 0.415724 | 6.84224 | 0.854932 | 453.734 | 22.4239 | 0.688336 | 505.681 | 72.8332 | 0.763569 | 33.1085 | 281.476 | 414.459 | 61.50566 | 4538.213 |
| 21002.2 | 21.239 | 0.900038 | 74.1681 | 1.16347 | 24.2676 | 0.168251 | 196.935 | 80.1027 | 0.739322 | 327.842 | 89.1866 | 0.702242 | 48.0163 | 60.8853 | 167.292 | 171.5554 | 12825.37 |
| 18077.9 | 33.3855 | 0.916313 | 84.926 | 1.27285 | 23.3509 | 0.167996 | 88.1264 | 12.292 | 0.470277 | 478.8 | 31.5129 | 0.790048 | 41.3787 | 75.3915 | 447.496 | 211.1053 | 16589.42 |
| 25713.1 | 29.9808 | 0.87385 | 111.937 | 0.43745 | 3.79411 | 0.629627 | 322.24 | 39.4585 | 0.908145 | 285.224 | 24.6878 | 0.389416 | 32.6113 | 210.962 | 275.555 | 106.6403 | 6755.893 |
| 11069.3 | 34.3891 | 0.95529 | 77.1279 | 0.428093 | 67.8149 | 0.278689 | 496.946 | 99.7897 | 0.45651 | 445.628 | 57.1477 | 0.638773 | 30.5438 | 489.677 | 316.435 | 176.8598 | 17021.26 |
| 19555.7 | 15.6171 | 0.908078 | 62.1131 | 0.551855 | 12.5547 | 0.375439 | 204.619 | 7.60116 | 0.301086 | 342.641 | 81.4282 | 0.80948 | 24.3149 | 120.226 | 126.053 | 143.6575 | 10251.84 |
| 29322.8 | 32.505 | 0.85378 | 51.4628 | 2.81017 | 11.2873 | 0.346693 | 486.331 | 66.3203 | 0.938182 | 179.935 | 88.3285 | 0.953152 | 150.422 | 333.178 | 105.171 | 66.04671 | 4272.49 |
| 12171.2 | 25.9542 | 0.94915 | 136.715 | 1.41596 | 52.2411 | 0.486509 | 98.7946 | 18.6705 | 0.506743 | 394.868 | 55.2264 | 0.952858 | 136.667 | 54.0078 | 364.225 | 60.97098 | 5369.101 |
| 16937.1 | 29.3893 | 0.922652 | 43.7755 | 1.20818 | 74.1565 | 0.348719 | 134.162 | 85.7766 | 0.873804 | 106.006 | 6.75072 | 0.763705 | 20.4332 | 68.4117 | 80.3382 | 67.01762 | 6163.385 |
| 31438.9 | 28.7342 | 0.842009 | 66.3462 | 0.921198 | 57.9991 | 0.338639 | 258.761 | 18.5237 | 0.965448 | 420.161 | 42.0534 | 0.411717 | 64.8492 | 66.1825 | 342.112 | 133.8754 | 10177.06 |
| 33147.4 | 16.1684 | 0.832498 | 91.25 | 0.914262 | 23.3718 | 0.326518 | 193.341 | 48.0013 | 0.912769 | 428.857 | 31.3979 | 0.8975 | 11.6984 | 106.868 | 300.533 | 71.34627 | 4793.791 |
| 31288.4 | 33.911 | 0.842851 | 150.822 | 0.997706 | 30.6511 | 0.264783 | 252.038 | 11.6873 | 0.721553 | 118.862 | 91.7037 | 0.848588 | 31.4597 | 183.64 | 61.6027 | 140.6067 | 9480.901 |
| 56538.8 | 21.4977 | 0.702427 | 44.7362 | 3.31477 | 46.0679 | 0.431383 | 151.329 | 19.5649 | 0.850026 | 259.038 | 91.76 | 0.856957 | 16.8887 | 133.636 | 112.353 | 80.08477 | 4876.136 |
| 37030.7 | 21.312 | 0.810907 | 127.248 | 2.21359 | 77.7384 | 0.275212 | 187.923 | 25.754 | 0.935515 | 475.19 | 83.311 | 0.63916 | 3.6539 | 150.519 | 180.212 | 135.0269 | 10361.2 |
| 21403.6 | 25.7942 | 0.89781 | 108.086 | 0.286238 | 38.3023 | 0.494772 | 316.71 | 72.1474 | 0.6672 | 159.485 | 57.7004 | 0.813505 | 14.1954 | 263.593 | 102.633 | 71.42462 | 5251.62 |
| 39115.2 | 16.4676 | 0.799313 | 109.703 | 0.459151 | 97.207 | 0.592156 | 337.002 | 71.4203 | 0.513676 | 141.272 | 16.9631 | 0.842242 | 22.9047 | 119.998 | 124.005 | 98.44883 | 6631.988 |
| 48794.8 | 19.1686 | 0.745489 | 43.707 | 1.99047 | 99.4567 | 0.49074 | 83.2011 | 10.0749 | 0.711758 | 264.537 | 92.0918 | 0.726023 | 134.302 | 49.9409 | 179.792 | 90.38178 | 6055.139 |
| 18011.7 | 23.3371 | 0.91667 | 33.4937 | 3.63661 | 28.4249 | 0.356999 | 361.485 | 38.4179 | 0.8586 | 347.316 | 14.0515 | 0.457946 | 132.231 | 83.5135 | 178.971 | 97.24037 | 7602.479 |
| 34847.6 | 20.775 | 0.823046 | 62.4953 | 0.431111 | 14.3637 | 0.368869 | 397.905 | 17.4276 | 0.906016 | 155.96 | 96.8334 | 0.681591 | 20.6934 | 234.448 | 56.6045 | 81.41939 | 5136.599 |
| 33861.1 | 29.245 | 0.828539 | 157.066 | 2.02759 | 61.0472 | 0.606258 | 367.147 | 82.6899 | 0.836553 | 115.841 | 27.7824 | 0.412152 | 34.9215 | 88.6956 | 94.4855 | 121.1578 | 7775.082 |
| 35815.5 | 16.9547 | 0.817662 | 154.267 | 3.21512 | 3.96667 | 0.283779 | 141.625 | 26.9073 | 0.889589 | 78.647 | 81.3704 | 0.825437 | 38.2578 | 63.721 | 46.7522 | 99.33615 | 5930.18 |
| 60024.1 | 23.0057 | 0.683047 | 141.16 | 0.15278 | 47.8772 | 0.60414 | 431.262 | 25.0757 | 0.40408 | 490.157 | 10.0883 | 0.717771 | 5.23632 | 217.569 | 342.26 | 206.2077 | 11198.89 |
| 16956.9 | 33.1607 | 0.922547 | 137.662 | 2.17556 | 96.7073 | 0.598737 | 486.965 | 75.0352 | 0.814237 | 272.05 | 79.6815 | 0.771517 | 83.6324 | 464.734 | 181.424 | 58.6961 | 4625.542 |
| 36569.3 | 17.3034 | 0.813471 | 139.577 | 2.40157 | 71.5933 | 0.559303 | 385.09 | 42.039 | 0.909668 | 519.967 | 26.9987 | 0.311581 | 185.682 | 230.41 | 396.75 | 152.4907 | 9953.639 |
| 19591.1 | 23.9197 | 0.907887 | 39.8118 | 0.265761 | 57.976 | 0.25344 | 170.784 | 21.5896 | 0.419783 | 255.853 | 92.8258 | 0.956356 | 25.6056 | 165.02 | 74.8776 | 147.5732 | 12891.88 |
| 33212.1 | 25.637 | 0.832145 | 105.719 | 2.14034 | 88.8166 | 0.262067 | 322.582 | 48.5985 | 0.51161 | 419.624 | 86.8512 | 0.779773 | 32.4001 | 294.813 | 385.064 | 191.7888 | 15933.28 |
| 13343.3 | 27.1252 | 0.942634 | 144.487 | 0.558639 | 68.8286 | 0.682993 | 438.89 | 40.9218 | 0.998194 | 327.535 | 39.0656 | 0.915428 | 14.5762 | 267.728 | 205.589 | 32.58716 | 2688.369 |
| 32452.4 | 25.6988 | 0.836369 | 162.17 | 0.546324 | 27.5003 | 0.318902 | 193.542 | 14.4255 | 0.808029 | 305.969 | 26.7974 | 0.429248 | 12.1784 | 61.6205 | 258.389 | 226.5824 | 14674.9 |
| 40264.8 | 13.0925 | 0.792919 | 48.2906 | 3.11218 | 50.4233 | 0.522449 | 197.836 | 95.7187 | 0.791426 | 170.211 | 5.41151 | 0.754056 | 17.6406 | 122.321 | 136.817 | 77.08377 | 4951.528 |
| 24860.6 | 19.7566 | 0.878582 | 158.604 | 1.28607 | 31.9469 | 0.404883 | 159.043 | 48.2947 | 0.832763 | 515.525 | 59.8841 | 0.531819 | 11.1675 | 137.269 | 513.498 | 116.3212 | 8154.597 |
| 18115.6 | 17.4788 | 0.916087 | 35.7987 | 1.64247 | 74.5383 | 0.247988 | 277.853 | 60.6761 | 0.572515 | 172.187 | 80.5247 | 0.717285 | 89.4349 | 81.5849 | 74.2182 | 152.2983 | 14129.62 |
| 32315.5 | 26.424 | 0.837131 | 98.3987 | 2.02654 | 50.1316 | 0.336275 | 422.671 | 16.3421 | 0.735619 | 141.705 | 34.4112 | 0.62334 | 59.4438 | 127.331 | 82.8279 | 114.2647 | 8483.381 |
| 39367.1 | 16.9723 | 0.797913 | 127.842 | 0.788668 | 58.8484 | 0.35524 | 318.05 | 15.3186 | 0.866899 | 180.049 | 79.9865 | 0.429131 | 45.1733 | 89.0631 | 165.357 | 182.436 | 12450.56 |
| 56309.7 | 25.6471 | 0.703703 | 57.1969 | 0.756092 | 92.0744 | 0.349687 | 492.274 | 64.7178 | 0.585701 | 219.285 | 33.0746 | 0.585062 | 29.4218 | 70.6402 | 173.471 | 218.6123 | 15057.81 |
| 32505.4 | 29.7488 | 0.836079 | 124.685 | 3.72928 | 15.3462 | 0.395846 | 505.155 | 40.1149 | 0.677163 | 374.889 | 52.6465 | 0.680689 | 68.2567 | 314.271 | 115.086 | 96.19358 | 6164.184 |
| 52835.9 | 28.9612 | 0.723023 | 83.1396 | 0.593295 | 34.0978 | 0.532035 | 313.458 | 88.2848 | 0.701346 | 362.004 | 66.6957 | 0.816084 | 58.2417 | 185.941 | 300.814 | 87.68924 | 5010.942 |
| 10675.7 | 21.0582 | 0.957462 | 128.14 | 0.868456 | 65.0948 | 0.532232 | 446.134 | 94.0712 | 0.369804 | 198.614 | 64.6291 | 0.63563 | 65.5572 | 274.316 | 108.368 | 123.0409 | 10631.08 |
| 13189.4 | 26.6096 | 0.943489 | 85.1337 | 1.74181 | 17.4544 | 0.278506 | 250.915 | 0.503088 | 0.586339 | 462.103 | 53.8489 | 0.461291 | 71.8175 | 188.404 | 340.136 | 153.3507 | 12316.32 |
| 28857.9 | 28.2675 | 0.856361 | 117.175 | 0.299442 | 4.82134 | 0.432935 | 342.42 | 32.5244 | 0.394202 | 82.5081 | 88.5858 | 0.940153 | 22.2143 | 153.639 | 66.1542 | 127.8698 | 7972.163 |
| 13004.9 | 33.4458 | 0.944524 | 64.0779 | 0.512468 | 71.4025 | 0.31864 | 493.805 | 16.7928 | 0.596287 | 503.654 | 86.3437 | 0.536585 | 24.3046 | 209.779 | 396.602 | 134.2872 | 13007.27 |
| 21963.4 | 14.1699 | 0.894689 | 95.9793 | 0.169262 | 93.0723 | 0.298915 | 442.774 | 63.4418 | 0.962889 | 273.744 | 49.6878 | 0.75901 | 2.08193 | 81.5814 | 76.5383 | 96.24173 | 8461.195 |
| 48580.5 | 26.0546 | 0.746684 | 73.7715 | 1.47228 | 46.8808 | 0.25466 | 200.032 | 23.0127 | 0.778413 | 328.537 | 74.6678 | 0.533836 | 65.3569 | 51.809 | 109.268 | 214.1765 | 13915.95 |
| 22255.8 | 29.4998 | 0.893075 | 134.049 | 0.757437 | 3.72034 | 0.474801 | 356.742 | 51.7543 | 0.997347 | 79.1689 | 69.3892 | 0.94667 | 16.9296 | 42.8943 | 69.2027 | 51.29957 | 3437.299 |
| 11122.7 | 33.0885 | 0.95499 | 69.9448 | 3.02911 | 77.5336 | 0.382748 | 324.95 | 49.1639 | 0.722304 | 194.186 | 97.1553 | 0.807123 | 85.5899 | 197.318 | 102.128 | 64.41717 | 6205.413 |
| 36596 | 18.1094 | 0.813322 | 46.849 | 1.50072 | 49.5456 | 0.432463 | 100.812 | 28.6743 | 0.548835 | 315.104 | 45.9085 | 0.480707 | 8.26999 | 80.4524 | 216.573 | 163.8553 | 11285.62 |
| 18710 | 33.9141 | 0.912799 | 145.88 | 2.08281 | 51.0818 | 0.286736 | 184.594 | 14.7771 | 0.872926 | 260.861 | 99.6183 | 0.306445 | 98.2404 | 177.056 | 230.729 | 222.8944 | 18270.63 |
| 21728.8 | 26.2561 | 0.896002 | 33.8382 | 2.58284 | 78.0211 | 0.505776 | 237.912 | 53.5108 | 0.796257 | 460.576 | 82.6191 | 0.298129 | 253.211 | 198.359 | 312.782 | 168.0471 | 12706.24 |
| 40160.5 | 27.0048 | 0.793507 | 131.76 | 0.269899 | 69.1882 | 0.523951 | 395.015 | 69.2344 | 0.623684 | 313.097 | 13.3652 | 0.898399 | 22.0104 | 194.004 | 254.063 | 93.44923 | 6202.383 |
| 35308.8 | 16.9843 | 0.82048 | 151.132 | 1.57953 | 69.4314 | 0.449857 | 460.605 | 47.746 | 0.684512 | 184.772 | 43.619 | 0.857261 | 103.56 | 188.454 | 95.2901 | 89.10601 | 6349.57 |
| 41492.2 | 20.9704 | 0.786098 | 131.342 | 2.55716 | 57.6714 | 0.320601 | 476.029 | 90.6667 | 0.849619 | 331.138 | 21.7658 | 0.506947 | 47.7917 | 56.1392 | 273.874 | 170.8849 | 11651.64 |
| 12814.1 | 19.4938 | 0.945569 | 147.914 | 1.52863 | 15.8994 | 0.239137 | 276.308 | 12.3338 | 0.917599 | 109.938 | 48.9808 | 0.291264 | 89.7879 | 145.682 | 100.046 | 224.6734 | 17557.75 |
| 21755 | 22.4437 | 0.895853 | 64.93 | 0.585548 | 40.8913 | 0.280266 | 316.733 | 76.7769 | 0.498478 | 80.6745 | 41.8732 | 0.851315 | 47.7886 | 252.808 | 50.3952 | 127.5718 | 10116.9 |
| 16095.2 | 34.5478 | 0.927341 | 120.532 | 1.52202 | 7.38864 | 0.523302 | 217.929 | 74.7355 | 0.840686 | 365.478 | 39.0845 | 0.46446 | 129.14 | 81.9672 | 289.438 | 76.821 | 5391.23 |
| 37979.5 | 29.8967 | 0.805638 | 158.129 | 2.21008 | 33.5822 | 0.393138 | 386.948 | 3.15376 | 0.843988 | 128.152 | 22.7151 | 0.975353 | 101.046 | 304.356 | 74.4506 | 71.45948 | 4717.12 |
| 56555 | 21.4666 | 0.702337 | 98.3932 | 0.240571 | 42.5413 | 0.47225 | 240.049 | 34.5103 | 0.300997 | 365.737 | 84.8821 | 0.875852 | 11.9905 | 126.536 | 271.742 | 233.5337 | 13294.63 |
| 56597.2 | 21.2235 | 0.702102 | 166.414 | 0.991728 | 7.94568 | 0.636643 | 397.821 | 60.4918 | 0.812984 | 315.476 | 3.85689 | 0.418557 | 67.1658 | 369.863 | 171.706 | 157.1609 | 8174.718 |
| 27263.7 | 14.6078 | 0.865215 | 15.5473 | 1.38675 | 63.5898 | 0.354207 | 300.965 | 78.4037 | 0.779542 | 408.978 | 97.3271 | 0.695076 | 84.6133 | 50.0738 | 304.932 | 97.20613 | 7568.805 |
| 27051.8 | 15.7668 | 0.866394 | 87.6519 | 3.63755 | 4.53626 | 0.528744 | 441.685 | 79.6634 | 0.975363 | 444.341 | 26.277 | 0.736032 | 182.432 | 101.654 | 361.785 | 52.6792 | 3377.534 |
| 16479.7 | 16.1042 | 0.925183 | 48.1894 | 0.490714 | 44.5275 | 0.261572 | 399.678 | 27.1337 | 0.453873 | 258.03 | 24.6714 | 0.614907 | 14.6806 | 206.609 | 209.781 | 182.3124 | 15826.08 |
| 58653.1 | 21.5509 | 0.69067 | 86.3551 | 0.552601 | 56.6451 | 0.488289 | 357.38 | 23.985 | 0.312982 | 191.123 | 76.5536 | 0.956612 | 16.4793 | 69.2959 | 78.8523 | 183.305 | 10825.25 |
| 43912.3 | 26.4269 | 0.772644 | 51.3062 | 1.11021 | 42.2187 | 0.453819 | 363.519 | 46.8535 | 0.438452 | 167.559 | 6.51228 | 0.823977 | 99.1624 | 328.282 | 74.3197 | 124.3224 | 7926.113 |
| 10552.1 | 31.2226 | 0.95816 | 141.916 | 1.33706 | 31.7561 | 0.311212 | 229.956 | 16.9079 | 0.819667 | 172.45 | 75.744 | 0.583832 | 123.799 | 181.717 | 153.17 | 96.06004 | 8229.501 |
| 45674.8 | 22.772 | 0.76284 | 101.89 | 1.48005 | 61.7357 | 0.555309 | 410.497 | 73.2009 | 0.514506 | 293.475 | 51.6206 | 0.633958 | 69.5194 | 383.013 | 212.267 | 169.4967 | 10336.61 |
| 55453.1 | 18.163 | 0.708463 | 141.537 | 2.13338 | 93.0197 | 0.378762 | 188.24 | 21.4415 | 0.440667 | 500.344 | 37.1176 | 0.708398 | 41.5454 | 185.034 | 333.616 | 238.4602 | 15998.88 |
| 44852.5 | 15.9598 | 0.767409 | 27.5207 | 0.244781 | 63.6553 | 0.248344 | 260.295 | 48.334 | 0.780402 | 112.068 | 0.78107 | 0.820608 | 22.6628 | 104.472 | 77.826 | 140.4692 | 10122.93 |
| 31017.3 | 25.1002 | 0.844349 | 165.035 | 1.13705 | 76.5828 | 0.339119 | 477.715 | 50.6306 | 0.956303 | 220.599 | 25.9042 | 0.377926 | 27.7023 | 130.505 | 83.1336 | 207.3307 | 15412.42 |
| 20795.2 | 19.4766 | 0.901188 | 77.6225 | 0.792762 | 9.45515 | 0.302305 | 386.962 | 37.4935 | 0.422682 | 168.1 | 75.3883 | 0.9888 | 17.4359 | 279.45 | 83.5371 | 111.3364 | 7768.747 |
| 40640.1 | 29.4194 | 0.790843 | 159.816 | 2.00213 | 64.0141 | 0.351572 | 302.884 | 47.5793 | 0.337021 | 331.545 | 69.5265 | 0.951937 | 143.471 | 224.356 | 297.907 | 228.3741 | 15460.28 |
| 37288.8 | 13.4377 | 0.809468 | 74.4219 | 0.493232 | 44.8911 | 0.303065 | 248.294 | 31.8489 | 0.975233 | 163.737 | 13.9869 | 0.394731 | 21.0558 | 160.2 | 118.75 | 171.4208 | 11861.61 |
| 46619.1 | 23.1839 | 0.757589 | 100.59 | 0.58549 | 36.9039 | 0.425095 | 351.798 | 18.6774 | 0.891295 | 149.414 | 19.5291 | 0.455642 | 54.4679 | 253.274 | 114.188 | 137.4905 | 8421.249 |
| 17406 | 30.4736 | 0.920046 | 88.4398 | 2.76163 | 81.6963 | 0.278428 | 514.681 | 41.4123 | 0.565937 | 286.91 | 54.8716 | 0.474089 | 145.342 | 236.73 | 112.795 | 203.2951 | 19314.27 |
| 14207.2 | 14.9993 | 0.93782 | 157.984 | 0.83368 | 98.1841 | 0.491948 | 244.784 | 25.6064 | 0.945815 | 101.77 | 30.5255 | 0.489613 | 46.2118 | 112.887 | 73.9765 | 81.01781 | 7387.239 |
| 49300.3 | 18.317 | 0.742677 | 80.9743 | 1.91226 | 53.4641 | 0.403904 | 131.431 | 12.8758 | 0.835773 | 402.492 | 56.1187 | 0.410572 | 162.433 | 45.7735 | 332.881 | 159.6747 | 10240.07 |
| 44506.4 | 13.6605 | 0.769333 | 145.415 | 0.170186 | 66.0509 | 0.653374 | 95.5511 | 19.6211 | 0.734544 | 289.966 | 87.5997 | 0.918643 | 4.62429 | 76.9712 | 285.453 | 72.07505 | 4461.845 |
| 37964.9 | 33.9902 | 0.805724 | 161.315 | 2.22136 | 26.1693 | 0.373902 | 70.2077 | 49.6602 | 0.708863 | 259.838 | 55.5098 | 0.558151 | 54.851 | 52.933 | 193.499 | 164.5767 | 10203.19 |
| 41715.4 | 22.5675 | 0.784857 | 116.258 | 3.00406 | 51.2715 | 0.240106 | 208.799 | 7.33236 | 0.620338 | 373.859 | 66.6165 | 0.849084 | 55.976 | 161.037 | 229.57 | 162.2766 | 11382.68 |
| 44509.2 | 18.8475 | 0.769319 | 46.7095 | 1.85071 | 86.7174 | 0.457359 | 240.873 | 72.7147 | 0.530943 | 52.8646 | 90.8566 | 0.764915 | 13.7055 | 72.9251 | 52.2282 | 124.1988 | 8725.28 |
| 25175.4 | 29.4381 | 0.87684 | 31.1152 | 3.02699 | 59.4385 | 0.37214 | 284.419 | 59.6172 | 0.888508 | 145.429 | 67.3134 | 0.641487 | 125.355 | 255.019 | 136.345 | 83.11908 | 6552.766 |
| 40993.8 | 33.4573 | 0.78888 | 140.947 | 3.04783 | 95.401 | 0.585717 | 353.104 | 4.28142 | 0.952113 | 340.767 | 38.7338 | 0.778566 | 58.2892 | 87.6071 | 254.47 | 55.23649 | 3823.526 |
| 13462.2 | 21.9216 | 0.941967 | 106.521 | 3.28611 | 91.0888 | 0.355456 | 414.59 | 93.7284 | 0.724508 | 284.165 | 50.9184 | 0.752143 | 126.999 | 279.145 | 174.491 | 79.39173 | 7729.779 |
| 33748.9 | 32.0172 | 0.829166 | 35.6385 | 1.72357 | 23.5204 | 0.407762 | 391.571 | 25.9791 | 0.403682 | 319.278 | 94.3058 | 0.996617 | 127.733 | 305.533 | 91.3585 | 111.3746 | 7231.573 |
| 16375.9 | 13.9949 | 0.925759 | 46.5912 | 0.660491 | 15.9285 | 0.422832 | 296.971 | 74.4433 | 0.641881 | 519.345 | 57.3081 | 0.380717 | 5.20081 | 192.47 | 204.925 | 133.099 | 9665.35 |
| 19428 | 23.257 | 0.908794 | 131.682 | 2.44026 | 56.3975 | 0.332211 | 439.38 | 28.0119 | 0.980795 | 495.93 | 5.11335 | 0.371556 | 60.4729 | 311.913 | 258.236 | 132.6293 | 11183.61 |
| 14948.8 | 33.1122 | 0.933714 | 144.027 | 0.494918 | 78.6744 | 0.413089 | 450.27 | 81.023 | 0.96337 | 386.102 | 8.8587 | 0.321485 | 38.5682 | 185.407 | 183.372 | 159.6717 | 13531.78 |
| 31929.4 | 17.3951 | 0.839272 | 32.6251 | 0.554641 | 75.5993 | 0.412596 | 72.3285 | 66.3918 | 0.445146 | 389.1 | 60.8148 | 0.881425 | 40.4776 | 63.2685 | 96.876 | 115.7365 | 8959.176 |
| 26465.9 | 24.1419 | 0.869658 | 134.627 | 1.58468 | 7.99794 | 0.457801 | 184.078 | 55.0247 | 0.63169 | 422.19 | 28.604 | 0.505397 | 112.176 | 122.737 | 272.808 | 123.7076 | 7955.789 |
| 15035 | 26.4923 | 0.933226 | 136.628 | 0.588711 | 84.415 | 0.374929 | 133.871 | 22.4524 | 0.92475 | 324.814 | 39.7107 | 0.373364 | 38.539 | 105.909 | 221.004 | 138.7116 | 12633.93 |
| 10682.1 | 16.4535 | 0.957422 | 128.623 | 0.759365 | 70.3788 | 0.389692 | 326.857 | 26.4583 | 0.29064 | 472.57 | 3.6188 | 0.822331 | 39.5585 | 71.8609 | 129.674 | 156.4821 | 14952.96 |
| 10596 | 30.6312 | 0.957915 | 111.591 | 1.63789 | 2.03056 | 0.252949 | 294.105 | 23.8033 | 0.818165 | 506.332 | 89.6036 | 0.363615 | 147.057 | 278.94 | 504.36 | 155.3913 | 11692.24 |
| 41458.7 | 26.7502 | 0.786288 | 129.245 | 0.426376 | 56.4359 | 0.63698 | 457.775 | 63.6187 | 0.412071 | 438.12 | 61.0754 | 0.59355 | 23.6454 | 154.262 | 77.9304 | 175.9493 | 10577.32 |
| 23774.9 | 23.1477 | 0.884621 | 86.5438 | 2.38304 | 35.6208 | 0.488901 | 270.704 | 66.1624 | 0.967413 | 502.538 | 38.3889 | 0.624698 | 91.1818 | 220.882 | 413.128 | 56.89823 | 4052.651 |
| 35060.8 | 14.1933 | 0.821857 | 58.23 | 1.92893 | 26.6989 | 0.250143 | 399.294 | 6.95696 | 0.767112 | 386.818 | 58.9653 | 0.816019 | 86.4287 | 306.75 | 247.284 | 112.2917 | 7580.21 |
| 34891.7 | 29.2211 | 0.822808 | 30.7506 | 2.734 | 95.6672 | 0.434922 | 127.138 | 9.9931 | 0.640989 | 53.2574 | 89.5529 | 0.74423 | 145.887 | 122.83 | 45.3291 | 96.04214 | 7563.958 |
| 41102.1 | 22.0764 | 0.788268 | 76.6983 | 0.123892 | 19.9592 | 0.300599 | 116.209 | 11.2924 | 0.598347 | 207.92 | 59.4835 | 0.90732 | 6.78488 | 110.712 | 82.1274 | 139.105 | 8463.929 |
| 20905.5 | 33.4917 | 0.900589 | 169.391 | 1.09017 | 32.4151 | 0.379187 | 103.945 | 80.9495 | 0.515177 | 438.576 | 5.95782 | 0.960994 | 9.42924 | 66.0544 | 336.49 | 108.4917 | 7994.037 |
| 22955.7 | 24.4212 | 0.889178 | 25.4703 | 0.758339 | 31.7527 | 0.252569 | 373.256 | 72.3962 | 0.562457 | 153.2 | 67.9999 | 0.491601 | 38.0906 | 223.245 | 92.5083 | 221.1616 | 16550.8 |
| 35796.6 | 17.7854 | 0.817768 | 89.6711 | 1.77127 | 1.75042 | 0.149325 | 163.487 | 30.2029 | 0.658945 | 497.018 | 2.74852 | 0.940365 | 136.731 | 100.691 | 362.183 | 188.5503 | 11065.5 |
| 38287.1 | 13.5843 | 0.803917 | 38.4034 | 2.65773 | 91.2286 | 0.412685 | 174.203 | 27.3901 | 0.786441 | 456.089 | 40.8012 | 0.492089 | 96.7852 | 60.4168 | 270.558 | 126.4935 | 9737.958 |
| 35355.6 | 14.5196 | 0.820218 | 146.384 | 1.35067 | 54.4603 | 0.274606 | 474.778 | 40.3372 | 0.722023 | 379.313 | 94.3404 | 0.724236 | 14.4929 | 236.561 | 363.386 | 164.5075 | 11591.68 |
| 34561 | 13.2236 | 0.824636 | 68.6419 | 0.213061 | 96.3771 | 0.538773 | 295.295 | 1.68668 | 0.354799 | 519.071 | 90.2917 | 0.5708 | 18.016 | 290.297 | 413.479 | 195.7529 | 13980.73 |
| 37259.8 | 21.6483 | 0.809633 | 75.0839 | 0.427642 | 36.8137 | 0.486864 | 80.3928 | 13.4354 | 0.634033 | 260.373 | 38.7438 | 0.610101 | 4.406 | 70.7381 | 160.89 | 102.6707 | 6731.485 |
| 27996.4 | 33.1121 | 0.861157 | 122.59 | 1.59543 | 11.2641 | 0.474962 | 139.624 | 57.1894 | 0.893487 | 442.574 | 58.1228 | 0.532496 | 10.1675 | 53.83 | 231.602 | 84.6121 | 5443.926 |
| 58024.4 | 22.9784 | 0.694167 | 57.6488 | 3.17188 | 50.0969 | 0.298077 | 212.323 | 95.1082 | 0.664251 | 144.029 | 8.76886 | 0.544023 | 110.125 | 112.06 | 74.0137 | 239.3944 | 14639.31 |
| 17290.6 | 33.3197 | 0.920691 | 139.707 | 3.25366 | 83.9163 | 0.279929 | 225.426 | 72.9725 | 0.584865 | 510.855 | 21.2207 | 0.69878 | 70.4168 | 145.094 | 156.127 | 144.7311 | 13619.58 |
| 33115.7 | 27.8465 | 0.832683 | 158.871 | 0.92173 | 43.3261 | 0.482336 | 346.268 | 35.227 | 0.765674 | 307.207 | 10.8806 | 0.945205 | 21.3831 | 170.352 | 286.417 | 67.40241 | 4616.112 |
| 25766.8 | 19.9733 | 0.873542 | 78.7758 | 0.561864 | 67.6711 | 0.191843 | 100.474 | 72.4279 | 0.728958 | 415.02 | 91.4987 | 0.750691 | 42.7657 | 85.5959 | 182.402 | 176.7981 | 14810.59 |
| 20524.1 | 20.0377 | 0.902696 | 44.9907 | 1.47454 | 89.6005 | 0.439132 | 151.486 | 37.6048 | 0.753136 | 472.544 | 7.34628 | 0.933683 | 6.62124 | 50.5941 | 198.753 | 48.38612 | 4551.906 |
| 33272.2 | 20.4407 | 0.831807 | 51.1474 | 3.7743 | 63.6408 | 0.341454 | 344.073 | 5.3127 | 0.718828 | 479.861 | 17.7036 | 0.673794 | 124.932 | 107.864 | 126.226 | 106.8722 | 8298.169 |
| 39919.1 | 16.8059 | 0.794843 | 143.512 | 3.1782 | 40.6352 | 0.519401 | 385.725 | 57.3863 | 0.734993 | 506.444 | 80.9766 | 0.383499 | 84.3118 | 127.646 | 92.0704 | 154.9429 | 9606.486 |
| 10521.4 | 31.5319 | 0.958332 | 45.2065 | 1.15588 | 79.0937 | 0.369066 | 370.967 | 97.1926 | 0.935045 | 206.301 | 25.7157 | 0.590037 | 63.5487 | 329.214 | 83.0348 | 72.52442 | 6991.28 |
| 17265.6 | 25.7301 | 0.920821 | 105.474 | 0.227145 | 16.2049 | 0.47167 | 338.596 | 4.88038 | 0.531761 | 513.871 | 99.0374 | 0.486389 | 6.08006 | 285.63 | 117.046 | 132.0634 | 9580.398 |
| 12560.8 | 16.2211 | 0.946976 | 33.6141 | 2.93458 | 80.6305 | 0.269114 | 494.151 | 56.974 | 0.757253 | 379.546 | 6.48371 | 0.90256 | 118.287 | 76.5961 | 127.468 | 74.46754 | 7749.508 |
| 25653.1 | 18.7232 | 0.874174 | 108.479 | 2.34492 | 60.2277 | 0.223095 | 60.8864 | 66.0553 | 0.552197 | 222.927 | 12.1641 | 0.584419 | 74.0357 | 55.551 | 108.191 | 233.5078 | 19314.27 |
| 22038.1 | 31.7861 | 0.894289 | 120.243 | 1.12832 | 1.30486 | 0.452922 | 436.801 | 95.1495 | 0.618335 | 495.844 | 30.5838 | 0.894931 | 54.2279 | 68.0244 | 241.158 | 68.07256 | 4520.492 |
| 53455.8 | 27.0268 | 0.719574 | 67.8069 | 3.44422 | 67.8094 | 0.460982 | 217.799 | 67.3731 | 0.980915 | 476.446 | 85.7964 | 0.468211 | 73.0395 | 84.6399 | 207.514 | 125.8778 | 7904.625 |
| 43332.6 | 33.0052 | 0.775873 | 38.3364 | 1.93619 | 47.7017 | 0.495501 | 509.131 | 27.336 | 0.762868 | 371.342 | 86.755 | 0.629088 | 82.0331 | 336.734 | 215.329 | 91.48952 | 5807.214 |
| 44140.1 | 30.6848 | 0.771381 | 100.379 | 2.96478 | 19.4886 | 0.435039 | 226.139 | 61.6098 | 0.626907 | 248.612 | 84.0576 | 0.428753 | 52.8538 | 55.5052 | 67.0072 | 185.0108 | 10789.17 |
| 17307.9 | 32.4525 | 0.920594 | 46.0335 | 2.51566 | 89.738 | 0.388058 | 346.05 | 80.6282 | 0.967637 | 172.046 | 3.98907 | 0.704341 | 163.792 | 277.076 | 142.338 | 61.13892 | 5719.221 |
| 44293.2 | 14.7636 | 0.770519 | 26.7219 | 3.03089 | 96.6778 | 0.56031 | 431.314 | 42.1981 | 0.519721 | 498.643 | 93.755 | 0.689365 | 255.361 | 329.085 | 485.452 | 175.1837 | 11353.31 |
| 49361.5 | 28.8308 | 0.742343 | 124.974 | 0.102134 | 68.7696 | 0.619598 | 130.259 | 15.8772 | 0.994705 | 181.513 | 39.7548 | 0.419761 | 2.02233 | 104.354 | 137.048 | 123.9267 | 7437.425 |
| 26175.5 | 29.8713 | 0.871278 | 65.4114 | 2.35637 | 90.3288 | 0.381427 | 111.405 | 18.7315 | 0.551204 | 246.645 | 47.8558 | 0.506459 | 39.0449 | 61.117 | 189.61 | 161.3731 | 13948.78 |
| 19500.7 | 29.448 | 0.908396 | 58.8424 | 3.34802 | 47.6949 | 0.399181 | 386.159 | 76.1208 | 0.924808 | 365.993 | 50.0657 | 0.38572 | 135.241 | 54.6482 | 180.978 | 114.2233 | 8905.023 |
| 28372.7 | 14.0569 | 0.859048 | 138.422 | 0.261466 | 76.2304 | 0.661507 | 207.114 | 65.5029 | 0.467832 | 415.822 | 53.726 | 0.786765 | 18.0478 | 110.593 | 254.055 | 97.12389 | 6694.473 |
| 15672.5 | 22.9446 | 0.929677 | 70.1385 | 1.25626 | 55.6163 | 0.45689 | 367.683 | 50.5098 | 0.867636 | 369.185 | 58.3626 | 0.65886 | 98.9153 | 79.5809 | 62.053 | 55.60588 | 4690.975 |
| 40681.8 | 26.5758 | 0.790608 | 110.822 | 0.117476 | 85.8056 | 0.265219 | 137.676 | 60.3612 | 0.800923 | 455.273 | 29.2991 | 0.937318 | 5.25794 | 76.6397 | 60.7672 | 164.3705 | 11939.48 |
| 52461.8 | 24.0206 | 0.7251 | 111.037 | 3.21253 | 1.05268 | 0.518963 | 352.048 | 94.934 | 0.904523 | 335.943 | 31.3974 | 0.467987 | 88.0544 | 326.274 | 229.698 | 125.7092 | 6635.659 |
| 19506.8 | 26.691 | 0.908359 | 56.6987 | 0.461465 | 34.1985 | 0.471679 | 381.917 | 67.1691 | 0.886929 | 457.198 | 88.3982 | 0.94574 | 16.4905 | 90.147 | 423.196 | 41.98339 | 3172.066 |
| 21181 | 31.19 | 0.899054 | 45.6737 | 1.6875 | 34.3876 | 0.192359 | 484.765 | 43.117 | 0.886704 | 292.882 | 65.6029 | 0.977292 | 28.6651 | 53.7029 | 228.813 | 121.0012 | 9505.192 |
| 16814.3 | 29.7916 | 0.923335 | 167.856 | 1.02978 | 3.00109 | 0.680101 | 501.543 | 96.3392 | 0.267445 | 400.518 | 21.0141 | 0.868465 | 35.581 | 340.271 | 259.882 | 131 | 9038.476 |
| 16398.5 | 28.008 | 0.925645 | 137.056 | 0.145056 | 70.2618 | 0.421886 | 137.962 | 26.5704 | 0.952635 | 452.294 | 61.9633 | 0.519246 | 10.3995 | 65.4423 | 276.505 | 98.23621 | 8211.542 |
| 25308.2 | 30.7942 | 0.876103 | 59.7358 | 2.4018 | 28.1968 | 0.544463 | 443.694 | 25.7786 | 0.737273 | 353.525 | 64.6602 | 0.98465 | 218.81 | 145.957 | 235.624 | 47.59435 | 3321.99 |
| 21581.1 | 27.2987 | 0.896825 | 124.036 | 1.87778 | 54.3771 | 0.433901 | 458.192 | 33.8782 | 0.717871 | 124.134 | 3.71255 | 0.230404 | 9.65999 | 251.381 | 45.2169 | 230.7574 | 18091.72 |
| 27801.5 | 33.473 | 0.862241 | 101.176 | 2.15929 | 53.1266 | 0.474748 | 296.766 | 13.0219 | 0.376695 | 335.265 | 36.4461 | 0.935128 | 38.174 | 114.57 | 203.613 | 96.4719 | 7232.865 |
| 31672.6 | 14.1216 | 0.840698 | 160.69 | 1.02949 | 47.906 | 0.649308 | 399.938 | 68.4999 | 0.796211 | 303.057 | 47.6245 | 0.613233 | 16.8349 | 395.536 | 269.662 | 80.14965 | 5171.276 |
| 35999.8 | 18.6999 | 0.816638 | 159.81 | 2.89726 | 92.3804 | 0.429358 | 474.292 | 10.9692 | 0.445611 | 227.025 | 87.1111 | 0.7729 | 144.924 | 256.926 | 45.5531 | 156.8542 | 11716.07 |
| 24157.8 | 26.2858 | 0.882495 | 70.9066 | 1.13126 | 30.6048 | 0.286792 | 209.693 | 78.0127 | 0.871992 | 387.852 | 34.2055 | 0.74621 | 19.5762 | 58.2421 | 367.551 | 86.91821 | 6444.971 |
| 19118.7 | 30.3144 | 0.910521 | 122.468 | 0.795557 | 45.935 | 0.430553 | 308.103 | 63.7052 | 0.850005 | 75.3897 | 86.2545 | 0.301371 | 69.4318 | 292.801 | 64.9369 | 166.682 | 12631.32 |
| 39883.2 | 24.0096 | 0.795047 | 172.345 | 0.85743 | 18.9898 | 0.530899 | 263.611 | 87.3812 | 0.992538 | 323.072 | 36.176 | 0.261008 | 82.0094 | 192.234 | 320.492 | 226.5228 | 13058.98 |
| 24792 | 28.988 | 0.878971 | 104.258 | 1.40491 | 98.2807 | 0.316761 | 477.178 | 99.7587 | 0.957867 | 328.501 | 85.9739 | 0.584078 | 65.6292 | 213.418 | 318.038 | 117.0626 | 10067.43 |
| 28536.4 | 22.9988 | 0.858144 | 100.451 | 1.3322 | 62.9206 | 0.213689 | 147.674 | 40.7441 | 0.743988 | 110.909 | 83.678 | 0.562297 | 41.1774 | 128.839 | 54.6979 | 207.925 | 16718.14 |
| 25321.6 | 24.2687 | 0.876021 | 120.859 | 0.111633 | 75.1625 | 0.454502 | 505.939 | 55.4471 | 0.587545 | 446.457 | 50.5851 | 0.981917 | 10.4118 | 170.16 | 140.017 | 87.9044 | 6765.164 |
| 48443.4 | 26.0455 | 0.747447 | 47.1357 | 1.84037 | 27.0563 | 0.341853 | 173.861 | 15.1149 | 0.374741 | 495.891 | 26.4222 | 0.718101 | 61.4633 | 156.201 | 471.173 | 230.7466 | 13750.47 |
| 23995 | 13.9011 | 0.883392 | 56.5112 | 3.73952 | 67.8624 | 0.42495 | 299.662 | 22.9509 | 0.599646 | 283.643 | 20.5934 | 0.407335 | 165.22 | 174.315 | 279.079 | 149.4951 | 12210.71 |
| 36760.4 | 30.9162 | 0.812419 | 106.964 | 1.2257 | 8.76065 | 0.485164 | 279.364 | 73.8222 | 0.303554 | 285.538 | 19.3734 | 0.999114 | 27.3428 | 158.726 | 139.987 | 133.5052 | 7951.489 |
| 15832.2 | 17.0674 | 0.928785 | 128.692 | 0.246857 | 9.69338 | 0.607528 | 222.351 | 13.2909 | 0.502325 | 117.314 | 14.079 | 0.913043 | 24.2068 | 141.082 | 70.8722 | 55.88141 | 4206.864 |
| 36854.3 | 13.6029 | 0.811884 | 124.891 | 3.48663 | 64.1463 | 0.400758 | 175.682 | 0.793377 | 0.634505 | 409.017 | 20.5376 | 0.398259 | 46.6579 | 77.7067 | 130.674 | 185.9929 | 13561.61 |
| 23380.2 | 15.5151 | 0.886811 | 123.173 | 0.491173 | 21.8843 | 0.173211 | 309.915 | 75.958 | 0.99744 | 104.285 | 53.966 | 0.899535 | 30.7278 | 194.294 | 83.9802 | 205.373 | 14380.11 |
| 42894.1 | 14.9109 | 0.778299 | 140.251 | 2.18933 | 52.1981 | 0.51868 | 494.822 | 87.2375 | 0.521483 | 467.638 | 82.6559 | 0.997128 | 175.783 | 172.192 | 351.691 | 93.01261 | 5884.302 |
| 17465.4 | 32.4363 | 0.919718 | 105.729 | 3.51133 | 42.2526 | 0.255979 | 185.757 | 45.7576 | 0.790943 | 132.393 | 38.7331 | 0.543081 | 113.978 | 144.762 | 53.1306 | 128.9624 | 10836.8 |
| 26668.7 | 28.4874 | 0.868535 | 172.393 | 2.67665 | 87.3199 | 0.483699 | 189.862 | 94.9478 | 0.559433 | 252.961 | 50.4788 | 0.912613 | 130.423 | 181.021 | 188.296 | 92.609 | 7129.444 |
| 54762.1 | 21.5013 | 0.712307 | 138.837 | 0.898475 | 16.1352 | 0.558242 | 224.975 | 65.1985 | 0.631999 | 385.675 | 82.4256 | 0.894692 | 57.4429 | 124.104 | 80.1937 | 97.1083 | 5289.806 |
| 28173.7 | 21.3621 | 0.860159 | 59.7107 | 2.05791 | 65.0489 | 0.228459 | 480.214 | 41.4686 | 0.952865 | 453.121 | 67.4233 | 0.872936 | 62.5263 | 230.911 | 242.627 | 110.3653 | 9060.391 |
| 17211.5 | 30.9938 | 0.921128 | 158.865 | 1.70996 | 58.1596 | 0.602449 | 430.579 | 56.3484 | 0.882053 | 326.602 | 52.9697 | 0.895647 | 170.659 | 369.161 | 125.109 | 39.30511 | 3085.861 |
| 30087.1 | 25.0403 | 0.849522 | 145.729 | 0.181231 | 25.4302 | 0.60223 | 472.486 | 53.5903 | 0.982447 | 439.145 | 52.6246 | 0.698004 | 7.432 | 376.287 | 281.601 | 63.83406 | 4144.484 |
| 40557.9 | 16.9207 | 0.791291 | 165.23 | 1.02584 | 11.0582 | 0.4627 | 335.25 | 32.868 | 0.387147 | 285.193 | 5.63193 | 0.775707 | 41.0407 | 73.515 | 149.402 | 185.5277 | 10719.73 |
| 25484.3 | 18.5553 | 0.875112 | 111.699 | 2.70283 | 39.5722 | 0.23876 | 509.16 | 56.2207 | 0.410759 | 328.207 | 24.6792 | 0.807044 | 140.338 | 148.477 | 304.54 | 198.789 | 15238.39 |
| 52137.5 | 23.6862 | 0.726903 | 157.868 | 0.388694 | 51.4829 | 0.698788 | 445.41 | 55.5021 | 0.391054 | 418.077 | 90.2365 | 0.766729 | 31.4501 | 281.818 | 130.971 | 164.2538 | 9145.705 |
| 39614.2 | 19.2556 | 0.796539 | 73.347 | 2.92279 | 11.372 | 0.487014 | 415.485 | 56.9861 | 0.658106 | 223.966 | 66.8928 | 0.560515 | 106.646 | 256.821 | 198.245 | 109.1801 | 6389.969 |
| 25115.3 | 14.8049 | 0.877162 | 127.542 | 0.257504 | 15.1178 | 0.53641 | 248.435 | 79.6017 | 0.699135 | 309.553 | 45.2583 | 0.534267 | 11.431 | 93.4443 | 135.012 | 107.8362 | 7045.802 |
| 55367.6 | 19.4435 | 0.708939 | 152.162 | 1.14492 | 69.3593 | 0.581184 | 442.856 | 16.8718 | 0.717319 | 443.985 | 69.2009 | 0.657494 | 82.3743 | 438.237 | 315.613 | 112.7494 | 6698.574 |
| 42417 | 34.7127 | 0.780967 | 75.2561 | 2.65983 | 79.1357 | 0.517988 | 396.377 | 85.7184 | 0.939187 | 431.894 | 53.9293 | 0.625151 | 35.5867 | 243.09 | 370.143 | 82.15831 | 5399.679 |
| 27431.6 | 22.4178 | 0.864287 | 49.4265 | 3.39768 | 62.2621 | 0.20655 | 399.265 | 30.2582 | 0.871693 | 159.964 | 20.1046 | 0.500344 | 29.7476 | 147.315 | 87.3355 | 191.2741 | 15880.91 |
| 55710.8 | 22.171 | 0.707032 | 108.146 | 0.601722 | 75.1715 | 0.528428 | 206.966 | 92.3822 | 0.951648 | 143.417 | 72.858 | 0.28245 | 36.3815 | 96.2559 | 63.7167 | 222.6202 | 13306.1 |
| 31745.8 | 30.906 | 0.840304 | 99.0855 | 0.473401 | 67.7504 | 0.491524 | 324.503 | 58.8582 | 0.529065 | 204.24 | 80.6211 | 0.624251 | 41.9239 | 241.48 | 168.283 | 132.4146 | 9467.886 |
| 20871.9 | 24.4957 | 0.900766 | 146.43 | 1.45996 | 55.0544 | 0.413777 | 359.502 | 15.5413 | 0.654542 | 200.561 | 58.4878 | 0.853665 | 51.2095 | 169.578 | 156.706 | 77.63479 | 6238.057 |
| 39102.4 | 24.5849 | 0.799389 | 59.3946 | 2.97215 | 43.2734 | 0.433525 | 236.713 | 50.2212 | 0.938166 | 176.552 | 5.19486 | 0.614845 | 146.044 | 144.191 | 96.4116 | 79.50464 | 5338.111 |
| 50807.1 | 25.7565 | 0.734303 | 111.87 | 3.29209 | 76.2319 | 0.555909 | 271.529 | 32.1858 | 0.861391 | 195.46 | 66.6921 | 0.619484 | 58.1095 | 153.756 | 179.782 | 100.8846 | 6237.069 |
| 34333.8 | 27.9406 | 0.825909 | 151.942 | 1.05364 | 77.8562 | 0.459599 | 164.52 | 84.5088 | 0.550749 | 315.133 | 88.378 | 0.981052 | 48.6735 | 148.306 | 215.971 | 105.544 | 7476.879 |
| 41677.1 | 14.531 | 0.785066 | 121.824 | 1.01003 | 92.603 | 0.554493 | 415.88 | 95.9795 | 0.89733 | 325.345 | 46.1206 | 0.403167 | 52.409 | 252.183 | 311.328 | 132.4823 | 8716.049 |
| 14143.3 | 13.2225 | 0.938174 | 102.354 | 3.29989 | 66.6563 | 0.3101 | 132.61 | 44.4279 | 0.955193 | 364.589 | 95.0557 | 0.879932 | 109.513 | 108.053 | 357.854 | 61.36839 | 5666.546 |
| 32645.3 | 21.2168 | 0.835293 | 121.226 | 3.28616 | 51.7984 | 0.412194 | 515.675 | 36.5785 | 0.839115 | 157.628 | 83.6721 | 0.436064 | 138.411 | 221.208 | 128.216 | 125.3657 | 8909.483 |
| 36923.2 | 32.3157 | 0.811515 | 64.6216 | 2.17241 | 33.4128 | 0.219783 | 472.921 | 42.4705 | 0.708995 | 277.033 | 84.1624 | 0.522656 | 80.8296 | 273.418 | 117.282 | 238.6739 | 15993.25 |
| 26906.9 | 15.9418 | 0.8672 | 133.622 | 1.49764 | 56.4156 | 0.250494 | 63.5664 | 95.4378 | 0.667127 | 288.908 | 42.7301 | 0.897442 | 73.4527 | 55.1886 | 211.601 | 133.1439 | 10325.56 |
| 49623.2 | 31.4281 | 0.740891 | 168.887 | 0.336984 | 27.6145 | 0.964028 | 422.726 | 1.3372 | 0.907277 | 514.615 | 39.1715 | 0.582135 | 16.1392 | 263.455 | 485.388 | 114.4828 | 6171.83 |
| 36770.5 | 24.3046 | 0.812356 | 144.095 | 1.6263 | 82.3345 | 0.668494 | 445.005 | 1.18972 | 0.946767 | 323.248 | 54.5404 | 0.910698 | 132.086 | 263.79 | 257.95 | 45.46895 | 3086.114 |
| 20922.1 | 33.4254 | 0.900497 | 118.17 | 2.39452 | 3.87924 | 0.417527 | 409.664 | 97.5506 | 0.638878 | 340.412 | 15.5974 | 0.969127 | 74.646 | 67.124 | 106.781 | 58.4999 | 4011.761 |
| 19126.9 | 34.0137 | 0.910481 | 64.4565 | 3.2185 | 88.9367 | 0.397074 | 236.85 | 18.6005 | 0.550444 | 242.643 | 20.5882 | 0.910338 | 36.4056 | 225.872 | 191.026 | 74.33288 | 7079.409 |
| 40862.8 | 34.2565 | 0.789609 | 63.84 | 0.739439 | 35.0892 | 0.407956 | 162.416 | 7.04783 | 0.346462 | 384.82 | 90.1687 | 0.705467 | 69.7295 | 86.0345 | 234.884 | 201.0042 | 12770.82 |
| 14935.7 | 33.214 | 0.933786 | 103.61 | 1.39891 | 83.69 | 0.374931 | 97.3928 | 35.6136 | 0.608246 | 262.319 | 93.833 | 0.437728 | 34.5004 | 51.0158 | 110.891 | 153.8678 | 14392.68 |
| 27999.4 | 13.7269 | 0.861124 | 74.5754 | 2.60396 | 89.7483 | 0.469935 | 242.768 | 91.4174 | 0.974529 | 159.662 | 6.96772 | 0.942171 | 41.2252 | 60.49 | 60.5007 | 46.06912 | 3751.201 |
| 27732.5 | 25.3099 | 0.862616 | 134.216 | 3.21691 | 88.0171 | 0.40616 | 415.764 | 50.8994 | 0.957333 | 276.27 | 52.9634 | 0.726482 | 164.117 | 164.603 | 150.084 | 69.74957 | 5729.865 |
| 31746.1 | 16.9309 | 0.840291 | 79.2877 | 0.279877 | 6.36533 | 0.313955 | 232.925 | 48.0663 | 0.51375 | 461.529 | 66.4769 | 0.49952 | 13.1367 | 128.424 | 280.863 | 230.3875 | 14047.48 |
| 35022.2 | 26.1428 | 0.82208 | 80.9885 | 2.50738 | 11.2886 | 0.222878 | 365.414 | 49.185 | 0.834096 | 284.025 | 7.84473 | 0.467377 | 12.6854 | 355.774 | 227.779 | 207.5145 | 12808.48 |
| 57481.6 | 23.7459 | 0.697186 | 163.68 | 2.20672 | 35.8306 | 0.579664 | 182.983 | 82.4745 | 0.872218 | 346.329 | 96.1925 | 0.739124 | 48.8585 | 49.7831 | 65.5131 | 92.085 | 5116.466 |
| 11310 | 32.7273 | 0.953948 | 57.282 | 2.27783 | 20.2517 | 0.572585 | 180.113 | 20.7102 | 0.957671 | 284.319 | 75.6203 | 0.902587 | 226.606 | 165.626 | 238.065 | 32.56134 | 2582.59 |
| 28041.6 | 13.7641 | 0.860889 | 139.485 | 0.340806 | 21.5007 | 0.568574 | 394.236 | 57.9944 | 0.778085 | 418.884 | 56.5692 | 0.853624 | 28.3868 | 169.263 | 86.5965 | 61.11465 | 4044.043 |
| 24866.5 | 34.024 | 0.878563 | 53.6406 | 3.40292 | 64.2465 | 0.143439 | 454.745 | 45.6383 | 0.941243 | 298.179 | 74.3357 | 0.813132 | 86.3504 | 204.552 | 47.3095 | 218.0201 | 18594.06 |
| 22062.5 | 14.6621 | 0.894138 | 43.65 | 1.74468 | 79.6189 | 0.3855 | 349.529 | 78.7063 | 0.981655 | 507.654 | 99.2901 | 0.929111 | 161.554 | 61.441 | 61.911 | 60.25283 | 4983.758 |
| 40044.7 | 27.5199 | 0.794151 | 63.1348 | 0.863798 | 50.0453 | 0.365629 | 340.416 | 16.1083 | 0.388455 | 288.409 | 61.9678 | 0.906257 | 41.0749 | 234.709 | 141.196 | 154.4284 | 10579.67 |
| 11962.8 | 25.3463 | 0.950308 | 90.5042 | 3.61968 | 36.2292 | 0.411964 | 195.444 | 19.8704 | 0.914635 | 136.076 | 50.4768 | 0.521661 | 174.412 | 148.216 | 52.1367 | 61.62715 | 5346.068 |
| 35081.8 | 34.8408 | 0.821758 | 100.191 | 0.84509 | 2.44969 | 0.372217 | 230.489 | 98.1153 | 0.720513 | 235.951 | 48.8474 | 0.787389 | 4.17129 | 166.48 | 146.182 | 98.55922 | 5837.032 |
| 45324.9 | 25.1492 | 0.764787 | 116.682 | 3.51688 | 25.0246 | 0.520537 | 385.272 | 57.6937 | 0.635692 | 431.94 | 88.6292 | 0.585602 | 50.693 | 312.271 | 138.12 | 131.6678 | 7596.325 |
| 18019.1 | 13.3859 | 0.916622 | 158.993 | 1.64592 | 71.0977 | 0.582608 | 79.2326 | 26.5438 | 0.362574 | 371.738 | 58.0769 | 0.66658 | 150.014 | 49.069 | 192.695 | 123.9743 | 9853.983 |
| 33537.1 | 15.3613 | 0.830331 | 127.667 | 2.79929 | 1.58762 | 0.182643 | 416.521 | 18.4141 | 0.780372 | 443.214 | 3.41833 | 0.801336 | 111.427 | 85.0149 | 373.846 | 153.1672 | 9177.471 |
| 37695.8 | 24.7478 | 0.807211 | 142.592 | 3.72621 | 42.8848 | 0.451345 | 188.315 | 20.9217 | 0.261484 | 367.349 | 0.046597 | 0.857732 | 30.8583 | 80.7381 | 354.341 | 196.3801 | 12982.6 |
| 23532.3 | 17.6754 | 0.885966 | 137.827 | 3.54177 | 7.66686 | 0.496767 | 490.042 | 66.5014 | 0.528126 | 95.8031 | 22.6284 | 0.544598 | 18.877 | 233.044 | 65.5053 | 110.0957 | 7266.074 |
| 19498.8 | 24.001 | 0.908401 | 157.143 | 0.824693 | 68.5715 | 0.336929 | 209.296 | 89.1542 | 0.663377 | 382.563 | 89.2542 | 0.888534 | 41.0093 | 131.035 | 100.338 | 109.1392 | 8864.092 |
| 27332.2 | 32.1569 | 0.864849 | 169.367 | 0.137265 | 86.3888 | 0.729427 | 472.584 | 42.6679 | 0.521475 | 224.787 | 93.7846 | 0.546164 | 2.7745 | 196.488 | 93.2658 | 138.8075 | 9398.705 |
| 20083.6 | 23.7996 | 0.905148 | 133.998 | 2.2336 | 50.8511 | 0.440025 | 505.917 | 32.0722 | 0.304559 | 156.428 | 73.9073 | 0.723012 | 18.774 | 434.535 | 131.459 | 165.2635 | 13071.77 |
| 25689.4 | 31.874 | 0.873984 | 97.9791 | 2.80806 | 55.5943 | 0.5787 | 457.2 | 86.3374 | 0.628666 | 472.879 | 44.5843 | 0.719139 | 72.1014 | 207.56 | 382.128 | 103.352 | 7166.736 |
| 20280.5 | 28.7136 | 0.904059 | 30.1487 | 1.64157 | 23.5632 | 0.301616 | 112.091 | 99.9652 | 0.283097 | 144.451 | 52.6217 | 0.705974 | 111.332 | 97.132 | 53.1749 | 236.2381 | 17421.74 |
| 37978.4 | 26.8325 | 0.805641 | 111.907 | 0.542436 | 85.4219 | 0.261848 | 109.206 | 87.9041 | 0.642016 | 94.1419 | 3.63374 | 0.674666 | 5.00149 | 74.576 | 90.5917 | 219.525 | 16674.69 |
| 16571.2 | 15.0344 | 0.924674 | 26.0193 | 2.34382 | 81.3537 | 0.220994 | 364.996 | 5.05199 | 0.793738 | 192.057 | 47.2512 | 0.943725 | 13.5691 | 43.3325 | 189.146 | 93.4425 | 9450.067 |
| 26648.9 | 17.8541 | 0.868636 | 56.4503 | 3.02996 | 47.7716 | 0.299254 | 133.773 | 66.3201 | 0.956753 | 401.227 | 89.6556 | 0.522952 | 94.5382 | 63.6328 | 292.178 | 119.6364 | 9028.327 |
| 41727.4 | 28.3531 | 0.784795 | 55.1635 | 1.02118 | 76.9955 | 0.399113 | 475.14 | 70.3109 | 0.706066 | 497.476 | 6.01635 | 0.5482 | 54.5291 | 348.312 | 190.598 | 141.4479 | 10176.95 |
| 47875.9 | 27.2416 | 0.750603 | 116.7 | 0.19717 | 97.7585 | 0.354818 | 131.278 | 77.1646 | 0.894154 | 115.626 | 82.2712 | 0.980154 | 5.22592 | 74.2839 | 66.0224 | 124.8279 | 8560.03 |
| 11108.3 | 20.8338 | 0.955056 | 134.989 | 1.21152 | 44.6876 | 0.449053 | 415.386 | 7.30544 | 0.497464 | 426.427 | 27.487 | 0.446463 | 56.5127 | 365.609 | 162.861 | 136.5832 | 11950.33 |
| 42350.6 | 34.6933 | 0.781336 | 36.0936 | 3.5824 | 16.2916 | 0.416049 | 294.35 | 19.871 | 0.752316 | 180.019 | 23.9718 | 0.764602 | 142.605 | 66.6171 | 77.1886 | 81.94731 | 4961.552 |
| 42252.6 | 24.9573 | 0.781872 | 75.8826 | 0.218891 | 47.0362 | 0.259187 | 218.712 | 59.1738 | 0.466844 | 413.75 | 52.7433 | 0.97351 | 3.02655 | 179.068 | 318.859 | 198.1881 | 13199.22 |
| 27514.1 | 16.6644 | 0.863824 | 111.837 | 2.55851 | 99.1297 | 0.470451 | 292.362 | 58.6406 | 0.863097 | 235.083 | 18.0627 | 0.377806 | 174.902 | 188.067 | 61.7412 | 119.5777 | 9628.812 |
| 38010.6 | 23.2366 | 0.80546 | 33.6241 | 2.55829 | 20.0346 | 0.177413 | 464.218 | 23.5224 | 0.593929 | 263.118 | 35.8136 | 0.945973 | 70.2426 | 447.904 | 135.297 | 183.9765 | 11738.12 |
| 33770.2 | 29.3079 | 0.829045 | 65.909 | 2.964 | 54.4673 | 0.405694 | 66.2966 | 58.435 | 0.48673 | 446.233 | 81.76 | 0.918261 | 73.5372 | 45.4202 | 240.459 | 106.1836 | 7608.402 |
| 21481.2 | 14.6608 | 0.89737 | 90.6895 | 1.92009 | 92.1212 | 0.265327 | 192.1 | 44.4094 | 0.654165 | 519.877 | 94.616 | 0.511438 | 54.4269 | 135.021 | 246.744 | 189.983 | 17782.12 |
| 49146.5 | 19.0212 | 0.743533 | 80.9675 | 1.83164 | 29.3782 | 0.294535 | 149.764 | 15.9986 | 0.87238 | 269.043 | 29.3991 | 0.78145 | 133.578 | 102.735 | 52.3599 | 105.9034 | 6517.095 |
| 34359.8 | 29.8882 | 0.825767 | 64.1301 | 3.26439 | 78.1549 | 0.24735 | 164.675 | 35.6412 | 0.793613 | 303.533 | 44.7207 | 0.68909 | 95.3442 | 124.489 | 96.5972 | 146.6253 | 11845.49 |
| 38029.1 | 13.497 | 0.805351 | 80.6761 | 2.46309 | 68.0188 | 0.393087 | 298.032 | 7.8098 | 0.948249 | 376.425 | 35.6361 | 0.545821 | 73.4968 | 107.33 | 327.472 | 93.67081 | 6976.153 |
| 55008.8 | 22.3648 | 0.710936 | 165.918 | 3.34903 | 40.5321 | 0.490415 | 370.206 | 19.7258 | 0.94551 | 454.071 | 23.4614 | 0.734569 | 151.78 | 179.856 | 103.702 | 81.67762 | 4802.043 |
| 27411.7 | 23.9669 | 0.864399 | 168.599 | 0.484185 | 5.8539 | 0.331326 | 153.566 | 23.4768 | 0.494836 | 151.528 | 31.6066 | 0.589445 | 37.7168 | 93.7221 | 113.727 | 240.0981 | 15111.85 |
| 19288.7 | 33.5821 | 0.90958 | 68.1789 | 1.80001 | 56.3747 | 0.485754 | 237 | 89.6093 | 0.979494 | 161.121 | 8.23465 | 0.617101 | 39.0282 | 113.675 | 118.638 | 55.71138 | 4348.155 |
| 33337.7 | 27.3066 | 0.831448 | 75.4999 | 1.27446 | 67.9989 | 0.36579 | 357.946 | 31.9383 | 0.983231 | 278.326 | 49.2692 | 0.713333 | 55.2798 | 318.733 | 228.976 | 74.52212 | 5764.22 |
| 28098.8 | 16.677 | 0.860573 | 135.604 | 2.90512 | 41.7746 | 0.45272 | 206.88 | 60.6546 | 0.706116 | 383.433 | 64.5909 | 0.971627 | 163.556 | 156.699 | 361.728 | 60.58138 | 4356.061 |
| 33331.6 | 22.7781 | 0.831478 | 86.9432 | 1.53637 | 16.6251 | 0.387213 | 363.127 | 18.5831 | 0.621746 | 237.159 | 57.65 | 0.37078 | 72.3712 | 348.632 | 77.3491 | 191.1562 | 12085.48 |
| 24563.2 | 22.3896 | 0.880237 | 129.123 | 3.13019 | 37.9058 | 0.263439 | 359.635 | 56.7537 | 0.424652 | 312.708 | 24.1928 | 0.650596 | 24.5478 | 134.23 | 46.3976 | 222.4652 | 16850.29 |
| 36910.8 | 17.8006 | 0.811572 | 170.904 | 2.17053 | 20.4428 | 0.639512 | 167.532 | 16.4836 | 0.874562 | 496.569 | 16.5842 | 0.709886 | 107.015 | 101.147 | 181.542 | 59.93491 | 3710.21 |
| 43072.2 | 23.9021 | 0.777313 | 33.4632 | 3.62495 | 10.7386 | 0.39845 | 438.782 | 90.8079 | 0.583654 | 489.14 | 20.5124 | 0.657355 | 143.953 | 315.788 | 390.202 | 133.6494 | 7717.926 |
| 30713.5 | 20.2978 | 0.846035 | 48.1596 | 3.76116 | 94.0217 | 0.372611 | 508.638 | 76.1038 | 0.358801 | 134.57 | 25.3861 | 0.747569 | 8.50525 | 208.612 | 74.3568 | 186.6435 | 15585.28 |
| 40799.9 | 25.6752 | 0.78995 | 90.0047 | 3.25954 | 89.3279 | 0.520307 | 361.626 | 24.0811 | 0.92253 | 494.775 | 91.1982 | 0.299616 | 181.396 | 322.502 | 288.52 | 181.3536 | 12086.1 |
| 43528.9 | 15.4686 | 0.774769 | 36.1362 | 0.530699 | 19.6006 | 0.469438 | 456.361 | 61.1714 | 0.738391 | 56.6222 | 89.8889 | 0.968402 | 47.3848 | 333.393 | 53.6058 | 64.86831 | 3904.723 |
| 35530.4 | 21.058 | 0.81925 | 125.278 | 1.86231 | 86.3049 | 0.439355 | 114.575 | 23.3165 | 0.935357 | 306.562 | 98.0344 | 0.885669 | 120.445 | 75.0724 | 142.335 | 62.53126 | 4727.387 |
| 13503.3 | 24.5146 | 0.941741 | 61.1731 | 1.8728 | 297.882 | 0.379441 | 291.202 | 172.051 | 0.844157 | 476.867 | 958.164 | 0.639074 | 129.474 | 157.146 | 408.326 | 183.1742 | 17447.99 |
| 42850.6 | 21.3497 | 0.778544 | 50.2539 | 1.72106 | 357.29 | 0.335488 | 424.829 | 44.333 | 0.952509 | 102.541 | 990.87 | 0.942155 | 129.365 | 91.7865 | 66.8896 | 200.0274 | 17306.74 |
| 14716.3 | 23.8678 | 0.934995 | 89.7415 | 0.169361 | 135.397 | 0.545657 | 418.204 | 451.149 | 0.889551 | 381.631 | 829.372 | 0.58666 | 16.5787 | 302.54 | 377.951 | 177.6005 | 11765.15 |
| 56001.7 | 22.5719 | 0.705415 | 88.1568 | 1.87169 | 87.8839 | 0.474091 | 376.999 | 259.915 | 0.851076 | 366.82 | 678.542 | 0.451463 | 62.6591 | 332.752 | 316.797 | 226.3284 | 13437.62 |
| 45480.7 | 31.966 | 0.763927 | 46.1504 | 1.17772 | 62.5793 | 0.279525 | 176.145 | 440.114 | 0.786996 | 169.362 | 122.842 | 0.850031 | 15.0242 | 130.084 | 89.5387 | 164.5154 | 10674.12 |
| 27136.5 | 19.4754 | 0.865925 | 116.347 | 3.08818 | 67.6722 | 0.405681 | 413.357 | 186.983 | 0.906863 | 220.551 | 952.752 | 0.413521 | 105.985 | 143.127 | 117.127 | 215.7426 | 14107.97 |
| 14688.4 | 19.8087 | 0.935147 | 157.793 | 0.121644 | 525.775 | 0.548526 | 312.122 | 548.407 | 0.642808 | 96.4408 | 354.901 | 0.954895 | 10.7182 | 228.898 | 73.3309 | 155.9114 | 14602.46 |
| 43803.3 | 30.6831 | 0.773253 | 158.721 | 0.663467 | 547.283 | 0.806112 | 269.49 | 185.583 | 0.502999 | 481.309 | 335.863 | 0.9907 | 37.8125 | 263.217 | 412.696 | 168.1643 | 11302.08 |
| 28857.7 | 28.8609 | 0.856362 | 124.013 | 0.893536 | 217.625 | 0.480334 | 136.614 | 15.3146 | 0.83617 | 393.637 | 327.814 | 0.395281 | 50.9279 | 46.7449 | 89.4521 | 169.9893 | 15402.51 |
| 13280.2 | 20.4975 | 0.942978 | 152.926 | 1.65892 | 136.72 | 0.590177 | 165.607 | 716.863 | 0.594117 | 441.016 | 726.356 | 0.715858 | 48.0399 | 51.3167 | 411.75 | 195.6575 | 12546.31 |
| 52781.2 | 24.3336 | 0.723324 | 100.042 | 1.22248 | 350.53 | 0.474007 | 333.169 | 285.647 | 0.886462 | 207.916 | 728.022 | 0.6848 | 85.9603 | 79.4145 | 80.6633 | 193.9144 | 14869.63 |
| 43677.9 | 29.5424 | 0.773949 | 32.9011 | 2.79731 | 245.885 | 0.479128 | 252.073 | 709.427 | 0.814832 | 126.599 | 860.835 | 0.696756 | 41.7874 | 138.244 | 86.5034 | 236.2813 | 15812.11 |
| 40683.7 | 20.5067 | 0.790593 | 128.747 | 1.43034 | 266.903 | 0.272848 | 260.074 | 181.919 | 0.963883 | 404.112 | 310.671 | 0.776778 | 23.0919 | 235.183 | 244.406 | 190.9108 | 17945.44 |
| 20845.7 | 13.4252 | 0.900904 | 110.946 | 0.143288 | 356.648 | 0.368781 | 115.63 | 171.499 | 0.940361 | 220.183 | 751.867 | 0.869126 | 10.8082 | 76.0844 | 53.0717 | 175.5751 | 16150.05 |
| 47176 | 31.2869 | 0.754499 | 112.06 | 0.497479 | 505.798 | 0.476458 | 352.412 | 30.8706 | 0.584828 | 179.009 | 181.874 | 0.786774 | 30.214 | 326.699 | 157.152 | 177.6562 | 18815.12 |
| 24955.4 | 20.1717 | 0.878055 | 153.355 | 1.20879 | 201.313 | 0.623659 | 376.605 | 767.043 | 0.355869 | 516.164 | 226.355 | 0.792119 | 95.515 | 364.423 | 127.277 | 220.0614 | 15223.86 |
| 21195 | 30.7893 | 0.898976 | 32.8974 | 0.374259 | 125.873 | 0.49018 | 469.964 | 223.809 | 0.276586 | 438.226 | 399.67 | 0.95338 | 30.2483 | 81.5688 | 359.467 | 169.4486 | 13347 |
| 43883.3 | 32.105 | 0.77281 | 90.3465 | 3.42587 | 301.046 | 0.506556 | 181.219 | 558.742 | 0.643853 | 290.252 | 212.754 | 0.536417 | 152.978 | 97.1822 | 146.68 | 239.6044 | 17527.62 |
| 13086.1 | 33.6299 | 0.944073 | 170.897 | 2.85727 | 284.55 | 0.487618 | 316.94 | 160.581 | 0.683319 | 173.373 | 118.913 | 0.63657 | 88.8248 | 208.021 | 65.365 | 121.2561 | 13030.7 |
| 12267.2 | 16.5443 | 0.948608 | 143.055 | 0.623132 | 507.746 | 0.475403 | 317.405 | 197.33 | 0.970699 | 451.021 | 16.0581 | 0.711096 | 54.3853 | 173.385 | 135.481 | 99.88385 | 12558.52 |
| 35859.6 | 21.0421 | 0.817419 | 97.1612 | 3.59298 | 648.308 | 0.485857 | 250.458 | 58.0921 | 0.934675 | 329.202 | 734.416 | 0.976567 | 78.5063 | 175.875 | 157.965 | 131.3806 | 12050.63 |
| 40812.7 | 16.7688 | 0.789874 | 162.256 | 0.807636 | 197.39 | 0.738791 | 356.714 | 583.186 | 0.645934 | 328.298 | 845.862 | 0.9239 | 32.8381 | 183.488 | 320.886 | 215.9807 | 12234.26 |
| 35624.1 | 21.9701 | 0.81873 | 97.783 | 0.129341 | 954.346 | 0.562598 | 331.119 | 103.615 | 0.936411 | 249.309 | 135.055 | 0.787271 | 5.37114 | 66.7406 | 154.681 | 113.715 | 14161.37 |
| 13938.3 | 26.8398 | 0.939325 | 104.346 | 1.16993 | 72.2795 | 0.362459 | 374.283 | 200.518 | 0.726508 | 518.878 | 726.107 | 0.358319 | 104.684 | 102.867 | 392.69 | 244.8777 | 18884.13 |
| 33270.2 | 23.4253 | 0.83182 | 24.4603 | 2.87253 | 372.779 | 0.565423 | 287.842 | 622.764 | 0.794107 | 396.035 | 157.632 | 0.738206 | 200.325 | 280.598 | 351.843 | 185.9441 | 13592.97 |
| 48765.1 | 27.8844 | 0.745659 | 147.118 | 0.652413 | 200.55 | 0.365459 | 401.778 | 409.793 | 0.79586 | 472.518 | 176.411 | 0.719199 | 26.5645 | 61.2534 | 142.78 | 216.1278 | 16025.56 |
| 42404.6 | 24.4063 | 0.781026 | 119.061 | 0.523426 | 248.441 | 0.420244 | 497.949 | 693.976 | 0.674157 | 191.67 | 993.748 | 0.912644 | 9.94394 | 465.474 | 64.9802 | 246.9499 | 17306.77 |
| 22162.4 | 21.3707 | 0.893587 | 130.666 | 0.539804 | 14.3348 | 0.207552 | 276.431 | 235.179 | 0.741013 | 283.962 | 204.107 | 0.691521 | 39.5118 | 63.6048 | 227.988 | 206.6104 | 13664.18 |
| 20993.3 | 19.4337 | 0.900086 | 132.133 | 1.71188 | 327.872 | 0.406009 | 249.993 | 432.699 | 0.969989 | 394.839 | 292.653 | 0.537868 | 127.717 | 231.598 | 194.816 | 194.9568 | 18110.97 |
| 23888.8 | 13.5613 | 0.883982 | 69.9046 | 1.83444 | 123.354 | 0.395601 | 276.568 | 771.744 | 0.446947 | 461.987 | 187.72 | 0.702664 | 52.6167 | 230.366 | 437.102 | 231.8256 | 17892.83 |
| 35946.2 | 24.22 | 0.81694 | 66.0515 | 0.132721 | 24.2845 | 0.36984 | 264.719 | 69.217 | 0.765012 | 300.648 | 665.458 | 0.889663 | 12.7301 | 138.811 | 144.791 | 134.4913 | 7948.499 |
| 11468.8 | 26.1895 | 0.953056 | 35.0517 | 2.46037 | 61.1524 | 0.350234 | 69.6397 | 872.551 | 0.536379 | 473.778 | 833.267 | 0.767115 | 45.8234 | 62.2109 | 259.162 | 237.5524 | 15963.1 |
| 16381.2 | 29.0753 | 0.925743 | 158.901 | 0.577205 | 92.1014 | 0.616587 | 241.851 | 521.199 | 0.661058 | 326.162 | 553.193 | 0.623053 | 46.8417 | 71.2284 | 272.433 | 180.0602 | 11577.53 |
| 21073.2 | 21.1422 | 0.899644 | 85.389 | 1.77651 | 88.7071 | 0.424333 | 169.656 | 503.188 | 0.451709 | 242.264 | 499.884 | 0.988152 | 38.5604 | 131.795 | 129.746 | 156.6297 | 11171.37 |
| 34156.8 | 29.5633 | 0.826895 | 78.78 | 0.598833 | 305.138 | 0.334035 | 418.885 | 722.905 | 0.965797 | 360.536 | 126.847 | 0.979839 | 3.11035 | 206.17 | 292.128 | 182.5782 | 15921.46 |
| 35720.8 | 33.7579 | 0.818203 | 83.5902 | 3.78521 | 230.072 | 0.424143 | 381.02 | 619.087 | 0.901643 | 471.555 | 484.036 | 0.550029 | 118.752 | 132.775 | 398.644 | 233.1252 | 17267 |
| 14582.4 | 26.159 | 0.935742 | 87.4226 | 2.04352 | 429.368 | 0.358965 | 289.137 | 119.124 | 0.997391 | 91.5069 | 558.387 | 0.924719 | 150.871 | 119.457 | 59.4445 | 139.5199 | 15160.59 |
| 15582.8 | 21.503 | 0.930175 | 55.7336 | 1.30481 | 3.48107 | 0.451639 | 383.83 | 184.995 | 0.537713 | 398.111 | 331.014 | 0.282284 | 29.3549 | 207.686 | 73.449 | 243.5249 | 15833.92 |
| 12165.2 | 31.8254 | 0.949191 | 166.1 | 1.15727 | 218.829 | 0.361824 | 120.376 | 915.469 | 0.772722 | 169.853 | 97.2446 | 0.699255 | 104.807 | 80.7776 | 160.736 | 216.8976 | 18305.88 |
| 19057.5 | 23.6209 | 0.910854 | 110.114 | 0.231543 | 443.745 | 0.430362 | 368.874 | 22.5544 | 0.763398 | 517.794 | 585.576 | 0.732726 | 12.8098 | 238.752 | 473.907 | 154.8667 | 17232.21 |
| 42303.9 | 34.1879 | 0.781595 | 117.448 | 1.89056 | 75.2993 | 0.508341 | 449.77 | 614.197 | 0.628309 | 356.351 | 787.637 | 0.770039 | 161.652 | 401.701 | 98.6472 | 209.2091 | 12146.73 |
| 20677 | 32.3908 | 0.901858 | 79.1115 | 0.325712 | 132.733 | 0.420575 | 464.204 | 691.193 | 0.904298 | 286.617 | 371.567 | 0.827563 | 30.9927 | 263.751 | 126.917 | 148.7442 | 10284.15 |
| 13482.7 | 23.2648 | 0.941855 | 163.034 | 1.43228 | 52.6131 | 0.19805 | 246.403 | 383.995 | 0.95966 | 327.237 | 99.8805 | 0.583921 | 94.5042 | 136.343 | 158.041 | 213.324 | 16666.6 |
| 32551.2 | 14.5517 | 0.835813 | 37.5392 | 1.48506 | 309.029 | 0.510919 | 395.919 | 108.933 | 0.659155 | 203.408 | 76.1396 | 0.654991 | 86.2087 | 178.8 | 180.409 | 126.588 | 11810.46 |
| 35313.3 | 33.1772 | 0.820468 | 107.023 | 0.332125 | 864.032 | 0.520408 | 373.292 | 702.165 | 0.814242 | 203.139 | 10.1338 | 0.987952 | 1.75806 | 298.682 | 158.716 | 147.1711 | 15821.08 |
| 33997.8 | 19.2793 | 0.827771 | 90.8626 | 3.51511 | 53.7101 | 0.405161 | 379.147 | 561.471 | 0.626117 | 378.848 | 145.066 | 0.502203 | 95.0551 | 224.528 | 362.192 | 233.6855 | 14813.08 |
| 18850.1 | 27.6147 | 0.912012 | 147.914 | 1.746 | 36.5803 | 0.430882 | 477.332 | 442.504 | 0.341569 | 83.7946 | 854.038 | 0.966234 | 109.564 | 272.524 | 49.724 | 214.0067 | 13840.42 |
| 31917.7 | 26.0679 | 0.839343 | 133.41 | 0.155585 | 577.603 | 0.561897 | 459.606 | 875.417 | 0.544728 | 324.733 | 218.584 | 0.884734 | 12.6888 | 256.448 | 281.338 | 216.6123 | 19086.57 |
| 25347.5 | 22.352 | 0.875876 | 24.2333 | 2.41963 | 142.828 | 0.45967 | 426.525 | 131.906 | 0.844702 | 192.788 | 80.0973 | 0.83877 | 23.2938 | 178.594 | 76.4013 | 67.86089 | 5928.809 |
| 54066.3 | 20.2036 | 0.716176 | 86.9085 | 0.515427 | 355.523 | 0.413349 | 141.93 | 908.857 | 0.963424 | 214.875 | 431.513 | 0.849744 | 5.20111 | 134.012 | 174.739 | 217.2763 | 15996.92 |
| 35843.4 | 34.613 | 0.817523 | 52.4001 | 2.55776 | 244.289 | 0.497744 | 158.701 | 36.4632 | 0.544495 | 241.703 | 969.02 | 0.912922 | 77.0093 | 63.7821 | 144.665 | 163.9559 | 12100.24 |
| 41971.6 | 19.6198 | 0.783431 | 172.4 | 0.690371 | 601.088 | 0.618793 | 232.641 | 78.5626 | 0.841528 | 177.766 | 886.231 | 0.987685 | 6.63847 | 51.8349 | 121.152 | 149.4936 | 11491.2 |
| 38313.2 | 23.7793 | 0.803777 | 171.05 | 0.920224 | 148.735 | 0.654416 | 485.6 | 322.281 | 0.317254 | 409.245 | 120.945 | 0.925945 | 48.3445 | 180.199 | 191.441 | 179.0299 | 11994.59 |
| 10535.7 | 20.7824 | 0.95824 | 94.1766 | 0.74884 | 96.711 | 0.171751 | 309.744 | 217.976 | 0.70621 | 384.458 | 354.497 | 0.855065 | 12.5993 | 119.809 | 204.898 | 189.7339 | 18492.66 |
| 27625.6 | 23.6656 | 0.863209 | 103.088 | 2.68719 | 265.789 | 0.387749 | 479.011 | 485.335 | 0.769442 | 343.346 | 953.623 | 0.962701 | 149.354 | 374.64 | 166.842 | 185.9477 | 14426.75 |
| 25352.3 | 15.2839 | 0.875845 | 51.2127 | 3.22698 | 13.8686 | 0.417645 | 415.329 | 57.7891 | 0.913819 | 168.221 | 200.206 | 0.243739 | 108.735 | 366.485 | 119.127 | 185.0229 | 11950.34 |
| 40102.2 | 24.9787 | 0.79383 | 58.2029 | 1.29706 | 6.13349 | 0.232607 | 307.872 | 118.518 | 0.787796 | 287.738 | 517.09 | 0.735424 | 118.485 | 148.38 | 253.407 | 185.4322 | 10453.71 |
| 22236 | 17.6674 | 0.893175 | 41.0498 | 2.62574 | 511.459 | 0.416046 | 268.219 | 313.525 | 0.653294 | 282.888 | 732.497 | 0.98087 | 104.838 | 56.5984 | 69.3252 | 177.859 | 18361.45 |
| 28841 | 26.661 | 0.856453 | 134.577 | 0.955711 | 123.013 | 0.366308 | 112.338 | 321.727 | 0.888386 | 485.649 | 378.613 | 0.555317 | 65.379 | 80.5392 | 445.998 | 195.1637 | 14375.1 |
| 11929.4 | 21.7767 | 0.950491 | 71.565 | 0.725593 | 884.718 | 0.408988 | 425.957 | 127.45 | 0.980132 | 298.647 | 159.385 | 0.93721 | 2.37601 | 360.739 | 107.61 | 120.2224 | 18936.6 |
| 29348.2 | 19.9718 | 0.853627 | 134.459 | 2.93657 | 85.3588 | 0.24686 | 219.13 | 484.489 | 0.876562 | 192.233 | 456.568 | 0.67629 | 11.0429 | 135.778 | 190.165 | 223.3873 | 15929.67 |
| 15904.2 | 25.8353 | 0.928391 | 50.2797 | 1.38242 | 132.977 | 0.210138 | 228.628 | 22.7617 | 0.978458 | 337.438 | 301.482 | 0.498913 | 73.1009 | 38.9044 | 233.315 | 181.8435 | 19398.92 |
| 17841.6 | 33.8496 | 0.917628 | 95.1448 | 3.19548 | 239.915 | 0.510002 | 458.621 | 193.122 | 0.966529 | 410.925 | 277.781 | 0.665633 | 213.036 | 308.615 | 347.652 | 97.79717 | 7968.763 |
| 25050 | 22.2555 | 0.87753 | 115.668 | 1.83779 | 7.58542 | 0.329877 | 448.167 | 170.868 | 0.836488 | 450.413 | 844.603 | 0.732109 | 65.9638 | 48.2534 | 283.082 | 155.9493 | 9142.47 |
| 43091.8 | 28.392 | 0.777208 | 75.638 | 3.60233 | 427.877 | 0.497069 | 221.169 | 933.244 | 0.469376 | 264.675 | 312.105 | 0.859049 | 86.8457 | 85.3776 | 164.539 | 239.4593 | 19111.73 |
| 15803.6 | 14.4762 | 0.928942 | 136.028 | 2.29418 | 180.886 | 0.424145 | 408.243 | 162.339 | 0.832063 | 336.75 | 134.901 | 0.980421 | 125.291 | 314.904 | 274.625 | 70.3492 | 6802.466 |
| 17811.4 | 15.0971 | 0.917777 | 108.437 | 0.911597 | 283.614 | 0.466401 | 148.118 | 550.275 | 0.968227 | 381.401 | 119.915 | 0.498342 | 69.8017 | 70.3602 | 256.213 | 187.8874 | 15863.11 |
| 22348.5 | 31.2407 | 0.892562 | 144.397 | 0.110201 | 134.418 | 0.599468 | 495.646 | 22.7269 | 0.331765 | 267.36 | 628.166 | 0.853317 | 5.34143 | 221.47 | 148.07 | 186.1232 | 13744.38 |
| 39237 | 30.881 | 0.798646 | 87.9478 | 0.417528 | 467.385 | 0.580699 | 136.827 | 359.593 | 0.763704 | 332.402 | 276.548 | 0.594962 | 40.275 | 82.3326 | 154.002 | 190.9672 | 15238.58 |
| 47449.8 | 16.1212 | 0.752967 | 153.671 | 2.40447 | 91.3134 | 0.448205 | 111.454 | 541.054 | 0.655307 | 468.216 | 87.343 | 0.545764 | 45.3965 | 80.0055 | 296.624 | 244.9122 | 15301.03 |
| 30584.6 | 21.6439 | 0.846753 | 133.341 | 2.98779 | 581.683 | 0.562547 | 312.308 | 526.922 | 0.577345 | 280.143 | 711.858 | 0.860761 | 98.5703 | 250.596 | 237.188 | 229.9785 | 18644.02 |
| 29161 | 33.8822 | 0.854681 | 157.649 | 3.35682 | 53.9064 | 0.223079 | 207.822 | 82.4862 | 0.72352 | 140.616 | 26.572 | 0.934826 | 122.941 | 142.181 | 98.3678 | 139.0205 | 10552.1 |
| 43023.2 | 30.7534 | 0.777592 | 137.629 | 3.4511 | 363.612 | 0.431911 | 215.065 | 118.588 | 0.519097 | 138.699 | 34.0052 | 0.834387 | 62.2994 | 75.8733 | 54.1004 | 167.382 | 17584.67 |
| 56838.9 | 19.3019 | 0.700757 | 141.624 | 0.364792 | 220.367 | 0.344299 | 376.163 | 144.153 | 0.896914 | 411.55 | 695.419 | 0.688277 | 29.3183 | 326.177 | 85.3624 | 245.4917 | 17732.55 |
| 11498.9 | 22.3876 | 0.952885 | 142.103 | 1.20249 | 220.877 | 0.305782 | 232.338 | 833.161 | 0.9568 | 143.788 | 534.885 | 0.792794 | 0.571662 | 157.156 | 48.9416 | 222.2211 | 18087.53 |
| 25590.8 | 30.4495 | 0.874531 | 68.3181 | 3.25281 | 28.1677 | 0.497357 | 350.346 | 71.152 | 0.858294 | 405.908 | 44.4528 | 0.903292 | 153.632 | 80.2439 | 123.974 | 45.08811 | 3145.258 |
| 19438.7 | 20.6912 | 0.908732 | 82.4581 | 0.731767 | 157.643 | 0.426125 | 470.497 | 463.83 | 0.753282 | 210.159 | 932.331 | 0.814965 | 8.80465 | 49.9398 | 141.493 | 181.0559 | 12804.98 |
| 50153.4 | 17.969 | 0.737933 | 143.276 | 3.56783 | 332.337 | 0.397041 | 399.086 | 551.776 | 0.967045 | 492.97 | 818.304 | 0.676013 | 144.703 | 73.1156 | 221.453 | 249.3759 | 18789.95 |
| 43035.9 | 16.5108 | 0.777511 | 140.371 | 3.50975 | 59.2653 | 0.442512 | 136.163 | 936.166 | 0.622839 | 79.8112 | 187.126 | 0.97749 | 158.727 | 62.756 | 69.907 | 168.1371 | 9875.109 |

Table B4. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 247.87.

| X1 | X2 | X3 | X4 | X5 | X6 | X7 | X8 | X9 | X10 | X11 | X12 | X13 | X14 | X15 | X16 | UED | UPC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 22193.3 | 25 | 0.95 | 100 | 1.1 | 0.4 | 0.482 | 110 | 0.6 | 0.895 | 130 | 30.9048 | 0.939426 | 100 | 100 | 100 | 44.29242 | 3254.378 |
| 21239.7 | 20.4652 | 0.952482 | 50.7055 | 3.66666 | 68.7679 | 0.476007 | 431.748 | 24.06 | 0.897079 | 72.6242 | 66.2893 | 0.639937 | 161.208 | 172.39 | 47.1405 | 71.6098 | 5801.943 |
| 34862.8 | 13.5894 | 0.916963 | 133.352 | 0.456601 | 66.3568 | 0.483991 | 314.538 | 51.7114 | 0.856411 | 106.629 | 62.1278 | 0.784491 | 43.4387 | 223.243 | 86.3382 | 94.28321 | 6723.086 |
| 53332.2 | 21.6479 | 0.868819 | 73.8098 | 2.52168 | 55.4621 | 0.349555 | 353.78 | 98.2379 | 0.853977 | 486.346 | 30.2145 | 0.932611 | 28.9898 | 192.589 | 268.556 | 105.74 | 7034.75 |
| 38515.5 | 29.3492 | 0.907453 | 84.1058 | 0.601881 | 24.5046 | 0.49057 | 256.16 | 74.0441 | 0.727829 | 55.9559 | 97.3188 | 0.789743 | 52.8093 | 186.727 | 52.3669 | 96.49165 | 6232.484 |
| 43847.8 | 25.1016 | 0.893547 | 100.407 | 3.67263 | 94.8571 | 0.479654 | 491.561 | 11.6149 | 0.666316 | 291.864 | 50.8521 | 0.393271 | 79.6147 | 72.1622 | 72.5313 | 204.9849 | 14827.65 |
| 38903.9 | 24.1047 | 0.906435 | 74.5449 | 1.59342 | 43.8445 | 0.452205 | 236.949 | 96.5909 | 0.652566 | 240.267 | 21.8893 | 0.572284 | 153.814 | 199.533 | 54.2512 | 147.395 | 9946.597 |
| 25130.8 | 27.8344 | 0.942345 | 140.511 | 1.01318 | 60.0404 | 0.595131 | 420.552 | 82.7658 | 0.464144 | 248.543 | 91.4939 | 0.442222 | 47.013 | 145.003 | 225.059 | 214.4131 | 15331.8 |
| 26663 | 28.1471 | 0.938351 | 159.211 | 0.227357 | 51.7852 | 0.724519 | 195.249 | 6.18193 | 0.606824 | 179.376 | 37.1054 | 0.609226 | 7.31254 | 83.5078 | 62.3344 | 112.5913 | 7931.808 |
| 61658.1 | 16.6435 | 0.847111 | 22.1792 | 1.20138 | 47.5491 | 0.439753 | 313.87 | 26.1283 | 0.557783 | 376.833 | 1.93899 | 0.54669 | 81.0672 | 310.409 | 82.4217 | 218.1725 | 13347.33 |
| 29311 | 30.6838 | 0.931451 | 142.679 | 1.54717 | 73.5429 | 0.370395 | 299.038 | 11.5053 | 0.508073 | 480.431 | 61.7879 | 0.556967 | 64.8866 | 233.375 | 259.889 | 247.9647 | 19205.28 |
| 39560.8 | 19.9489 | 0.904719 | 167.405 | 1.48826 | 85.213 | 0.633441 | 442.211 | 77.5662 | 0.842551 | 112.253 | 93.4921 | 0.97397 | 69.3829 | 133.359 | 89.6589 | 69.84976 | 4702.9 |
| 60117.5 | 14.706 | 0.851126 | 49.8042 | 2.79345 | 54.7713 | 0.377013 | 459.693 | 76.5736 | 0.740284 | 420.641 | 16.9503 | 0.866151 | 139.004 | 346.318 | 90.1731 | 123.6393 | 7908.245 |
| 29132.4 | 28.4469 | 0.931914 | 41.4693 | 0.952015 | 89.0431 | 0.314759 | 228.252 | 78.2083 | 0.574059 | 178.375 | 7.46876 | 0.49354 | 26.956 | 58.4786 | 113.413 | 258.9069 | 21607.08 |
| 29698.9 | 25.6851 | 0.930434 | 74.9136 | 3.42805 | 18.4112 | 0.469098 | 458.017 | 1.93124 | 0.482734 | 215.997 | 96.7525 | 0.804531 | 16.8004 | 163.042 | 123.251 | 113.3024 | 7769.665 |
| 36081.5 | 22.5541 | 0.913792 | 152.166 | 0.282258 | 7.48394 | 0.546658 | 194.716 | 69.1883 | 0.675027 | 106.91 | 63.63 | 0.372757 | 11.9533 | 170.521 | 97.1281 | 247.752 | 15348.64 |
| 76326.8 | 15.6383 | 0.80887 | 59.9816 | 3.28478 | 33.8755 | 0.311224 | 449.902 | 91.3612 | 0.579257 | 228.127 | 26.5289 | 0.547687 | 146.286 | 419.624 | 140.044 | 344.8004 | 19387.04 |
| 51313.9 | 20.1606 | 0.87408 | 90.8882 | 1.68976 | 8.16656 | 0.453643 | 327.046 | 9.08775 | 0.752046 | 182.014 | 81.3696 | 0.692042 | 75.8077 | 217.175 | 63.7681 | 111.1921 | 6562.6 |
| 33613 | 16.6115 | 0.920223 | 133.212 | 2.18848 | 10.1635 | 0.439634 | 487.475 | 79.8491 | 0.585337 | 101.148 | 85.0814 | 0.540998 | 165.136 | 465.458 | 82.4615 | 178.9563 | 11447.71 |
| 46533.3 | 26.9999 | 0.886548 | 142.971 | 3.39778 | 86.1743 | 0.303812 | 276.138 | 27.3875 | 0.797982 | 371.617 | 66.0501 | 0.917882 | 25.327 | 78.9337 | 163.318 | 135.1763 | 9972.069 |
| 60872.4 | 20.0441 | 0.849161 | 89.1517 | 2.25458 | 93.9024 | 0.555176 | 390.128 | 67.6423 | 0.840856 | 264.403 | 49.813 | 0.951102 | 132.943 | 138.231 | 225.632 | 82.91928 | 5240.297 |
| 30778.8 | 16.8116 | 0.927611 | 142.697 | 0.393861 | 18.9855 | 0.4402 | 466.441 | 23.3417 | 0.900947 | 478.938 | 12.0804 | 0.516176 | 27.0922 | 55.6213 | 368.465 | 137.5953 | 9296.718 |
| 25074.9 | 18.1388 | 0.942482 | 74.0711 | 2.73296 | 13.5336 | 0.435129 | 192.695 | 66.8857 | 0.77777 | 511.17 | 58.6169 | 0.552197 | 168.029 | 187.008 | 371.832 | 108.6317 | 7516.087 |
| 51479.8 | 25.2843 | 0.873651 | 40.2883 | 2.03448 | 23.499 | 0.330547 | 124.487 | 63.8766 | 0.50177 | 457.623 | 55.8067 | 0.626744 | 152.894 | 52.8105 | 352.174 | 261.8151 | 15936.89 |
| 44659.4 | 19.328 | 0.891427 | 29.8006 | 2.28864 | 70.7608 | 0.312844 | 199.256 | 33.7191 | 0.533484 | 272.901 | 34.9852 | 0.563296 | 74.9753 | 101.833 | 261.498 | 275.2923 | 19984.2 |
| 30187.7 | 21.0614 | 0.929155 | 69.1045 | 2.30339 | 48.0328 | 0.413266 | 357.127 | 87.3065 | 0.337287 | 140.334 | 22.6201 | 0.79877 | 93.2603 | 155.192 | 113.675 | 192.929 | 14185.15 |
| 45766 | 13.5425 | 0.888539 | 43.255 | 0.576165 | 62.9496 | 0.300118 | 295.133 | 94.0803 | 0.787998 | 174.601 | 82.133 | 0.836757 | 46.7601 | 282.156 | 76.557 | 139.6151 | 9842.151 |
| 35362.4 | 25.2897 | 0.915669 | 125.689 | 0.829082 | 25.4476 | 0.466113 | 358.839 | 57.856 | 0.524447 | 232.974 | 43.3113 | 0.655542 | 15.1179 | 57.2236 | 176.164 | 168.8311 | 11124.53 |
| 25360.7 | 27.7396 | 0.941745 | 76.752 | 1.33671 | 78.0198 | 0.380578 | 305.541 | 36.9531 | 0.938695 | 165.871 | 11.4441 | 0.913354 | 99.5972 | 294.576 | 126.022 | 63.36801 | 5454.177 |
| 60224.9 | 20.7592 | 0.850849 | 113.396 | 2.81001 | 13.9365 | 0.473936 | 480.483 | 68.3276 | 0.750062 | 168.618 | 74.475 | 0.696409 | 177.703 | 418.275 | 68.6456 | 122.8487 | 6988.981 |
| 47192.5 | 26.6779 | 0.884829 | 117.141 | 0.62636 | 74.5102 | 0.614173 | 310.1 | 23.2188 | 0.936982 | 506.029 | 46.4246 | 0.692311 | 13.549 | 270.151 | 300.432 | 83.94593 | 5467.946 |
| 57137.8 | 19.5558 | 0.858897 | 166.038 | 0.579156 | 48.5259 | 0.554454 | 389.655 | 43.5775 | 0.426762 | 330.318 | 70.5389 | 0.922537 | 20.9989 | 205.317 | 194.341 | 193.7797 | 11494.82 |
| 76759.8 | 16.4264 | 0.807741 | 74.3491 | 1.32871 | 96.4803 | 0.337085 | 368.342 | 1.99424 | 0.973966 | 411.734 | 4.47807 | 0.426814 | 53.7349 | 277.414 | 95.8135 | 249.5594 | 16358.25 |
| 60919.1 | 16.4999 | 0.849037 | 165.169 | 2.76002 | 65.3424 | 0.542195 | 210.079 | 23.7275 | 0.570102 | 110.849 | 9.11027 | 0.885617 | 162.447 | 165.467 | 109.461 | 129.6246 | 7971.16 |
| 27038 | 32.304 | 0.937378 | 130.851 | 1.93988 | 19.2743 | 0.444471 | 342.004 | 45.9876 | 0.423344 | 256.82 | 12.8464 | 0.584383 | 57.1152 | 118.601 | 139.425 | 201.9417 | 14005.75 |
| 46658 | 23.4502 | 0.88622 | 142.784 | 3.62034 | 88.0401 | 0.635237 | 263.172 | 22.6778 | 0.79131 | 478.503 | 86.5255 | 0.640264 | 313.549 | 214.668 | 443.283 | 134.5209 | 8629.496 |
| 71230 | 16.4699 | 0.822157 | 93.7597 | 3.18836 | 12.4972 | 0.522108 | 463.402 | 68.6392 | 0.606993 | 153.731 | 8.50593 | 0.629915 | 199.669 | 197.789 | 137.381 | 182.7511 | 9771.052 |
| 25501.9 | 17.768 | 0.941369 | 82.1467 | 2.45398 | 12.5864 | 0.4566 | 281.826 | 5.06968 | 0.577136 | 227.045 | 98.1923 | 0.30789 | 177.818 | 69.684 | 146.793 | 233.2875 | 16031.65 |
| 68566.8 | 14.6391 | 0.829099 | 101.955 | 3.59304 | 6.04108 | 0.306099 | 405.807 | 21.7312 | 0.871319 | 223.501 | 33.231 | 0.767661 | 134.595 | 241.038 | 131.319 | 147.2283 | 8008.809 |
| 46546.9 | 14.2471 | 0.886503 | 104.443 | 1.57573 | 6.84429 | 0.508454 | 313.958 | 34.6668 | 0.990467 | 191.085 | 59.4185 | 0.92693 | 104.914 | 293.558 | 55.1607 | 59.43131 | 3646.247 |
| 36990.4 | 19.033 | 0.91142 | 126.037 | 2.35091 | 61.0276 | 0.348228 | 401.334 | 98.6531 | 0.57967 | 376.017 | 16.6145 | 0.952197 | 63.316 | 104.326 | 310.761 | 134.1301 | 9821.222 |
| 52807.5 | 18.2445 | 0.870185 | 128.121 | 0.492352 | 9.9513 | 0.397279 | 190.901 | 86.51 | 0.859451 | 171.494 | 35.1347 | 0.615724 | 39.024 | 125.2 | 123.174 | 167.6335 | 9696.026 |
| 57805.6 | 19.6807 | 0.857156 | 93.6529 | 2.24563 | 56.5863 | 0.435709 | 248.968 | 31.2539 | 0.787369 | 454.62 | 14.0687 | 0.464084 | 162.765 | 152.897 | 45.0091 | 181.1922 | 11512.09 |
| 55354.1 | 23.3577 | 0.863549 | 128.591 | 0.7788 | 24.2213 | 0.59487 | 371.652 | 46.6274 | 0.798355 | 479.466 | 73.6139 | 0.991068 | 56.1334 | 50.7313 | 77.621 | 75.76456 | 4495.742 |
| 24187.7 | 31.5783 | 0.944808 | 54.7502 | 0.574111 | 48.1155 | 0.313244 | 225.469 | 17.35 | 0.82587 | 500.606 | 40.6349 | 0.903223 | 24.6514 | 60.0307 | 151.328 | 84.88017 | 6869.124 |
| 47940.4 | 18.6836 | 0.882873 | 108.177 | 1.28699 | 37.8328 | 0.337225 | 277.025 | 5.08554 | 0.686356 | 227.891 | 65.3202 | 0.311673 | 20.0325 | 44.3144 | 192.252 | 380.9125 | 24493.99 |
| 68528 | 18.693 | 0.829202 | 55.2541 | 1.19863 | 68.0574 | 0.419131 | 126.086 | 2.10162 | 0.616812 | 511.089 | 9.67601 | 0.560481 | 64.5629 | 49.6638 | 309.927 | 216.8579 | 13559.07 |
| 46589.3 | 24.4041 | 0.8864 | 91.4208 | 0.744354 | 95.1427 | 0.433336 | 321.866 | 87.7556 | 0.936642 | 264.247 | 81.9047 | 0.778702 | 66.0917 | 151.181 | 211.56 | 100.9269 | 7201.755 |
| 79599.3 | 13.0273 | 0.800337 | 171.458 | 0.46977 | 70.1527 | 0.338916 | 288.643 | 80.2262 | 0.922257 | 305.671 | 97.1091 | 0.803827 | 6.38595 | 123.229 | 220.668 | 226.2077 | 12917.92 |
| 40556.3 | 26.1638 | 0.902129 | 29.8087 | 1.08157 | 19.864 | 0.408001 | 446.505 | 65.8631 | 0.916104 | 208.59 | 35.1686 | 0.923915 | 11.9113 | 349.116 | 48.4046 | 71.21258 | 4667.368 |
| 59973.9 | 15.5098 | 0.851501 | 31.0227 | 0.780287 | 16.0078 | 0.340192 | 407.28 | 14.8257 | 0.775603 | 364.468 | 27.7013 | 0.983389 | 35.2079 | 70.1515 | 219.752 | 107.1064 | 6292.607 |
| 20819.8 | 32.5422 | 0.95359 | 77.0123 | 3.00966 | 42.3783 | 0.346057 | 375.881 | 99.7305 | 0.549521 | 221.628 | 14.0095 | 0.875398 | 44.7267 | 352.565 | 134.176 | 117.0706 | 9298.216 |
| 24993.3 | 23.3826 | 0.942699 | 153.922 | 0.552461 | 28.5121 | 0.390627 | 222.885 | 80.7952 | 0.914596 | 455.464 | 14.8469 | 0.31059 | 45.7234 | 44.3577 | 315.565 | 262.0573 | 18339.84 |
| 43687.2 | 25.7369 | 0.893966 | 116.244 | 0.721075 | 70.9721 | 0.356256 | 128.876 | 54.9684 | 0.722127 | 347.062 | 64.4209 | 0.61996 | 40.8637 | 59.3791 | 77.6724 | 193.6471 | 13564.54 |
| 37480.4 | 17.4218 | 0.910141 | 126.729 | 2.51209 | 55.5538 | 0.622898 | 492.745 | 60.0752 | 0.885052 | 319.52 | 79.4692 | 0.709957 | 133.818 | 168.403 | 303.354 | 96.33739 | 6295.028 |
| 65945.7 | 13.5244 | 0.835931 | 14.7431 | 0.538412 | 86.5465 | 0.431783 | 315.43 | 57.8849 | 0.411907 | 452.597 | 60.1377 | 0.528767 | 42.2424 | 78.2921 | 63.8573 | 339.3179 | 21935.37 |
| 52185.8 | 24.5738 | 0.87181 | 93.5076 | 0.424287 | 71.1183 | 0.465277 | 196.782 | 15.6765 | 0.728047 | 298.718 | 44.0444 | 0.461841 | 36.4564 | 158.921 | 98.2558 | 200.115 | 13193.1 |
| 74203.7 | 16.5213 | 0.814405 | 55.3147 | 0.470819 | 34.6796 | 0.319921 | 342.921 | 81.9394 | 0.742396 | 396.259 | 68.3516 | 0.729624 | 25.4887 | 79.6073 | 365.329 | 197.3711 | 11285.76 |
| 28989.8 | 20.3657 | 0.932278 | 40.6302 | 1.49482 | 75.2318 | 0.467779 | 168.575 | 94.3027 | 0.875655 | 185.742 | 61.5253 | 0.388226 | 63.3215 | 146.235 | 146.413 | 151.3808 | 11328.9 |
| 40256.7 | 16.4866 | 0.902903 | 67.7338 | 0.937503 | 39.703 | 0.551083 | 171.849 | 83.402 | 0.918231 | 261.365 | 65.3663 | 0.566842 | 93.7041 | 163.435 | 224.097 | 120.0158 | 7624.473 |
| 53087.2 | 17.123 | 0.869455 | 77.7925 | 2.25678 | 93.0267 | 0.417284 | 463.174 | 68.177 | 0.63273 | 487.007 | 48.6121 | 0.875865 | 106.881 | 280.337 | 336.662 | 126.4392 | 8945.412 |
| 46730.1 | 26.8427 | 0.886035 | 32.1881 | 2.13076 | 80.595 | 0.494785 | 213.12 | 95.4185 | 0.489196 | 219.607 | 41.5389 | 0.796483 | 12.7691 | 71.5433 | 145.769 | 143.707 | 9830.76 |
| 38450.8 | 26.418 | 0.907618 | 162.296 | 0.644609 | 77.8905 | 0.488624 | 208.897 | 16.4656 | 0.340842 | 317.502 | 67.6029 | 0.64731 | 19.4302 | 84.5089 | 57.0124 | 316.2138 | 21898.52 |
| 58807.9 | 20.5344 | 0.854543 | 172.935 | 3.21273 | 2.42243 | 0.444296 | 331.389 | 68.0147 | 0.382431 | 362.972 | 49.6752 | 0.682889 | 9.24383 | 167.343 | 302.079 | 306.5227 | 16829.39 |
| 52868.1 | 24.2144 | 0.870031 | 77.478 | 1.44771 | 31.445 | 0.377707 | 124.109 | 21.5832 | 0.776992 | 130.036 | 39.0854 | 0.869378 | 128.422 | 75.4296 | 124.055 | 106.1874 | 6688.803 |
| 30670.5 | 26.9541 | 0.927902 | 128.913 | 1.11469 | 58.6163 | 0.328189 | 329.12 | 0.880071 | 0.960884 | 157.964 | 91.5872 | 0.846692 | 68.7665 | 88.1934 | 113.909 | 99.98495 | 7593.433 |
| 64692.3 | 16.9384 | 0.839201 | 155.47 | 1.13809 | 96.5258 | 0.588264 | 414.644 | 62.8818 | 0.575469 | 290.826 | 13.8728 | 0.944264 | 111.373 | 221.421 | 151.566 | 126.9742 | 7835.173 |
| 72218.1 | 15.4297 | 0.81958 | 106.282 | 1.67279 | 23.1683 | 0.415314 | 344.933 | 34.0906 | 0.601791 | 360.205 | 5.43112 | 0.600209 | 39.9827 | 248.335 | 244.544 | 218.8397 | 12103.07 |
| 37537.9 | 18.3803 | 0.909992 | 18.7998 | 3.27997 | 77.2585 | 0.460183 | 277.07 | 94.0507 | 0.488143 | 405.149 | 85.9973 | 0.865507 | 37.7522 | 193.668 | 158.502 | 130.5483 | 9520.158 |
| 63659.6 | 14.6494 | 0.841892 | 135.368 | 2.67947 | 70.6315 | 0.441956 | 384.622 | 88.1965 | 0.622846 | 270.324 | 17.5059 | 0.599106 | 100.452 | 332.385 | 87.9858 | 207.7946 | 12994.35 |
| 34657.9 | 24.9754 | 0.917505 | 43.7261 | 0.880339 | 71.9527 | 0.416347 | 161.569 | 85.3958 | 0.374418 | 304.873 | 71.3758 | 0.991248 | 3.36069 | 107.612 | 86.783 | 155.9002 | 11726.63 |
| 64757.6 | 17.6449 | 0.839031 | 149.629 | 0.665297 | 46.557 | 0.587424 | 191.559 | 72.4217 | 0.951144 | 148.899 | 53.9688 | 0.955718 | 18.9387 | 97.2888 | 122.341 | 85.87073 | 5017.163 |
| 31959.7 | 25.4592 | 0.92454 | 115.258 | 2.92418 | 27.5949 | 0.488725 | 258.978 | 44.5327 | 0.61336 | 306.087 | 10.8116 | 0.537037 | 30.7787 | 205.607 | 237.305 | 132.8265 | 9070.38 |
| 48135.7 | 16.9994 | 0.882363 | 100.112 | 1.39384 | 20.4372 | 0.517639 | 260.928 | 39.3103 | 0.912231 | 386.844 | 30.1739 | 0.909665 | 50.3294 | 127.104 | 118.776 | 62.74087 | 3915.687 |
| 74932.8 | 15.5453 | 0.812504 | 18.5966 | 2.76484 | 6.87495 | 0.555978 | 497.128 | 92.5903 | 0.65701 | 382.307 | 54.5478 | 0.708114 | 205.436 | 267.638 | 272.182 | 173.0585 | 9050.904 |
| 41473.6 | 13.4797 | 0.899729 | 85.9428 | 0.25309 | 7.98175 | 0.44959 | 164.816 | 20.8227 | 0.591729 | 330.465 | 73.5353 | 0.325543 | 13.2332 | 98.0128 | 150.436 | 308.3567 | 18726.75 |
| 69521.7 | 20.1914 | 0.826612 | 88.7964 | 0.30084 | 18.2493 | 0.416298 | 435.305 | 60.5506 | 0.492037 | 407.936 | 78.2653 | 0.855134 | 12.7571 | 119.725 | 331.703 | 209.656 | 11504.69 |
| 32902.3 | 18.8194 | 0.922077 | 155.467 | 1.57171 | 81.1292 | 0.317614 | 250.815 | 67.742 | 0.570706 | 404.777 | 99.0531 | 0.717994 | 14.9132 | 111.526 | 126.465 | 228.7715 | 17411.09 |
| 26451.9 | 26.5917 | 0.9389 | 154.168 | 1.82079 | 64.1434 | 0.587018 | 392.877 | 53.8571 | 0.523359 | 309.493 | 26.6877 | 0.82536 | 141.252 | 384.003 | 211.695 | 98.95343 | 7289.843 |
| 25652.3 | 24.5734 | 0.940982 | 115.604 | 2.06103 | 49.9241 | 0.49687 | 245.893 | 55.0615 | 0.931315 | 383.519 | 28.262 | 0.706565 | 81.2553 | 104.259 | 104.082 | 66.77049 | 5041.87 |
| 73349.5 | 15.0982 | 0.816631 | 31.007 | 0.500521 | 69.2545 | 0.452816 | 119.244 | 47.2802 | 0.787305 | 296.416 | 33.0806 | 0.948853 | 24.0319 | 104.032 | 136.786 | 99.18199 | 6128.557 |
| 32928.9 | 20.2831 | 0.922009 | 89.5028 | 0.600596 | 98.2784 | 0.439579 | 313.176 | 90.7856 | 0.537118 | 108.694 | 20.321 | 0.760161 | 13.2949 | 267.515 | 100.26 | 143.0776 | 11293.58 |
| 57067 | 19.1931 | 0.859081 | 55.7192 | 1.939 | 78.4059 | 0.510219 | 332.297 | 95.7241 | 0.584223 | 337.779 | 17.5487 | 0.852499 | 130.216 | 179.832 | 236.998 | 123.9457 | 7831.007 |
| 24346.3 | 14.7377 | 0.94438 | 137.211 | 2.9556 | 11.2376 | 0.465269 | 404.933 | 47.5937 | 0.76981 | 437.752 | 77.4585 | 0.651306 | 75.1628 | 343.065 | 119.064 | 92.57647 | 6425.937 |
| 34763.3 | 29.1372 | 0.917235 | 140.532 | 1.16661 | 47.7314 | 0.601397 | 482.765 | 36.1393 | 0.95088 | 295.465 | 49.7555 | 0.711981 | 71.5038 | 231.081 | 209.309 | 69.81983 | 4740.159 |
| 21843.8 | 16.1744 | 0.950904 | 162.731 | 2.70722 | 15.8449 | 0.448607 | 108.956 | 30.372 | 0.418534 | 485.29 | 21.1578 | 0.698684 | 95.1248 | 92.5396 | 335.877 | 166.9228 | 11982.59 |
| 21582.5 | 15.1515 | 0.951585 | 22.757 | 2.75604 | 58.7927 | 0.458132 | 411.899 | 69.3461 | 0.617177 | 388.579 | 57.5169 | 0.514494 | 171.673 | 377.386 | 342.684 | 137.3829 | 10763.66 |
| 41715.2 | 28.3964 | 0.89911 | 145.197 | 0.950831 | 37.0548 | 0.406879 | 358.491 | 38.7429 | 0.418515 | 358.98 | 26.7589 | 0.890884 | 34.5655 | 312.838 | 200.847 | 203.6372 | 13290.52 |
| 58296.2 | 23.6022 | 0.855879 | 158.751 | 0.658967 | 18.5731 | 0.459249 | 455.561 | 31.1063 | 0.451003 | 385.741 | 88.327 | 0.946179 | 59.6572 | 106.213 | 320.85 | 207.0921 | 11798.22 |
| 61232.2 | 21.7469 | 0.848224 | 60.2201 | 2.9379 | 81.4382 | 0.69483 | 499.156 | 59.0783 | 0.830799 | 492.034 | 2.63935 | 0.911211 | 248.4 | 370.89 | 354.448 | 92.08744 | 5533.701 |
| 54565.3 | 23.3163 | 0.865605 | 99.0986 | 2.54437 | 65.7378 | 0.323526 | 393.649 | 57.6549 | 0.412846 | 243.473 | 48.269 | 0.943437 | 151.16 | 195.823 | 175.569 | 229.5538 | 15478.1 |
| 45400.9 | 22.2134 | 0.889496 | 153.947 | 3.27554 | 38.0019 | 0.62802 | 301.915 | 52.5457 | 0.728624 | 441.72 | 98.2702 | 0.827704 | 45.6268 | 136.385 | 420.558 | 101.3815 | 6247.18 |
| 52445.9 | 24.096 | 0.871131 | 155.291 | 3.54576 | 31.743 | 0.478693 | 329.539 | 51.692 | 0.9267 | 457.655 | 93.5586 | 0.5682 | 57.9086 | 153.113 | 418.405 | 130.7595 | 7938.382 |
| 44088.6 | 19.3715 | 0.892915 | 98.0811 | 0.145367 | 31.39 | 0.347977 | 283.303 | 33.3888 | 0.546592 | 212.668 | 65.4386 | 0.417273 | 3.47729 | 83.1149 | 128.753 | 390.3062 | 24760.19 |
| 27095.7 | 13.505 | 0.937211 | 26.1202 | 1.79213 | 31.062 | 0.306745 | 163.488 | 45.6688 | 0.425195 | 467.915 | 1.27723 | 0.73978 | 6.7344 | 81.9831 | 425.422 | 205.1594 | 15148.46 |
| 44510.5 | 25.6133 | 0.89182 | 78.1607 | 1.40944 | 88.1133 | 0.453428 | 264.119 | 21.0244 | 0.66328 | 174.198 | 53.8378 | 0.411433 | 85.2754 | 170.696 | 73.6663 | 212.2795 | 15309.69 |
| 52497.9 | 14.425 | 0.87099 | 75.6491 | 0.808201 | 97.2066 | 0.320471 | 88.5394 | 78.3381 | 0.821202 | 287.138 | 94.4377 | 0.846779 | 33.1227 | 80.8093 | 191.858 | 138.085 | 10086.8 |
| 63319.9 | 17.8655 | 0.842779 | 150.264 | 1.85209 | 37.352 | 0.429778 | 482.861 | 58.345 | 0.392104 | 289.31 | 35.7991 | 0.771287 | 158.044 | 351.353 | 223.695 | 279.3544 | 16233.91 |
| 41214.8 | 28.8038 | 0.900415 | 148.224 | 1.02751 | 71.2975 | 0.56573 | 279.601 | 99.5237 | 0.872819 | 77.789 | 92.0732 | 0.89262 | 31.9543 | 121.103 | 53.1379 | 82.41139 | 5509.623 |
| 32225 | 24.3752 | 0.923847 | 48.0034 | 2.53241 | 29.5354 | 0.574538 | 291.748 | 77.5644 | 0.73626 | 441.022 | 3.77743 | 0.936714 | 151.749 | 247.514 | 289.692 | 71.19478 | 4835.674 |
| 73158.8 | 17.1499 | 0.817129 | 126.13 | 1.50125 | 67.9708 | 0.320023 | 317.773 | 47.0503 | 0.653216 | 382.339 | 56.5489 | 0.708196 | 122.948 | 193.323 | 176.601 | 257.3987 | 15712.37 |
| 28611.3 | 14.6531 | 0.933261 | 114.348 | 0.33707 | 44.2137 | 0.456396 | 487.664 | 21.4661 | 0.318171 | 342.206 | 23.2548 | 0.63483 | 14.7985 | 258.28 | 150.185 | 271.2278 | 19511.3 |
| 34697.3 | 26.6493 | 0.917404 | 171.238 | 1.71708 | 90.4474 | 0.460566 | 383.877 | 51.7572 | 0.811017 | 127.789 | 74.5798 | 0.541997 | 39.9602 | 374.304 | 103.853 | 161.1817 | 11798.08 |
| 44974.8 | 27.0008 | 0.890611 | 160.24 | 0.190214 | 0.300405 | 0.388842 | 98.2504 | 99.2699 | 0.647044 | 203.149 | 54.3442 | 0.89909 | 3.26773 | 68.1306 | 45.5301 | 178.6884 | 10502.7 |
| 40357 | 18.706 | 0.902643 | 66.7722 | 2.1068 | 67.6929 | 0.397341 | 354.399 | 30.1121 | 0.650821 | 297.929 | 96.2937 | 0.738336 | 121.679 | 123.697 | 228.756 | 132.149 | 9565.38 |
| 20774.2 | 14.1925 | 0.953692 | 146.476 | 3.06881 | 29.7389 | 0.466527 | 477.911 | 73.5554 | 0.680038 | 388.047 | 73.2527 | 0.38927 | 93.7803 | 400.89 | 242.104 | 177.0784 | 12921.65 |
| 25581.6 | 16.7483 | 0.94116 | 48.5759 | 2.72814 | 52.9236 | 0.316408 | 199.465 | 52.648 | 0.542688 | 313.924 | 18.2508 | 0.829755 | 168.516 | 79.5689 | 146.835 | 141.5121 | 11267.49 |
| 57453.3 | 22.5232 | 0.858076 | 99.9941 | 2.04153 | 71.2666 | 0.427222 | 307.088 | 27.0239 | 0.510216 | 128.98 | 11.9001 | 0.613043 | 159.165 | 76.4658 | 46.025 | 216.8324 | 14254.84 |
| 74782.5 | 18.1478 | 0.812897 | 25.0765 | 3.11922 | 71.846 | 0.480032 | 350.957 | 18.203 | 0.409665 | 269.22 | 98.7918 | 0.803218 | 93.9714 | 288.06 | 158.085 | 215.7218 | 12842.03 |
| 22999.5 | 32.7599 | 0.947908 | 122.38 | 3.54337 | 19.2898 | 0.440987 | 132.255 | 9.82574 | 0.361926 | 167.458 | 94.2068 | 0.935865 | 119.909 | 112.287 | 152.652 | 127.7214 | 9225.833 |
| 46961.6 | 13.976 | 0.885422 | 155.264 | 0.477844 | 82.2492 | 0.497415 | 132.531 | 95.6308 | 0.884741 | 426.448 | 8.1558 | 0.507784 | 33.7266 | 67.8302 | 226.506 | 176.6811 | 11642.63 |
| 68736.1 | 19.4298 | 0.82866 | 148.468 | 2.94959 | 21.8867 | 0.534097 | 192.899 | 65.728 | 0.373652 | 436.073 | 76.0094 | 0.911223 | 98.2524 | 129.014 | 131.844 | 198.7942 | 10912.08 |
| 58096.2 | 18.8119 | 0.856398 | 36.9742 | 1.94336 | 42.4045 | 0.350067 | 368.841 | 30.7157 | 0.722545 | 291.219 | 8.71046 | 0.729478 | 165.208 | 310.91 | 274.79 | 153.7869 | 9678.244 |
| 36158.2 | 29.0946 | 0.913598 | 117.271 | 3.19372 | 13.9166 | 0.41709 | 117.874 | 21.9601 | 0.50204 | 195.384 | 62.788 | 0.674594 | 101.545 | 68.7676 | 94.489 | 158.1122 | 10244.72 |
| 45466.1 | 25.7585 | 0.889329 | 83.98 | 2.61889 | 25.6887 | 0.337011 | 375.734 | 19.5436 | 0.457394 | 430.857 | 30.5732 | 0.485934 | 64.5209 | 131.378 | 199.16 | 332.1597 | 21070.14 |
| 27374.2 | 20.4975 | 0.93649 | 21.893 | 2.0379 | 57.9297 | 0.407665 | 315.311 | 65.4503 | 0.712742 | 135.452 | 11.211 | 0.788369 | 107.552 | 64.8318 | 96.4185 | 92.0043 | 7195.292 |
| 33287.7 | 24.9763 | 0.921077 | 51.1727 | 0.850861 | 98.2745 | 0.373979 | 350.496 | 97.2035 | 0.947067 | 334.59 | 58.3232 | 0.436273 | 27.4601 | 163.045 | 282.608 | 169.3666 | 13432.22 |
| 48060.5 | 15.2426 | 0.882558 | 145.994 | 0.634933 | 61.5581 | 0.417794 | 302.947 | 81.0411 | 0.694285 | 357.889 | 1.26195 | 0.672883 | 50.8167 | 253.59 | 52.31 | 182.7564 | 11965.85 |
| 25238 | 16.2608 | 0.942056 | 73.7629 | 2.95597 | 8.40378 | 0.399837 | 355.467 | 86.8608 | 0.818003 | 175.618 | 0.231104 | 0.317194 | 2.24923 | 74.6982 | 103.905 | 198.2645 | 13350.48 |
| 32029.4 | 19.7369 | 0.924353 | 116.735 | 1.11552 | 8.68769 | 0.492193 | 83.1369 | 50.3285 | 0.429682 | 165.544 | 47.576 | 0.979321 | 58.7893 | 72.5623 | 57.7125 | 113.8448 | 7465.25 |
| 54051.4 | 16.7487 | 0.866941 | 148.873 | 2.49522 | 63.264 | 0.530109 | 280.37 | 57.9637 | 0.963382 | 250.393 | 78.422 | 0.714331 | 166.764 | 134.623 | 77.1191 | 95.11624 | 6014.734 |
| 22799.4 | 13.6022 | 0.948412 | 117.85 | 3.39617 | 71.1467 | 0.678055 | 343.701 | 65.1836 | 0.893536 | 516.857 | 85.3923 | 0.776783 | 249.86 | 268.252 | 318.809 | 85.23078 | 6045.161 |
| 54992.2 | 13.0599 | 0.864486 | 169.068 | 1.9565 | 52.4142 | 0.611917 | 432.889 | 25.2176 | 0.895286 | 201.731 | 13.084 | 0.767284 | 136.312 | 177.322 | 56.5061 | 83.66905 | 5157.895 |
| 21246.5 | 13.1464 | 0.95246 | 170.508 | 1.33377 | 55.9124 | 0.451059 | 158.064 | 16.8022 | 0.775187 | 509.022 | 65.6806 | 0.370978 | 33.9111 | 85.3325 | 272.332 | 200.6966 | 15458.46 |
| 46187 | 22.9606 | 0.887447 | 172.295 | 1.24989 | 36.7655 | 0.667383 | 77.7657 | 30.1829 | 0.40014 | 318.59 | 75.3433 | 0.770192 | 68.7657 | 69.1339 | 278.952 | 173.2781 | 10524.56 |
| 34425.5 | 24.7949 | 0.918111 | 156.795 | 2.89826 | 50.8162 | 0.54363 | 218.179 | 12.2729 | 0.818879 | 327.925 | 61.5185 | 0.400867 | 33.9581 | 97.7773 | 272.545 | 147.649 | 10220.53 |
| 57884.3 | 20.013 | 0.856951 | 129.58 | 1.90865 | 83.4959 | 0.438058 | 349.222 | 55.1367 | 0.910947 | 478.432 | 40.7251 | 0.59942 | 21.0338 | 181.811 | 385.933 | 141.7823 | 9386.19 |
| 29028.2 | 17.2126 | 0.932176 | 165.605 | 1.51465 | 32.4162 | 0.436263 | 282.333 | 57.2767 | 0.925503 | 207.965 | 22.46 | 0.405735 | 28.7467 | 275.971 | 181.664 | 173.1671 | 11993.07 |
| 24878.1 | 23.9324 | 0.943 | 34.8554 | 1.56851 | 2.75367 | 0.682804 | 393.581 | 22.3514 | 0.962567 | 431.353 | 56.8105 | 0.594418 | 67.6052 | 326.054 | 373.596 | 104.611 | 6988.912 |
| 21999.4 | 24.2839 | 0.950505 | 148.8 | 0.637241 | 48.86 | 0.63406 | 202.161 | 74.5639 | 0.775186 | 107.767 | 62.0116 | 0.952685 | 39.4235 | 124.196 | 95.8097 | 59.43017 | 4374.58 |
| 31562.3 | 23.0029 | 0.925573 | 67.5546 | 0.251809 | 97.3065 | 0.395629 | 378.348 | 84.5114 | 0.884423 | 388.364 | 63.2995 | 0.697213 | 21.9729 | 271.585 | 187.899 | 109.9036 | 8759.125 |
| 28305.5 | 19.8482 | 0.934061 | 107.696 | 1.50828 | 20.7795 | 0.371435 | 108.347 | 56.1371 | 0.390446 | 121.838 | 91.3409 | 0.770928 | 29.3723 | 65.3645 | 111.478 | 194.0698 | 13428.49 |
| 23882.9 | 14.551 | 0.945588 | 160.779 | 1.06378 | 17.4624 | 0.605175 | 219.517 | 57.492 | 0.480211 | 348.608 | 79.6611 | 0.422205 | 61.4724 | 201.556 | 193.368 | 214.4783 | 14683.64 |
| 22666.5 | 19.8732 | 0.948762 | 147.032 | 1.19905 | 95.0753 | 0.592346 | 315.162 | 9.35792 | 0.449749 | 446.661 | 92.2037 | 0.877632 | 63.8197 | 204.951 | 225.412 | 105.6271 | 8306.115 |
| 28956.4 | 31.5322 | 0.932376 | 55.4665 | 2.18014 | 1.65635 | 0.430468 | 479.719 | 78.9091 | 0.643277 | 283.065 | 81.6237 | 0.881778 | 24.9459 | 314.576 | 100.198 | 89.48569 | 5862.886 |
| 26087.2 | 31.9736 | 0.939857 | 137.883 | 2.33593 | 98.5711 | 0.353419 | 338.203 | 77.4344 | 0.820519 | 407.092 | 31.5511 | 0.992278 | 89.8797 | 204.943 | 109.842 | 89.18 | 7593.477 |
| 41913.3 | 19.9927 | 0.898586 | 38.7747 | 3.51399 | 83.7028 | 0.410035 | 341.941 | 52.8308 | 0.613507 | 389.207 | 29.8549 | 0.784845 | 9.13241 | 130.202 | 181.65 | 129.5692 | 9683.03 |
| 23802.9 | 21.2511 | 0.945801 | 80.6318 | 2.15107 | 12.9554 | 0.532299 | 192.328 | 43.0414 | 0.748181 | 219.239 | 97.865 | 0.869885 | 50.2461 | 155.833 | 137.476 | 70.3335 | 4860.003 |
| 53976.2 | 16.6131 | 0.867137 | 22.7908 | 0.838637 | 27.3883 | 0.463026 | 274.884 | 85.1012 | 0.307832 | 287.672 | 75.3508 | 0.545087 | 50.7521 | 97.3483 | 193.709 | 354.6295 | 21095.98 |
| 36316.8 | 29.3463 | 0.913185 | 114.699 | 0.186805 | 96.9152 | 0.527041 | 428.604 | 42.91 | 0.960506 | 157.653 | 4.99529 | 0.560823 | 4.08095 | 178.874 | 84.5684 | 111.1133 | 8169.159 |
| 36701.8 | 19.4887 | 0.912172 | 22.2859 | 0.475548 | 36.4118 | 0.309256 | 322.755 | 55.1409 | 0.641195 | 216.992 | 93.7301 | 0.395292 | 35.3164 | 127.251 | 130.193 | 300.0139 | 20650.33 |
| 30000.3 | 31.5066 | 0.929655 | 47.0072 | 2.14183 | 74.267 | 0.374178 | 388.128 | 57.3592 | 0.944394 | 311.249 | 27.4091 | 0.975924 | 56.7205 | 291.106 | 66.3039 | 72.65046 | 5860.775 |
| 36442.5 | 20.2209 | 0.912849 | 143.039 | 2.66506 | 0.185638 | 0.453378 | 115.961 | 83.2359 | 0.995455 | 490.803 | 93.3859 | 0.474082 | 18.3577 | 53.8373 | 52.7 | 130.7947 | 7992.472 |
| 62484.5 | 13.7081 | 0.844955 | 165.954 | 0.690773 | 71.6524 | 0.506371 | 245.915 | 58.3728 | 0.953056 | 69.1176 | 38.7384 | 0.738967 | 44.6658 | 193.229 | 58.2047 | 125.3744 | 7623.32 |
| 48322.8 | 13.9076 | 0.881874 | 100.33 | 3.18471 | 22.1461 | 0.417286 | 209.329 | 41.6284 | 0.698952 | 259.692 | 73.675 | 0.496601 | 133.715 | 165.887 | 80.2227 | 179.1483 | 10992.53 |
| 32439.1 | 30.9556 | 0.923296 | 128.98 | 0.322662 | 74.4821 | 0.440346 | 285.972 | 12.3014 | 0.710108 | 453.21 | 41.8131 | 0.930414 | 25.567 | 130.187 | 56.0985 | 100.4805 | 7543.315 |
| 53901.3 | 24.3584 | 0.867337 | 128.216 | 1.86735 | 12.198 | 0.33243 | 256.655 | 19.392 | 0.920569 | 498.491 | 32.6869 | 0.365256 | 68.2227 | 92.4762 | 419.71 | 268.9833 | 15623.09 |
| 24273.1 | 23.0438 | 0.944576 | 34.1098 | 2.17549 | 73.7646 | 0.437455 | 178.939 | 74.7621 | 0.362806 | 179.858 | 32.0704 | 0.671371 | 101.91 | 160.863 | 93.3079 | 192.6855 | 15571.03 |
| 51813.9 | 17.2507 | 0.872774 | 77.3832 | 0.629274 | 98.7725 | 0.411913 | 435.406 | 64.1476 | 0.699424 | 430.364 | 54.2596 | 0.936792 | 1.76742 | 247.986 | 426.619 | 111.7717 | 8070.974 |
| 32715.5 | 23.132 | 0.922567 | 105.632 | 0.596471 | 99.6858 | 0.526622 | 437.383 | 13.3521 | 0.430904 | 495.155 | 63.5504 | 0.994997 | 38.9169 | 362.385 | 451.366 | 114.7541 | 8853.681 |
| 41192.6 | 17.3673 | 0.900464 | 137.023 | 2.12202 | 30.7164 | 0.391981 | 129.667 | 21.5961 | 0.821754 | 341.952 | 1.25956 | 0.764987 | 96.5445 | 74.7972 | 144.503 | 106.7229 | 7116.478 |
| 37727.2 | 19.2742 | 0.909499 | 117.249 | 3.14375 | 70.9346 | 0.450837 | 205.349 | 10.379 | 0.913414 | 501.178 | 67.2259 | 0.651834 | 16.7836 | 55.0045 | 87.6003 | 89.24274 | 6641.709 |
| 24505.3 | 31.3352 | 0.94398 | 46.45 | 3.22839 | 18.6854 | 0.499181 | 385.068 | 42.9422 | 0.430126 | 400.086 | 64.631 | 0.995241 | 186.631 | 195.42 | 322.4 | 95.41652 | 6711.812 |
| 46011.9 | 26.1047 | 0.887906 | 121.09 | 1.52167 | 68.804 | 0.372658 | 454.433 | 66.8272 | 0.578456 | 217.412 | 10.2191 | 0.689626 | 56.3617 | 174.166 | 205.325 | 197.7841 | 13740.98 |
| 64890.5 | 16.5993 | 0.838684 | 24.2045 | 0.513597 | 99.7931 | 0.468362 | 364.877 | 45.52 | 0.662018 | 209.872 | 54.6602 | 0.323569 | 45.1547 | 330.548 | 176.467 | 320.9443 | 20974.39 |
| 68784.8 | 19.7718 | 0.828533 | 19.797 | 0.620851 | 90.1635 | 0.447109 | 52.0384 | 85.8324 | 0.618717 | 391.281 | 6.35003 | 0.433917 | 10.6962 | 46.1008 | 88.5421 | 282.7509 | 18044.99 |
| 31159.3 | 18.5338 | 0.926621 | 26.3097 | 1.02705 | 62.0707 | 0.362343 | 150.785 | 90.4277 | 0.550452 | 169.244 | 28.4657 | 0.62076 | 24.3595 | 120.503 | 45.5813 | 183.25 | 13967 |
| 20606 | 32.1132 | 0.954146 | 72.2693 | 3.49043 | 31.0019 | 0.433553 | 348.041 | 32.4304 | 0.92581 | 376.032 | 98.0753 | 0.909705 | 158.911 | 263.625 | 133.463 | 55.60353 | 4244.841 |
| 37503.6 | 19.3959 | 0.910082 | 32.9003 | 3.55289 | 7.04417 | 0.344571 | 312.736 | 33.1437 | 0.826177 | 203.509 | 54.2788 | 0.513969 | 121.153 | 239.226 | 156.366 | 153.6483 | 9692.05 |
| 71670.5 | 18.5496 | 0.82101 | 122.933 | 3.14451 | 3.98915 | 0.372389 | 147.448 | 42.2451 | 0.328864 | 171.605 | 22.1406 | 0.667308 | 99.5832 | 130.485 | 115.634 | 390.1509 | 20423.46 |
| 57582.2 | 21.5225 | 0.857739 | 114.287 | 1.29673 | 94.963 | 0.511604 | 268.53 | 69.78 | 0.454451 | 280.845 | 14.6876 | 0.38487 | 106.085 | 186.755 | 154.124 | 367.0235 | 23860.83 |
| 52777.3 | 16.9963 | 0.870263 | 170.482 | 3.51002 | 18.9027 | 0.459292 | 263.214 | 20.8562 | 0.612837 | 290.533 | 4.83574 | 0.882374 | 15.2098 | 62.6578 | 134.72 | 127.4751 | 7627.013 |
| 46320.8 | 16.7557 | 0.887094 | 19.987 | 3.74759 | 47.3503 | 0.363063 | 280.626 | 0.485144 | 0.903289 | 261.411 | 15.6502 | 0.863314 | 4.90729 | 86.0448 | 215.89 | 86.27343 | 6006.742 |
| 35941.9 | 18.3816 | 0.914153 | 92.8737 | 2.06424 | 87.2879 | 0.458812 | 307.149 | 12.6221 | 0.636929 | 113.29 | 51.629 | 0.418192 | 109.185 | 239.614 | 89.2608 | 190.3639 | 14479.43 |
| 33975.2 | 16.953 | 0.919279 | 168.11 | 2.58242 | 43.8211 | 0.610552 | 219.26 | 44.3298 | 0.657554 | 131.046 | 38.6478 | 0.887529 | 164.811 | 191.382 | 84.7844 | 80.09751 | 5402.377 |
| 29915.8 | 14.0311 | 0.92986 | 28.6144 | 1.45223 | 82.6654 | 0.321311 | 249.907 | 45.5716 | 0.6242 | 172.981 | 18.5064 | 0.887796 | 135.864 | 154.346 | 84.2169 | 123.6882 | 10318.99 |
| 41864.2 | 16.8706 | 0.898712 | 30.4709 | 1.93682 | 83.5055 | 0.478827 | 256.202 | 90.6497 | 0.303081 | 151.94 | 1.34214 | 0.67953 | 132.027 | 158.307 | 99.3428 | 253.5111 | 17933.9 |
| 60184 | 19.8338 | 0.850955 | 47.0047 | 2.91985 | 29.3212 | 0.459374 | 113.305 | 41.5969 | 0.956284 | 407.538 | 60.8432 | 0.500399 | 85.559 | 51.8845 | 301.258 | 136.9637 | 8078.031 |
| 41601.4 | 20.0397 | 0.8994 | 162.257 | 0.954937 | 9.38716 | 0.427672 | 72.0618 | 96.9375 | 0.798338 | 186.879 | 57.9376 | 0.698449 | 3.37266 | 55.0919 | 101.919 | 145.3086 | 8859.028 |
| 45322.2 | 20.686 | 0.8897 | 160.598 | 0.277789 | 16.9316 | 0.619785 | 404.239 | 29.855 | 0.80428 | 196.068 | 47.148 | 0.74819 | 13.3322 | 251.135 | 177.089 | 102.5233 | 6254.576 |
| 76121.2 | 13.8565 | 0.809405 | 151.379 | 0.869622 | 45.3639 | 0.65296 | 207.003 | 9.37499 | 0.525091 | 171.905 | 2.83938 | 0.663851 | 56.7117 | 102.455 | 127.488 | 197.119 | 10579.12 |
| 45646.2 | 20.4609 | 0.888855 | 84.8034 | 0.778741 | 23.2471 | 0.458996 | 214.696 | 55.4944 | 0.37067 | 479.235 | 4.3677 | 0.762874 | 9.29523 | 181.524 | 478.532 | 197.4781 | 12315.51 |
| 48289.9 | 19.9947 | 0.881963 | 147.738 | 1.1848 | 90.1786 | 0.437401 | 454.814 | 43.4595 | 0.994776 | 107.041 | 45.0432 | 0.476877 | 20.3921 | 75.1973 | 75.1064 | 168.3592 | 11576.34 |
| 34149.9 | 18.6989 | 0.918824 | 49.656 | 1.51732 | 6.36951 | 0.49845 | 477.427 | 30.6898 | 0.691728 | 277.379 | 87.9985 | 0.33043 | 33.9552 | 278.065 | 196.389 | 213.2127 | 13426.32 |
| 28833.7 | 16.1661 | 0.932682 | 128.772 | 1.5516 | 48.3433 | 0.57812 | 293.981 | 16.556 | 0.750244 | 231.948 | 17.9727 | 0.709512 | 89.218 | 122.092 | 110.219 | 81.063 | 5823.39 |
| 54255.5 | 14.2022 | 0.866408 | 101.496 | 2.45582 | 29.4789 | 0.357211 | 276.346 | 76.922 | 0.404456 | 383.207 | 4.3678 | 0.50764 | 82.5407 | 100.406 | 77.9527 | 373.0219 | 22691.16 |
| 58387.5 | 19.1375 | 0.855638 | 19.9517 | 2.36117 | 41.6117 | 0.411882 | 312.251 | 78.6062 | 0.562149 | 199.432 | 48.624 | 0.454797 | 3.91995 | 213.986 | 146.202 | 282.0253 | 17201.27 |
| 74737.4 | 14.5973 | 0.813013 | 79.273 | 1.62897 | 91.5174 | 0.386007 | 340.687 | 83.8458 | 0.37093 | 503.7 | 32.1619 | 0.986376 | 136.939 | 268.003 | 414.99 | 244.7358 | 15650.99 |
| 23242.7 | 29.7136 | 0.94727 | 168.713 | 1.06459 | 25.5742 | 0.576935 | 319.678 | 24.474 | 0.998512 | 312.425 | 38.8678 | 0.408122 | 68.7967 | 155.651 | 311.705 | 114.851 | 8182.516 |
| 28645.8 | 26.3797 | 0.93318 | 56.7997 | 0.907774 | 43.1567 | 0.45493 | 360.099 | 13.6921 | 0.938454 | 251.007 | 7.48591 | 0.469701 | 73.0822 | 226.999 | 181.198 | 100.8943 | 7541.782 |
| 24137.8 | 18.045 | 0.944925 | 71.4776 | 2.02171 | 33.6172 | 0.466525 | 251.719 | 96.2775 | 0.593105 | 212.577 | 48.1117 | 0.902736 | 71.4648 | 63.9102 | 83.8016 | 82.62612 | 6053.394 |
| 53456.3 | 20.6205 | 0.868495 | 91.7281 | 2.2258 | 39.8889 | 0.420716 | 484.279 | 56.2811 | 0.349462 | 467.089 | 6.57213 | 0.817186 | 125.752 | 46.787 | 458.026 | 226.1742 | 14154.63 |
| 44752.2 | 18.9954 | 0.891185 | 27.1384 | 2.51286 | 21.6948 | 0.496821 | 96.7694 | 93.0955 | 0.604379 | 201.576 | 1.48296 | 0.475949 | 85.4573 | 77.9468 | 186.617 | 186.7817 | 11385.07 |
| 57270.8 | 17.3301 | 0.858548 | 26.4973 | 1.69153 | 12.3076 | 0.599571 | 408.829 | 38.4779 | 0.874142 | 333.832 | 8.02838 | 0.938592 | 45.4179 | 250.602 | 224.464 | 70.92419 | 4149.919 |
| 34075.1 | 29.633 | 0.919029 | 142.563 | 1.78247 | 85.022 | 0.405219 | 216.487 | 48.8733 | 0.736381 | 514.55 | 31.2897 | 0.539061 | 159.501 | 116.705 | 309.95 | 173.867 | 13169.3 |
| 46274.8 | 18.7235 | 0.887215 | 153.928 | 1.38118 | 86.4012 | 0.532732 | 229.069 | 83.5067 | 0.867177 | 391.548 | 15.738 | 0.428421 | 128.957 | 102.833 | 168.077 | 177.6414 | 11841.39 |
| 49938.6 | 23.1623 | 0.877667 | 129.313 | 3.68749 | 20.3811 | 0.355444 | 279.443 | 79.2728 | 0.310607 | 112.54 | 56.0391 | 0.876632 | 70.3221 | 207.958 | 110.036 | 278.9661 | 16911.38 |
| 33723.8 | 16.107 | 0.919934 | 153.535 | 1.97468 | 11.172 | 0.585266 | 74.09 | 39.3428 | 0.860342 | 208.853 | 74.9847 | 0.309943 | 148.69 | 64.0811 | 126.897 | 174.7678 | 11061.63 |
| 27359.3 | 13.2293 | 0.936524 | 84.8385 | 0.244743 | 9.71088 | 0.444433 | 458.985 | 43.1959 | 0.571773 | 262.067 | 18.5968 | 0.341278 | 15.3651 | 406.411 | 220.605 | 259.6422 | 17395.29 |
| 31169 | 15.6482 | 0.926594 | 165.715 | 0.119445 | 79.0723 | 0.635998 | 416.974 | 96.6217 | 0.521609 | 294.774 | 64.8391 | 0.492963 | 9.03768 | 70.3498 | 275.86 | 232.2229 | 15914.48 |
| 52016.6 | 13.7613 | 0.872244 | 79.7714 | 0.578374 | 27.6702 | 0.425058 | 262.364 | 55.8317 | 0.877456 | 202.438 | 0.963748 | 0.951398 | 28.1222 | 124.888 | 195.449 | 78.8753 | 4964.592 |
| 44469.4 | 26.4734 | 0.891928 | 159.796 | 3.13286 | 79.1557 | 0.716096 | 238.328 | 73.9242 | 0.910777 | 370.968 | 80.1821 | 0.616105 | 307.909 | 214.494 | 295.217 | 129.7745 | 8033.781 |
| 74033.9 | 13.0091 | 0.814846 | 56.734 | 2.55092 | 71.8501 | 0.313447 | 275.86 | 58.0658 | 0.966207 | 82.4544 | 94.131 | 0.493034 | 47.9431 | 259.18 | 74.0193 | 235.8559 | 14742.24 |
| 51373.8 | 20.7305 | 0.873924 | 162.406 | 0.527767 | 91.163 | 0.660463 | 202.582 | 53.3199 | 0.32834 | 307.911 | 52.5943 | 0.816094 | 32.7462 | 64.845 | 229.983 | 225.0836 | 14086.89 |
| 57448.1 | 23.2476 | 0.85809 | 161.642 | 0.260911 | 16.9803 | 0.369146 | 438.113 | 68.4407 | 0.685834 | 158.331 | 51.6472 | 0.867363 | 20.3759 | 310.549 | 117.765 | 203.4339 | 11619.72 |
| 22793.4 | 19.8195 | 0.948431 | 37.9173 | 2.10155 | 20.4318 | 0.32421 | 326.161 | 45.2582 | 0.934304 | 293.415 | 47.5331 | 0.407095 | 170.872 | 77.1643 | 192.936 | 156.721 | 11387.72 |
| 34100.4 | 18.7431 | 0.918953 | 139.424 | 1.10542 | 62.7292 | 0.537986 | 355.228 | 94.0458 | 0.998992 | 347.805 | 59.7984 | 0.712673 | 46.5311 | 267.71 | 60.8676 | 81.08338 | 5651.338 |
| 23476.5 | 13.3635 | 0.946646 | 24.584 | 1.97497 | 6.55057 | 0.329007 | 445.041 | 98.5497 | 0.579704 | 207.632 | 56.3537 | 0.336856 | 113.33 | 105.672 | 88.3499 | 301.6969 | 20465.77 |
| 56941 | 20.5698 | 0.85941 | 72.5171 | 1.99268 | 81.3242 | 0.458981 | 214.404 | 89.7297 | 0.488506 | 518.155 | 8.58366 | 0.97574 | 35.0719 | 80.82 | 509.469 | 135.6275 | 9093.617 |
| 67526.6 | 14.6246 | 0.831811 | 155.009 | 0.14856 | 41.4722 | 0.420127 | 227.061 | 88.1422 | 0.96835 | 488.521 | 36.2587 | 0.633492 | 8.63968 | 155.357 | 487.208 | 197.5116 | 11193.52 |
| 26895.9 | 15.4465 | 0.937733 | 164.654 | 1.14616 | 96.6433 | 0.366475 | 387.361 | 92.41 | 0.714615 | 321.716 | 85.8142 | 0.383024 | 55.8009 | 75.041 | 103.751 | 306.1108 | 24118.92 |
| 23829.8 | 25.3152 | 0.945734 | 92.5878 | 3.51237 | 4.7826 | 0.352285 | 138.301 | 43.1847 | 0.877564 | 110.375 | 89.0671 | 0.87189 | 56.2872 | 95.7921 | 63.7503 | 73.97945 | 5127.383 |
| 47510.4 | 25.525 | 0.883999 | 117.412 | 0.280486 | 25.6259 | 0.602731 | 162.822 | 75.9133 | 0.826062 | 177.959 | 72.7198 | 0.472362 | 22.5227 | 44.6342 | 66.2038 | 150.74 | 9040.945 |
| 47476.6 | 18.9258 | 0.884082 | 104.959 | 3.60244 | 56.8997 | 0.529809 | 145.542 | 78.5517 | 0.960619 | 342.933 | 96.0754 | 0.382725 | 284.753 | 93.3336 | 225.415 | 187.1109 | 11605.21 |
| 60550.5 | 14.1359 | 0.849997 | 104.831 | 2.60085 | 44.1142 | 0.439344 | 231.77 | 66.2144 | 0.580477 | 278.502 | 81.7303 | 0.98057 | 55.9243 | 162.017 | 241.123 | 121.8954 | 7471.398 |
| 48281.2 | 14.9792 | 0.881983 | 131.604 | 0.778719 | 20.4047 | 0.454341 | 174.036 | 26.454 | 0.935432 | 132.392 | 84.1094 | 0.400691 | 69.1965 | 94.068 | 54.8034 | 187.8845 | 11330.56 |
| 25971.1 | 19.8193 | 0.940147 | 138.541 | 0.961287 | 43.4083 | 0.338127 | 367.528 | 64.0084 | 0.345728 | 189.628 | 8.75372 | 0.920797 | 27.564 | 292.805 | 99.8461 | 228.9658 | 17099.93 |
| 21387.2 | 23.0378 | 0.9521 | 145.799 | 2.50022 | 80.0585 | 0.475026 | 331.097 | 98.2882 | 0.956638 | 343.323 | 73.367 | 0.729107 | 77.125 | 186.56 | 246.09 | 78.33666 | 6214.873 |
| 41598.1 | 18.823 | 0.899407 | 143.368 | 2.07395 | 37.4649 | 0.493321 | 416.152 | 30.006 | 0.584075 | 346.62 | 47.0866 | 0.464448 | 122.205 | 162.074 | 289.326 | 208.4333 | 13503.82 |
| 23026.7 | 19.5714 | 0.947823 | 53.3513 | 1.69504 | 19.688 | 0.381017 | 361.865 | 23.6336 | 0.439968 | 164.051 | 9.2002 | 0.728507 | 161.564 | 67.8943 | 69.5789 | 147.9286 | 10853.22 |
| 24253.2 | 13.3534 | 0.944621 | 133.093 | 3.2287 | 71.0457 | 0.428077 | 444.109 | 23.0027 | 0.487289 | 364.473 | 36.9822 | 0.841689 | 146.434 | 341.76 | 151.683 | 118.831 | 9705.417 |
| 63726.1 | 15.6202 | 0.841719 | 169.205 | 1.26474 | 62.1657 | 0.438648 | 291.023 | 56.8513 | 0.744679 | 505.696 | 60.9003 | 0.622347 | 2.11557 | 234.836 | 486.129 | 211.0931 | 12670.8 |
| 42333.3 | 22.1198 | 0.897493 | 98.1526 | 2.50208 | 15.5583 | 0.38521 | 426.361 | 11.1645 | 0.756784 | 150.54 | 62.4824 | 0.900255 | 78.9686 | 85.2018 | 116.03 | 90.66426 | 5804.246 |
| 70146 | 13.881 | 0.824982 | 94.8699 | 2.78232 | 97.0739 | 0.521763 | 208.813 | 16.653 | 0.943985 | 226.438 | 61.2259 | 0.894653 | 72.4339 | 126.514 | 207.366 | 79.29848 | 4960.012 |
| 32714.6 | 28.6784 | 0.922575 | 117.994 | 0.42919 | 62.9203 | 0.317944 | 418.585 | 26.973 | 0.999375 | 177.686 | 6.60863 | 0.683278 | 18.1073 | 301.089 | 176.226 | 127.7006 | 9649.763 |
| 38593.5 | 15.8221 | 0.907238 | 42.1376 | 0.121954 | 13.8803 | 0.393939 | 247.402 | 64.7643 | 0.634421 | 510.147 | 33.2076 | 0.443372 | 1.57948 | 217.53 | 432.471 | 217.7768 | 13764.51 |
| 32060.2 | 26.5228 | 0.924279 | 48.2072 | 1.0745 | 47.5416 | 0.419077 | 368.76 | 14.3234 | 0.471178 | 438.668 | 54.8399 | 0.709759 | 17.2885 | 65.0805 | 137.47 | 154.8002 | 11332.25 |
| 77583.7 | 14.275 | 0.805592 | 150.411 | 1.22019 | 77.2397 | 0.469429 | 286.939 | 72.8419 | 0.839467 | 195.931 | 93.7584 | 0.379631 | 58.3332 | 46.5871 | 62.288 | 306.7094 | 17710.24 |
| 30839.7 | 23.1038 | 0.927457 | 101.619 | 1.52848 | 69.9533 | 0.313588 | 365.782 | 20.6864 | 0.655458 | 226.067 | 97.8548 | 0.365435 | 93.881 | 121.852 | 79.8015 | 308.2638 | 24178.29 |
| 21801.5 | 25.9128 | 0.951022 | 149.719 | 3.52649 | 90.326 | 0.479026 | 463.098 | 82.6622 | 0.602199 | 134.476 | 86.1737 | 0.893285 | 22.4704 | 81.824 | 111.727 | 93.87644 | 7692.362 |
| 23855.1 | 15.5686 | 0.945661 | 25.9306 | 2.47045 | 1.05315 | 0.482909 | 454.115 | 78.8657 | 0.502342 | 120.23 | 86.5845 | 0.793576 | 62.5168 | 450.764 | 98.2286 | 102.9278 | 6928.023 |
| 38960.6 | 19.8764 | 0.906284 | 162.849 | 1.35925 | 91.1162 | 0.605435 | 269.171 | 85.0839 | 0.603636 | 193.661 | 33.6355 | 0.590495 | 130.064 | 185.396 | 176.523 | 153.5956 | 10502.42 |
| 22669.7 | 22.7089 | 0.948756 | 72.2946 | 2.19225 | 47.3381 | 0.382583 | 119.751 | 3.62716 | 0.786831 | 325.419 | 18.6964 | 0.309302 | 173.31 | 96.6096 | 213.647 | 201.5332 | 15984.48 |
| 64787.8 | 13.3562 | 0.83895 | 28.6233 | 3.45007 | 34.7839 | 0.64905 | 467.884 | 88.0799 | 0.818765 | 475.956 | 97.859 | 0.855365 | 139.832 | 439.414 | 324.769 | 117.3173 | 6573.651 |
| 70132.5 | 17.473 | 0.825019 | 33.0333 | 3.51076 | 62.007 | 0.449816 | 170.005 | 92.0888 | 0.858884 | 350.28 | 55.2622 | 0.664601 | 6.76848 | 101.207 | 227.018 | 135.3674 | 8207.531 |
| 39147.1 | 28.7297 | 0.905806 | 167.524 | 1.77394 | 20.3671 | 0.52865 | 449.263 | 21.7398 | 0.839854 | 480.334 | 1.78162 | 0.356514 | 28.7777 | 120.106 | 128.765 | 194.5129 | 12313.02 |
| 58329.5 | 17.5815 | 0.855788 | 100.359 | 0.16463 | 71.5964 | 0.565897 | 469.43 | 27.3063 | 0.559634 | 279.145 | 43.7354 | 0.761481 | 11.674 | 354.586 | 95.1409 | 149.4059 | 9279.029 |
| 36854.3 | 16.9267 | 0.911773 | 153.51 | 0.595705 | 85.6476 | 0.484377 | 71.1633 | 3.29626 | 0.406335 | 222.053 | 28.6905 | 0.544625 | 4.84697 | 59.2573 | 116.322 | 296.1008 | 21225.01 |
| 65066.7 | 21.6823 | 0.838228 | 90.1013 | 0.194334 | 43.0369 | 0.57014 | 497.189 | 94.6986 | 0.830372 | 500.82 | 17.7219 | 0.55734 | 18.8222 | 346.01 | 170.905 | 146.6541 | 8433.908 |
| 44778.8 | 21.6665 | 0.891117 | 141.97 | 3.72005 | 48.9212 | 0.534176 | 424.932 | 3.91619 | 0.721962 | 461.957 | 67.4915 | 0.570037 | 50.7151 | 259.059 | 190.209 | 124.7924 | 8046.489 |
| 43518.4 | 13.3894 | 0.894398 | 63.1929 | 0.761417 | 90.9592 | 0.353354 | 288.565 | 84.7292 | 0.631784 | 509.13 | 35.3332 | 0.372285 | 38.7144 | 118.759 | 241.611 | 323.8191 | 24230.95 |
| 61197.4 | 16.2657 | 0.848311 | 77.0776 | 1.88833 | 60.5718 | 0.360185 | 398.022 | 5.16501 | 0.840146 | 84.8024 | 68.7885 | 0.639347 | 112.023 | 94.2521 | 56.0388 | 154.2538 | 9970.032 |
| 44106 | 18.1626 | 0.892869 | 121.012 | 2.13999 | 18.0912 | 0.317683 | 112.77 | 4.70174 | 0.617582 | 368.138 | 79.1994 | 0.980067 | 157.786 | 103.39 | 97.3841 | 134.4597 | 8494.288 |
| 73655.3 | 17.3668 | 0.815835 | 21.4497 | 3.55589 | 65.3505 | 0.405329 | 225.317 | 34.6935 | 0.410233 | 203.773 | 86.3008 | 0.703692 | 34.7637 | 147.747 | 92.6658 | 288.7252 | 17457.31 |
| 46597.3 | 16.0234 | 0.886373 | 157.672 | 2.21685 | 10.7667 | 0.519122 | 188.33 | 91.5347 | 0.885185 | 503.846 | 81.559 | 0.8358 | 69.2706 | 175.962 | 380.505 | 88.11035 | 5302.072 |
| 37466 | 15.7258 | 0.910178 | 86.8155 | 1.64467 | 68.0689 | 0.431791 | 470.195 | 53.3742 | 0.841431 | 399.526 | 92.8276 | 0.687797 | 39.1495 | 380.795 | 109.77 | 101.2895 | 7378.189 |
| 70036.3 | 16.8118 | 0.825269 | 172.635 | 3.71719 | 39.8274 | 0.501401 | 139.861 | 55.3636 | 0.350697 | 236.162 | 31.2288 | 0.608027 | 133.121 | 112.406 | 61.7166 | 363.0074 | 20319.46 |
| 30596.2 | 22.14 | 0.928091 | 79.5989 | 3.60677 | 3.97356 | 0.396205 | 340.045 | 31.6355 | 0.630385 | 256.939 | 18.2733 | 0.672264 | 59.5171 | 245.342 | 155.859 | 119.1018 | 7858.635 |
| 76722.5 | 13.5962 | 0.807837 | 159.307 | 0.742265 | 52.6122 | 0.601036 | 423.891 | 69.3254 | 0.84619 | 160.549 | 46.5231 | 0.561603 | 46.7862 | 75.6354 | 54.8819 | 170.1339 | 9340.116 |
| 25719.8 | 20.0843 | 0.940802 | 30.5386 | 2.97231 | 18.8179 | 0.433072 | 293.863 | 47.3392 | 0.929602 | 84.0822 | 84.2858 | 0.479949 | 31.0902 | 95.2532 | 55.3279 | 107.9736 | 7536.755 |
| 29872.5 | 27.4131 | 0.929983 | 133.336 | 1.11377 | 82.6808 | 0.378196 | 368.481 | 19.1166 | 0.726403 | 229.01 | 44.2171 | 0.474059 | 68.8704 | 181.484 | 190.415 | 202.1443 | 15889.73 |
| 45182.5 | 21.8664 | 0.890065 | 142.966 | 1.69981 | 6.6647 | 0.565056 | 76.0976 | 25.7989 | 0.426032 | 174.904 | 79.4806 | 0.814663 | 96.0088 | 51.5672 | 67.9884 | 149.6534 | 8933.616 |
| 26848.7 | 14.8776 | 0.937856 | 63.7437 | 3.00749 | 87.9827 | 0.509076 | 478.477 | 62.2605 | 0.580462 | 486.592 | 98.8453 | 0.472304 | 151.831 | 415.443 | 413.837 | 193.8439 | 14534 |
| 62323.8 | 21.7655 | 0.845378 | 72.4287 | 0.488256 | 36.8828 | 0.352506 | 399.885 | 59.3466 | 0.586056 | 244.986 | 80.1931 | 0.696772 | 19.2154 | 223.624 | 114.814 | 221.967 | 13268.04 |
| 56113.6 | 20.2609 | 0.861567 | 104.42 | 1.53442 | 80.2137 | 0.516731 | 450.894 | 30.5726 | 0.334768 | 487.621 | 83.529 | 0.924898 | 90.5453 | 154.692 | 90.2965 | 187.5004 | 11826.2 |
| 36827.2 | 18.0105 | 0.911844 | 42.5176 | 1.89187 | 72.8926 | 0.386488 | 343.188 | 47.5384 | 0.923511 | 379.398 | 69.7812 | 0.434368 | 24.7645 | 289.837 | 93.0933 | 160.1215 | 11957.64 |
| 38599.6 | 22.9679 | 0.907227 | 167.557 | 0.166228 | 88.6883 | 0.429985 | 403.813 | 62.7659 | 0.541169 | 368.355 | 98.703 | 0.873653 | 11.3912 | 388.574 | 69.5376 | 202.2115 | 14078.91 |
| 21185.1 | 25.4722 | 0.952629 | 140.764 | 0.587182 | 77.2418 | 0.500247 | 99.9415 | 29.8332 | 0.425473 | 483.293 | 1.85688 | 0.476982 | 48.7838 | 54.887 | 381.89 | 244.9337 | 19568.75 |
| 20672 | 18.3167 | 0.95396 | 73.3452 | 0.257139 | 69.886 | 0.42793 | 209.348 | 20.5834 | 0.765704 | 243.586 | 59.5327 | 0.552686 | 14.9772 | 194.818 | 233.285 | 116.9193 | 9714.541 |
| 25955.7 | 15.9985 | 0.940185 | 166.468 | 0.691091 | 47.0922 | 0.30853 | 75.2932 | 92.9427 | 0.979266 | 167.815 | 42.373 | 0.622774 | 47.9386 | 54.4051 | 55.3098 | 164.6105 | 12039.98 |
| 30110.8 | 17.7996 | 0.929354 | 156.021 | 0.242359 | 9.99417 | 0.731592 | 457.209 | 41.7574 | 0.869507 | 276.82 | 5.65242 | 0.513341 | 21.8549 | 187.236 | 223.812 | 102.1212 | 6718.204 |
| 38699.1 | 23.8142 | 0.906969 | 120.073 | 1.69638 | 47.6926 | 0.39254 | 239.433 | 19.738 | 0.680547 | 114.74 | 36.0551 | 0.918977 | 87.889 | 100.947 | 83.6106 | 103.3081 | 7286.224 |
| 41925.9 | 13.3084 | 0.89855 | 26.6378 | 1.70147 | 41.7991 | 0.48157 | 373.737 | 88.105 | 0.445729 | 246.127 | 39.9757 | 0.790371 | 109.008 | 179.423 | 182.958 | 144.8515 | 9466.854 |
| 45868.9 | 15.065 | 0.888272 | 23.851 | 1.96071 | 25.1102 | 0.446977 | 352.585 | 51.4456 | 0.691146 | 346.242 | 59.7369 | 0.523189 | 92.5928 | 193.961 | 179.046 | 157.8439 | 9864.738 |
| 61500.8 | 18.391 | 0.847522 | 69.242 | 1.24028 | 81.0336 | 0.364904 | 447.536 | 62.9843 | 0.660502 | 412.136 | 88.5472 | 0.955709 | 69.913 | 310.027 | 243.187 | 139.3134 | 9334.977 |
| 51134 | 23.8392 | 0.874551 | 31.2688 | 1.34892 | 21.4289 | 0.395178 | 287.986 | 69.5615 | 0.939433 | 146.949 | 98.0803 | 0.353292 | 104.266 | 65.2965 | 44.9243 | 218.7562 | 13088.94 |
| 54027.2 | 18.2141 | 0.867005 | 110.172 | 0.89798 | 86.6836 | 0.512716 | 199.772 | 78.4996 | 0.561895 | 169.837 | 69.3746 | 0.302283 | 76.4229 | 183.599 | 98.3104 | 377.7489 | 24512.15 |
| 55349.6 | 19.9297 | 0.863558 | 117.962 | 0.701532 | 27.5968 | 0.525656 | 381.774 | 15.4447 | 0.565925 | 474.861 | 15.0746 | 0.409916 | 35.5904 | 369.924 | 113.947 | 262.3378 | 15419.79 |
| 22854.3 | 25.2691 | 0.948277 | 159.092 | 0.500803 | 88.995 | 0.359499 | 321.813 | 6.46529 | 0.485045 | 154.987 | 96.2473 | 0.643365 | 22.3745 | 260.884 | 84.4019 | 258.284 | 21049.91 |
| 32630 | 20.9009 | 0.922788 | 67.7379 | 0.478495 | 89.4776 | 0.364344 | 101.46 | 33.9788 | 0.914006 | 249.061 | 1.84825 | 0.490786 | 7.17291 | 85.5534 | 153.392 | 147.4254 | 12000.15 |
| 33698.1 | 17.6026 | 0.920001 | 65.8758 | 1.11887 | 32.0163 | 0.327128 | 488.436 | 69.5506 | 0.94773 | 411.202 | 47.3768 | 0.302904 | 44.2309 | 310.034 | 57.4797 | 246.3382 | 16942.52 |
| 40918.7 | 15.8189 | 0.901177 | 169.005 | 1.95836 | 18.268 | 0.425508 | 441.866 | 81.6096 | 0.311995 | 411.405 | 66.3133 | 0.810295 | 34.7333 | 214.944 | 97.6257 | 288.8808 | 17963.66 |
| 40829.2 | 21.4286 | 0.901414 | 118.601 | 2.77007 | 6.38395 | 0.491444 | 363.053 | 85.1222 | 0.627391 | 320.737 | 78.7044 | 0.583317 | 71.756 | 348.755 | 120.545 | 141.8734 | 8627.741 |
| 50765.4 | 13.3348 | 0.875506 | 82.9618 | 3.17249 | 68.3213 | 0.565576 | 386.733 | 48.0116 | 0.977052 | 371.045 | 77.7061 | 0.589202 | 194.431 | 362.45 | 306.733 | 116.4972 | 7324.127 |
| 71248.3 | 13.9977 | 0.822108 | 166.582 | 1.15561 | 86.5499 | 0.40843 | 167.395 | 24.4812 | 0.916128 | 449.95 | 61.3606 | 0.685323 | 6.99472 | 113.465 | 275.909 | 178.1513 | 10893.97 |
| 72278.8 | 17.882 | 0.819423 | 160.345 | 2.53347 | 82.6901 | 0.334933 | 180.358 | 50.9962 | 0.722106 | 514.003 | 87.0569 | 0.85537 | 68.1976 | 101.605 | 401.857 | 202.6912 | 12611.84 |
| 56238.8 | 14.244 | 0.861237 | 126.399 | 1.45034 | 6.57918 | 0.40457 | 351.499 | 56.9559 | 0.976711 | 266.064 | 1.00364 | 0.589217 | 98.0733 | 108.104 | 180.044 | 136.6088 | 7797.443 |
| 28873.4 | 31.9353 | 0.932593 | 110.21 | 0.820386 | 49.3216 | 0.410262 | 301.905 | 85.4494 | 0.866508 | 270.049 | 17.2718 | 0.834687 | 78.4779 | 61.2247 | 183.154 | 84.99683 | 6308.8 |
| 29350.8 | 32.2488 | 0.931349 | 151.357 | 1.94269 | 32.9666 | 0.42084 | 418.192 | 92.1632 | 0.780677 | 461.865 | 74.4234 | 0.755909 | 117.949 | 195.726 | 136.885 | 111.5859 | 7752.936 |
| 32928.3 | 13.8697 | 0.922006 | 73.6599 | 1.89131 | 74.4033 | 0.385819 | 213.216 | 35.0958 | 0.700695 | 405.954 | 88.5207 | 0.462722 | 19.7369 | 115.73 | 196.051 | 185.7331 | 14340.51 |
| 56534.4 | 16.6168 | 0.860468 | 46.91 | 0.431293 | 11.3659 | 0.486391 | 446.477 | 74.972 | 0.645698 | 146.29 | 43.7311 | 0.559679 | 22.3712 | 421.633 | 96.396 | 161.8177 | 9233.619 |
| 24547.8 | 23.4358 | 0.94386 | 90.8012 | 2.92965 | 3.47668 | 0.437022 | 276.091 | 21.104 | 0.429279 | 386.224 | 42.5643 | 0.853029 | 166.298 | 187.166 | 248.061 | 114.6599 | 7891.996 |
| 76115.2 | 14.4378 | 0.80942 | 40.4499 | 0.520979 | 63.6168 | 0.451657 | 387.277 | 42.4821 | 0.896422 | 493.094 | 15.8774 | 0.726098 | 24.292 | 345.93 | 218.185 | 115.3968 | 6953.689 |
| 28470.8 | 25.1332 | 0.933635 | 135.769 | 1.71877 | 10.5181 | 0.483916 | 77.6734 | 12.2074 | 0.498452 | 189.928 | 90.6518 | 0.819201 | 97.8528 | 50.3803 | 172.403 | 118.1547 | 7960.218 |
| 76310.6 | 13.4016 | 0.808911 | 110.804 | 2.44044 | 22.4746 | 0.432738 | 437.441 | 7.49447 | 0.76571 | 110.851 | 6.24668 | 0.903601 | 163.392 | 135.415 | 45.1823 | 106.2346 | 5891.949 |
| 59952.7 | 16.3909 | 0.851556 | 68.0545 | 0.671776 | 64.8849 | 0.459248 | 358.649 | 50.9637 | 0.896825 | 431.613 | 99.2576 | 0.607248 | 49.9575 | 70.3588 | 340.627 | 126.0033 | 7994.859 |
| 25249.5 | 18.598 | 0.942027 | 31.4143 | 2.15618 | 21.3259 | 0.328165 | 144.989 | 71.702 | 0.400273 | 466.531 | 58.768 | 0.450979 | 63.9225 | 108.744 | 342.886 | 330.7896 | 23527.18 |
| 40275.4 | 20.2145 | 0.902856 | 145.808 | 1.85012 | 94.2388 | 0.532659 | 478.246 | 1.91069 | 0.713075 | 94.4638 | 39.7324 | 0.437909 | 69.1034 | 142.629 | 63.5917 | 171.559 | 12340.54 |
| 76998.3 | 16.2042 | 0.807119 | 24.5028 | 0.844223 | 27.6033 | 0.516326 | 252.678 | 58.1349 | 0.464476 | 295.644 | 45.4176 | 0.918066 | 31.0668 | 218.369 | 263.826 | 165.9539 | 8951.304 |
| 61672.7 | 13.6762 | 0.847071 | 168.748 | 1.02907 | 84.7725 | 0.446115 | 95.5121 | 71.4085 | 0.869109 | 259.39 | 74.6157 | 0.341159 | 32.6644 | 74.2322 | 135.851 | 335.9872 | 20773.95 |
| 72326.8 | 15.3567 | 0.819297 | 149.44 | 3.76839 | 43.5013 | 0.556474 | 139.068 | 63.5446 | 0.358458 | 230.57 | 56.3454 | 0.594509 | 105.754 | 122.991 | 156.208 | 340.2365 | 18624.94 |
| 28263.4 | 28.6476 | 0.934179 | 167.787 | 1.98606 | 81.0422 | 0.44776 | 204.96 | 87.6471 | 0.780794 | 255.241 | 65.2327 | 0.669839 | 0.825186 | 105.198 | 58.9205 | 128.2476 | 9700.451 |
| 22445.2 | 32.0545 | 0.949352 | 91.6922 | 2.53403 | 56.5198 | 0.483266 | 335.272 | 88.2667 | 0.997518 | 450.922 | 72.8805 | 0.688087 | 22.7801 | 85.4989 | 165.471 | 69.27919 | 5247.121 |
| 41442.4 | 25.657 | 0.899819 | 168.82 | 0.440748 | 3.11973 | 0.301591 | 494.778 | 33.7515 | 0.866062 | 268.183 | 17.95 | 0.963938 | 36.225 | 260.961 | 170.989 | 166.1746 | 10108.45 |
| 31628.2 | 24.8074 | 0.925403 | 156.082 | 3.56068 | 76.4483 | 0.418639 | 285.29 | 13.1524 | 0.310881 | 215.729 | 64.2618 | 0.745509 | 81.622 | 131.756 | 206.312 | 260.483 | 19864.29 |
| 37378.8 | 29.0437 | 0.910416 | 111.553 | 1.37139 | 98.0969 | 0.411302 | 425.5 | 56.5519 | 0.451013 | 276.966 | 5.76448 | 0.613969 | 48.8395 | 139.489 | 179.499 | 234.4097 | 18103.89 |
| 60248.3 | 22.8698 | 0.85079 | 125.36 | 1.30103 | 11.6117 | 0.568291 | 203.227 | 34.6989 | 0.680604 | 283.622 | 8.38834 | 0.711763 | 35.7356 | 68.9106 | 259.719 | 118.1209 | 6666.424 |
| 41925.2 | 20.2969 | 0.898556 | 28.7297 | 3.62928 | 55.3244 | 0.493229 | 362.6 | 1.1868 | 0.554929 | 281.161 | 34.2005 | 0.468035 | 146.436 | 305.699 | 184.586 | 186.1077 | 12386.3 |
| 36236.8 | 13.0796 | 0.913381 | 121.878 | 1.58728 | 88.6551 | 0.415761 | 141.573 | 54.3847 | 0.50296 | 379.47 | 98.4734 | 0.797215 | 146.894 | 70.0635 | 339.72 | 161.7504 | 12219.71 |
| 35844.4 | 23.3703 | 0.914411 | 151.583 | 3.77026 | 96.1086 | 0.588897 | 269.307 | 8.07553 | 0.414486 | 316.672 | 12.1568 | 0.899789 | 125.248 | 239.627 | 204.805 | 142.4118 | 10173.46 |
| 25559.2 | 28.9128 | 0.941229 | 169.302 | 0.406118 | 15.0785 | 0.767908 | 465.236 | 15.4581 | 0.962164 | 385.309 | 55.3153 | 0.490516 | 20.6724 | 139.79 | 190.612 | 95.7552 | 6521.543 |
| 19208.7 | 28.9462 | 0.957785 | 164.245 | 0.147095 | 29.1214 | 0.47916 | 301.341 | 68.0081 | 0.820999 | 118.598 | 34.3504 | 0.456229 | 5.3905 | 236.767 | 79.3688 | 171.9015 | 12533.83 |
| 32259 | 30.737 | 0.923765 | 83.9122 | 2.02573 | 79.3956 | 0.446304 | 234.373 | 82.9447 | 0.389709 | 411.427 | 76.6197 | 0.515126 | 130.074 | 133.137 | 287.129 | 263.6591 | 19969.81 |
| 33734.1 | 15.5469 | 0.919906 | 88.3293 | 0.973104 | 66.3493 | 0.585119 | 234.693 | 72.5692 | 0.762727 | 510.674 | 81.3447 | 0.977054 | 38.6836 | 218.968 | 184.318 | 74.32313 | 5132.47 |
| 43430.6 | 14.5617 | 0.894628 | 26.3136 | 2.54426 | 42.5579 | 0.523761 | 240.665 | 83.6824 | 0.652776 | 372.958 | 1.51565 | 0.37806 | 100.935 | 224.948 | 296.933 | 276.4689 | 17379.42 |
| 27535.7 | 25.6848 | 0.936073 | 35.8957 | 2.68075 | 62.1371 | 0.459501 | 486.874 | 71.3754 | 0.904634 | 472.699 | 23.4841 | 0.672856 | 174.917 | 223.019 | 471.308 | 78.78584 | 6041.532 |
| 21438.5 | 24.7407 | 0.951967 | 140.611 | 1.35567 | 22.5062 | 0.611532 | 356.292 | 42.157 | 0.824212 | 502.624 | 30.8983 | 0.885112 | 132.286 | 330.189 | 388.886 | 54.02174 | 3965.764 |
| 35073.6 | 19.3212 | 0.916417 | 134.135 | 0.179638 | 69.2296 | 0.648615 | 360.802 | 85.5188 | 0.809557 | 378.711 | 68.3333 | 0.704413 | 15.2633 | 238.477 | 240.789 | 94.32349 | 6375.187 |
| 68530.9 | 15.042 | 0.829193 | 62.7188 | 1.51022 | 89.1568 | 0.355209 | 141.713 | 55.4232 | 0.768256 | 430.721 | 98.3829 | 0.914485 | 126.453 | 95.1135 | 91.2552 | 137.5616 | 9093.017 |
| 61312.5 | 21.9124 | 0.848015 | 28.2231 | 0.527168 | 10.4148 | 0.312119 | 88.2942 | 46.3577 | 0.73469 | 496.53 | 29.5043 | 0.845475 | 4.90486 | 84.1698 | 177.653 | 150.1376 | 8516.72 |
| 33432.7 | 18.4659 | 0.920694 | 132.087 | 2.78802 | 85.9435 | 0.49949 | 490.984 | 21.3425 | 0.561536 | 415.276 | 73.0544 | 0.745015 | 100.224 | 143.275 | 254.83 | 117.1577 | 8845.817 |
| 63022 | 21.2059 | 0.843557 | 125.897 | 0.588219 | 2.42309 | 0.33166 | 214.247 | 19.0085 | 0.824147 | 288.283 | 10.5812 | 0.823294 | 7.18042 | 57.342 | 258.189 | 159.1547 | 8721.454 |
| 39379.8 | 17.6921 | 0.90519 | 150.273 | 1.24214 | 41.8965 | 0.477085 | 100.424 | 52.3249 | 0.839023 | 186.643 | 69.6031 | 0.852243 | 53.8324 | 76.2913 | 156.072 | 91.62101 | 6114.641 |
| 28677 | 25.3743 | 0.933098 | 79.4851 | 3.11971 | 72.6272 | 0.410638 | 52.2538 | 81.4029 | 0.356443 | 438.738 | 87.2552 | 0.815432 | 45.281 | 47.5307 | 76.702 | 187.6518 | 14675.78 |
| 51739.4 | 20.9209 | 0.872971 | 171.268 | 1.03562 | 66.0473 | 0.727845 | 166.71 | 19.634 | 0.737877 | 442.494 | 99.9524 | 0.45798 | 60.8099 | 122.869 | 221.249 | 198.6772 | 11769.38 |
| 40302.2 | 25.9622 | 0.902791 | 146.619 | 1.08972 | 16.2114 | 0.412048 | 218.936 | 52.3586 | 0.545162 | 469.84 | 24.7324 | 0.49589 | 67.229 | 203.833 | 436.545 | 268.6515 | 16769.41 |
| 41888.5 | 18.1691 | 0.89865 | 119.878 | 0.793837 | 79.256 | 0.358387 | 363.526 | 0.786657 | 0.87755 | 215.162 | 99.0517 | 0.596078 | 18.6797 | 314.503 | 150.124 | 158.7233 | 11545.85 |
| 53760.5 | 23.257 | 0.867703 | 49.1339 | 2.54101 | 80.0873 | 0.439062 | 198.922 | 8.43171 | 0.845131 | 387.92 | 88.3949 | 0.386104 | 137.214 | 138.588 | 81.0633 | 200.7635 | 13593.48 |
| 74816.3 | 17.5803 | 0.812808 | 31.0099 | 1.90887 | 37.4213 | 0.349468 | 257.384 | 16.3286 | 0.687858 | 431.733 | 7.73484 | 0.537906 | 116.386 | 241.608 | 212.42 | 253.5358 | 14507.21 |
| 57004.9 | 19.2504 | 0.859243 | 121.402 | 1.89082 | 21.616 | 0.404924 | 412.951 | 47.9585 | 0.722232 | 311.769 | 12.3338 | 0.966293 | 144.65 | 389.52 | 261.463 | 105.6997 | 6319.854 |
| 21531 | 31.5434 | 0.951734 | 45.9149 | 1.34395 | 25.6735 | 0.450854 | 421.183 | 86.4461 | 0.967831 | 361.054 | 86.475 | 0.849577 | 53.1178 | 219.619 | 139.77 | 59.64693 | 4348.336 |
| 38750 | 20.0198 | 0.906833 | 42.3546 | 1.2581 | 80.9977 | 0.318542 | 206.233 | 2.28396 | 0.995974 | 404.169 | 60.4864 | 0.731131 | 60.6078 | 92.5538 | 269.952 | 105.4945 | 8297.474 |
| 32374.2 | 28.9939 | 0.923463 | 144.696 | 0.392725 | 94.0146 | 0.37652 | 73.5145 | 39.5274 | 0.452518 | 319.776 | 12.5698 | 0.76234 | 21.9841 | 64.9963 | 276.658 | 241.7549 | 18586.03 |
| 40719.5 | 22.0259 | 0.9017 | 135.768 | 0.446325 | 95.5867 | 0.445356 | 410.392 | 85.4725 | 0.480045 | 418.682 | 50.8066 | 0.729706 | 32.9413 | 213.495 | 131.124 | 215.8868 | 15442.32 |
| 29512.9 | 24.7687 | 0.930918 | 73.3819 | 0.158001 | 1.66715 | 0.538643 | 174.692 | 48.6849 | 0.979945 | 302.392 | 55.2283 | 0.726744 | 4.28395 | 102.121 | 195.142 | 64.28532 | 4266.126 |
| 38758.1 | 13.0534 | 0.906808 | 80.9694 | 0.469677 | 84.821 | 0.538357 | 279.081 | 17.2394 | 0.836976 | 392.036 | 3.15013 | 0.582217 | 43.7184 | 244.956 | 290.795 | 100.1174 | 7156.531 |
| 68203.1 | 14.8434 | 0.830047 | 159.747 | 0.225519 | 21.6874 | 0.584083 | 452.888 | 28.6142 | 0.737113 | 377.064 | 9.16468 | 0.796485 | 20.1015 | 391.894 | 346.803 | 137.5242 | 7564.271 |
| 21811.9 | 18.1535 | 0.950989 | 132.717 | 0.216773 | 24.2715 | 0.681377 | 91.8881 | 80.1649 | 0.776556 | 454.412 | 41.0915 | 0.927083 | 13.6609 | 80.8818 | 101.854 | 59.37038 | 4223.47 |
| 47284.7 | 20.5009 | 0.884584 | 57.5489 | 0.287751 | 61.7715 | 0.372478 | 293.018 | 77.0828 | 0.702348 | 270.765 | 59.3254 | 0.812422 | 4.64407 | 163.883 | 168.064 | 133.6582 | 9176.841 |
| 33617.1 | 27.0185 | 0.92022 | 85.7418 | 1.97167 | 31.7828 | 0.365874 | 298.269 | 91.1201 | 0.784592 | 269.58 | 12.4863 | 0.836802 | 52.1248 | 218.808 | 262.916 | 95.55137 | 6702.988 |
| 25025.9 | 31.4327 | 0.942623 | 154.568 | 1.35567 | 6.49115 | 0.594025 | 245.091 | 71.0289 | 0.345604 | 164.513 | 43.1903 | 0.511548 | 122.701 | 123.683 | 128.247 | 238.7811 | 15996.98 |
| 69502.5 | 17.3254 | 0.826661 | 117.947 | 2.27386 | 44.4928 | 0.414206 | 369.953 | 85.6647 | 0.436102 | 394.309 | 15.2994 | 0.714834 | 55.7621 | 61.9402 | 310.26 | 259.8222 | 15176.42 |
| 30113.6 | 27.3632 | 0.929354 | 152.302 | 0.581016 | 20.5927 | 0.300008 | 249.129 | 76.2363 | 0.97713 | 465.361 | 41.9538 | 0.431106 | 21.1015 | 75.1303 | 243.658 | 239.8143 | 16093.02 |
| 66344.6 | 15.9243 | 0.834893 | 123.634 | 2.6189 | 92.1352 | 0.457841 | 184.625 | 82.0042 | 0.340864 | 227.49 | 37.5405 | 0.7867 | 118.856 | 85.1106 | 70.194 | 273.8105 | 17559.66 |
| 24644.2 | 29.729 | 0.943616 | 141.573 | 2.51514 | 63.6994 | 0.394226 | 440.383 | 94.2053 | 0.810121 | 149.577 | 58.5874 | 0.704317 | 45.9611 | 271.675 | 49.4999 | 110.6162 | 8593.347 |
| 43464.9 | 27.4394 | 0.894548 | 172.317 | 1.87678 | 42.1997 | 0.668207 | 329.455 | 77.5094 | 0.883081 | 449.161 | 36.5487 | 0.474181 | 62.3334 | 127.663 | 392.409 | 138.6487 | 8512.687 |
| 26787.5 | 27.6754 | 0.938026 | 89.4124 | 1.39721 | 2.19202 | 0.381634 | 231.158 | 64.2514 | 0.487634 | 478.551 | 79.3728 | 0.416365 | 17.8381 | 153.7 | 304.158 | 257.9563 | 16939.73 |
| 35579.6 | 22.9491 | 0.9151 | 108.224 | 3.48986 | 42.0688 | 0.374622 | 154.31 | 85.9731 | 0.758514 | 466.574 | 96.3883 | 0.534277 | 17.111 | 103.171 | 51.54 | 162.8119 | 11277.16 |
| 29293.7 | 26.6963 | 0.931491 | 151.005 | 0.341814 | 10.9842 | 0.331796 | 67.849 | 78.0062 | 0.819516 | 496.853 | 93.4957 | 0.638174 | 16.258 | 53.8067 | 79.1737 | 179.9441 | 11850.32 |
| 23094.5 | 32.1227 | 0.947659 | 85.6849 | 0.717833 | 14.7677 | 0.511577 | 129.401 | 23.4979 | 0.675403 | 175.596 | 25.1368 | 0.515072 | 54.4087 | 80.2182 | 151.325 | 109.1492 | 7765.057 |
| 66617.1 | 20.7853 | 0.834185 | 149.852 | 0.504657 | 22.2982 | 0.547292 | 171.792 | 8.47543 | 0.95631 | 485.172 | 41.8851 | 0.606412 | 46.2722 | 133.313 | 119.131 | 132.6019 | 7392.102 |
| 26751.9 | 23.501 | 0.938115 | 147.111 | 1.39266 | 72.3657 | 0.530758 | 89.4489 | 85.5819 | 0.74666 | 155.364 | 26.0788 | 0.905888 | 84.4661 | 70.15 | 69.2974 | 74.60213 | 5671.425 |
| 68178 | 20.3188 | 0.830115 | 119.916 | 0.477767 | 35.1116 | 0.455416 | 136.372 | 30.7499 | 0.791599 | 485.585 | 15.1071 | 0.405371 | 11.4697 | 79.8151 | 95.7949 | 264.6851 | 14962.64 |
| 58951.3 | 17.4009 | 0.854167 | 28.112 | 0.409752 | 60.3341 | 0.374914 | 354.288 | 79.8926 | 0.927328 | 286.984 | 39.398 | 0.725212 | 10.0134 | 264.9 | 100.711 | 122.6779 | 7961.014 |
| 76959.6 | 15.6449 | 0.80722 | 169.569 | 1.53262 | 79.5141 | 0.443273 | 485.743 | 36.7738 | 0.397449 | 323.436 | 4.28825 | 0.825416 | 115.724 | 282.894 | 264.286 | 316.7539 | 18475.39 |
| 56998.3 | 13.5864 | 0.859257 | 44.0229 | 3.68599 | 68.4597 | 0.314451 | 472.168 | 64.5201 | 0.752506 | 213.756 | 1.67054 | 0.807617 | 150.049 | 278.228 | 159.549 | 153.5136 | 10434.2 |
| 21777.3 | 23.5635 | 0.951083 | 40.6742 | 1.55493 | 9.71012 | 0.390293 | 387.82 | 28.5128 | 0.307174 | 210.389 | 73.6329 | 0.757891 | 153.001 | 80.6065 | 182.05 | 198.3506 | 14039.23 |
| 25176.1 | 32.7268 | 0.942233 | 147.267 | 2.42227 | 76.2739 | 0.378081 | 339.666 | 15.778 | 0.982984 | 359.645 | 27.2765 | 0.351389 | 59.2417 | 296.719 | 147.636 | 184.2446 | 14937.08 |
| 57003.1 | 17.9699 | 0.859247 | 71.3351 | 0.155651 | 1.38475 | 0.442381 | 296.387 | 24.394 | 0.476241 | 397.201 | 10.8591 | 0.804538 | 1.48664 | 56.8938 | 396.964 | 179.7641 | 10044.41 |
| 37423.9 | 29.9626 | 0.910299 | 87.1142 | 1.37593 | 3.27464 | 0.34504 | 213.051 | 29.9193 | 0.612351 | 433.513 | 5.93249 | 0.885542 | 20.7244 | 185.229 | 317.394 | 117.2792 | 7421.3 |
| 23964.2 | 13.0216 | 0.945375 | 155.29 | 1.16045 | 62.2641 | 0.536516 | 361.138 | 37.8661 | 0.778816 | 351.442 | 77.7523 | 0.827404 | 71.0857 | 250.702 | 248.795 | 77.25612 | 5867.917 |
| 30013.8 | 30.25 | 0.929618 | 75.4053 | 1.42207 | 46.6053 | 0.398168 | 402.387 | 53.8885 | 0.41557 | 186.421 | 13.1568 | 0.952926 | 56.7472 | 395.259 | 140.923 | 134.8663 | 10068.43 |
| 26092.9 | 26.5772 | 0.939835 | 60.9022 | 0.980109 | 99.849 | 0.336462 | 491.209 | 54.3874 | 0.514152 | 464.648 | 57.6838 | 0.967702 | 96.4691 | 126.883 | 198.136 | 133.2027 | 11676.02 |
| 52998.9 | 15.5594 | 0.869684 | 36.0209 | 0.712129 | 79.9178 | 0.46927 | 302.024 | 55.9942 | 0.314274 | 314.766 | 61.9336 | 0.63863 | 45.0086 | 129.024 | 138.023 | 297.2383 | 19893.17 |
| 76970.2 | 16.6836 | 0.807193 | 70.9331 | 0.869844 | 83.2703 | 0.461192 | 98.9449 | 66.5049 | 0.589232 | 474.62 | 46.1596 | 0.480537 | 53.0877 | 71.8127 | 86.064 | 271.7879 | 16465.02 |
| 61076.2 | 13.0884 | 0.848626 | 105.999 | 1.48452 | 78.7525 | 0.515084 | 311.592 | 99.7258 | 0.526222 | 231.768 | 90.9979 | 0.875797 | 40.0992 | 270.596 | 159.856 | 139.6528 | 8597.995 |
| 20579.6 | 27.5706 | 0.95421 | 66.9969 | 0.425753 | 36.969 | 0.375904 | 145.866 | 46.4402 | 0.935869 | 435.49 | 31.0121 | 0.86213 | 19.0134 | 129.489 | 398.773 | 64.45196 | 5133.001 |
| 54017.8 | 20.9504 | 0.867031 | 157.171 | 3.38453 | 8.3547 | 0.543915 | 84.3529 | 73.2877 | 0.323793 | 143.725 | 69.0429 | 0.74138 | 86.7878 | 67.8191 | 50.805 | 242.7931 | 13780.95 |
| 37428.8 | 21.7053 | 0.910279 | 40.2597 | 0.703486 | 33.1071 | 0.328687 | 273.711 | 16.949 | 0.594656 | 473.811 | 33.1963 | 0.677814 | 60.9562 | 218.282 | 358.999 | 170.4414 | 11762.27 |
| 53226.3 | 18.7058 | 0.869093 | 88.5924 | 3.5626 | 73.063 | 0.398893 | 390.79 | 31.2381 | 0.374252 | 504.134 | 40.4127 | 0.572611 | 30.1643 | 265.671 | 106.689 | 327.0268 | 22205.17 |
| 46064.1 | 17.889 | 0.887764 | 39.5236 | 2.44229 | 98.3632 | 0.427718 | 92.9628 | 34.7303 | 0.556422 | 468.061 | 71.7701 | 0.665643 | 142.443 | 61.0149 | 378.839 | 170.2984 | 12544.32 |
| 78472 | 15.9559 | 0.803277 | 169.209 | 0.36081 | 2.58079 | 0.792529 | 340.243 | 51.1983 | 0.913268 | 416.758 | 36.277 | 0.698976 | 32.3634 | 313.018 | 337.284 | 119.5677 | 6204.028 |
| 59580.7 | 15.8001 | 0.852526 | 74.4653 | 2.68483 | 78.7259 | 0.430512 | 201.94 | 85.1187 | 0.422069 | 512.705 | 72.0623 | 0.935608 | 128.74 | 171.421 | 155.659 | 180.6709 | 11865.5 |
| 46418.4 | 26.5066 | 0.886847 | 56.9219 | 3.55326 | 3.76599 | 0.462976 | 399.575 | 68.8103 | 0.961018 | 273.97 | 0.749331 | 0.545243 | 165.282 | 135.729 | 190.294 | 108.9389 | 6492.344 |
| 75317 | 15.7828 | 0.811502 | 86.047 | 1.73733 | 50.6911 | 0.345395 | 443.962 | 0.019941 | 0.459988 | 212.256 | 65.1044 | 0.609361 | 161.29 | 125.909 | 142.069 | 343.2641 | 20177.7 |
| 48697.5 | 22.3568 | 0.880902 | 92.7337 | 1.5353 | 86.1146 | 0.479169 | 296.488 | 10.3224 | 0.500093 | 435.98 | 86.9341 | 0.557799 | 52.2111 | 235.509 | 357.14 | 202.3084 | 14016.5 |
| 76577.2 | 16.9252 | 0.808217 | 80.0836 | 1.43812 | 50.0502 | 0.516665 | 289.076 | 16.5606 | 0.960796 | 309.063 | 89.7209 | 0.729824 | 138.76 | 282.827 | 76.5365 | 100.5038 | 5673.28 |
| 19110.4 | 31.7538 | 0.958045 | 60.004 | 2.73366 | 62.7797 | 0.374937 | 310.029 | 5.19879 | 0.582882 | 423.565 | 69.6278 | 0.632708 | 119.945 | 304.147 | 271.237 | 135.5243 | 11546.32 |
| 60656.3 | 22.9547 | 0.849726 | 143.186 | 1.335 | 14.4527 | 0.48601 | 351.219 | 60.1094 | 0.39118 | 396.155 | 99.0881 | 0.782405 | 101.857 | 311.63 | 225.932 | 243.9109 | 13630.18 |
| 55150.7 | 23.5897 | 0.86408 | 143.739 | 1.24188 | 4.9251 | 0.548953 | 228.002 | 75.8702 | 0.8783 | 77.2229 | 14.1892 | 0.792815 | 59.252 | 189.315 | 58.1205 | 91.40393 | 5266.315 |
| 48995.5 | 26.011 | 0.880128 | 27.993 | 1.83559 | 20.3441 | 0.484363 | 463.628 | 68.0837 | 0.87319 | 81.0715 | 91.8345 | 0.596017 | 96.3445 | 112.716 | 51.0319 | 113.0928 | 6832.63 |
| 27341.7 | 31.7092 | 0.936586 | 155.496 | 1.54686 | 48.2367 | 0.350755 | 427.754 | 19.9602 | 0.791465 | 487.288 | 72.9592 | 0.312013 | 92.5951 | 113.743 | 411.73 | 305.283 | 22496.95 |
| 68847.6 | 20.125 | 0.82837 | 35.6525 | 2.84563 | 66.9213 | 0.608457 | 397.453 | 85.3214 | 0.901286 | 455.893 | 15.9784 | 0.562367 | 212.224 | 239.115 | 303.804 | 171.3088 | 9776.109 |
| 62991.3 | 20.3803 | 0.843637 | 156.577 | 2.38397 | 53.3021 | 0.442215 | 349.551 | 94.7187 | 0.740438 | 374.493 | 82.227 | 0.842488 | 62.0576 | 91.2142 | 338.201 | 141.8608 | 8536.648 |
| 73672 | 18.4028 | 0.815792 | 163.968 | 2.86348 | 59.9077 | 0.439372 | 402.581 | 78.3419 | 0.710451 | 374.077 | 74.8055 | 0.724501 | 159.67 | 132.488 | 130.549 | 187.3347 | 10869.41 |
| 32424.4 | 30.6222 | 0.923334 | 47.4073 | 0.766104 | 73.2587 | 0.397468 | 141.25 | 31.1952 | 0.611308 | 404.091 | 4.02283 | 0.339998 | 20.5752 | 89.6185 | 46.6373 | 276.8498 | 21388.9 |
| 48448.2 | 16.3835 | 0.881548 | 154.179 | 2.69467 | 71.1751 | 0.365158 | 441.576 | 44.2957 | 0.971468 | 415.769 | 46.3846 | 0.541344 | 86.6904 | 258.871 | 262.594 | 167.2967 | 11436.99 |
| 39647.2 | 28.2992 | 0.904501 | 31.4112 | 3.08623 | 3.92127 | 0.503548 | 415.59 | 33.4487 | 0.508053 | 465.306 | 43.8046 | 0.644654 | 127.981 | 314.809 | 191.586 | 144.7865 | 8895.974 |
| 67888.8 | 19.9122 | 0.830869 | 138.147 | 0.66581 | 91.2089 | 0.527223 | 356.323 | 93.9314 | 0.807886 | 482.688 | 34.82 | 0.601775 | 47.1411 | 234.66 | 414.024 | 169.2137 | 10292.93 |
| 57595.1 | 19.1727 | 0.857704 | 92.2003 | 1.57423 | 75.8393 | 0.384748 | 479.124 | 36.1522 | 0.395344 | 98.8214 | 43.3749 | 0.786934 | 33.3232 | 209.83 | 76.2192 | 245.2864 | 16488.46 |
| 46726.8 | 23.5214 | 0.88604 | 149.056 | 1.89549 | 61.1555 | 0.497791 | 490.172 | 54.7018 | 0.658163 | 206.68 | 14.2728 | 0.373867 | 90.9989 | 287.974 | 119.616 | 259.6404 | 16901.76 |
| 25489.9 | 19.9708 | 0.941402 | 123.065 | 1.0309 | 96.6564 | 0.553207 | 355.42 | 2.39819 | 0.704242 | 188.771 | 4.09057 | 0.795218 | 65.3088 | 229.772 | 83.6245 | 71.0947 | 5827.131 |
| 58652.5 | 15.3122 | 0.854945 | 30.9753 | 1.08811 | 76.161 | 0.30626 | 314.974 | 22.2936 | 0.844386 | 251.628 | 76.1687 | 0.42761 | 63.4464 | 231.807 | 190.388 | 272.0776 | 18531.24 |
| 29254.7 | 22.5842 | 0.931589 | 70.7346 | 1.75354 | 72.3344 | 0.409252 | 404.249 | 84.8021 | 0.64843 | 490.62 | 87.1568 | 0.409759 | 99.8079 | 102.789 | 185.474 | 214.1127 | 16423.41 |
| 34556.9 | 22.7005 | 0.917766 | 51.1068 | 0.220289 | 1.38592 | 0.37138 | 157.76 | 40.932 | 0.455839 | 75.8669 | 15.7909 | 0.557057 | 4.38633 | 106.797 | 60.0176 | 231.1211 | 14496.98 |
| 27377.7 | 30.1963 | 0.93649 | 113.239 | 1.42225 | 46.6087 | 0.46151 | 319.08 | 51.6627 | 0.401564 | 264.463 | 64.3103 | 0.869513 | 43.7576 | 78.6866 | 176.057 | 140.7958 | 10380.73 |
| 50246.3 | 13.9446 | 0.876859 | 57.2042 | 2.07243 | 66.8711 | 0.475741 | 254.639 | 65.8758 | 0.452404 | 369.776 | 34.0801 | 0.922619 | 118.161 | 79.8959 | 59.0101 | 135.4301 | 8994.426 |
| 52286.6 | 14.8616 | 0.871541 | 119.238 | 0.58235 | 95.6918 | 0.332716 | 216.885 | 43.5338 | 0.911585 | 432.874 | 58.1863 | 0.349663 | 31.9481 | 192.29 | 115.115 | 328.3898 | 22978.3 |
| 45829.7 | 18.1321 | 0.888375 | 84.7508 | 0.80186 | 45.4431 | 0.520307 | 405.593 | 99.4628 | 0.908669 | 176.548 | 54.8448 | 0.499194 | 69.7076 | 79.3983 | 153.191 | 130.6827 | 8164.283 |
| 74100.4 | 14.1105 | 0.814673 | 102.718 | 2.01751 | 9.17969 | 0.480471 | 193.392 | 16.1027 | 0.405701 | 355.847 | 32.95 | 0.965037 | 25.5452 | 184.908 | 45.8281 | 167.1316 | 8884.827 |
| 26616.8 | 15.0044 | 0.938461 | 26.0033 | 2.70209 | 83.8202 | 0.465956 | 350.769 | 32.2389 | 0.761703 | 293.745 | 11.2845 | 0.659249 | 154.676 | 182.844 | 75.4904 | 87.2367 | 7128.061 |
| 63127.8 | 22.301 | 0.843282 | 168.006 | 1.96269 | 4.55704 | 0.528844 | 446.178 | 33.2439 | 0.613102 | 152.469 | 57.76 | 0.521508 | 146.833 | 367.471 | 127.176 | 229.788 | 12477.58 |
| 55086.6 | 23.5529 | 0.864247 | 118.166 | 2.53295 | 36.3936 | 0.34805 | 370.738 | 53.4991 | 0.8218 | 330.726 | 34.7219 | 0.535617 | 59.5736 | 192.475 | 288.185 | 192.6808 | 11951.92 |
| 55424.7 | 16.2134 | 0.863361 | 85.4109 | 0.196522 | 5.64673 | 0.523495 | 214.952 | 87.3987 | 0.992766 | 244.804 | 64.7348 | 0.593528 | 13.1446 | 161.664 | 99.4687 | 113.8164 | 6468.845 |
| 28148.1 | 25.0095 | 0.934476 | 154.134 | 1.06448 | 22.4414 | 0.6155 | 61.5822 | 94.0804 | 0.565501 | 179.085 | 59.8442 | 0.934619 | 64.6903 | 52.2533 | 67.3449 | 87.75927 | 5935.595 |
| 78153.2 | 15.579 | 0.804108 | 126.438 | 1.78317 | 35.5358 | 0.457583 | 487.28 | 55.5408 | 0.548029 | 320.521 | 32.8766 | 0.78526 | 66.8251 | 121.516 | 262.961 | 191.2642 | 10544.79 |
| 53459.1 | 23.1859 | 0.868489 | 151.046 | 1.55098 | 20.5995 | 0.370078 | 495.483 | 56.4349 | 0.59469 | 209.061 | 44.5356 | 0.742041 | 9.08722 | 198.432 | 182.701 | 208.9285 | 12363.17 |
| 45021.2 | 26.762 | 0.89049 | 89.4235 | 1.35884 | 82.8932 | 0.409956 | 499.637 | 34.5947 | 0.578764 | 332.296 | 61.0336 | 0.749632 | 42.5119 | 304.838 | 327.762 | 150.5489 | 10946.17 |
| 49989.3 | 14.2639 | 0.877529 | 147.613 | 1.72461 | 70.9394 | 0.407278 | 287.056 | 6.94114 | 0.953524 | 142.233 | 79.8323 | 0.638652 | 104.292 | 198.3 | 69.1926 | 131.8238 | 8891.44 |
| 39899.3 | 28.9897 | 0.903845 | 51.2823 | 3.79533 | 77.3816 | 0.322471 | 55.7258 | 64.4641 | 0.828692 | 412.834 | 51.1256 | 0.847235 | 14.0389 | 45.4736 | 290.781 | 116.0133 | 8800.095 |
| 51340.4 | 15.0106 | 0.874008 | 115.567 | 0.652221 | 59.2544 | 0.491764 | 78.0685 | 20.8411 | 0.73818 | 465.598 | 11.5307 | 0.484208 | 64.0956 | 57.6784 | 422.657 | 177.1796 | 11418.04 |
| 30841.9 | 27.8771 | 0.927456 | 77.1273 | 0.179911 | 92.5026 | 0.37126 | 492.209 | 97.7105 | 0.976458 | 312.483 | 74.5913 | 0.576554 | 16.8408 | 84.8537 | 74.2176 | 138.609 | 10787.68 |
| 39522.1 | 16.602 | 0.904818 | 71.7936 | 0.472375 | 3.80892 | 0.41192 | 397.222 | 18.4918 | 0.767038 | 67.653 | 49.2888 | 0.548562 | 29.5145 | 216.503 | 49.5958 | 134.9157 | 8350.098 |
| 46700 | 18.4974 | 0.886107 | 172.015 | 1.81955 | 65.6045 | 0.492026 | 392.676 | 13.3249 | 0.564361 | 158.609 | 31.8356 | 0.79208 | 49.61 | 321.18 | 155.894 | 154.5839 | 10216.59 |
| 33923.5 | 25.9833 | 0.919421 | 129.981 | 0.367245 | 16.8908 | 0.361871 | 235.741 | 19.019 | 0.731328 | 445.968 | 79.0494 | 0.696563 | 16.6378 | 73.1985 | 271.052 | 155.8708 | 10250.49 |
| 65133.6 | 18.1154 | 0.838051 | 65.8158 | 3.15614 | 0.334525 | 0.489574 | 291.852 | 32.8378 | 0.349704 | 434.931 | 10.4517 | 0.941551 | 82.5448 | 218.567 | 108.356 | 179.7499 | 9670.699 |
| 37735.2 | 22.3093 | 0.90948 | 167.04 | 0.733233 | 19.0422 | 0.461356 | 219.156 | 12.3624 | 0.506111 | 364.219 | 97.4735 | 0.784369 | 37.9178 | 136.29 | 143.278 | 181.293 | 11531.71 |
| 52105.8 | 18.6117 | 0.872014 | 166.178 | 3.62455 | 82.7378 | 0.402103 | 447.581 | 96.7014 | 0.803344 | 500.569 | 0.693012 | 0.421988 | 119.465 | 323.86 | 315.744 | 258.1098 | 17280.88 |
| 34787.8 | 24.9169 | 0.917166 | 123.86 | 0.99229 | 16.3243 | 0.597935 | 284.715 | 12.9096 | 0.929913 | 438.499 | 94.8281 | 0.78459 | 61.5682 | 94.8402 | 124.388 | 66.36413 | 4335.2 |
| 67768.2 | 18.337 | 0.831183 | 75.7843 | 3.16643 | 90.4829 | 0.480265 | 201.729 | 30.4181 | 0.91263 | 324.995 | 86.4754 | 0.944351 | 109.101 | 97.4708 | 158.14 | 81.8102 | 5272.765 |
| 51919.9 | 18.8322 | 0.872499 | 47.065 | 2.71932 | 78.6478 | 0.471285 | 498.237 | 20.9347 | 0.5016 | 242.874 | 97.8576 | 0.790079 | 120.048 | 173.314 | 229.718 | 150.4108 | 10132.46 |
| 51084.4 | 15.4192 | 0.874675 | 117.702 | 2.94693 | 92.2492 | 0.370592 | 427.828 | 71.0806 | 0.616658 | 332.716 | 23.2573 | 0.52679 | 7.9436 | 349.95 | 299.809 | 239.9132 | 17265.43 |
| 21043.6 | 29.8764 | 0.953003 | 87.4854 | 1.06352 | 78.7244 | 0.341875 | 398.977 | 80.5226 | 0.515789 | 444.811 | 89.4925 | 0.994864 | 64.9265 | 196.842 | 360.002 | 123.3735 | 10558.09 |
| 28893.2 | 28.5079 | 0.932537 | 64.9928 | 2.03857 | 74.8055 | 0.491207 | 344.188 | 81.3491 | 0.510295 | 395.233 | 85.7732 | 0.347978 | 32.4237 | 325.62 | 78.6262 | 258.8832 | 19047.3 |
| 23591.8 | 29.4118 | 0.946359 | 83.2864 | 2.70019 | 56.3593 | 0.41367 | 391.299 | 89.9754 | 0.607309 | 503.119 | 25.7739 | 0.868911 | 50.0397 | 216.382 | 247.289 | 94.94209 | 7535.036 |
| 30703.2 | 21.3944 | 0.927812 | 104.012 | 1.25292 | 28.8757 | 0.35776 | 237.643 | 81.5993 | 0.550955 | 400.768 | 73.774 | 0.75694 | 84.1109 | 129.154 | 293.678 | 156.1584 | 10866.7 |
| 31926.1 | 28.6935 | 0.924631 | 150.417 | 1.21288 | 35.8615 | 0.329358 | 412.058 | 82.6258 | 0.859312 | 455.604 | 66.3466 | 0.67901 | 12.0328 | 59.7921 | 430.891 | 152.5399 | 10566.01 |
| 30956.7 | 13.1146 | 0.927146 | 73.0882 | 2.35017 | 87.0928 | 0.486084 | 265.828 | 39.4179 | 0.777893 | 434.639 | 91.8806 | 0.521146 | 34.7101 | 233.592 | 364.812 | 117.5917 | 8823.205 |
| 46618.2 | 13.1504 | 0.886317 | 115.511 | 0.610822 | 83.7208 | 0.334592 | 459.414 | 6.9617 | 0.709098 | 483.057 | 2.85688 | 0.524957 | 55.0438 | 62.626 | 87.8239 | 246.9275 | 17757.23 |
| 63196.2 | 17.9831 | 0.843102 | 149.456 | 0.794716 | 18.062 | 0.50112 | 453.825 | 25.5683 | 0.786598 | 250.25 | 38.2678 | 0.324188 | 61.8652 | 384.986 | 213.576 | 306.6634 | 16986.88 |
| 40101.8 | 22.7318 | 0.903311 | 110.144 | 0.949408 | 31.7528 | 0.520848 | 105.434 | 29.0854 | 0.988333 | 429.591 | 14.8702 | 0.398954 | 8.97893 | 63.096 | 271.175 | 128.8179 | 8401.945 |
| 27247.2 | 31.8145 | 0.936832 | 49.4645 | 1.10347 | 62.4806 | 0.441373 | 383.935 | 25.441 | 0.987679 | 262.814 | 48.0193 | 0.681795 | 95.862 | 221.795 | 55.4249 | 71.86015 | 5668.746 |
| 57374.8 | 18.1099 | 0.858278 | 167.2 | 1.8979 | 16.2287 | 0.498783 | 464.037 | 69.4842 | 0.597177 | 471.819 | 7.20804 | 0.930572 | 161.036 | 146.903 | 222.877 | 131.9712 | 7607.181 |
| 31745.1 | 13.3277 | 0.925091 | 101.596 | 2.13603 | 53.9259 | 0.426451 | 398.034 | 45.675 | 0.365725 | 73.0169 | 70.8922 | 0.520979 | 71.8778 | 245.374 | 72.7669 | 268.2016 | 19652.24 |
| 54166.4 | 20.8081 | 0.866643 | 171.212 | 1.82529 | 67.5371 | 0.438073 | 270.516 | 4.44202 | 0.334581 | 189.467 | 9.49502 | 0.796143 | 146.721 | 206.995 | 78.1281 | 315.2186 | 20055.65 |
| 53506.9 | 13.7936 | 0.868359 | 92.1602 | 1.5628 | 16.1625 | 0.461028 | 94.864 | 56.5491 | 0.61983 | 399.948 | 92.9252 | 0.614526 | 143.968 | 64.2625 | 204.508 | 158.0789 | 9263.469 |
| 44614.7 | 24.3809 | 0.891547 | 140.91 | 3.69441 | 45.7692 | 0.480848 | 283.154 | 61.026 | 0.331086 | 497.916 | 64.1588 | 0.622887 | 42.0275 | 231.85 | 371.06 | 274.5074 | 17827.13 |
| 36002.7 | 13.7953 | 0.913992 | 171.5 | 0.354526 | 17.7982 | 0.585072 | 495.273 | 75.2599 | 0.346321 | 441.608 | 71.3042 | 0.764626 | 4.91892 | 400.058 | 345.475 | 230.1 | 14518.47 |
| 55703.5 | 15.622 | 0.862634 | 74.8148 | 0.790933 | 38.4369 | 0.357821 | 394.728 | 96.9993 | 0.625152 | 431.99 | 90.4136 | 0.376966 | 22.5254 | 374.031 | 236.137 | 348.4774 | 21422.95 |
| 51590.6 | 13.7629 | 0.873355 | 35.8446 | 3.42296 | 90.8532 | 0.443386 | 96.0274 | 44.1266 | 0.361404 | 350.372 | 73.6497 | 0.924925 | 28.42 | 55.3634 | 230.359 | 189.1938 | 13296.9 |
| 29925.5 | 21.62 | 0.929839 | 162.902 | 0.767237 | 91.5474 | 0.588632 | 186.564 | 17.315 | 0.901127 | 276.938 | 30.1585 | 0.448954 | 70.9852 | 87.1439 | 58.7212 | 126.2411 | 9372.496 |
| 40294.8 | 16.7151 | 0.902804 | 48.3074 | 1.99615 | 76.4581 | 0.516727 | 469.281 | 19.4452 | 0.619514 | 282.186 | 16.1691 | 0.489299 | 136.092 | 467.698 | 257.9 | 183.7795 | 12690.27 |
| 46934.3 | 22.958 | 0.885499 | 126.572 | 0.227715 | 7.01307 | 0.377311 | 286.841 | 16.3705 | 0.81311 | 393.943 | 96.4154 | 0.443643 | 17.9453 | 160.11 | 147.377 | 250.4503 | 14754.31 |
| 23768.9 | 13.5958 | 0.945884 | 163.648 | 1.24589 | 12.7877 | 0.56205 | 194.387 | 72.8386 | 0.837103 | 173.228 | 94.5929 | 0.527783 | 2.51709 | 104.147 | 78.5922 | 113.28 | 7698.958 |
| 28060.2 | 32.2132 | 0.934713 | 102.808 | 1.02799 | 35.8779 | 0.313371 | 433.505 | 20.8828 | 0.828492 | 310.009 | 63.3665 | 0.420547 | 83.5216 | 283.85 | 266.347 | 206.4541 | 15094.5 |
| 59083.1 | 13.8168 | 0.853822 | 171.884 | 3.48704 | 47.9556 | 0.501806 | 152.274 | 2.59762 | 0.699883 | 196.952 | 76.7759 | 0.791786 | 32.1042 | 108.249 | 180.841 | 127.1335 | 7725.771 |
| 78994.1 | 14.4308 | 0.801915 | 56.2886 | 0.657261 | 83.6306 | 0.472918 | 148.71 | 98.9364 | 0.435175 | 351.22 | 26.7546 | 0.91402 | 41.2051 | 108.775 | 279.442 | 189.5488 | 11426.13 |
| 32488.5 | 18.9742 | 0.923156 | 28.673 | 2.47789 | 66.3505 | 0.314611 | 136.809 | 92.2391 | 0.693755 | 411.957 | 16.5955 | 0.645175 | 63.7438 | 51.0275 | 155.838 | 166.0403 | 12831.57 |
| 64561 | 21.641 | 0.839546 | 54.395 | 3.63492 | 27.9454 | 0.37583 | 472.872 | 86.7449 | 0.722253 | 378.035 | 91.7242 | 0.88992 | 1.64937 | 262.829 | 305.169 | 134.3655 | 7833.594 |
| 37735.5 | 29.3617 | 0.909486 | 105.232 | 0.174369 | 91.2208 | 0.562767 | 274.644 | 40.6996 | 0.738691 | 236.911 | 10.2235 | 0.586114 | 9.28743 | 94.4035 | 191.103 | 125.1771 | 8973.622 |
| 44829.8 | 27.3966 | 0.890989 | 133.505 | 0.790636 | 30.6271 | 0.393955 | 359.355 | 58.999 | 0.529589 | 169.866 | 14.3048 | 0.528955 | 71.1766 | 103.517 | 71.0201 | 284.0247 | 17871.29 |
| 51796.1 | 23.4765 | 0.872825 | 147.445 | 3.48441 | 67.8275 | 0.408324 | 395.259 | 14.2744 | 0.836751 | 106.73 | 40.0033 | 0.473482 | 57.5086 | 249.287 | 102.841 | 188.5421 | 12608.19 |
| 29197.4 | 13.8191 | 0.931732 | 58.8557 | 3.43638 | 16.3205 | 0.633991 | 491.725 | 13.5089 | 0.69878 | 384.918 | 23.2256 | 0.713901 | 186.991 | 350.454 | 363.166 | 118.9447 | 7982.154 |
| 36322.7 | 19.7453 | 0.913161 | 105.904 | 3.16652 | 88.5833 | 0.468182 | 179.005 | 95.8229 | 0.594271 | 424.769 | 62.7947 | 0.906479 | 152.628 | 96.4286 | 373.271 | 100.386 | 7486.058 |
| 40248.6 | 25.734 | 0.902931 | 157.737 | 0.898511 | 83.7626 | 0.551968 | 212.102 | 97.727 | 0.571132 | 266.794 | 88.9217 | 0.588162 | 47.346 | 180.419 | 130.552 | 191.4767 | 12951.7 |
| 61439.7 | 20.0594 | 0.847682 | 104.037 | 0.605015 | 84.9712 | 0.388495 | 137.583 | 22.812 | 0.904769 | 337.455 | 67.1523 | 0.760318 | 58.6181 | 107.977 | 180.016 | 132.3612 | 8760.811 |
| 32295.9 | 21.7097 | 0.92366 | 84.6115 | 1.84 | 16.3905 | 0.506359 | 214.047 | 73.5627 | 0.785536 | 324.286 | 33.5019 | 0.38475 | 77.101 | 183.619 | 132.111 | 167.7911 | 10839.82 |
| 50838.3 | 18.0147 | 0.875318 | 101.291 | 1.86323 | 57.3362 | 0.482048 | 189.347 | 73.4976 | 0.733363 | 342.651 | 60.072 | 0.519626 | 11.4927 | 169.956 | 133.909 | 156.1127 | 10069.73 |
| 33033.5 | 29.3057 | 0.921744 | 124.368 | 0.153048 | 11.2251 | 0.472829 | 116.441 | 26.8875 | 0.846201 | 445.785 | 9.20214 | 0.730937 | 9.15517 | 57.1602 | 312.234 | 99.5013 | 6578.807 |
| 41386.3 | 14.4813 | 0.899957 | 133.869 | 1.84703 | 6.94721 | 0.45088 | 314.529 | 56.9614 | 0.797594 | 503.145 | 16.403 | 0.967218 | 20.191 | 237.885 | 122.13 | 75.95889 | 4777.491 |
| 47185 | 22.7366 | 0.884845 | 61.1112 | 0.79593 | 40.0978 | 0.427406 | 444.404 | 95.6199 | 0.417884 | 221.094 | 75.2992 | 0.76495 | 76.145 | 105.122 | 121.122 | 196.737 | 12623.07 |
| 21328.1 | 26.2171 | 0.952257 | 87.4193 | 0.110669 | 74.4089 | 0.435189 | 245.736 | 65.736 | 0.463986 | 263.078 | 19.5768 | 0.967054 | 3.98363 | 47.7019 | 249.944 | 122.7954 | 10048.28 |
| 77601.2 | 13.0012 | 0.805546 | 75.2599 | 1.66173 | 75.8736 | 0.425996 | 450.788 | 68.2091 | 0.418858 | 258.943 | 0.86116 | 0.683286 | 154.179 | 135.635 | 157.577 | 284.0567 | 17167.84 |
| 35803.9 | 21.1746 | 0.914514 | 172.243 | 1.50385 | 45.0639 | 0.503171 | 317.048 | 18.5261 | 0.698498 | 270.216 | 90.026 | 0.473469 | 67.7631 | 195.978 | 53.4597 | 188.8596 | 12676.79 |
| 32878.2 | 26.5639 | 0.922146 | 77.1872 | 3.44388 | 50.5085 | 0.320315 | 199.408 | 58.6001 | 0.856899 | 387.477 | 64.0099 | 0.878972 | 105.985 | 133.794 | 243.702 | 97.36496 | 7249.269 |
| 31148.7 | 25.54 | 0.926654 | 55.9539 | 1.27551 | 52.5006 | 0.37947 | 115.269 | 81.2591 | 0.822253 | 375.94 | 27.9734 | 0.342741 | 68.1431 | 108.66 | 209.039 | 217.7365 | 15935.3 |
| 26339.8 | 17.3692 | 0.939184 | 52.4207 | 3.63678 | 88.4417 | 0.683074 | 493.726 | 92.4138 | 0.799469 | 492.459 | 99.9257 | 0.86608 | 51.1407 | 487.098 | 335.927 | 94.38706 | 6590.353 |
| 77629 | 15.1341 | 0.805474 | 154.218 | 2.12998 | 45.5844 | 0.551801 | 271.323 | 42.5795 | 0.464849 | 402.082 | 3.04151 | 0.958242 | 42.3159 | 85.9774 | 170.78 | 164.2818 | 9092.52 |
| 62485.7 | 21.0939 | 0.844956 | 122.545 | 2.20711 | 22.9763 | 0.524669 | 438.439 | 20.4382 | 0.98386 | 432.765 | 90.3592 | 0.849691 | 28.4215 | 184.836 | 118.346 | 75.22838 | 4377.207 |
| 74056.8 | 15.249 | 0.814787 | 139.901 | 1.37728 | 51.9613 | 0.638551 | 472.758 | 63.9349 | 0.727455 | 194.571 | 54.8717 | 0.84546 | 128.809 | 247.85 | 140.945 | 119.8726 | 6611.181 |
| 41372.9 | 17.7858 | 0.899994 | 62.5387 | 2.11097 | 20.5532 | 0.427013 | 232.774 | 22.9862 | 0.774103 | 444.927 | 68.2866 | 0.977777 | 155.047 | 164.55 | 429.146 | 73.97172 | 4831.218 |
| 34197.9 | 18.3048 | 0.918699 | 79.2223 | 1.87227 | 33.875 | 0.34223 | 382.669 | 32.9377 | 0.997407 | 414.216 | 71.5953 | 0.477317 | 72.2723 | 142.538 | 383.664 | 139.4957 | 9752.839 |
| 30921 | 14.9908 | 0.92724 | 170.917 | 3.58413 | 79.6092 | 0.518212 | 394.483 | 34.0115 | 0.596194 | 156.337 | 67.2689 | 0.952802 | 39.3502 | 275.453 | 114.771 | 92.06309 | 6927.53 |
| 22164.8 | 16.1946 | 0.950067 | 123.673 | 2.22855 | 14.4634 | 0.382583 | 322.634 | 86.0767 | 0.361076 | 448.997 | 75.9363 | 0.506718 | 94.083 | 100.131 | 337.614 | 287.1391 | 20246 |
| 46381.9 | 22.4136 | 0.886939 | 167.409 | 1.72292 | 85.0689 | 0.397588 | 219.164 | 77.6802 | 0.435186 | 142.436 | 81.3228 | 0.848838 | 29.6953 | 199.773 | 81.0141 | 243.5897 | 16730 |
| 53243.4 | 18.9537 | 0.869049 | 109.624 | 3.05452 | 87.6036 | 0.400109 | 456.447 | 33.5019 | 0.916822 | 350.112 | 11.691 | 0.751719 | 137.083 | 159.238 | 330.903 | 102.5709 | 7330.952 |
| 43355.9 | 25.0572 | 0.89483 | 116.288 | 2.78681 | 98.9782 | 0.425423 | 352.034 | 99.7426 | 0.925532 | 193.044 | 39.7456 | 0.492925 | 57.7232 | 344.882 | 92.5871 | 149.8586 | 11015.62 |
| 33297.1 | 19.8771 | 0.921048 | 20.124 | 3.61007 | 66.9047 | 0.344047 | 227.598 | 20.4715 | 0.815666 | 461.456 | 82.7198 | 0.837664 | 135.07 | 136.547 | 60.3568 | 98.969 | 7661.754 |
| 54691.6 | 17.0401 | 0.865272 | 144.079 | 2.55154 | 39.4122 | 0.32713 | 181.085 | 61.2873 | 0.853704 | 363.259 | 63.6382 | 0.388117 | 59.1219 | 84.5447 | 221.524 | 300.5033 | 18540.92 |
| 37286.4 | 21.2576 | 0.910649 | 163.862 | 0.777182 | 30.6938 | 0.509351 | 420.234 | 13.9348 | 0.743519 | 410.023 | 5.16904 | 0.582844 | 40.8074 | 141.013 | 151.324 | 142.5175 | 9376.431 |
| 44726.6 | 16.8432 | 0.89125 | 115.678 | 1.4385 | 9.02444 | 0.419293 | 218.754 | 79.7677 | 0.811354 | 466.606 | 70.6997 | 0.464628 | 20.11 | 70.3757 | 420.491 | 178.2657 | 10681.85 |
| 42917.6 | 21.9526 | 0.89597 | 124.455 | 1.54531 | 4.6855 | 0.48649 | 423.405 | 57.0531 | 0.895934 | 295.695 | 98.8458 | 0.728898 | 50.4705 | 50.7535 | 241.975 | 91.72995 | 5568.633 |
| 47168 | 21.4452 | 0.884889 | 76.7463 | 3.75897 | 38.605 | 0.434031 | 111.629 | 25.1333 | 0.522684 | 239.96 | 70.7878 | 0.748236 | 135.168 | 76.2579 | 158.935 | 152.1444 | 9824.683 |
| 23185 | 13.8124 | 0.947407 | 67.3282 | 3.48919 | 44.4477 | 0.306009 | 303.962 | 41.0968 | 0.907464 | 504.136 | 44.1005 | 0.454357 | 57.7572 | 90.2488 | 206.155 | 157.4412 | 12384.44 |
| 59627.1 | 13.2236 | 0.852404 | 59.3338 | 1.8183 | 54.4422 | 0.47114 | 126.118 | 95.8595 | 0.590339 | 204.606 | 65.549 | 0.675914 | 19.625 | 109.006 | 49.3013 | 163.2878 | 10078.58 |
| 71806.5 | 13.3639 | 0.820653 | 169.527 | 2.49695 | 41.7746 | 0.565381 | 391.501 | 63.5813 | 0.966198 | 313.665 | 5.68684 | 0.837463 | 32.9596 | 194.823 | 283.529 | 90.96448 | 5185.869 |
| 36133.2 | 29.7874 | 0.913664 | 66.5262 | 0.655192 | 57.221 | 0.302179 | 349.645 | 97.7006 | 0.446267 | 306.452 | 98.5515 | 0.705212 | 26.1599 | 105.081 | 203.692 | 259.5252 | 18971.57 |
| 21343.4 | 21.9881 | 0.952213 | 28.7778 | 1.23037 | 0.896194 | 0.386675 | 85.864 | 40.0969 | 0.550851 | 123.159 | 8.60912 | 0.540361 | 35.8222 | 60.5831 | 75.6062 | 152.5968 | 10596.57 |
| 28173.6 | 17.3445 | 0.934404 | 100.626 | 0.165754 | 60.867 | 0.389181 | 479.458 | 11.0698 | 0.612245 | 395.033 | 84.0843 | 0.625109 | 3.00588 | 187.427 | 390.651 | 175.6527 | 13277.38 |
| 45246.4 | 22.9466 | 0.889899 | 52.7064 | 3.74601 | 14.0853 | 0.560591 | 356.607 | 42.0535 | 0.605043 | 452.583 | 79.8318 | 0.985841 | 257.193 | 220.211 | 324.172 | 97.37858 | 5908.113 |
| 53740.1 | 18.7354 | 0.867754 | 104.204 | 2.47105 | 87.3434 | 0.468589 | 111.573 | 10.4936 | 0.764242 | 489.027 | 29.3477 | 0.758659 | 173.454 | 71.1148 | 46.8855 | 101.2931 | 7012.573 |
| 21966.5 | 29.9513 | 0.950597 | 60.8451 | 0.126968 | 93.7865 | 0.452256 | 197.226 | 62.016 | 0.523987 | 495.878 | 38.1644 | 0.53041 | 8.72724 | 124.132 | 472.048 | 182.1592 | 15302.77 |
| 26385.4 | 25.9537 | 0.939072 | 165.289 | 1.40541 | 67.3998 | 0.56075 | 435.224 | 51.2814 | 0.916301 | 165.343 | 82.5767 | 0.887991 | 38.2844 | 133.125 | 162.527 | 65.47815 | 4863.37 |
| 27951.2 | 22.8868 | 0.934987 | 120.613 | 0.876419 | 40.1819 | 0.509218 | 464.898 | 43.5127 | 0.716066 | 319.341 | 78.3884 | 0.946701 | 80.2364 | 327.27 | 188.76 | 72.73306 | 5246.564 |
| 51565.8 | 23.0062 | 0.873425 | 117.82 | 2.44156 | 18.2289 | 0.472594 | 226.072 | 62.8508 | 0.974441 | 270.443 | 86.115 | 0.88777 | 167.453 | 63.1284 | 266.188 | 74.25458 | 4496.652 |
| 37519.8 | 18.9077 | 0.910039 | 78.9183 | 1.14577 | 14.7729 | 0.387619 | 351.293 | 26.4628 | 0.719843 | 395.934 | 7.19767 | 0.94904 | 94.9855 | 298.659 | 186.305 | 81.52305 | 5420.3 |
| 27504.1 | 25.4958 | 0.936155 | 144.246 | 0.975916 | 62.1119 | 0.33929 | 342.48 | 92.4692 | 0.809597 | 219.867 | 98.3639 | 0.896321 | 62.6929 | 133.852 | 213.736 | 117.9064 | 8878.814 |
| 57872.4 | 18.3955 | 0.856981 | 126.236 | 2.5287 | 51.5699 | 0.429816 | 206.486 | 69.5259 | 0.912835 | 232.638 | 39.9012 | 0.798061 | 34.0803 | 60.2118 | 65.3923 | 102.1967 | 6455.358 |
| 47584.2 | 18.868 | 0.883802 | 108.342 | 0.212123 | 2.05792 | 0.398762 | 470.21 | 86.6756 | 0.786354 | 83.3748 | 3.91241 | 0.868123 | 10.8322 | 432.286 | 69.0945 | 118.4032 | 6987.307 |
| 22930.9 | 27.723 | 0.94808 | 39.5867 | 0.554502 | 38.4928 | 0.314023 | 382.1 | 52.2192 | 0.85224 | 169.378 | 15.0682 | 0.522032 | 2.61423 | 127.035 | 168.407 | 141.8544 | 11019.17 |
| 67288.1 | 15.2441 | 0.832433 | 32.7532 | 1.05385 | 76.2339 | 0.360019 | 61.9722 | 17.4929 | 0.940642 | 264.369 | 67.8099 | 0.641934 | 38.7591 | 47.8322 | 116.222 | 148.7555 | 9693.903 |
| 70996.6 | 17.5366 | 0.822766 | 112.044 | 0.330175 | 74.0241 | 0.354614 | 416.179 | 46.4545 | 0.813566 | 346.672 | 6.58614 | 0.48541 | 8.5126 | 309.451 | 138.578 | 294.3259 | 17987.02 |
| 32638.8 | 23.9518 | 0.922768 | 171.754 | 1.58599 | 47.611 | 0.536857 | 408.722 | 51.7938 | 0.648611 | 245.103 | 7.76387 | 0.471738 | 17.7389 | 189.037 | 51.8539 | 182.8115 | 12551.75 |
| 48295.8 | 15.3317 | 0.881945 | 171.817 | 1.81275 | 37.014 | 0.620352 | 244.909 | 95.7686 | 0.670675 | 459.539 | 98.1148 | 0.340331 | 129.01 | 234.428 | 385.553 | 262.645 | 15663.37 |
| 35896.7 | 15.7089 | 0.914269 | 16.1332 | 0.944959 | 32.754 | 0.43919 | 162.461 | 45.6 | 0.453179 | 260.344 | 20.4777 | 0.332499 | 85.5423 | 62.6269 | 148.269 | 337.3174 | 22690.86 |
| 21517 | 30.6583 | 0.95177 | 168.299 | 1.78093 | 68.0201 | 0.558588 | 427.127 | 10.0045 | 0.339302 | 237.872 | 92.0215 | 0.634087 | 61.5907 | 387.179 | 156.083 | 209.7104 | 16146.69 |
| 42781.2 | 23.3572 | 0.896326 | 144.907 | 1.51001 | 53.4123 | 0.337192 | 208.837 | 46.3686 | 0.668063 | 336.689 | 45.7839 | 0.7862 | 83.2142 | 198.404 | 133.219 | 172.4737 | 11765.24 |
| 53594.5 | 15.3048 | 0.868131 | 65.6242 | 2.26226 | 41.3892 | 0.358372 | 51.4431 | 76.7871 | 0.796672 | 83.7879 | 0.994025 | 0.30647 | 60.2017 | 44.5937 | 82.2766 | 327.18 | 20545.46 |
| 67849.6 | 18.2987 | 0.83097 | 130.868 | 1.24211 | 45.5635 | 0.533209 | 282.076 | 35.3543 | 0.696708 | 168.975 | 76.7129 | 0.729514 | 103.66 | 89.6368 | 114.594 | 138.4088 | 7991.125 |
| 47148.3 | 26.9951 | 0.884945 | 103.207 | 1.01369 | 63.4151 | 0.464105 | 413.307 | 98.2766 | 0.551537 | 156.465 | 44.2032 | 0.613615 | 70.9847 | 79.6891 | 133.901 | 190.6233 | 12638.89 |
| 78252 | 16.4958 | 0.803851 | 146.154 | 2.81892 | 20.1308 | 0.338601 | 479.499 | 11.4138 | 0.79415 | 432.172 | 53.3442 | 0.811709 | 59.0995 | 478.117 | 106.05 | 173.4033 | 9366.597 |
| 39657.8 | 22.2994 | 0.904468 | 102.714 | 0.987574 | 87.933 | 0.453743 | 383.127 | 13.8843 | 0.648293 | 428.188 | 48.0689 | 0.477947 | 44.0502 | 86.6366 | 86.3014 | 188.0672 | 13931.14 |
| 36092.8 | 24.9034 | 0.913764 | 119.914 | 2.65464 | 36.9233 | 0.336136 | 450.02 | 99.7225 | 0.95653 | 371.757 | 21.9582 | 0.928463 | 97.9949 | 283.59 | 104.267 | 90.39321 | 6308.312 |
| 24144.1 | 25.7037 | 0.944915 | 56.6306 | 3.51116 | 12.871 | 0.566244 | 263.148 | 62.3876 | 0.827421 | 435.407 | 13.0483 | 0.938369 | 313.988 | 248.257 | 160.296 | 54.49295 | 3864.979 |
| 23298.4 | 13.4763 | 0.947111 | 71.2586 | 2.98826 | 79.4054 | 0.384751 | 228.542 | 86.0294 | 0.712772 | 113.958 | 63.9871 | 0.87258 | 91.1595 | 62.1046 | 58.8599 | 91.11623 | 7599.065 |
| 32303 | 19.027 | 0.923639 | 21.9301 | 0.373374 | 78.1373 | 0.318465 | 396.22 | 40.8809 | 0.472715 | 348.698 | 86.544 | 0.57572 | 32.5602 | 168.46 | 279.154 | 266.6507 | 21257.02 |
| 24213.7 | 33.4203 | 0.944743 | 169.658 | 0.941374 | 78.3963 | 0.513634 | 482.273 | 38.1301 | 0.989353 | 423.595 | 14.3166 | 0.319092 | 39.1438 | 302.26 | 290.609 | 182.1671 | 13899.22 |
| 22840.3 | 28.625 | 0.948317 | 132.037 | 3.13984 | 99.3451 | 0.503246 | 367.476 | 35.4498 | 0.603209 | 133.727 | 1.32515 | 0.629066 | 99.7696 | 214.781 | 107.861 | 109.8817 | 9240.531 |
| 46638 | 14.6551 | 0.886266 | 169.35 | 1.16499 | 84.8954 | 0.533842 | 450.88 | 95.1374 | 0.930163 | 355.239 | 78.4413 | 0.747611 | 31.3646 | 374.304 | 302.061 | 107.4684 | 7098.948 |
| 32242.3 | 27.4434 | 0.923805 | 43.7675 | 0.32208 | 76.6613 | 0.475614 | 312.175 | 36.5017 | 0.595817 | 493.918 | 51.1226 | 0.856393 | 15.5248 | 154.923 | 372.501 | 93.74663 | 7208.477 |
| 21970.6 | 26.3539 | 0.950582 | 42.0378 | 1.11023 | 64.17 | 0.441032 | 238.957 | 5.99641 | 0.915809 | 277.089 | 72.1251 | 0.923854 | 54.7103 | 44.3228 | 234.208 | 52.90995 | 4438.246 |
| 66118.1 | 14.816 | 0.835483 | 124.149 | 2.27072 | 98.65 | 0.30025 | 233.473 | 55.5965 | 0.64338 | 338.386 | 61.8664 | 0.972535 | 49.7271 | 148.089 | 308.238 | 187.1068 | 12823.44 |
| 67482.6 | 19.7132 | 0.831928 | 103.369 | 3.06086 | 83.3192 | 0.332752 | 283.184 | 75.0722 | 0.68287 | 354.287 | 29.6546 | 0.691986 | 166.113 | 115.24 | 112.994 | 211.7742 | 13910.05 |
| 64547.6 | 14.2761 | 0.839577 | 37.1131 | 2.61098 | 67.6055 | 0.452848 | 148.348 | 70.2503 | 0.809338 | 322.839 | 53.5462 | 0.587276 | 115.865 | 80.365 | 182.319 | 149.694 | 9344.554 |
| 29062.3 | 26.578 | 0.932094 | 172.397 | 1.91138 | 3.56257 | 0.333254 | 337.73 | 13.2286 | 0.87198 | 213.62 | 84.5482 | 0.430252 | 158.409 | 139.202 | 133.813 | 217.129 | 14201.06 |
| 42915.5 | 25.1898 | 0.895978 | 105.723 | 1.09379 | 73.5048 | 0.490263 | 441.084 | 63.0614 | 0.674619 | 214.385 | 42.4848 | 0.388678 | 104.211 | 332.08 | 100.517 | 220.2516 | 15109.77 |
| 22035.5 | 26.6811 | 0.950413 | 118.761 | 1.98077 | 32.5835 | 0.476313 | 223.675 | 69.5047 | 0.441225 | 142.082 | 53.7617 | 0.544651 | 127.207 | 153.183 | 113.821 | 179.7083 | 13206.5 |
| 48447.5 | 15.1096 | 0.881549 | 42.5048 | 1.03165 | 35.0194 | 0.407222 | 473.833 | 75.9039 | 0.888449 | 306.388 | 95.785 | 0.432597 | 1.8627 | 43.2661 | 212.29 | 178.8812 | 11265.07 |
| 50249.9 | 24.5793 | 0.876857 | 43.9472 | 3.46427 | 36.9034 | 0.469772 | 311.874 | 98.5242 | 0.821802 | 118.707 | 22.2179 | 0.895156 | 163.932 | 94.8504 | 65.0576 | 81.83913 | 5186.909 |
| 23829.5 | 27.6719 | 0.945737 | 45.8304 | 2.46038 | 6.49045 | 0.419355 | 498.748 | 78.4701 | 0.566537 | 254.551 | 82.2153 | 0.319683 | 171.574 | 303.861 | 52.7781 | 260.5956 | 17580.77 |
| 20640.5 | 28.336 | 0.954052 | 138.238 | 1.40297 | 42.0703 | 0.522661 | 166.178 | 3.43092 | 0.64964 | 52.717 | 27.2351 | 0.505204 | 133.099 | 83.6898 | 48.8539 | 123.6457 | 9512.339 |
| 29925.5 | 21.9729 | 0.92984 | 168.517 | 3.69346 | 36.8395 | 0.494476 | 155.036 | 50.6648 | 0.892642 | 399.334 | 36.0548 | 0.548715 | 141.707 | 78.9141 | 85.9422 | 107.645 | 7536.387 |
| 40991.2 | 19.8536 | 0.90099 | 155.726 | 0.452303 | 73.2676 | 0.608894 | 260.678 | 75.452 | 0.835819 | 103.505 | 6.38941 | 0.523792 | 9.16603 | 213.164 | 70.6979 | 136.2094 | 9018.873 |
| 28053.4 | 23.6888 | 0.934722 | 63.2653 | 1.72723 | 20.5574 | 0.470582 | 278.327 | 58.5568 | 0.491948 | 180.429 | 37.832 | 0.563685 | 31.0407 | 157.668 | 94.9489 | 156.5114 | 10781.87 |
| 56815.6 | 21.5802 | 0.859738 | 24.7985 | 0.994213 | 77.9598 | 0.472475 | 381.346 | 10.8094 | 0.4782 | 200.207 | 19.3597 | 0.420013 | 48.8924 | 165.022 | 92.3281 | 301.909 | 19826.29 |
| 24227.3 | 26.2306 | 0.944699 | 147.403 | 1.4137 | 13.5173 | 0.304868 | 149.876 | 84.7069 | 0.679525 | 388.193 | 98.3298 | 0.394503 | 124.145 | 64.1744 | 350.972 | 302.2024 | 20780.95 |
| 56316.5 | 19.5063 | 0.861038 | 116.937 | 3.21361 | 16.7054 | 0.455415 | 120.74 | 93.5838 | 0.949416 | 246.997 | 88.2742 | 0.323122 | 39.1455 | 94.3238 | 223.645 | 220.6733 | 12637.89 |
| 32459.5 | 18.0908 | 0.923231 | 83.8884 | 2.76197 | 71.8164 | 0.430012 | 207.262 | 59.4553 | 0.536293 | 135.022 | 45.3184 | 0.351064 | 9.60926 | 173.079 | 79.4119 | 283.3205 | 21428.11 |
| 39747.6 | 24.9315 | 0.904236 | 128.733 | 2.47786 | 12.6177 | 0.408363 | 484.738 | 45.8302 | 0.540001 | 317.653 | 63.4624 | 0.991721 | 112.655 | 89.1051 | 250.685 | 116.3737 | 7374.98 |
| 35655.7 | 27.0345 | 0.914906 | 132.176 | 0.653942 | 79.4701 | 0.434011 | 439.744 | 63.7674 | 0.432327 | 426.369 | 51.9923 | 0.994835 | 32.3391 | 243.885 | 281.917 | 160.6038 | 11768.47 |
| 23083.1 | 26.6644 | 0.947682 | 106.984 | 0.164626 | 74.2228 | 0.382247 | 420.609 | 38.682 | 0.651086 | 438.292 | 35.9982 | 0.636127 | 5.19164 | 136.061 | 60.3112 | 161.8651 | 13058.68 |
| 57260.6 | 19.1088 | 0.858576 | 83.001 | 0.419923 | 94.559 | 0.344609 | 221.505 | 20.4036 | 0.916586 | 455.428 | 62.2017 | 0.411873 | 7.85258 | 75.5365 | 401.218 | 252.5278 | 17564.77 |
| 45416.6 | 13.4269 | 0.88945 | 95.0343 | 2.84509 | 16.8178 | 0.548435 | 355.186 | 67.096 | 0.97846 | 490.05 | 26.2296 | 0.385938 | 230.402 | 337.255 | 352.015 | 181.986 | 10849.02 |
| 27434.6 | 21.432 | 0.936333 | 45.078 | 1.98861 | 54.7056 | 0.566954 | 464.584 | 71.6388 | 0.865012 | 502.38 | 26.201 | 0.725228 | 26.6826 | 344.083 | 301.115 | 80.41212 | 5788.782 |
| 71111.3 | 17.946 | 0.822467 | 94.8404 | 2.43561 | 63.9837 | 0.369513 | 358.822 | 8.54638 | 0.750507 | 298.886 | 69.7814 | 0.802085 | 9.18702 | 163.921 | 230.537 | 148.0463 | 9226.822 |
| 68075.4 | 18.4369 | 0.830382 | 21.8084 | 1.60207 | 1.58869 | 0.402009 | 351.28 | 46.9216 | 0.849905 | 223.028 | 70.9871 | 0.567235 | 135.853 | 247.021 | 125.467 | 162.3133 | 8672.787 |
| 25283.2 | 23.5623 | 0.941943 | 128.288 | 1.60336 | 23.5402 | 0.340508 | 91.5103 | 17.0923 | 0.974828 | 460.045 | 9.09867 | 0.335563 | 141.683 | 79.2777 | 203.611 | 196.0309 | 14116.86 |
| 35386.4 | 27.3261 | 0.915608 | 50.2289 | 1.96852 | 8.13512 | 0.371279 | 417.545 | 43.7189 | 0.664544 | 108.895 | 0.880259 | 0.599397 | 65.429 | 108.761 | 79.0479 | 148.2449 | 9547.68 |
| 22690 | 19.1402 | 0.9487 | 132.828 | 1.56451 | 22.5232 | 0.306147 | 476.879 | 29.121 | 0.916048 | 367.069 | 99.0067 | 0.925183 | 50.3399 | 97.2762 | 192.338 | 94.06684 | 6889.813 |
| 35778.9 | 14.1513 | 0.914575 | 110.877 | 1.80692 | 29.8454 | 0.326529 | 300.642 | 23.5996 | 0.957235 | 388.732 | 60.8462 | 0.643341 | 31.1878 | 297.252 | 356.264 | 116.9938 | 8072.107 |
| 48316.3 | 14.4795 | 0.881891 | 171.732 | 0.375683 | 53.4016 | 0.498077 | 482.365 | 96.9912 | 0.530186 | 189.636 | 19.884 | 0.622492 | 12.8395 | 122.15 | 129.863 | 255.0773 | 15859.72 |
| 62197.3 | 20.2779 | 0.845707 | 112.496 | 0.480653 | 23.5842 | 0.556817 | 327.134 | 19.1545 | 0.835081 | 211.166 | 90.8734 | 0.604909 | 31.5148 | 174.09 | 101.407 | 128.3953 | 7315.034 |
| 26072.7 | 31.5806 | 0.939894 | 73.5448 | 2.25251 | 7.8366 | 0.466434 | 479.879 | 13.7379 | 0.429889 | 236.675 | 29.2128 | 0.981593 | 140.957 | 69.8623 | 59.9576 | 95.31595 | 6621.968 |
| 42521.3 | 17.3432 | 0.897 | 76.4051 | 1.07051 | 10.0852 | 0.543297 | 233.431 | 79.2834 | 0.931532 | 400.87 | 52.4118 | 0.666576 | 21.5435 | 176.982 | 393.867 | 93.60191 | 5702.69 |
| 24939.4 | 25.0656 | 0.942841 | 146.973 | 3.51365 | 72.9649 | 0.491367 | 183.023 | 53.9797 | 0.325324 | 333.13 | 28.9244 | 0.484858 | 31.7835 | 166.202 | 314.849 | 289.119 | 22567.96 |
| 51505.2 | 21.1632 | 0.873582 | 161.567 | 0.148961 | 23.9039 | 0.429567 | 433.905 | 54.4409 | 0.588043 | 361.188 | 6.35895 | 0.911625 | 13.1114 | 365.381 | 285.992 | 186.8407 | 11107.81 |
| 56344 | 15.0112 | 0.860963 | 75.4103 | 1.87227 | 48.5126 | 0.524594 | 433.659 | 40.1947 | 0.781857 | 118.042 | 35.6858 | 0.964434 | 87.5295 | 146.485 | 109.374 | 77.65296 | 4812.516 |
| 51810.8 | 22.5129 | 0.872786 | 164.762 | 2.11962 | 6.98176 | 0.393871 | 464.391 | 68.0645 | 0.351527 | 379.015 | 3.91535 | 0.8204 | 97.0107 | 137.037 | 261.63 | 295.1993 | 16964.86 |
| 62228.5 | 15.1055 | 0.845623 | 123.506 | 3.18223 | 46.2085 | 0.442986 | 74.504 | 95.8332 | 0.727327 | 117.847 | 27.5799 | 0.684808 | 97.0392 | 50.7124 | 104.849 | 144.2291 | 8737.494 |
| 22917.2 | 30.4612 | 0.948119 | 144.45 | 1.89606 | 5.53331 | 0.442741 | 431.415 | 99.0385 | 0.622638 | 362.475 | 66.2334 | 0.543638 | 77.8102 | 374.097 | 231.313 | 157.5424 | 10702.62 |
| 71970.7 | 14.6674 | 0.820225 | 41.2318 | 0.583148 | 56.8517 | 0.435019 | 122.164 | 29.932 | 0.341868 | 266.772 | 76.8161 | 0.719342 | 6.60023 | 88.3362 | 202.075 | 304.6834 | 18119.39 |
| 26667.6 | 24.9749 | 0.938336 | 169.412 | 0.633502 | 95.7391 | 0.429366 | 240.294 | 11.9172 | 0.533825 | 233.085 | 72.1733 | 0.750085 | 51.6604 | 97.5759 | 208.417 | 181.4196 | 14252.98 |
| 35818.1 | 13.77 | 0.914473 | 133.804 | 0.269011 | 15.8562 | 0.399106 | 213.484 | 58.4084 | 0.914287 | 172.645 | 83.1708 | 0.838153 | 6.26297 | 84.6999 | 124.246 | 104.4961 | 6748.586 |
| 71870 | 13.5619 | 0.820487 | 133.693 | 1.55134 | 48.7375 | 0.533116 | 317.143 | 10.0193 | 0.641111 | 379.145 | 88.7664 | 0.395258 | 58.6152 | 51.7188 | 64.6467 | 274.9123 | 15536.96 |
| 59872 | 20.3283 | 0.851769 | 144.277 | 1.6616 | 87.4911 | 0.619177 | 367.483 | 30.1576 | 0.577851 | 473.092 | 86.1496 | 0.9327 | 79.9687 | 120.87 | 228.671 | 120.2399 | 7290.809 |
| 70189.1 | 16.3816 | 0.824871 | 95.3716 | 1.69925 | 32.7444 | 0.427247 | 97.3769 | 64.8408 | 0.981442 | 283.589 | 21.3055 | 0.900828 | 66.2981 | 82.7416 | 94.3774 | 87.90087 | 5133.394 |
| 23582.6 | 18.9184 | 0.946373 | 155.968 | 0.341267 | 53.7329 | 0.423327 | 204.002 | 10.4117 | 0.544325 | 301.103 | 81.7908 | 0.740076 | 21.0036 | 89.7045 | 271.116 | 167.7937 | 12650.12 |
| 65032.9 | 21.0912 | 0.838315 | 110.629 | 1.28939 | 50.0756 | 0.391323 | 496.427 | 5.08552 | 0.79605 | 456.519 | 64.1947 | 0.763155 | 60.6602 | 453.863 | 67.107 | 140.2342 | 8572.911 |
| 57560.1 | 20.0188 | 0.857796 | 151.719 | 0.851307 | 33.0422 | 0.313062 | 276.123 | 56.4822 | 0.57075 | 333.848 | 77.9657 | 0.860583 | 45.9402 | 123.881 | 280.422 | 249.5597 | 14857.3 |
| 76756.7 | 14.5528 | 0.807748 | 73.4223 | 0.787152 | 76.5472 | 0.485223 | 466.605 | 26.4953 | 0.632016 | 343.593 | 99.6736 | 0.592316 | 53.887 | 301.356 | 140.577 | 191.6435 | 11387.52 |
| 28000.1 | 20.6483 | 0.934858 | 166.188 | 0.129059 | 13.4349 | 0.73945 | 118.062 | 67.4075 | 0.940555 | 324.473 | 56.5038 | 0.9038 | 6.02623 | 95.3715 | 54.0441 | 58.51681 | 3950.275 |
| 66303.5 | 13.74 | 0.834999 | 168.692 | 2.40074 | 30.5252 | 0.356723 | 326.37 | 45.9429 | 0.972066 | 394.425 | 41.016 | 0.370975 | 49.039 | 289.509 | 264.34 | 308.585 | 17507.47 |
| 57694.7 | 22.3218 | 0.857446 | 58.0509 | 2.79412 | 61.0065 | 0.355325 | 461.283 | 29.7765 | 0.533951 | 165.112 | 60.1148 | 0.537769 | 29.1602 | 201.61 | 45.5187 | 288.6349 | 18793.91 |
| 31700.2 | 30.0107 | 0.925221 | 111.65 | 1.4381 | 32.8669 | 0.478702 | 75.7938 | 0.417943 | 0.955972 | 229.272 | 16.0538 | 0.302086 | 119.835 | 44.8472 | 217.014 | 161.7204 | 11298.15 |
| 26805 | 15.3805 | 0.93797 | 72.2987 | 1.15024 | 84.575 | 0.469068 | 323.149 | 41.3298 | 0.828126 | 267.012 | 38.3357 | 0.448861 | 64.4483 | 168.003 | 175.362 | 122.9731 | 9821.23 |
| 27160.4 | 31.993 | 0.937059 | 169.403 | 3.38248 | 77.6712 | 0.449671 | 418.697 | 31.6213 | 0.778096 | 513.693 | 25.1537 | 0.838845 | 46.3048 | 166.534 | 147.177 | 87.46193 | 6940.783 |
| 26349.1 | 30.5456 | 0.939172 | 32.2553 | 3.42806 | 69.6738 | 0.39956 | 94.4528 | 3.53654 | 0.697228 | 86.4364 | 87.5341 | 0.783735 | 147.819 | 64.391 | 68.7776 | 97.29222 | 7873.993 |
| 79330.8 | 13.7657 | 0.801037 | 59.3349 | 2.57748 | 9.32935 | 0.423895 | 139.937 | 70.3238 | 0.995631 | 485.865 | 14.8349 | 0.603508 | 55.2926 | 62.0664 | 258.691 | 136.5383 | 7190.156 |
| 22920.1 | 17.0516 | 0.948099 | 44.9432 | 0.320107 | 98.2322 | 0.529685 | 224.039 | 8.7294 | 0.674402 | 365.669 | 8.13772 | 0.622377 | 16.3018 | 127.976 | 178.413 | 107.8626 | 8980.313 |
| 42020.1 | 19.9971 | 0.898308 | 91.5475 | 1.52107 | 8.22176 | 0.300241 | 393.326 | 23.4488 | 0.765268 | 249.851 | 51.3421 | 0.627954 | 8.745 | 229.043 | 89.7958 | 162.3733 | 10049.34 |
| 24407.4 | 33.0717 | 0.944238 | 161.5 | 0.337272 | 25.9223 | 0.3439 | 198.337 | 98.9395 | 0.700313 | 428.936 | 37.3174 | 0.917524 | 19.5171 | 144.776 | 409.485 | 138.7066 | 9862.168 |
| 56680.9 | 20.6902 | 0.860088 | 122.019 | 2.46862 | 12.0876 | 0.54367 | 283.595 | 88.3325 | 0.881563 | 255.741 | 54.1894 | 0.642796 | 156.568 | 175.585 | 183.531 | 112.313 | 6397.849 |
| 37883 | 16.793 | 0.909091 | 63.8836 | 0.151074 | 72.2398 | 0.374579 | 353.864 | 69.8314 | 0.438637 | 158.886 | 49.6747 | 0.936678 | 7.67048 | 222.306 | 129.818 | 174.5487 | 12857.23 |
| 50578.4 | 17.2393 | 0.875995 | 165.966 | 1.37944 | 19.3069 | 0.652729 | 342.147 | 57.8923 | 0.549775 | 198.892 | 49.7051 | 0.305726 | 98.9112 | 114.135 | 155.951 | 355.6965 | 20451.16 |
| 52629.5 | 23.9723 | 0.870653 | 53.947 | 2.72803 | 85.1872 | 0.6365 | 259.692 | 54.2597 | 0.887015 | 384.048 | 73.0415 | 0.603502 | 48.2654 | 231.387 | 323.65 | 149.6701 | 9322.161 |
| 73927.6 | 18.4361 | 0.815125 | 166.641 | 0.810188 | 44.9568 | 0.389468 | 314.707 | 41.7996 | 0.710933 | 107.387 | 88.6575 | 0.666254 | 57.9324 | 127.703 | 63.325 | 261.4993 | 14632 |
| 71284.9 | 13.7811 | 0.822013 | 105.757 | 1.56136 | 72.6027 | 0.391606 | 444.984 | 23.7786 | 0.654146 | 246.407 | 25.8132 | 0.35159 | 129.375 | 340.783 | 161.503 | 377.7474 | 23329.98 |
| 28179.6 | 27.6193 | 0.934397 | 64.7315 | 1.88459 | 57.7579 | 0.392032 | 371.012 | 28.794 | 0.51731 | 248.093 | 7.54369 | 0.874175 | 136.964 | 283.785 | 173.021 | 116.1774 | 9130.159 |
| 55820.8 | 16.6297 | 0.862328 | 100.121 | 0.267116 | 52.5581 | 0.390795 | 244.882 | 72.2578 | 0.563018 | 297.37 | 19.5828 | 0.580369 | 0.80431 | 196.5 | 106.904 | 268.8784 | 16817.58 |
| 57285.2 | 13.576 | 0.858509 | 141.566 | 0.816884 | 22.8678 | 0.480239 | 223.113 | 43.6374 | 0.585251 | 400.477 | 35.8026 | 0.447048 | 22.586 | 174.904 | 211.629 | 283.8597 | 16342 |
| 30541.5 | 26.5647 | 0.928238 | 65.4033 | 1.45355 | 41.6871 | 0.479284 | 267.712 | 58.022 | 0.36164 | 214.504 | 81.2987 | 0.920748 | 66.3927 | 152.724 | 64.5672 | 136.7686 | 9679.428 |
| 59764.4 | 20.0606 | 0.852049 | 169.635 | 2.45592 | 93.805 | 0.582255 | 308.362 | 10.954 | 0.802106 | 496.084 | 97.0378 | 0.383278 | 38.0325 | 187.222 | 84.4857 | 214.5604 | 13379.29 |
| 20348.8 | 14.8287 | 0.954801 | 128.508 | 0.952408 | 31.8264 | 0.420723 | 263.753 | 76.1647 | 0.636862 | 298.129 | 26.1225 | 0.818742 | 63.2315 | 249.426 | 165.307 | 101.5436 | 7686.115 |
| 53930.4 | 20.7076 | 0.867259 | 93.7475 | 1.28459 | 65.0543 | 0.420688 | 364.387 | 19.1041 | 0.814188 | 518.812 | 29.8138 | 0.810331 | 22.8487 | 256.974 | 48.9537 | 101.8758 | 6879.336 |
| 51457.8 | 21.3913 | 0.873705 | 73.0368 | 0.996334 | 24.9759 | 0.360368 | 484.6 | 14.2393 | 0.410447 | 421.555 | 57.1655 | 0.771215 | 64.1918 | 220.584 | 370.36 | 230.5369 | 14154.85 |
| 74063.7 | 13.1591 | 0.814768 | 57.6878 | 3.31765 | 92.6828 | 0.363058 | 232.921 | 86.467 | 0.552964 | 415.215 | 93.8449 | 0.456013 | 99.8284 | 203.089 | 185.564 | 385.8752 | 24741.08 |
| 45098.9 | 17.8682 | 0.89028 | 38.9396 | 0.666042 | 55.4799 | 0.453526 | 481.105 | 0.316177 | 0.742813 | 440.78 | 94.8417 | 0.880839 | 33.7958 | 476.602 | 364.961 | 86.60359 | 5954.88 |
| 33658.2 | 23.6681 | 0.92011 | 101.438 | 0.870082 | 63.2159 | 0.422697 | 414.074 | 66.7657 | 0.911841 | 268.151 | 31.3996 | 0.40755 | 9.81468 | 84.2566 | 160.13 | 166.1732 | 12091.45 |
| 26425.4 | 14.0492 | 0.938959 | 36.2218 | 0.266138 | 41.0646 | 0.326913 | 432.003 | 49.4282 | 0.728742 | 369.629 | 95.4269 | 0.77891 | 16.6999 | 347.653 | 115.493 | 114.1047 | 8615.679 |
| 48718.7 | 14.432 | 0.880842 | 24.8617 | 0.525946 | 13.7723 | 0.447535 | 271.809 | 13.8098 | 0.702569 | 343.042 | 84.4244 | 0.567885 | 21.1032 | 209.594 | 217.659 | 142.3868 | 8581.523 |
| 70338.8 | 17.358 | 0.824481 | 140.872 | 2.32147 | 95.5437 | 0.434431 | 231.618 | 35.6251 | 0.714593 | 312.371 | 23.6548 | 0.67621 | 99.8286 | 179.688 | 197.892 | 178.4342 | 11377.83 |
| 21862.7 | 32.3597 | 0.950871 | 152.838 | 2.67974 | 15.9152 | 0.538276 | 401.201 | 58.9884 | 0.7443 | 227.769 | 71.7898 | 0.771196 | 9.91401 | 394.15 | 102.388 | 75.5775 | 5386.191 |
| 47852.7 | 13.5673 | 0.883099 | 70.4866 | 1.43516 | 30.7266 | 0.378497 | 366.612 | 66.7428 | 0.552639 | 349.474 | 76.124 | 0.783035 | 125.385 | 182.276 | 106.671 | 160.4372 | 10161.61 |
| 28688.7 | 26.7424 | 0.933068 | 31.9895 | 0.883897 | 61.9413 | 0.461348 | 274.969 | 64.1853 | 0.729871 | 445.333 | 12.2963 | 0.405482 | 33.1702 | 85.5204 | 215.65 | 161.9148 | 12191.54 |
| 57557.2 | 13.5688 | 0.8578 | 66.7927 | 2.76827 | 99.3095 | 0.466675 | 460.904 | 49.159 | 0.644814 | 500.496 | 77.254 | 0.965871 | 98.7609 | 445.986 | 330.364 | 104.8052 | 7188.275 |
| 39607 | 18.7995 | 0.904598 | 64.8229 | 2.72576 | 69.8208 | 0.40924 | 422.614 | 26.1846 | 0.605362 | 116.729 | 17.9153 | 0.62844 | 34.9636 | 156.361 | 49.587 | 153.6893 | 11337.35 |
| 52339 | 18.6477 | 0.871406 | 39.8234 | 1.04545 | 62.6418 | 0.331928 | 66.3561 | 89.5432 | 0.668879 | 126.621 | 72.6706 | 0.48655 | 19.2152 | 59.683 | 126.175 | 269.5273 | 18060.76 |
| 30052.5 | 27.194 | 0.929513 | 76.358 | 0.354695 | 56.2162 | 0.303297 | 393.942 | 71.738 | 0.864075 | 339.032 | 93.059 | 0.392307 | 7.44427 | 110.758 | 308.073 | 243.6506 | 18225.21 |
| 35946.1 | 14.7743 | 0.914139 | 87.5263 | 2.78086 | 26.3679 | 0.402082 | 297.083 | 48.5026 | 0.608038 | 346.425 | 82.9307 | 0.75208 | 81.6767 | 234.742 | 240.385 | 124.8575 | 8388.106 |
| 51138 | 14.9624 | 0.874535 | 138.244 | 2.10791 | 96.3147 | 0.485805 | 390.11 | 63.2007 | 0.455405 | 486.085 | 68.6477 | 0.850026 | 14.7122 | 264.754 | 485.992 | 170.2922 | 11704.5 |
| 42171.6 | 27.2566 | 0.897919 | 63.3387 | 1.36966 | 86.6517 | 0.451532 | 138.588 | 16.0271 | 0.769279 | 317.669 | 13.8874 | 0.459764 | 3.79778 | 129.637 | 151.429 | 158.2564 | 11748.64 |
| 57013.8 | 14.7503 | 0.859217 | 75.0074 | 2.65317 | 55.1633 | 0.575873 | 324.514 | 81.0506 | 0.872255 | 464.702 | 25.3722 | 0.635579 | 188.375 | 211.437 | 413.519 | 129.1489 | 7739.865 |
| 57889.5 | 16.9847 | 0.856935 | 19.6391 | 3.25495 | 23.3062 | 0.368203 | 429.666 | 49.031 | 0.857563 | 447.212 | 22.831 | 0.879068 | 17.3049 | 182.016 | 155.12 | 101.7586 | 6140.111 |
| 21847.7 | 31.56 | 0.950909 | 135.335 | 2.33789 | 60.2942 | 0.570829 | 394.275 | 36.9732 | 0.835433 | 332.166 | 83.7848 | 0.820045 | 40.468 | 345.498 | 228.164 | 63.8017 | 4817.959 |
| 66553.5 | 21.0632 | 0.834351 | 79.8469 | 2.1027 | 21.8719 | 0.473394 | 414.6 | 98.0089 | 0.904665 | 475.708 | 49.7501 | 0.997199 | 159.791 | 259.896 | 378.641 | 80.30088 | 4603.99 |
| 68525.4 | 15.8323 | 0.829207 | 123.733 | 0.378501 | 36.9881 | 0.461623 | 310.946 | 81.5627 | 0.85819 | 501.263 | 71.4595 | 0.819788 | 11.0939 | 96.5691 | 380.388 | 129.9562 | 7417.942 |
| 47072.1 | 20.1164 | 0.885138 | 97.0244 | 0.783735 | 2.77982 | 0.395968 | 295.007 | 83.3727 | 0.742914 | 124.446 | 50.4895 | 0.843857 | 41.838 | 291.081 | 82.9468 | 113.4653 | 6713.129 |
| 39618.6 | 17.8013 | 0.904567 | 108.187 | 1.68223 | 71.0908 | 0.490397 | 401.937 | 97.9988 | 0.7128 | 272.254 | 17.0963 | 0.643008 | 28.6157 | 287.046 | 235.548 | 118.4084 | 8341.45 |
| 64167.5 | 13.7632 | 0.840567 | 34.5392 | 3.37486 | 78.6439 | 0.476948 | 484.871 | 76.8525 | 0.392984 | 356.982 | 55.7766 | 0.856198 | 91.6208 | 249.015 | 132.156 | 194.6984 | 12262.74 |
| 68345.6 | 17.6955 | 0.829677 | 160.884 | 3.23362 | 92.3492 | 0.638726 | 301.723 | 0.83691 | 0.680275 | 228.897 | 79.3473 | 0.807904 | 52.676 | 183.679 | 174.216 | 129.4657 | 7602.816 |
| 63346.8 | 20.421 | 0.84271 | 124.367 | 1.44893 | 23.2406 | 0.474789 | 434.048 | 6.27934 | 0.777573 | 182.006 | 5.95179 | 0.892342 | 61.5028 | 76.4696 | 66.4571 | 97.15397 | 5658.833 |
| 46818.6 | 23.5685 | 0.885801 | 83.8853 | 1.72242 | 71.6411 | 0.420479 | 404.907 | 30.6154 | 0.778164 | 465.746 | 60.8808 | 0.367027 | 100.271 | 126.194 | 427.551 | 224.0009 | 15543.92 |
| 54213.1 | 23.6711 | 0.866524 | 61.1083 | 0.354222 | 7.40102 | 0.482163 | 256.504 | 16.131 | 0.912073 | 324.018 | 7.74596 | 0.648031 | 23.1557 | 143.79 | 255.758 | 94.73655 | 5559.037 |
| 36808.7 | 17.5829 | 0.911892 | 19.7739 | 1.48466 | 46.1943 | 0.33132 | 276.747 | 49.9287 | 0.481768 | 451.809 | 70.5235 | 0.559543 | 62.5425 | 57.0794 | 240.071 | 261.3742 | 18527.2 |
| 29178.3 | 25.378 | 0.931791 | 151.821 | 0.972337 | 57.7583 | 0.496259 | 427.107 | 85.5883 | 0.430074 | 199.286 | 64.3462 | 0.724239 | 87.8314 | 350.266 | 107.548 | 184.8299 | 13255.55 |
| 50307.7 | 16.7069 | 0.876701 | 155.671 | 1.95607 | 23.191 | 0.405779 | 156.093 | 10.0072 | 0.543856 | 272.477 | 24.3824 | 0.797177 | 141.684 | 98.0939 | 73.1324 | 178.2323 | 10834.12 |
| 24868.2 | 31.0261 | 0.943034 | 155.85 | 0.836624 | 16.6912 | 0.660388 | 432.806 | 37.3405 | 0.781094 | 323.994 | 90.6702 | 0.567312 | 33.5366 | 286.771 | 288.731 | 98.80638 | 6734.302 |
| 62815.3 | 17.65 | 0.844094 | 110.446 | 1.0006 | 15.8698 | 0.42781 | 488.001 | 78.2106 | 0.729763 | 305.596 | 15.1528 | 0.800791 | 25.5745 | 180.115 | 79.4575 | 132.7869 | 7533.074 |
| 27858.2 | 25.008 | 0.935232 | 148.784 | 3.15758 | 8.33221 | 0.303862 | 489.724 | 73.9007 | 0.807508 | 290.552 | 58.7215 | 0.714914 | 89.6408 | 319.696 | 273.278 | 133.3386 | 8960.332 |
| 69029.2 | 18.0406 | 0.827895 | 163.701 | 2.24489 | 4.23286 | 0.492394 | 282.674 | 65.7794 | 0.895974 | 497.844 | 42.1643 | 0.578503 | 116.687 | 68.2213 | 50.9712 | 158.4288 | 8467.288 |
| 40640.3 | 13.4508 | 0.901901 | 82.4052 | 0.641409 | 14.2448 | 0.39152 | 340.05 | 9.7126 | 0.400834 | 473.09 | 48.4447 | 0.775918 | 50.8811 | 78.3325 | 374.451 | 195.1594 | 12315.25 |
| 44178.4 | 25.3526 | 0.892686 | 154.706 | 0.68048 | 10.4703 | 0.417838 | 374.765 | 54.2787 | 0.417976 | 107.493 | 21.0082 | 0.564769 | 66.3371 | 369.015 | 56.5702 | 340.9469 | 20458.01 |
| 45059.9 | 22.3356 | 0.890385 | 134.935 | 1.30529 | 24.6722 | 0.357243 | 461.38 | 3.96511 | 0.743071 | 477.77 | 61.4208 | 0.975602 | 124.523 | 282.071 | 185.812 | 112.9691 | 7205.609 |
| 48491.5 | 19.4522 | 0.881437 | 81.5982 | 2.59163 | 44.2189 | 0.475041 | 255.695 | 29.1343 | 0.812658 | 67.0826 | 80.5088 | 0.441997 | 118.092 | 64.6759 | 54.39 | 156.3839 | 9975.289 |
| 47291.9 | 26.6679 | 0.88457 | 106.886 | 0.29577 | 14.1419 | 0.631177 | 329.859 | 46.2894 | 0.972994 | 492.108 | 14.3086 | 0.569389 | 20.2815 | 326.324 | 373.94 | 98.32718 | 5909.478 |
| 68248.7 | 19.7376 | 0.829931 | 85.9625 | 0.805166 | 45.8705 | 0.305829 | 168.134 | 76.4486 | 0.568129 | 248.665 | 40.4477 | 0.525595 | 17.5086 | 157.611 | 176.01 | 368.4829 | 22008.94 |
| 27674.9 | 19.557 | 0.935705 | 168.463 | 2.76425 | 78.4969 | 0.407198 | 231.132 | 91.8882 | 0.993637 | 157.049 | 37.1615 | 0.419491 | 138.344 | 184.551 | 136.349 | 170.4516 | 12942.46 |
| 37419.2 | 14.7093 | 0.910299 | 148.834 | 1.92962 | 84.679 | 0.57461 | 278.357 | 72.0485 | 0.43652 | 312.569 | 55.0844 | 0.929998 | 116.881 | 266.879 | 225.53 | 122.3257 | 8460.137 |
| 37798.2 | 27.5004 | 0.909321 | 133.74 | 0.800299 | 58.2879 | 0.383439 | 151.623 | 35.553 | 0.743608 | 288.458 | 84.8381 | 0.853188 | 31.5553 | 74.7381 | 185.868 | 124.7358 | 8778.956 |
| 29708.5 | 28.1605 | 0.930411 | 149.642 | 2.56908 | 55.187 | 0.36266 | 240.255 | 39.2792 | 0.560018 | 150.419 | 41.3436 | 0.633184 | 139.005 | 135.535 | 54.3879 | 194.6975 | 14521.11 |
| 36184.7 | 19.8525 | 0.913521 | 83.7788 | 0.273982 | 50.9067 | 0.464119 | 213.513 | 73.9841 | 0.442247 | 126.591 | 64.7284 | 0.735253 | 15.0984 | 167.367 | 46.2659 | 176.556 | 12214.73 |
| 75197.8 | 14.8317 | 0.811812 | 154.846 | 2.40369 | 59.8649 | 0.33337 | 337.63 | 48.8873 | 0.873521 | 458.3 | 75.2849 | 0.458198 | 86.9808 | 77.5599 | 358.203 | 309.4177 | 18158.54 |
| 78154 | 16.4183 | 0.804107 | 44.2947 | 1.06719 | 48.9308 | 0.375344 | 340.892 | 51.6602 | 0.891386 | 222.506 | 24.5722 | 0.913935 | 86.4371 | 262.008 | 87.83 | 113.2575 | 6664.415 |
| 68189.2 | 14.3854 | 0.830083 | 35.6764 | 0.306227 | 18.0766 | 0.389603 | 385.505 | 94.6721 | 0.572362 | 314.279 | 63.3511 | 0.401887 | 12.4108 | 148.869 | 48.4889 | 355.1104 | 19556.96 |
| 31175.9 | 31.3332 | 0.92659 | 68.9381 | 0.494058 | 81.8617 | 0.462417 | 137.726 | 97.9684 | 0.782531 | 279.863 | 19.382 | 0.77561 | 19.3746 | 44.9415 | 130.384 | 88.27005 | 6823.666 |
| 23689.5 | 16.9056 | 0.946093 | 38.6396 | 2.10436 | 50.0702 | 0.478834 | 494.462 | 17.529 | 0.851325 | 452.023 | 95.6989 | 0.837803 | 30.0162 | 372.816 | 160.518 | 59.78962 | 4602.422 |
| 21634.3 | 23.2384 | 0.951456 | 93.2432 | 1.39166 | 17.9637 | 0.368742 | 338.35 | 83.8862 | 0.968569 | 454.488 | 20.7221 | 0.964809 | 86.9496 | 324.009 | 244.663 | 63.22623 | 4680.317 |
| 30177.5 | 23.1848 | 0.929184 | 72.6693 | 2.59659 | 12.4541 | 0.35557 | 349.241 | 91.9209 | 0.421975 | 330.841 | 6.11793 | 0.679653 | 162.305 | 139.175 | 207.641 | 203.6496 | 13626.12 |
| 27142.2 | 19.9973 | 0.937094 | 131.674 | 0.336714 | 29.9917 | 0.611295 | 109.942 | 97.372 | 0.457064 | 257.125 | 6.39279 | 0.829578 | 9.49525 | 99.3667 | 210.331 | 117.0058 | 8095.937 |
| 36571.3 | 23.167 | 0.912515 | 100.079 | 3.17979 | 7.51333 | 0.504541 | 299.327 | 37.6807 | 0.605807 | 315.426 | 16.9067 | 0.824044 | 29.8438 | 94.6582 | 156.968 | 91.23617 | 5849.653 |
| 54058.5 | 16.0962 | 0.866922 | 51.8861 | 2.76007 | 62.0495 | 0.428344 | 155.902 | 99.7912 | 0.849515 | 219.889 | 66.8163 | 0.915635 | 115.187 | 49.2377 | 199.877 | 91.97891 | 6039.006 |
| 51190.7 | 25.6053 | 0.874405 | 149.111 | 0.294048 | 95.3451 | 0.464848 | 168.505 | 23.2682 | 0.587301 | 100.889 | 93.8064 | 0.603668 | 2.87223 | 105.447 | 51.7543 | 247.2762 | 16342.74 |
| 46619.3 | 15.3663 | 0.886315 | 167.733 | 3.34169 | 29.5602 | 0.576273 | 239.833 | 30.145 | 0.662525 | 351.693 | 14.3292 | 0.7637 | 17.1645 | 229.751 | 119.737 | 102.1732 | 6378.376 |
| 34280.2 | 25.1098 | 0.91849 | 50.8333 | 0.386194 | 85.691 | 0.494209 | 268.893 | 38.5563 | 0.558363 | 426.051 | 6.60131 | 0.974199 | 28.9034 | 144.484 | 225.155 | 83.39132 | 6310.879 |
| 52705.2 | 21.8773 | 0.870454 | 34.2743 | 0.618188 | 96.5447 | 0.409611 | 488.518 | 58.5322 | 0.485597 | 172.355 | 26.3825 | 0.446384 | 44.7605 | 196.233 | 123.491 | 327.129 | 23183.11 |
| 22559.5 | 20.7043 | 0.949042 | 106.368 | 3.52698 | 28.4201 | 0.344024 | 373.283 | 29.6735 | 0.811713 | 66.5079 | 90.442 | 0.734642 | 119.796 | 168.256 | 46.7335 | 95.44438 | 7180.059 |
| 72308.6 | 13.2457 | 0.819344 | 86.9842 | 1.02807 | 3.18078 | 0.500234 | 388.099 | 97.917 | 0.640424 | 360.606 | 85.6109 | 0.728161 | 29.6961 | 329.871 | 134.028 | 147.292 | 7777.901 |
| 23567.5 | 19.717 | 0.946413 | 80.254 | 0.447142 | 93.3412 | 0.518927 | 407.866 | 0.016539 | 0.562648 | 94.4299 | 81.7057 | 0.825997 | 19.5299 | 284.754 | 54.1754 | 88.71885 | 7221.303 |
| 26872.2 | 17.0159 | 0.937796 | 100.541 | 0.946654 | 32.9062 | 0.332384 | 453.785 | 1.43542 | 0.559613 | 184.397 | 71.1209 | 0.335815 | 23.9914 | 383.024 | 130.016 | 340.3982 | 24859.74 |
| 55600.2 | 19.4695 | 0.862905 | 83.6784 | 2.95804 | 95.9851 | 0.36641 | 255.678 | 81.9716 | 0.594977 | 198.818 | 25.7805 | 0.777626 | 104.632 | 130.492 | 75.2228 | 177.8315 | 12631.66 |
| 55025.2 | 15.4944 | 0.864402 | 154.826 | 2.84695 | 87.9644 | 0.477423 | 231.479 | 77.5346 | 0.654395 | 351.183 | 46.2974 | 0.84805 | 72.3682 | 211.386 | 91.0208 | 130.4501 | 8664.702 |
| 47876.8 | 19.8963 | 0.88304 | 153.444 | 2.314 | 68.8775 | 0.374873 | 332.708 | 62.5349 | 0.621782 | 373.554 | 79.1827 | 0.993184 | 131.337 | 44.9009 | 295.662 | 142.4712 | 9671.513 |
| 20803.6 | 28.0913 | 0.953626 | 67.0939 | 1.4647 | 27.9413 | 0.426013 | 354.102 | 35.2492 | 0.705039 | 71.3079 | 93.9226 | 0.665032 | 41.754 | 229.635 | 44.8198 | 96.83605 | 7267.004 |
| 32985.1 | 19.705 | 0.921862 | 80.5796 | 0.901609 | 61.8214 | 0.62468 | 376.08 | 16.6345 | 0.945418 | 394.642 | 89.8873 | 0.997701 | 49.7245 | 203.971 | 324.068 | 56.60931 | 3954.736 |
| 20867.1 | 29.3171 | 0.953462 | 160.248 | 2.01321 | 3.65791 | 0.462213 | 453.063 | 56.421 | 0.685513 | 474.667 | 0.288625 | 0.457538 | 27.4682 | 125.672 | 211.792 | 159.1879 | 11099.45 |
| 34494.9 | 27.3977 | 0.917932 | 75.1792 | 1.2777 | 71.3582 | 0.384848 | 373.823 | 8.61558 | 0.579336 | 336.639 | 36.6341 | 0.350004 | 1.37593 | 143.027 | 216.177 | 294.8091 | 22533.1 |
| 29191 | 32.162 | 0.931765 | 81.6657 | 2.06678 | 87.4792 | 0.442494 | 109.51 | 95.6988 | 0.705815 | 240.256 | 0.639691 | 0.489121 | 78.5478 | 101.41 | 134.231 | 155.4493 | 12275.2 |
| 40508.2 | 20.0711 | 0.902249 | 28.9109 | 3.0521 | 16.8733 | 0.372224 | 378.269 | 75.6214 | 0.366017 | 516.866 | 1.75422 | 0.67041 | 136.139 | 258.714 | 48.3579 | 255.777 | 16209.06 |
| 35359.1 | 23.2329 | 0.915675 | 75.4075 | 3.24545 | 20.7063 | 0.342701 | 430.864 | 30.7345 | 0.77004 | 487.902 | 58.0935 | 0.817329 | 83.1065 | 262.308 | 178.851 | 103.6641 | 7004.584 |
| 21937.6 | 19.9436 | 0.950662 | 28.2738 | 0.872752 | 0.029562 | 0.471882 | 166.556 | 0.94766 | 0.683894 | 440.544 | 60.7765 | 0.897857 | 28.517 | 58.4046 | 369.852 | 60.34029 | 4303.517 |
| 55549.8 | 22.7096 | 0.863038 | 23.2972 | 1.66417 | 51.8879 | 0.317449 | 121.938 | 38.1679 | 0.880285 | 284.097 | 61.7253 | 0.998325 | 30.1725 | 64.7827 | 252.994 | 113.3172 | 7454.213 |
| 67460.2 | 15.5011 | 0.831984 | 143.757 | 0.182084 | 81.7692 | 0.464 | 403.049 | 6.65169 | 0.67732 | 458.005 | 39.6741 | 0.883254 | 13.2203 | 155.805 | 325.804 | 164.8303 | 10011.02 |
| 34824.6 | 13.3723 | 0.917063 | 112.736 | 2.60623 | 17.9169 | 0.396302 | 259.764 | 35.9009 | 0.395268 | 212.555 | 53.4168 | 0.663622 | 103.358 | 85.7842 | 118.993 | 209.356 | 13793.93 |
| 59037 | 21.3687 | 0.853946 | 108.518 | 2.73891 | 97.9957 | 0.309144 | 255.732 | 51.4177 | 0.655875 | 464.786 | 5.18523 | 0.5449 | 26.3829 | 204.589 | 387.608 | 281.9106 | 20119.29 |
| 21572 | 21.3381 | 0.951617 | 166.734 | 3.73275 | 92.2236 | 0.527197 | 445.912 | 59.8568 | 0.878185 | 263.008 | 8.07689 | 0.387405 | 51.3076 | 121.333 | 177.89 | 136.4188 | 11018.97 |
| 66693 | 18.7294 | 0.833986 | 144.786 | 0.433661 | 64.8235 | 0.330754 | 354.72 | 79.2203 | 0.969198 | 331.022 | 62.6822 | 0.390435 | 10.4924 | 343.297 | 238.509 | 361.0661 | 21686.37 |
| 66196.1 | 19.2837 | 0.835282 | 168.588 | 2.50207 | 51.0701 | 0.49101 | 432.722 | 0.510574 | 0.379712 | 469.505 | 30.4674 | 0.935819 | 125.986 | 357.849 | 51.7302 | 220.4869 | 12892.17 |
| 77672.9 | 16.2988 | 0.805361 | 141.142 | 1.82093 | 93.4406 | 0.535518 | 375.895 | 78.3866 | 0.971815 | 192.037 | 45.1004 | 0.335716 | 171.922 | 151.551 | 123.703 | 247.5321 | 14470.27 |
| 65324.4 | 17.3576 | 0.837553 | 132.052 | 1.08521 | 59.4802 | 0.390359 | 177.091 | 83.138 | 0.803278 | 401.392 | 43.9814 | 0.649968 | 4.38256 | 46.8443 | 56.1983 | 188.4369 | 11457.59 |
| 70970.9 | 19.3344 | 0.822834 | 152.407 | 2.3913 | 59.4478 | 0.456822 | 56.674 | 60.7041 | 0.590166 | 192.479 | 71.4572 | 0.737185 | 155.678 | 48.9041 | 100.967 | 199.4995 | 11688.37 |
| 34736.4 | 21.0494 | 0.917297 | 103.332 | 0.356541 | 40.2366 | 0.625704 | 201.823 | 35.5709 | 0.994391 | 279.487 | 43.9571 | 0.652807 | 16.0897 | 185.734 | 276.174 | 76.10378 | 5095.485 |
| 66830.4 | 15.6799 | 0.833626 | 159.585 | 1.87817 | 9.73359 | 0.510794 | 93.4241 | 60.2809 | 0.344124 | 137.806 | 76.9025 | 0.692759 | 137.351 | 71.1533 | 100.08 | 316.7982 | 17021.07 |
| 34879.9 | 24.9637 | 0.916926 | 111.304 | 2.71678 | 55.0201 | 0.321682 | 402.867 | 81.2645 | 0.869859 | 394.626 | 92.2221 | 0.362566 | 148.617 | 165.488 | 309.385 | 244.0806 | 17648.5 |
| 67582.1 | 14.5052 | 0.831666 | 108.893 | 2.30704 | 82.5341 | 0.542407 | 359.692 | 96.5815 | 0.857736 | 468.837 | 33.9039 | 0.6397 | 196.945 | 351.459 | 382.07 | 134.8264 | 8031.601 |
| 56240.2 | 22.9412 | 0.861239 | 158.648 | 0.686727 | 21.4843 | 0.304707 | 268.901 | 18.4424 | 0.409565 | 189.978 | 95.7838 | 0.891139 | 4.52102 | 222.639 | 165.174 | 353.3674 | 20517.04 |
| 47808.8 | 25.1966 | 0.883221 | 41.1752 | 2.52483 | 8.02632 | 0.303011 | 242.9 | 41.6109 | 0.737059 | 406.234 | 11.5805 | 0.911264 | 67.7398 | 218.398 | 185.88 | 123.1248 | 7447.391 |
| 59636 | 18.0186 | 0.852383 | 138.819 | 3.25746 | 11.0008 | 0.553405 | 232.714 | 2.19033 | 0.880698 | 379.59 | 52.2245 | 0.810422 | 122.158 | 206.682 | 287.758 | 80.50611 | 4626.972 |
| 30664.7 | 24.1252 | 0.927915 | 125.61 | 1.4455 | 76.8791 | 0.563277 | 411.592 | 10.3742 | 0.624859 | 490.59 | 76.6165 | 0.788438 | 139.136 | 138.371 | 485.905 | 92.22141 | 6691.969 |
| 31626 | 30.456 | 0.925415 | 75.54 | 1.06154 | 94.5059 | 0.200702 | 412.196 | 45.1819 | 0.836125 | 305.883 | 87.3018 | 0.628416 | 36.1889 | 120.253 | 118.424 | 232.9412 | 19935.88 |
| 78398.4 | 15.1795 | 0.803469 | 153.212 | 2.87742 | 36.0442 | 0.29508 | 199.975 | 92.9683 | 0.924917 | 255.867 | 59.5532 | 0.663802 | 162.618 | 186.458 | 149.397 | 228.2805 | 12707.76 |
| 47885.8 | 26.5318 | 0.883022 | 59.1574 | 1.94701 | 46.3608 | 0.618067 | 236.308 | 46.2165 | 0.982436 | 277.737 | 56.637 | 0.871568 | 61.3534 | 184.792 | 220.457 | 69.10656 | 4353.822 |
| 20822.8 | 29.9237 | 0.953578 | 157.427 | 2.19564 | 62.7128 | 0.540058 | 230.172 | 25.6979 | 0.766819 | 388.662 | 58.1311 | 0.558551 | 74.3022 | 198.239 | 239.436 | 101.6556 | 7962.982 |
| 61681.2 | 14.5803 | 0.847049 | 159.39 | 1.75238 | 84.5021 | 0.574958 | 166.158 | 86.6858 | 0.59852 | 364.214 | 73.6556 | 0.718159 | 112.232 | 97.2596 | 89.5613 | 161.9351 | 9891.337 |
| 24355.9 | 23.5946 | 0.944361 | 164.357 | 2.26349 | 9.05215 | 0.613454 | 356.29 | 37.7704 | 0.363007 | 254.412 | 41.3451 | 0.351117 | 101.899 | 202.043 | 228.259 | 362.6707 | 24399.64 |
| 22577.4 | 31.8598 | 0.949007 | 117.3 | 1.66838 | 62.9408 | 0.203147 | 216.046 | 90.376 | 0.988288 | 474.717 | 14.9207 | 0.382764 | 21.0577 | 91.8474 | 270.304 | 300.7372 | 24809.87 |
| 35504.7 | 28.0963 | 0.915301 | 127.727 | 1.78456 | 22.5214 | 0.44661 | 357.683 | 2.69206 | 0.757007 | 153.013 | 66.705 | 0.405934 | 136.107 | 342.511 | 110.665 | 179.0346 | 11826.64 |
| 50877.5 | 20.6589 | 0.875217 | 76.6434 | 1.75079 | 15.9953 | 0.249619 | 440.078 | 88.8348 | 0.636431 | 109.904 | 62.1622 | 0.685401 | 137.149 | 262.561 | 88.9478 | 247.2906 | 14847.71 |
| 27202.4 | 25.4015 | 0.936942 | 108.764 | 1.09194 | 10.047 | 0.424184 | 79.3346 | 88.9002 | 0.533093 | 108.164 | 35.9929 | 0.640126 | 31.9474 | 60.5236 | 56.3467 | 154.7809 | 10413.69 |
| 44140.3 | 20.3329 | 0.892781 | 152.987 | 1.11385 | 97.8451 | 0.556866 | 153.885 | 62.0713 | 0.635616 | 487.061 | 82.9755 | 0.811497 | 3.92761 | 76.9391 | 266.953 | 121.6779 | 8360.09 |
| 55299.3 | 21.9145 | 0.863691 | 92.7001 | 0.286279 | 49.3144 | 0.29923 | 439.874 | 14.4768 | 0.697291 | 516.658 | 58.3719 | 0.526647 | 25.8461 | 279.488 | 455.893 | 299.0859 | 18998.8 |
| 45947.4 | 14.2633 | 0.888066 | 22.4329 | 0.436199 | 22.9651 | 0.237791 | 386.04 | 83.3052 | 0.686772 | 453.903 | 29.1376 | 0.681004 | 33.3405 | 311.132 | 95.125 | 227.044 | 14407.09 |
| 31656.1 | 29.169 | 0.925335 | 52.935 | 3.14834 | 50.0132 | 0.397379 | 463.04 | 33.2112 | 0.428447 | 515.368 | 53.5813 | 0.656813 | 95.7054 | 248.439 | 148.652 | 196.6044 | 14461.3 |
| 48899.1 | 20.0534 | 0.880375 | 42.1985 | 0.543586 | 86.5308 | 0.347489 | 407.169 | 55.4054 | 0.381353 | 363.756 | 95.1872 | 0.827368 | 14.8317 | 341.254 | 212.657 | 255.6307 | 18522.67 |
| 44177 | 18.5638 | 0.892684 | 158.159 | 0.168952 | 53.703 | 0.68895 | 156.362 | 55.5596 | 0.344769 | 166.49 | 89.949 | 0.834434 | 2.04438 | 61.3282 | 110.024 | 200.8383 | 12454.02 |
| 60862.9 | 17.2989 | 0.849184 | 114.017 | 0.340851 | 28.0096 | 0.613986 | 419.811 | 87.6104 | 0.685967 | 84.339 | 53.8045 | 0.992648 | 15.4626 | 327.082 | 56.1883 | 92.5805 | 5312.581 |
| 22347.2 | 31.0736 | 0.949606 | 60.1745 | 1.4729 | 93.1766 | 0.466471 | 263.979 | 66.4677 | 0.635341 | 474.628 | 24.5817 | 0.99859 | 49.6176 | 234.261 | 472.804 | 70.18323 | 6049.245 |
| 40296.6 | 17.4218 | 0.902799 | 38.9069 | 1.35422 | 23.3088 | 0.439164 | 339.697 | 5.29571 | 0.886495 | 287.105 | 9.38069 | 0.302955 | 75.7054 | 172.701 | 60.9034 | 192.1939 | 12461.78 |
| 45327.2 | 21.8583 | 0.889688 | 156.462 | 1.25549 | 59.9976 | 0.44407 | 293.367 | 39.2969 | 0.646966 | 145.923 | 61.724 | 0.852189 | 81.3021 | 246.419 | 107.933 | 137.8606 | 9161.416 |
| 22621.8 | 29.2497 | 0.948888 | 162.725 | 2.07107 | 10.0576 | 0.501 | 155.016 | 35.2938 | 0.591406 | 468.846 | 98.7576 | 0.399498 | 50.3024 | 150.412 | 270.292 | 203.9657 | 14079.17 |
| 64796.6 | 21.1188 | 0.838931 | 155.783 | 1.79417 | 99.4424 | 0.603317 | 203.675 | 30.9139 | 0.74986 | 187.258 | 1.2837 | 0.337021 | 75.4933 | 132.115 | 50.5309 | 255.9442 | 15470.99 |
| 57369 | 22.3217 | 0.858296 | 99.9875 | 1.0583 | 97.2289 | 0.582329 | 483.881 | 11.7795 | 0.820195 | 462.26 | 45.7224 | 0.608884 | 41.108 | 467.776 | 195.441 | 129.2947 | 8239.233 |
| 51099.5 | 19.1783 | 0.874638 | 88.2351 | 0.798538 | 4.67838 | 0.439122 | 442.678 | 54.2884 | 0.454376 | 327.506 | 58.3909 | 0.70747 | 46.6951 | 184.56 | 130.96 | 194.8987 | 11238.16 |
| 67435.5 | 13.3958 | 0.832048 | 81.9171 | 2.46442 | 1.36583 | 0.388446 | 425.882 | 53.1512 | 0.675419 | 270.557 | 8.35912 | 0.303363 | 134.361 | 118.191 | 264.145 | 381.3004 | 20119.99 |
| 26940.6 | 15.866 | 0.937617 | 143.009 | 1.51427 | 75.557 | 0.190886 | 430.228 | 41.4309 | 0.667803 | 401.018 | 53.5117 | 0.91498 | 142.495 | 137.02 | 356.996 | 220.594 | 18193.8 |
| 56686.2 | 13.4971 | 0.860071 | 106.762 | 1.28503 | 84.1301 | 0.472745 | 433.377 | 52.0317 | 0.621538 | 465.033 | 50.9428 | 0.297778 | 118.487 | 111.247 | 174.846 | 359.281 | 23465.54 |
| 50349.2 | 24.6308 | 0.876598 | 54.975 | 0.546161 | 63.62 | 0.403785 | 156.296 | 41.2784 | 0.690721 | 287.397 | 93.9438 | 0.454735 | 44.5264 | 97.5227 | 248.605 | 223.0378 | 14943.06 |
| 23758.6 | 27.2512 | 0.945922 | 129.437 | 1.5549 | 88.1408 | 0.383423 | 341.839 | 36.2986 | 0.37864 | 505.347 | 14.4296 | 0.697779 | 49.5092 | 338.265 | 502.253 | 227.8272 | 19197.89 |
| 20589.7 | 19.7441 | 0.954176 | 35.6032 | 3.33717 | 64.6419 | 0.263796 | 447.194 | 13.1954 | 0.621563 | 249.951 | 24.9092 | 0.467723 | 135.23 | 61.5333 | 113.419 | 248.8147 | 21550.55 |
| 35286.9 | 19.035 | 0.915861 | 116.334 | 0.551685 | 55.2022 | 0.461579 | 214.172 | 6.92819 | 0.345043 | 200.62 | 10.0254 | 0.747152 | 52.7638 | 192.611 | 59.2104 | 221.0331 | 15630 |
| 54062 | 18.1232 | 0.866914 | 99.2204 | 3.76743 | 17.898 | 0.470488 | 343.416 | 86.7692 | 0.883045 | 53.8844 | 22.7322 | 0.998771 | 165.278 | 77.2817 | 44.9012 | 69.35565 | 4190.119 |
| 29986.2 | 18.7802 | 0.929679 | 102.342 | 0.918672 | 84.9376 | 0.421702 | 190.991 | 1.90751 | 0.992449 | 430.504 | 63.901 | 0.849507 | 42.4611 | 115.419 | 418.358 | 66.74947 | 5457.588 |
| 50529.1 | 16.7164 | 0.876123 | 64.1144 | 0.117667 | 62.3391 | 0.32447 | 153.941 | 94.4976 | 0.926176 | 97.7219 | 67.4695 | 0.669352 | 3.69136 | 88.2682 | 46.3609 | 163.272 | 10888.83 |
| 53797.7 | 16.5253 | 0.867602 | 158.279 | 3.13051 | 57.6221 | 0.598218 | 308.765 | 44.151 | 0.941132 | 199.882 | 61.9812 | 0.737517 | 127.408 | 76.7078 | 181.636 | 87.40015 | 5352.427 |
| 63156.4 | 18.0314 | 0.843205 | 72.5086 | 0.600055 | 34.2871 | 0.178614 | 333.077 | 25.7773 | 0.635793 | 319.344 | 45.2226 | 0.901957 | 6.76681 | 278.262 | 184.858 | 298.4752 | 18136.58 |
| 38371.5 | 24.2918 | 0.907823 | 153.767 | 3.72359 | 93.3729 | 0.535289 | 369.106 | 62.5404 | 0.949569 | 95.3698 | 83.8638 | 0.908872 | 29.3014 | 83.7965 | 67.783 | 65.72162 | 4750.111 |
| 25567.4 | 21.3302 | 0.941201 | 146.738 | 1.74976 | 43.3577 | 0.43053 | 321.865 | 23.9148 | 0.801987 | 513.474 | 37.7929 | 0.902619 | 167.431 | 240.508 | 371.085 | 75.7078 | 5749.257 |
| 32963.6 | 13.811 | 0.921914 | 56.6346 | 2.04974 | 31.0048 | 0.131916 | 401.915 | 92.5699 | 0.66355 | 88.7963 | 41.8714 | 0.938193 | 119.597 | 50.5627 | 88.7951 | 276.1879 | 19764.43 |
| 23723.3 | 16.7283 | 0.946005 | 41.1309 | 1.27895 | 41.1307 | 0.368651 | 239.229 | 57.0002 | 0.839456 | 96.3852 | 66.8989 | 0.882852 | 123.909 | 123.26 | 80.9406 | 75.35461 | 5812.606 |
| 59352.7 | 21.158 | 0.853123 | 92.2043 | 1.41426 | 47.5719 | 0.270351 | 130.67 | 44.4526 | 0.809038 | 343.742 | 80.612 | 0.446874 | 37.3652 | 117.938 | 268.285 | 310.4759 | 19615.39 |
| 56657.6 | 20.4295 | 0.860149 | 148.635 | 2.54562 | 18.0581 | 0.664623 | 458.922 | 38.6634 | 0.773236 | 465.358 | 49.2337 | 0.635546 | 246.824 | 246.213 | 353.215 | 144.4684 | 8201.428 |
| 29983.3 | 19.0761 | 0.929687 | 28.0969 | 2.19684 | 6.84645 | 0.517196 | 384.167 | 77.5329 | 0.980434 | 441.472 | 31.7715 | 0.605288 | 14.8848 | 103.819 | 120.961 | 82.11459 | 5367.265 |
| 27721.8 | 19.2444 | 0.935583 | 47.4204 | 0.987364 | 29.5992 | 0.405353 | 326.17 | 96.2821 | 0.327486 | 455.765 | 0.785775 | 0.588488 | 42.6001 | 65.535 | 64.317 | 261.7348 | 18621.62 |
| 31887.8 | 27.4173 | 0.924729 | 130.273 | 0.856811 | 50.0368 | 0.242106 | 276.8 | 31.5192 | 0.704829 | 279.803 | 61.2114 | 0.687582 | 18.5663 | 193.78 | 184.725 | 229.9056 | 16932.19 |
| 35808.2 | 24.0409 | 0.914505 | 82.2855 | 2.05 | 4.86288 | 0.3644 | 389.808 | 85.3889 | 0.881235 | 250.173 | 36.9627 | 0.594975 | 121.827 | 232.866 | 79.4994 | 122.003 | 7690.67 |
| 79030.2 | 13.3563 | 0.801821 | 21.7991 | 1.4093 | 74.6672 | 0.389756 | 89.0291 | 35.7586 | 0.89905 | 222.463 | 4.69793 | 0.821948 | 130.195 | 67.7383 | 76.1495 | 120.8093 | 7475.464 |
| 73276.6 | 16.7024 | 0.816822 | 107 | 2.69798 | 76.8176 | 0.4651 | 67.4042 | 92.6073 | 0.786063 | 361.421 | 66.0592 | 0.526129 | 160.525 | 50.2445 | 187.171 | 186.0217 | 11229.8 |
| 27072.5 | 22.4365 | 0.937278 | 128.937 | 2.15262 | 96.7497 | 0.268756 | 368.88 | 28.7872 | 0.818302 | 392.237 | 16.8159 | 0.995329 | 2.84898 | 240.74 | 284.292 | 115.1431 | 10173.68 |
| 33173.3 | 14.7946 | 0.921368 | 42.9753 | 0.641566 | 32.8513 | 0.413266 | 209.363 | 9.25917 | 0.520453 | 494.128 | 82.538 | 0.692826 | 12.8005 | 165.069 | 173.225 | 144.6072 | 10115.65 |
| 28865.7 | 26.0534 | 0.932606 | 159.749 | 2.62116 | 83.4627 | 0.331521 | 419.041 | 29.6514 | 0.634576 | 78.9559 | 75.8298 | 0.546483 | 146.367 | 378.683 | 46.2612 | 232.5871 | 18477.13 |
| 46603.8 | 23.743 | 0.886361 | 94.8565 | 2.16102 | 87.404 | 0.464179 | 447.364 | 4.36061 | 0.851426 | 314.667 | 86.5875 | 0.536644 | 170.834 | 77.523 | 303.019 | 126.2439 | 8982.214 |
| 42066 | 23.4091 | 0.898191 | 56.2632 | 3.17457 | 41.5477 | 0.470782 | 253.386 | 39.1715 | 0.535804 | 465.229 | 8.08347 | 0.980649 | 171.764 | 170.62 | 338.968 | 96.01114 | 6480.989 |
| 45945.9 | 26.4803 | 0.888079 | 125.8 | 0.929754 | 40.4968 | 0.510661 | 271.822 | 83.1537 | 0.525573 | 371.507 | 92.4359 | 0.492523 | 45.4039 | 150.859 | 327.638 | 240.263 | 15043.89 |
| 39831.9 | 25.093 | 0.904017 | 34.1169 | 2.43199 | 4.26355 | 0.458908 | 272.244 | 20.9303 | 0.697181 | 382.544 | 93.9144 | 0.596195 | 79.12 | 117.191 | 134.448 | 123.7222 | 7627.57 |
| 29592.2 | 25.776 | 0.930712 | 67.3302 | 0.544292 | 31.5991 | 0.388922 | 333.505 | 40.1232 | 0.458936 | 175.426 | 2.34609 | 0.339224 | 35.8548 | 70.1498 | 150.095 | 348.6204 | 24686.55 |
| 50514.7 | 18.718 | 0.876162 | 143.224 | 2.1128 | 68.9354 | 0.327038 | 145.758 | 28.7473 | 0.515297 | 163.262 | 80.5572 | 0.708176 | 62.5238 | 45.8973 | 115.273 | 266.8035 | 18078.67 |
| 46318.1 | 14.2003 | 0.8871 | 127.507 | 0.541711 | 13.1665 | 0.422049 | 390.994 | 82.7224 | 0.7904 | 376.61 | 35.8933 | 0.976222 | 35.6078 | 181.009 | 81.7978 | 98.6467 | 6025.865 |
| 74188.5 | 17.2693 | 0.814445 | 55.2142 | 3.30126 | 93.5492 | 0.474736 | 121.591 | 61.6578 | 0.973083 | 271.835 | 71.437 | 0.566603 | 22.4419 | 114.725 | 121.076 | 138.8115 | 8671.7 |
| 35083.1 | 26.8602 | 0.916398 | 49.1312 | 0.101139 | 80.1913 | 0.291429 | 339.868 | 51.6712 | 0.937795 | 352.368 | 22.3863 | 0.380623 | 3.94162 | 177.731 | 254.135 | 255.9688 | 19861.31 |
| 63737.6 | 15.5467 | 0.841689 | 44.0272 | 0.541554 | 63.5329 | 0.262499 | 221.488 | 37.4706 | 0.650603 | 473.532 | 43.1362 | 0.791472 | 47.3827 | 189.211 | 358.734 | 228.647 | 14950.13 |
| 54230 | 14.6908 | 0.866474 | 159.124 | 0.292368 | 73.4324 | 0.370985 | 428.877 | 1.43407 | 0.936735 | 285.701 | 82.661 | 0.769949 | 2.68686 | 159.374 | 267.401 | 159.2914 | 10292.85 |
| 36711.7 | 28.7305 | 0.912155 | 92.492 | 3.33519 | 96.161 | 0.512475 | 373.497 | 6.95149 | 0.918629 | 231.494 | 38.8474 | 0.730556 | 155.132 | 226.393 | 200.582 | 70.43104 | 5269.946 |
| 78618.8 | 15.1098 | 0.802894 | 47.5093 | 2.18423 | 67.7796 | 0.558206 | 299.328 | 90.9724 | 0.627167 | 322.629 | 43.7507 | 0.498483 | 191.268 | 223.373 | 283.132 | 315.9341 | 17452.45 |
| 53500.2 | 20.0061 | 0.86838 | 148.485 | 2.59681 | 98.1735 | 0.55222 | 297.327 | 54.2068 | 0.903447 | 334.627 | 48.297 | 0.938631 | 138.021 | 230.961 | 271.728 | 72.1217 | 4834.633 |
| 40439.9 | 27.3621 | 0.902434 | 56.1072 | 2.46768 | 83.0303 | 0.226362 | 401.754 | 86.0556 | 0.70462 | 180.403 | 60.8969 | 0.601359 | 82.4302 | 172.111 | 58.6972 | 277.2948 | 21487.24 |
| 60187.4 | 19.7901 | 0.850946 | 36.8221 | 0.62075 | 84.1028 | 0.549913 | 381.018 | 90.3855 | 0.517685 | 391.181 | 27.9266 | 0.520675 | 23.8169 | 167.523 | 382.073 | 323.0112 | 19830.05 |
| 71560.7 | 13.9491 | 0.821294 | 116.126 | 2.18028 | 68.5618 | 0.329855 | 398.109 | 4.3931 | 0.568863 | 479.897 | 13.2664 | 0.807315 | 78.2441 | 145.653 | 96.9586 | 221.4156 | 13906.42 |
| 29120.9 | 18.412 | 0.931935 | 161.878 | 3.48768 | 36.2333 | 0.62497 | 186.589 | 46.7304 | 0.904207 | 512.354 | 11.1933 | 0.326391 | 46.1558 | 123.298 | 446.994 | 205.1042 | 13745.25 |
| 28119.3 | 29.5527 | 0.934556 | 55.0369 | 1.11038 | 99.7358 | 0.474641 | 166.142 | 73.431 | 0.948734 | 353.15 | 0.806489 | 0.467316 | 15.5589 | 120.609 | 168.177 | 112.9331 | 9125.206 |
| 52300.2 | 23.4281 | 0.871511 | 123.406 | 3.64314 | 57.697 | 0.446466 | 205.577 | 70.8046 | 0.974468 | 65.055 | 59.2821 | 0.413002 | 105.183 | 86.0535 | 62.8817 | 166.5511 | 10716.89 |
| 21963.2 | 31.6633 | 0.950608 | 165.636 | 1.86412 | 32.3035 | 0.617386 | 258.749 | 62.216 | 0.728894 | 490.781 | 83.0685 | 0.455665 | 88.2888 | 136.869 | 342.949 | 128.1104 | 9028.523 |
| 41214.6 | 15.8463 | 0.900405 | 170.358 | 0.456524 | 82.3163 | 0.599932 | 304.121 | 7.12736 | 0.944221 | 330.078 | 32.3881 | 0.994726 | 33.4708 | 280.062 | 258.841 | 70.79626 | 4893.491 |
| 36866.3 | 24.6656 | 0.911748 | 58.5969 | 0.154613 | 3.43637 | 0.339958 | 433.166 | 5.00174 | 0.454771 | 324.63 | 12.2018 | 0.678553 | 4.01667 | 152.303 | 162.758 | 223.2109 | 13963.67 |
| 67011.1 | 16.6173 | 0.833155 | 39.7729 | 1.78873 | 22.8158 | 0.470053 | 286.083 | 47.3575 | 0.948096 | 248.941 | 99.8811 | 0.673063 | 6.56282 | 259.056 | 223.18 | 109.1239 | 6201.223 |
| 50657.3 | 20.6369 | 0.875792 | 102.244 | 2.95684 | 56.6107 | 0.628409 | 254.871 | 99.473 | 0.814986 | 507.727 | 52.9453 | 0.860113 | 127.648 | 227.113 | 463.158 | 99.28752 | 6083.287 |
| 57086.8 | 16.1715 | 0.859027 | 166.448 | 1.64659 | 37.6798 | 0.603605 | 173.795 | 20.4412 | 0.691786 | 345.266 | 50.6376 | 0.734622 | 14.8786 | 122.977 | 240.56 | 120.4758 | 7137.46 |
| 21598.1 | 21.7486 | 0.951549 | 64.9049 | 0.788033 | 22.8128 | 0.484161 | 336.188 | 34.8434 | 0.493134 | 150.618 | 46.2583 | 0.876692 | 57.6466 | 317.522 | 129.523 | 87.00134 | 6389.398 |
| 58903 | 20.9323 | 0.854296 | 63.8099 | 0.367569 | 70.0913 | 0.382971 | 184.497 | 30.8981 | 0.691054 | 123.278 | 39.8114 | 0.83042 | 18.4658 | 121.054 | 64.9469 | 139.7418 | 9260.939 |
| 37441.8 | 26.9983 | 0.910249 | 137.325 | 0.992622 | 25.0243 | 0.519742 | 117.626 | 35.316 | 0.872808 | 151.244 | 56.2566 | 0.456282 | 16.537 | 91.6577 | 69.2158 | 139.6693 | 9033.269 |
| 48798.4 | 13.6583 | 0.880634 | 70.3312 | 2.24797 | 50.4789 | 0.399728 | 386.483 | 47.9988 | 0.78787 | 415.92 | 5.83577 | 0.276044 | 15.96 | 198.972 | 74.4169 | 307.4596 | 20210.67 |
| 51684.5 | 16.7871 | 0.873111 | 22.3953 | 0.722594 | 19.659 | 0.200359 | 148.218 | 82.7907 | 0.740178 | 201.011 | 24.0772 | 0.856201 | 56.0132 | 98.6112 | 58.6424 | 210.3049 | 12870.02 |
| 38194.9 | 17.0059 | 0.908278 | 154.823 | 0.721795 | 44.9294 | 0.472555 | 338.045 | 7.5799 | 0.361201 | 124.469 | 3.55591 | 0.546252 | 67.3992 | 317.664 | 116.299 | 332.7944 | 22151.37 |
| 33908.7 | 20.4486 | 0.919454 | 91.3872 | 2.55601 | 81.7948 | 0.48272 | 165.008 | 40.0166 | 0.822005 | 334.305 | 90.678 | 0.711094 | 75.5592 | 47.3036 | 247.333 | 85.77044 | 6379.565 |
| 26120.4 | 20.5829 | 0.939758 | 141.582 | 2.08403 | 10.5043 | 0.617225 | 246.046 | 61.8298 | 0.921832 | 346.425 | 74.0036 | 0.752447 | 63.4472 | 174.197 | 316.176 | 69.73733 | 4685.626 |
| 34111.3 | 24.8216 | 0.91893 | 98.8985 | 1.79509 | 20.7259 | 0.145149 | 141.4 | 48.7015 | 0.853527 | 255.605 | 24.1493 | 0.919881 | 109.417 | 50.096 | 175.309 | 242.431 | 16572.21 |
| 29676.4 | 31.7407 | 0.930499 | 156.949 | 1.01764 | 84.492 | 0.533202 | 138.926 | 53.663 | 0.791998 | 244.316 | 58.7274 | 0.332843 | 20.8425 | 78.1782 | 168.311 | 216.1237 | 15846.96 |
| 49874.1 | 16.5709 | 0.877831 | 34.9378 | 2.71576 | 67.3881 | 0.510982 | 346.998 | 5.21271 | 0.659479 | 413.155 | 20.6688 | 0.478509 | 225.45 | 94.7278 | 389.882 | 181.2166 | 11686.32 |
| 35437.8 | 22.7498 | 0.91547 | 81.8482 | 2.01958 | 75.978 | 0.367109 | 184.839 | 84.0271 | 0.899988 | 183.983 | 28.2428 | 0.466421 | 166.584 | 168.724 | 63.6517 | 163.0188 | 12313.82 |
| 32344.3 | 20.8938 | 0.923533 | 66.6105 | 3.05457 | 60.4832 | 0.429305 | 341.272 | 87.186 | 0.632789 | 69.1204 | 36.5867 | 0.722738 | 22.9902 | 249.475 | 58.046 | 118.3021 | 8790.813 |
| 23464.9 | 27.7482 | 0.946688 | 142.286 | 1.49759 | 99.5025 | 0.439748 | 144.327 | 51.0935 | 0.592912 | 480.501 | 84.6375 | 0.749429 | 75.2335 | 85.7776 | 298.996 | 131.3208 | 10881.11 |
| 38593.2 | 13.0991 | 0.907238 | 36.6397 | 2.22579 | 97.3205 | 0.242051 | 203.66 | 77.2035 | 0.449828 | 422.031 | 82.3913 | 0.838586 | 164.976 | 176.641 | 333.336 | 280.6251 | 22816.33 |
| 42357.8 | 28.0568 | 0.897435 | 65.1608 | 0.977313 | 72.221 | 0.453066 | 222.131 | 53.6902 | 0.651695 | 331.734 | 8.46278 | 0.652438 | 28.9552 | 164.9 | 262.031 | 132.9527 | 9515.744 |
| 77835.8 | 15.5132 | 0.804935 | 124.401 | 3.67965 | 68.9618 | 0.396574 | 410.824 | 26.3746 | 0.902871 | 339.872 | 34.779 | 0.506568 | 102.549 | 252.998 | 110.529 | 192.5387 | 11632.45 |
| 68311.9 | 16.8826 | 0.829765 | 28.7208 | 3.36034 | 99.6842 | 0.305633 | 463.986 | 58.2449 | 0.965379 | 466.179 | 45.7743 | 0.810261 | 23.107 | 294.199 | 120.464 | 143.0805 | 9877.793 |
| 37699 | 23.0927 | 0.909575 | 136.031 | 1.35332 | 72.9092 | 0.627693 | 417.837 | 58.1371 | 0.94943 | 275.345 | 57.4123 | 0.820925 | 118.341 | 177.791 | 178.274 | 68.7238 | 4632.819 |
| 60404 | 18.9416 | 0.850381 | 139.284 | 0.296131 | 92.2446 | 0.452963 | 85.3973 | 42.9693 | 0.930469 | 340.593 | 21.5137 | 0.504416 | 2.14321 | 61.1711 | 288.214 | 199.3481 | 12710.2 |
| 44541.9 | 21.9318 | 0.891735 | 81.3493 | 1.32934 | 65.6033 | 0.465993 | 292.947 | 20.0812 | 0.392158 | 452.505 | 28.8219 | 0.387256 | 67.9827 | 75.2823 | 151.752 | 355.5405 | 24327.82 |
| 23986.4 | 25.7163 | 0.945326 | 132.59 | 0.438386 | 54.8152 | 0.183687 | 286.506 | 62.7397 | 0.76383 | 174.72 | 61.6599 | 0.9136 | 30.8481 | 41.8717 | 152.595 | 239.7438 | 18866.82 |
| 38736.1 | 26.8479 | 0.906875 | 28.1896 | 2.16499 | 37.8792 | 0.399019 | 213.428 | 6.90995 | 0.546695 | 135.968 | 47.7078 | 0.462993 | 45.4475 | 185.87 | 134.279 | 230.0397 | 15674.83 |
| 22566.8 | 26.2964 | 0.949028 | 39.6893 | 3.66569 | 43.9685 | 0.368075 | 128.193 | 22.1855 | 0.489625 | 445.057 | 74.859 | 0.79858 | 160.663 | 85.0223 | 231.936 | 134.5552 | 10557.67 |
| 25200.2 | 24.903 | 0.942161 | 156.485 | 1.86666 | 63.4258 | 0.471519 | 110.998 | 44.7774 | 0.536159 | 445.524 | 35.4089 | 0.48877 | 137.53 | 67.1993 | 100.913 | 204.4285 | 15508.4 |
| 45020.9 | 18.7051 | 0.890484 | 48.6122 | 1.03411 | 66.8333 | 0.262894 | 172.71 | 50.0105 | 0.566381 | 405.457 | 43.0395 | 0.738788 | 0.756575 | 143.721 | 185.667 | 238.2478 | 17328.49 |
| 22533 | 18.2708 | 0.949109 | 26.9405 | 1.79287 | 87.9617 | 0.158618 | 143.516 | 77.042 | 0.960863 | 250.672 | 36.0222 | 0.845803 | 40.0999 | 70.7402 | 226.11 | 208.4217 | 19080.92 |
| 41041.5 | 29.0252 | 0.900867 | 97.8285 | 0.960301 | 67.7393 | 0.345209 | 145.463 | 77.6625 | 0.811621 | 395.048 | 22.6567 | 0.893596 | 21.2846 | 131.825 | 294.065 | 110.3022 | 8031.602 |
| 40926.7 | 28.774 | 0.901166 | 83.3308 | 2.472 | 24.5798 | 0.45496 | 331.707 | 87.1309 | 0.649165 | 386.945 | 40.1114 | 0.395955 | 108.736 | 230.997 | 157.842 | 216.9181 | 13739.07 |
| 32094 | 16.6662 | 0.924183 | 108.277 | 1.18836 | 84.1887 | 0.372209 | 275.75 | 10.8841 | 0.637075 | 421.925 | 70.2804 | 0.465437 | 104.225 | 173.724 | 224.672 | 220.864 | 17458.22 |
| 62511.2 | 15.8757 | 0.844886 | 58.3495 | 2.34588 | 80.6276 | 0.214262 | 77.3988 | 60.9456 | 0.992115 | 207.727 | 27.4073 | 0.563374 | 63.6128 | 36.3451 | 108.791 | 267.1242 | 18433.48 |
| 34972.9 | 23.1135 | 0.916682 | 155.779 | 0.619327 | 90.0358 | 0.212531 | 351.467 | 48.2666 | 0.871977 | 238.534 | 82.2859 | 0.734398 | 46.8256 | 337.781 | 173.909 | 250.0571 | 19275.35 |
| 52788.6 | 13.4489 | 0.870231 | 171.24 | 0.425516 | 64.4304 | 0.246025 | 324.84 | 84.5948 | 0.975092 | 134.969 | 55.5355 | 0.911804 | 28.3126 | 97.1116 | 49.8911 | 280.9974 | 18019.03 |
| 62808.6 | 15.5333 | 0.844111 | 148.692 | 1.81828 | 54.398 | 0.346234 | 277.708 | 25.0994 | 0.512941 | 373.797 | 21.7877 | 0.865055 | 59.1264 | 263.72 | 263.04 | 233.6159 | 14381.24 |
| 65862.8 | 14.2364 | 0.836148 | 89.1047 | 0.872801 | 70.8913 | 0.510584 | 445.847 | 74.7806 | 0.986533 | 247.564 | 36.8196 | 0.43866 | 18.9695 | 310.464 | 208.041 | 155.8966 | 9428.96 |
| 22295.3 | 27.0862 | 0.949736 | 146.14 | 0.922092 | 75.7517 | 0.5719 | 183.021 | 92.1463 | 0.893136 | 142.289 | 37.8411 | 0.178543 | 79.23 | 72.5642 | 57.2901 | 307.8633 | 22754.58 |
| 75908.5 | 17.1151 | 0.809961 | 88.2241 | 0.417262 | 37.3134 | 0.422529 | 342.544 | 36.3741 | 0.470326 | 210.513 | 82.8854 | 0.933566 | 12.4952 | 297.939 | 190.674 | 202.5312 | 11335.81 |
| 39680.1 | 19.6734 | 0.904408 | 94.1373 | 2.34271 | 34.3866 | 0.242347 | 229.75 | 74.9334 | 0.741146 | 119.379 | 2.12024 | 0.703637 | 159.015 | 219.03 | 111.775 | 191.1447 | 13107.34 |
| 25989.7 | 28.2314 | 0.940106 | 110.173 | 0.944175 | 74.7814 | 0.549884 | 130.027 | 15.3888 | 0.74737 | 309.879 | 55.5316 | 0.323675 | 68.5333 | 122.207 | 269.304 | 177.4547 | 13208.94 |
| 38252.2 | 13.0575 | 0.908127 | 60.9512 | 0.581597 | 83.2153 | 0.194555 | 254.021 | 13.4578 | 0.662278 | 210.612 | 7.88264 | 0.81457 | 54.5191 | 145.531 | 185.798 | 232.679 | 18959.47 |
| 67672.3 | 14.6863 | 0.831431 | 122.827 | 1.65804 | 15.7659 | 0.313357 | 220.025 | 8.36194 | 0.537341 | 395.788 | 25.2942 | 0.719822 | 158.194 | 103.232 | 124.898 | 271.9753 | 15044.31 |
| 52183.8 | 22.0002 | 0.871813 | 150.802 | 2.04389 | 52.8184 | 0.401255 | 254.498 | 45.5949 | 0.774436 | 380.993 | 74.9406 | 0.705263 | 71.2403 | 50.8579 | 150.763 | 154.8557 | 9895.417 |
| 69643.4 | 14.7446 | 0.826292 | 39.277 | 0.320376 | 52.2635 | 0.367231 | 197.712 | 35.6205 | 0.895096 | 487.71 | 93.6565 | 0.428694 | 8.96227 | 147.658 | 60.5977 | 233.52 | 14073.34 |
| 29775.2 | 24.2024 | 0.930233 | 153.04 | 0.280797 | 67.8563 | 0.421427 | 294.243 | 22.3839 | 0.647929 | 245.842 | 37.5685 | 0.868018 | 12.0941 | 68.02 | 123.229 | 132.2554 | 9822.784 |
| 87671.9 | 13.1532 | 0.779292 | 76.3944 | 0.354588 | 54.9632 | 0.352063 | 397.206 | 63.6259 | 0.694785 | 204.245 | 68.876 | 0.719378 | 13.8189 | 322.911 | 136.838 | 231.9074 | 13067.24 |
| 62366.9 | 17.1144 | 0.845263 | 124.744 | 0.896454 | 8.79737 | 0.348659 | 330.193 | 74.594 | 0.813935 | 275.916 | 27.9921 | 0.319794 | 6.9799 | 286.651 | 126.358 | 390.8448 | 21427.77 |
| 27577 | 24.6941 | 0.935965 | 133.42 | 0.635222 | 37.7357 | 0.529974 | 119.664 | 99.6127 | 0.724813 | 127.819 | 87.2845 | 0.526801 | 50.656 | 44.2136 | 84.7507 | 141.5305 | 9748.382 |
| 21958.1 | 22.8423 | 0.950611 | 124.966 | 1.73591 | 33.4245 | 0.508529 | 194.113 | 87.7304 | 0.735851 | 154.997 | 19.2675 | 0.410691 | 89.0639 | 112.771 | 116.9 | 145.0578 | 10500.67 |
| 28221.1 | 13.3279 | 0.934277 | 33.7522 | 1.25794 | 70.4673 | 0.31794 | 285.493 | 11.8696 | 0.636806 | 205.786 | 12.7026 | 0.748354 | 119.338 | 184.598 | 55.9726 | 136.6815 | 11309.38 |
| 49677.4 | 21.2717 | 0.878347 | 120.698 | 2.95291 | 8.18014 | 0.205806 | 223.242 | 36.5336 | 0.719659 | 328.902 | 45.798 | 0.968028 | 135.244 | 123.244 | 143.163 | 182.8512 | 10867.95 |
| 65995.8 | 14.2608 | 0.835801 | 26.0588 | 0.185505 | 89.3309 | 0.274054 | 450.256 | 17.3069 | 0.593192 | 372.119 | 84.3519 | 0.693815 | 17.6501 | 183.518 | 362.3 | 286.3859 | 19624.42 |
| 37468.2 | 26.9337 | 0.91018 | 134.185 | 1.13799 | 73.239 | 0.51777 | 121.794 | 69.7513 | 0.991477 | 292.697 | 20.4111 | 0.90536 | 49.8836 | 109.41 | 157.654 | 66.21121 | 4765.564 |
| 71675.6 | 14.1046 | 0.820994 | 51.9113 | 2.98248 | 8.89801 | 0.384038 | 242.016 | 33.7218 | 0.657037 | 228.941 | 30.1641 | 0.888038 | 40.1108 | 77.2468 | 181.569 | 138.6636 | 7509.739 |
| 35033.6 | 23.2367 | 0.916524 | 143.263 | 2.49571 | 85.31 | 0.597344 | 483.601 | 61.1945 | 0.569798 | 487.011 | 19.7231 | 0.867979 | 83.1387 | 213.318 | 350.266 | 104.3523 | 7333.229 |
| 33023.3 | 28.7052 | 0.92177 | 96.7729 | 1.00302 | 55.4935 | 0.246661 | 134.832 | 36.2422 | 0.979328 | 164.588 | 21.209 | 0.33334 | 57.3012 | 99.0653 | 132.053 | 303.5355 | 22821.91 |
| 40550 | 17.5574 | 0.902139 | 43.9761 | 3.53324 | 66.8023 | 0.25563 | 471.912 | 77.9858 | 0.918365 | 459.957 | 65.1896 | 0.691056 | 145.664 | 117.375 | 443.02 | 160.7972 | 11908.99 |
| 24592.7 | 19.7667 | 0.94374 | 76.3818 | 1.95583 | 30.7738 | 0.482782 | 445.888 | 18.3927 | 0.772041 | 72.5778 | 40.132 | 0.884595 | 22.3781 | 54.0877 | 46.8419 | 57.01898 | 4278.488 |
| 37591.4 | 16.2167 | 0.909851 | 24.2766 | 1.5765 | 49.7383 | 0.273819 | 254.924 | 21.9262 | 0.658815 | 397.949 | 24.0556 | 0.778862 | 149.478 | 130.619 | 48.3927 | 163.5126 | 11965.12 |
| 24854.9 | 20.441 | 0.943058 | 127.224 | 0.250989 | 52.3436 | 0.428675 | 392.407 | 38.2039 | 0.97153 | 398.645 | 0.406257 | 0.927115 | 4.64129 | 119.46 | 374.058 | 73.29249 | 5682.243 |
| 33790.2 | 30.6556 | 0.919773 | 66.5154 | 2.49001 | 88.6143 | 0.335174 | 138.169 | 83.5894 | 0.984094 | 68.839 | 70.9272 | 0.76694 | 54.1687 | 89.2905 | 45.7664 | 103.5318 | 8204.953 |
| 48170.9 | 24.8165 | 0.882277 | 147.16 | 1.75521 | 84.861 | 0.520596 | 177.672 | 8.4349 | 0.720712 | 499.167 | 18.7553 | 0.594509 | 11.6251 | 73.8381 | 483.032 | 140.7956 | 9616.483 |
| 25493.4 | 29.1771 | 0.941401 | 116.754 | 2.203 | 26.2671 | 0.50286 | 461.826 | 76.6321 | 0.944063 | 481.617 | 6.64444 | 0.40429 | 178.483 | 346.292 | 481.54 | 115.7277 | 8075.689 |
| 57675.5 | 21.4479 | 0.857496 | 127.503 | 2.66911 | 91.1901 | 0.534118 | 95.9994 | 81.1858 | 0.705932 | 502.044 | 53.866 | 0.858656 | 142.054 | 81.7481 | 338.915 | 103.3663 | 6547.251 |
| 40001.6 | 26.9002 | 0.903576 | 110.962 | 1.16783 | 30.039 | 0.460571 | 276.755 | 63.0373 | 0.908468 | 267.852 | 51.3025 | 0.357626 | 82.7509 | 211.568 | 169.399 | 184.3485 | 11863.81 |
| 44196.9 | 18.853 | 0.892632 | 129.87 | 1.12549 | 93.5386 | 0.271624 | 227.339 | 72.5711 | 0.71876 | 202.296 | 96.8133 | 0.696969 | 9.3961 | 63.3388 | 200.792 | 237.0665 | 17612.37 |
| 22985.8 | 19.8233 | 0.94793 | 118.801 | 0.282097 | 18.8278 | 0.357288 | 277.774 | 15.0608 | 0.39658 | 305.649 | 34.3523 | 0.657576 | 25.6121 | 104.442 | 176.188 | 251.9487 | 18041.12 |
| 35968.7 | 16.4938 | 0.914082 | 135.123 | 0.692476 | 85.2019 | 0.308979 | 345.822 | 99.5208 | 0.552776 | 455.487 | 88.4617 | 0.54622 | 35.0819 | 147.656 | 357.801 | 331.9337 | 24877.95 |
| 69702.4 | 16.3281 | 0.826139 | 25.3243 | 0.812118 | 57.7954 | 0.33469 | 475.511 | 75.937 | 0.845272 | 448.667 | 0.915177 | 0.655254 | 19.5563 | 303.552 | 264.383 | 181.0592 | 11201.3 |
| 53354.6 | 18.289 | 0.868758 | 89.3224 | 1.9415 | 8.03013 | 0.430191 | 126.762 | 96.4958 | 0.871092 | 480.237 | 55.73 | 0.847886 | 43.1573 | 90.9539 | 318.209 | 90.98163 | 5324.898 |
| 27400.2 | 16.1472 | 0.936419 | 161.882 | 0.602938 | 30.7032 | 0.391081 | 139.182 | 95.5334 | 0.902809 | 282.202 | 94.8775 | 0.475031 | 17.4838 | 45.1216 | 70.0889 | 189.3009 | 12984.75 |
| 37788.5 | 22.4315 | 0.909341 | 153.068 | 2.44156 | 93.8067 | 0.331291 | 304.255 | 17.0824 | 0.99819 | 359.663 | 9.29266 | 0.315294 | 118.436 | 93.819 | 329.654 | 279.2219 | 21469.42 |
| 24217.9 | 31.4012 | 0.944729 | 171.057 | 2.01967 | 5.26924 | 0.348135 | 271.535 | 75.3293 | 0.997816 | 243.348 | 29.8092 | 0.929235 | 151.93 | 203.971 | 95.7794 | 96.03359 | 6592.429 |
| 33341.9 | 25.3221 | 0.920936 | 159.796 | 1.85388 | 98.3262 | 0.288271 | 113.2 | 15.8433 | 0.808073 | 130.165 | 37.7439 | 0.473182 | 0.878278 | 51.9405 | 46.4388 | 268.9433 | 21536.42 |
| 24666.2 | 29.2129 | 0.943558 | 163.526 | 1.23741 | 20.4368 | 0.463381 | 195.727 | 98.6914 | 0.678125 | 505.103 | 72.4437 | 0.399484 | 101.638 | 125.15 | 417.5 | 223.9958 | 15340.03 |
| 45191.1 | 16.4493 | 0.890039 | 117.118 | 0.949328 | 60.1532 | 0.514934 | 373.972 | 14.4597 | 0.408139 | 473.863 | 76.6612 | 0.764688 | 18.3991 | 122.226 | 174.309 | 179.0148 | 11881.02 |
| 29683 | 16.9317 | 0.930468 | 68.1585 | 0.964126 | 11.7836 | 0.476645 | 168.036 | 95.0431 | 0.693237 | 371.724 | 46.5962 | 0.354016 | 86.2643 | 144.902 | 201.138 | 188.3231 | 12269.18 |
| 60370.1 | 19.8092 | 0.85047 | 168.079 | 3.31748 | 57.9234 | 0.546512 | 362.632 | 93.5498 | 0.86169 | 330.366 | 20.4647 | 0.972864 | 88.3755 | 125.819 | 233.282 | 82.29099 | 5050.591 |
| 73874.2 | 17.0467 | 0.815264 | 83.4875 | 2.40668 | 4.59863 | 0.509398 | 399.104 | 7.10495 | 0.591482 | 373.741 | 68.8305 | 0.434736 | 143.523 | 186.721 | 105.633 | 263.2845 | 13684.98 |
| 70561.8 | 16.1621 | 0.823899 | 166.98 | 0.43877 | 17.6082 | 0.431309 | 486.525 | 57.3994 | 0.971859 | 390.217 | 71.4339 | 0.981437 | 32.4773 | 284.22 | 363.955 | 146.0307 | 7946.347 |
| 24290.7 | 15.2854 | 0.944525 | 151.041 | 0.516096 | 37.3757 | 0.34757 | 384.249 | 70.7476 | 0.872237 | 124.675 | 76.7887 | 0.968967 | 23.5982 | 98.2811 | 63.342 | 107.074 | 7822.331 |
| 63384.9 | 19.0687 | 0.84261 | 158.302 | 0.12649 | 39.3931 | 0.590647 | 280.16 | 80.067 | 0.602356 | 269.565 | 28.8049 | 0.691654 | 9.47014 | 147.583 | 187.652 | 201.2554 | 11352.06 |
| 36617.8 | 16.9123 | 0.91239 | 166.321 | 1.28416 | 49.7075 | 0.318789 | 90.3271 | 41.9208 | 0.780056 | 415.776 | 98.1412 | 0.54451 | 96.4628 | 47.7737 | 353.403 | 236.7243 | 16319.87 |
| 59972.6 | 17.2634 | 0.851505 | 113.585 | 1.22234 | 25.5586 | 0.317472 | 466.637 | 40.2883 | 0.484904 | 118.503 | 73.605 | 0.673449 | 67.6977 | 302.906 | 80.9585 | 306.6256 | 17943.2 |
| 23898.6 | 25.2215 | 0.945554 | 77.2858 | 2.08174 | 25.144 | 0.386355 | 349.648 | 61.9451 | 0.835084 | 243.149 | 93.0038 | 0.424661 | 133.82 | 325.432 | 60.4829 | 150.5166 | 10796.06 |
| 60601.5 | 20.7934 | 0.849868 | 142.939 | 0.610966 | 58.7694 | 0.430668 | 195.859 | 80.1113 | 0.653903 | 248.371 | 75.9613 | 0.575058 | 35.2528 | 107.527 | 247.511 | 251.7796 | 15233.97 |
| 79400.9 | 14.3164 | 0.800855 | 62.0984 | 3.02267 | 89.5298 | 0.495666 | 413.929 | 55.4756 | 0.924367 | 372.381 | 35.1023 | 0.63155 | 54.9647 | 261.32 | 246.563 | 124.2241 | 7408.896 |
| 38179.1 | 14.5386 | 0.908318 | 129.387 | 1.2998 | 13.1748 | 0.301033 | 448.666 | 97.1203 | 0.718275 | 438.66 | 25.2502 | 0.700555 | 73.968 | 287.178 | 155.531 | 177.821 | 11290.33 |
| 30594.8 | 25.6334 | 0.928098 | 155.821 | 3.14248 | 45.02 | 0.461315 | 194.24 | 15.5807 | 0.979882 | 238.486 | 16.1666 | 0.9349 | 73.0586 | 124.653 | 51.9449 | 60.12257 | 4493.338 |
| 63021.6 | 13.8982 | 0.843555 | 53.364 | 0.715796 | 45.9665 | 0.176449 | 378.782 | 83.9427 | 0.8099 | 303.526 | 28.1964 | 0.715391 | 66.1213 | 175.461 | 64.4184 | 300.8553 | 18975.63 |
| 36781.2 | 26.4154 | 0.911971 | 48.6697 | 2.19173 | 26.2498 | 0.488253 | 437.839 | 61.9287 | 0.762786 | 511.011 | 46.8831 | 0.878305 | 84.1533 | 345.079 | 440.591 | 72.2021 | 4821.68 |
| 81758.9 | 14.8568 | 0.794708 | 19.31 | 0.270715 | 64.6765 | 0.333797 | 130.735 | 96.5493 | 0.667994 | 237.441 | 49.4961 | 0.640996 | 19.8247 | 108.011 | 194.436 | 258.6508 | 15368.91 |
| 37323 | 14.453 | 0.91055 | 117.845 | 0.362793 | 37.0366 | 0.340587 | 484.919 | 7.60332 | 0.331877 | 305.895 | 10.2215 | 0.74195 | 5.90622 | 330.152 | 177.668 | 333.1976 | 22552.42 |
| 62799.9 | 19.2104 | 0.844135 | 48.338 | 2.1435 | 39.0314 | 0.253595 | 134.834 | 55.4651 | 0.90004 | 210.292 | 65.3013 | 0.738817 | 13.8307 | 106.737 | 115.073 | 184.0379 | 11292.88 |
| 61001.3 | 17.9425 | 0.848823 | 133.985 | 3.78381 | 92.5879 | 0.445139 | 495.374 | 34.429 | 0.674401 | 447.619 | 83.7867 | 0.647758 | 96.5285 | 428.956 | 428.572 | 166.3226 | 11076.84 |
| 63566.9 | 20.0985 | 0.842136 | 155.879 | 0.873201 | 28.742 | 0.446158 | 195.733 | 54.182 | 0.576854 | 247.675 | 25.6683 | 0.522799 | 46.9445 | 186.795 | 187.927 | 302.7885 | 17119.65 |
| 28262.9 | 26.4343 | 0.934178 | 36.8419 | 1.51849 | 0.295528 | 0.498611 | 403.489 | 5.51483 | 0.614152 | 465.587 | 14.6264 | 0.555471 | 17.2134 | 63.7749 | 368.316 | 117.1551 | 7805.197 |
| 31982.7 | 13.4265 | 0.924471 | 71.2705 | 3.39696 | 53.3863 | 0.233166 | 237.543 | 55.1403 | 0.856364 | 395.351 | 36.844 | 0.987568 | 66.1029 | 207.21 | 369.816 | 125.4967 | 9701.164 |
| 22536.6 | 17.2252 | 0.949099 | 90.1444 | 0.429524 | 22.2791 | 0.303425 | 247.305 | 62.879 | 0.674857 | 203.586 | 13.3395 | 0.3888 | 31.534 | 178.886 | 48.6149 | 265.7654 | 19330.72 |
| 85635.9 | 13.2104 | 0.7846 | 16.1974 | 2.09546 | 79.9755 | 0.324983 | 415.182 | 72.0883 | 0.896796 | 138.205 | 96.2227 | 0.672074 | 127.737 | 363.43 | 117.114 | 199.1124 | 12089.93 |
| 26820.1 | 25.81 | 0.937939 | 122.736 | 0.705159 | 72.3015 | 0.552157 | 190.695 | 65.2095 | 0.738665 | 245.551 | 4.25627 | 0.333909 | 40.1076 | 137.422 | 139.905 | 190.2837 | 14102.14 |
| 71021.5 | 16.7657 | 0.822701 | 73.4224 | 1.45623 | 82.6841 | 0.43152 | 352.802 | 37.2027 | 0.558588 | 151.286 | 92.6441 | 0.463211 | 84.9738 | 80.8858 | 104.709 | 301.1478 | 18856.93 |
| 30654.9 | 27.5631 | 0.927943 | 58.2224 | 3.66936 | 22.7657 | 0.473768 | 252.434 | 1.6769 | 0.419362 | 308.848 | 64.5654 | 0.345851 | 155.572 | 113.268 | 162.999 | 298.0949 | 20204.22 |
| 66416.2 | 13.352 | 0.834705 | 76.3678 | 1.32433 | 25.3378 | 0.453067 | 465.575 | 66.2528 | 0.967045 | 452.175 | 60.2488 | 0.432988 | 83.7404 | 299.249 | 156.964 | 169.3396 | 9586.651 |
| 42259.7 | 16.8387 | 0.897681 | 112.344 | 0.659442 | 48.5846 | 0.48171 | 78.1268 | 39.6393 | 0.587277 | 399.32 | 17.5894 | 0.417326 | 33.8382 | 51.8149 | 231.763 | 239.5411 | 15830.5 |
| 34258.7 | 29.9663 | 0.918551 | 108.976 | 2.18812 | 29.5774 | 0.393851 | 474.128 | 97.8499 | 0.595161 | 317.002 | 66.2103 | 0.63018 | 22.489 | 52.2413 | 50.6506 | 163.4078 | 11043.47 |
| 46469.7 | 27.1956 | 0.886714 | 57.8682 | 2.1039 | 39.3205 | 0.447729 | 223.885 | 1.65707 | 0.439847 | 445.153 | 94.6401 | 0.339977 | 31.4861 | 48.0878 | 284.595 | 381.9038 | 24505.46 |
| 77739.7 | 13.5872 | 0.805185 | 171.963 | 2.31162 | 7.00349 | 0.65614 | 131.602 | 19.7155 | 0.950385 | 448.27 | 95.3768 | 0.791284 | 166.632 | 113.34 | 185.863 | 97.44841 | 5133.071 |
| 21110 | 14.3625 | 0.952816 | 148.669 | 0.837021 | 52.8012 | 0.354246 | 200.59 | 61.6299 | 0.739556 | 329.193 | 85.9964 | 0.820342 | 69.7747 | 192.956 | 292.041 | 121.0753 | 9431.107 |
| 28638.6 | 19.1167 | 0.933193 | 24.1967 | 1.74946 | 33.2221 | 0.386249 | 308.756 | 83.1513 | 0.339906 | 239.259 | 73.714 | 0.742398 | 162.926 | 93.7012 | 223.575 | 215.3565 | 15371.51 |
| 56750.8 | 16.7399 | 0.859904 | 19.8883 | 1.25982 | 73.7386 | 0.371312 | 264.919 | 41.9872 | 0.727846 | 267 | 53.5757 | 0.612388 | 98.7834 | 55.7327 | 92.8983 | 178.4504 | 12029.23 |
| 54200.4 | 23.7077 | 0.866557 | 61.2011 | 3.6324 | 97.4616 | 0.292901 | 168.147 | 73.0282 | 0.625395 | 308.951 | 14.8671 | 0.763868 | 60.3305 | 66.7465 | 106.166 | 214.894 | 15774.4 |
| 32179.9 | 24.6049 | 0.923965 | 150.313 | 1.7749 | 82.9362 | 0.372971 | 428.116 | 89.6509 | 0.901958 | 490.488 | 59.9328 | 0.776433 | 6.86567 | 130.146 | 406.693 | 113.9966 | 8687.42 |
| 33577.1 | 22.951 | 0.920321 | 35.0227 | 2.41038 | 23.3746 | 0.443073 | 440.136 | 73.7638 | 0.805599 | 181.74 | 7.08144 | 0.269904 | 159.976 | 57.7203 | 46.4726 | 238.416 | 15726.43 |
| 33991.8 | 18.4627 | 0.919237 | 116.14 | 2.51978 | 91.6335 | 0.447576 | 471.604 | 86.8551 | 0.548469 | 430.733 | 89.4455 | 0.986427 | 63.0826 | 283.61 | 326.082 | 105.7348 | 8149.364 |
| 31811.5 | 27.5818 | 0.924928 | 50.5257 | 2.38773 | 5.23129 | 0.535511 | 401.302 | 67.0195 | 0.90548 | 498.26 | 25.9139 | 0.889238 | 238.166 | 105.846 | 129.285 | 57.44399 | 3800.88 |
| 38132.9 | 29.7917 | 0.908451 | 112.392 | 1.31592 | 66.7013 | 0.292078 | 207.318 | 22.2819 | 0.716496 | 374.3 | 57.4335 | 0.411405 | 7.15492 | 76.3158 | 273.94 | 309.1829 | 22832.47 |
| 74271.4 | 14.63 | 0.814227 | 54.5132 | 1.98302 | 14.8578 | 0.262315 | 223.143 | 54.8623 | 0.771719 | 181.813 | 35.5772 | 0.621397 | 42.5878 | 219.958 | 139.411 | 258.8649 | 14022.06 |
| 67314.1 | 18.1279 | 0.832366 | 22.4159 | 0.374828 | 52.6095 | 0.179719 | 203.083 | 18.1494 | 0.718381 | 317.052 | 51.1616 | 0.729718 | 6.0623 | 124.481 | 108.521 | 338.0185 | 21351.65 |
| 63462.1 | 19.0802 | 0.842409 | 49.3711 | 1.23283 | 15.3426 | 0.47933 | 327.355 | 92.6745 | 0.657956 | 309.045 | 26.4799 | 0.901937 | 93.6032 | 282.91 | 127.315 | 107.6955 | 6104.129 |
| 36846.1 | 17.7576 | 0.911795 | 159.276 | 1.81373 | 147.738 | 0.579168 | 97.5946 | 7.25332 | 0.352414 | 219.206 | 438.653 | 0.984355 | 144.796 | 71.7892 | 152.623 | 179.7013 | 12940.37 |
| 40829 | 17.9846 | 0.901412 | 103.144 | 0.401068 | 80.5318 | 0.459441 | 245.649 | 22.9829 | 0.410798 | 442.731 | 661.011 | 0.592698 | 35.8945 | 129.355 | 240.229 | 303.9161 | 20638.74 |
| 44149.7 | 16.406 | 0.892754 | 99.7159 | 0.610164 | 60.4237 | 0.430595 | 471.569 | 273.648 | 0.568428 | 463.41 | 790.926 | 0.403985 | 13.2146 | 142.548 | 123.586 | 391.4629 | 24668.26 |
| 21571.8 | 30.6595 | 0.951627 | 57.3324 | 2.10061 | 578.421 | 0.469297 | 309.741 | 214.968 | 0.836179 | 518 | 444.135 | 0.923646 | 42.3329 | 264.617 | 391.585 | 131.1168 | 13891.67 |
| 23832.2 | 31.7636 | 0.945735 | 39.5192 | 1.8236 | 37.4313 | 0.490752 | 273.801 | 267.698 | 0.8315 | 298.72 | 940.47 | 0.931903 | 74.4154 | 219.331 | 296.505 | 140.9705 | 8387.763 |
| 72335.9 | 19.0989 | 0.819275 | 132.451 | 1.32062 | 276.548 | 0.601166 | 250.974 | 645.084 | 0.94963 | 175.547 | 741.155 | 0.426305 | 34.7778 | 233.521 | 133.298 | 379.171 | 22391.36 |
| 37782.3 | 24.0629 | 0.909359 | 70.5199 | 1.1637 | 148.204 | 0.357507 | 456.814 | 737.12 | 0.485409 | 200.577 | 19.4274 | 0.787445 | 86.3297 | 69.0326 | 128.145 | 262.2662 | 20397.61 |
| 23534.3 | 29.1533 | 0.946509 | 156.671 | 3.63058 | 132.948 | 0.515317 | 274.449 | 356.617 | 0.617706 | 399.289 | 374.903 | 0.740701 | 19.264 | 122.613 | 134.814 | 163.5285 | 11999.59 |
| 39689.7 | 25.9266 | 0.904388 | 57.1708 | 3.1033 | 682.453 | 0.51193 | 148.137 | 109.979 | 0.658761 | 268.367 | 160.714 | 0.766602 | 17.3687 | 101.411 | 103.687 | 162.318 | 17751.05 |
| 58614.4 | 22.4287 | 0.855049 | 93.8875 | 2.57788 | 330.371 | 0.457235 | 405.989 | 58.39 | 0.942495 | 372.784 | 369.373 | 0.814792 | 49.3953 | 199.702 | 336.635 | 130.2737 | 10958.52 |
| 41578.2 | 19.4041 | 0.89946 | 33.811 | 1.40816 | 162.151 | 0.321998 | 313.243 | 458.952 | 0.818605 | 251.876 | 268.925 | 0.584043 | 74.5328 | 309.623 | 138.945 | 255.9806 | 19891.59 |
| 34837.6 | 27.5832 | 0.917039 | 140.637 | 1.92027 | 49.3376 | 0.512658 | 125.805 | 203.906 | 0.773342 | 515.29 | 445.486 | 0.306787 | 51.0909 | 76.6943 | 514.149 | 293.678 | 18777.01 |
| 36674.6 | 30.24 | 0.912253 | 90.03 | 2.31369 | 406.416 | 0.511662 | 412.029 | 278.625 | 0.504863 | 237.496 | 918.734 | 0.742394 | 34.903 | 182.327 | 224.395 | 267.5063 | 21653.19 |
| 32457.1 | 20.449 | 0.923239 | 158.953 | 0.817936 | 328.157 | 0.602959 | 177.913 | 882.381 | 0.807483 | 348.177 | 376.67 | 0.666025 | 31.2664 | 140.538 | 182.944 | 235.4295 | 16231.66 |
| 42830.7 | 25.696 | 0.896199 | 40.4117 | 0.26883 | 47.2122 | 0.325857 | 339.035 | 613.566 | 0.522768 | 221.492 | 470.894 | 0.880236 | 1.0332 | 262.457 | 195.139 | 251.8671 | 15829.91 |
| 21598.4 | 18.4245 | 0.951546 | 157.118 | 2.478 | 511.425 | 0.698036 | 331.017 | 950.937 | 0.954152 | 467.919 | 551.848 | 0.900222 | 156.608 | 164.735 | 187.805 | 220.4858 | 13907.7 |
| 34127.6 | 20.4761 | 0.918884 | 124.44 | 1.96292 | 43.6823 | 0.484675 | 257.777 | 337.215 | 0.992558 | 506.499 | 928.675 | 0.82217 | 56.2326 | 214.638 | 213.427 | 162.017 | 9455.339 |
| 43417.5 | 17.9952 | 0.894664 | 155.371 | 2.71173 | 546.492 | 0.606198 | 82.7519 | 110.55 | 0.975321 | 468.583 | 643.78 | 0.61319 | 106.351 | 76.9172 | 331.8 | 174.8659 | 13461.99 |
| 27473.1 | 18.8845 | 0.936231 | 168.74 | 3.29209 | 835.164 | 0.54724 | 338.793 | 257.054 | 0.986717 | 379.872 | 898.961 | 0.806234 | 125.031 | 260.34 | 95.6235 | 183.4109 | 16693.06 |
| 54665 | 18.4445 | 0.865342 | 76.4009 | 0.3787 | 415.889 | 0.486599 | 494.335 | 577.715 | 0.547641 | 463.141 | 293.582 | 0.961055 | 4.95846 | 340.835 | 387.988 | 211.4585 | 17871.53 |
| 64490.3 | 16.9465 | 0.839727 | 46.7239 | 2.36795 | 583.38 | 0.420917 | 449.808 | 328.612 | 0.70702 | 145.409 | 800.425 | 0.904084 | 24.8463 | 374.747 | 73.8978 | 249.4893 | 22767.52 |
| 41139.5 | 28.8055 | 0.900611 | 70.9927 | 3.10737 | 878.77 | 0.496069 | 373.459 | 633.005 | 0.681104 | 80.2899 | 530.455 | 0.881451 | 136.364 | 53.0243 | 55.7499 | 225.7387 | 21605.95 |
| 35958.1 | 18.4217 | 0.91411 | 19.3697 | 2.21209 | 90.7997 | 0.364652 | 243.033 | 374.6 | 0.889723 | 240.257 | 412.981 | 0.969999 | 123.107 | 57.2975 | 204.243 | 137.6284 | 9316.353 |
| 22640.4 | 32.2876 | 0.948843 | 168.573 | 0.506544 | 40.5605 | 0.428801 | 257.984 | 509.223 | 0.606371 | 445.437 | 959.09 | 0.771396 | 15.9734 | 74.7849 | 201.839 | 266.2308 | 16827.51 |
| 32581.8 | 22.8237 | 0.922915 | 71.5323 | 1.72193 | 286.093 | 0.241225 | 466.51 | 11.2485 | 0.774408 | 114.893 | 658.163 | 0.831291 | 102.474 | 390.831 | 77.2039 | 240.3954 | 24650.13 |
| 54692.2 | 18.8352 | 0.865272 | 149.385 | 1.85109 | 869.709 | 0.55509 | 459.293 | 509.883 | 0.841079 | 436.114 | 908.618 | 0.689234 | 55.5082 | 376.948 | 303.788 | 273.427 | 23549.92 |
| 44853.4 | 21.1916 | 0.890923 | 151.654 | 2.13798 | 83.714 | 0.231004 | 350.253 | 916.693 | 0.93846 | 395.825 | 410.932 | 0.75866 | 110.191 | 50.6089 | 359.353 | 325.3735 | 20902.84 |
| 43432.5 | 21.148 | 0.894627 | 64.7345 | 2.65158 | 175.725 | 0.421047 | 249.469 | 112.53 | 0.911112 | 316.542 | 875.221 | 0.716198 | 84.8761 | 147.887 | 314.946 | 176.629 | 12616.83 |
| 37113.8 | 14.7759 | 0.911095 | 89.8838 | 2.45394 | 951.892 | 0.461577 | 497.897 | 771.325 | 0.659893 | 436.332 | 98.0612 | 0.984679 | 23.1798 | 395.062 | 234.628 | 206.9962 | 24248.54 |
| 48256.8 | 15.5662 | 0.882047 | 126.023 | 2.01331 | 128.526 | 0.466847 | 329.837 | 251.343 | 0.766976 | 174.92 | 512.939 | 0.529469 | 93.5997 | 135.141 | 141.353 | 229.8876 | 15451.21 |
| 44738.6 | 27.1306 | 0.891227 | 167.574 | 1.61007 | 885.137 | 0.633376 | 136.217 | 363.333 | 0.937313 | 221.406 | 394.765 | 0.469444 | 115.757 | 51.778 | 127.05 | 252.8343 | 22058.83 |
| 54178.5 | 14.8759 | 0.866609 | 103.05 | 1.56316 | 175.367 | 0.447386 | 297.168 | 890.293 | 0.801384 | 443.203 | 438.628 | 0.542089 | 135.574 | 141.818 | 327.363 | 318.9129 | 20673.38 |
| 28544.9 | 29.9717 | 0.933447 | 100.01 | 0.42421 | 605.533 | 0.546617 | 165.106 | 504.16 | 0.688944 | 164.122 | 307.434 | 0.813781 | 18.4128 | 50.8839 | 158.787 | 181.6537 | 17149.02 |
| 21594.6 | 30.3654 | 0.951567 | 157.864 | 0.266334 | 867.148 | 0.635027 | 293.201 | 225.442 | 0.936726 | 319.612 | 948.175 | 0.713703 | 11.4842 | 153.574 | 172.692 | 192.9036 | 16860.13 |
| 30198.4 | 22.3969 | 0.929129 | 128.684 | 1.3552 | 200.982 | 0.326169 | 461.931 | 452.283 | 0.714731 | 147.162 | 331.954 | 0.767618 | 9.55125 | 299.862 | 80.4188 | 228.1208 | 19241.18 |
| 28426.1 | 16.7903 | 0.933745 | 133.156 | 2.55509 | 484.533 | 0.428826 | 297.868 | 439.883 | 0.568122 | 59.9187 | 598.385 | 0.984673 | 129.714 | 159.498 | 47.2033 | 215.7249 | 21107.2 |
| 58573.9 | 20.5796 | 0.855153 | 30.1986 | 2.93472 | 343.523 | 0.563136 | 292.988 | 904.242 | 0.613037 | 478.964 | 170.929 | 0.779653 | 49.4308 | 166.83 | 312.361 | 298.8878 | 20118.46 |
| 60821.2 | 23.0058 | 0.849296 | 165.832 | 0.989274 | 196.807 | 0.632876 | 481.001 | 721.657 | 0.809709 | 246.252 | 884.608 | 0.734831 | 10.5166 | 156.334 | 106.897 | 258.3268 | 15036.66 |
| 59223.9 | 14.1794 | 0.853455 | 52.4304 | 0.543066 | 124.133 | 0.307993 | 59.9818 | 884.188 | 0.97287 | 462.622 | 239.445 | 0.540921 | 37.698 | 49.9644 | 217.217 | 346.2506 | 22345.5 |
| 45636.6 | 15.5227 | 0.888877 | 148.213 | 0.957141 | 274.753 | 0.586983 | 423.715 | 618.456 | 0.893065 | 473.987 | 283.794 | 0.887725 | 92.9552 | 290.208 | 358.083 | 148.4379 | 10008.07 |
| 40232.3 | 24.5664 | 0.902972 | 165.074 | 1.34348 | 130.965 | 0.524596 | 359.975 | 794.599 | 0.908365 | 292.79 | 360.346 | 0.869744 | 93.3309 | 96.2526 | 88.6188 | 179.5496 | 11083.62 |
| 63541.5 | 19.5732 | 0.842202 | 53.0673 | 0.852811 | 177.017 | 0.309807 | 288.185 | 785.887 | 0.956617 | 184.253 | 594.044 | 0.717323 | 49.1013 | 184.618 | 158.088 | 293.8467 | 19801.54 |
| 20829 | 27.7279 | 0.95356 | 79.4163 | 0.164004 | 15.7233 | 0.4598 | 112.48 | 28.3554 | 0.476877 | 346.374 | 830.115 | 0.914028 | 7.35024 | 56.7937 | 59.8719 | 167.4164 | 10785.97 |
| 43266 | 13.0353 | 0.895056 | 168.606 | 0.847525 | 123.75 | 0.54885 | 468.144 | 21.9565 | 0.688164 | 183.673 | 83.6088 | 0.687462 | 78.5526 | 456.524 | 60.6153 | 142.8286 | 10109.46 |
| 31158.5 | 26.6659 | 0.92663 | 142.842 | 1.86153 | 219.615 | 0.270088 | 347.401 | 964.168 | 0.807418 | 376.472 | 860.854 | 0.935376 | 65.219 | 89.2638 | 371.082 | 296.9584 | 22711.61 |
| 34100.7 | 22.6687 | 0.918956 | 26.4454 | 1.85479 | 160.254 | 0.419039 | 418.983 | 401.622 | 0.639181 | 194.947 | 561.738 | 0.960452 | 87.8028 | 128.189 | 82.1772 | 170.0802 | 12466.82 |
| 46912.6 | 25.0515 | 0.885557 | 100.57 | 0.214039 | 440.948 | 0.545819 | 374.417 | 381.233 | 0.894287 | 511.272 | 631.169 | 0.924997 | 20.0712 | 221.373 | 225.268 | 164.0306 | 12389.77 |
| 25630.6 | 24.3258 | 0.941038 | 169.018 | 0.819949 | 80.7045 | 0.291469 | 340.358 | 236.678 | 0.732052 | 365.287 | 496.113 | 0.73428 | 75.8164 | 289.587 | 86.4949 | 249.4031 | 18222.82 |
| 26370.7 | 22.58 | 0.939107 | 147.458 | 1.12265 | 373.521 | 0.543049 | 467.789 | 921.971 | 0.7882 | 166.222 | 740.241 | 0.817889 | 75.266 | 388.436 | 130.758 | 230.4857 | 16579.09 |
| 59805.8 | 16.4833 | 0.851939 | 36.6881 | 1.64159 | 570.843 | 0.596904 | 293.442 | 711.27 | 0.923818 | 247.642 | 498.858 | 0.965558 | 139.994 | 188.854 | 215.96 | 203.6773 | 13726.43 |
| 48636.9 | 18.7863 | 0.881057 | 59.9746 | 0.412517 | 179.132 | 0.331617 | 422.637 | 121.533 | 0.781129 | 485.11 | 11.3166 | 0.471686 | 7.52964 | 273.047 | 222.67 | 264.0623 | 22508.02 |
| 36689.7 | 16.8634 | 0.912202 | 132.294 | 0.38766 | 834.22 | 0.458344 | 288.574 | 811.806 | 0.907738 | 478.789 | 321.853 | 0.854313 | 20.0208 | 140.329 | 288.939 | 233.2806 | 22665.11 |
| 30996.9 | 17.3192 | 0.927043 | 19.5244 | 0.398133 | 90.3022 | 0.434297 | 178.251 | 635.686 | 0.68312 | 72.5787 | 14.1788 | 0.968381 | 24.6359 | 97.5998 | 56.3379 | 125.9084 | 8807.955 |
| 38611.2 | 23.3792 | 0.907197 | 69.4913 | 2.56848 | 257.449 | 0.375829 | 398.351 | 194.113 | 0.540454 | 407.799 | 726.72 | 0.692143 | 70.7431 | 259.559 | 205.995 | 280.4483 | 24676.42 |
| 82065.6 | 14.6719 | 0.793908 | 41.7556 | 0.795383 | 28.0944 | 0.513738 | 215.025 | 736.219 | 0.863201 | 422.988 | 636.847 | 0.889465 | 66.187 | 136.789 | 242.417 | 208.0382 | 10804.32 |
| 70413 | 16.6756 | 0.824287 | 106.855 | 1.24761 | 465.049 | 0.478194 | 321.026 | 359.782 | 0.468282 | 64.5059 | 681.086 | 0.90293 | 36.9862 | 76.4198 | 62.3997 | 295.4625 | 24495.68 |
| 21423 | 27.777 | 0.952011 | 133.693 | 2.00429 | 330.746 | 0.301927 | 398.919 | 368.41 | 0.837931 | 228.492 | 773.534 | 0.913416 | 20.7849 | 293.268 | 179.927 | 217.4377 | 20431.13 |
| 24094.5 | 16.8151 | 0.945037 | 142.823 | 1.2064 | 93.0225 | 0.335293 | 449.738 | 890.999 | 0.700886 | 414.847 | 229.16 | 0.82777 | 74.2543 | 372.506 | 380.61 | 224.6739 | 15824.96 |
| 74889 | 15.6501 | 0.812618 | 23.9983 | 2.80318 | 934.223 | 0.509756 | 386.383 | 897.996 | 0.801667 | 436.206 | 210.884 | 0.925943 | 106.014 | 365.47 | 257.986 | 218.0515 | 18418.57 |
| 22223.1 | 32.7137 | 0.949932 | 154.652 | 0.637891 | 785.289 | 0.741736 | 252.127 | 218.078 | 0.968404 | 450.702 | 95.2948 | 0.898032 | 53.0607 | 206.451 | 122.57 | 84.29252 | 7360.135 |
| 58331.5 | 16.5424 | 0.855783 | 119.127 | 0.16546 | 814.149 | 0.607045 | 458.507 | 741.259 | 0.503605 | 403.005 | 127.501 | 0.925171 | 7.5241 | 167.843 | 211.597 | 248.4286 | 22033.74 |
| 58116.6 | 22.1739 | 0.856346 | 164.877 | 0.42992 | 552.632 | 0.543966 | 335.557 | 573.176 | 0.793131 | 310.98 | 640.667 | 0.879907 | 30.2104 | 172.153 | 157.762 | 237.1993 | 17705.93 |
| 21181.4 | 26.1785 | 0.952639 | 134.123 | 1.51602 | 63.7464 | 0.258217 | 125.47 | 613.183 | 0.638455 | 364.083 | 358.295 | 0.884371 | 56.7318 | 81.1864 | 109.467 | 232.8439 | 16910.84 |
| 61451.5 | 20.0255 | 0.847651 | 20.4449 | 2.80092 | 45.5377 | 0.263249 | 160.862 | 13.4896 | 0.63127 | 435.062 | 467.11 | 0.706031 | 117.32 | 56.7631 | 225.118 | 286.0021 | 17537.16 |
| 49977.1 | 25.1839 | 0.877568 | 65.35 | 2.34005 | 503.114 | 0.40132 | 328.969 | 32.4224 | 0.703285 | 378.974 | 580.245 | 0.990272 | 158.937 | 176.828 | 119.262 | 181.8354 | 18157.27 |
| 40730.3 | 20.9374 | 0.901671 | 82.2701 | 1.66519 | 657.279 | 0.466139 | 145.052 | 502.536 | 0.548381 | 54.2817 | 117.612 | 0.979241 | 87.9462 | 71.3059 | 49.413 | 193.4942 | 21011.6 |
| 38034.4 | 27.1862 | 0.908705 | 44.5482 | 2.22253 | 337.706 | 0.435116 | 442.542 | 593.028 | 0.615838 | 333.875 | 400.923 | 0.940457 | 146.87 | 190.634 | 209.374 | 196.3292 | 16662.88 |
| 23493.3 | 13.5018 | 0.946603 | 49.2407 | 0.757336 | 27.0626 | 0.533643 | 488.543 | 53.7635 | 0.590377 | 512.621 | 699.356 | 0.661118 | 29.6932 | 207.734 | 481.503 | 194.4379 | 12348.99 |
| 49880.4 | 22.7734 | 0.877819 | 129.081 | 0.147994 | 718.939 | 0.664492 | 333.214 | 133.77 | 0.432501 | 285.806 | 623.774 | 0.956746 | 5.87371 | 277.548 | 120.799 | 224.0687 | 19041.45 |
| 49883.1 | 25.4047 | 0.877814 | 41.0908 | 1.86078 | 289.561 | 0.343922 | 493.903 | 17.4036 | 0.650641 | 137.378 | 668.873 | 0.705624 | 71.365 | 467.178 | 92.3702 | 263.0281 | 23721.16 |
| 36811.9 | 15.7113 | 0.911883 | 65.5902 | 0.7045 | 108.757 | 0.267843 | 152.72 | 702.856 | 0.997096 | 425.306 | 694.957 | 0.71704 | 55.2871 | 105.122 | 200.521 | 263.8315 | 17862.25 |
| 61358.7 | 20.1917 | 0.847893 | 171.691 | 0.616083 | 479.311 | 0.534311 | 145.045 | 125.969 | 0.658911 | 498.358 | 579.124 | 0.824342 | 57.4318 | 116.828 | 246.462 | 234.7591 | 18410.44 |
| 32356 | 28.092 | 0.923509 | 66.3063 | 2.22517 | 402.157 | 0.45921 | 217.439 | 84.7997 | 0.821463 | 314.195 | 982.997 | 0.509404 | 135.033 | 160.125 | 55.8681 | 240.637 | 21920.61 |
| 70283.3 | 13.7451 | 0.824624 | 143.52 | 0.101227 | 82.9309 | 0.458077 | 453.503 | 169.847 | 0.829775 | 517.313 | 594.295 | 0.69571 | 4.01217 | 317.205 | 434.276 | 245.3368 | 14073.56 |
| 58248.4 | 22.5085 | 0.856003 | 151.282 | 2.40749 | 325.41 | 0.561194 | 448.292 | 486.8 | 0.443753 | 280.11 | 317.927 | 0.739917 | 154.818 | 173.03 | 121.143 | 280.4766 | 20535.49 |
| 47132.9 | 20.9515 | 0.88498 | 160 | 3.2146 | 380.802 | 0.604337 | 199.868 | 640.126 | 0.919267 | 514.883 | 614.671 | 0.605405 | 122.507 | 93.7123 | 160.303 | 257.8014 | 16638.03 |
| 51344.3 | 25.5809 | 0.874004 | 130.079 | 0.472902 | 612.613 | 0.535667 | 326.941 | 46.4891 | 0.622119 | 77.3783 | 707.764 | 0.959832 | 36.7801 | 301.792 | 74.2173 | 198.7312 | 17716.75 |
| 40578 | 13.9387 | 0.902064 | 52.3527 | 1.02572 | 196.245 | 0.475944 | 276.406 | 278.445 | 0.985343 | 516.065 | 138.978 | 0.737704 | 9.61668 | 129.548 | 377.584 | 113.9308 | 8710.46 |
| 49609.8 | 23.4155 | 0.878524 | 112.951 | 0.19421 | 163.259 | 0.63005 | 134.877 | 817.151 | 0.980058 | 209.768 | 515.452 | 0.895983 | 16.2234 | 111.227 | 122.646 | 176.4887 | 10235.59 |
| 36138.8 | 17.0396 | 0.913638 | 44.541 | 0.396632 | 98.8669 | 0.413969 | 232.696 | 316.226 | 0.616199 | 332.678 | 163.995 | 0.915444 | 9.92476 | 108.24 | 90.4637 | 137.473 | 10033.46 |
| 31616.9 | 18.2682 | 0.925428 | 139.655 | 2.02509 | 50.8827 | 0.230316 | 468.787 | 878.073 | 0.967688 | 449.93 | 508.499 | 0.552658 | 116.039 | 129.234 | 176.318 | 374.1302 | 23816.1 |
| 78975.5 | 14.8948 | 0.801964 | 168.457 | 1.47164 | 197.282 | 0.54869 | 128.922 | 792.939 | 0.529654 | 343.919 | 870.393 | 0.884068 | 77.3209 | 90.4437 | 56.9909 | 326.2014 | 19215.82 |
| 40676.9 | 25.5394 | 0.901814 | 100.808 | 0.961989 | 76.0427 | 0.322801 | 269.7 | 168.044 | 0.717187 | 238.659 | 900.559 | 0.66314 | 6.41986 | 74.4329 | 152.513 | 261.3263 | 17401.31 |
| 31473.6 | 30.3521 | 0.925812 | 78.2156 | 1.48809 | 68.7796 | 0.389881 | 109.619 | 396.077 | 0.608668 | 272.769 | 420.513 | 0.776751 | 85.595 | 74.8654 | 99.6962 | 189.9161 | 12913.02 |
| 53726.4 | 25.2828 | 0.867794 | 152.151 | 0.137617 | 610.172 | 0.544941 | 106.108 | 205.494 | 0.519416 | 415.216 | 778.724 | 0.893263 | 1.44712 | 58.8847 | 143.039 | 288.5286 | 24046.97 |
| 46886.8 | 16.2861 | 0.885618 | 20.4039 | 0.708351 | 577.074 | 0.473612 | 167.213 | 427.315 | 0.60297 | 425.075 | 321.317 | 0.944578 | 33.0594 | 122.243 | 270.916 | 191.8769 | 18736.44 |
| 33202 | 17.0463 | 0.921295 | 61.869 | 1.8896 | 103.216 | 0.450819 | 404.159 | 420.169 | 0.60747 | 307.942 | 257.394 | 0.769018 | 107.246 | 145.927 | 159.01 | 166.9432 | 11749.84 |
| 57213.6 | 13.8884 | 0.858696 | 154.94 | 2.26135 | 474.352 | 0.579164 | 418.495 | 440.024 | 0.969835 | 210.107 | 701.401 | 0.457292 | 27.0755 | 287.577 | 137.731 | 285.162 | 20468.38 |
| 51209.2 | 25.8538 | 0.874357 | 141.638 | 0.244036 | 645.491 | 0.696351 | 225.029 | 760.91 | 0.96512 | 405.932 | 590.658 | 0.934975 | 17.3515 | 142.213 | 365.963 | 183.747 | 11794.63 |
| 26588.6 | 32.9629 | 0.938551 | 138.5 | 1.46557 | 14.9248 | 0.379102 | 150.616 | 334.184 | 0.491949 | 331.457 | 828.313 | 0.935387 | 40.9178 | 132.419 | 175.45 | 222.0364 | 13743.04 |
| 35710.1 | 17.1783 | 0.914756 | 121.554 | 1.29025 | 432.718 | 0.440646 | 393.081 | 401.656 | 0.970655 | 399.432 | 88.6434 | 0.47388 | 25.7773 | 236.366 | 79.6125 | 241.484 | 22945.57 |
| 55039.5 | 18.0077 | 0.864366 | 168.911 | 1.55694 | 505.613 | 0.640747 | 385.83 | 393.473 | 0.823453 | 250.759 | 173.444 | 0.420752 | 19.3671 | 382.905 | 132.331 | 275.0757 | 20583.42 |
| 27048.1 | 31.2821 | 0.937351 | 126.02 | 2.23196 | 581.907 | 0.522923 | 114.312 | 146.793 | 0.409685 | 494.432 | 783.319 | 0.942532 | 25.95 | 93.6703 | 487.793 | 223.2863 | 22541.78 |
| 55968.9 | 21.8531 | 0.861945 | 148.865 | 1.15799 | 118.582 | 0.602547 | 214.752 | 464.284 | 0.979654 | 158.95 | 207.217 | 0.491083 | 58.6969 | 121.251 | 104.17 | 215.5332 | 12776.19 |
| 23006.5 | 17.2892 | 0.947874 | 59.6226 | 0.609946 | 294.73 | 0.423451 | 482.799 | 357.166 | 0.872909 | 184.346 | 788.501 | 0.573778 | 12.8277 | 200.667 | 102.559 | 225.6612 | 19179.04 |
| 79632.5 | 14.4354 | 0.800251 | 112.139 | 2.61259 | 35.6509 | 0.466418 | 279.098 | 271.509 | 0.734242 | 150.233 | 556.207 | 0.602243 | 2.74945 | 76.6204 | 130.375 | 239.8658 | 12905.68 |
| 63001.5 | 14.2457 | 0.843607 | 134.959 | 1.07239 | 365.314 | 0.512836 | 377.981 | 245.411 | 0.692949 | 371.381 | 9.94238 | 0.46714 | 14.2989 | 306.161 | 339.63 | 292.2157 | 23873.34 |
| 33354.7 | 28.9121 | 0.920907 | 44.633 | 3.01441 | 528.002 | 0.54135 | 383.976 | 364.641 | 0.834326 | 169.647 | 639.013 | 0.889044 | 274.994 | 343.09 | 120.323 | 172.4425 | 13305.94 |
| 33596.4 | 15.1804 | 0.920265 | 80.0856 | 3.68382 | 760.658 | 0.438137 | 103.217 | 950.549 | 0.811938 | 152.302 | 8.79139 | 0.878214 | 16.5598 | 98.0184 | 108.95 | 208.5847 | 22097.67 |
| 30677.3 | 31.6283 | 0.92789 | 171.205 | 0.135668 | 522.955 | 0.656661 | 263.291 | 921.345 | 0.454508 | 401.032 | 612.351 | 0.836771 | 5.07375 | 237.508 | 212.345 | 302.2179 | 22806.19 |
| 39243.5 | 28.5335 | 0.905554 | 96.1786 | 0.683408 | 300.653 | 0.639372 | 381.631 | 301.921 | 0.93608 | 461.551 | 531.18 | 0.89176 | 17.7883 | 280.671 | 424.369 | 146.7434 | 9666.891 |
| 29724.5 | 14.1962 | 0.930359 | 126.937 | 1.00271 | 269.034 | 0.483019 | 185.266 | 609.916 | 0.967894 | 355.046 | 770.877 | 0.940946 | 23.1044 | 85.2622 | 197.65 | 188.2177 | 13030.15 |
| 22508.2 | 33.2443 | 0.949189 | 121.524 | 3.16298 | 252.566 | 0.418183 | 108.435 | 41.6804 | 0.916856 | 456.493 | 549.284 | 0.484625 | 86.6814 | 55.0627 | 401.844 | 176.4254 | 16830.44 |
| 21463.5 | 25.7691 | 0.951903 | 103.253 | 0.713828 | 810.885 | 0.47186 | 481.204 | 320.064 | 0.88218 | 416.832 | 584.959 | 0.804316 | 3.30149 | 247.273 | 323.471 | 186.6066 | 20651.86 |
| 34780.8 | 16.6082 | 0.917178 | 29.8574 | 1.63553 | 204.721 | 0.306385 | 302.817 | 636.815 | 0.911568 | 171.768 | 491.941 | 0.830501 | 54.1619 | 64.9917 | 49.8335 | 215.1937 | 16784.79 |
| 30860.6 | 17.0569 | 0.927398 | 80.3225 | 2.2206 | 550.262 | 0.530936 | 214.358 | 389.137 | 0.786107 | 382.423 | 953.539 | 0.767378 | 119.759 | 154.574 | 322.218 | 236.6239 | 18417.94 |
| 36233.1 | 20.9854 | 0.913395 | 112.388 | 2.45061 | 247.366 | 0.245764 | 202.684 | 805.682 | 0.847505 | 432.111 | 47.8514 | 0.782883 | 146.249 | 144.262 | 209.624 | 265.6752 | 23783.68 |
| 64186.3 | 18.4717 | 0.840521 | 50.2063 | 3.23713 | 436.758 | 0.513948 | 246.022 | 387.084 | 0.762414 | 518.397 | 938.153 | 0.721533 | 123.23 | 136.945 | 329.558 | 254.6148 | 17833.29 |
| 26111.7 | 18.5649 | 0.93978 | 77.184 | 0.341382 | 936.269 | 0.458673 | 205.118 | 748.949 | 0.916283 | 169.008 | 568.533 | 0.873059 | 17.8937 | 116.03 | 53.3986 | 226.2363 | 23169.2 |
| 23756.6 | 31.0897 | 0.945931 | 153.205 | 3.52553 | 214.58 | 0.54043 | 126.455 | 46.6922 | 0.254471 | 382.451 | 794.073 | 0.780444 | 106.342 | 103.249 | 295.19 | 289.258 | 24193.2 |
| 28926.9 | 31.7002 | 0.932453 | 123.322 | 0.381691 | 397.667 | 0.414247 | 348.549 | 199.787 | 0.853638 | 113.567 | 717.88 | 0.870181 | 21.2763 | 87.0411 | 105.611 | 186.2802 | 16590.2 |
| 20994.6 | 15.7052 | 0.953118 | 40.1104 | 1.96055 | 19.3106 | 0.337481 | 485.625 | 944.015 | 0.888525 | 341.738 | 758.985 | 0.415399 | 172.513 | 321.942 | 317.481 | 374.241 | 22266.02 |
| 24664 | 31.3717 | 0.943566 | 44.5822 | 3.00731 | 27.1679 | 0.321116 | 277.171 | 465.819 | 0.918053 | 237.298 | 239.485 | 0.652791 | 40.4077 | 85.7983 | 59.3476 | 173.901 | 11230.86 |
| 24346.4 | 31.4516 | 0.944394 | 84.6779 | 1.76597 | 99.191 | 0.39346 | 342.364 | 583.012 | 0.991977 | 355.317 | 236.107 | 0.800914 | 147.322 | 309.589 | 242.234 | 140.044 | 9674.946 |
| 32270.5 | 28.145 | 0.923732 | 153.066 | 2.61515 | 418.672 | 0.465416 | 429.451 | 134.968 | 0.631039 | 169.5 | 207.423 | 0.842336 | 10.3205 | 257.676 | 75.4827 | 162.0168 | 16632.49 |
| 63008.9 | 16.0646 | 0.843589 | 136.256 | 2.83777 | 74.7053 | 0.461583 | 197.627 | 224.62 | 0.851131 | 409.856 | 866.3 | 0.94603 | 68.6777 | 64.6443 | 383.872 | 169.4177 | 9797.599 |
| 35663.3 | 16.1169 | 0.914877 | 156.741 | 2.36819 | 802.077 | 0.566486 | 400.595 | 473.634 | 0.751265 | 190.562 | 105.833 | 0.638415 | 133.659 | 49.0583 | 123.078 | 208.5543 | 20710.16 |
| 30190.4 | 16.1329 | 0.929145 | 157.851 | 0.619365 | 38.903 | 0.387991 | 464.685 | 940.539 | 0.886103 | 177.412 | 595.872 | 0.976743 | 61.2101 | 332.583 | 124.381 | 225.2134 | 13326.4 |
| 32294.2 | 18.6218 | 0.923662 | 20.0862 | 2.15465 | 626.598 | 0.410215 | 232.125 | 854.266 | 0.909878 | 274.419 | 12.2896 | 0.998144 | 33.8787 | 153.973 | 181.765 | 171.7889 | 17675.94 |
| 42717.3 | 18.3979 | 0.896489 | 44.2087 | 1.31951 | 193.672 | 0.331987 | 318.171 | 718.232 | 0.764592 | 54.1394 | 574.234 | 0.975753 | 102.527 | 135.135 | 45.4886 | 215.5962 | 15849.47 |
| 33934.4 | 28.4942 | 0.919395 | 57.9613 | 1.64044 | 227.577 | 0.275295 | 419.486 | 814.158 | 0.798266 | 292.591 | 9.05161 | 0.97351 | 129.116 | 366.015 | 71.025 | 193.1293 | 17037.83 |
| 72711.7 | 15.829 | 0.818294 | 51.1037 | 0.967823 | 5.3282 | 0.331375 | 202.737 | 105.644 | 0.527087 | 444.173 | 618.385 | 0.978842 | 85.8556 | 128.546 | 90.1072 | 236.0482 | 12378.12 |
| 36715.9 | 15.9056 | 0.912133 | 109.626 | 1.50805 | 142.1 | 0.374791 | 407.652 | 187.332 | 0.961887 | 358.588 | 660.899 | 0.859451 | 125.91 | 67.4526 | 144.055 | 152.1909 | 10844.26 |
| 44034.8 | 13.1043 | 0.893052 | 156.976 | 0.553636 | 95.74 | 0.429294 | 205.977 | 487.939 | 0.796496 | 224.316 | 683.528 | 0.954923 | 51.1099 | 87.7395 | 219.179 | 199.8748 | 12361.5 |
| 35108.2 | 30.014 | 0.916337 | 119.635 | 1.13777 | 5.134 | 0.431909 | 485.365 | 498.366 | 0.911734 | 122.81 | 901.8 | 0.733782 | 2.64856 | 130.989 | 121.575 | 207.2149 | 11647.19 |
| 52851.8 | 24.7288 | 0.870074 | 128.854 | 1.88565 | 392.332 | 0.421794 | 259.489 | 220.995 | 0.896607 | 393.102 | 979.837 | 0.926675 | 112.922 | 192.646 | 300.831 | 202.0631 | 15802.93 |
| 56013.2 | 24.2466 | 0.861832 | 87.8419 | 3.47712 | 659.095 | 0.569281 | 371.188 | 685.122 | 0.987276 | 516.48 | 237.623 | 0.727452 | 162.656 | 308.887 | 315.417 | 218.7405 | 16244.06 |
| 26371 | 15.631 | 0.939102 | 75.671 | 1.164 | 104.416 | 0.397184 | 266.167 | 237.964 | 0.557344 | 58.0261 | 976.267 | 0.489114 | 76.9622 | 46.8342 | 45.5705 | 308.8719 | 22763.26 |
| 29322.1 | 31.2023 | 0.931422 | 156.483 | 0.7172 | 228.423 | 0.452793 | 192.36 | 220.372 | 0.960565 | 223.966 | 354.73 | 0.639088 | 59.7021 | 151.163 | 83.9193 | 171.2473 | 13649.04 |
| 88532.4 | 13.1252 | 0.777049 | 43.2049 | 1.67036 | 346.762 | 0.401886 | 270.607 | 122.448 | 0.680736 | 371.89 | 635.106 | 0.686669 | 3.6123 | 191.351 | 296.326 | 294.3685 | 23292.19 |
| 20471.8 | 27.9458 | 0.954491 | 90.2573 | 2.21716 | 476.402 | 0.320009 | 281.755 | 51.8137 | 0.718175 | 261.727 | 112.152 | 0.823503 | 19.4176 | 48.796 | 79.8785 | 174.7826 | 23999.33 |
| 78572.3 | 16.5101 | 0.803016 | 155.11 | 0.486157 | 63.8122 | 0.451856 | 289.303 | 960.323 | 0.803753 | 100.206 | 335.088 | 0.860973 | 18.3341 | 153.4 | 47.4932 | 266.2863 | 14414.23 |
| 34681.3 | 24.144 | 0.917443 | 131.992 | 1.35107 | 320.655 | 0.617018 | 419.51 | 829.019 | 0.948842 | 515.908 | 655.236 | 0.762928 | 26.756 | 107.414 | 397.376 | 230.5223 | 14383.18 |
| 29702.6 | 26.7095 | 0.930425 | 54.321 | 3.15199 | 52.8421 | 0.395884 | 120.989 | 466.292 | 0.834082 | 317.615 | 227.498 | 0.879117 | 52.9264 | 77.3731 | 99.0859 | 128.9125 | 8464.615 |
| 26116.6 | 28.9866 | 0.939776 | 125.735 | 0.958617 | 650.929 | 0.513162 | 458.425 | 694.909 | 0.796378 | 388.974 | 587.615 | 0.750678 | 62.6113 | 128.349 | 327.671 | 231.9351 | 20922.34 |
| 43344.6 | 26.337 | 0.89486 | 125.228 | 1.0468 | 62.3717 | 0.579073 | 124.972 | 406.662 | 0.920841 | 461.769 | 678.529 | 0.415064 | 87.7066 | 88.2395 | 71.8676 | 262.8037 | 15147.05 |
| 21458.9 | 26.6304 | 0.951916 | 56.3652 | 1.40441 | 213.075 | 0.427766 | 381.033 | 903.975 | 0.646703 | 382.518 | 796.654 | 0.7042 | 32.3008 | 315.238 | 162.703 | 274.5613 | 20420.47 |
| 37576.8 | 25.0959 | 0.909896 | 162.283 | 0.176301 | 963.81 | 0.649417 | 314.468 | 698.611 | 0.675959 | 414.588 | 494.016 | 0.925167 | 7.76484 | 138.574 | 236.422 | 218.5865 | 18574.42 |
| 38448.2 | 19.423 | 0.907619 | 166.961 | 2.44026 | 476.135 | 0.440969 | 149.366 | 14.5352 | 0.979803 | 201.396 | 525.785 | 0.556947 | 115.98 | 73.7787 | 59.428 | 203.3522 | 20074.79 |
| 73757.2 | 16.2427 | 0.815569 | 171.44 | 1.79122 | 364.959 | 0.496158 | 240.308 | 457.719 | 0.506237 | 291.62 | 392.38 | 0.995265 | 144.657 | 189.694 | 124.713 | 266.2031 | 19358.83 |
| 64910.9 | 15.4627 | 0.83863 | 35.396 | 1.58992 | 289.818 | 0.43988 | 386.772 | 191.632 | 0.585118 | 315.903 | 901.548 | 0.738879 | 17.5447 | 323.491 | 82.5642 | 276.3008 | 21062.5 |
| 49870 | 15.1727 | 0.877841 | 51.222 | 1.7118 | 309.731 | 0.260984 | 349.683 | 753.064 | 0.855909 | 211.134 | 64.3212 | 0.813834 | 161.434 | 338.174 | 152.88 | 264.0774 | 23973.93 |
| 53515.4 | 16.5884 | 0.868338 | 56.9812 | 2.01304 | 55.07 | 0.475233 | 499.688 | 492.701 | 0.679032 | 438.337 | 3.02557 | 0.444859 | 165.185 | 49.8931 | 184.365 | 274.0566 | 16308.47 |
| 61628.3 | 16.3284 | 0.847188 | 19.5614 | 2.7223 | 535.589 | 0.421385 | 240.477 | 294.805 | 0.872294 | 168.234 | 536.57 | 0.63358 | 47.0741 | 82.1918 | 87.2931 | 253.5264 | 23599.3 |
| 51883.7 | 15.7961 | 0.872591 | 83.0315 | 3.64161 | 256.338 | 0.444202 | 314.82 | 93.2828 | 0.624216 | 95.4913 | 954.799 | 0.77877 | 62.8623 | 186.804 | 77.7427 | 226.6512 | 17262.91 |
| 34038.5 | 29.3007 | 0.919124 | 156.147 | 3.69683 | 109.532 | 0.703072 | 404.263 | 46.482 | 0.860532 | 499.334 | 463.267 | 0.748518 | 171.121 | 363.314 | 279.906 | 139.173 | 8712.128 |
| 44523.4 | 15.2931 | 0.891779 | 28.5329 | 0.378678 | 938.34 | 0.386726 | 186.102 | 227.5 | 0.951291 | 186.773 | 281.255 | 0.868443 | 7.16537 | 109.165 | 150.268 | 191.7706 | 24533.62 |
| 61793.2 | 21.9157 | 0.846761 | 80.209 | 1.28944 | 291.386 | 0.533751 | 304.652 | 143.649 | 0.973213 | 406.303 | 42.3926 | 0.475827 | 112.232 | 212.615 | 254.821 | 181.719 | 13397.16 |
| 37421.4 | 22.7847 | 0.910299 | 43.1126 | 1.26032 | 43.8178 | 0.492898 | 380.837 | 713.777 | 0.573241 | 416.929 | 941.637 | 0.753994 | 76.2523 | 147.81 | 351.52 | 250.4359 | 14459.42 |
| 25312.8 | 19.6324 | 0.941863 | 152.009 | 0.298294 | 713.816 | 0.476198 | 308.915 | 891.792 | 0.812853 | 403.415 | 2.96858 | 0.998554 | 10.0473 | 276.363 | 78.4666 | 182.3044 | 18168.3 |
| 45801.9 | 14.7719 | 0.888446 | 77.5824 | 2.18812 | 439.188 | 0.356887 | 82.8739 | 684.794 | 0.963634 | 509.649 | 40.3647 | 0.667049 | 42.8739 | 61.8916 | 291.877 | 242.8981 | 22778.81 |
| 28523.5 | 16.9662 | 0.933491 | 39.281 | 2.03358 | 467.534 | 0.397764 | 112.254 | 688.544 | 0.631138 | 284.804 | 226.289 | 0.857173 | 153.224 | 49.9738 | 151.652 | 222.649 | 22579.96 |
| 58082.2 | 13.5131 | 0.856431 | 29.3584 | 3.22946 | 287.631 | 0.542253 | 258.78 | 72.1249 | 0.849389 | 453.342 | 326.852 | 0.791909 | 99.4342 | 145.931 | 333.362 | 134.4108 | 9739.311 |
| 77005.3 | 13.9094 | 0.8071 | 17.4093 | 1.54821 | 97.3188 | 0.49187 | 188.352 | 266.787 | 0.98312 | 338.626 | 918.964 | 0.492063 | 152.321 | 154.861 | 254.513 | 254.0481 | 14292.92 |
| 38516.2 | 17.1696 | 0.907441 | 21.0762 | 0.746116 | 166.43 | 0.491973 | 405.103 | 239.185 | 0.615372 | 189.103 | 231.216 | 0.425696 | 69.0438 | 358.199 | 79.0208 | 256.4557 | 18792.22 |
| 54861.5 | 13.294 | 0.864827 | 113.571 | 1.28282 | 304.166 | 0.341217 | 108.496 | 869.4 | 0.73578 | 361.24 | 799.328 | 0.822148 | 51.8496 | 83.1713 | 263.619 | 323.5579 | 24653.1 |
| 80270.4 | 15.4076 | 0.798589 | 38.8426 | 3.05165 | 174.868 | 0.363143 | 345.416 | 531.767 | 0.824843 | 125.356 | 833.216 | 0.75044 | 7.54858 | 271.996 | 72.8707 | 286.4582 | 18389.4 |
| 24140.7 | 22.6669 | 0.944921 | 86.3142 | 2.07466 | 988.302 | 0.395603 | 266.022 | 314.845 | 0.907982 | 349.492 | 95.1196 | 0.897926 | 90.566 | 199.497 | 226.551 | 167.0164 | 23784.27 |
| 25856.4 | 22.0986 | 0.940448 | 48.4811 | 2.89265 | 96.1283 | 0.506048 | 270.872 | 638.105 | 0.99429 | 365.894 | 105.574 | 0.579841 | 141.756 | 230.076 | 276.874 | 177.0339 | 11150.78 |
| 57302.7 | 17.7561 | 0.858465 | 128.815 | 1.0364 | 764.646 | 0.561808 | 166.252 | 533.908 | 0.425556 | 387.536 | 33.7357 | 0.996683 | 92.1069 | 87.2854 | 247.729 | 233.5825 | 22741.37 |
| 54148.2 | 18.1486 | 0.866689 | 100.108 | 1.16258 | 302.049 | 0.296034 | 396.922 | 435.997 | 0.966215 | 270.206 | 845.545 | 0.854049 | 11.7288 | 249.048 | 179.599 | 265.7669 | 21196.12 |
| 85468.8 | 13.1441 | 0.785036 | 154.805 | 1.1511 | 407.445 | 0.635814 | 344.13 | 254.374 | 0.886605 | 473.037 | 604.276 | 0.929625 | 49.1681 | 154.059 | 145.279 | 161.8239 | 9924.009 |
| 74342.1 | 17.2236 | 0.814044 | 155.443 | 2.17686 | 551.736 | 0.595951 | 302.552 | 472.31 | 0.860874 | 424.559 | 625.877 | 0.780885 | 173.878 | 234.685 | 336.337 | 206.0199 | 13838.99 |
| 31642.4 | 31.4885 | 0.925374 | 120.875 | 0.632235 | 508.094 | 0.572751 | 414.705 | 221.865 | 0.951527 | 380.21 | 846.318 | 0.365552 | 56.2012 | 77.7297 | 46.4613 | 283.0092 | 24043.14 |
| 51389.1 | 20.8721 | 0.873884 | 169.167 | 2.84001 | 351.764 | 0.369744 | 186.64 | 964.716 | 0.844252 | 178.445 | 184.01 | 0.818345 | 114.185 | 105.484 | 158.554 | 268.1476 | 21071.75 |
| 84803.7 | 14.202 | 0.78677 | 45.0395 | 1.58609 | 263.992 | 0.405146 | 239.049 | 294.966 | 0.853615 | 425.495 | 87.0819 | 0.667299 | 80.3587 | 205.658 | 74.7578 | 215.0063 | 16068.79 |

Table B5. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 377.48.

| X1 | X2 | X3 | X4 | X5 | X6 | X7 | X8 | X9 | X10 | X11 | X12 | X13 | X14 | X15 | X16 | UED | UPC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 29390.9 | 25 | 0.95 | 100 | 1.1 | 0.4 | 0.482 | 110 | 0.6 | 0.895 | 130 | 30.9048 | 0.939426 | 100 | 100 | 100 | 57.25093 | 4040.298 |
| 59288 | 17.6905 | 0.893363 | 170.179 | 0.296515 | 790.633 | 0.662008 | 92.4632 | 483.79 | 0.430934 | 355.063 | 93.7434 | 0.957742 | 28.0802 | 54.8166 | 59.0281 | 267.9449 | 22410.24 |
| 41396.1 | 16.9121 | 0.927253 | 28.5209 | 3.16228 | 427.383 | 0.251273 | 120.614 | 825.929 | 0.63046 | 430.681 | 219.425 | 0.79531 | 67.1463 | 106.088 | 206.66 | 408.1467 | 42642.21 |
| 78853.7 | 13.0145 | 0.856299 | 53.2696 | 1.36906 | 42.6435 | 0.299247 | 100.418 | 505.928 | 0.518891 | 407.598 | 181.723 | 0.659525 | 1.43102 | 70.0482 | 369.785 | 430.5279 | 24874.45 |
| 42158.6 | 15.85 | 0.925808 | 77.109 | 2.23043 | 411.681 | 0.495209 | 236.561 | 648.318 | 0.570087 | 306.736 | 384.937 | 0.485005 | 57.4173 | 198.618 | 260.409 | 384.5632 | 31007.79 |
| 47490.5 | 14.9106 | 0.915708 | 98.9691 | 1.88092 | 393.09 | 0.33179 | 439.361 | 61.8264 | 0.674021 | 179.756 | 237.762 | 0.451636 | 81.472 | 339.841 | 178.502 | 404.9796 | 43163.63 |
| 36378.6 | 23.9881 | 0.936763 | 161.851 | 2.13465 | 387.032 | 0.233226 | 114.252 | 860.457 | 0.793034 | 186.003 | 940.92 | 0.812875 | 102.178 | 66.5879 | 144.387 | 449.7723 | 40592.61 |
| 38160.7 | 13.6342 | 0.933379 | 163.939 | 0.787399 | 340.856 | 0.238794 | 174.918 | 904.894 | 0.740301 | 439.068 | 36.9244 | 0.487163 | 74.1839 | 56.0726 | 256.333 | 696.9632 | 63545.56 |
| 30759.1 | 21.3518 | 0.947405 | 51.9845 | 0.190107 | 260.93 | 0.240855 | 456.366 | 726.841 | 0.553279 | 303.121 | 283.518 | 0.589421 | 16.8841 | 116.295 | 179.788 | 528.7861 | 50950.61 |
| 57870.3 | 13.8489 | 0.896046 | 35.2537 | 2.10917 | 524.468 | 0.399828 | 212.965 | 240.886 | 0.486338 | 465.204 | 406.367 | 0.586104 | 11.9928 | 59.6143 | 345.821 | 441.8617 | 45667.07 |
| 41922.7 | 15.2533 | 0.926254 | 20.1551 | 3.59516 | 699.31 | 0.426614 | 199.998 | 569.334 | 0.76489 | 403.424 | 617.422 | 0.368968 | 82.3001 | 174.567 | 360.803 | 519.5826 | 54070.47 |
| 26902.2 | 23.3684 | 0.954713 | 94.8105 | 2.4302 | 779.392 | 0.244358 | 344.982 | 614.963 | 0.844502 | 465.394 | 139.406 | 0.709507 | 105.95 | 260.921 | 340.434 | 397.781 | 53717.29 |
| 62881.9 | 18.5277 | 0.886556 | 171.491 | 3.34391 | 766.585 | 0.482398 | 184.155 | 551.523 | 0.772725 | 257.616 | 598.746 | 0.803449 | 22.5525 | 131.42 | 96.665 | 287.2476 | 25678.05 |
| 29266.8 | 26.9358 | 0.950237 | 51.9277 | 2.82805 | 66.308 | 0.147542 | 429.569 | 27.8294 | 0.530687 | 502.964 | 339.653 | 0.486139 | 139.52 | 74.0282 | 190.236 | 680.917 | 55162.48 |
| 87599.9 | 13.5282 | 0.839732 | 89.7789 | 1.94773 | 752.363 | 0.396241 | 286.773 | 388.915 | 0.977374 | 163.84 | 995.493 | 0.887379 | 48.4202 | 115.047 | 98.6535 | 288.9599 | 25396.73 |
| 45225.5 | 15.3697 | 0.919998 | 44.7013 | 1.02539 | 316.307 | 0.292252 | 336.186 | 977.799 | 0.689164 | 128.415 | 609.759 | 0.793286 | 85.0467 | 136.03 | 114.951 | 368.506 | 31209.85 |
| 55649.6 | 15.8059 | 0.900253 | 119.177 | 1.27964 | 539.026 | 0.539454 | 343.968 | 187.766 | 0.863897 | 70.5163 | 95.4032 | 0.509161 | 106.492 | 325.727 | 59.7175 | 210.749 | 18984.93 |
| 28863.5 | 17.4076 | 0.950992 | 103.764 | 1.46045 | 290.22 | 0.211533 | 290.456 | 115.872 | 0.876746 | 395.021 | 429.705 | 0.691788 | 124.73 | 46.6036 | 356.278 | 300.1986 | 31866.97 |
| 49722.1 | 16.5938 | 0.911482 | 81.2702 | 1.43533 | 257.551 | 0.524868 | 370.223 | 222.524 | 0.354885 | 369.043 | 333.12 | 0.897944 | 53.5177 | 288.951 | 319.466 | 288.3061 | 21844.26 |
| 57516.9 | 20.031 | 0.896719 | 159.39 | 1.37742 | 600.026 | 0.610925 | 384.305 | 438.683 | 0.234468 | 369.283 | 73.9495 | 0.746909 | 37.2026 | 297.857 | 48.0243 | 510.6253 | 44877.1 |
| 57501.5 | 16.9613 | 0.896746 | 124.292 | 3.53545 | 432.271 | 0.512602 | 288.941 | 718.875 | 0.551986 | 210.431 | 854.195 | 0.806067 | 94.0989 | 90.2612 | 178.431 | 316.627 | 22685.68 |
| 31524.9 | 20.453 | 0.945954 | 106.362 | 1.74148 | 209.04 | 0.398435 | 480.298 | 986.919 | 0.36478 | 373.305 | 835.892 | 0.803006 | 52.1863 | 370.907 | 317.531 | 404.9195 | 31936.78 |
| 42112.9 | 18.033 | 0.925896 | 46.6418 | 2.902 | 491.557 | 0.219201 | 217.515 | 914.33 | 0.858107 | 101.858 | 912.276 | 0.606262 | 14.366 | 65.3608 | 96.493 | 567.8572 | 57357.45 |
| 39049.3 | 14.2944 | 0.931697 | 119.572 | 2.21734 | 717.103 | 0.453717 | 300.319 | 325.005 | 0.862225 | 259.226 | 657.097 | 0.249631 | 110.389 | 122.713 | 142.121 | 589.9974 | 63506.41 |
| 48539.2 | 15.8619 | 0.913722 | 33.862 | 2.00797 | 812.31 | 0.490811 | 205.213 | 29.0238 | 0.43755 | 292.572 | 687.27 | 0.65289 | 126.783 | 165.918 | 179.458 | 347.711 | 37194.9 |
| 60385 | 18.4839 | 0.891285 | 106.189 | 2.16808 | 129.611 | 0.366139 | 301.385 | 316.634 | 0.444526 | 206.71 | 22.5305 | 0.713264 | 99.0978 | 110.535 | 174.803 | 331.0667 | 23907.4 |
| 43556.3 | 18.224 | 0.923162 | 95.907 | 1.69816 | 330.689 | 0.615149 | 342.891 | 487.574 | 0.969526 | 360.423 | 475.036 | 0.829337 | 27.9262 | 187.483 | 220.822 | 195.9205 | 12888.29 |
| 31151.9 | 23.3966 | 0.946663 | 96.5056 | 2.13203 | 196.641 | 0.334341 | 265.865 | 741.613 | 0.2542 | 105.296 | 874.007 | 0.713614 | 150.543 | 184.308 | 55.8238 | 616.9859 | 53389.28 |
| 86599.5 | 14.2915 | 0.841628 | 21.793 | 2.06103 | 348.708 | 0.244043 | 147.568 | 195.464 | 0.530043 | 439.817 | 798.414 | 0.75203 | 113.126 | 142.972 | 311.374 | 583.2058 | 50665.35 |
| 56947.3 | 15.2497 | 0.897795 | 69.7662 | 3.56372 | 867.269 | 0.465026 | 203.182 | 752.861 | 0.798986 | 160.948 | 172.109 | 0.63465 | 152.977 | 129.543 | 130.655 | 309.3775 | 30865.07 |
| 72791.9 | 17.533 | 0.867783 | 37.47 | 3.15709 | 390.607 | 0.169172 | 49.6093 | 110.627 | 0.944958 | 96.8585 | 838.377 | 0.631551 | 89.5696 | 35.2784 | 69.4232 | 556.4014 | 53991.88 |
| 49943.4 | 21.4078 | 0.911066 | 115.216 | 3.741 | 600.362 | 0.333197 | 161.956 | 561.302 | 0.573138 | 441.363 | 922.546 | 0.543755 | 164.71 | 68.8269 | 430.383 | 583.8716 | 61312.33 |
| 53401.4 | 13.3293 | 0.90451 | 84.7695 | 2.02768 | 22.2 | 0.3974 | 493.292 | 537.467 | 0.552284 | 257.01 | 611.447 | 0.3479 | 8.35309 | 295.644 | 191 | 545.2277 | 31833.37 |
| 45980.2 | 22.6406 | 0.918574 | 53.1943 | 1.61305 | 514.22 | 0.330873 | 465.107 | 903.526 | 0.695237 | 474.77 | 385.861 | 0.769524 | 21.2789 | 271.707 | 395.539 | 354.2565 | 34652.42 |
| 54612.7 | 17.5409 | 0.902218 | 168.562 | 1.12026 | 869.918 | 0.291142 | 454.355 | 341.291 | 0.728676 | 474.022 | 754.747 | 0.719793 | 72.7119 | 243.492 | 276.633 | 534.5896 | 59910.74 |
| 35206.4 | 13.092 | 0.938975 | 69.9462 | 2.39193 | 68.5151 | 0.401289 | 228.989 | 423.984 | 0.880423 | 486.668 | 306.847 | 0.400411 | 3.67794 | 64.5733 | 400.107 | 284.6685 | 19036.45 |
| 67785.5 | 15.9955 | 0.877266 | 124.126 | 3.40427 | 955.98 | 0.284633 | 467.012 | 773.933 | 0.854154 | 355.74 | 831.06 | 0.673008 | 99.7522 | 142.362 | 88.7556 | 538.3365 | 60329.04 |
| 49190 | 18.6372 | 0.912491 | 125.605 | 2.051 | 696.832 | 0.450644 | 169.396 | 940.586 | 0.391465 | 510.394 | 104.128 | 0.707761 | 132.309 | 142.1 | 216.169 | 482.2018 | 49976.98 |
| 70946.1 | 17.3854 | 0.87128 | 120.805 | 0.473304 | 704.224 | 0.436252 | 366.845 | 350.941 | 0.518716 | 322.62 | 726.955 | 0.523176 | 18.0098 | 50.6903 | 169.579 | 606.892 | 58031.77 |
| 30123.9 | 23.8498 | 0.94861 | 159.138 | 1.51466 | 612.58 | 0.613271 | 152.481 | 19.7725 | 0.722733 | 343.592 | 424.554 | 0.702003 | 110.37 | 65.243 | 309.965 | 154.9238 | 14677.02 |
| 47848.1 | 19.7605 | 0.915034 | 100.58 | 2.53132 | 868.34 | 0.313599 | 352.143 | 170.366 | 0.822654 | 304.967 | 511.211 | 0.555518 | 36.6561 | 59.7115 | 218.716 | 432.6993 | 56059.48 |
| 44032.5 | 15.1937 | 0.922258 | 120.122 | 0.354569 | 125.768 | 0.149497 | 75.5827 | 231.678 | 0.902813 | 492.053 | 228.846 | 0.947909 | 28.0746 | 69.4273 | 77.2984 | 572.022 | 44450.31 |
| 63496.9 | 18.4019 | 0.885391 | 168.862 | 1.64419 | 33.9371 | 0.47553 | 346.778 | 208.877 | 0.906832 | 408.367 | 156.155 | 0.370798 | 105.861 | 227.373 | 145.879 | 326.5791 | 18887.83 |
| 86177.1 | 13.9188 | 0.842427 | 136.531 | 0.585058 | 142.968 | 0.614801 | 309.592 | 345.458 | 0.904246 | 436.599 | 541.931 | 0.815626 | 4.46054 | 291.243 | 270.531 | 184.4578 | 10528.75 |
| 29464.3 | 25.0068 | 0.949861 | 30.1253 | 2.98583 | 125.994 | 0.40748 | 213.268 | 706.195 | 0.717706 | 516.09 | 77.4379 | 0.232536 | 45.5119 | 163.811 | 312.479 | 621.4617 | 45164.58 |
| 70393.8 | 13.9537 | 0.872324 | 112.793 | 2.24223 | 580.77 | 0.552169 | 402.373 | 938.129 | 0.60149 | 343.257 | 693.154 | 0.639156 | 19.1124 | 308.77 | 244.88 | 470.4473 | 34064.39 |
| 27235.3 | 15.1955 | 0.954075 | 112.669 | 0.425165 | 245.631 | 0.320172 | 287.553 | 765.052 | 0.875098 | 501.644 | 703.139 | 0.971832 | 1.86754 | 85.3099 | 178.336 | 268.5129 | 20804.16 |
| 34065.7 | 20.1134 | 0.94114 | 128.49 | 1.66625 | 427.174 | 0.412327 | 58.5846 | 767.622 | 0.726844 | 455.136 | 215.227 | 0.81504 | 90.6719 | 49.2972 | 59.5594 | 242.5378 | 21849.48 |
| 52568.4 | 18.4346 | 0.906091 | 153.618 | 2.22383 | 141.893 | 0.543757 | 141.981 | 594.612 | 0.812435 | 513.114 | 698.766 | 0.421652 | 153.853 | 61.184 | 196.317 | 365.2101 | 22632.17 |
| 58122.3 | 13.1216 | 0.895568 | 24.685 | 3.32983 | 356.438 | 0.415679 | 117.795 | 621.991 | 0.583148 | 511.69 | 583.781 | 0.512344 | 128.6 | 76.8752 | 346.878 | 449.468 | 37090.36 |
| 52344.1 | 21.8762 | 0.906519 | 143.888 | 1.56011 | 472.892 | 0.48589 | 152.796 | 88.1917 | 0.605755 | 234.17 | 425.02 | 0.952319 | 63.7021 | 130.234 | 145.878 | 199.0347 | 17944.82 |
| 42912.4 | 22.5404 | 0.924385 | 84.9175 | 2.50848 | 192.592 | 0.434088 | 429.641 | 787.637 | 0.570672 | 422.999 | 464.712 | 0.582677 | 172.091 | 131.294 | 270.169 | 352.1303 | 25509.65 |
| 77774.6 | 16.351 | 0.858345 | 72.7329 | 1.19966 | 338.796 | 0.485368 | 349.884 | 369.221 | 0.336921 | 325.111 | 424.126 | 0.674592 | 17.848 | 99.7591 | 92.286 | 460.6307 | 35852.4 |
| 59803.4 | 20.715 | 0.892389 | 136.405 | 1.10554 | 209.928 | 0.650327 | 238.518 | 113.745 | 0.957632 | 443.514 | 862.261 | 0.83739 | 107.766 | 203.431 | 423.394 | 169.3508 | 10115.16 |
| 65250.4 | 16.9834 | 0.882068 | 144.882 | 1.69138 | 178.384 | 0.404981 | 317.302 | 225.058 | 0.795467 | 337.772 | 32.9712 | 0.299871 | 99.4443 | 141.461 | 200.995 | 508.0205 | 36190.4 |
| 62427.7 | 18.5398 | 0.887416 | 135.249 | 1.17913 | 658.057 | 0.512358 | 219.239 | 48.6708 | 0.728665 | 212.913 | 752.41 | 0.871877 | 19.9507 | 50.4151 | 71.0946 | 219.7748 | 19579.87 |
| 25847.7 | 17.3714 | 0.956705 | 160.409 | 1.96766 | 472.594 | 0.529201 | 289.411 | 272.577 | 0.394187 | 203.922 | 342.279 | 0.993487 | 16.0278 | 215.568 | 121.538 | 223.6103 | 22163.49 |
| 80870.6 | 15.3493 | 0.85248 | 131.447 | 2.72483 | 23.2389 | 0.439789 | 229.592 | 209.371 | 0.923744 | 385.434 | 852.121 | 0.910093 | 52.8387 | 171.113 | 89.0814 | 189.9662 | 10231.23 |
| 45619.6 | 13.7064 | 0.919251 | 124.57 | 2.47181 | 874.561 | 0.297577 | 202.028 | 607.918 | 0.947938 | 334.117 | 673.622 | 0.608031 | 148.564 | 143.066 | 252.709 | 450.028 | 51877.98 |
| 48426 | 20.2703 | 0.913939 | 122.732 | 1.3651 | 252.996 | 0.404802 | 352.35 | 164.329 | 0.899587 | 457.778 | 74.5158 | 0.41043 | 7.1793 | 143.037 | 298.036 | 287.1665 | 24430.81 |
| 47261.5 | 22.988 | 0.916147 | 129.287 | 2.04226 | 608.406 | 0.466685 | 413.662 | 537.112 | 0.515485 | 162.558 | 75.4916 | 0.490646 | 133.278 | 309.533 | 141.286 | 460.7722 | 46747.19 |
| 40785.2 | 23.5563 | 0.928415 | 46.927 | 0.847511 | 446.261 | 0.354825 | 377.246 | 697.779 | 0.881082 | 450.455 | 217.638 | 0.550091 | 83.593 | 181.13 | 226.071 | 335.6269 | 31743.23 |
| 84478.9 | 13.7823 | 0.845644 | 84.3841 | 2.09627 | 43.8996 | 0.269721 | 295.191 | 722.321 | 0.416624 | 199.865 | 195.027 | 0.882293 | 68.0046 | 178.449 | 111.623 | 464.6911 | 26522.76 |
| 29861.4 | 20.9234 | 0.949105 | 144.235 | 1.59765 | 2.2149 | 0.608678 | 241.714 | 833.618 | 0.27513 | 400.554 | 690.574 | 0.62799 | 157.631 | 145.581 | 386.959 | 566.3349 | 34141.49 |
| 33479.8 | 15.9432 | 0.942247 | 144.208 | 1.74832 | 350.965 | 0.351124 | 351.696 | 198.292 | 0.729426 | 445.463 | 107.244 | 0.757337 | 141.862 | 68.2846 | 226.557 | 219.8698 | 22297.77 |
| 61290 | 18.9284 | 0.889571 | 90.0779 | 0.439043 | 195.946 | 0.265589 | 491.495 | 995.018 | 0.718768 | 99.5189 | 218.43 | 0.791363 | 14.5078 | 392.592 | 74.231 | 381.0081 | 28054.8 |
| 73240 | 16.9963 | 0.866934 | 30.7272 | 1.74229 | 330.051 | 0.316216 | 376.655 | 381.845 | 0.625525 | 489.602 | 352.678 | 0.748917 | 58.2394 | 214.049 | 229.421 | 361.0894 | 30913.95 |
| 34635 | 20.3064 | 0.940062 | 133.243 | 2.05079 | 656.058 | 0.505479 | 128.247 | 852.306 | 0.603776 | 398.581 | 266.07 | 0.307614 | 43.2892 | 66.3393 | 183.891 | 671.8595 | 64222.54 |
| 52260.4 | 13.474 | 0.906672 | 91.8027 | 2.77478 | 30.8176 | 0.185671 | 426.766 | 320.977 | 0.737763 | 414.993 | 422.542 | 0.972397 | 138.082 | 356.574 | 394.923 | 285.2959 | 17827.12 |
| 35720.4 | 19.9181 | 0.938006 | 36.6987 | 1.19317 | 168.476 | 0.327038 | 283.789 | 55.7937 | 0.372097 | 464.476 | 438.407 | 0.432591 | 57.0556 | 134.239 | 242.436 | 589.2251 | 52552.26 |
| 26421.9 | 21.8759 | 0.955621 | 32.3642 | 0.259621 | 663.578 | 0.426806 | 395.364 | 629.336 | 0.305711 | 290.344 | 774.175 | 0.766833 | 14.0057 | 178.428 | 135.666 | 502.5583 | 58683.18 |
| 28230.8 | 23.6542 | 0.952196 | 100.728 | 1.74249 | 373.838 | 0.360763 | 385.768 | 460.637 | 0.217212 | 74.1027 | 905.047 | 0.854428 | 135.447 | 77.6696 | 53.3298 | 598.9955 | 63094.89 |
| 46371.4 | 22.1116 | 0.917833 | 158.356 | 1.39952 | 142.587 | 0.399694 | 357.187 | 197.219 | 0.494163 | 422.636 | 534.454 | 0.691199 | 121.033 | 325.653 | 273.66 | 346.3484 | 24941.36 |
| 25914.3 | 18.1111 | 0.956579 | 158.432 | 1.56685 | 179.526 | 0.225497 | 225.518 | 243.768 | 0.929399 | 187.069 | 663.778 | 0.448918 | 46.058 | 85.3388 | 185.714 | 454.1351 | 39506 |
| 70493.7 | 16.8908 | 0.872136 | 30.1899 | 1.07206 | 27.5936 | 0.146594 | 117.873 | 405.874 | 0.526983 | 440.477 | 478.745 | 0.7803 | 105.075 | 62.252 | 164.737 | 648.2922 | 37876.5 |
| 60285.3 | 19.9682 | 0.891475 | 41.8093 | 2.48832 | 729.495 | 0.263606 | 214.845 | 812.989 | 0.777768 | 289.105 | 877.532 | 0.793012 | 25.1432 | 190.489 | 278.24 | 479.0813 | 51093.94 |
| 31843.5 | 25.1063 | 0.945354 | 84.9536 | 0.957905 | 325.636 | 0.419125 | 218.596 | 850.035 | 0.310326 | 312.046 | 653.088 | 0.835071 | 83.9442 | 119.885 | 218.466 | 420.7039 | 37952.53 |
| 34804.5 | 19.7932 | 0.939741 | 41.8878 | 1.81006 | 58.2557 | 0.449135 | 236.891 | 325.412 | 0.647195 | 159.693 | 583.1 | 0.728143 | 64.6941 | 44.7013 | 61.0656 | 197.0941 | 12789.29 |
| 67802 | 15.6386 | 0.877234 | 131.713 | 0.898054 | 550.706 | 0.28233 | 244.652 | 181.183 | 0.878795 | 492.171 | 162.769 | 0.861077 | 40.2318 | 212.305 | 435.248 | 300.2448 | 30779.98 |
| 50450.8 | 18.3819 | 0.910103 | 19.1701 | 1.20882 | 267.568 | 0.432642 | 192.554 | 769.453 | 0.666976 | 341.098 | 680.641 | 0.827064 | 61.2692 | 145.872 | 59.9147 | 268.8879 | 19598.66 |
| 39811.7 | 14.4634 | 0.930252 | 122.49 | 1.55997 | 636.84 | 0.352213 | 296.89 | 509.742 | 0.369753 | 210.614 | 596.488 | 0.792304 | 12.4571 | 87.3193 | 133.803 | 538.0094 | 61520.49 |
| 42225 | 21.2585 | 0.925686 | 126.651 | 0.132774 | 490.94 | 0.325955 | 52.6101 | 573.637 | 0.389122 | 105.205 | 629.47 | 0.943664 | 4.4325 | 46.8337 | 82.1183 | 522.0765 | 51084.27 |
| 42839.5 | 22.8179 | 0.924523 | 39.7066 | 0.567314 | 102.148 | 0.21114 | 398.304 | 939.5 | 0.695674 | 120.204 | 673.892 | 0.534729 | 24.931 | 255.466 | 106.486 | 564.0125 | 40094.42 |
| 38850 | 17.4402 | 0.932076 | 58.5713 | 1.92102 | 383.02 | 0.493144 | 325.808 | 899.844 | 0.558117 | 351.227 | 169.408 | 0.581939 | 26.6096 | 154.181 | 191.136 | 335.2203 | 26503.17 |
| 30568.7 | 23.379 | 0.947767 | 154.48 | 1.01483 | 322.893 | 0.558238 | 357.151 | 620.799 | 0.320234 | 418.436 | 869.884 | 0.751886 | 80.2948 | 216.12 | 272.53 | 400.2872 | 31969.95 |
| 82289.1 | 14.4303 | 0.849792 | 149.856 | 2.67989 | 574.185 | 0.205238 | 151.439 | 625.834 | 0.772706 | 324.13 | 764.073 | 0.870732 | 17.7845 | 129.06 | 275.68 | 583.4023 | 56335.64 |
| 47556.3 | 19.8185 | 0.915586 | 156.607 | 1.37427 | 797.922 | 0.618897 | 72.9843 | 851.485 | 0.698947 | 76.4193 | 90.8099 | 0.891326 | 89.0331 | 47.9878 | 51.0875 | 202.5169 | 16638.92 |
| 47518.9 | 16.3241 | 0.915655 | 32.6631 | 1.72474 | 260.177 | 0.493906 | 203.806 | 730.262 | 0.675519 | 446.184 | 148.315 | 0.532498 | 115.844 | 108.088 | 261.443 | 296.4915 | 20842.07 |
| 27941 | 24.8423 | 0.952746 | 146.07 | 1.5351 | 437.618 | 0.573622 | 286.483 | 767.383 | 0.351426 | 507.135 | 951.937 | 0.775535 | 64.742 | 72.0015 | 115.665 | 372.9615 | 30487.7 |
| 39730.2 | 18.2489 | 0.930409 | 52.1716 | 1.09712 | 349.966 | 0.305529 | 83.7261 | 364.213 | 0.748385 | 443.763 | 548.128 | 0.83064 | 75.6188 | 66.2911 | 262.355 | 261.204 | 24804.48 |
| 32713.4 | 23.19 | 0.943705 | 23.6518 | 0.554165 | 17.8832 | 0.187238 | 102.769 | 654.321 | 0.514161 | 442.355 | 911.074 | 0.989432 | 4.57285 | 71.9127 | 407.188 | 375.8848 | 23894.72 |
| 59833.5 | 18.521 | 0.89233 | 153.669 | 0.233118 | 203.931 | 0.4367 | 365.512 | 186.356 | 0.823309 | 56.2497 | 39.7804 | 0.875537 | 19.4923 | 326.189 | 44.9719 | 180.2543 | 12996.56 |
| 32298.1 | 19.6353 | 0.944488 | 168.815 | 0.462342 | 219.072 | 0.553073 | 361.541 | 264.043 | 0.836274 | 84.6805 | 90.0349 | 0.502867 | 23.1697 | 162.32 | 67.612 | 217.5668 | 16671.08 |
| 47379 | 16.4722 | 0.91592 | 132.15 | 1.35042 | 854.936 | 0.379604 | 196.498 | 420.833 | 0.636481 | 394.112 | 746.72 | 0.888943 | 131 | 159.956 | 241.427 | 346.1754 | 37956.32 |
| 50765.2 | 16.6998 | 0.909506 | 48.419 | 2.67796 | 827.407 | 0.525889 | 428.52 | 643.359 | 0.298133 | 342.794 | 613.086 | 0.988805 | 267.307 | 338.844 | 232.843 | 453.0341 | 42421.2 |
| 35952 | 22.4854 | 0.937569 | 68.6633 | 0.715555 | 730.009 | 0.375134 | 472.685 | 920.677 | 0.50125 | 305.278 | 653.137 | 0.670131 | 55.2826 | 441.589 | 294.609 | 500.1984 | 55928.23 |
| 25032 | 25.3517 | 0.958257 | 123.688 | 3.05263 | 340.08 | 0.174165 | 396.645 | 669.673 | 0.756854 | 117.661 | 662.916 | 0.931839 | 29.1588 | 110.09 | 80.5525 | 421.7944 | 44216.95 |
| 64506.9 | 19.129 | 0.883478 | 94.3628 | 2.87486 | 582.559 | 0.462222 | 204.133 | 769.882 | 0.955365 | 87.9833 | 602.951 | 0.39862 | 172.121 | 138.241 | 56.2648 | 457.3001 | 37144.76 |
| 56241 | 16.7826 | 0.899134 | 43.0458 | 1.76222 | 645.41 | 0.443453 | 236.504 | 578.761 | 0.387026 | 326.931 | 680.97 | 0.564526 | 103.622 | 94.8859 | 145.566 | 592.7463 | 60075.88 |
| 37783.6 | 21.312 | 0.934099 | 170.132 | 0.301951 | 809.24 | 0.608628 | 283.149 | 213.35 | 0.181091 | 392.017 | 314.452 | 0.822695 | 17.8189 | 223.949 | 321.737 | 634.7454 | 64709.3 |
| 31328.4 | 23.5722 | 0.946329 | 52.7522 | 1.53352 | 894.162 | 0.269646 | 218.007 | 183.961 | 0.920932 | 127.89 | 520.969 | 0.964856 | 11.3682 | 140.307 | 76.9112 | 312.2744 | 42082.81 |
| 37964.5 | 24.9174 | 0.93376 | 110.968 | 3.60838 | 399.109 | 0.406697 | 372.73 | 147.864 | 0.476339 | 125.786 | 47.181 | 0.539449 | 137.127 | 314.53 | 46.1536 | 355.005 | 38278.24 |
| 51501.5 | 17.9341 | 0.908112 | 59.3854 | 3.48989 | 674.336 | 0.438596 | 476.734 | 126.655 | 0.637858 | 236.181 | 47.7932 | 0.659737 | 14.5057 | 295.638 | 72.4112 | 256.7946 | 30310.35 |
| 36083.3 | 15.3187 | 0.937315 | 127.249 | 1.29434 | 814.197 | 0.463203 | 132.878 | 685.32 | 0.447626 | 107.097 | 239.32 | 0.898875 | 11.4972 | 118.696 | 80.766 | 327.229 | 36925.1 |
| 54611.7 | 20.276 | 0.902222 | 66.5677 | 3.48254 | 197.003 | 0.502608 | 216.013 | 487.801 | 0.601256 | 258.101 | 262.367 | 0.25211 | 182.757 | 100.183 | 210.001 | 631.2257 | 42501.07 |
| 39852.1 | 20.4097 | 0.93018 | 89.8404 | 0.692111 | 424.821 | 0.234698 | 304.709 | 629.26 | 0.783931 | 130.106 | 321.262 | 0.903358 | 59.7814 | 72.5156 | 89.0123 | 325.1988 | 33600.21 |
| 39715.7 | 15.4414 | 0.930435 | 121.598 | 2.93131 | 4.84689 | 0.510249 | 247.639 | 854.199 | 0.593384 | 157.647 | 849.373 | 0.442398 | 188.069 | 164.734 | 112.956 | 441.0012 | 24878.9 |
| 30912.8 | 20.7463 | 0.947113 | 60.0985 | 2.00612 | 918.024 | 0.389559 | 336.417 | 34.0887 | 0.51198 | 437.096 | 853.323 | 0.611854 | 65.1091 | 234.827 | 175.128 | 452.2834 | 61242.29 |
| 54949.3 | 17.0861 | 0.901581 | 96.3617 | 1.15829 | 644.943 | 0.367206 | 401.298 | 92.1132 | 0.8559 | 317.373 | 852.793 | 0.845547 | 113.796 | 332.675 | 132.472 | 252.9131 | 25591.74 |
| 73455.3 | 16.0495 | 0.866526 | 170.208 | 0.847439 | 586.065 | 0.694974 | 498.868 | 927.21 | 0.533832 | 118.698 | 894.776 | 0.555632 | 27.4741 | 393.251 | 51.7742 | 471.1292 | 30236.28 |
| 33416 | 18.597 | 0.94237 | 81.2768 | 0.332518 | 352.933 | 0.437498 | 65.8172 | 639.248 | 0.612688 | 426.386 | 429.421 | 0.700668 | 8.33478 | 45.7312 | 390.255 | 286.7132 | 24829.7 |
| 69253.7 | 14.7709 | 0.874484 | 160.169 | 1.35525 | 889.061 | 0.583227 | 303.632 | 601.085 | 0.714471 | 49.7318 | 730.938 | 0.946086 | 129.294 | 271.494 | 47.0953 | 255.2072 | 20624.44 |
| 47850.4 | 16.226 | 0.915027 | 160.637 | 2.56717 | 87.3571 | 0.305603 | 218.177 | 617.61 | 0.868445 | 210.512 | 598.583 | 0.716738 | 125.511 | 165.128 | 125.319 | 303.6492 | 19542.44 |
| 63147 | 14.2516 | 0.886051 | 118.583 | 0.425631 | 187.861 | 0.474836 | 163.118 | 122.848 | 0.523561 | 281.557 | 459.019 | 0.403449 | 39.8967 | 101.876 | 84.6812 | 487.9149 | 34418.53 |
| 29560.7 | 26.4671 | 0.94968 | 40.581 | 1.05978 | 373.978 | 0.229344 | 258.038 | 496.13 | 0.612172 | 92.7098 | 230.555 | 0.555499 | 95.165 | 124.081 | 90.9775 | 533.4948 | 60007.77 |
| 30768.5 | 18.5206 | 0.947385 | 40.7535 | 1.83232 | 355.641 | 0.249213 | 225.196 | 961.525 | 0.680001 | 199.554 | 89.4438 | 0.666265 | 61.9641 | 156.871 | 156.834 | 420.5682 | 42715 |
| 33115.1 | 25.3351 | 0.942946 | 102.884 | 2.63102 | 165.172 | 0.498877 | 392.051 | 118.903 | 0.537724 | 450.42 | 721.516 | 0.73092 | 50.5243 | 218.249 | 158.691 | 206.2107 | 14921.73 |
| 33500.6 | 26.1481 | 0.942217 | 163.638 | 1.8388 | 797.242 | 0.554996 | 155.171 | 264.32 | 0.56614 | 327.341 | 189.818 | 0.529001 | 91.5191 | 136.07 | 158.662 | 327.6074 | 35693.7 |
| 38818.8 | 18.7083 | 0.932136 | 69.2163 | 2.73992 | 27.89 | 0.18696 | 214.545 | 664.589 | 0.541535 | 120.877 | 578.737 | 0.842124 | 128.129 | 167.869 | 111.414 | 406.8419 | 26234.44 |
| 35556.7 | 15.5412 | 0.938313 | 52.6193 | 2.51802 | 97.9886 | 0.457074 | 420.513 | 225.132 | 0.133162 | 441.746 | 447.903 | 0.942704 | 174.773 | 115.195 | 279.296 | 502.033 | 37648.28 |
| 37674.8 | 20.4814 | 0.934304 | 156.93 | 1.73525 | 806.463 | 0.434964 | 464.142 | 700.07 | 0.903802 | 237.177 | 347.537 | 0.777615 | 82.5498 | 376.845 | 187.961 | 260.7505 | 26126.94 |
| 44659.2 | 14.0164 | 0.92107 | 164.593 | 1.68766 | 465.772 | 0.571465 | 189.512 | 207.214 | 0.33158 | 479.383 | 500.811 | 0.973146 | 123.59 | 95.9486 | 376.814 | 285.9805 | 24744.96 |
| 48961.8 | 15.014 | 0.912921 | 154.361 | 0.557059 | 283.428 | 0.565217 | 64.0021 | 815.285 | 0.928271 | 439.998 | 353.619 | 0.436638 | 40.1927 | 59.6068 | 260.864 | 372.1232 | 24609.82 |
| 63958.9 | 14.5615 | 0.884513 | 130.946 | 0.346895 | 585.027 | 0.257637 | 201.973 | 713.983 | 0.744286 | 155.473 | 315.345 | 0.94465 | 30.2486 | 66.7674 | 58.1872 | 427.7295 | 41777.21 |
| 72631.4 | 15.4036 | 0.868086 | 108.025 | 3.78836 | 281.774 | 0.415065 | 387.34 | 218.408 | 0.993928 | 144.709 | 699.005 | 0.639683 | 45.5505 | 180.068 | 108.174 | 235.6596 | 17325.25 |
| 34829.2 | 15.3084 | 0.939691 | 72.134 | 1.34592 | 450.913 | 0.449704 | 187.475 | 930.479 | 0.728032 | 457.179 | 480.52 | 0.521761 | 104.543 | 95.9066 | 451.448 | 373.7818 | 31668.82 |
| 47397.8 | 16.0609 | 0.915884 | 86.9298 | 3.00874 | 920.966 | 0.36338 | 440.059 | 128.149 | 0.411724 | 134.36 | 960.276 | 0.914406 | 75.1839 | 96.0369 | 71.0051 | 467.1148 | 58663.84 |
| 27133 | 22.3467 | 0.954274 | 31.0482 | 2.36547 | 812.628 | 0.405336 | 460.48 | 103.821 | 0.631806 | 212.819 | 482.351 | 0.472585 | 7.27695 | 115.873 | 198.626 | 405.3636 | 54789.64 |
| 44899.7 | 13.6815 | 0.920614 | 138.217 | 0.584008 | 531.473 | 0.474783 | 201.375 | 566.699 | 0.365632 | 120.321 | 650.433 | 0.75456 | 48.3424 | 174.41 | 114.131 | 463.1784 | 42667.78 |
| 54778.2 | 19.0446 | 0.901906 | 43.4826 | 1.04337 | 55.0817 | 0.250767 | 198.77 | 650.38 | 0.989153 | 219.887 | 553.92 | 0.539225 | 47.1414 | 156.858 | 131.027 | 374.8421 | 23046.58 |
| 59924.5 | 13.5246 | 0.892155 | 133.757 | 1.40699 | 442.259 | 0.187546 | 156.482 | 770.859 | 0.96614 | 465.184 | 948.539 | 0.911582 | 100.658 | 56.2104 | 281.986 | 636.1457 | 56880.82 |
| 28400.3 | 23.4516 | 0.951875 | 85.5695 | 0.505714 | 753.733 | 0.481464 | 148.44 | 851.016 | 0.425114 | 77.8723 | 25.1547 | 0.565414 | 4.31046 | 67.9852 | 59.6493 | 474.5914 | 53798.02 |
| 53240.2 | 17.6678 | 0.904818 | 106.686 | 3.32387 | 124.561 | 0.243575 | 471.961 | 128.752 | 0.742376 | 125.576 | 942.089 | 0.591826 | 76.8243 | 406.413 | 118.373 | 393.954 | 28881.38 |
| 80330.6 | 14.6754 | 0.853502 | 127.118 | 3.69023 | 580.357 | 0.331871 | 97.6088 | 970.949 | 0.562848 | 457.158 | 310.517 | 0.631549 | 88.4324 | 75.9843 | 424.424 | 595.0887 | 56065.28 |
| 52266 | 22.0095 | 0.906667 | 133.928 | 0.791657 | 982.839 | 0.488756 | 229.411 | 189.762 | 0.607492 | 434.586 | 898.653 | 0.523808 | 78.3138 | 67.5227 | 326.544 | 465.1329 | 50393.68 |
| 43668.6 | 14.0763 | 0.922947 | 60.195 | 2.90441 | 195.209 | 0.182859 | 433.421 | 531.08 | 0.871932 | 153.587 | 385.102 | 0.719687 | 107.099 | 137.86 | 114.734 | 375.4112 | 32150.96 |
| 49566.2 | 16.503 | 0.911777 | 171.772 | 1.74708 | 508.623 | 0.479497 | 354.048 | 668.867 | 0.556039 | 332.534 | 979.891 | 0.834439 | 121.488 | 289.685 | 56.9746 | 357.8587 | 28808.04 |
| 46243.6 | 16.6165 | 0.918071 | 48.9131 | 2.8776 | 82.271 | 0.372561 | 176.077 | 120.538 | 0.691287 | 338.434 | 161.504 | 0.441991 | 62.9557 | 151.928 | 156.277 | 284.7365 | 20318.51 |
| 72356.6 | 15.6482 | 0.868607 | 166.654 | 1.91787 | 606.513 | 0.320906 | 205.882 | 136.541 | 0.873633 | 287.056 | 258.169 | 0.39961 | 120.099 | 190.336 | 194.937 | 599.5756 | 59771.25 |
| 57832.4 | 13.9987 | 0.896118 | 107.096 | 2.08732 | 832.397 | 0.35701 | 295.291 | 921.154 | 0.784122 | 373.631 | 624.22 | 0.722224 | 38.2876 | 105.913 | 257.361 | 411.7086 | 42475.42 |
| 77009.2 | 16.7263 | 0.859795 | 66.8533 | 0.807365 | 743.806 | 0.479993 | 465.677 | 774.704 | 0.714994 | 418.068 | 7.43222 | 0.660624 | 7.7151 | 158.862 | 341.91 | 319.8901 | 29758.98 |
| 42525.7 | 16.7563 | 0.925113 | 40.0695 | 1.91954 | 281.956 | 0.454294 | 392.338 | 616.461 | 0.66472 | 498.956 | 820.251 | 0.784979 | 110.334 | 171.774 | 113.015 | 258.8662 | 19218.47 |
| 62132.9 | 17.5884 | 0.887974 | 24.9919 | 1.6323 | 467.138 | 0.344687 | 178.866 | 442.667 | 0.422702 | 455.274 | 18.8142 | 0.760163 | 55.8148 | 115.547 | 59.485 | 445.9984 | 45655.32 |
| 44189.9 | 23.6518 | 0.921966 | 99.3943 | 0.433876 | 382.227 | 0.437 | 411.907 | 910.528 | 0.948806 | 444.538 | 306.358 | 0.813344 | 19.5056 | 153.213 | 375.573 | 230.7562 | 17740.09 |
| 57525.6 | 14.6573 | 0.896699 | 30.7885 | 2.56003 | 362.304 | 0.256555 | 398.279 | 571.421 | 0.472289 | 481.147 | 39.8845 | 0.773291 | 106.898 | 112.982 | 304.245 | 499.5348 | 49559.96 |
| 46152.8 | 14.5097 | 0.918241 | 42.3609 | 0.815292 | 794.144 | 0.257645 | 480.959 | 16.8547 | 0.998895 | 297.344 | 985.37 | 0.81601 | 18.0009 | 52.1856 | 129.969 | 348.2489 | 42395.22 |
| 43233 | 13.571 | 0.923771 | 49.4751 | 3.33487 | 453.901 | 0.411567 | 475.275 | 648.804 | 0.574013 | 322.075 | 397.905 | 0.829758 | 46.9772 | 271.879 | 142.129 | 279.0199 | 26173.04 |
| 51463.9 | 13.9615 | 0.908181 | 170.563 | 2.5169 | 934.606 | 0.571314 | 172.991 | 856.222 | 0.440017 | 392.349 | 116.15 | 0.435962 | 151.409 | 50.9825 | 357.168 | 647.9734 | 62860.18 |
| 34443.5 | 24.7541 | 0.940429 | 120.628 | 2.54746 | 941.397 | 0.510979 | 430.489 | 138.185 | 0.478621 | 212.136 | 36.5895 | 0.596477 | 24.826 | 138.343 | 60.9915 | 303.0046 | 38433.36 |
| 83464.2 | 14.5697 | 0.847566 | 82.0183 | 2.50515 | 324.924 | 0.346286 | 445.456 | 364.334 | 0.425563 | 409.083 | 784.474 | 0.593344 | 150.659 | 330.144 | 211.263 | 631.0868 | 51091.01 |
| 25936.6 | 24.1906 | 0.956542 | 26.0554 | 1.26171 | 112.942 | 0.356119 | 259.694 | 40.1165 | 0.788743 | 450.521 | 429.006 | 0.981648 | 93.9412 | 130.058 | 100.819 | 123.3101 | 9829.276 |
| 30930.9 | 26.9561 | 0.947085 | 131.379 | 0.366477 | 168.582 | 0.566934 | 229.334 | 289.814 | 0.329825 | 222.155 | 149.1 | 0.658619 | 13.3394 | 48.0881 | 198.022 | 316.9602 | 24530.24 |
| 56948.3 | 19.4603 | 0.897796 | 85.0301 | 1.24789 | 854.661 | 0.466391 | 382.225 | 520.546 | 0.951908 | 498.398 | 853.461 | 0.309772 | 42.757 | 309.906 | 445.025 | 551.8647 | 54424.86 |
| 53273.5 | 18.5981 | 0.904756 | 147.429 | 1.28373 | 80.3562 | 0.563674 | 78.9222 | 8.64715 | 0.645255 | 310.555 | 170.721 | 0.483594 | 65.0299 | 58.8928 | 78.074 | 225.4613 | 14661.12 |
| 31952.8 | 16.1944 | 0.94514 | 143.649 | 0.421946 | 664.41 | 0.355493 | 184.89 | 280.317 | 0.72679 | 119.531 | 374.484 | 0.501273 | 37.604 | 76.06 | 114.598 | 458.6526 | 52311.69 |
| 53955.5 | 18.901 | 0.903464 | 36.698 | 1.99702 | 624.397 | 0.426404 | 125.891 | 364.561 | 0.865242 | 374.46 | 903.48 | 0.750481 | 117.984 | 105.707 | 253.368 | 265.27 | 24178.64 |
| 36335.3 | 19.431 | 0.936841 | 118.999 | 1.00444 | 347.895 | 0.283371 | 278.305 | 818.858 | 0.918205 | 143.593 | 518.69 | 0.888031 | 74.2901 | 249.75 | 97.0619 | 301.9498 | 26028.84 |
| 66492.2 | 14.2352 | 0.879714 | 156.863 | 2.96783 | 421.395 | 0.279147 | 250.587 | 513.265 | 0.53783 | 348.202 | 272.131 | 0.706138 | 97.1844 | 186.414 | 119.765 | 557.3323 | 51829.72 |
| 58350.4 | 17.0933 | 0.895138 | 60.2842 | 0.559098 | 3.15138 | 0.169845 | 66.2232 | 267.462 | 0.430108 | 146.275 | 311.318 | 0.673312 | 47.514 | 47.9131 | 112.732 | 666.6618 | 38060.5 |
| 57438.9 | 17.2088 | 0.896865 | 53.4948 | 0.42958 | 871.23 | 0.409313 | 294.208 | 178.052 | 0.868835 | 247.362 | 221.452 | 0.542619 | 5.70058 | 85.3302 | 85.8678 | 311.4553 | 37762.02 |
| 28091.3 | 25.9058 | 0.952463 | 145.421 | 1.98329 | 302.219 | 0.219996 | 356.644 | 583.768 | 0.996035 | 338.091 | 340.794 | 0.55509 | 107.558 | 321.696 | 88.254 | 410.5886 | 39216.08 |
| 28170 | 25.0762 | 0.952313 | 149.186 | 1.96302 | 483.47 | 0.564798 | 394.768 | 776.324 | 0.368477 | 263.537 | 22.9764 | 0.822943 | 73.043 | 90.0555 | 137.634 | 279.5493 | 25747.19 |
| 69069.7 | 14.9838 | 0.874833 | 117.558 | 3.71568 | 741.042 | 0.272307 | 328.143 | 120.917 | 0.797873 | 157.55 | 140.95 | 0.631177 | 35.632 | 288.427 | 119.056 | 433.5938 | 53539.06 |
| 55218.9 | 13.5996 | 0.901068 | 147.097 | 2.02351 | 569.364 | 0.497128 | 219.862 | 874.219 | 0.457333 | 374.545 | 444.661 | 0.437663 | 19.4167 | 86.391 | 254.532 | 664.5298 | 58512.88 |
| 34781.1 | 15.2907 | 0.939782 | 143.68 | 3.03187 | 480.754 | 0.371637 | 409.883 | 341.507 | 0.855497 | 381.275 | 322.065 | 0.969639 | 54.0354 | 334.459 | 56.6721 | 179.7352 | 18149.71 |
| 42514 | 22.8427 | 0.92514 | 74.9282 | 1.03705 | 227.267 | 0.44672 | 258.86 | 809.711 | 0.559346 | 331.144 | 593.076 | 0.887736 | 6.81293 | 233.694 | 48.6584 | 256.9089 | 18809.3 |
| 33182.1 | 13.1958 | 0.94281 | 134.851 | 0.112292 | 143.451 | 0.183952 | 141.356 | 233.25 | 0.808669 | 370.584 | 507.013 | 0.575981 | 6.67835 | 100.703 | 234.048 | 535.7818 | 43393.34 |
| 60274.3 | 16.7291 | 0.891494 | 159.595 | 0.664615 | 381.318 | 0.312724 | 391.706 | 395.34 | 0.749498 | 254.852 | 984.413 | 0.525148 | 26.9887 | 359.821 | 221.278 | 578.7404 | 47756.73 |
| 29066.3 | 26.4246 | 0.950616 | 79.4411 | 0.754888 | 71.8716 | 0.342115 | 282.805 | 374.734 | 0.368011 | 91.9509 | 673.749 | 0.739543 | 18.7005 | 250.556 | 72.0173 | 357.9751 | 26091.81 |
| 36064 | 22.8242 | 0.937358 | 56.1631 | 1.13792 | 378.202 | 0.589972 | 214.93 | 482.612 | 0.78096 | 486.607 | 541.666 | 0.834471 | 106.861 | 186.172 | 382.033 | 219.3366 | 15451.67 |
| 25410.7 | 15.0266 | 0.957531 | 48.536 | 3.30824 | 407.021 | 0.449717 | 144.918 | 599.333 | 0.833374 | 300.387 | 916.51 | 0.810973 | 126.928 | 139.794 | 299.176 | 225.7101 | 18205.63 |
| 62468.9 | 16.9046 | 0.887337 | 147.84 | 1.3053 | 156.218 | 0.538542 | 465.329 | 701.824 | 0.944255 | 84.6409 | 88.4752 | 0.697128 | 17.4132 | 235.435 | 45.892 | 203.7737 | 12649.27 |
| 36732.9 | 25.5606 | 0.936093 | 87.4345 | 0.550175 | 381.96 | 0.383885 | 268.775 | 686.493 | 0.549018 | 314.769 | 234.429 | 0.567552 | 36.629 | 217.899 | 67.7316 | 417.7296 | 39362.34 |
| 36905.2 | 15.7755 | 0.935759 | 156.195 | 1.7678 | 68.4866 | 0.373178 | 208.954 | 8.48356 | 0.552193 | 141.687 | 938.929 | 0.588228 | 83.1865 | 129.111 | 141.555 | 339.3367 | 23230.68 |
| 44671.6 | 17.9435 | 0.921049 | 118.574 | 2.35854 | 892.155 | 0.487993 | 423.048 | 966.035 | 0.651077 | 326.33 | 937.369 | 0.813463 | 118.059 | 330.687 | 298.182 | 339.0287 | 31151.33 |
| 39121.2 | 20.9137 | 0.931565 | 50.471 | 2.01189 | 818.9 | 0.45341 | 128.911 | 738.607 | 0.815413 | 497.663 | 206.633 | 0.676669 | 54.2806 | 122.284 | 116.712 | 275.0599 | 28791.41 |
| 60473.9 | 18.3516 | 0.891117 | 152.955 | 0.527694 | 262.631 | 0.543156 | 188.766 | 844.509 | 0.756938 | 451.511 | 189.655 | 0.625629 | 30.0342 | 48.1826 | 109.568 | 309.762 | 20406.01 |
| 61953.2 | 16.7326 | 0.888314 | 55.9948 | 2.69629 | 766.505 | 0.208942 | 318.451 | 792.812 | 0.930131 | 506.528 | 178.165 | 0.675168 | 100.97 | 201.251 | 88.8746 | 545.4376 | 64507.81 |
| 59496.9 | 19.7019 | 0.892968 | 90.0545 | 1.99572 | 283.047 | 0.291639 | 458.446 | 483.408 | 0.878697 | 109.776 | 513.125 | 0.514064 | 8.48464 | 174.544 | 47.2906 | 411.868 | 34177.86 |
| 27432 | 15.8053 | 0.953703 | 107.456 | 2.73207 | 151.688 | 0.262534 | 447.057 | 824.757 | 0.974463 | 205.256 | 913.857 | 0.693754 | 90.3478 | 360.969 | 199.65 | 314.118 | 22900.34 |
| 47538 | 14.0876 | 0.915617 | 50.1084 | 0.738998 | 261.049 | 0.400252 | 383.165 | 852.725 | 0.794478 | 179.803 | 235.009 | 0.955978 | 45.6574 | 302.264 | 148.437 | 195.1959 | 14857.07 |
| 25971.4 | 17.8139 | 0.956471 | 171.102 | 1.59326 | 358.09 | 0.664085 | 412.816 | 394.956 | 0.28753 | 503.493 | 47.4069 | 0.534803 | 110.887 | 134.638 | 380.878 | 493.038 | 39931.42 |
| 50383.3 | 15.2821 | 0.910228 | 60.1519 | 3.67226 | 146.855 | 0.5739 | 486.824 | 216.623 | 0.660319 | 341.915 | 428.004 | 0.948074 | 276.235 | 441.172 | 251.481 | 171.9865 | 10947.79 |
| 30863.7 | 17.9947 | 0.947204 | 48.0915 | 2.58783 | 801.657 | 0.4653 | 291.975 | 407.4 | 0.711703 | 306.427 | 7.9047 | 0.302808 | 162.758 | 76.359 | 271.187 | 502.8498 | 59403.77 |
| 42998.4 | 15.3346 | 0.924217 | 87.3218 | 3.08495 | 301.554 | 0.418033 | 426.416 | 600.774 | 0.991391 | 333.051 | 171.173 | 0.243798 | 168.028 | 338.233 | 109.632 | 537.4403 | 43062.36 |
| 48777.6 | 13.8455 | 0.913269 | 26.3366 | 2.77876 | 175.113 | 0.432954 | 439.579 | 715.016 | 0.353192 | 458.897 | 238.129 | 0.904101 | 137.913 | 127.072 | 181.391 | 305.372 | 22732.28 |
| 48449.5 | 21.1096 | 0.913896 | 100.432 | 1.48651 | 996.757 | 0.464657 | 432.151 | 46.4706 | 0.454995 | 343.131 | 222.644 | 0.884344 | 145.226 | 320.283 | 71.3906 | 288.668 | 37367.73 |
| 42382.8 | 21.1879 | 0.925387 | 150.464 | 2.58871 | 515.646 | 0.482741 | 96.253 | 302.57 | 0.430947 | 252.735 | 287.06 | 0.929968 | 169.16 | 68.5967 | 164.677 | 260.49 | 25512.53 |
| 40246.6 | 15.4194 | 0.929429 | 89.1021 | 1.87838 | 248.509 | 0.411885 | 401.227 | 425.223 | 0.892084 | 459.784 | 615.36 | 0.343975 | 175.38 | 200.666 | 68.8635 | 390.0235 | 30832.24 |
| 32702.4 | 25.1942 | 0.943727 | 120.142 | 0.178806 | 0.332178 | 0.257444 | 331.401 | 822.84 | 0.928033 | 384.919 | 429.282 | 0.502104 | 5.94928 | 199.653 | 367.415 | 431.808 | 25747.62 |
| 64042.5 | 13.4459 | 0.884354 | 131.27 | 1.16027 | 215.838 | 0.551959 | 331.531 | 711.159 | 0.829318 | 480.993 | 601.705 | 0.238023 | 32.7963 | 184.088 | 102.238 | 661.0333 | 41884.26 |
| 45544.9 | 16.9179 | 0.919394 | 73.9193 | 0.982568 | 334.957 | 0.390729 | 313.214 | 970.847 | 0.733459 | 351.552 | 770.868 | 0.770399 | 8.66604 | 200.271 | 148.676 | 317.1977 | 24573.02 |
| 75987.6 | 15.5131 | 0.861729 | 148.842 | 3.47529 | 937.676 | 0.54247 | 165.937 | 225.189 | 0.468201 | 347.346 | 147.726 | 0.758821 | 25.0384 | 135.118 | 299.743 | 322.3913 | 32911.74 |
| 70455.1 | 15.0459 | 0.872208 | 31.8291 | 0.285513 | 989.127 | 0.499701 | 283.248 | 808.246 | 0.972693 | 401.545 | 865.172 | 0.423727 | 17.4204 | 152.778 | 126.891 | 470.7193 | 39457.2 |
| 72943 | 17.1268 | 0.867497 | 31.9774 | 0.153038 | 377.201 | 0.341076 | 194.868 | 227.61 | 0.336468 | 356.391 | 797.665 | 0.821665 | 9.2038 | 53.6309 | 346.978 | 557.3197 | 49945.89 |
| 48524.2 | 21.8785 | 0.913755 | 142.404 | 1.16247 | 798.071 | 0.454938 | 142.084 | 108.593 | 0.912763 | 331.28 | 722.708 | 0.580908 | 103.384 | 114.838 | 66.4856 | 289.6894 | 29952.43 |
| 35930.9 | 20.924 | 0.937608 | 123.599 | 1.95522 | 961.274 | 0.519985 | 405.173 | 356.524 | 0.857516 | 501.878 | 31.5365 | 0.931251 | 71.1759 | 108.555 | 214.513 | 136.224 | 15745.84 |
| 26670.1 | 26.2151 | 0.955155 | 165.55 | 0.598092 | 169.235 | 0.182272 | 86.1719 | 730.938 | 0.979528 | 360.994 | 497.153 | 0.816855 | 4.68497 | 72.5815 | 329.812 | 617.1589 | 48986.96 |
| 56964.5 | 13.1123 | 0.897761 | 137.288 | 3.24254 | 47.9277 | 0.496342 | 467.286 | 957.861 | 0.453945 | 466.51 | 111.654 | 0.3762 | 73.7656 | 280.524 | 391.058 | 589.5438 | 34479.48 |
| 43459.7 | 15.1124 | 0.923343 | 79.7343 | 2.04203 | 494.621 | 0.165328 | 319.141 | 398.316 | 0.764291 | 447.892 | 30.3311 | 0.958234 | 80.1892 | 124.018 | 366.967 | 443.6086 | 54616.88 |
| 25346.6 | 14.5133 | 0.957652 | 129.994 | 3.58808 | 885.403 | 0.354684 | 399.909 | 726.808 | 0.638034 | 444.928 | 982.829 | 0.909025 | 53.8698 | 162.816 | 281.179 | 362.8173 | 41884.4 |
| 39042.4 | 14.6064 | 0.93171 | 57.1461 | 1.90592 | 347.354 | 0.377135 | 285.071 | 242.828 | 0.436575 | 234.454 | 727.966 | 0.609139 | 109.906 | 153.686 | 186.004 | 423.7796 | 41032.94 |
| 26114.1 | 18.7013 | 0.956201 | 127.962 | 3.14946 | 426.007 | 0.536505 | 283.921 | 44.301 | 0.958341 | 201.739 | 740.356 | 0.629278 | 187.621 | 139.873 | 114.289 | 167.4007 | 13712.76 |
| 76781.4 | 13.9782 | 0.860225 | 39.8568 | 2.4409 | 760.63 | 0.539797 | 437.28 | 266.077 | 0.850212 | 494.226 | 368.42 | 0.429525 | 229.853 | 156.006 | 383.42 | 391.4318 | 32830.41 |
| 34584.8 | 22.7197 | 0.940159 | 154.834 | 0.842077 | 144.657 | 0.497667 | 382.85 | 748.301 | 0.861721 | 330.5 | 741.422 | 0.609948 | 63.6571 | 303.889 | 194.852 | 286.0514 | 18445.36 |
| 29582.2 | 13.9765 | 0.949629 | 71.5186 | 0.495228 | 156.518 | 0.324913 | 449.561 | 470.277 | 0.943531 | 246.065 | 754.763 | 0.347469 | 42.4576 | 349.835 | 112.816 | 423.8846 | 32610.5 |
| 69740 | 17.5381 | 0.873564 | 21.0235 | 3.53259 | 342.092 | 0.504809 | 183.128 | 113.603 | 0.900006 | 319.871 | 891.412 | 0.578503 | 177.11 | 79.1068 | 164.28 | 233.5522 | 16124.7 |
| 39849.1 | 20.9247 | 0.930186 | 74.1081 | 0.266903 | 291.882 | 0.481199 | 415.005 | 81.3253 | 0.896551 | 440.585 | 93.3708 | 0.508114 | 7.83436 | 176.256 | 334.818 | 172.9504 | 15810.66 |
| 38191.2 | 23.6004 | 0.933329 | 159.378 | 2.41139 | 0.283312 | 0.422772 | 454.91 | 161.523 | 0.42107 | 380.424 | 785.619 | 0.706218 | 107.077 | 228.469 | 60.7022 | 320.26 | 19332.41 |
| 52366.9 | 21.6194 | 0.906475 | 126.633 | 1.54739 | 225.949 | 0.615102 | 201.951 | 913.891 | 0.49159 | 241.345 | 667.541 | 0.988976 | 73.7686 | 198.918 | 224.152 | 305.0574 | 18731.24 |
| 56223.9 | 14.7888 | 0.899165 | 41.6279 | 0.415666 | 740.36 | 0.502163 | 338.427 | 404.579 | 0.624293 | 275.685 | 552.08 | 0.993115 | 18.2347 | 214.427 | 79.9384 | 216.2102 | 19336.76 |
| 57864.5 | 20.1624 | 0.896061 | 70.5929 | 1.48011 | 351.945 | 0.270317 | 204.893 | 826.07 | 0.748717 | 339.781 | 789.324 | 0.430759 | 28.3885 | 186.604 | 86.6169 | 684.7328 | 59741.44 |
| 39119.6 | 18.0892 | 0.931566 | 97.9747 | 0.348631 | 422.145 | 0.221913 | 260.76 | 140.771 | 0.849732 | 411.081 | 82.3451 | 0.859496 | 25.8057 | 42.5541 | 56.8493 | 305.5026 | 34672.78 |
| 49076.3 | 20.7752 | 0.912708 | 125.479 | 2.25383 | 35.6614 | 0.431331 | 62.9712 | 853.267 | 0.92299 | 485.664 | 904.994 | 0.386531 | 109.088 | 51.5286 | 421.833 | 448.1712 | 25468.24 |
| 27563.6 | 23.304 | 0.95346 | 151.523 | 1.73645 | 462.593 | 0.440634 | 224.089 | 817.784 | 0.793912 | 139.703 | 583.4 | 0.972758 | 86.3441 | 183.352 | 136.355 | 221.9958 | 18594.6 |
| 44763.4 | 18.8433 | 0.920876 | 136.689 | 3.09867 | 897.572 | 0.49499 | 340.063 | 788.134 | 0.941202 | 269.707 | 679.162 | 0.326546 | 175.849 | 256.863 | 218.075 | 551.8935 | 51605.89 |
| 34562.5 | 17.212 | 0.940197 | 104.032 | 1.546 | 196.596 | 0.309331 | 488.092 | 216.01 | 0.401502 | 166.654 | 875.225 | 0.674864 | 31.0238 | 162.621 | 55.7275 | 454.5896 | 39638.56 |
| 67308.2 | 16.397 | 0.87817 | 27.5405 | 1.8417 | 169.646 | 0.457097 | 366.908 | 497.768 | 0.702102 | 471.664 | 904.442 | 0.71869 | 41.1749 | 180.67 | 330.851 | 278.6743 | 17883.74 |
| 28983.1 | 14.8504 | 0.950764 | 44.1217 | 1.13008 | 800.036 | 0.455903 | 119.626 | 460.936 | 0.254356 | 62.3157 | 657.959 | 0.882436 | 7.99834 | 53.8677 | 47.7608 | 488.6286 | 60822.07 |
| 51662.6 | 20.953 | 0.907809 | 38.4377 | 1.75148 | 506.087 | 0.488499 | 497.291 | 282.57 | 0.319154 | 230.583 | 306.277 | 0.781281 | 5.91405 | 96.7871 | 229.791 | 370.1034 | 36375.4 |
| 60713.5 | 16.9478 | 0.890662 | 49.9228 | 3.43548 | 624.954 | 0.32387 | 99.5453 | 839.648 | 0.486621 | 239.49 | 825.769 | 0.790708 | 169.03 | 63.8202 | 97.0268 | 538.956 | 54623.85 |
| 28875.2 | 25.6322 | 0.950978 | 130.608 | 0.435995 | 535.517 | 0.474565 | 312.133 | 347.321 | 0.438073 | 412.991 | 647.814 | 0.832863 | 2.6539 | 72.5082 | 95.4765 | 320.5381 | 31683.09 |
| 42504.2 | 22.4626 | 0.925158 | 81.5351 | 2.37308 | 383.647 | 0.17178 | 146.338 | 16.3505 | 0.883498 | 140.451 | 114.864 | 0.677088 | 82.0036 | 45.8822 | 103.966 | 394.5186 | 46676.55 |
| 26721.4 | 17.4187 | 0.95505 | 41.5341 | 2.8917 | 149.341 | 0.300209 | 240.649 | 923.897 | 0.485736 | 337.276 | 470.583 | 0.625539 | 17.4872 | 106.335 | 173.211 | 436.5265 | 35062.78 |
| 36678.7 | 25.5616 | 0.936196 | 44.4714 | 0.917167 | 173.707 | 0.166038 | 477.313 | 604.713 | 0.995803 | 216.068 | 278.584 | 0.454685 | 18.2711 | 262.705 | 166.003 | 542.3822 | 46652.9 |
| 41187.4 | 23.1258 | 0.927653 | 138.997 | 0.73818 | 4.50039 | 0.637254 | 454.904 | 856.044 | 0.959326 | 482.934 | 605.741 | 0.866695 | 14.3052 | 90.851 | 66.9617 | 196.4718 | 10837.1 |
| 43282.2 | 14.014 | 0.923678 | 17.6961 | 1.725 | 718.051 | 0.484892 | 59.449 | 907.774 | 0.641977 | 168.782 | 873.616 | 0.878361 | 11.753 | 54.8139 | 163.231 | 295.7151 | 25503.7 |
| 44143.7 | 14.5041 | 0.922047 | 31.4077 | 1.30027 | 673.278 | 0.293125 | 380.542 | 111.25 | 0.748263 | 410.888 | 967.34 | 0.732727 | 15.4903 | 335.686 | 90.8464 | 376.326 | 43857.71 |
| 76361.6 | 16.2347 | 0.861021 | 110.968 | 2.2794 | 40.7341 | 0.239721 | 145.722 | 188.971 | 0.293177 | 165.132 | 229.397 | 0.83661 | 85.0178 | 111.974 | 67.5346 | 661.8849 | 39120.52 |
| 57912 | 14.7972 | 0.895967 | 160.275 | 2.54715 | 151.115 | 0.582925 | 277.706 | 410.623 | 0.229337 | 139.118 | 955.768 | 0.981454 | 174.351 | 269.427 | 110.978 | 402.8332 | 25495.09 |
| 71863.3 | 13.9769 | 0.86954 | 149.343 | 1.58756 | 914.804 | 0.464077 | 100.203 | 695.08 | 0.660658 | 323.499 | 605.263 | 0.81586 | 149.674 | 47.2939 | 233.279 | 362.8538 | 34036.36 |
| 39140.1 | 16.8662 | 0.931526 | 170.459 | 2.91558 | 562.145 | 0.244056 | 220.368 | 740.751 | 0.547406 | 219.753 | 274.845 | 0.971792 | 94.2935 | 217.471 | 180.312 | 461.7293 | 51438.42 |
| 61920.1 | 14.7782 | 0.888375 | 170.379 | 3.06852 | 553.093 | 0.576281 | 279.332 | 872.525 | 0.353164 | 416.6 | 175.354 | 0.622981 | 158.952 | 67.6369 | 392.2 | 503.8763 | 40700.81 |
| 54485.3 | 16.7588 | 0.902459 | 112.073 | 2.63194 | 452.992 | 0.472234 | 93.8961 | 363.442 | 0.626519 | 438.42 | 972.304 | 0.627618 | 7.9379 | 74.1764 | 204.262 | 330.9861 | 27844 |
| 38922.5 | 21.4657 | 0.931942 | 23.3136 | 1.30716 | 703.945 | 0.410651 | 159.454 | 715.285 | 0.428882 | 401.668 | 441.411 | 0.631401 | 28.2401 | 145.615 | 121.615 | 507.3784 | 57397.24 |
| 40609.6 | 21.4347 | 0.928746 | 136.923 | 3.59527 | 999.066 | 0.390495 | 273.446 | 665.073 | 0.893315 | 380.836 | 26.8877 | 0.52432 | 11.8392 | 107.812 | 199.368 | 396.6703 | 48046.18 |
| 33558.7 | 23.3909 | 0.942104 | 128.203 | 0.527058 | 836.65 | 0.517998 | 86.3703 | 309.327 | 0.382026 | 233.336 | 767.546 | 0.881606 | 51.6635 | 59.2152 | 55.3479 | 357.6591 | 38527.55 |
| 40499.7 | 13.821 | 0.928949 | 23.604 | 3.41294 | 699.859 | 0.271757 | 385.072 | 184.294 | 0.909617 | 247.739 | 600.119 | 0.81777 | 19.6781 | 211.985 | 89.476 | 296.5095 | 36187.07 |
| 38145.4 | 20.9699 | 0.933413 | 172.805 | 0.889497 | 774.22 | 0.41251 | 97.1794 | 330.928 | 0.979 | 388.233 | 588.892 | 0.719252 | 39.5861 | 63.0984 | 105.153 | 276.8676 | 27749.43 |
| 46281.2 | 16.4575 | 0.917999 | 117.548 | 1.29011 | 230.817 | 0.27994 | 385.751 | 638.969 | 0.51379 | 509.454 | 555.875 | 0.957532 | 121.549 | 255.234 | 100.429 | 361.1502 | 29726.21 |
| 79760.4 | 15.3318 | 0.854582 | 47.5563 | 0.600666 | 371.07 | 0.371661 | 465.748 | 899.936 | 0.886315 | 305.323 | 762.965 | 0.59054 | 42.9008 | 65.1339 | 242.214 | 417.0515 | 30862.59 |
| 36523.5 | 13.4794 | 0.93648 | 122.409 | 3.02369 | 373.979 | 0.271006 | 165.589 | 172.378 | 0.788324 | 310.32 | 954.953 | 0.534764 | 131.042 | 134.268 | 300.736 | 414.2744 | 42132.02 |
| 29122.4 | 13.7457 | 0.9505 | 108.425 | 1.92629 | 335.329 | 0.489586 | 407.458 | 941.647 | 0.884828 | 151.611 | 107.034 | 0.430719 | 144.03 | 364.041 | 66.3443 | 329.7112 | 24895.93 |
| 46801.7 | 17.2277 | 0.917014 | 54.7481 | 2.86457 | 225.177 | 0.58761 | 386.353 | 393.145 | 0.689708 | 444.821 | 714.403 | 0.584541 | 282.155 | 271.969 | 429.362 | 389.8871 | 25186.8 |
| 43000.4 | 18.2825 | 0.924215 | 104.79 | 3.69145 | 569.202 | 0.568797 | 404.336 | 368.857 | 0.670031 | 448.585 | 908.958 | 0.417095 | 70.4946 | 236.26 | 430.141 | 680.8655 | 55273.29 |
| 35500 | 17.2133 | 0.938421 | 156.36 | 1.46417 | 646.174 | 0.654241 | 341.847 | 520.625 | 0.753954 | 205.236 | 305.491 | 0.827156 | 124.428 | 144.429 | 128.97 | 184.603 | 14083.02 |
| 31430.1 | 16.2781 | 0.94613 | 157.352 | 1.64577 | 382.936 | 0.476522 | 415.534 | 274.367 | 0.762712 | 365.274 | 700.851 | 0.536451 | 18.8974 | 90.4261 | 166.007 | 286.896 | 24876.13 |
| 51687.7 | 22.331 | 0.907763 | 146.817 | 1.70509 | 938.532 | 0.58747 | 333.556 | 891.712 | 0.278307 | 351.609 | 386.46 | 0.644547 | 134.923 | 265.915 | 251.159 | 599.7866 | 57380.87 |
| 43031.5 | 20.2144 | 0.924158 | 113.954 | 0.889015 | 625.547 | 0.267546 | 348.056 | 566.869 | 0.64998 | 519.386 | 149.858 | 0.694943 | 54.6328 | 113.687 | 280.081 | 482.8287 | 56372.44 |
| 57683.5 | 19.0565 | 0.896403 | 75.1222 | 0.898967 | 78.4791 | 0.170068 | 165.261 | 347.778 | 0.80587 | 514.511 | 897.802 | 0.836174 | 63.2279 | 58.5294 | 432.769 | 400.3647 | 26665.27 |
| 52837.7 | 16.1734 | 0.90558 | 169.99 | 1.07642 | 521.384 | 0.261549 | 480.048 | 796.985 | 0.839497 | 505.841 | 301.721 | 0.506569 | 26.5149 | 163.491 | 67.1116 | 668.0447 | 63204.37 |
| 80977.2 | 14.1277 | 0.852277 | 147.481 | 1.76867 | 389.09 | 0.407552 | 237.247 | 436.308 | 0.993212 | 367.91 | 232.497 | 0.637146 | 78.0568 | 232.042 | 148.508 | 279.9579 | 21501.71 |
| 50888.6 | 14.4287 | 0.909271 | 52.0728 | 1.03203 | 255.495 | 0.290807 | 293.074 | 453.058 | 0.731728 | 171.685 | 483.221 | 0.925284 | 94.8808 | 94.6437 | 120.06 | 255.2203 | 21335.06 |
| 68287.5 | 15.5571 | 0.876315 | 109.862 | 1.13526 | 750.013 | 0.449207 | 233.734 | 387.237 | 0.648932 | 316.616 | 820.649 | 0.829363 | 43.5426 | 115.637 | 69.8188 | 321.7145 | 30262.49 |
| 59401.4 | 17.6334 | 0.893148 | 128.108 | 0.326127 | 371.173 | 0.623699 | 417.754 | 213.651 | 0.964335 | 406.086 | 726.894 | 0.514735 | 22.6587 | 236.818 | 231.815 | 235.9452 | 16297.39 |
| 40851.4 | 17.3585 | 0.928285 | 130.818 | 1.58807 | 311.007 | 0.41323 | 170.882 | 86.7517 | 0.719616 | 293.748 | 130.38 | 0.973787 | 129.534 | 60.8669 | 85.548 | 140.924 | 13300.26 |
| 37395.6 | 20.0226 | 0.934833 | 137.704 | 0.146066 | 754.735 | 0.641582 | 224.382 | 51.7094 | 0.998284 | 464.743 | 291.513 | 0.950044 | 13.4683 | 206.096 | 353.022 | 113.6259 | 10610.54 |
| 60818.5 | 19.3824 | 0.890465 | 25.0505 | 1.80447 | 572.829 | 0.264229 | 297.204 | 678.639 | 0.77414 | 325.986 | 927.399 | 0.547364 | 155.766 | 219.388 | 122.937 | 604.976 | 61000.7 |
| 26146.9 | 17.8987 | 0.956139 | 155.545 | 1.44843 | 170.034 | 0.477415 | 233.962 | 828.02 | 0.564286 | 432.913 | 604.904 | 0.958592 | 60.7475 | 172.546 | 208.256 | 234.0589 | 16498.05 |
| 33142.6 | 21.4221 | 0.94289 | 50.427 | 0.266492 | 121.515 | 0.280872 | 421.724 | 128.049 | 0.635728 | 405.89 | 141.632 | 0.611936 | 10.8177 | 104.453 | 196.055 | 274.8687 | 23343.37 |
| 79937.9 | 15.8786 | 0.854247 | 158.445 | 0.902315 | 979.283 | 0.538488 | 465.637 | 315.205 | 0.294968 | 484.557 | 283.907 | 0.832346 | 58.4449 | 419.251 | 435.931 | 569.5923 | 56054.07 |
| 78821.9 | 13.9509 | 0.85636 | 61.7755 | 2.00685 | 184.149 | 0.276313 | 333.014 | 580.488 | 0.975722 | 502.776 | 340.689 | 0.803431 | 108.043 | 323.54 | 114.189 | 274.3455 | 19126.57 |
| 28522.7 | 16.4467 | 0.951637 | 132.1 | 1.49664 | 671.529 | 0.276118 | 484.026 | 919.238 | 0.423809 | 197.679 | 99.2211 | 0.929916 | 113.136 | 139.957 | 155.252 | 509.4624 | 63891.14 |
| 64323.6 | 13.4529 | 0.883822 | 75.3911 | 1.16327 | 110.313 | 0.509874 | 469.938 | 124.984 | 0.222966 | 312.137 | 264.556 | 0.835267 | 101.396 | 128.01 | 275.575 | 452.9923 | 28868.31 |
| 39665.5 | 24.1624 | 0.930537 | 35.1573 | 3.31067 | 647.678 | 0.370086 | 382.642 | 652.17 | 0.641653 | 279.335 | 48.4546 | 0.907875 | 52.1476 | 315.352 | 189.315 | 255.292 | 29158.25 |
| 29898.8 | 14.719 | 0.94903 | 102.513 | 0.277587 | 169.591 | 0.350791 | 417.528 | 81.7834 | 0.852441 | 169.021 | 989.497 | 0.740839 | 3.62888 | 51.5388 | 62.8933 | 228.8139 | 17483.45 |
| 30783.2 | 13.0719 | 0.947353 | 21.874 | 2.79759 | 8.64616 | 0.307101 | 275.931 | 207.634 | 0.913088 | 318.775 | 577.201 | 0.83484 | 155.527 | 68.255 | 253.829 | 159.0317 | 9871.204 |
| 49749.2 | 15.6395 | 0.91143 | 55.0711 | 2.0987 | 60.9045 | 0.500216 | 495.715 | 723.425 | 0.705267 | 301.356 | 790.947 | 0.382459 | 22.8989 | 472.385 | 91.3536 | 445.0995 | 25923.65 |
| 52642.3 | 19.114 | 0.905952 | 70.1759 | 1.70145 | 452.164 | 0.593229 | 491.566 | 915.139 | 0.762969 | 283.12 | 411.671 | 0.685448 | 151.126 | 394.978 | 251.162 | 361.5624 | 24306.2 |
| 42689.3 | 13.0224 | 0.924801 | 126.492 | 1.92638 | 334.965 | 0.269675 | 278.879 | 649.711 | 0.668441 | 233.57 | 66.6544 | 0.841481 | 7.21893 | 135.926 | 118.316 | 319.8628 | 30846.3 |
| 35294.6 | 14.1478 | 0.938809 | 42.3816 | 2.47885 | 689.975 | 0.427519 | 364.487 | 281.202 | 0.214812 | 284.32 | 575.111 | 0.978881 | 15.2158 | 60.6274 | 135.131 | 519.9198 | 64039.46 |
| 82711.9 | 13.1275 | 0.848991 | 25.4649 | 3.63068 | 150.182 | 0.305146 | 328.969 | 180.994 | 0.784897 | 268.702 | 320.897 | 0.979401 | 82.6423 | 243.604 | 47.4386 | 213.4428 | 14656.86 |
| 60711.3 | 16.0492 | 0.890666 | 19.4563 | 1.46047 | 162.886 | 0.378496 | 466.653 | 592.564 | 0.804911 | 510.266 | 889.843 | 0.940416 | 77.7247 | 313.654 | 154.179 | 238.0344 | 15542.75 |
| 63059.4 | 15.9376 | 0.886218 | 142.461 | 2.43467 | 975.314 | 0.655879 | 454.709 | 984.487 | 0.835661 | 466.228 | 814.292 | 0.914631 | 110.141 | 418.655 | 382.843 | 299.7708 | 20524.32 |
| 27586.7 | 22.9714 | 0.953416 | 95.8936 | 2.96824 | 722.035 | 0.287692 | 283.312 | 999.089 | 0.928671 | 227.847 | 790.475 | 0.772318 | 41.1839 | 61.931 | 106.031 | 383.5406 | 40621.36 |
| 50149.3 | 21.5507 | 0.910676 | 143.578 | 3.50166 | 844.141 | 0.605412 | 341.331 | 539.322 | 0.875362 | 364.54 | 706.63 | 0.579846 | 260.623 | 319.322 | 229.12 | 336.5545 | 25807.46 |
| 73162 | 14.8311 | 0.867081 | 151.77 | 3.28412 | 910.552 | 0.561339 | 130.419 | 628.607 | 0.821695 | 398.787 | 973.047 | 0.642284 | 108.586 | 60.2595 | 336.923 | 326.8856 | 24871.05 |
| 47237 | 15.8904 | 0.916188 | 51.392 | 2.2149 | 207.946 | 0.479515 | 465.166 | 950.213 | 0.628678 | 120.985 | 671.76 | 0.426331 | 104.045 | 296.096 | 64.7799 | 465.3801 | 31389.39 |
| 42914.4 | 22.5473 | 0.924381 | 40.0071 | 0.762465 | 397.885 | 0.281453 | 309.741 | 871.181 | 0.57104 | 222.791 | 230.139 | 0.901058 | 20.5367 | 272.659 | 188.06 | 356.0453 | 35420.39 |
| 72734.6 | 17.4208 | 0.867892 | 24.4189 | 0.326693 | 968.686 | 0.3567 | 168.99 | 411.055 | 0.909597 | 185.014 | 790.755 | 0.5532 | 4.59919 | 84.186 | 51.7335 | 462.7984 | 51196.6 |
| 68788.2 | 15.9794 | 0.875366 | 73.5109 | 1.94263 | 413.139 | 0.499015 | 265.056 | 682.268 | 0.641606 | 418.356 | 521.407 | 0.500353 | 139.711 | 247.505 | 393.053 | 390.0383 | 28007.33 |
| 38352.3 | 14.3366 | 0.933017 | 101.894 | 1.20544 | 114.215 | 0.329089 | 448.804 | 247.51 | 0.442373 | 150.263 | 800.918 | 0.372709 | 60.3999 | 394.494 | 71.3279 | 651.1564 | 49741.01 |
| 86812.4 | 13.9505 | 0.841224 | 92.9944 | 3.3362 | 672.303 | 0.323189 | 400.777 | 80.6188 | 0.596793 | 244.588 | 920.301 | 0.774557 | 139.122 | 222.573 | 150.056 | 460.8332 | 46940.47 |
| 35073.6 | 19.4673 | 0.939231 | 49.3054 | 1.08231 | 160.176 | 0.443097 | 435.655 | 759.843 | 0.378339 | 156.318 | 868.089 | 0.361924 | 21.5764 | 86.8731 | 64.5069 | 688.9884 | 51423.34 |
| 39333.6 | 19.9008 | 0.931162 | 41.3167 | 1.65182 | 25.9908 | 0.474299 | 215.927 | 289.867 | 0.458921 | 440.121 | 846.743 | 0.44253 | 139.43 | 165.885 | 46.9523 | 380.3678 | 23411.72 |
| 50338.7 | 13.1435 | 0.910312 | 168.906 | 0.719825 | 68.9548 | 0.462427 | 290.591 | 349.681 | 0.772329 | 405.328 | 554.234 | 0.701828 | 14.0585 | 174.274 | 164.38 | 250.349 | 15343.85 |
| 31267.7 | 22.1427 | 0.946442 | 168.945 | 2.73509 | 850.802 | 0.312041 | 361.457 | 341.969 | 0.527783 | 165.182 | 178.218 | 0.757384 | 107.003 | 112.178 | 142.5 | 480.2052 | 63766.38 |
| 30287.4 | 16.2159 | 0.948295 | 76.2592 | 3.37707 | 711.208 | 0.448486 | 128.452 | 586.209 | 0.981742 | 319.863 | 569.863 | 0.477697 | 103.711 | 119.654 | 153.697 | 327.3914 | 32190.84 |
| 35235.3 | 18.9516 | 0.938924 | 116.518 | 1.36284 | 820.668 | 0.50947 | 411.055 | 623.442 | 0.993017 | 109.598 | 143.598 | 0.330517 | 70.1357 | 139.398 | 108.647 | 422.2731 | 41473.56 |
| 56370.1 | 19.5342 | 0.898891 | 67.66 | 0.255685 | 232.687 | 0.466128 | 143.608 | 537.101 | 0.976561 | 338.702 | 46.4511 | 0.436876 | 19.5785 | 92.7659 | 54.0678 | 291.9733 | 20879.58 |
| 50786.8 | 16.2012 | 0.909465 | 66.7248 | 1.04899 | 76.7744 | 0.282657 | 271.396 | 13.4165 | 0.724248 | 163.302 | 196.684 | 0.784902 | 96.0026 | 255.397 | 151.144 | 201.5695 | 14458.38 |
| 70214.8 | 15.4642 | 0.872664 | 165.961 | 3.72424 | 421.837 | 0.508919 | 183.151 | 743.163 | 0.333562 | 231.033 | 318.277 | 0.567868 | 130.012 | 89.8599 | 224.347 | 629.6919 | 49786.04 |
| 35852.4 | 24.781 | 0.93776 | 88.3413 | 3.36403 | 814.05 | 0.488454 | 167.372 | 624.587 | 0.488723 | 202.86 | 355.206 | 0.779347 | 56.5598 | 53.4161 | 105.243 | 303.7161 | 32345.03 |
| 27469.6 | 22.1895 | 0.953637 | 30.0269 | 0.203306 | 799.864 | 0.39649 | 283.573 | 389.419 | 0.606477 | 188.08 | 343.403 | 0.908147 | 10.6921 | 138.171 | 80.3167 | 253.9386 | 31908.93 |
| 72844.7 | 13.8764 | 0.867681 | 162.327 | 3.02815 | 267.532 | 0.46652 | 353.335 | 361.148 | 0.576713 | 168.016 | 955.489 | 0.630343 | 64.1298 | 248.489 | 87.2988 | 395.4352 | 27391.34 |
| 58431.3 | 15.6681 | 0.894984 | 46.3849 | 3.63228 | 473.411 | 0.184849 | 476.811 | 850.915 | 0.91258 | 396.496 | 483.75 | 0.677345 | 50.4793 | 154.282 | 252.344 | 550.9365 | 55722.87 |
| 57289 | 13.7423 | 0.897147 | 91.489 | 3.29595 | 232.896 | 0.417986 | 163.104 | 592.116 | 0.893547 | 86.7575 | 826.55 | 0.518074 | 108.149 | 78.4564 | 85.8395 | 337.2112 | 23521.81 |
| 63077.1 | 17.1561 | 0.886185 | 124.792 | 3.17312 | 172.509 | 0.612422 | 275.789 | 52.035 | 0.833171 | 503.946 | 360.462 | 0.546867 | 142.992 | 170.414 | 340.483 | 247.1194 | 15739.7 |
| 50976.1 | 15.0754 | 0.909105 | 169.592 | 2.96932 | 102.008 | 0.345481 | 156.689 | 606.539 | 0.499232 | 228.953 | 776.713 | 0.756181 | 108.331 | 93.301 | 206.087 | 413.2998 | 27159.45 |
| 36500.9 | 19.8541 | 0.936528 | 167.261 | 1.60688 | 198.301 | 0.245918 | 418.358 | 203.803 | 0.755633 | 321.371 | 830.646 | 0.909151 | 127.422 | 257.328 | 92.5787 | 312.824 | 25222.99 |
| 29779.8 | 17.5949 | 0.949257 | 74.6336 | 1.11966 | 373.983 | 0.42817 | 138.271 | 174.599 | 0.682633 | 207.848 | 2.7626 | 0.968304 | 97.4076 | 112.88 | 183.962 | 122.5684 | 13426.99 |
| 49589.1 | 21.4447 | 0.911737 | 72.8237 | 1.58688 | 124.007 | 0.371684 | 185.871 | 243.062 | 0.555743 | 401.76 | 227.546 | 0.574328 | 123.097 | 161.139 | 284.465 | 310.5389 | 22920.09 |
| 49578.3 | 16.7162 | 0.911754 | 34.7372 | 3.02843 | 174.457 | 0.256456 | 212.212 | 692.028 | 0.504458 | 331.876 | 695.623 | 0.816847 | 154.884 | 176.748 | 232.595 | 431.7224 | 33583.55 |
| 57086.7 | 21.3889 | 0.897535 | 144.143 | 1.07804 | 662.294 | 0.373443 | 305.924 | 38.4828 | 0.680951 | 441.438 | 237.491 | 0.770775 | 37.4006 | 156.497 | 45.6802 | 304.0803 | 33151.97 |
| 26842.6 | 23.0564 | 0.954825 | 75.9463 | 0.84244 | 36.7799 | 0.324048 | 451.415 | 200.731 | 0.893333 | 375.145 | 892.987 | 0.880044 | 12.2512 | 355.038 | 147.765 | 174.5355 | 11202.56 |
| 28316 | 20.5244 | 0.952032 | 100.719 | 2.48892 | 941.312 | 0.368817 | 457.645 | 553.315 | 0.64107 | 166.152 | 472.425 | 0.964642 | 157.898 | 129.04 | 83.2225 | 287.3187 | 36122.66 |
| 28597.9 | 19.1211 | 0.951497 | 113.041 | 1.66848 | 91.3462 | 0.171846 | 492.33 | 486.946 | 0.883181 | 383.479 | 578.846 | 0.662576 | 61.0905 | 199.236 | 315.415 | 369.927 | 28397.08 |
| 30225.3 | 19.6719 | 0.948415 | 143.335 | 0.944019 | 90.1757 | 0.196652 | 441.883 | 523.61 | 0.727732 | 487.101 | 653.857 | 0.851886 | 83.9837 | 234.703 | 55.5733 | 360.0795 | 26518.64 |
| 63298.8 | 19.1967 | 0.885766 | 92.1047 | 3.77061 | 153.482 | 0.417706 | 282.167 | 450.988 | 0.64503 | 313.495 | 270.464 | 0.439312 | 38.8689 | 184.788 | 119.03 | 398.509 | 27498.05 |
| 61087.2 | 13.2076 | 0.889952 | 156.141 | 0.126491 | 173.185 | 0.307274 | 459.583 | 123.244 | 0.861674 | 436.003 | 664.946 | 0.833863 | 11.2025 | 374.565 | 386.384 | 327.4247 | 22464.5 |
| 31861.4 | 13.4866 | 0.945311 | 49.0265 | 1.11043 | 383.366 | 0.434281 | 393.458 | 601.995 | 0.974404 | 310.755 | 209.887 | 0.289355 | 2.47304 | 172.262 | 136.649 | 447.5786 | 39313.36 |
| 36611.7 | 13.2709 | 0.936313 | 105.496 | 0.1722 | 168.179 | 0.427876 | 171.68 | 783.251 | 0.230395 | 154.611 | 313.39 | 0.704633 | 3.78082 | 105.538 | 84.5434 | 614.2684 | 47561.14 |
| 27577.6 | 17.6289 | 0.953428 | 53.3064 | 2.71559 | 234.956 | 0.31729 | 301.568 | 909.934 | 0.983783 | 497.687 | 931.051 | 0.462713 | 86.2843 | 120.886 | 332.501 | 432.6669 | 33026.71 |
| 32625.7 | 25.0121 | 0.943873 | 42.1731 | 3.53599 | 51.8798 | 0.256926 | 141.331 | 357.863 | 0.581811 | 401.307 | 712.521 | 0.938039 | 72.6268 | 60.2869 | 225.708 | 261.0452 | 17877.46 |
| 35436.8 | 16.2309 | 0.93854 | 46.9183 | 0.395495 | 815.063 | 0.524746 | 369.703 | 382.433 | 0.476929 | 379.151 | 962.433 | 0.641463 | 18.8087 | 352.578 | 271.809 | 459.2704 | 45112.61 |
| 26923.6 | 14.5235 | 0.954665 | 159.918 | 0.658555 | 918.608 | 0.590399 | 342.381 | 78.1135 | 0.623505 | 390.944 | 510.66 | 0.584191 | 31.6649 | 205.537 | 312.682 | 265.995 | 29624.3 |
| 44470.2 | 22.1087 | 0.921434 | 88.7425 | 2.606 | 736.922 | 0.515196 | 333.248 | 40.3852 | 0.944624 | 409.909 | 200.876 | 0.966824 | 200.651 | 218.834 | 92.5309 | 104.3767 | 10692.5 |
| 50730.2 | 22.2089 | 0.909576 | 72.3626 | 1.02487 | 612.021 | 0.486588 | 490.558 | 456.512 | 0.907162 | 509.373 | 277.371 | 0.412831 | 7.03351 | 214.916 | 51.9017 | 332.5371 | 31062.85 |
| 41157.3 | 17.1224 | 0.927705 | 39.7416 | 0.514927 | 529.509 | 0.459144 | 238.313 | 170.307 | 0.583487 | 251.693 | 786.429 | 0.503129 | 25.2114 | 205.744 | 158.193 | 363.2052 | 36731.29 |
| 30595.4 | 18.4233 | 0.947713 | 57.1132 | 1.85835 | 177.982 | 0.221299 | 206.515 | 93.0762 | 0.445479 | 120.472 | 808.079 | 0.856731 | 52.3504 | 108.861 | 59.7322 | 407.2567 | 37446.64 |
| 72967.7 | 16.9291 | 0.86745 | 28.7631 | 2.70027 | 894.357 | 0.294786 | 156.691 | 141.254 | 0.785155 | 323.437 | 878.794 | 0.779004 | 35.7632 | 67.7382 | 104.857 | 422.5119 | 49236.51 |
| 27485.2 | 14.5332 | 0.953601 | 55.976 | 3.32719 | 582.624 | 0.453912 | 333.804 | 612.408 | 0.56804 | 384.728 | 658.777 | 0.653435 | 57.4115 | 210.183 | 323.715 | 327.9379 | 32940.69 |
| 61722.6 | 18.5712 | 0.888752 | 126.357 | 2.5158 | 904.323 | 0.49017 | 343.825 | 769.005 | 0.827359 | 386.434 | 871.22 | 0.92959 | 46.0147 | 50.1201 | 88.2192 | 272.7273 | 23727.02 |
| 37218.1 | 22.7557 | 0.935171 | 161.09 | 0.464825 | 918.16 | 0.660585 | 144.799 | 688.416 | 0.512851 | 137.569 | 899.529 | 0.786905 | 14.7308 | 45.6219 | 122.496 | 326.4784 | 27461.26 |
| 72315.6 | 16.3549 | 0.868685 | 32.3321 | 1.94054 | 302.133 | 0.490156 | 293.551 | 771.994 | 0.702943 | 402.049 | 568.478 | 0.626342 | 92.8855 | 57.8889 | 198.594 | 324.6562 | 21961.9 |
| 44940.8 | 16.3198 | 0.920538 | 166.777 | 3.79227 | 420.333 | 0.33442 | 356.079 | 868.615 | 0.909645 | 448.33 | 275.628 | 0.718969 | 33.326 | 199.564 | 438.379 | 315.9995 | 27472.62 |
| 54612.3 | 21.8673 | 0.902222 | 22.6221 | 0.29788 | 751.925 | 0.428964 | 408.678 | 432.636 | 0.690528 | 342.766 | 577.489 | 0.560457 | 16.0589 | 251.404 | 252.152 | 391.0845 | 41301.48 |
| 25880.6 | 13.8486 | 0.95664 | 30.3827 | 0.831467 | 958.148 | 0.477179 | 354.929 | 201.165 | 0.939603 | 182.894 | 15.1046 | 0.870713 | 50.5732 | 103.05 | 114.093 | 120.1679 | 16070.05 |
| 46972.9 | 20.548 | 0.916692 | 72.8698 | 0.780104 | 712.014 | 0.294895 | 274.256 | 36.9559 | 0.776719 | 67.6683 | 729.666 | 0.610263 | 67.1592 | 98.219 | 56.6057 | 408.8587 | 50376.45 |
| 47525.8 | 22.824 | 0.915646 | 168.686 | 3.42668 | 966.062 | 0.52867 | 324.049 | 661.585 | 0.473483 | 154.823 | 669.843 | 0.529145 | 40.6699 | 128.879 | 99.5569 | 551.7171 | 56913.52 |
| 65553.4 | 15.0542 | 0.881493 | 157.199 | 2.23421 | 87.8727 | 0.225786 | 108.922 | 752.744 | 0.767653 | 409.975 | 108.972 | 0.604256 | 79.5301 | 66.3759 | 203.723 | 512.9929 | 32791.57 |
| 41185.3 | 15.5825 | 0.927651 | 164.183 | 0.322269 | 964.467 | 0.264219 | 342.768 | 0.281433 | 0.830549 | 106.601 | 972.3 | 0.940183 | 1.525 | 95.6913 | 47.3091 | 517.0716 | 61391.31 |
| 58493.6 | 14.2733 | 0.894865 | 32.2236 | 3.0754 | 115.671 | 0.520959 | 133.352 | 393.627 | 0.579492 | 405.664 | 525.782 | 0.466083 | 252.439 | 122.417 | 247.603 | 415.04 | 25427.41 |
| 36811.5 | 13.2995 | 0.935935 | 118.744 | 2.83969 | 23.7327 | 0.436108 | 78.5637 | 477.294 | 0.715082 | 71.8848 | 589.7 | 0.326286 | 116.418 | 62.9338 | 49.8133 | 408.2692 | 24815.69 |
| 61594.2 | 14.5889 | 0.888992 | 15.5008 | 1.5692 | 867.717 | 0.455692 | 207.86 | 555.898 | 0.547509 | 292.61 | 616.964 | 0.973269 | 78.07 | 97.5964 | 182.83 | 299.6063 | 30634.97 |
| 38630.5 | 15.9336 | 0.932491 | 88.4025 | 0.251128 | 167.68 | 0.278066 | 434.65 | 964.081 | 0.844632 | 283.785 | 487.662 | 0.927267 | 21.3878 | 210.504 | 74.9026 | 289.6397 | 20994.92 |
| 90778.9 | 13.0807 | 0.83371 | 45.4723 | 3.6243 | 917.985 | 0.53004 | 120.234 | 816.956 | 0.609163 | 405.498 | 305.898 | 0.852773 | 109.353 | 97.5975 | 324.486 | 326.0331 | 26705.04 |
| 60317.4 | 16.4538 | 0.891412 | 144.285 | 0.251201 | 227.819 | 0.605607 | 422.823 | 754.156 | 0.561934 | 56.341 | 205.172 | 0.788465 | 1.17508 | 69.6364 | 48.0513 | 269.7499 | 17378.88 |
| 77383 | 13.3998 | 0.859085 | 155.374 | 0.121824 | 477.735 | 0.732995 | 288.598 | 341.872 | 0.884233 | 311.186 | 770.975 | 0.94392 | 10.3732 | 132.374 | 309.587 | 187.2432 | 11481.4 |
| 35957.2 | 25.7282 | 0.937563 | 54.3957 | 1.24786 | 453.424 | 0.371423 | 215.558 | 323.866 | 0.915534 | 294.898 | 848.029 | 0.363646 | 94.9038 | 106.523 | 272.377 | 431.2633 | 42246.91 |
| 70652.9 | 15.0867 | 0.871834 | 80.062 | 0.665867 | 374.788 | 0.498157 | 375.611 | 622.236 | 0.946057 | 367.261 | 383.217 | 0.91543 | 31.3473 | 98.1302 | 87.485 | 181.1025 | 12850.91 |
| 43278.4 | 15.5531 | 0.923687 | 49.6241 | 1.36776 | 679.485 | 0.4794 | 286.341 | 432.275 | 0.65478 | 417.699 | 651.874 | 0.606446 | 13.3296 | 218.613 | 62.2452 | 315.9167 | 31088.78 |
| 54613.7 | 20.7568 | 0.902219 | 55.5039 | 2.4149 | 25.9962 | 0.171541 | 96.5178 | 731.841 | 0.637795 | 499.924 | 213.947 | 0.969674 | 61.7989 | 80.5285 | 168.888 | 361.233 | 22006.37 |
| 39914.1 | 16.8339 | 0.93006 | 103.692 | 2.29014 | 380.79 | 0.440308 | 287.495 | 302.742 | 0.955282 | 413.995 | 901.896 | 0.37877 | 120.002 | 217.618 | 403.186 | 342.8911 | 29327.66 |
| 25012.4 | 18.4465 | 0.958288 | 121.363 | 2.96703 | 684.883 | 0.410843 | 283.771 | 128.556 | 0.780264 | 432.684 | 726.374 | 0.793388 | 89.8228 | 58.7988 | 112.269 | 220.0472 | 24975.65 |
| 37329.8 | 13.8682 | 0.934953 | 40.5452 | 3.54185 | 572.433 | 0.471449 | 431.178 | 103.336 | 0.801764 | 256.382 | 537.321 | 0.820926 | 7.86577 | 293.659 | 73.1455 | 167.6583 | 16950.63 |
| 32173.7 | 19.3157 | 0.944724 | 156.024 | 0.390588 | 362.158 | 0.633645 | 400.697 | 273.083 | 0.76477 | 191.853 | 178.507 | 0.579649 | 36.1358 | 126.758 | 160.556 | 189.5581 | 15195.52 |
| 59440 | 16.0274 | 0.893074 | 111.911 | 1.77529 | 507.353 | 0.488608 | 482.549 | 382.63 | 0.505832 | 277.543 | 336.552 | 0.591591 | 95.6836 | 363.328 | 220.631 | 363.9718 | 32991.27 |
| 48634.7 | 14.1389 | 0.91354 | 54.547 | 2.87327 | 256.399 | 0.332342 | 480.393 | 629.371 | 0.221043 | 315.43 | 668.07 | 0.848621 | 117.878 | 201.42 | 120.86 | 663.0813 | 58575.22 |
| 28149.6 | 24.1929 | 0.95235 | 150.784 | 3.78223 | 164.831 | 0.29454 | 463.343 | 128.126 | 0.16858 | 405.504 | 742.766 | 0.969463 | 12.1601 | 369.918 | 376.657 | 680.3169 | 61542.95 |
| 64596.5 | 16.3527 | 0.883307 | 138.573 | 2.49247 | 336.325 | 0.319658 | 176.305 | 255.116 | 0.875847 | 435.969 | 20.8352 | 0.323103 | 46.0055 | 62.3364 | 61.3821 | 571.5217 | 50666.83 |
| 34496.1 | 24.0294 | 0.940329 | 95.2686 | 2.13322 | 791.114 | 0.378937 | 268.719 | 1.85809 | 0.890451 | 471.764 | 853.213 | 0.919207 | 52.9973 | 188.325 | 273.129 | 208.5795 | 24076.07 |
| 46927.5 | 14.3446 | 0.916774 | 134.156 | 0.223968 | 593.25 | 0.239335 | 340.291 | 310.691 | 0.747878 | 253.601 | 392.606 | 0.860617 | 6.92516 | 176.988 | 195.647 | 430.4046 | 46843.57 |
| 59126.2 | 15.6202 | 0.893668 | 22.8082 | 0.344593 | 527.618 | 0.475387 | 197.897 | 553.564 | 0.430876 | 320.933 | 364.786 | 0.547191 | 19.588 | 117.236 | 150.949 | 478.236 | 44381.82 |
| 30846.4 | 13.1971 | 0.947234 | 16.3938 | 3.42169 | 265.857 | 0.379315 | 225.399 | 846.983 | 0.242191 | 340.445 | 534.94 | 0.746329 | 156.268 | 152.439 | 311.272 | 557.7566 | 51530.59 |
| 45780.6 | 18.0307 | 0.918948 | 121.431 | 1.32508 | 380.55 | 0.391374 | 351.432 | 220.607 | 0.946586 | 506.684 | 988.34 | 0.546989 | 77.1934 | 317.117 | 401.445 | 302.0721 | 25697.82 |
| 41286.7 | 23.1895 | 0.927465 | 152.193 | 1.82336 | 388.807 | 0.565391 | 477.462 | 620.832 | 0.772034 | 364.547 | 276.749 | 0.527709 | 18.9612 | 285.627 | 283.441 | 278.3882 | 21404.69 |
| 35560.5 | 23.4164 | 0.938312 | 46.6984 | 1.78009 | 367.366 | 0.455252 | 310.017 | 210.973 | 0.867166 | 459.777 | 248.765 | 0.957523 | 47.2856 | 151.229 | 145.043 | 119.4152 | 11098.87 |
| 49234.7 | 20.8402 | 0.912408 | 110.266 | 0.365392 | 431.974 | 0.625867 | 191.014 | 926.128 | 0.774319 | 171.153 | 467.608 | 0.53038 | 26.2718 | 125.33 | 141.626 | 370.7512 | 24429.49 |
| 56864.6 | 17.0138 | 0.897953 | 142.286 | 1.6996 | 619.032 | 0.434224 | 429.205 | 913.244 | 0.749653 | 467.219 | 435.479 | 0.505051 | 24.1678 | 236.012 | 390.61 | 479.2825 | 42332.63 |
| 53004.6 | 15.601 | 0.905263 | 163.759 | 1.32528 | 171.023 | 0.573419 | 159.883 | 854.749 | 0.607103 | 184.49 | 696.066 | 0.88132 | 21.9987 | 91.2622 | 119.884 | 265.7024 | 16403.18 |
| 28285.3 | 19.4015 | 0.952089 | 119.655 | 2.92301 | 227.57 | 0.281301 | 480.499 | 324.742 | 0.396125 | 405.8 | 728.674 | 0.934105 | 113.261 | 249.148 | 245.03 | 363.6071 | 34097.38 |
| 57201.1 | 17.1238 | 0.897315 | 149.47 | 1.99293 | 713.027 | 0.480666 | 197.47 | 431.892 | 0.860426 | 144.8 | 800.53 | 0.457272 | 14.3823 | 59.3344 | 106.214 | 411.6979 | 37452.61 |
| 79517.1 | 13.9507 | 0.855043 | 68.2431 | 1.94782 | 393.45 | 0.405154 | 403.439 | 845.051 | 0.210067 | 450.054 | 106.3 | 0.996212 | 11.5649 | 45.5416 | 420.043 | 617.0325 | 53714.51 |
| 37257.9 | 19.3286 | 0.935093 | 44.5678 | 0.222065 | 620.755 | 0.30519 | 389.652 | 211.636 | 0.996929 | 485.768 | 323.103 | 0.551612 | 5.41716 | 151.05 | 336.755 | 311.6977 | 37782.99 |
| 59225.1 | 17.24 | 0.893481 | 140.606 | 1.07793 | 668.134 | 0.46474 | 412.898 | 551.063 | 0.618143 | 402.353 | 936.62 | 0.8062 | 60.9725 | 330.266 | 224.678 | 352.7363 | 30921.24 |
| 56305.3 | 20.8564 | 0.899015 | 23.2316 | 2.94605 | 572.893 | 0.390031 | 435.712 | 12.6085 | 0.755026 | 358.909 | 101.463 | 0.347725 | 122.438 | 206.922 | 104.944 | 444.6848 | 50773.3 |
| 41690.4 | 16.9715 | 0.926695 | 54.896 | 1.01832 | 412.167 | 0.436898 | 150.196 | 857.651 | 0.279714 | 392.484 | 296.244 | 0.661937 | 99.0397 | 92.8948 | 250.044 | 559.2867 | 53517.4 |
| 71071.4 | 15.288 | 0.871041 | 34.3161 | 1.71161 | 115.682 | 0.316249 | 415.725 | 712.676 | 0.922283 | 212.932 | 925.363 | 0.562577 | 33.3847 | 143.434 | 161.329 | 399.1302 | 24760.62 |
| 33613.4 | 13.9856 | 0.941993 | 119.129 | 2.75849 | 518.015 | 0.191617 | 260.683 | 35.1603 | 0.833538 | 127.15 | 791.128 | 0.704562 | 13.773 | 185.092 | 94.0294 | 437.5874 | 54058.01 |
| 43070.2 | 23.7147 | 0.924087 | 102.072 | 1.31722 | 822.93 | 0.31708 | 159.293 | 886.348 | 0.858701 | 338.721 | 858.858 | 0.903581 | 107.729 | 116.027 | 83.6766 | 354.7771 | 36848.52 |
| 64871.4 | 14.756 | 0.882785 | 71.1165 | 1.55269 | 723.214 | 0.497412 | 382.023 | 609.716 | 0.612922 | 470.877 | 81.0796 | 0.491648 | 43.6738 | 148.651 | 222.529 | 397.8322 | 35924.84 |
| 31289 | 14.024 | 0.946396 | 24.5247 | 2.68872 | 189.966 | 0.394357 | 456.639 | 808.838 | 0.843834 | 294.312 | 822.187 | 0.662478 | 132.926 | 361.741 | 85.7231 | 280.6567 | 19834.57 |
| 76633.3 | 13.9934 | 0.860505 | 21.5052 | 1.24823 | 315.479 | 0.250471 | 121.903 | 288.115 | 0.843231 | 332.077 | 189.399 | 0.429142 | 106.898 | 65.7763 | 104.409 | 565.3338 | 49707.99 |
| 70293 | 15.9907 | 0.872516 | 61.6269 | 0.710188 | 22.9955 | 0.407219 | 383.036 | 624.708 | 0.875228 | 104.674 | 100.778 | 0.46429 | 21.0469 | 121.605 | 88.6524 | 316.8778 | 17542.49 |
| 53173.2 | 15.5871 | 0.904944 | 101.812 | 0.32229 | 489.221 | 0.59139 | 293.232 | 26.854 | 0.900285 | 433.539 | 456.689 | 0.352377 | 27.847 | 238.183 | 186.804 | 267.8328 | 21884.28 |
| 32329.1 | 25.9923 | 0.944436 | 32.875 | 2.21964 | 654.311 | 0.486521 | 203.884 | 781.782 | 0.954554 | 252.166 | 950.407 | 0.696663 | 88.1059 | 145.144 | 187.617 | 273.662 | 21999.49 |
| 47225.5 | 15.5982 | 0.91621 | 49.9667 | 2.83928 | 460.307 | 0.465897 | 150.203 | 591.203 | 0.287284 | 450.027 | 305.643 | 0.506202 | 155.128 | 67.3538 | 111.744 | 657.1313 | 62970.58 |
| 66055.9 | 15.6636 | 0.880542 | 148.687 | 2.20514 | 450.305 | 0.380882 | 475.153 | 533.579 | 0.880022 | 408.735 | 982.467 | 0.707653 | 122.318 | 130.811 | 214.906 | 345.9525 | 27380.95 |
| 48848.5 | 17.6734 | 0.913137 | 146.394 | 1.30382 | 271.195 | 0.387812 | 345.666 | 875.153 | 0.974261 | 260.851 | 655.695 | 0.32056 | 125.433 | 282.494 | 206.885 | 614.7585 | 44154.11 |
| 45214 | 13.2134 | 0.920019 | 97.0232 | 0.974297 | 17.307 | 0.496075 | 275.828 | 951.411 | 0.446444 | 322.852 | 651.027 | 0.426139 | 40.184 | 145.735 | 211.949 | 525.0518 | 30243.18 |
| 28482.4 | 25.731 | 0.951722 | 30.9813 | 1.659 | 173.441 | 0.386122 | 399.966 | 642.808 | 0.247327 | 361.255 | 297.023 | 0.691857 | 116.577 | 119.598 | 92.7097 | 498.3475 | 43041.76 |
| 36442.1 | 20.2356 | 0.936639 | 55.0178 | 1.12145 | 202.5 | 0.411357 | 335.689 | 288.804 | 0.771981 | 312.777 | 563.424 | 0.307015 | 62.2448 | 162.177 | 229.15 | 415.5643 | 33741.06 |
| 35759.9 | 23.2164 | 0.937934 | 59.7384 | 3.31283 | 456.882 | 0.323958 | 107.775 | 682.355 | 0.924143 | 318.771 | 179.497 | 0.619213 | 22.1875 | 54.5096 | 188.064 | 306.1697 | 30332.5 |
| 83261.9 | 14.1769 | 0.84795 | 143.596 | 1.81373 | 772.366 | 0.503633 | 59.4756 | 777.782 | 0.63561 | 407.421 | 982.598 | 0.707983 | 111.201 | 52.5357 | 121.38 | 428.4334 | 34975.66 |
| 26491.7 | 15.9996 | 0.955484 | 170.33 | 1.88713 | 300.04 | 0.354526 | 385.296 | 291.584 | 0.625822 | 210.874 | 39.0577 | 0.9166 | 145.737 | 228.562 | 142.974 | 206.7952 | 20318.38 |
| 49976.5 | 19.9295 | 0.911002 | 162.547 | 3.29732 | 549.405 | 0.472788 | 404.535 | 954.992 | 0.6408 | 471.092 | 476.761 | 0.677205 | 66.5944 | 323.593 | 323.369 | 366.367 | 30960.13 |
| 53946 | 13.0689 | 0.903479 | 147.503 | 1.62926 | 587.207 | 0.515843 | 452.625 | 354.799 | 0.388181 | 134.269 | 118.192 | 0.607987 | 7.2282 | 204.538 | 63.3244 | 442.3307 | 42855.63 |
| 66974.3 | 14.0803 | 0.878801 | 87.9705 | 0.192065 | 145.275 | 0.573048 | 152.346 | 109.069 | 0.871606 | 451.68 | 936.717 | 0.51685 | 11.682 | 148.254 | 401.687 | 243.3298 | 14889 |
| 47344.1 | 15.9318 | 0.915986 | 149.805 | 3.48546 | 160.498 | 0.470519 | 314.86 | 358.601 | 0.468883 | 394.481 | 240.139 | 0.534374 | 50.2928 | 210.142 | 253.25 | 355.9179 | 26085.18 |
| 48312 | 18.847 | 0.914154 | 59.1379 | 1.73435 | 874.653 | 0.406285 | 73.1748 | 155.531 | 0.654729 | 502.624 | 159.104 | 0.401789 | 159.24 | 60.5295 | 489.176 | 501.838 | 64626.01 |
| 57368.7 | 17.4581 | 0.896998 | 94.7179 | 1.13268 | 153.364 | 0.29967 | 324.212 | 226.856 | 0.953184 | 233.21 | 663.884 | 0.376407 | 97.5997 | 168.199 | 188.274 | 430.3359 | 31464.21 |
| 55216.9 | 13.8787 | 0.901072 | 129.61 | 1.76439 | 186.048 | 0.41868 | 493.929 | 922.993 | 0.788771 | 469.699 | 531.316 | 0.977862 | 111.227 | 430.767 | 115.289 | 226.9113 | 14939.82 |
| 34766.9 | 22.6499 | 0.939814 | 99.4624 | 2.30548 | 303.242 | 0.410175 | 129.4 | 815.059 | 0.7567 | 477.484 | 607.455 | 0.981686 | 154.477 | 57.2579 | 201.456 | 214.4105 | 16527.73 |
| 40314.4 | 21.4872 | 0.929305 | 83.9292 | 1.49768 | 190.874 | 0.251565 | 275.201 | 245.185 | 0.783083 | 242.808 | 223.792 | 0.616473 | 104.716 | 170.596 | 55.5561 | 304.4116 | 26990.17 |
| 82304.2 | 13.4722 | 0.849763 | 29.0908 | 1.76894 | 356.298 | 0.447025 | 412.103 | 537.678 | 0.96976 | 442.401 | 848.794 | 0.61912 | 2.81186 | 155.264 | 240.935 | 301.9595 | 21345.53 |
| 41495.1 | 21.1807 | 0.927069 | 148.155 | 2.47953 | 142.904 | 0.501606 | 242.925 | 795.913 | 0.196562 | 128.012 | 775.768 | 0.944306 | 92.5463 | 145.962 | 125.185 | 479.3961 | 33772.2 |
| 34632.4 | 24.7603 | 0.940071 | 48.8276 | 2.59995 | 764.486 | 0.451595 | 180.788 | 780.021 | 0.805915 | 499.038 | 19.4197 | 0.958822 | 115.182 | 100.263 | 410.987 | 181.7063 | 19296.29 |
| 53667.5 | 14.2895 | 0.904007 | 56.7464 | 0.207239 | 128.083 | 0.462274 | 475.953 | 460.174 | 0.454567 | 165.47 | 84.215 | 0.911855 | 16.6551 | 390.642 | 151.848 | 215.1559 | 15028.48 |
| 25602.9 | 14.4881 | 0.957167 | 159.951 | 1.60902 | 834.216 | 0.322229 | 315.184 | 360.505 | 0.971843 | 230.809 | 623.199 | 0.802858 | 106.255 | 42.518 | 118.435 | 297.2744 | 34690.37 |
| 37132.3 | 17.3406 | 0.93533 | 101.696 | 3.08591 | 397.776 | 0.30968 | 180.469 | 183.441 | 0.585185 | 186.695 | 459.144 | 0.546138 | 9.43177 | 98.9931 | 112.691 | 425.5608 | 46335.34 |
| 26284.2 | 27.5493 | 0.955888 | 141.526 | 1.28317 | 867.252 | 0.282465 | 385.336 | 528.664 | 0.904657 | 260.163 | 646.043 | 0.95228 | 30.2531 | 231.327 | 227.368 | 368.8223 | 44095.61 |
| 34191.2 | 13.1325 | 0.940898 | 165.667 | 1.02056 | 641.204 | 0.505499 | 208.213 | 647.542 | 0.785583 | 405.82 | 284.291 | 0.920324 | 65.3966 | 50.0135 | 111.56 | 203.5511 | 18415.97 |
| 25137 | 23.1491 | 0.958056 | 150.705 | 1.06927 | 51.9165 | 0.304395 | 455.3 | 269.743 | 0.669132 | 222.091 | 92.2475 | 0.941576 | 90.5718 | 419.995 | 162.065 | 178.0383 | 13189.89 |
| 38692.1 | 16.0756 | 0.932374 | 109.977 | 0.654227 | 219.655 | 0.512573 | 394.117 | 224.611 | 0.28038 | 492.788 | 496.442 | 0.77392 | 20.3818 | 228.415 | 84.2099 | 357.3713 | 28754.08 |
| 40069.4 | 14.2105 | 0.929764 | 61.7677 | 2.44395 | 815.795 | 0.367905 | 345.116 | 626.459 | 0.450222 | 170.965 | 245.336 | 0.976677 | 55.1957 | 249.721 | 153.434 | 358.9427 | 44831.89 |
| 32315.6 | 13.8629 | 0.944451 | 57.9369 | 1.8401 | 149.754 | 0.302248 | 243.546 | 787.852 | 0.676192 | 431.422 | 696.64 | 0.378328 | 10.1951 | 227.309 | 151.354 | 569.6518 | 43668.76 |
| 37024.8 | 19.9479 | 0.935535 | 50.6012 | 1.01749 | 255.043 | 0.238308 | 234.577 | 563.273 | 0.737457 | 251.54 | 241.114 | 0.940296 | 20.8849 | 168.892 | 185.988 | 261.3915 | 24396.57 |
| 68660.6 | 15.4661 | 0.875608 | 102.34 | 1.85077 | 18.6899 | 0.502573 | 357.17 | 775.696 | 0.833501 | 372.581 | 43.5782 | 0.596884 | 161.691 | 250.05 | 124.976 | 235.6043 | 12821.27 |
| 75897.4 | 14.0431 | 0.861899 | 23.6609 | 1.74294 | 517.729 | 0.454824 | 133.253 | 150.598 | 0.683419 | 234.515 | 682.539 | 0.968815 | 153.312 | 45.9245 | 88.8575 | 217.4075 | 18407.64 |
| 31958.7 | 19.6921 | 0.945131 | 169.194 | 3.28841 | 308.864 | 0.589204 | 140.494 | 334.781 | 0.339608 | 455.795 | 624.074 | 0.931085 | 43.2594 | 60.9549 | 350.406 | 249.3216 | 19093.02 |
| 63621 | 18.7652 | 0.885156 | 128.606 | 2.37396 | 166.396 | 0.231851 | 385.117 | 547.32 | 0.957473 | 294.185 | 196.433 | 0.519227 | 72.6448 | 204.906 | 289.132 | 446.4866 | 32756.69 |
| 27714.9 | 16.5146 | 0.953167 | 120.084 | 0.591902 | 369.619 | 0.485609 | 117.416 | 810.616 | 0.591739 | 344.879 | 321.398 | 0.748648 | 34.1624 | 105.361 | 310.271 | 269.0967 | 22651.03 |
| 43506.7 | 20.0163 | 0.923257 | 130.154 | 1.6973 | 346.816 | 0.470939 | 443.751 | 745.643 | 0.49769 | 102.718 | 1.31591 | 0.991506 | 38.3217 | 290.091 | 86.3067 | 218.7863 | 18774.71 |
| 69954.4 | 16.0278 | 0.873157 | 65.0254 | 0.835297 | 717.262 | 0.435984 | 375.946 | 766.955 | 0.732796 | 167.261 | 262.047 | 0.375172 | 19.0744 | 65.5601 | 156.344 | 605.4996 | 57902.52 |
| 52468.4 | 22.0661 | 0.906284 | 42.8176 | 2.39153 | 437.241 | 0.463897 | 478.713 | 530.604 | 0.298021 | 159.607 | 84.8608 | 0.830617 | 156.24 | 172.344 | 136.772 | 387.5676 | 36647.3 |
| 30287 | 25.4072 | 0.948303 | 94.9041 | 1.49888 | 996.912 | 0.517556 | 207.092 | 12.4365 | 0.706126 | 505.53 | 843.73 | 0.495187 | 73.9541 | 78.9005 | 248.225 | 317.2041 | 35944.66 |
| 53857.9 | 14.3825 | 0.903646 | 106.025 | 1.26392 | 44.0778 | 0.22719 | 250.549 | 565.21 | 0.916623 | 400.742 | 529.77 | 0.587625 | 70.6943 | 128.693 | 243.697 | 382.5813 | 23491.02 |
| 28553.3 | 25.4312 | 0.951587 | 102.413 | 1.38299 | 667.612 | 0.493991 | 452.227 | 627.147 | 0.358561 | 370.797 | 348.787 | 0.583864 | 126.415 | 370.459 | 201.844 | 460.3959 | 50152.53 |
| 34865.3 | 20.7461 | 0.939626 | 117.239 | 2.39649 | 37.8617 | 0.456466 | 318.642 | 87.6463 | 0.125447 | 187.971 | 508.591 | 0.919504 | 122.019 | 182.65 | 142.5 | 529.0258 | 36100.53 |
| 46702.2 | 20.2633 | 0.917204 | 164.826 | 1.92844 | 331.412 | 0.610223 | 312.516 | 877.608 | 0.886994 | 254.146 | 356.061 | 0.949056 | 160.187 | 166.008 | 138.3 | 176.0957 | 11481.71 |
| 47050.1 | 21.0175 | 0.916546 | 56.0543 | 2.64897 | 208.953 | 0.240135 | 392.226 | 727.074 | 0.612937 | 326.331 | 914.969 | 0.617767 | 81.8347 | 381.058 | 69.5309 | 533.8569 | 43323.98 |
| 67983 | 16.6886 | 0.876892 | 59.0877 | 1.27024 | 288.519 | 0.506681 | 368.807 | 943.811 | 0.544235 | 312.661 | 775.107 | 0.635381 | 89.1727 | 85.6894 | 248.815 | 409.8577 | 26563.8 |
| 74738.2 | 14.9145 | 0.864095 | 117.52 | 0.865913 | 368.224 | 0.391268 | 109.232 | 212.721 | 0.878076 | 234.533 | 641.394 | 0.370263 | 59.7436 | 67.1056 | 135.525 | 485.1206 | 39155.74 |
| 58150.3 | 15.9324 | 0.895517 | 139.291 | 2.90015 | 334.399 | 0.537353 | 277.914 | 825.082 | 0.289357 | 158.305 | 699.403 | 0.760682 | 67.6516 | 272.945 | 125.266 | 462.2879 | 33654.1 |
| 63067.1 | 18.9399 | 0.886205 | 104.747 | 2.55805 | 40.1063 | 0.161359 | 277.283 | 855.633 | 0.864306 | 141.301 | 617.324 | 0.582475 | 102.629 | 201.841 | 118.942 | 576.2079 | 34423.71 |
| 43749.2 | 18.0431 | 0.922796 | 41.4712 | 2.51772 | 500.677 | 0.462503 | 135.731 | 281.041 | 0.502759 | 90.5153 | 472.029 | 0.464365 | 134.728 | 109.96 | 74.2405 | 425.1268 | 42244.83 |
| 33340.3 | 16.405 | 0.942512 | 140.74 | 1.36349 | 751.251 | 0.48901 | 113.346 | 635.039 | 0.224457 | 436.066 | 231.796 | 0.880636 | 111.632 | 83.9984 | 367.098 | 535.1517 | 61747.95 |
| 78901.2 | 15.4149 | 0.85621 | 103.919 | 3.11674 | 670.556 | 0.491344 | 383.002 | 94.9113 | 0.354872 | 293.481 | 138.064 | 0.567797 | 135.199 | 160.086 | 247.708 | 510.2705 | 49828.68 |
| 33854.8 | 17.9572 | 0.941538 | 115.052 | 2.30312 | 335.238 | 0.422817 | 397.016 | 201.568 | 0.913531 | 131.469 | 262.752 | 0.424567 | 2.18039 | 352.237 | 120.965 | 253.6634 | 24290.64 |
| 33563.4 | 15.165 | 0.942088 | 79.7067 | 2.24431 | 260.512 | 0.180221 | 320.696 | 40.4177 | 0.858498 | 495.506 | 500.134 | 0.493579 | 83.6582 | 74.4537 | 326.156 | 467.1544 | 49528.7 |
| 28222.2 | 26.6042 | 0.952216 | 130.62 | 2.62116 | 239.376 | 0.431968 | 368.023 | 549.803 | 0.248942 | 397.967 | 426.684 | 0.534413 | 115.41 | 89.6085 | 361.302 | 628.3838 | 56694.67 |
| 73828.2 | 16.0379 | 0.86582 | 146.778 | 3.30758 | 7.53748 | 0.417007 | 497.621 | 926.553 | 0.726781 | 497.959 | 6.35862 | 0.994147 | 148.533 | 475.234 | 426.485 | 197.0816 | 10636.28 |
| 36867.9 | 22.7568 | 0.935835 | 132.776 | 2.49345 | 747.694 | 0.354394 | 295.01 | 323.458 | 0.923797 | 443.148 | 186.38 | 0.572079 | 133.942 | 227.21 | 85.3619 | 310.4345 | 37446.7 |
| 31876.2 | 26.0563 | 0.945293 | 79.2139 | 1.00308 | 541.672 | 0.429831 | 454.61 | 65.6388 | 0.421897 | 476.316 | 435.66 | 0.633 | 74.1517 | 230.499 | 234.482 | 354.9145 | 41610.64 |
| 39942.9 | 16.1908 | 0.930005 | 157.825 | 2.96422 | 531.673 | 0.378897 | 445.37 | 936.133 | 0.57484 | 329.096 | 225.943 | 0.871106 | 70.9244 | 333.389 | 315.24 | 329.1745 | 32061.18 |
| 39456.8 | 24.4065 | 0.930933 | 147.928 | 0.269544 | 238.614 | 0.66528 | 323.56 | 727.242 | 0.437131 | 505.906 | 588.879 | 0.831406 | 8.30036 | 101.331 | 90.9917 | 280.8439 | 18730.23 |
| 56048.6 | 19.6271 | 0.8995 | 41.7148 | 0.889953 | 191.1 | 0.313709 | 442.171 | 272.364 | 0.813081 | 442.245 | 723.496 | 0.571495 | 67.7946 | 323.519 | 265.792 | 331.5374 | 25267.45 |
| 30945.7 | 15.3116 | 0.947047 | 158.571 | 0.913323 | 811.572 | 0.523464 | 444.312 | 289.91 | 0.48637 | 147.058 | 537.51 | 0.825703 | 86.3216 | 207.082 | 69.6047 | 294.3762 | 31452.55 |
| 57466.1 | 17.4426 | 0.896814 | 125.978 | 3.39524 | 228.748 | 0.458127 | 432.921 | 847.622 | 0.314753 | 499.49 | 712.582 | 0.807561 | 35.337 | 231.122 | 74.3048 | 443.4584 | 32408.32 |
| 85120.8 | 14.5972 | 0.844429 | 67.5534 | 2.83798 | 570.831 | 0.463844 | 347.437 | 74.8481 | 0.417614 | 390.638 | 905.925 | 0.872736 | 130.021 | 192.186 | 238.25 | 369.8089 | 32447.25 |
| 82169 | 14.449 | 0.85002 | 143.598 | 1.44639 | 321.707 | 0.425977 | 253.181 | 807.335 | 0.394739 | 434.943 | 489.244 | 0.952424 | 60.0499 | 96.3702 | 327.838 | 430.447 | 31221.45 |
| 68537 | 18.7061 | 0.875844 | 119.387 | 0.906608 | 187.813 | 0.485619 | 249.057 | 438.474 | 0.723742 | 332.86 | 593.954 | 0.852209 | 83.0534 | 115.524 | 226.997 | 225.9758 | 14596.13 |
| 53246.4 | 14.0165 | 0.904804 | 121.32 | 2.0001 | 701.976 | 0.575348 | 293.374 | 599.54 | 0.293763 | 476.894 | 152.407 | 0.720191 | 21.1049 | 286.475 | 354.497 | 691.8465 | 63436.62 |
| 62503.3 | 14.5408 | 0.88727 | 42.8175 | 3.08426 | 269.58 | 0.513182 | 130.85 | 526.963 | 0.889325 | 472.897 | 299.234 | 0.88746 | 234.151 | 100.303 | 98.5257 | 163.2045 | 10729.08 |
| 54487.4 | 19.618 | 0.902457 | 74.9998 | 2.42108 | 327.484 | 0.49329 | 360.135 | 751.706 | 0.339739 | 157.543 | 205.623 | 0.761 | 126.483 | 72.3176 | 134.934 | 366.793 | 28655.94 |
| 39080.8 | 23.9834 | 0.931644 | 68.8055 | 0.661479 | 0.577333 | 0.581453 | 264.61 | 952.111 | 0.634178 | 372.443 | 409.868 | 0.977541 | 50.8689 | 202.19 | 341.822 | 236.2502 | 13195.77 |
| 44496.8 | 22.6364 | 0.921384 | 64.632 | 0.65576 | 173.595 | 0.354797 | 320.057 | 892.235 | 0.865276 | 87.3916 | 761.425 | 0.412298 | 22.9883 | 261.358 | 84.1414 | 474.5328 | 33104.16 |
| 65992.3 | 15.4105 | 0.880662 | 80.4226 | 2.15511 | 16.1981 | 0.432462 | 361.87 | 665.142 | 0.688723 | 91.4434 | 356.206 | 0.736325 | 50.0898 | 318.27 | 61.7541 | 242.4549 | 13405.63 |
| 45424.2 | 19.4921 | 0.919625 | 70.7599 | 0.297584 | 265.756 | 0.442882 | 152.22 | 852.239 | 0.233375 | 460.137 | 147.294 | 0.673882 | 28.4467 | 147.917 | 85.4081 | 613.6634 | 51687.81 |
| 57301 | 13.5102 | 0.897124 | 120.189 | 2.00924 | 686.088 | 0.311637 | 174.961 | 240.786 | 0.390145 | 510.501 | 555.359 | 0.964212 | 52.7371 | 129.844 | 229.619 | 505.2533 | 58662.51 |
| 42275.3 | 18.5969 | 0.925589 | 124.026 | 1.55011 | 914.339 | 0.445675 | 231.597 | 658.173 | 0.990131 | 154.233 | 256.804 | 0.662443 | 41.2774 | 70.0555 | 87.0099 | 274.9525 | 28594.88 |
| 28875.9 | 21.903 | 0.950972 | 169.716 | 3.20575 | 138.788 | 0.461677 | 433.258 | 774.07 | 0.903683 | 327.03 | 83.2342 | 0.890033 | 1.68869 | 193.416 | 117.858 | 156.0062 | 10839.36 |
| 61555.7 | 14.4576 | 0.889065 | 160.867 | 1.7997 | 53.6325 | 0.544599 | 322.003 | 478.6 | 0.929448 | 290.594 | 448.478 | 0.481887 | 169.303 | 102.824 | 82.3231 | 280.1532 | 15973.57 |
| 56261.6 | 16.6182 | 0.899094 | 162.263 | 1.21373 | 535.894 | 0.42455 | 55.5722 | 209.18 | 0.715364 | 272.149 | 597.841 | 0.992257 | 44.5452 | 45.489 | 218.475 | 239.8051 | 21195.9 |
| 27609.5 | 15.1075 | 0.953366 | 168.562 | 2.11049 | 814.763 | 0.570003 | 183.646 | 426.389 | 0.786259 | 329.886 | 160.441 | 0.847168 | 26.3525 | 70.3316 | 165.107 | 164.2373 | 16869.22 |
| 44649.4 | 18.6112 | 0.921092 | 128.515 | 0.477559 | 698.54 | 0.552283 | 256.56 | 320.751 | 0.264819 | 338.385 | 593.656 | 0.720486 | 43.1378 | 235.719 | 164.821 | 528.3966 | 53049.5 |
| 33734.7 | 20.1251 | 0.941767 | 55.8267 | 1.31733 | 458.003 | 0.471925 | 259.681 | 550.747 | 0.95109 | 359.074 | 362.94 | 0.433631 | 63.5719 | 52.6401 | 101.287 | 301.5233 | 26055 |
| 43226.6 | 22.4039 | 0.92379 | 71.58 | 3.43141 | 365.922 | 0.463898 | 394.173 | 451.785 | 0.993407 | 267.109 | 446.084 | 0.88137 | 11.8438 | 158.93 | 186.998 | 160.8818 | 12761.74 |
| 39875.6 | 23.1408 | 0.930138 | 42.5764 | 1.4237 | 320.601 | 0.262728 | 130.927 | 188.181 | 0.795501 | 389.354 | 411.754 | 0.712209 | 29.1727 | 45.7596 | 181.554 | 288.8905 | 29082.95 |
| 74322.5 | 13.5317 | 0.864882 | 46.7997 | 2.62421 | 284.859 | 0.416764 | 268.668 | 860.319 | 0.552446 | 289.944 | 796.575 | 0.596708 | 123.254 | 137.39 | 142.555 | 474.6791 | 34020.73 |
| 38772.2 | 19.2758 | 0.932225 | 93.198 | 1.37 | 479.724 | 0.362323 | 395.736 | 65.8987 | 0.723616 | 359.394 | 691.432 | 0.856654 | 35.0294 | 304.225 | 336.093 | 226.6553 | 23574.62 |
| 34662 | 21.5278 | 0.940012 | 170.519 | 1.96182 | 501.492 | 0.340972 | 306.181 | 460.45 | 0.609571 | 393.013 | 625.705 | 0.922596 | 37.5278 | 284.163 | 356.158 | 323.5532 | 32037.43 |
| 44175.3 | 20.6362 | 0.921991 | 34.1317 | 1.48353 | 550.424 | 0.512568 | 296.35 | 173.177 | 0.396833 | 438.713 | 929.702 | 0.671905 | 127.306 | 127.105 | 333.078 | 400.6364 | 35530.09 |
| 50864.7 | 16.2263 | 0.909317 | 159.209 | 2.05139 | 695.892 | 0.564457 | 90.7926 | 277.542 | 0.475273 | 305.223 | 493.42 | 0.472831 | 50.1173 | 44.568 | 155.041 | 461.9702 | 43993.38 |
| 76362.1 | 13.5702 | 0.861019 | 48.6474 | 1.38581 | 648.629 | 0.40638 | 145.191 | 941.26 | 0.333099 | 169.206 | 461.238 | 0.756973 | 135.651 | 107.634 | 101.856 | 632.2122 | 61509.26 |
| 33972.7 | 20.9178 | 0.941317 | 134.158 | 1.21698 | 980.679 | 0.535554 | 185.778 | 952.674 | 0.686761 | 397.132 | 75.8723 | 0.352678 | 61.112 | 160.199 | 108.817 | 584.5719 | 59425.7 |
| 29848.8 | 13.256 | 0.949123 | 75.2372 | 2.11326 | 255.745 | 0.521551 | 319.939 | 900.337 | 0.385748 | 477.394 | 794.697 | 0.575675 | 122.861 | 305.157 | 460.109 | 602.0208 | 43618.51 |
| 44687.9 | 13.6979 | 0.921016 | 161.244 | 1.59964 | 623.381 | 0.341741 | 122.312 | 514.24 | 0.941849 | 366.699 | 703.564 | 0.648204 | 34.0174 | 98.3943 | 160.821 | 369.1151 | 35631.95 |
| 32507.6 | 14.1521 | 0.944088 | 114.283 | 1.51324 | 163.647 | 0.487206 | 345.039 | 378.661 | 0.617127 | 117.981 | 887.263 | 0.382763 | 57.1842 | 94.7812 | 56.8018 | 393.1901 | 28597.76 |
| 29045.7 | 17.8667 | 0.950648 | 70.0479 | 3.64869 | 771.869 | 0.397539 | 87.7907 | 124.94 | 0.96534 | 435.04 | 336.654 | 0.694231 | 58.871 | 46.9893 | 206.621 | 196.2147 | 24907.59 |
| 51374.4 | 21.7826 | 0.908356 | 122.091 | 2.36741 | 466.696 | 0.387154 | 327.998 | 935.886 | 0.598125 | 362.637 | 182.939 | 0.99542 | 81.5315 | 272.446 | 140.761 | 271.0455 | 24632.59 |
| 52449.8 | 14.9724 | 0.906314 | 158.38 | 1.23288 | 682.78 | 0.515703 | 199.292 | 400.087 | 0.820974 | 144.066 | 391.896 | 0.690522 | 16.5348 | 87.1195 | 143.44 | 252.1227 | 22730.93 |
| 27073.6 | 17.4449 | 0.954383 | 108.282 | 0.929187 | 842.151 | 0.342434 | 389.713 | 752.418 | 0.940717 | 157.382 | 426.228 | 0.479021 | 17.154 | 134.288 | 93.3572 | 473.3641 | 54544.41 |
| 47303.3 | 16.3008 | 0.916063 | 96.937 | 2.08949 | 330.897 | 0.306766 | 214.255 | 608.034 | 0.509727 | 137.88 | 159.815 | 0.644548 | 42.1187 | 155.713 | 55.8606 | 450.1208 | 43010.46 |
| 81512.7 | 13.974 | 0.851263 | 98.2892 | 1.50709 | 148.833 | 0.435487 | 456.195 | 366.233 | 0.417046 | 211.732 | 793.921 | 0.522793 | 125.979 | 267.806 | 179.707 | 540.6998 | 34770.26 |
| 32114.4 | 15.1774 | 0.944833 | 55.394 | 1.71037 | 21.5869 | 0.281926 | 348.157 | 698.324 | 0.828412 | 267.874 | 411.176 | 0.345178 | 39.0528 | 134.021 | 88.7664 | 482.2881 | 30096.96 |
| 59895.1 | 16.8603 | 0.892212 | 137.871 | 0.992803 | 123.443 | 0.393577 | 192.848 | 624.777 | 0.557947 | 272.446 | 151.451 | 0.799861 | 69.0013 | 71.9247 | 145.031 | 305.0122 | 20141.57 |
| 53998 | 20.1523 | 0.903385 | 114.038 | 1.74115 | 609.197 | 0.463037 | 254.269 | 271.874 | 0.620716 | 290.236 | 650.175 | 0.801272 | 152.659 | 74.287 | 257.085 | 268.1442 | 25420.19 |
| 72616 | 16.4376 | 0.868116 | 102.813 | 2.52452 | 339.826 | 0.394733 | 283.19 | 736.657 | 0.837941 | 465.779 | 228.677 | 0.424643 | 3.85589 | 206.949 | 433.484 | 456.5852 | 35423.4 |
| 69965.7 | 14.9595 | 0.873135 | 85.3764 | 3.05497 | 207.705 | 0.516118 | 121.386 | 419.396 | 0.878013 | 452.82 | 516.418 | 0.567408 | 85.8498 | 87.7106 | 386.291 | 257.8281 | 16156.48 |
| 47393.2 | 14.2224 | 0.915892 | 167.446 | 1.28664 | 883.275 | 0.490437 | 462.472 | 642.148 | 0.645058 | 470.83 | 226.997 | 0.504793 | 2.45529 | 440.087 | 290.409 | 467.6246 | 47827.7 |
| 77735.8 | 15.2489 | 0.858418 | 127.297 | 3.38387 | 269.857 | 0.264854 | 196.606 | 528.087 | 0.50237 | 453.571 | 44.7435 | 0.850008 | 137.374 | 161.325 | 378.029 | 445.7611 | 36829.96 |
| 25814.3 | 15.1387 | 0.956767 | 121.235 | 1.82647 | 169.78 | 0.465244 | 98.7818 | 564.419 | 0.704898 | 157.498 | 569.831 | 0.933763 | 47.4321 | 45.6764 | 127.726 | 178.3636 | 12779.29 |
| 45223.8 | 19.4271 | 0.920004 | 32.8303 | 1.51441 | 640.582 | 0.577636 | 425.993 | 42.0845 | 0.805552 | 482.754 | 580.842 | 0.848575 | 58.4422 | 323.152 | 460.724 | 173.917 | 14965.02 |
| 55779.2 | 18.3784 | 0.900009 | 168.2 | 0.493724 | 108.124 | 0.213179 | 476.564 | 483.679 | 0.543926 | 515.892 | 541.273 | 0.730043 | 41.5786 | 202.884 | 115.187 | 670.1984 | 45342.44 |
| 27772.2 | 17.8468 | 0.95306 | 95.9273 | 3.78655 | 406.77 | 0.500683 | 171.666 | 420.594 | 0.560015 | 405.033 | 155.649 | 0.363731 | 109.22 | 116.968 | 334.536 | 443.2033 | 39886.69 |
| 46473.9 | 21.2912 | 0.917638 | 102.744 | 0.25552 | 20.8288 | 0.383152 | 343.02 | 732.584 | 0.95437 | 377.644 | 608.808 | 0.363485 | 9.6532 | 156.663 | 194.624 | 466.2008 | 26801.39 |
| 36579.7 | 23.9201 | 0.936382 | 110.623 | 0.397453 | 172.03 | 0.2509 | 205.16 | 944.875 | 0.323153 | 216.358 | 839.562 | 0.96072 | 8.31631 | 160.052 | 197.747 | 594.1753 | 47811.12 |
| 41329.1 | 14.2032 | 0.927378 | 15.7629 | 2.96459 | 496.063 | 0.23524 | 332.303 | 317.566 | 0.869361 | 259.035 | 964.736 | 0.961163 | 153.558 | 239.328 | 183.029 | 347.621 | 35737.01 |
| 35934 | 16.2235 | 0.937599 | 58.9095 | 3.66675 | 228.529 | 0.468873 | 175.261 | 50.6347 | 0.580043 | 206.87 | 990.281 | 0.45255 | 74.0997 | 167.58 | 62.4849 | 318.2685 | 25891.95 |
| 37209.3 | 24.2682 | 0.93519 | 31.8541 | 2.70588 | 806.53 | 0.433539 | 460.14 | 89.1776 | 0.729481 | 349.052 | 732.88 | 0.833955 | 162.916 | 253.534 | 258.605 | 227.4977 | 25841.31 |
| 53138 | 18.9662 | 0.905013 | 150.345 | 2.24476 | 370.453 | 0.614816 | 497.415 | 744.875 | 0.772843 | 388.429 | 339.575 | 0.597485 | 84.666 | 480.185 | 276.16 | 294.4387 | 19405.13 |
| 63592.4 | 18.8355 | 0.88521 | 133.89 | 0.381197 | 61.6366 | 0.418519 | 476.628 | 22.8363 | 0.437349 | 491.984 | 356.519 | 0.81283 | 35.0767 | 163.684 | 482.542 | 320.7041 | 19680.54 |
| 41444.4 | 18.6522 | 0.927163 | 96.8506 | 1.58037 | 582.656 | 0.253691 | 198.391 | 958.34 | 0.791563 | 166.381 | 244.882 | 0.690045 | 63.7608 | 166.333 | 55.0812 | 447.6246 | 49057.65 |
| 76043 | 14.3845 | 0.861624 | 77.2419 | 0.444016 | 295.792 | 0.393306 | 268.34 | 548.465 | 0.607342 | 205.749 | 724.752 | 0.694083 | 4.08957 | 248.933 | 143.722 | 386.5855 | 28691.94 |
| 52540.1 | 21.029 | 0.906147 | 142.705 | 1.53172 | 263.207 | 0.35501 | 183.834 | 547.38 | 0.627081 | 153.647 | 386.23 | 0.771333 | 39.412 | 157.133 | 53.4427 | 328.0945 | 25947.83 |
| 37374.1 | 15.9741 | 0.934871 | 90.2092 | 0.676107 | 481.777 | 0.447206 | 224.029 | 977.223 | 0.53805 | 466.282 | 351.136 | 0.61364 | 13.2059 | 193.261 | 228.436 | 405.0754 | 36871.43 |
| 47517.8 | 16.1347 | 0.915657 | 102.934 | 1.57916 | 822.3 | 0.763364 | 429.939 | 297.851 | 0.91681 | 449.068 | 253.08 | 0.670935 | 14.0733 | 309.257 | 432.865 | 277.2005 | 21031.63 |
| 71508.3 | 14.6676 | 0.870213 | 19.3292 | 3.61279 | 117.551 | 0.520937 | 315.401 | 185.877 | 0.56969 | 464.048 | 148.473 | 0.870544 | 156.685 | 259.666 | 323.811 | 177.9586 | 11017.89 |
| 28729.9 | 18.4348 | 0.951246 | 44.9447 | 3.4514 | 327.65 | 0.417266 | 319.593 | 74.3356 | 0.980243 | 126.982 | 50.4351 | 0.640284 | 53.7574 | 84.0645 | 83.9862 | 125.41 | 13511.5 |
| 48596.2 | 14.7112 | 0.913613 | 55.3784 | 0.286797 | 568.561 | 0.502038 | 263.331 | 55.1325 | 0.537054 | 516.572 | 369.838 | 0.837095 | 16.5787 | 146.696 | 427.819 | 198.5405 | 19433.21 |
| 64893 | 19.4089 | 0.882747 | 88.1783 | 1.3606 | 442.537 | 0.300276 | 460.401 | 745.404 | 0.662337 | 427.996 | 173.043 | 0.91066 | 12.71 | 320.875 | 118.402 | 325.2669 | 30759.4 |
| 53008.1 | 13.3204 | 0.905255 | 130.357 | 1.08265 | 899.071 | 0.577037 | 318.199 | 385.822 | 0.262114 | 471.997 | 74.232 | 0.967715 | 31.7835 | 104.148 | 200.86 | 358.3169 | 36525.62 |
| 32018.1 | 22.0625 | 0.945021 | 40.9246 | 3.56105 | 699.756 | 0.306643 | 453.382 | 210.645 | 0.670341 | 72.3452 | 575.382 | 0.79176 | 2.62409 | 440.229 | 67.1098 | 334.0331 | 42335.05 |
| 71489.7 | 16.577 | 0.87025 | 17.9669 | 1.64496 | 273.168 | 0.183397 | 280.128 | 310.522 | 0.716425 | 328.714 | 221.798 | 0.941917 | 67.4914 | 193.104 | 96.6875 | 392.6722 | 34913.24 |
| 60678.4 | 14.137 | 0.890727 | 56.4787 | 1.80014 | 809.266 | 0.429761 | 272.6 | 988.329 | 0.89232 | 373.236 | 619.58 | 0.851573 | 152.238 | 118.082 | 358.954 | 289.831 | 25983.68 |
| 30860 | 25.9366 | 0.947218 | 44.0943 | 1.08622 | 840.489 | 0.417585 | 336.668 | 249.953 | 0.432162 | 365.104 | 976.2 | 0.867993 | 76.566 | 99.5611 | 204.628 | 376.1754 | 45337.77 |
| 65936.9 | 16.1609 | 0.880767 | 38.5634 | 1.30205 | 682.353 | 0.38345 | 162.272 | 404.875 | 0.73844 | 218.534 | 319.141 | 0.609696 | 59.1691 | 120.392 | 116.34 | 366.1066 | 38364.65 |
| 73225.7 | 13.5313 | 0.86696 | 145.658 | 1.87025 | 698.902 | 0.427315 | 446.83 | 506.513 | 0.895476 | 114.706 | 30.2275 | 0.762664 | 58.4423 | 125.388 | 89.7642 | 251.9911 | 24011.64 |
| 35345.6 | 24.7351 | 0.93872 | 35.9516 | 3.38201 | 21.3559 | 0.335096 | 136.527 | 100.414 | 0.59172 | 448.151 | 175.591 | 0.584163 | 103.04 | 123.557 | 376.029 | 236.0407 | 15817.7 |
| 42864 | 24.5389 | 0.924479 | 117.682 | 3.58743 | 531.095 | 0.391346 | 498.558 | 475.128 | 0.897119 | 472.193 | 192.332 | 0.620669 | 73.0646 | 206.954 | 187.053 | 256.7023 | 25896.12 |
| 43967.7 | 21.8596 | 0.922385 | 67.5445 | 1.23509 | 533.874 | 0.347785 | 331.729 | 289.595 | 0.85557 | 366.399 | 297.582 | 0.532503 | 73.2225 | 169.732 | 239.738 | 324.0987 | 35263.06 |
| 70888.4 | 13.4437 | 0.871387 | 116.158 | 3.6163 | 433.513 | 0.586995 | 275.453 | 63.3459 | 0.991839 | 284.786 | 483.481 | 0.971116 | 13.6553 | 154.938 | 247.217 | 147.5187 | 10489.35 |
| 26956.9 | 24.015 | 0.954609 | 164.759 | 0.844126 | 30.1453 | 0.470999 | 322.552 | 29.2566 | 0.349018 | 336.398 | 188.922 | 0.940053 | 23.6998 | 298.93 | 116.252 | 219.6779 | 15474.23 |
| 41347.3 | 22.2145 | 0.927349 | 139.289 | 3.18586 | 741.288 | 0.337015 | 181.148 | 967.948 | 0.927464 | 453.945 | 421.775 | 0.478812 | 69.6201 | 120.601 | 65.5617 | 526.5996 | 54165.18 |
| 39146.2 | 24.126 | 0.931521 | 157.146 | 1.41474 | 778.073 | 0.25143 | 327.25 | 760.836 | 0.776232 | 287.343 | 973.49 | 0.818475 | 43.7387 | 230.845 | 107.697 | 510.2161 | 56353.12 |
| 40861.4 | 24.1552 | 0.928272 | 141.977 | 1.76885 | 523.199 | 0.341802 | 352.723 | 147.676 | 0.419227 | 275.845 | 244.285 | 0.661599 | 88.1727 | 122.556 | 216.075 | 509.663 | 57443.15 |
| 34467 | 19.4816 | 0.94038 | 166.632 | 1.17275 | 374.729 | 0.49084 | 488.096 | 23.0508 | 0.416757 | 290.163 | 136.546 | 0.983413 | 49.2855 | 451.755 | 156.858 | 214.2632 | 20616.62 |
| 61059.9 | 17.0064 | 0.890006 | 100.358 | 0.785501 | 664.836 | 0.381255 | 92.324 | 342.812 | 0.682498 | 506.527 | 697.064 | 0.734775 | 69.0737 | 74.5373 | 315.017 | 357.9554 | 35878.32 |
| 45664.5 | 20.081 | 0.91917 | 69.7228 | 1.66963 | 537.1 | 0.462277 | 338.698 | 264.651 | 0.910014 | 495.081 | 3.60895 | 0.371757 | 27.3591 | 248.122 | 363.328 | 307.8497 | 31727.82 |
| 62042.5 | 13.5034 | 0.888143 | 120.478 | 0.689059 | 827.928 | 0.513428 | 396.065 | 399.147 | 0.695293 | 378.416 | 208.623 | 0.536813 | 45.6617 | 288.444 | 212.094 | 355.0023 | 35413 |
| 30073 | 17.4849 | 0.948701 | 112.961 | 0.237594 | 694.806 | 0.595214 | 495.426 | 75.0038 | 0.407804 | 337.252 | 30.0947 | 0.480007 | 19.3182 | 236.848 | 97.7334 | 360.6316 | 40482.44 |
| 73304.8 | 17.5278 | 0.866812 | 85.9584 | 0.534589 | 1.08343 | 0.399504 | 422.737 | 486.572 | 0.530909 | 370.065 | 295.177 | 0.534982 | 41.3546 | 354.375 | 281.67 | 416.3233 | 22224.34 |
| 73782.6 | 13.4267 | 0.865905 | 60.4553 | 0.726604 | 111.188 | 0.408332 | 234.996 | 609.166 | 0.924526 | 268.368 | 420.48 | 0.647408 | 57.7259 | 114.286 | 231.801 | 257.0452 | 15649.18 |
| 44421.7 | 16.6712 | 0.921522 | 137.032 | 2.26463 | 299.951 | 0.239624 | 436.643 | 363.299 | 0.58111 | 64.9508 | 990.598 | 0.510565 | 77.249 | 108.181 | 48.2425 | 686.6017 | 63620.49 |
| 40148.9 | 19.5441 | 0.929617 | 37.4944 | 3.6311 | 80.7128 | 0.438634 | 398.74 | 420.459 | 0.74009 | 209.224 | 415.577 | 0.649095 | 141.841 | 79.0432 | 51.8231 | 209.6026 | 13753.49 |
| 34409.5 | 14.5271 | 0.940485 | 107.487 | 1.60644 | 5.67572 | 0.316052 | 414.905 | 511.111 | 0.868443 | 143.036 | 863.759 | 0.405807 | 116.533 | 193.244 | 50.6937 | 388.6101 | 23046.46 |
| 62658.1 | 18.8481 | 0.88698 | 150.22 | 1.81741 | 751.975 | 0.329769 | 447.074 | 356.817 | 0.991845 | 290.373 | 382.163 | 0.864588 | 135.895 | 350.008 | 47.8486 | 302.9277 | 31310.11 |
| 28360.6 | 15.7786 | 0.951944 | 84.2899 | 1.94686 | 518.224 | 0.313517 | 349.515 | 558.579 | 0.738468 | 165.784 | 79.5446 | 0.39717 | 148.15 | 126.449 | 125.869 | 519.0606 | 59840.51 |
| 53818.7 | 13.4885 | 0.90372 | 104.519 | 2.32326 | 898.397 | 0.475018 | 139.135 | 307.041 | 0.496526 | 463.079 | 620.664 | 0.96149 | 104.654 | 47.2254 | 205.855 | 279.4904 | 29964.85 |
| 35055 | 14.4415 | 0.939263 | 162.984 | 0.894785 | 348.649 | 0.544621 | 272.467 | 988.847 | 0.221325 | 179.701 | 860.554 | 0.831154 | 23.3373 | 95.463 | 145.812 | 562.4778 | 45308.25 |
| 43376.7 | 22.226 | 0.923505 | 139.874 | 0.823394 | 140.296 | 0.58314 | 476.68 | 513.663 | 0.638647 | 416.196 | 770.705 | 0.318157 | 25.7014 | 121.167 | 229.397 | 489.204 | 31586.62 |
| 31819.8 | 14.745 | 0.945391 | 29.8788 | 1.34255 | 745.628 | 0.481163 | 396.552 | 716.735 | 0.631142 | 160.47 | 147.665 | 0.890712 | 31.7432 | 138.658 | 136.002 | 210.5791 | 21824.16 |
| 52523.4 | 21.488 | 0.906179 | 55.3561 | 3.45821 | 688.776 | 0.409041 | 378.976 | 470.2 | 0.583136 | 315.39 | 638.226 | 0.520399 | 115.348 | 250.18 | 124.97 | 489.3628 | 51712.94 |
| 51307.4 | 15.1002 | 0.908478 | 142.098 | 3.01774 | 745.016 | 0.446156 | 372.996 | 243.449 | 0.711748 | 150.957 | 799.185 | 0.591511 | 29.5431 | 116.338 | 149.398 | 353.4705 | 36435.01 |
| 53047.5 | 16.3192 | 0.905182 | 87.7113 | 1.83712 | 143.464 | 0.353921 | 80.8419 | 151.963 | 0.650096 | 125.193 | 404.107 | 0.785793 | 154.125 | 48.7176 | 81.6985 | 223.6316 | 16603.94 |
| 35345.1 | 24.0416 | 0.938721 | 132.335 | 2.48958 | 776.955 | 0.530201 | 390.843 | 67.3575 | 0.500547 | 239.624 | 731.145 | 0.843247 | 134.815 | 359.131 | 198.385 | 235.9056 | 24153.69 |
| 32123.6 | 17.375 | 0.944817 | 39.1491 | 2.07858 | 598.226 | 0.260423 | 257.704 | 326.354 | 0.757541 | 228.327 | 793.872 | 0.752493 | 102.385 | 137.394 | 88.0922 | 376.874 | 44361.38 |
| 59682.8 | 19.185 | 0.892616 | 127.82 | 2.46492 | 305.43 | 0.489359 | 492.615 | 450.172 | 0.714378 | 107.778 | 354.813 | 0.268893 | 154.364 | 486.567 | 94.8714 | 570.0517 | 43305.81 |
| 27861.6 | 26.9731 | 0.952899 | 77.5428 | 1.48333 | 147.305 | 0.280791 | 417.413 | 148.089 | 0.845053 | 310.247 | 405.542 | 0.195934 | 30.4852 | 61.5755 | 145.388 | 664.9979 | 59213.07 |
| 33070.3 | 16.1338 | 0.943023 | 46.9329 | 1.68344 | 946.642 | 0.440135 | 471.512 | 478.574 | 0.815776 | 253.693 | 111.559 | 0.450712 | 52.4034 | 132.236 | 101.45 | 372.4367 | 45957.83 |
| 65903.6 | 17.4401 | 0.880831 | 165.019 | 2.02591 | 117.357 | 0.451448 | 153.733 | 573.114 | 0.974613 | 255.294 | 8.86644 | 0.401068 | 123.725 | 88.1264 | 181.183 | 374.8478 | 23017.77 |
| 64746.9 | 13.7012 | 0.88302 | 139.36 | 0.87452 | 286.038 | 0.548817 | 442.687 | 336.355 | 0.389845 | 335.244 | 232.634 | 0.50853 | 44.596 | 55.978 | 81.7817 | 487.4647 | 35696.54 |
| 53364.9 | 15.4943 | 0.904581 | 121.271 | 1.66831 | 248.224 | 0.37291 | 450.235 | 191.496 | 0.505153 | 424.368 | 391.292 | 0.925496 | 134.053 | 342.103 | 190.758 | 261.6744 | 21616.94 |
| 25695.7 | 21.1038 | 0.956996 | 150.96 | 1.70758 | 532.093 | 0.529025 | 347.71 | 497.392 | 0.561396 | 279.828 | 413.113 | 0.77792 | 16.074 | 108.996 | 252.009 | 240.9791 | 22774.96 |
| 26573.4 | 17.5221 | 0.95533 | 164.55 | 2.41544 | 719.949 | 0.472862 | 363.219 | 763.839 | 0.786426 | 353.433 | 665.555 | 0.835078 | 168.295 | 276.353 | 136.39 | 260.0557 | 24118.22 |
| 26531.5 | 23.6853 | 0.955415 | 122.284 | 0.891595 | 489.697 | 0.210489 | 229.029 | 454.194 | 0.917521 | 298.493 | 209.226 | 0.624757 | 11.6917 | 84.3594 | 87.8476 | 427.0135 | 50075.28 |
| 67701.4 | 15.648 | 0.877425 | 114.326 | 0.892767 | 587.739 | 0.384159 | 335.912 | 321.134 | 0.785739 | 218.803 | 713.231 | 0.790396 | 19.39 | 82.8893 | 65.0438 | 307.8801 | 28155.63 |
| 48316.1 | 16.4394 | 0.914145 | 160.897 | 2.28516 | 617.379 | 0.495362 | 168.921 | 380.4 | 0.552885 | 515.419 | 603.046 | 0.488005 | 115.374 | 99.1785 | 423.163 | 459.9809 | 43551.26 |
| 37947.8 | 24.7878 | 0.933791 | 110.395 | 3.3497 | 766.267 | 0.361814 | 296.182 | 574.933 | 0.804531 | 508.756 | 470.842 | 0.714565 | 144.32 | 276.106 | 446.376 | 314.5243 | 35505.21 |
| 42559.5 | 14.8012 | 0.925048 | 90.9478 | 1.75742 | 468.777 | 0.426844 | 278.184 | 150.444 | 0.990976 | 159.022 | 946.766 | 0.251712 | 116.059 | 48.9734 | 92.9142 | 470.6114 | 45587.13 |
| 31983.9 | 26.6271 | 0.94509 | 56.0273 | 1.24001 | 659.37 | 0.317533 | 264.415 | 990.87 | 0.923529 | 387.765 | 829.802 | 0.841228 | 9.35828 | 132.59 | 150.118 | 333.6814 | 32627.63 |
| 39431.1 | 13.582 | 0.930973 | 170.071 | 2.33652 | 18.5388 | 0.656974 | 378.804 | 622.554 | 0.943425 | 420.76 | 410.86 | 0.922728 | 160.943 | 350.004 | 175.824 | 153.1234 | 8712.433 |
| 27986.1 | 21.7595 | 0.952658 | 24.1089 | 2.06826 | 924.63 | 0.499523 | 328.37 | 62.2173 | 0.837223 | 244.357 | 810.649 | 0.5195 | 113.617 | 123.663 | 217.799 | 253.2707 | 27575.11 |
| 32074.3 | 25.8838 | 0.944918 | 91.5125 | 0.52298 | 799.469 | 0.228908 | 456.689 | 929.856 | 0.787371 | 266.117 | 963.21 | 0.833117 | 29.5139 | 110.775 | 176.953 | 512.6135 | 60290.24 |
| 53131.1 | 19.3158 | 0.905026 | 33.8059 | 3.50429 | 625.362 | 0.316301 | 255.358 | 371.23 | 0.99741 | 167.938 | 963.997 | 0.582694 | 139.817 | 237.83 | 68.3226 | 382.4856 | 38476.56 |
| 71462.1 | 13.5141 | 0.8703 | 97.866 | 1.54638 | 112.154 | 0.207096 | 381.712 | 243.461 | 0.518585 | 371.408 | 463.27 | 0.792337 | 88.925 | 368.842 | 237.034 | 500.8231 | 34844.97 |
| 53525.4 | 14.9082 | 0.904276 | 60.6574 | 1.35698 | 441.902 | 0.403926 | 195.622 | 2.78313 | 0.624959 | 309.082 | 271.693 | 0.422602 | 69.7714 | 87.2849 | 268.74 | 392.5625 | 41036.32 |
| 76117.6 | 16.7513 | 0.861483 | 150.314 | 1.21181 | 146.013 | 0.486279 | 455.415 | 275.482 | 0.748017 | 148.934 | 549.442 | 0.492979 | 16.7226 | 419.065 | 91.1723 | 351.3591 | 21793.22 |
| 69844.9 | 17.5878 | 0.873366 | 146.547 | 1.26397 | 358.029 | 0.605692 | 277.32 | 922.506 | 0.964305 | 345.647 | 176.219 | 0.351218 | 60.6745 | 234.287 | 326.774 | 453.0709 | 28569.52 |
| 38436.1 | 24.1047 | 0.932866 | 148.17 | 0.904122 | 559.271 | 0.537381 | 424.708 | 102.673 | 0.431421 | 192.399 | 123.364 | 0.67005 | 27.3596 | 111.915 | 77.7005 | 301.1697 | 30907.65 |
| 32360.3 | 25.2049 | 0.944376 | 153.837 | 0.407585 | 731.801 | 0.512575 | 110.998 | 340.665 | 0.982093 | 268.074 | 291.041 | 0.476777 | 13.8574 | 89.7643 | 48.4161 | 285.8065 | 28157.17 |
| 36224.7 | 14.4805 | 0.937047 | 93.5382 | 2.95141 | 765.301 | 0.437635 | 227.113 | 599.57 | 0.778218 | 349.969 | 382.118 | 0.469197 | 106.633 | 106.604 | 225.811 | 391.3892 | 42107.95 |
| 69211.7 | 14.0865 | 0.874563 | 124.999 | 0.818388 | 477.034 | 0.434669 | 437.238 | 375.973 | 0.940032 | 302.148 | 908.791 | 0.642534 | 21.8502 | 165.93 | 151.428 | 311.5353 | 24472.43 |
| 41337.7 | 14.2345 | 0.927362 | 50.8006 | 2.44719 | 533.016 | 0.313911 | 216.268 | 398.127 | 0.750642 | 406.136 | 728.182 | 0.689437 | 115.738 | 135.819 | 92.8548 | 352.7402 | 37007.43 |
| 46849.3 | 15.9957 | 0.916923 | 32.1676 | 2.48436 | 335.255 | 0.356639 | 295.521 | 363.365 | 0.566421 | 170.816 | 439.168 | 0.605701 | 83.4003 | 110.028 | 165.519 | 374.2021 | 34722 |
| 42696.3 | 16.7442 | 0.92479 | 51.6186 | 2.43586 | 371.709 | 0.260217 | 353.335 | 776.636 | 0.610567 | 191.393 | 572.764 | 0.657525 | 70.0377 | 292 | 75.2887 | 494.0535 | 48038.2 |
| 41972 | 23.7701 | 0.926168 | 73.5443 | 1.47415 | 427.004 | 0.350425 | 192.076 | 435.033 | 0.648018 | 118.792 | 607.007 | 0.93428 | 55.0633 | 165.35 | 115.92 | 260.2562 | 24805.03 |
| 36535.1 | 21.425 | 0.936464 | 149.252 | 0.174764 | 860.907 | 0.303482 | 54.5356 | 631.793 | 0.784559 | 331.107 | 602.778 | 0.9944 | 15.2868 | 42.0998 | 246.715 | 409.866 | 45005.42 |
| 34221.3 | 13.3641 | 0.940841 | 87.143 | 1.00542 | 825.96 | 0.483378 | 453.727 | 948.996 | 0.955635 | 254.274 | 819.935 | 0.780291 | 62.0453 | 339.088 | 223.547 | 270.7633 | 23227.39 |
| 31525.4 | 17.878 | 0.945951 | 29.214 | 3.6147 | 834.466 | 0.368791 | 195.129 | 57.8526 | 0.578156 | 413.499 | 315.214 | 0.975973 | 65.9619 | 99.8309 | 133.96 | 245.243 | 33813.86 |
| 53193 | 17.8862 | 0.904908 | 111.514 | 0.174185 | 249.461 | 0.549203 | 235.14 | 804.799 | 0.619804 | 405.487 | 236.215 | 0.379657 | 1.70505 | 61.4426 | 172.825 | 514.7648 | 35141.95 |
| 39377.4 | 13.3598 | 0.931075 | 49.4042 | 1.00317 | 646.526 | 0.522619 | 353.137 | 684.623 | 0.604384 | 490.204 | 460.025 | 0.547604 | 54.3659 | 245.016 | 458.999 | 423.0856 | 36873.89 |
| 59673.9 | 17.0097 | 0.892631 | 25.267 | 0.139743 | 28.832 | 0.429349 | 131.384 | 739.8 | 0.301467 | 288.276 | 420.922 | 0.797207 | 10.5571 | 75.3472 | 227.362 | 405.3486 | 23619.47 |
| 58015.9 | 15.2581 | 0.895771 | 166.355 | 2.37774 | 63.3147 | 0.625567 | 315.356 | 851.661 | 0.869297 | 116.317 | 290.466 | 0.422535 | 181.773 | 75.1769 | 103.223 | 378.2714 | 20984.62 |
| 61919.3 | 19.1559 | 0.888379 | 23.9404 | 0.545967 | 191.581 | 0.154687 | 414.596 | 564.797 | 0.446623 | 296.441 | 91.306 | 0.940238 | 1.05352 | 270.607 | 52.081 | 640.1095 | 54454.32 |
| 49632.7 | 20.9313 | 0.911654 | 172.982 | 1.94557 | 943.871 | 0.497022 | 460.629 | 404.279 | 0.955166 | 82.1673 | 173.659 | 0.86918 | 25.079 | 277.509 | 71.8654 | 189.4195 | 19506.76 |
| 64144 | 13.8419 | 0.884162 | 161.322 | 2.26836 | 243.582 | 0.585948 | 330.236 | 771.789 | 0.48193 | 261.326 | 465.756 | 0.514508 | 65.733 | 227.875 | 106.684 | 450.7977 | 29312.75 |
| 66016.8 | 18.4022 | 0.880617 | 20.5686 | 0.212265 | 937.446 | 0.344032 | 222.655 | 211.802 | 0.401224 | 126.52 | 44.1361 | 0.982849 | 13.4484 | 104.839 | 87.9011 | 454.0133 | 59581.3 |
| 45947.5 | 23.5583 | 0.918637 | 48.1519 | 1.11965 | 280.968 | 0.384006 | 316.795 | 81.5378 | 0.331095 | 193.899 | 374.6 | 0.615564 | 93.2588 | 249.231 | 90.4026 | 476.4828 | 44572.6 |
| 38329.2 | 13.5011 | 0.93306 | 45.5649 | 0.629296 | 372.658 | 0.461888 | 197.134 | 215.408 | 0.98365 | 292.563 | 751.126 | 0.856781 | 27.5255 | 83.1538 | 288.543 | 160.1757 | 12926.46 |
| 42110.4 | 16.9543 | 0.9259 | 134.547 | 2.16751 | 222.347 | 0.351218 | 95.7001 | 939.373 | 0.413027 | 425.261 | 260.275 | 0.596159 | 155.452 | 72.6753 | 299.135 | 546.8225 | 44103.63 |
| 64086.6 | 18.8198 | 0.884274 | 32.7771 | 2.09894 | 908.872 | 0.377154 | 355.313 | 661.431 | 0.733018 | 180.757 | 174.9 | 0.511731 | 168.966 | 49.4341 | 75.4559 | 509.9609 | 57474.05 |
| 26230.1 | 16.3226 | 0.95598 | 140.55 | 0.264915 | 481.073 | 0.519309 | 463.748 | 356.327 | 0.269378 | 73.0023 | 990.048 | 0.784236 | 11.4366 | 105.54 | 72.6518 | 481.3234 | 45543.83 |
| 47561.5 | 20.2371 | 0.915577 | 102.468 | 1.90976 | 369.703 | 0.467797 | 184.254 | 795.204 | 0.634465 | 125.998 | 713.305 | 0.429524 | 5.54561 | 165.291 | 111.959 | 482.0715 | 38357.89 |
| 26264.8 | 25.7569 | 0.955922 | 39.1933 | 1.32408 | 412.378 | 0.51509 | 292.396 | 744.298 | 0.787019 | 464.474 | 367.89 | 0.353318 | 101.874 | 126.546 | 152.49 | 479.5765 | 37202.7 |
| 28519.1 | 16.9413 | 0.951644 | 150.849 | 2.72776 | 687.102 | 0.250503 | 259.098 | 95.8414 | 0.741887 | 328.69 | 751.077 | 0.663402 | 87.3536 | 141.413 | 79.4761 | 455.5362 | 58536.53 |
| 43506.9 | 15.6649 | 0.923254 | 61.7273 | 1.64585 | 339.906 | 0.363096 | 276.034 | 683.548 | 0.942282 | 413.622 | 137.524 | 0.869416 | 6.84485 | 157.079 | 134.053 | 190.9797 | 16448.83 |
| 30795.1 | 22.2721 | 0.947338 | 93.4716 | 0.758864 | 747.103 | 0.521241 | 279.269 | 354.208 | 0.375729 | 177.426 | 436.236 | 0.816241 | 50.9086 | 257.99 | 62.5271 | 301.413 | 32631.25 |
| 71898.6 | 16.2634 | 0.869475 | 75.4156 | 0.383297 | 372.643 | 0.5028 | 320.379 | 221.892 | 0.607548 | 481.073 | 527.879 | 0.572834 | 35.6541 | 260.365 | 365.614 | 319.0175 | 24992.73 |
| 27421.7 | 20.4098 | 0.953726 | 43.1486 | 3.28998 | 533.793 | 0.274749 | 355.594 | 577.944 | 0.730269 | 468.195 | 517.452 | 0.979462 | 31.6545 | 185.024 | 287.365 | 281.6234 | 31678.04 |
| 47831.8 | 22.4597 | 0.915067 | 147.339 | 2.29435 | 369.503 | 0.563716 | 395.559 | 403.899 | 0.340367 | 437.097 | 47.9567 | 0.742055 | 53.7176 | 101.332 | 237.559 | 315.0263 | 26201.15 |
| 55521.8 | 15.3119 | 0.900495 | 33.203 | 0.472427 | 405.928 | 0.479143 | 365.383 | 585.172 | 0.627694 | 488.008 | 178.427 | 0.860023 | 33.3785 | 363.715 | 282.068 | 208.3883 | 17450.26 |
| 38251.9 | 21.6946 | 0.933212 | 110.057 | 0.432563 | 649.595 | 0.515107 | 164.118 | 642.417 | 0.985063 | 214.674 | 570.255 | 0.584113 | 5.62507 | 123.776 | 199.64 | 279.9543 | 23845.18 |
| 36754.4 | 25.7343 | 0.936053 | 62.9842 | 2.327 | 733.392 | 0.517747 | 185.205 | 436.603 | 0.76834 | 507.125 | 340.055 | 0.521266 | 231.371 | 81.9529 | 467.18 | 294.2127 | 27213.83 |
| 60667.2 | 15.4839 | 0.890749 | 115.037 | 1.78259 | 100.789 | 0.481096 | 366.253 | 558.128 | 0.55741 | 341.008 | 479.679 | 0.27305 | 5.75164 | 83.8625 | 319.978 | 673.3764 | 42196.15 |
| 51927 | 20.2619 | 0.907308 | 92.7937 | 0.901556 | 926.494 | 0.393046 | 393.343 | 749.164 | 0.834706 | 380.835 | 908.933 | 0.439301 | 49.2606 | 236.93 | 212.224 | 579.6913 | 61321.78 |
| 44939.2 | 16.4342 | 0.920541 | 140.331 | 0.527048 | 1.65661 | 0.325996 | 499.671 | 205.118 | 0.90801 | 308.382 | 618.503 | 0.582887 | 33.8787 | 152.993 | 253.04 | 278.8683 | 16357.76 |
| 42217.9 | 17.2559 | 0.925696 | 131.372 | 1.40276 | 69.0647 | 0.509566 | 379.83 | 912.749 | 0.286412 | 288.057 | 685.236 | 0.820752 | 61.5687 | 235.092 | 230.305 | 398.9574 | 25172.82 |
| 31302.6 | 22.0164 | 0.946376 | 166.703 | 1.49495 | 227.169 | 0.365694 | 82.9008 | 532.383 | 0.637942 | 396.588 | 805.7 | 0.408343 | 104.002 | 53.9099 | 257.842 | 554.7727 | 44546.74 |
| 37088.2 | 21.0728 | 0.935416 | 103.71 | 1.01822 | 575.517 | 0.413002 | 195.194 | 214.777 | 0.301538 | 99.3838 | 79.9002 | 0.727267 | 32.0005 | 142.429 | 79.7867 | 480.7536 | 57133.77 |
| 36724.8 | 13.6786 | 0.936099 | 28.3545 | 1.23621 | 859.387 | 0.403012 | 187.735 | 816.56 | 0.698745 | 457.548 | 581.268 | 0.527808 | 6.41427 | 140.071 | 87.6287 | 478.2395 | 53291.51 |
| 49204.4 | 21.2259 | 0.912466 | 124.544 | 1.60222 | 396.709 | 0.425997 | 483.196 | 835.204 | 0.530027 | 188.58 | 794.22 | 0.849576 | 46.3095 | 160.931 | 160.95 | 350.4159 | 28481.16 |
| 31600 | 19.5943 | 0.945811 | 159.689 | 3.60796 | 167.411 | 0.328246 | 389.071 | 738.273 | 0.37804 | 399.865 | 382.824 | 0.94961 | 79.1198 | 54.5146 | 123.707 | 357.432 | 28919.17 |
| 39720.4 | 18.9612 | 0.930429 | 42.1445 | 0.764441 | 318.959 | 0.274046 | 87.1276 | 804.217 | 0.703359 | 374.456 | 211.2 | 0.504345 | 68.6848 | 47.6883 | 229.236 | 502.2014 | 46916.67 |
| 55603.7 | 19.7055 | 0.900343 | 170.279 | 0.410737 | 404.778 | 0.376004 | 462.473 | 707.614 | 0.569421 | 221.726 | 671.651 | 0.731192 | 14.7866 | 380.521 | 111.237 | 491.3758 | 39382.07 |
| 54316.6 | 17.9138 | 0.90278 | 104.28 | 2.01338 | 166.247 | 0.498755 | 218.986 | 272.332 | 0.556394 | 152.9 | 880.319 | 0.78082 | 54.4826 | 84.6871 | 86.4352 | 243.0011 | 15861.4 |
| 26362.2 | 19.5299 | 0.955732 | 27.1016 | 1.89812 | 378.364 | 0.479333 | 407.048 | 760.231 | 0.404016 | 283.752 | 702.424 | 0.63676 | 70.3291 | 173.657 | 269.026 | 379.4628 | 33098.08 |
| 32528.8 | 18.0032 | 0.94405 | 171.489 | 0.107349 | 23.2815 | 0.440612 | 477.018 | 339.351 | 0.225485 | 412.581 | 662.357 | 0.952034 | 8.05893 | 186.311 | 362.384 | 519.2482 | 33711.53 |
| 29866.3 | 22.9578 | 0.949097 | 121.77 | 2.46194 | 381.389 | 0.542925 | 203.024 | 884.694 | 0.553452 | 492.706 | 472.841 | 0.600622 | 165.259 | 145.073 | 426.825 | 379.7176 | 28231.83 |
| 28183.3 | 13.0396 | 0.952278 | 40.1433 | 2.68784 | 309.433 | 0.325384 | 394.5 | 507.789 | 0.638043 | 166.111 | 330.98 | 0.498943 | 29.4339 | 263.401 | 71.963 | 399.7925 | 39405.87 |
| 26121.2 | 24.1787 | 0.956193 | 113.216 | 1.76337 | 812.72 | 0.234235 | 352.961 | 603.379 | 0.786593 | 132.315 | 552.703 | 0.72206 | 103.566 | 110.694 | 97.2172 | 479.9035 | 63245.77 |
| 56182.4 | 21.2558 | 0.899248 | 156.338 | 2.07946 | 23.633 | 0.484852 | 274.524 | 543.48 | 0.983911 | 329.883 | 379.479 | 0.407752 | 25.9195 | 40.982 | 112.562 | 332.7138 | 18741.24 |
| 45156.6 | 22.0261 | 0.920134 | 101.99 | 1.9399 | 93.7414 | 0.265949 | 452.007 | 931.134 | 0.876906 | 241.648 | 54.6996 | 0.546969 | 90.1835 | 117.68 | 235.856 | 376.3453 | 25438.17 |
| 66269.1 | 15.6506 | 0.880138 | 38.0293 | 1.32505 | 419.935 | 0.485493 | 216.122 | 218.056 | 0.670661 | 105.575 | 756.146 | 0.291054 | 6.50299 | 120.984 | 80.4639 | 550.5269 | 46370.97 |
| 33948.4 | 20.4649 | 0.941363 | 149.913 | 0.237831 | 63.1329 | 0.502996 | 140.505 | 906.754 | 0.502034 | 264.754 | 462.756 | 0.595167 | 11.5128 | 46.2434 | 91.7286 | 400.3568 | 25222.52 |
| 51789.6 | 17.6292 | 0.907566 | 85.1615 | 1.78267 | 494.425 | 0.441086 | 488.594 | 481.904 | 0.743996 | 222.036 | 969.174 | 0.444547 | 139.222 | 144.334 | 49.7132 | 433.2999 | 37746.37 |
| 26024.4 | 19.5259 | 0.956372 | 147.181 | 1.27811 | 1.82697 | 0.556592 | 445.689 | 352.403 | 0.177196 | 224.546 | 279.866 | 0.670063 | 30.6448 | 189.425 | 121.449 | 467.7811 | 30858.84 |
| 28141.9 | 27.5438 | 0.952369 | 92.6841 | 1.16651 | 790.477 | 0.450714 | 493.298 | 97.1827 | 0.318757 | 302.433 | 598.243 | 0.873347 | 19.857 | 406.331 | 209.754 | 383.4021 | 49275.89 |
| 28352.4 | 25.1264 | 0.951967 | 145.602 | 0.482459 | 519.874 | 0.46868 | 308.198 | 584.174 | 0.214924 | 420.051 | 364.12 | 0.866501 | 44.206 | 120.291 | 345.326 | 565.8617 | 58833.29 |
| 81778 | 13.6459 | 0.85076 | 143.316 | 0.445406 | 343.519 | 0.300408 | 54.7971 | 340.255 | 0.996886 | 345.219 | 389.711 | 0.362654 | 9.39258 | 43.4897 | 85.4579 | 667.3817 | 51534.2 |
| 36586.2 | 25.5853 | 0.936371 | 139.541 | 1.32057 | 481.988 | 0.471947 | 156.875 | 355.042 | 0.418353 | 354.36 | 931.854 | 0.602809 | 15.5183 | 112.796 | 247.82 | 458.6866 | 43162.61 |
| 36884.5 | 22.6807 | 0.935803 | 96.0354 | 2.07925 | 467.553 | 0.360029 | 340.681 | 26.1436 | 0.440312 | 469.989 | 924.056 | 0.89548 | 67.2908 | 149.502 | 467.353 | 331.8052 | 35419.86 |
| 44823.6 | 17.8378 | 0.920761 | 143.558 | 0.85357 | 239.702 | 0.327802 | 282.674 | 541.594 | 0.602233 | 416.063 | 283.608 | 0.660542 | 12.0224 | 50.2765 | 341.857 | 399.659 | 32498.82 |
| 39092 | 16.8253 | 0.931617 | 123.682 | 2.36028 | 967.382 | 0.523254 | 201.278 | 397.002 | 0.698706 | 378.739 | 966.218 | 0.303181 | 139.658 | 143.649 | 310.144 | 570.899 | 56495.94 |
| 77421.1 | 15.3181 | 0.859014 | 154.86 | 3.53428 | 232.769 | 0.360557 | 365.006 | 439.913 | 0.396418 | 177.331 | 451.965 | 0.771112 | 166.151 | 297.666 | 132.085 | 499.9727 | 36536.26 |
| 32266.5 | 24.3688 | 0.944552 | 97.4749 | 2.86111 | 175.228 | 0.469386 | 294.761 | 141.531 | 0.724462 | 387.161 | 534.315 | 0.166099 | 48.5088 | 101.09 | 173.271 | 585.3099 | 47789.83 |
| 30691.9 | 21.1318 | 0.947532 | 154.43 | 0.325859 | 25.1324 | 0.687649 | 424.609 | 177.374 | 0.887843 | 378.868 | 927.719 | 0.121333 | 19.5429 | 287.645 | 289.993 | 644.698 | 40368.76 |
| 56305.9 | 15.6078 | 0.89901 | 130.049 | 2.06348 | 299.737 | 0.49534 | 456.934 | 345.153 | 0.633061 | 395.668 | 787.857 | 0.630007 | 43.8214 | 121.636 | 197.882 | 299.6592 | 22289.17 |
| 31055.5 | 22.7069 | 0.946845 | 106.646 | 1.1128 | 436.657 | 0.367217 | 141.231 | 427.873 | 0.815624 | 399.683 | 719.314 | 0.837178 | 81.8861 | 74.2458 | 345.618 | 239.2653 | 22259.17 |
| 28868.3 | 14.9699 | 0.950982 | 166.373 | 1.59525 | 602.661 | 0.349741 | 427.914 | 246.953 | 0.476983 | 292.472 | 345.385 | 0.885093 | 123.223 | 327.834 | 129.704 | 359.5702 | 41782.24 |
| 60983.4 | 13.7179 | 0.890149 | 27.4743 | 0.333335 | 89.1235 | 0.386143 | 194.985 | 527.831 | 0.912408 | 242.526 | 966.742 | 0.541649 | 11.5406 | 182.567 | 151.045 | 324.0388 | 19665.19 |
| 68996.5 | 15.591 | 0.874972 | 32.0846 | 1.45752 | 386.618 | 0.443723 | 273.708 | 93.9627 | 0.848287 | 229.489 | 61.8047 | 0.418235 | 37.3608 | 234.614 | 86.7575 | 287.0365 | 26022.84 |
| 41259.8 | 16.8763 | 0.927511 | 126.707 | 1.0463 | 624.562 | 0.453841 | 201.591 | 444.346 | 0.862221 | 445.833 | 555.143 | 0.484235 | 5.7534 | 109.075 | 204.195 | 350.2693 | 33672.89 |
| 30649.9 | 14.7311 | 0.947607 | 170.141 | 1.73116 | 966.012 | 0.574257 | 489.594 | 734.828 | 0.503558 | 288.079 | 641.343 | 0.417135 | 171.723 | 89.7419 | 81.7621 | 586.0465 | 59275.92 |
| 31084.6 | 13.2232 | 0.946783 | 128.114 | 2.16904 | 331.35 | 0.340278 | 168.67 | 2.29774 | 0.970863 | 493.823 | 234.271 | 0.666599 | 138.507 | 106.777 | 141.073 | 169.7717 | 18069.45 |
| 37081.3 | 18.3494 | 0.935427 | 140.709 | 0.625527 | 889.989 | 0.58103 | 345.279 | 928.507 | 0.52342 | 154.833 | 776.04 | 0.381 | 30.4417 | 332.349 | 126.419 | 662.8084 | 61943.38 |
| 27371 | 22.4727 | 0.953824 | 75.8452 | 1.90471 | 958.141 | 0.49938 | 304.776 | 172.236 | 0.822126 | 384.796 | 134.512 | 0.622224 | 27.7541 | 85.0908 | 357.185 | 186.2349 | 23010.19 |
| 29164 | 26.8522 | 0.950432 | 42.072 | 1.81216 | 684.259 | 0.422662 | 422.189 | 205.52 | 0.481879 | 324.692 | 967.3 | 0.658717 | 105.071 | 90.8873 | 319.612 | 388.3777 | 44812.23 |
| 26760.5 | 22.7953 | 0.95498 | 121.848 | 3.37582 | 758.611 | 0.432367 | 207.197 | 699.216 | 0.566303 | 161.504 | 804.498 | 0.765672 | 22.113 | 69.7297 | 80.1657 | 349.904 | 37568.17 |
| 53857.2 | 13.159 | 0.903647 | 133.149 | 0.602647 | 609.489 | 0.348007 | 314.661 | 20.8914 | 0.827339 | 422.968 | 800.343 | 0.85078 | 48.4842 | 101.849 | 359.432 | 279.89 | 27940.21 |
| 59183.6 | 14.3801 | 0.893558 | 52.1392 | 1.90167 | 247.596 | 0.296712 | 281.88 | 937.376 | 0.465267 | 469.343 | 966.271 | 0.903062 | 25.6022 | 105.239 | 165.942 | 458.4464 | 35623.83 |
| 64718.3 | 13.1897 | 0.883074 | 113.222 | 1.08239 | 195.499 | 0.530054 | 435.675 | 215.287 | 0.794194 | 309.887 | 33.0916 | 0.397326 | 15.4002 | 108.204 | 224.858 | 276.5997 | 19292.8 |
| 50400.2 | 19.4977 | 0.910199 | 169.276 | 0.530619 | 156.566 | 0.593066 | 209.111 | 51.9026 | 0.740457 | 448.105 | 830.026 | 0.969739 | 45.4127 | 193.281 | 124.516 | 174.1571 | 10997.21 |
| 51540.1 | 14.6876 | 0.908037 | 95.0906 | 0.911312 | 375.569 | 0.357782 | 294.89 | 717.888 | 0.913962 | 108.913 | 242.519 | 0.628563 | 88.9684 | 86.841 | 89.3133 | 306.1238 | 25856.01 |
| 61902.7 | 14.1189 | 0.888408 | 62.9147 | 1.90807 | 477.333 | 0.470703 | 129.514 | 90.4566 | 0.890562 | 226.698 | 54.7231 | 0.397896 | 154.556 | 92.3618 | 178.594 | 264.9905 | 25431.3 |
| 27453.4 | 20.9564 | 0.953666 | 136.158 | 0.144699 | 376.494 | 0.201769 | 271.168 | 427.378 | 0.86185 | 197.572 | 634.112 | 0.650771 | 3.17532 | 242.335 | 193.954 | 509.5412 | 51400.63 |
| 40688.9 | 13.097 | 0.92859 | 122.207 | 1.60639 | 448.444 | 0.351954 | 422.037 | 370.093 | 0.979549 | 350.827 | 671.142 | 0.460103 | 90.0558 | 157.834 | 245.409 | 370.6325 | 34996.45 |
| 40837.7 | 23.1164 | 0.928316 | 109.962 | 0.116071 | 133.415 | 0.518514 | 239.547 | 350.91 | 0.297129 | 516.631 | 639.719 | 0.623636 | 2.37647 | 158.498 | 122.846 | 478.5395 | 33565.67 |
| 26632.4 | 18.9481 | 0.95522 | 20.4947 | 2.00885 | 257.746 | 0.357075 | 327.581 | 367.021 | 0.262073 | 130.244 | 56.1177 | 0.723886 | 166.649 | 249.454 | 96.2399 | 461.6767 | 47477.36 |
| 61342.4 | 16.7108 | 0.889471 | 79.934 | 1.6128 | 313.876 | 0.346786 | 307.535 | 962.765 | 0.636054 | 373.718 | 198.195 | 0.473071 | 58.3261 | 296.628 | 312.938 | 550.9899 | 44823.44 |
| 26406.8 | 21.259 | 0.955649 | 128.892 | 0.136568 | 998.354 | 0.443875 | 252.421 | 952.625 | 0.366772 | 147.424 | 466.305 | 0.870082 | 12.3058 | 205.232 | 90.7708 | 507.1323 | 59714.37 |
| 38282.8 | 23.9059 | 0.933156 | 169.908 | 1.73299 | 821.781 | 0.474977 | 350.511 | 406.157 | 0.781236 | 278.677 | 98.2863 | 0.87745 | 58.93 | 68.8273 | 253.524 | 201.8429 | 21909.92 |
| 73313 | 13.5688 | 0.866794 | 136.517 | 0.193221 | 170.316 | 0.42029 | 393.323 | 777.485 | 0.34708 | 185.671 | 333.14 | 0.812189 | 18.8714 | 376.103 | 134.19 | 544.4532 | 35306.48 |
| 59213.6 | 20.1288 | 0.893505 | 55.5375 | 3.46993 | 979.69 | 0.443165 | 193.026 | 231.862 | 0.505412 | 306.29 | 42.8987 | 0.736199 | 39.6376 | 182.368 | 172.393 | 352.3856 | 44583.08 |
| 43695.6 | 24.0988 | 0.922903 | 69.364 | 2.06011 | 836.223 | 0.479129 | 332.077 | 588.395 | 0.611075 | 396.501 | 40.5809 | 0.528547 | 4.47305 | 79.3056 | 54.7539 | 379.2901 | 42502.64 |
| 54973.4 | 19.0835 | 0.901536 | 39.9778 | 2.73965 | 307.956 | 0.282415 | 459.705 | 915.881 | 0.465737 | 318.458 | 570.688 | 0.667449 | 144.659 | 239.434 | 87.9522 | 590.3716 | 51569.49 |
| 34925.6 | 24.2224 | 0.939515 | 86.9928 | 0.654593 | 27.3466 | 0.365228 | 474.141 | 849.134 | 0.611301 | 491.699 | 901.435 | 0.894058 | 4.27014 | 50.2332 | 264.105 | 274.9037 | 16447.97 |
| 86552.1 | 14.1092 | 0.841717 | 132.496 | 0.405861 | 553.166 | 0.574193 | 425.201 | 104.756 | 0.777568 | 426.424 | 508.225 | 0.215726 | 7.62854 | 336.762 | 326.87 | 698.3201 | 54862.14 |
| 27328.8 | 26.8043 | 0.953908 | 66.2243 | 0.265377 | 776.257 | 0.38932 | 362.165 | 58.4761 | 0.70514 | 445.84 | 353.534 | 0.543037 | 17.6181 | 135.958 | 149.67 | 329.0731 | 44190.06 |
| 52597.7 | 18.2214 | 0.906036 | 168.422 | 2.15044 | 119.353 | 0.52835 | 161.646 | 253.356 | 0.616618 | 442.801 | 214.969 | 0.980535 | 156.836 | 87.9563 | 409.124 | 157.6078 | 10416.21 |
| 41833.3 | 23.3005 | 0.92643 | 59.5252 | 0.576069 | 857.946 | 0.398204 | 207.612 | 557.88 | 0.788934 | 320.134 | 282.312 | 0.640216 | 34.3589 | 158.88 | 94.1204 | 327.7307 | 38070.04 |
| 66935 | 13.865 | 0.878876 | 162.418 | 1.87474 | 610.173 | 0.618332 | 396.665 | 624.991 | 0.432611 | 453.518 | 871.09 | 0.527233 | 86.3851 | 277.858 | 440.857 | 506.7495 | 37155.72 |
| 33647.6 | 18.3953 | 0.941931 | 158.887 | 0.515986 | 731.979 | 0.410952 | 205.988 | 135.194 | 0.676342 | 488.95 | 79.5766 | 0.927314 | 1.2928 | 45.3862 | 51.2889 | 219.3455 | 26056.25 |
| 39512.7 | 21.0301 | 0.930823 | 139.566 | 0.589032 | 462.669 | 0.636726 | 352.794 | 228.28 | 0.817204 | 176.316 | 544.529 | 0.329067 | 24.9701 | 128.179 | 143.623 | 328.0443 | 25149.21 |
| 49499.3 | 18.3071 | 0.911905 | 48.0321 | 1.53631 | 636.059 | 0.539286 | 248.753 | 149.418 | 0.880512 | 276.145 | 907.678 | 0.315643 | 151.282 | 190.719 | 270.896 | 507.3094 | 43760.26 |
| 56366 | 21.1719 | 0.8989 | 169.131 | 2.46039 | 907.174 | 0.46229 | 482.315 | 336.209 | 0.842367 | 494.48 | 221.383 | 0.67646 | 65.8686 | 345.511 | 214.165 | 277.7233 | 29524.54 |
| 32104 | 22.1455 | 0.944858 | 170.809 | 3.16467 | 109.086 | 0.280973 | 477.699 | 490.385 | 0.635804 | 515.156 | 613.736 | 0.874188 | 56.5493 | 249.519 | 456.507 | 293.9315 | 21584.69 |
| 38413.4 | 17.4471 | 0.932903 | 58.791 | 0.703297 | 136.841 | 0.390718 | 241.23 | 201.238 | 0.998191 | 182.461 | 13.6124 | 0.279029 | 50.2482 | 222.413 | 136.015 | 319.6133 | 25091.71 |
| 28685.2 | 13.949 | 0.951328 | 153.607 | 1.38095 | 959.21 | 0.46138 | 377.922 | 663.364 | 0.920996 | 250.46 | 326.312 | 0.54427 | 95.7222 | 105.136 | 184.017 | 341.0003 | 36562.83 |
| 36659.2 | 21.0488 | 0.936229 | 36.6158 | 0.944291 | 213.267 | 0.393444 | 281.793 | 188.404 | 0.819586 | 456.019 | 705.376 | 0.640643 | 9.17939 | 70.9439 | 55.2376 | 221.0185 | 17729.92 |
| 50681.6 | 21.4274 | 0.909668 | 138.58 | 3.44752 | 303.572 | 0.447281 | 175.303 | 589.697 | 0.546479 | 408.527 | 130.902 | 0.301522 | 42.0963 | 153.51 | 166.198 | 671.4847 | 55069.48 |
| 84737.5 | 13.5913 | 0.845154 | 151.534 | 1.78513 | 694.794 | 0.210477 | 328.752 | 32.7252 | 0.870389 | 234.937 | 660.836 | 0.988161 | 6.74147 | 297.395 | 158.222 | 596.267 | 62225.27 |
| 45980.6 | 16.8427 | 0.918569 | 154.333 | 1.04101 | 4.11676 | 0.540648 | 479.801 | 200.385 | 0.35367 | 471.953 | 27.6059 | 0.761084 | 58.6718 | 170.312 | 225.154 | 263.8599 | 15971.35 |
| 29549.9 | 24.2818 | 0.949698 | 161.106 | 0.555855 | 845.141 | 0.598717 | 308.19 | 504.576 | 0.449467 | 127.08 | 607.263 | 0.746282 | 8.77477 | 81.6651 | 62.1977 | 336.7587 | 32889.88 |
| 27750.2 | 18.8618 | 0.953102 | 26.5503 | 2.57044 | 184.542 | 0.28924 | 389.061 | 328.613 | 0.490995 | 357.445 | 246.225 | 0.807181 | 137.478 | 312.433 | 81.6062 | 286.1977 | 26514.2 |
| 61085.2 | 19.7036 | 0.88996 | 127.815 | 3.47324 | 924.924 | 0.367235 | 215.792 | 835.615 | 0.820387 | 438.895 | 786.642 | 0.624152 | 5.20993 | 181.713 | 303.527 | 468.563 | 49042.06 |
| 44250.8 | 20.2235 | 0.921848 | 172.514 | 0.95483 | 805.66 | 0.472189 | 183.848 | 690.672 | 0.50002 | 154.307 | 846.191 | 0.909168 | 80.7291 | 119.905 | 101.391 | 390.275 | 36916.84 |
| 80029.6 | 13.3631 | 0.854072 | 118.591 | 1.21025 | 64.8214 | 0.426493 | 383.6 | 102.916 | 0.846853 | 437.859 | 853.089 | 0.740089 | 14.8943 | 221.318 | 176.857 | 231.2574 | 13221.36 |
| 33734.4 | 20.8822 | 0.941769 | 86.0321 | 0.312468 | 592.768 | 0.449559 | 270.539 | 269.172 | 0.871092 | 380.607 | 297.247 | 0.661657 | 10.2935 | 65.7461 | 160.91 | 210.4389 | 22087.11 |
| 37586 | 18.9992 | 0.934471 | 145.905 | 1.07353 | 803.325 | 0.442091 | 452.139 | 768.42 | 0.567071 | 480.689 | 811.071 | 0.609026 | 61.5846 | 190.021 | 196.168 | 491.4572 | 50187.58 |
| 62418.1 | 16.5201 | 0.887433 | 95.1843 | 3.75639 | 34.218 | 0.686303 | 347.568 | 603.351 | 0.956369 | 344.797 | 404.722 | 0.995619 | 131.461 | 344.046 | 238.669 | 193.325 | 10464.16 |
| 34064.3 | 20.0898 | 0.941143 | 47.459 | 1.51545 | 232.519 | 0.470319 | 273.609 | 714.727 | 0.546674 | 206.001 | 129.55 | 0.980456 | 31.9624 | 156.288 | 50.6274 | 177.6702 | 14064.69 |
| 34369 | 24.2947 | 0.94057 | 116.673 | 1.77396 | 465.991 | 0.514872 | 109.851 | 174.942 | 0.922385 | 50.8681 | 466.839 | 0.696575 | 85.0666 | 94.0362 | 49.612 | 157.4565 | 13957.39 |
| 25769.7 | 15.6087 | 0.956851 | 168.952 | 0.622262 | 476.55 | 0.536744 | 249.919 | 977.379 | 0.906156 | 218.612 | 21.8661 | 0.851182 | 22.8464 | 93.0955 | 129.428 | 193.8637 | 15489.88 |
| 46734.2 | 16.1922 | 0.917141 | 120.902 | 1.36121 | 656.596 | 0.362072 | 120.989 | 810.574 | 0.589857 | 132.748 | 659.443 | 0.809493 | 79.5765 | 73.6817 | 75.1627 | 408.3311 | 41104.03 |
| 39950.4 | 13.8187 | 0.929989 | 59.6302 | 3.67483 | 563.125 | 0.318191 | 476.472 | 14.7974 | 0.947487 | 63.1219 | 943.099 | 0.986273 | 4.75632 | 247.473 | 53.4634 | 252.5517 | 25747.57 |
| 40865.4 | 23.0763 | 0.928263 | 90.2777 | 2.61313 | 122.588 | 0.240702 | 374.558 | 269.073 | 0.614798 | 472.656 | 629.316 | 0.706463 | 124.867 | 315.785 | 224.351 | 357.4948 | 27814.04 |
| 34490.8 | 19.1857 | 0.940334 | 166.665 | 0.45139 | 213.322 | 0.381246 | 350.11 | 179.481 | 0.944755 | 70.9792 | 206.596 | 0.567117 | 25.5518 | 47.6594 | 65.105 | 246.43 | 20017.81 |
| 63368.5 | 17.671 | 0.885633 | 92.1824 | 1.43421 | 744.78 | 0.354701 | 241.911 | 262.518 | 0.412961 | 97.0074 | 893.845 | 0.987765 | 48.315 | 222.146 | 51.6497 | 453.0561 | 49983.58 |
| 49718.4 | 20.043 | 0.911491 | 106.719 | 2.16076 | 71.8894 | 0.2141 | 234.472 | 45.9689 | 0.60229 | 260.144 | 622.341 | 0.434067 | 37.1983 | 136.973 | 234.126 | 599.7853 | 42545.73 |
| 34871 | 23.1855 | 0.939618 | 138.708 | 1.39104 | 974.908 | 0.453518 | 84.9072 | 572.771 | 0.856325 | 262.447 | 675.117 | 0.789395 | 21.8896 | 70.1078 | 171.672 | 277.5292 | 28993.05 |
| 47588.4 | 20.5727 | 0.915526 | 120.932 | 1.06351 | 949.577 | 0.701594 | 364.781 | 439.457 | 0.539221 | 446.944 | 97.1944 | 0.887029 | 69.6175 | 280.623 | 441.347 | 280.596 | 24180.82 |
| 38878.5 | 13.8137 | 0.93202 | 169.286 | 0.281112 | 992.945 | 0.271717 | 300.325 | 688.384 | 0.90786 | 496.791 | 885.211 | 0.902545 | 7.04794 | 291.771 | 362.182 | 581.5289 | 64186.86 |
| 29990.3 | 22.7268 | 0.948862 | 146.817 | 0.247709 | 632.21 | 0.581371 | 390.962 | 171.907 | 0.439025 | 176.485 | 215.893 | 0.777222 | 10.5095 | 225.044 | 62.5985 | 256.2653 | 26088.48 |
| 51089.5 | 22.1056 | 0.908896 | 94.4285 | 3.23664 | 946.259 | 0.413125 | 437.456 | 363.831 | 0.895301 | 471.782 | 289.464 | 0.971784 | 96.3996 | 68.7514 | 198.512 | 199.5911 | 23094.78 |
| 36284.4 | 17.9481 | 0.936936 | 143.954 | 0.423369 | 945.774 | 0.258641 | 140.04 | 634.494 | 0.931986 | 330.615 | 43.0633 | 0.97832 | 36.2162 | 67.1809 | 70.055 | 437.9327 | 55191.38 |
| 29955.5 | 14.7051 | 0.948922 | 105.092 | 1.2691 | 187.202 | 0.509442 | 371.88 | 348.99 | 0.38031 | 254.267 | 360.723 | 0.42006 | 82.3081 | 49.3526 | 88.4252 | 426.3278 | 33757.11 |
| 26020.3 | 21.7276 | 0.956381 | 122.35 | 2.8689 | 676.161 | 0.47381 | 182.444 | 449.359 | 0.513968 | 190.314 | 101.614 | 0.507946 | 123.582 | 110.28 | 146.406 | 371.2734 | 42994.97 |
| 66287.5 | 17.1773 | 0.880104 | 27.9015 | 1.14328 | 594.298 | 0.238145 | 425.14 | 265.107 | 0.691472 | 402.829 | 431.416 | 0.657051 | 12.1952 | 47.9539 | 185.81 | 543.3235 | 61384.57 |
| 32595.6 | 20.8952 | 0.943926 | 33.4185 | 2.28778 | 860.775 | 0.52105 | 203.911 | 985.973 | 0.511424 | 425.624 | 647.269 | 0.980332 | 50.9261 | 155.6 | 308.427 | 310.7126 | 27975.08 |
| 32905.7 | 24.6537 | 0.943342 | 62.7393 | 2.96108 | 377.979 | 0.339166 | 164.148 | 430.198 | 0.549352 | 363.199 | 749.431 | 0.962382 | 78.9923 | 103.068 | 308.667 | 280.8861 | 26994.77 |
| 79717.4 | 14.5234 | 0.854664 | 153.776 | 1.80422 | 113.543 | 0.600741 | 102.726 | 439.082 | 0.412354 | 498.119 | 562.85 | 0.404135 | 109.429 | 45.9848 | 302.02 | 589.3156 | 33709.88 |
| 36545.3 | 17.1008 | 0.936441 | 158.211 | 2.34073 | 595.424 | 0.638515 | 183.772 | 422.049 | 0.751502 | 352.62 | 431.605 | 0.70652 | 165.867 | 155.895 | 339.343 | 221.459 | 16877.42 |
| 31161.6 | 17.4123 | 0.946639 | 98.9747 | 1.64716 | 114.731 | 0.343653 | 246.408 | 342.496 | 0.665891 | 422.081 | 925.362 | 0.926781 | 162.476 | 73.4225 | 250.787 | 221.8995 | 15721.79 |
| 31826.1 | 15.286 | 0.945379 | 146.454 | 1.3787 | 237.285 | 0.198601 | 371.127 | 416.374 | 0.793892 | 163.077 | 592.455 | 0.879668 | 33.005 | 151.346 | 150.498 | 382.7354 | 34426.08 |
| 32374.9 | 23.1705 | 0.944346 | 59.2125 | 1.81931 | 556.299 | 0.476145 | 119.476 | 108.93 | 0.279276 | 512.878 | 102.343 | 0.871917 | 179.151 | 87.9571 | 302.525 | 310.1948 | 35971.78 |
| 47186.8 | 16.9381 | 0.916284 | 84.5677 | 2.92012 | 254.884 | 0.189946 | 282.478 | 232.579 | 0.814179 | 366.923 | 164.218 | 0.807508 | 87.9945 | 149.803 | 128.864 | 321.0758 | 31162.65 |
| 40106.5 | 19.335 | 0.929697 | 158.012 | 0.374091 | 131.767 | 0.581236 | 189.798 | 400.246 | 0.940508 | 285.398 | 983.048 | 0.774014 | 35.5374 | 92.3671 | 227.142 | 211.1532 | 12889.66 |
| 55519.2 | 13.793 | 0.900499 | 133.152 | 1.01993 | 870.501 | 0.60952 | 356.073 | 418.069 | 0.634396 | 470.819 | 825.547 | 0.375804 | 23.5518 | 188.928 | 179.974 | 561.667 | 47261.43 |
| 55448.2 | 15.4492 | 0.900635 | 172.843 | 0.336089 | 88.8871 | 0.569655 | 162.633 | 323.23 | 0.678735 | 205.474 | 768.858 | 0.431268 | 31.6506 | 157.581 | 55.1179 | 413.545 | 24805.89 |
| 27951.1 | 22.9082 | 0.952725 | 140.935 | 1.82392 | 708.031 | 0.410435 | 257.545 | 575.935 | 0.757183 | 230.485 | 845.753 | 0.538902 | 69.2128 | 237.106 | 130.504 | 409.5055 | 42616.45 |
| 39939.7 | 15.6238 | 0.930011 | 158.086 | 0.385515 | 731.161 | 0.611114 | 388.997 | 732.439 | 0.83635 | 358.938 | 245.925 | 0.355998 | 36.9155 | 351.561 | 304.751 | 448.124 | 37306.22 |
| 33604.1 | 18.3121 | 0.942013 | 83.2837 | 1.28644 | 244.422 | 0.360552 | 352.209 | 936.785 | 0.979907 | 51.8638 | 405.296 | 0.675499 | 107.864 | 88.7732 | 46.8044 | 271.6572 | 20278.36 |
| 38452.8 | 19.7982 | 0.93283 | 51.7744 | 3.23604 | 282.094 | 0.370236 | 488.702 | 65.6425 | 0.458114 | 110.735 | 682.158 | 0.672151 | 36.7164 | 112.534 | 84.5358 | 342.7777 | 32210.39 |
| 38753.4 | 13.5371 | 0.932257 | 63.9134 | 3.5645 | 739.248 | 0.332871 | 281.682 | 842.124 | 0.827944 | 449.381 | 317.739 | 0.862694 | 162.333 | 186.067 | 418.464 | 289.6114 | 31891.33 |
| 54304.4 | 19.0545 | 0.902803 | 172.948 | 2.34699 | 910.601 | 0.613292 | 232.247 | 256.636 | 0.715306 | 72.4905 | 672.513 | 0.375359 | 155.33 | 47.0622 | 61.66 | 423.7356 | 38485.68 |
| 42356.7 | 24.278 | 0.925439 | 29.6838 | 3.77167 | 232.791 | 0.425698 | 323.504 | 911.829 | 0.918454 | 403.431 | 332.512 | 0.855517 | 85.242 | 279.615 | 375.672 | 200.9178 | 14234.99 |
| 45394.1 | 19.2089 | 0.919681 | 45.1809 | 1.98887 | 493.785 | 0.20359 | 156.105 | 168.008 | 0.667288 | 223.506 | 74.7584 | 0.953458 | 111.716 | 78.5406 | 131.828 | 352.9215 | 43379.88 |
| 37489.8 | 15.7432 | 0.934651 | 97.2604 | 1.97456 | 497.128 | 0.363543 | 72.2713 | 753.29 | 0.912637 | 240.26 | 70.3037 | 0.934778 | 96.0018 | 57.8556 | 176.239 | 195.3419 | 19109.28 |
| 67902.9 | 13.2258 | 0.877042 | 76.2984 | 0.514729 | 319.799 | 0.145959 | 139.044 | 790.988 | 0.858143 | 254.917 | 38.0526 | 0.884728 | 10.6938 | 60.5694 | 227.959 | 672.2363 | 61679.67 |
| 56134.4 | 15.5157 | 0.899335 | 134.062 | 0.211159 | 945.21 | 0.834471 | 498.802 | 377.844 | 0.445251 | 443.446 | 749.892 | 0.902451 | 15.6515 | 354.592 | 374.234 | 432.027 | 29047.59 |
| 41402.3 | 21.3462 | 0.927244 | 137.998 | 1.72206 | 478.018 | 0.457124 | 311.908 | 246.615 | 0.711351 | 314.971 | 557.293 | 0.436341 | 8.88794 | 213.745 | 149.744 | 375.8138 | 35756.92 |
| 53104.5 | 18.1693 | 0.905076 | 29.9478 | 2.82313 | 711.208 | 0.553422 | 476.242 | 688.858 | 0.845552 | 317.824 | 900.918 | 0.83243 | 204.229 | 161.983 | 170.941 | 280.1818 | 20288.09 |
| 30984.8 | 23.8213 | 0.94698 | 97.6713 | 2.72928 | 915.231 | 0.424951 | 300.306 | 526.628 | 0.554718 | 112.568 | 989.292 | 0.62965 | 147.502 | 231.195 | 84.1036 | 444.0533 | 51582.47 |
| 66087.2 | 13.5344 | 0.880481 | 147.918 | 3.43309 | 198.43 | 0.281162 | 483.496 | 300.598 | 0.646533 | 120.824 | 650.949 | 0.775319 | 133.37 | 70.0267 | 66.2215 | 375.8747 | 28021.4 |
| 59086.7 | 17.8556 | 0.893744 | 119.711 | 3.03837 | 609.203 | 0.333523 | 450.017 | 410.212 | 0.939869 | 402.958 | 331.243 | 0.364185 | 56.5793 | 271.941 | 374.823 | 537.082 | 56482.95 |
| 40931 | 21.0122 | 0.928137 | 156.431 | 1.16676 | 666.568 | 0.581158 | 91.1531 | 409.316 | 0.854322 | 301.786 | 697.72 | 0.768295 | 50.2703 | 57.6639 | 171.431 | 214.452 | 17661.15 |
| 39177.2 | 21.1428 | 0.931459 | 112.365 | 1.60342 | 204.196 | 0.206864 | 443.949 | 178.334 | 0.574169 | 301.238 | 669.117 | 0.912377 | 137.211 | 400.367 | 248.644 | 373.7698 | 33394.06 |
| 31863.6 | 18.0412 | 0.94531 | 162.387 | 2.484 | 964.521 | 0.565112 | 499.127 | 485.219 | 0.700316 | 305.816 | 437.998 | 0.37457 | 23.0757 | 291.923 | 188.469 | 444.8565 | 46990.02 |
| 51605.9 | 19.1282 | 0.907915 | 115.96 | 2.22266 | 981.612 | 0.629645 | 360.113 | 445.303 | 0.512774 | 395.235 | 448.994 | 0.944977 | 166.813 | 355.253 | 327.158 | 327.9396 | 28720.52 |
| 41853.8 | 15.1168 | 0.926385 | 28.2553 | 3.52363 | 415.145 | 0.419923 | 391.513 | 493.357 | 0.72282 | 375.541 | 734.3 | 0.584673 | 160.16 | 275.879 | 197.47 | 320.2791 | 28126.75 |
| 36208.4 | 24.25 | 0.937085 | 157.871 | 1.73566 | 392.956 | 0.532827 | 318.879 | 786.964 | 0.402539 | 348.741 | 396.81 | 0.449474 | 59.1238 | 91.6135 | 233.547 | 571.484 | 47866.78 |
| 33957.5 | 19.4251 | 0.941345 | 108.317 | 0.487139 | 304.997 | 0.586187 | 281.978 | 979.213 | 0.594417 | 181.029 | 953.7 | 0.761536 | 35.2474 | 266.567 | 119.267 | 312.2643 | 20454.66 |
| 28408.9 | 25.285 | 0.951861 | 75.8228 | 0.169136 | 229.992 | 0.328563 | 228.262 | 733.601 | 0.313934 | 203.354 | 26.2266 | 0.954479 | 8.86355 | 70.842 | 87.6984 | 388.4542 | 36161.54 |
| 42488.4 | 17.1677 | 0.925184 | 34.5843 | 0.665721 | 860.064 | 0.470491 | 376.852 | 907.585 | 0.743661 | 145.752 | 782.612 | 0.930256 | 55.4938 | 115.307 | 94.8218 | 273.0061 | 25058.66 |
| 25364.5 | 18.4594 | 0.957621 | 37.1785 | 1.19213 | 293.091 | 0.232075 | 341.75 | 225.802 | 0.869813 | 449.095 | 829.428 | 0.492972 | 61.7065 | 246.243 | 338.464 | 407.6695 | 41939.28 |
| 32053.4 | 18.0403 | 0.944951 | 73.2883 | 1.04059 | 197.094 | 0.242281 | 184.488 | 551.899 | 0.722857 | 329.413 | 17.5492 | 0.470162 | 51.148 | 142.692 | 59.2922 | 450.2143 | 41072.41 |
| 38714.5 | 22.5131 | 0.932337 | 131.855 | 0.757326 | 266.075 | 0.603126 | 274.188 | 447.557 | 0.31634 | 489.575 | 19.0843 | 0.744479 | 15.496 | 248.369 | 312.068 | 290.0791 | 22214.47 |
| 50090.2 | 21.5489 | 0.910788 | 98.1198 | 0.7875 | 448.423 | 0.466559 | 457.309 | 246.985 | 0.260926 | 287.445 | 332.563 | 0.974914 | 42.4041 | 169.089 | 261.429 | 387.6316 | 37546.77 |
| 36312.4 | 24.4394 | 0.936889 | 160.381 | 2.76676 | 372.705 | 0.405944 | 301.965 | 454.989 | 0.722001 | 313.895 | 755.482 | 0.591303 | 41.6111 | 74.7251 | 302.434 | 342.7031 | 29574.52 |
| 28287.5 | 26.772 | 0.952092 | 52.8011 | 1.27083 | 30.4287 | 0.207137 | 254.307 | 814.188 | 0.405903 | 352.891 | 66.4134 | 0.668711 | 74.4352 | 219.204 | 189.852 | 510.2644 | 35617.43 |
| 68620 | 18.5234 | 0.875687 | 161.054 | 0.676705 | 128.972 | 0.432383 | 124.991 | 482.271 | 0.740398 | 133.548 | 597.393 | 0.31392 | 21.5391 | 117.448 | 84.6383 | 670.4666 | 41460 |
| 63620 | 13.3088 | 0.885155 | 34.532 | 1.65505 | 316.645 | 0.409303 | 277.313 | 138.937 | 0.52497 | 276.097 | 119.614 | 0.436352 | 68.5021 | 266.261 | 129.855 | 450.1019 | 39940.63 |
| 36082.5 | 14.3838 | 0.937316 | 80.572 | 3.55016 | 188.948 | 0.275614 | 157.714 | 63.3068 | 0.377139 | 80.2678 | 879.988 | 0.729108 | 76.3062 | 90.6113 | 75.0502 | 466.5782 | 41735.68 |
| 47296.1 | 13.5169 | 0.916075 | 114.4 | 1.52958 | 478.395 | 0.377589 | 242.13 | 525.744 | 0.667312 | 94.2449 | 487.684 | 0.447794 | 125.777 | 223.866 | 77.3413 | 498.3057 | 47926.27 |
| 81242.4 | 13.9946 | 0.851775 | 58.6378 | 1.76301 | 982.18 | 0.426048 | 275.904 | 839.929 | 0.93995 | 274.995 | 356.271 | 0.556784 | 12.1654 | 97.2945 | 247.078 | 421.2804 | 41395.09 |
| 54213 | 17.1439 | 0.902975 | 165.419 | 0.554544 | 363.757 | 0.496924 | 221.734 | 456.265 | 0.796329 | 108.142 | 310.928 | 0.835365 | 3.73312 | 93.3992 | 57.4813 | 219.9112 | 16532.1 |
| 42499.7 | 16.5441 | 0.925162 | 172.306 | 0.446826 | 316.382 | 0.403277 | 326.661 | 521.584 | 0.640239 | 232.616 | 482.058 | 0.631019 | 30.5833 | 150.54 | 102.789 | 401.0039 | 31977.15 |
| 62092.8 | 16.351 | 0.888049 | 160.401 | 1.00283 | 948.629 | 0.626155 | 80.1849 | 249.643 | 0.404976 | 209.751 | 913.875 | 0.660106 | 76.4065 | 46.625 | 188.784 | 443.2754 | 39901.28 |
| 28548 | 18.6376 | 0.951591 | 125.634 | 2.76721 | 253.753 | 0.54755 | 276.556 | 537.181 | 0.784927 | 442.85 | 482.678 | 0.640791 | 227.222 | 221.794 | 337.263 | 232.0581 | 16108.93 |
| 37708.3 | 19.2283 | 0.93424 | 86.613 | 0.575584 | 192.204 | 0.364531 | 452.99 | 15.2158 | 0.713017 | 189.099 | 604.387 | 0.925224 | 28.8031 | 192.005 | 166.983 | 177.2403 | 14466.54 |
| 57021.3 | 20.8205 | 0.897658 | 93.0276 | 2.84008 | 421.523 | 0.529595 | 465.138 | 356.837 | 0.667069 | 375.625 | 81.7366 | 0.522728 | 98.3128 | 406.679 | 221.684 | 302.8242 | 24128.84 |
| 54638.3 | 19.0048 | 0.902171 | 29.4151 | 3.24583 | 182.499 | 0.415029 | 448.102 | 492.057 | 0.789371 | 429.691 | 98.6001 | 0.41871 | 76.8272 | 419.82 | 263.42 | 340.0348 | 24862.28 |
| 57651.6 | 15.0491 | 0.896461 | 105.559 | 0.426865 | 420.194 | 0.453091 | 155.632 | 226.661 | 0.924574 | 500.475 | 178.562 | 0.289824 | 7.24391 | 150.686 | 464.372 | 447.6352 | 39420.93 |
| 43810.5 | 18.0316 | 0.92268 | 129.333 | 0.96947 | 637.858 | 0.621302 | 432.159 | 377.111 | 0.721547 | 513.564 | 345.837 | 0.650437 | 24.5891 | 242.93 | 245.1 | 239.7028 | 19402.15 |
| 27466.8 | 25.3899 | 0.953645 | 139.085 | 1.50534 | 585.437 | 0.355191 | 262.162 | 787.546 | 0.871823 | 494.672 | 393.611 | 0.642467 | 62.6979 | 247.001 | 387.702 | 337.5433 | 34040.69 |
| 67536.3 | 17.1439 | 0.877738 | 56.6594 | 1.62289 | 754.77 | 0.37055 | 220.451 | 314.358 | 0.982069 | 208.084 | 52.6195 | 0.657053 | 72.5178 | 96.7209 | 134.262 | 263.9701 | 29507.86 |
| 51246 | 17.2566 | 0.908595 | 163.24 | 0.661858 | 350.842 | 0.496056 | 312.366 | 236.081 | 0.317844 | 208.449 | 833.516 | 0.880812 | 17.4047 | 227.917 | 159.469 | 433.8324 | 34318.25 |
| 61229.1 | 15.2007 | 0.889684 | 109.733 | 0.53542 | 150.388 | 0.159221 | 234.573 | 770.851 | 0.716998 | 342.971 | 388.677 | 0.687277 | 33.1639 | 221.631 | 256.664 | 652.379 | 48089.2 |
| 34440.2 | 21.2637 | 0.940432 | 77.7048 | 3.77083 | 857.754 | 0.470684 | 306.089 | 457.228 | 0.677228 | 297.094 | 671.564 | 0.794737 | 79.3157 | 116.049 | 66.0856 | 261.751 | 27634.47 |
| 26963.2 | 22.1831 | 0.954596 | 36.0696 | 0.280281 | 59.0384 | 0.357294 | 320.111 | 595.503 | 0.580942 | 145.447 | 595.92 | 0.541533 | 26.8033 | 55.4301 | 86.1187 | 339.4292 | 23146.6 |
| 51170.6 | 20.2018 | 0.90874 | 144.109 | 1.9728 | 228.313 | 0.349626 | 91.4503 | 477.443 | 0.910241 | 293.2 | 712.831 | 0.9898 | 11.7774 | 43.5909 | 53.1504 | 255.2594 | 18228.15 |
| 30026 | 19.1821 | 0.948792 | 157.139 | 0.525576 | 959.96 | 0.546512 | 262.838 | 489.171 | 0.870833 | 92.0855 | 792.819 | 0.662624 | 36.6265 | 101.575 | 70.9105 | 281.7534 | 26691.77 |
| 30299.6 | 16.661 | 0.948272 | 128.116 | 0.607497 | 311.187 | 0.412903 | 266.371 | 390.111 | 0.69769 | 203.468 | 564.283 | 0.89271 | 14.8272 | 215.718 | 94.6382 | 215.9279 | 18281.47 |
| 40635.6 | 23.325 | 0.928699 | 155.135 | 2.67951 | 376.32 | 0.55098 | 111.26 | 722.226 | 0.699558 | 353.783 | 869.748 | 0.543205 | 163.338 | 104.174 | 161.343 | 349.1213 | 25294.65 |
| 48326 | 20.0554 | 0.914129 | 149.559 | 1.45976 | 54.3491 | 0.257363 | 352.074 | 359.883 | 0.880841 | 272.057 | 362.262 | 0.848697 | 22.0586 | 157.635 | 111.069 | 264.2946 | 16954.73 |
| 46660.4 | 22.2644 | 0.917285 | 41.9966 | 0.282779 | 21.198 | 0.361342 | 324.11 | 374.692 | 0.994705 | 353.34 | 681.935 | 0.465125 | 8.44216 | 77.4888 | 97.425 | 285.0898 | 16732.39 |
| 30781.2 | 24.7547 | 0.947366 | 67.7867 | 2.67651 | 255.279 | 0.439557 | 242.802 | 97.076 | 0.564732 | 382.342 | 778.167 | 0.947961 | 92.1878 | 67.7018 | 168.879 | 188.4219 | 15773.1 |
| 32341.1 | 20.5308 | 0.944408 | 62.6412 | 2.67638 | 242.255 | 0.291255 | 326.058 | 250.548 | 0.558533 | 517.976 | 783.404 | 0.986121 | 123.391 | 308.145 | 454.588 | 266.1948 | 23958.88 |
| 54590.1 | 13.1684 | 0.902259 | 161.341 | 1.03599 | 124.595 | 0.382384 | 209.446 | 416.668 | 0.51848 | 238.954 | 520.845 | 0.394115 | 102.101 | 77.9243 | 227.753 | 672.724 | 45290.02 |
| 35072.7 | 24.792 | 0.939237 | 166.753 | 0.516525 | 378.075 | 0.634008 | 381.985 | 150.257 | 0.604453 | 278.277 | 540.317 | 0.722461 | 46.9462 | 50.8869 | 48.5196 | 209.5921 | 16410.62 |
| 25764.3 | 23.1881 | 0.956868 | 107.336 | 1.67217 | 301.421 | 0.506563 | 105.604 | 987.653 | 0.917258 | 175.421 | 909.282 | 0.35743 | 125.71 | 84.4241 | 121.393 | 457.4064 | 30997.76 |
| 49518.8 | 17.8596 | 0.911867 | 115.287 | 1.02948 | 955.278 | 0.592384 | 386.307 | 137.711 | 0.584861 | 372.511 | 397.813 | 0.885007 | 96.3523 | 210.925 | 335.069 | 211.3553 | 20287.09 |
| 71437.5 | 15.7121 | 0.870348 | 95.8622 | 3.37413 | 880.742 | 0.475268 | 323.366 | 544.114 | 0.781289 | 263.484 | 535.826 | 0.566562 | 114.058 | 198.359 | 192.211 | 362.7148 | 34902.9 |
| 54197.6 | 13.7993 | 0.903002 | 96.5638 | 1.26351 | 171.563 | 0.278282 | 269.971 | 176.878 | 0.315011 | 508.776 | 827.938 | 0.955327 | 115.746 | 265.474 | 410.963 | 493.0517 | 39014.14 |
| 42954.6 | 14.9807 | 0.9243 | 74.5409 | 1.3566 | 53.5188 | 0.14171 | 363.837 | 671.057 | 0.990508 | 381.796 | 647.265 | 0.506335 | 98.623 | 135.507 | 320.054 | 554.7898 | 36962.99 |
| 51401.7 | 20.4029 | 0.908303 | 168.493 | 1.09416 | 832 | 0.663039 | 374.463 | 997.593 | 0.947722 | 450.11 | 947.433 | 0.536605 | 97.9786 | 364.083 | 220.479 | 368.7894 | 25562.25 |
| 42110.2 | 23.8202 | 0.925906 | 117.53 | 2.19185 | 354.099 | 0.234253 | 274.651 | 186.05 | 0.475032 | 386.58 | 186.134 | 0.866639 | 127.978 | 166.668 | 297.344 | 430.2623 | 46494.87 |
| 61181.6 | 20.3063 | 0.889778 | 45.2186 | 2.2968 | 210.686 | 0.298954 | 217.023 | 881.085 | 0.48609 | 420.449 | 127.634 | 0.565926 | 24.0554 | 65.1037 | 75.3915 | 588.0516 | 45894.88 |
| 26564.9 | 15.6786 | 0.955345 | 145.867 | 3.07385 | 104.801 | 0.558125 | 469.507 | 114.882 | 0.603631 | 479.174 | 43.4864 | 0.644995 | 181.247 | 139.202 | 213.684 | 144.3198 | 10846.97 |
| 57313.9 | 16.9759 | 0.897101 | 64.7358 | 1.38856 | 838.55 | 0.496345 | 482.652 | 365.468 | 0.697653 | 121.411 | 598.745 | 0.458574 | 37.2417 | 84.5729 | 106.047 | 385.746 | 36913.34 |
| 37308.6 | 15.9701 | 0.934995 | 80.6624 | 2.4783 | 526.032 | 0.309672 | 417.255 | 68.7358 | 0.357331 | 351.573 | 827.309 | 0.922872 | 154.62 | 111.747 | 216.189 | 457.3026 | 53441.72 |
| 62120.4 | 17.5684 | 0.887997 | 37.5046 | 1.77166 | 346.745 | 0.594665 | 491.295 | 966.92 | 0.883701 | 285.938 | 709.403 | 0.930082 | 41.2285 | 279.733 | 220.482 | 266.2435 | 16188.13 |
| 29449.5 | 21.9441 | 0.949886 | 84.0942 | 2.11504 | 765.648 | 0.531853 | 324.851 | 895.771 | 0.90214 | 272.941 | 542.047 | 0.906192 | 185.413 | 187.697 | 233.622 | 220.6303 | 17321.61 |
| 25956.9 | 21.1037 | 0.956501 | 62.9325 | 2.42174 | 896.476 | 0.471223 | 489.225 | 826.647 | 0.675584 | 278.633 | 313.41 | 0.515619 | 165.782 | 305.342 | 91.4223 | 387.2227 | 41876.96 |
| 58740.6 | 15.6543 | 0.894398 | 143.696 | 0.721251 | 612.921 | 0.576587 | 136.04 | 148.368 | 0.744894 | 123.22 | 923.659 | 0.638277 | 3.23639 | 131.751 | 107.5 | 274.26 | 22323.64 |
| 29825 | 27.1347 | 0.94918 | 142.86 | 0.255119 | 751.271 | 0.629554 | 295.529 | 287.898 | 0.515716 | 231.219 | 407.556 | 0.805987 | 20.1056 | 230.399 | 84.9255 | 227.868 | 21910.85 |
| 59580.8 | 17.3959 | 0.892808 | 78.8814 | 0.971174 | 470.115 | 0.442107 | 335.199 | 614.587 | 0.466196 | 402.846 | 413.149 | 0.863519 | 82.5631 | 59.3898 | 277.024 | 319.2041 | 28510.82 |
| 38589.1 | 20.7806 | 0.932573 | 158.204 | 3.7874 | 283.485 | 0.536836 | 298.797 | 679.634 | 0.502492 | 482.374 | 377.314 | 0.971275 | 44.0193 | 188.087 | 286.712 | 210.6849 | 15867.46 |
| 63259.1 | 13.7315 | 0.885838 | 92.2244 | 1.15524 | 721.125 | 0.443972 | 443.151 | 19.7283 | 0.499336 | 254.151 | 35.0866 | 0.684547 | 76.6431 | 294.544 | 87.45 | 325.8817 | 37951.2 |
| 46355 | 13.9437 | 0.917858 | 143.045 | 0.179351 | 992.902 | 0.668909 | 282.007 | 369.015 | 0.859483 | 139.568 | 370.381 | 0.571117 | 4.95474 | 193.914 | 67.8994 | 241.3468 | 21324.03 |
| 57123.4 | 18.0001 | 0.897463 | 165.294 | 1.91896 | 759.775 | 0.422861 | 119.777 | 275.392 | 0.53295 | 233.074 | 901.997 | 0.4987 | 168.601 | 109.127 | 131.049 | 624.3576 | 63634.46 |
| 55186.8 | 14.0965 | 0.901129 | 141.537 | 2.17414 | 504.335 | 0.548828 | 338.639 | 103.976 | 0.33533 | 333.6 | 415.365 | 0.601283 | 138.715 | 258.375 | 163.563 | 424.4491 | 37871.51 |
| 82078.4 | 14.1949 | 0.850191 | 24.4417 | 0.915477 | 537.228 | 0.487785 | 435.667 | 30.8057 | 0.891703 | 328.126 | 90.9347 | 0.486073 | 35.4587 | 308.512 | 150.227 | 233.4136 | 21629.08 |
| 37762.3 | 24.7439 | 0.934143 | 124.515 | 3.3022 | 686.034 | 0.534455 | 416.767 | 742.106 | 0.747701 | 390.384 | 470.073 | 0.423439 | 87.4006 | 326.757 | 335.521 | 466.1856 | 39155.37 |
| 45901 | 23.388 | 0.918725 | 155.187 | 1.47728 | 271.133 | 0.259146 | 281.599 | 633.729 | 0.449063 | 478.94 | 159.225 | 0.733256 | 9.54606 | 177.941 | 367.467 | 584.4531 | 51713.91 |
| 58076.3 | 13.715 | 0.895656 | 79.0277 | 3.18247 | 638.675 | 0.409584 | 270.439 | 585.492 | 0.563196 | 382.774 | 645.24 | 0.983414 | 81.3619 | 231.461 | 80.7516 | 297.7186 | 28829.41 |
| 41914.1 | 14.1214 | 0.92627 | 156.787 | 2.9215 | 43.8018 | 0.390143 | 378.687 | 337.039 | 0.977802 | 492.61 | 833.896 | 0.452027 | 143.288 | 168.331 | 277.786 | 305.4292 | 18698.45 |
| 52444.5 | 15.8915 | 0.906324 | 141.56 | 1.84083 | 358.308 | 0.625156 | 396.275 | 58.8098 | 0.455258 | 402.373 | 437.018 | 0.640456 | 102.592 | 261.995 | 340.871 | 349.3523 | 25843 |
| 45173.1 | 23.1728 | 0.920103 | 94.4466 | 0.617031 | 491.11 | 0.475272 | 310.79 | 319.744 | 0.44886 | 309.286 | 828.959 | 0.468625 | 43.1191 | 77.1621 | 179.389 | 522.5063 | 49356.35 |
| 47575.3 | 23.282 | 0.915553 | 150.566 | 1.15924 | 835.017 | 0.311576 | 339.021 | 274.668 | 0.834352 | 503.837 | 237.845 | 0.912779 | 10.5471 | 93.8492 | 234.866 | 301.8028 | 36042.78 |
| 48074.6 | 20.3894 | 0.914605 | 169.271 | 0.292998 | 940.217 | 0.594411 | 306.39 | 958.82 | 0.843487 | 517.388 | 872.042 | 0.717077 | 27.8262 | 118.932 | 450.931 | 339.0529 | 26592.73 |
| 33351.6 | 23.9864 | 0.942497 | 78.6096 | 2.68071 | 195.385 | 0.361228 | 233.351 | 498.46 | 0.613853 | 169.452 | 24.1943 | 0.307205 | 148.488 | 227.324 | 76.0854 | 550.1773 | 46816.84 |
| 37257.6 | 23.1282 | 0.935097 | 83.6271 | 1.55833 | 519.531 | 0.453835 | 220.121 | 437.683 | 0.670635 | 305.242 | 287.23 | 0.330391 | 19.5137 | 155.576 | 206.343 | 489.0936 | 49566.5 |
| 52577.6 | 16.8579 | 0.906073 | 158.982 | 0.227972 | 423.484 | 0.661869 | 232.85 | 676.1 | 0.531081 | 204.274 | 818.046 | 0.865992 | 21.637 | 76.4515 | 77.1788 | 292.0748 | 19720.71 |
| 34989.9 | 18.6917 | 0.939389 | 24.103 | 0.481706 | 29.7238 | 0.341727 | 391.898 | 624.137 | 0.705759 | 193.671 | 735.169 | 0.718721 | 9.331 | 374.506 | 142.249 | 262.9888 | 16167.38 |
| 64191.2 | 14.1152 | 0.884073 | 148.035 | 1.03035 | 225.407 | 0.530728 | 451.755 | 924.894 | 0.827202 | 248.829 | 224.878 | 0.44791 | 9.32632 | 128.707 | 223.35 | 409.3618 | 26035.29 |
| 40599.8 | 21.8851 | 0.928765 | 141.495 | 0.403541 | 579.232 | 0.315875 | 310.129 | 645.979 | 0.816266 | 470.248 | 671.53 | 0.83595 | 19.6781 | 118.984 | 346.529 | 353.012 | 33998.41 |
| 25097.6 | 18.1039 | 0.958126 | 143.46 | 0.678068 | 161.214 | 0.455765 | 464.98 | 758.672 | 0.60823 | 109.72 | 781.638 | 0.459345 | 12.5203 | 61.0109 | 75.9416 | 441.2138 | 31622.73 |
| 33368.6 | 16.1566 | 0.942458 | 32.372 | 1.52716 | 883.072 | 0.479441 | 361.125 | 379.702 | 0.519742 | 497.202 | 122.634 | 0.660004 | 32.0366 | 152.382 | 490.583 | 301.6944 | 36989 |
| 58875.3 | 13.9975 | 0.894142 | 130.17 | 1.73983 | 755.771 | 0.545538 | 434.709 | 771.579 | 0.671111 | 344.202 | 498.846 | 0.831453 | 136.147 | 362.233 | 246.503 | 260.023 | 21447.9 |
| 81112.7 | 14.6472 | 0.852021 | 66.5299 | 1.65539 | 359.067 | 0.507893 | 390.125 | 974.698 | 0.892582 | 215.503 | 707.98 | 0.673766 | 150.272 | 338.261 | 204.967 | 309.7741 | 19351.29 |
| 39791.7 | 15.4162 | 0.930291 | 38.0714 | 0.159725 | 273.743 | 0.260375 | 136.828 | 249.213 | 0.80725 | 460.488 | 546.058 | 0.338284 | 4.65337 | 121.427 | 75.3574 | 575.714 | 55452.89 |
| 26444.7 | 15.3781 | 0.955573 | 127.791 | 0.830177 | 284.598 | 0.628348 | 115.485 | 523.466 | 0.717411 | 284.157 | 453.352 | 0.421948 | 82.8098 | 108.909 | 268.871 | 389.7116 | 27235.12 |
| 25594.5 | 26.7807 | 0.957193 | 51.5002 | 1.21469 | 771.754 | 0.479684 | 427.509 | 149.771 | 0.362246 | 172.995 | 742.035 | 0.893998 | 103.878 | 295.794 | 111.01 | 305.2185 | 35709.44 |
| 28493.5 | 13.1651 | 0.95169 | 23.2705 | 1.14276 | 842.495 | 0.415244 | 85.4321 | 205.119 | 0.705183 | 189.684 | 23.305 | 0.88555 | 7.53768 | 62.609 | 175.526 | 184.0949 | 25713.32 |
| 28590.6 | 23.2606 | 0.951514 | 36.4499 | 3.61942 | 953.703 | 0.309177 | 377.033 | 697.1 | 0.669042 | 352.658 | 645.519 | 0.938759 | 115.545 | 293.341 | 254.65 | 364.7635 | 46525.72 |
| 64974.8 | 15.4349 | 0.882589 | 27.1986 | 1.66176 | 1.23146 | 0.297379 | 341.681 | 133.523 | 0.819249 | 161.02 | 420.626 | 0.885986 | 144.961 | 69.0853 | 105.882 | 189.2153 | 10483.58 |
| 52429 | 19.7147 | 0.906356 | 27.9032 | 1.34884 | 538.697 | 0.23574 | 489.645 | 284.968 | 0.875277 | 226.622 | 336.92 | 0.782071 | 81.6316 | 49.1441 | 173.912 | 341.6008 | 38510.13 |
| 51100.5 | 17.5374 | 0.908871 | 77.8825 | 3.48059 | 29.5772 | 0.30561 | 406.888 | 119.482 | 0.508602 | 419.753 | 544.063 | 0.865001 | 159.255 | 177.741 | 386.613 | 264.096 | 16398.23 |
| 39884.5 | 14.6576 | 0.930115 | 140.891 | 0.843044 | 314.55 | 0.685208 | 253.895 | 379.068 | 0.729225 | 376.414 | 964.903 | 0.969775 | 58.6544 | 163.724 | 308.889 | 212.5287 | 13240.3 |
| 59292.1 | 19.2377 | 0.893356 | 145.837 | 2.17369 | 310.445 | 0.464834 | 309.975 | 122.707 | 0.933871 | 237.643 | 71.7316 | 0.323502 | 31.2688 | 240.894 | 99.9224 | 340.077 | 28135.88 |
| 70110.7 | 13.433 | 0.87286 | 145.077 | 0.694712 | 304.069 | 0.375783 | 227.07 | 688.172 | 0.808843 | 344.156 | 682.133 | 0.85592 | 43.5856 | 108.165 | 126.907 | 315.582 | 22351.44 |
| 30040.3 | 26.7965 | 0.948772 | 131.924 | 3.73417 | 660.758 | 0.237004 | 391.807 | 461.89 | 0.543179 | 214.343 | 778.735 | 0.897906 | 69.1159 | 90.8021 | 153.471 | 490.6369 | 61705.42 |
| 41998.7 | 14.4517 | 0.92611 | 162.141 | 0.171726 | 237.016 | 0.562062 | 161.585 | 821.824 | 0.353131 | 403.359 | 809.182 | 0.690371 | 13.433 | 71.0133 | 243.135 | 493.3641 | 34217.96 |
| 43183.6 | 13.9075 | 0.923865 | 132.565 | 1.69548 | 373.739 | 0.370823 | 378.685 | 254.927 | 0.674254 | 291.625 | 724.359 | 0.38551 | 18.4005 | 120.182 | 76.4293 | 519.9886 | 48569.91 |
| 45794.1 | 17.367 | 0.918922 | 81.32 | 0.322811 | 40.5226 | 0.452408 | 209.027 | 43.1758 | 0.840436 | 187.477 | 32.2583 | 0.597209 | 24.5541 | 81.2004 | 115.606 | 139.5855 | 9291.815 |
| 66057.1 | 18.7391 | 0.880541 | 144.795 | 2.06651 | 677.294 | 0.215719 | 215.714 | 585.049 | 0.960087 | 438.045 | 559.435 | 0.631741 | 3.42539 | 124.427 | 142.635 | 589.1566 | 62590.89 |
| 67398.2 | 14.46 | 0.877999 | 118.133 | 1.60267 | 429.488 | 0.545201 | 196.09 | 343.783 | 0.977046 | 446.495 | 210.257 | 0.176049 | 66.1559 | 57.5654 | 173.22 | 685.035 | 49875.3 |
| 35689.9 | 15.0004 | 0.93806 | 77.8096 | 1.873 | 404.326 | 0.413292 | 355.984 | 433.468 | 0.819832 | 168.037 | 580.532 | 0.314143 | 70.5955 | 257.166 | 119.591 | 469.6685 | 43895.72 |
| 45154.3 | 20.6403 | 0.920137 | 163.904 | 0.397963 | 617.568 | 0.645983 | 112.651 | 345.654 | 0.904234 | 140.576 | 177.45 | 0.166795 | 10.6991 | 64.6933 | 115.35 | 699.5549 | 57155.13 |
| 44696.2 | 20.1043 | 0.921004 | 134.681 | 2.64543 | 80.3301 | 0.354789 | 388.486 | 811.993 | 0.92381 | 261.994 | 368.441 | 0.591223 | 3.94635 | 307.445 | 76.4809 | 296.7174 | 18736.16 |
| 44470.6 | 19.608 | 0.921431 | 37.4651 | 2.86109 | 554.921 | 0.35493 | 450.499 | 432.129 | 0.809487 | 243.751 | 889.99 | 0.531344 | 41.6962 | 346.117 | 196.625 | 403.7775 | 40504.97 |
| 33490.3 | 21.1755 | 0.942231 | 129.865 | 0.498069 | 258.509 | 0.195177 | 337.445 | 313.174 | 0.79224 | 171.507 | 451.995 | 0.743383 | 19.2304 | 153.505 | 144.794 | 409.1923 | 38462.88 |
| 52525 | 21.1051 | 0.906176 | 43.4294 | 0.428797 | 215.376 | 0.199043 | 125.827 | 457.981 | 0.939952 | 135.594 | 853.364 | 0.487228 | 30.7172 | 38.3264 | 127.545 | 545.1461 | 44770.48 |
| 43558.7 | 20.0887 | 0.923159 | 85.7184 | 1.3946 | 61.8041 | 0.436289 | 450.526 | 939.239 | 0.864637 | 192.495 | 689.362 | 0.766108 | 79.1188 | 237.224 | 176.132 | 242.2692 | 14266.32 |
| 55589.8 | 20.329 | 0.90037 | 134.333 | 0.498211 | 352.378 | 0.615492 | 385.013 | 47.2173 | 0.500907 | 487.542 | 785.58 | 0.971507 | 24.7909 | 245.489 | 336.583 | 209.0616 | 15083.22 |
| 50767.1 | 19.5355 | 0.909504 | 150.892 | 1.55615 | 721.418 | 0.239074 | 336.632 | 400.733 | 0.562878 | 340.924 | 323.579 | 0.914197 | 105.353 | 101.879 | 56.4485 | 533.8297 | 63479.44 |
| 53270.7 | 13.693 | 0.904758 | 145.415 | 2.38637 | 794.039 | 0.416158 | 448.705 | 675.355 | 0.382207 | 208.259 | 526.739 | 0.77928 | 19.2119 | 160.814 | 80.976 | 536.7313 | 58358.42 |
| 64783.3 | 15.1049 | 0.882952 | 130.273 | 0.833554 | 386.286 | 0.493516 | 228.877 | 89.1354 | 0.507986 | 339.426 | 194.658 | 0.554727 | 48.5746 | 176.569 | 164.409 | 364.8097 | 30848.7 |
| 36826.7 | 14.7278 | 0.935907 | 39.0066 | 1.1817 | 296.075 | 0.446094 | 424.306 | 846.192 | 0.751322 | 335.473 | 15.8533 | 0.981111 | 57.473 | 284.134 | 72.2525 | 159.3547 | 12969.12 |
| 46798 | 15.3864 | 0.91702 | 145.464 | 1.10572 | 665.655 | 0.456315 | 494.34 | 385.957 | 0.583083 | 162.795 | 377.508 | 0.725156 | 3.39357 | 104.349 | 123.307 | 327.1083 | 32953.53 |
| 28608.5 | 13.0958 | 0.951473 | 143.449 | 1.01649 | 193.815 | 0.523944 | 188.846 | 734.354 | 0.835751 | 364.732 | 657.529 | 0.975071 | 36.2753 | 62.9754 | 243.849 | 183.3866 | 12177.24 |
| 31311.6 | 21.2707 | 0.946358 | 120.179 | 2.86951 | 402.446 | 0.368071 | 489.437 | 964.665 | 0.646295 | 113.254 | 546.944 | 0.785066 | 32.8131 | 400.241 | 77.6229 | 318.6178 | 28702.15 |
| 50725 | 19.8622 | 0.909584 | 141.376 | 3.02475 | 809.436 | 0.456707 | 211.709 | 220.657 | 0.900972 | 458.805 | 736.999 | 0.318826 | 33.3627 | 115.198 | 364.576 | 491.5995 | 52967.09 |
| 43338.7 | 18.2304 | 0.923574 | 117.126 | 0.548164 | 802.086 | 0.613692 | 376.568 | 254.083 | 0.713001 | 172.601 | 550.997 | 0.53265 | 54.1948 | 227.849 | 161.904 | 292.1045 | 25386.46 |
| 58481.1 | 14.8285 | 0.894889 | 56.0451 | 0.866316 | 13.3037 | 0.193016 | 296.084 | 216.983 | 0.700068 | 439.123 | 399.511 | 0.685832 | 76.5706 | 288.999 | 191.908 | 380.8482 | 22324 |
| 26578.1 | 15.9292 | 0.95532 | 172.72 | 2.02831 | 210.088 | 0.181203 | 227.464 | 200.041 | 0.644337 | 477.302 | 141.526 | 0.545915 | 110.413 | 63.1748 | 70.9951 | 607.6069 | 59068.85 |
| 62455.8 | 16.7143 | 0.887362 | 25.9497 | 2.80278 | 294.318 | 0.349057 | 132.65 | 513.755 | 0.997816 | 252.794 | 948.734 | 0.720834 | 133.66 | 47.9151 | 223.013 | 289.3416 | 21296.53 |
| 31911.8 | 22.0371 | 0.945222 | 116.281 | 2.74899 | 272.647 | 0.463617 | 420.142 | 939.68 | 0.852703 | 454.1 | 171.823 | 0.718169 | 155.076 | 195.591 | 319.627 | 215.9365 | 16055.62 |
| 31099.6 | 17.4465 | 0.946757 | 130.909 | 0.679673 | 35.4216 | 0.557581 | 201.281 | 524.3 | 0.929218 | 364.8 | 315.536 | 0.996211 | 31.882 | 71.4985 | 224.796 | 129.948 | 7897.579 |
| 70775.8 | 14.8448 | 0.871601 | 53.4222 | 2.53262 | 202.703 | 0.427331 | 383.759 | 955.935 | 0.54303 | 472.774 | 175.992 | 0.521659 | 5.68806 | 209.134 | 438.405 | 471.1251 | 32388.88 |
| 61691.1 | 19.0303 | 0.888812 | 64.9208 | 0.329771 | 353.967 | 0.326444 | 333.451 | 666.071 | 0.995845 | 230.397 | 925.334 | 0.587759 | 5.35839 | 267.609 | 152.034 | 388.4414 | 30417.94 |
| 51668.1 | 22.5644 | 0.9078 | 93.1694 | 1.93034 | 812.349 | 0.523656 | 232.656 | 439.053 | 0.414635 | 335.557 | 599.388 | 0.861813 | 66.8069 | 214.853 | 335.266 | 352.0025 | 33274.62 |
| 65343.6 | 16.1249 | 0.881891 | 152.726 | 1.85363 | 655.265 | 0.372554 | 364.483 | 676.045 | 0.813704 | 212.404 | 653.448 | 0.424945 | 101.323 | 256.524 | 130.844 | 616.4141 | 57180.01 |
| 28343.7 | 25.1103 | 0.951984 | 142.666 | 3.11657 | 495.771 | 0.558167 | 274.762 | 285.01 | 0.776732 | 402.226 | 517.643 | 0.334891 | 26.3684 | 172.189 | 178.359 | 382.3611 | 33327.26 |
| 59580.4 | 18.175 | 0.892809 | 37.8809 | 1.90825 | 232.047 | 0.193346 | 267.95 | 71.7613 | 0.760969 | 328.9 | 679.636 | 0.413583 | 111.045 | 73.728 | 274.034 | 697.3683 | 61951.67 |
| 52529 | 15.8804 | 0.906164 | 147.112 | 2.51227 | 45.1281 | 0.446808 | 119.214 | 33.4707 | 0.712468 | 178.541 | 824.693 | 0.879553 | 8.52595 | 70.1716 | 177.591 | 185.9022 | 11191.38 |
| 48299.5 | 15.8554 | 0.914176 | 22.8103 | 0.37926 | 266.993 | 0.483356 | 483.09 | 137.448 | 0.219659 | 354.007 | 881.34 | 0.888137 | 20.0556 | 461.49 | 240.667 | 424.1849 | 34612.04 |
| 43574.3 | 14.7429 | 0.923126 | 73.7942 | 1.72527 | 58.4463 | 0.493371 | 452.484 | 261.938 | 0.658103 | 350.177 | 157.431 | 0.521476 | 131.462 | 273.825 | 79.3247 | 211.0779 | 13486.29 |
| 48842 | 23.2038 | 0.913154 | 101.959 | 2.93046 | 237.177 | 0.495167 | 197.074 | 136.788 | 0.657646 | 359.446 | 762.104 | 0.476015 | 44.6645 | 188.412 | 99.1099 | 287.6661 | 21436.25 |
| 51740.4 | 19.6701 | 0.907661 | 140.741 | 2.23125 | 810.793 | 0.332676 | 449.013 | 277.705 | 0.567491 | 173.545 | 900.301 | 0.987577 | 31.2309 | 436.559 | 152.321 | 391.643 | 43944.15 |
| 62018.9 | 15.3135 | 0.888188 | 33.1026 | 1.97238 | 752.422 | 0.460147 | 311.538 | 916.908 | 0.859177 | 221.774 | 559.47 | 0.506815 | 122.17 | 198.47 | 50.8726 | 421.8195 | 37229.81 |
| 31138.7 | 23.9453 | 0.946688 | 32.9149 | 0.177843 | 395.489 | 0.434907 | 267.232 | 361.781 | 0.473084 | 53.5858 | 714.261 | 0.349718 | 7.40114 | 230.65 | 51.3414 | 587.3381 | 58672.5 |
| 31546.2 | 21.7637 | 0.945914 | 49.9671 | 0.32401 | 346.047 | 0.471579 | 452.711 | 566.905 | 0.847872 | 317.274 | 876.326 | 0.918991 | 11.0548 | 211.98 | 267.262 | 196.3142 | 14762.2 |
| 26575.7 | 14.1499 | 0.955324 | 66.7587 | 1.95906 | 441.491 | 0.386285 | 325.013 | 885.25 | 0.289591 | 252.808 | 443.082 | 0.87651 | 44.9885 | 192.485 | 92.4978 | 448.9716 | 47915.24 |
| 38064.9 | 17.2649 | 0.933563 | 125.867 | 2.23598 | 4.0187 | 0.249392 | 247.987 | 601.82 | 0.77217 | 291.41 | 295.003 | 0.386026 | 89.1316 | 151.113 | 113.081 | 502.4315 | 30207.81 |
| 55179.3 | 17.7274 | 0.901145 | 104.856 | 0.359 | 917.931 | 0.410275 | 383.532 | 108.584 | 0.861061 | 204.043 | 261.558 | 0.752837 | 15.9581 | 323.61 | 91.4381 | 248.9226 | 29526.46 |
| 26609.7 | 26.7177 | 0.95527 | 170.196 | 2.41925 | 542.744 | 0.45289 | 391.81 | 315.712 | 0.535688 | 127.675 | 913.657 | 0.722064 | 16.214 | 330.369 | 56.6035 | 337.9393 | 33114.79 |
| 41238.5 | 18.4022 | 0.927552 | 114.917 | 0.763794 | 278.659 | 0.263656 | 326.819 | 678.577 | 0.774005 | 301.351 | 191.093 | 0.943555 | 12.4149 | 55.0301 | 166.026 | 271.2404 | 23908.24 |
| 31511.9 | 24.6419 | 0.945982 | 165.797 | 1.54721 | 359.572 | 0.573468 | 120.4 | 380.446 | 0.659635 | 175.038 | 411.081 | 0.709041 | 37.093 | 53.5719 | 102.074 | 212.1417 | 17038.18 |
| 52777.4 | 21.6391 | 0.905698 | 113.42 | 0.990698 | 207.615 | 0.331316 | 135.406 | 839.483 | 0.813125 | 328.388 | 273.209 | 0.437208 | 71.3516 | 57.7714 | 210.054 | 499.8008 | 36604.51 |
| 75822.9 | 15.0517 | 0.862041 | 162.57 | 2.29731 | 961.64 | 0.599461 | 120.924 | 361.852 | 0.474507 | 428.423 | 543.28 | 0.659965 | 86.8798 | 83.8215 | 397.897 | 394.9832 | 35068.18 |
| 37983.4 | 19.316 | 0.933719 | 60.9032 | 2.34262 | 596.477 | 0.339069 | 468.683 | 251.818 | 0.760454 | 100.52 | 216.662 | 0.97563 | 20.8067 | 287.701 | 65.7 | 199.79 | 23721.21 |
| 33833.5 | 19.0807 | 0.941579 | 45.3621 | 1.86225 | 383.476 | 0.374722 | 402.608 | 556.024 | 0.687656 | 227.252 | 0.720019 | 0.398886 | 97.8789 | 250.198 | 135.542 | 440.5215 | 43827 |
| 44135.8 | 13.9075 | 0.922062 | 85.0746 | 2.31054 | 638.315 | 0.407264 | 288.475 | 640.668 | 0.587015 | 187.455 | 14.9982 | 0.452922 | 133.72 | 87.185 | 127.597 | 501.6883 | 54596.96 |
| 39655.9 | 18.8056 | 0.93055 | 57.4479 | 0.802499 | 490.613 | 0.432907 | 326.404 | 622.382 | 0.966888 | 201.525 | 421.211 | 0.484391 | 79.5528 | 306.253 | 72.8837 | 314.5601 | 27940.47 |
| 76980.9 | 14.4395 | 0.859847 | 163.218 | 0.185639 | 728.542 | 0.717162 | 246.49 | 268.461 | 0.666704 | 336.905 | 72.7994 | 0.284042 | 5.14419 | 118.976 | 206.952 | 566.5225 | 41615.48 |
| 58924.6 | 16.5973 | 0.89405 | 142.385 | 0.513573 | 120.874 | 0.486937 | 68.953 | 170.084 | 0.288522 | 293.955 | 889.109 | 0.792985 | 36.8288 | 46.9689 | 122.42 | 475.118 | 30702.15 |
| 33860.7 | 22.4702 | 0.941531 | 114.978 | 2.97774 | 900.975 | 0.36962 | 332.497 | 777.411 | 0.932345 | 324.526 | 688.115 | 0.933119 | 19.9569 | 197.569 | 281.377 | 280.3769 | 29810.08 |
| 35366.7 | 22.9007 | 0.938679 | 162.974 | 0.468418 | 572.006 | 0.710495 | 474.68 | 518.913 | 0.267726 | 513.596 | 409.046 | 0.563009 | 23.3056 | 154.53 | 454.579 | 520.8354 | 41158.86 |
| 28965 | 21.9276 | 0.950804 | 151.8 | 1.82449 | 438.248 | 0.493216 | 358.822 | 342.816 | 0.293465 | 477.863 | 540.898 | 0.701401 | 85.8374 | 254.502 | 323.257 | 440.6262 | 43547.85 |
| 33460.6 | 20.0265 | 0.942286 | 107.961 | 0.453048 | 344.352 | 0.578994 | 220.456 | 711.332 | 0.907173 | 116.111 | 66.6365 | 0.947402 | 27.6693 | 88.8655 | 116.051 | 128.683 | 9276.302 |
| 36994 | 23.0911 | 0.935596 | 149.051 | 3.49229 | 13.6953 | 0.309987 | 310.979 | 551.039 | 0.568761 | 247.973 | 279.305 | 0.677376 | 17.5397 | 169.578 | 151.712 | 315.2683 | 19613.78 |
| 31279 | 19.7557 | 0.946419 | 69.999 | 1.79259 | 180.954 | 0.410183 | 437.273 | 286.705 | 0.441882 | 213.012 | 261.934 | 0.656466 | 9.48382 | 432.513 | 196.703 | 280.2139 | 24168.49 |
| 57453 | 19.2128 | 0.89684 | 165.73 | 3.51707 | 98.4951 | 0.461875 | 63.3014 | 684.666 | 0.709106 | 456.996 | 253.44 | 0.910363 | 6.43666 | 53.7174 | 63.5858 | 205.6638 | 12745.85 |
| 53510.5 | 21.7562 | 0.904309 | 36.2167 | 1.28634 | 597.29 | 0.422552 | 495.31 | 137.444 | 0.850772 | 131.005 | 933.999 | 0.74028 | 104.88 | 93.889 | 45.187 | 250.4379 | 23534.19 |
| 27816.3 | 22.0296 | 0.95298 | 144.213 | 0.465961 | 939.365 | 0.518723 | 133.704 | 933.334 | 0.99068 | 322.418 | 47.5472 | 0.324311 | 27.9688 | 58.127 | 224.267 | 548.1933 | 51962.94 |
| 28835.7 | 22.4173 | 0.951049 | 118.616 | 1.45401 | 474.115 | 0.659034 | 318.98 | 988.399 | 0.793575 | 264.782 | 273.088 | 0.821721 | 123.343 | 294.196 | 246.808 | 260.3348 | 17585.37 |
| 46224.2 | 13.4388 | 0.918105 | 53.7772 | 2.29233 | 653.275 | 0.497673 | 196.538 | 954.972 | 0.837281 | 446.788 | 595.428 | 0.318708 | 100.89 | 77.8453 | 204.596 | 604.9712 | 47860.5 |
| 78080.8 | 15.0668 | 0.857764 | 45.4608 | 2.53834 | 716.186 | 0.424961 | 269.777 | 86.2541 | 0.558272 | 441.032 | 963.143 | 0.95173 | 162.678 | 231.66 | 303.77 | 312.2628 | 30071.39 |
| 33888.3 | 23.3885 | 0.941479 | 137.901 | 1.34928 | 612.659 | 0.545328 | 231.718 | 639.199 | 0.294523 | 184.4 | 174.692 | 0.887028 | 29.0189 | 65.6969 | 50.7175 | 351.1332 | 35636.93 |
| 78691.8 | 15.086 | 0.856607 | 124.323 | 2.31599 | 740.9 | 0.526668 | 202.469 | 615.309 | 0.932847 | 482.722 | 586.031 | 0.369028 | 37.1199 | 83.5135 | 135.041 | 462.0063 | 36978.02 |
| 46308.2 | 17.9727 | 0.917949 | 85.2839 | 0.676938 | 41.9636 | 0.406467 | 239.976 | 531.742 | 0.784687 | 176.395 | 94.7683 | 0.508659 | 14.0864 | 165.271 | 160.731 | 267.9463 | 16576.83 |
| 34804.4 | 15.5628 | 0.939738 | 129.025 | 1.0913 | 960.396 | 0.518516 | 163.761 | 15.0828 | 0.472961 | 311.649 | 522.547 | 0.854957 | 79.4575 | 51.7301 | 202.869 | 266.5253 | 32275.55 |
| 64340.3 | 15.9337 | 0.883791 | 156.308 | 2.82001 | 482.665 | 0.234204 | 114.3 | 1.27888 | 0.563442 | 174.884 | 840.875 | 0.737988 | 14.3296 | 89.7922 | 90.5951 | 614.6124 | 62340.92 |
| 76650.9 | 15.4124 | 0.860473 | 99.7172 | 2.3703 | 419.894 | 0.331997 | 339.293 | 574.466 | 0.552245 | 468.164 | 901.415 | 0.957031 | 45.1709 | 199.442 | 257.679 | 383.6721 | 32442.61 |
| 47960.3 | 16.4752 | 0.914819 | 130.88 | 0.163635 | 182.457 | 0.30798 | 383.427 | 535.934 | 0.981293 | 387.72 | 639.559 | 0.401451 | 11.2601 | 259.895 | 343.782 | 521.9901 | 37382.73 |
| 37785.2 | 14.7086 | 0.934091 | 152.672 | 1.04696 | 490.907 | 0.606561 | 234.557 | 124.48 | 0.98978 | 167.453 | 886.126 | 0.46499 | 94.9804 | 172.973 | 61.8574 | 232.9189 | 18422.8 |
| 36668.1 | 22.1792 | 0.936213 | 152.413 | 2.9149 | 490.917 | 0.643802 | 391.066 | 329.999 | 0.915685 | 303.993 | 390.224 | 0.413447 | 158.021 | 183.749 | 268.631 | 348.1041 | 25968.55 |
| 63390.9 | 16.4005 | 0.88559 | 102.246 | 1.15367 | 757.665 | 0.210038 | 416.621 | 727.745 | 0.760314 | 490.879 | 219.527 | 0.977057 | 80.0638 | 362.406 | 183.626 | 479.3758 | 56876.21 |
| 30669.4 | 21.0815 | 0.947575 | 29.9045 | 0.2969 | 277.988 | 0.317472 | 334.249 | 165.38 | 0.459092 | 95.4817 | 155.551 | 0.715071 | 1.88913 | 185.109 | 73.817 | 323.2738 | 33997.7 |
| 85999 | 14.5216 | 0.842765 | 124.533 | 0.110282 | 425.335 | 0.427598 | 428.198 | 791.348 | 0.84869 | 126.643 | 780.9 | 0.764346 | 3.71198 | 190.909 | 72.7376 | 372.4311 | 25889.51 |
| 70485.6 | 16.7507 | 0.872152 | 149.722 | 0.367263 | 896.432 | 0.347396 | 72.4461 | 610.751 | 0.744908 | 406.678 | 407.741 | 0.724795 | 22.2348 | 50.4711 | 79.8814 | 488.0487 | 49642.78 |
| 61215.1 | 20.4836 | 0.889714 | 158.093 | 0.683843 | 796.491 | 0.59225 | 305.159 | 464.439 | 0.878505 | 220.136 | 184.598 | 0.971596 | 37.9573 | 165.62 | 52.007 | 164.7607 | 14038.1 |
| 70948.5 | 14.3691 | 0.871274 | 38.4931 | 2.46526 | 67.8171 | 0.183993 | 209.744 | 298.942 | 0.890826 | 267.4 | 735.018 | 0.600085 | 71.4375 | 119.497 | 247.207 | 460.4539 | 28938.44 |
| 68122.1 | 13.4018 | 0.876627 | 59.3217 | 2.51956 | 971.108 | 0.482008 | 472.349 | 614.969 | 0.728733 | 173.586 | 312.212 | 0.786096 | 102.199 | 103.175 | 53.9348 | 272.4444 | 27128.34 |
| 38793.4 | 16.2214 | 0.932182 | 51.3034 | 0.951199 | 865.648 | 0.407211 | 324.756 | 437.314 | 0.751338 | 203.689 | 788.754 | 0.923615 | 52.5281 | 77.3322 | 79.5558 | 263.1509 | 28540.98 |
| 43317 | 18.6269 | 0.923616 | 172.899 | 1.67173 | 207.829 | 0.176354 | 402.87 | 765.09 | 0.787975 | 287.161 | 901.329 | 0.885801 | 71.9221 | 343.905 | 197.948 | 618.6566 | 48477.52 |
| 78948.3 | 15.5092 | 0.856121 | 113.522 | 0.920324 | 164.093 | 0.597885 | 376.07 | 170.246 | 0.896311 | 408.313 | 458.53 | 0.788534 | 60.9723 | 171.205 | 108.042 | 166.7018 | 9828.242 |
| 31266.9 | 20.6516 | 0.946442 | 39.2503 | 2.66794 | 209.059 | 0.460629 | 234.698 | 863.476 | 0.442193 | 70.3463 | 306.538 | 0.965188 | 143.997 | 168.948 | 49.1948 | 230.4128 | 17690.32 |
| 33003.9 | 20.2578 | 0.943152 | 64.6502 | 2.63906 | 618.405 | 0.278753 | 356.429 | 140.125 | 0.96354 | 492.551 | 16.2983 | 0.904907 | 148.363 | 262.258 | 306.907 | 204.9759 | 27653.44 |
| 56654.3 | 18.4477 | 0.898352 | 130.3 | 1.5519 | 524.436 | 0.523136 | 497.372 | 135.898 | 0.807983 | 212.503 | 139.889 | 0.608335 | 6.67302 | 384.375 | 127.158 | 198.9808 | 18688.55 |
| 42419.6 | 13.8418 | 0.925312 | 38.0874 | 1.25496 | 293.954 | 0.465305 | 374.022 | 131.676 | 0.937358 | 300.583 | 51.7984 | 0.870416 | 4.62746 | 314.805 | 111.838 | 97.19852 | 9028.763 |
| 31689.3 | 21.5107 | 0.945643 | 114.732 | 1.34343 | 69.9437 | 0.336688 | 387.233 | 144.415 | 0.697136 | 275.515 | 235.498 | 0.422148 | 119.057 | 343.946 | 261.401 | 315.2762 | 23440.92 |
| 29041.4 | 27.1266 | 0.950664 | 95.7337 | 2.20192 | 452.017 | 0.466849 | 247.774 | 875.52 | 0.699554 | 221.32 | 360.728 | 0.96092 | 19.5574 | 67.6817 | 146.204 | 201.9754 | 17331.17 |
| 32106.9 | 21.4427 | 0.944852 | 37.8921 | 1.00323 | 52.3797 | 0.200433 | 315.192 | 172.125 | 0.494385 | 60.6595 | 987.554 | 0.512285 | 45.2414 | 49.6999 | 54.9824 | 591.6367 | 42975.77 |
| 57245.4 | 13.4373 | 0.897229 | 24.3381 | 2.81515 | 172.651 | 0.144724 | 326.904 | 826.78 | 0.858941 | 320.268 | 451.928 | 0.751075 | 106.001 | 209.244 | 119.239 | 543.58 | 42706.39 |
| 54804.8 | 18.9795 | 0.901856 | 132.81 | 2.47136 | 315.969 | 0.37687 | 323.743 | 853.543 | 0.975435 | 332.537 | 661.604 | 0.45881 | 42.1244 | 220.095 | 166.063 | 442.4561 | 32906.85 |
| 53062.8 | 18.685 | 0.905155 | 101.82 | 0.174581 | 799.569 | 0.593936 | 392.739 | 434.882 | 0.367652 | 144.366 | 422.575 | 0.721285 | 17.0385 | 267.011 | 109.834 | 394.8135 | 37545.04 |
| 49620.8 | 19.7881 | 0.911676 | 76.6669 | 2.4928 | 308.748 | 0.368488 | 116.452 | 589.336 | 0.633844 | 65.2821 | 163.199 | 0.453391 | 171.75 | 102.271 | 47.4967 | 454.0434 | 39341.37 |
| 25999.1 | 15.0986 | 0.956416 | 156.209 | 0.38328 | 513.726 | 0.589153 | 441.683 | 32.0091 | 0.889389 | 306.9 | 437.77 | 0.612623 | 35.1243 | 239.135 | 84.1436 | 162.2356 | 15194.2 |
| 60829.1 | 14.4759 | 0.890442 | 54.2428 | 2.18695 | 959.192 | 0.446198 | 386.334 | 186.962 | 0.990197 | 451.808 | 773.662 | 0.933606 | 64.613 | 132.487 | 347.664 | 217.5386 | 22150.57 |
| 38377.4 | 21.3778 | 0.932974 | 168.418 | 0.471559 | 669.092 | 0.352133 | 452.726 | 259.481 | 0.718477 | 384.55 | 641.743 | 0.68189 | 15.0197 | 451.061 | 271.455 | 405.6242 | 42604.8 |
| 56096.4 | 15.774 | 0.899407 | 112.153 | 2.44324 | 169.74 | 0.40479 | 462.888 | 242.374 | 0.610732 | 276.489 | 561.518 | 0.689649 | 17.0298 | 114.816 | 193.477 | 268.9848 | 19578.29 |
| 40859.3 | 20.8934 | 0.928273 | 169.385 | 0.35709 | 630.046 | 0.490071 | 346.897 | 520.846 | 0.447879 | 383.647 | 148.061 | 0.570356 | 5.94393 | 183.873 | 97.7673 | 515.6794 | 49610.03 |
| 66994 | 13.9419 | 0.878764 | 49.9679 | 2.22161 | 366.966 | 0.506542 | 155.037 | 294.878 | 0.367826 | 482.223 | 536.454 | 0.717008 | 178.117 | 124.383 | 141.144 | 389.0409 | 29188.03 |
| 74281.3 | 13.814 | 0.86496 | 65.091 | 1.64474 | 691.861 | 0.278174 | 165.462 | 392.063 | 0.779644 | 252.547 | 372.245 | 0.656267 | 21.7985 | 103.913 | 54.8497 | 467.0919 | 51674.34 |
| 44308.4 | 15.5292 | 0.921735 | 162.29 | 3.72693 | 280.478 | 0.599985 | 352.924 | 77.7082 | 0.906475 | 431.02 | 850.425 | 0.553629 | 215.152 | 328.664 | 122.02 | 217.1125 | 14657.89 |
| 43208 | 23.7497 | 0.923826 | 91.0384 | 0.973017 | 300.448 | 0.46854 | 468.307 | 708.18 | 0.306844 | 146.485 | 551.773 | 0.479777 | 21.7304 | 348.079 | 77.1609 | 650.6857 | 55018.25 |
| 28885.1 | 27.2549 | 0.950961 | 72.339 | 3.64576 | 948.562 | 0.474837 | 273.178 | 492.108 | 0.777304 | 514.047 | 542.257 | 0.780049 | 98.5678 | 165.39 | 457.808 | 233.9496 | 25567.13 |
| 35648.4 | 24.9835 | 0.938147 | 84.8546 | 0.978411 | 335.401 | 0.500895 | 349.025 | 237.53 | 0.630309 | 148.552 | 135.461 | 0.564808 | 61.8298 | 323.238 | 59.0441 | 211.2121 | 18697.37 |
| 31317.3 | 19.6084 | 0.946346 | 60.9647 | 0.372997 | 712.53 | 0.381117 | 236.579 | 923.782 | 0.643959 | 410.67 | 753.795 | 0.803184 | 15.2029 | 133.678 | 72.1906 | 364.1866 | 37755.37 |
| 28469.9 | 16.7712 | 0.951738 | 95.8929 | 3.71004 | 923.519 | 0.451737 | 415.958 | 529.878 | 0.49055 | 452.018 | 322.222 | 0.776065 | 163.975 | 382.749 | 244.492 | 321.5137 | 39911.82 |
| 58247.8 | 15.5713 | 0.895332 | 128.817 | 1.84033 | 183.767 | 0.53524 | 388.36 | 354.432 | 0.638155 | 126.902 | 142.013 | 0.661457 | 25.0483 | 215.615 | 84.4615 | 213.3801 | 14676.14 |
| 67333.4 | 13.3982 | 0.878121 | 92.9926 | 1.10729 | 562.362 | 0.306168 | 489.468 | 269.95 | 0.886162 | 70.914 | 932.46 | 0.756402 | 70.8897 | 196.371 | 48.7995 | 345.3894 | 32999.36 |
| 47484.6 | 19.9234 | 0.915722 | 164.885 | 0.191974 | 410.862 | 0.635768 | 265.937 | 891.018 | 0.694482 | 246.798 | 591.159 | 0.85065 | 7.37231 | 128.244 | 199.92 | 263.1713 | 17670.87 |
| 50475.7 | 14.648 | 0.910053 | 49.9833 | 1.57973 | 182.221 | 0.283425 | 377.452 | 628.748 | 0.880462 | 98.6632 | 523.992 | 0.602096 | 3.93162 | 247.206 | 86.86 | 344.9944 | 25917.88 |
| 31514.7 | 13.6478 | 0.945968 | 81.34 | 0.548247 | 588.261 | 0.337055 | 114.047 | 333.557 | 0.6175 | 313.586 | 922.765 | 0.65162 | 36.862 | 90.4825 | 171.298 | 413.623 | 46020.96 |
| 48699.5 | 14.9033 | 0.913418 | 157.75 | 0.12691 | 476.742 | 0.462294 | 321.538 | 402.709 | 0.62011 | 412.918 | 96.1817 | 0.971769 | 11.9784 | 77.0484 | 80.8963 | 238.5696 | 20757.06 |
| 78104.3 | 15.3601 | 0.85772 | 130.267 | 0.350391 | 568.131 | 0.339132 | 263.618 | 188.628 | 0.882412 | 294.829 | 260.476 | 0.810039 | 10.9624 | 152.616 | 158.544 | 298.307 | 27658.2 |
| 63725.3 | 17.9145 | 0.884958 | 76.6065 | 3.66184 | 971.947 | 0.312805 | 388.015 | 752.305 | 0.761514 | 128.392 | 874.516 | 0.887436 | 79.6701 | 105.705 | 87.4249 | 420.845 | 46585.72 |
| 65049 | 15.7156 | 0.882449 | 80.0365 | 1.20542 | 67.5547 | 0.145453 | 296.701 | 130.239 | 0.84705 | 414.106 | 444.448 | 0.614519 | 90.9729 | 255.557 | 330.535 | 503.7847 | 33527.55 |
| 72747.3 | 15.7461 | 0.867867 | 135.019 | 0.208395 | 892.509 | 0.594012 | 426.181 | 735.219 | 0.607597 | 290.857 | 364.244 | 0.890144 | 14.9988 | 112.092 | 135.619 | 290.81 | 24153.8 |
| 27120.7 | 18.7555 | 0.954295 | 32.0524 | 1.6506 | 432.444 | 0.378716 | 300.047 | 53.562 | 0.66889 | 420.584 | 73.9591 | 0.707253 | 49.731 | 164.441 | 334.296 | 193.9399 | 23669.51 |
| 46288.1 | 16.1083 | 0.917986 | 135.217 | 2.83515 | 942.719 | 0.44829 | 283.965 | 174.495 | 0.647371 | 469.413 | 968.975 | 0.713912 | 53.1979 | 162.117 | 125.68 | 342.0402 | 38214.29 |
| 31830.5 | 26.5683 | 0.945381 | 150.043 | 1.75611 | 92.5475 | 0.496627 | 158.147 | 141.5 | 0.354337 | 273.177 | 776.602 | 0.854168 | 54.7124 | 102.849 | 58.1463 | 275.3641 | 19313.43 |
| 25286.7 | 20.3633 | 0.95777 | 126.607 | 0.630821 | 41.1777 | 0.586949 | 478.727 | 493.902 | 0.528548 | 485.972 | 64.1389 | 0.488885 | 12.6564 | 324.054 | 184.895 | 258.6184 | 17150.43 |
| 63034.1 | 15.3539 | 0.886265 | 91.3666 | 2.22273 | 405.258 | 0.241375 | 287.063 | 77.0362 | 0.94587 | 240.541 | 108.956 | 0.610764 | 43.7798 | 267.113 | 81.028 | 336.4994 | 35490.26 |
| 35746.2 | 14.8859 | 0.937954 | 152.133 | 2.33394 | 941.552 | 0.489399 | 219.12 | 593.322 | 0.892743 | 77.9468 | 802.702 | 0.313238 | 81.1449 | 175.552 | 50.3145 | 572.7862 | 58878.71 |
| 68238.2 | 14.7809 | 0.876407 | 89.2977 | 3.22362 | 666.531 | 0.308525 | 237.82 | 453.042 | 0.411744 | 507.47 | 551.976 | 0.960746 | 100.489 | 224.715 | 488.472 | 506.8832 | 55990.24 |
| 26910.1 | 25.724 | 0.9547 | 45.1426 | 3.78419 | 82.4147 | 0.230411 | 85.4676 | 80.3316 | 0.321021 | 196.276 | 668.827 | 0.821674 | 90.4389 | 76.7241 | 90.3246 | 462.3842 | 37679.58 |
| 45971.9 | 18.3006 | 0.918586 | 40.8048 | 2.82377 | 105.15 | 0.472329 | 229.304 | 292.554 | 0.610383 | 380.453 | 474.205 | 0.795078 | 47.2257 | 84.0158 | 330.619 | 189.2013 | 12687.99 |
| 34545.8 | 14.5946 | 0.940227 | 136.311 | 0.35646 | 982.769 | 0.515026 | 214.239 | 299.329 | 0.7526 | 277.386 | 614.795 | 0.565851 | 22.7997 | 80.3272 | 55.3513 | 329.716 | 35732.19 |
| 47944.2 | 20.5684 | 0.914852 | 112.675 | 3.44711 | 257.016 | 0.387215 | 353.06 | 664.602 | 0.452708 | 405.597 | 336.135 | 0.988284 | 124.614 | 327.692 | 99.716 | 273.5951 | 22464.91 |
| 60214.6 | 18.7588 | 0.891608 | 109.605 | 2.52884 | 968.502 | 0.406236 | 371.661 | 788.256 | 0.65253 | 350.122 | 682.39 | 0.955717 | 46.5474 | 68.2925 | 186.937 | 337.2329 | 35551.1 |
| 28874.7 | 17.2791 | 0.950971 | 35.7011 | 1.24675 | 488.181 | 0.412125 | 174.077 | 602.223 | 0.552407 | 177.014 | 130.617 | 0.659123 | 54.2874 | 169.869 | 165.692 | 309.1916 | 32920.21 |
| 42933.5 | 16.4665 | 0.92434 | 160.148 | 1.51122 | 14.0596 | 0.361148 | 172.648 | 221.609 | 0.915393 | 97.9547 | 480.828 | 0.20323 | 103.054 | 113.809 | 55.6304 | 640.1935 | 39021.14 |
| 55680.8 | 13.6566 | 0.900193 | 150.737 | 0.307713 | 878.326 | 0.544452 | 483.89 | 334.713 | 0.652769 | 354.867 | 587.426 | 0.829079 | 27.0209 | 432.975 | 348.759 | 277.9757 | 25804.22 |
| 41287.6 | 18.8138 | 0.92746 | 88.7385 | 1.63505 | 527.071 | 0.298049 | 193.824 | 450.53 | 0.858216 | 196.124 | 372.163 | 0.605783 | 147.379 | 163.894 | 126.468 | 353.3131 | 38201.56 |
| 67353.5 | 18.3386 | 0.878085 | 40.8772 | 2.92919 | 523.053 | 0.382162 | 223.675 | 597.256 | 0.780558 | 299.974 | 539.808 | 0.75997 | 124.221 | 121.293 | 154.357 | 307.8969 | 27310.51 |
| 51801.4 | 22.0551 | 0.907547 | 140.717 | 1.37146 | 258.302 | 0.564146 | 119.821 | 629.954 | 0.631195 | 410.297 | 500.342 | 0.545175 | 116.684 | 80.0008 | 158.605 | 332.2768 | 22728.07 |
| 34167 | 14.6185 | 0.940945 | 151.202 | 1.19862 | 283.079 | 0.618074 | 87.0605 | 676.15 | 0.79156 | 153.304 | 897.709 | 0.62817 | 64.2061 | 49.4961 | 102.661 | 271.4378 | 17396.57 |
| 43993.2 | 20.1397 | 0.922336 | 155.662 | 2.33346 | 109.388 | 0.201487 | 329.754 | 320.58 | 0.50839 | 461.78 | 740.982 | 0.602609 | 117.609 | 127.532 | 202.595 | 679.8348 | 50798.52 |
| 50130.9 | 17.4054 | 0.910708 | 48.9312 | 1.66361 | 326.043 | 0.421915 | 429.193 | 355.567 | 0.89555 | 139.625 | 115.261 | 0.260522 | 52.1154 | 310.767 | 57.9519 | 480.0779 | 41677.13 |
| 43072.5 | 18.0132 | 0.924078 | 43.8133 | 2.32452 | 125.141 | 0.393595 | 259.597 | 221.547 | 0.914441 | 264.862 | 767.831 | 0.882484 | 71.2196 | 238.508 | 248.912 | 168.857 | 11468.84 |
| 70615.3 | 17.8236 | 0.871907 | 168.121 | 3.30475 | 781.233 | 0.643989 | 391.13 | 475.917 | 0.755886 | 442.866 | 75.7736 | 0.473005 | 174.298 | 270.528 | 386.235 | 379.0384 | 28662.13 |
| 31059.4 | 16.6727 | 0.946832 | 120.052 | 0.561558 | 589.469 | 0.446752 | 126.555 | 550.25 | 0.721198 | 142.801 | 36.0587 | 0.896912 | 4.41762 | 95.0539 | 96.2774 | 194.4498 | 20318.09 |
| 51443.5 | 16.5707 | 0.908221 | 129.646 | 2.12308 | 189.211 | 0.459242 | 436.317 | 741.394 | 0.290806 | 292.256 | 380.495 | 0.732414 | 32.9845 | 122.682 | 165.104 | 472.3078 | 34816.02 |
| 67669.6 | 16.7441 | 0.877486 | 77.857 | 3.36065 | 327.307 | 0.51418 | 207.504 | 352.907 | 0.465397 | 392.994 | 90.1097 | 0.931937 | 69.3377 | 180.583 | 237.824 | 220.1856 | 16525.75 |
| 26512.7 | 15.2899 | 0.955444 | 65.3521 | 3.00548 | 168.877 | 0.170674 | 489.374 | 339.855 | 0.525533 | 365.753 | 792.792 | 0.708908 | 95.8187 | 467.57 | 234.527 | 529.3195 | 49684.9 |
| 54277.7 | 20.8566 | 0.902855 | 164.326 | 1.93043 | 637.91 | 0.510356 | 188.507 | 128.277 | 0.877021 | 451.103 | 932.451 | 0.691031 | 155.444 | 126.752 | 327.707 | 249.8014 | 21473.11 |

Table B6. Compilation of the Aspen Plus-based dataset for the optimization of the DtMG system with the optimized hydrogen-to-ester ratios of 477.29.

| X1 | X2 | X3 | X4 | X5 | X6 | X7 | X8 | X9 | X10 | X11 | X12 | X13 | X14 | X15 | X16 | UED | UPC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 36420.9 | 25 | 0.95 | 100 | 1.1 | 0.4 | 0.482 | 110 | 0.6 | 0.895 | 130 | 30.9048 | 0.939426 | 100 | 100 | 100 | 71.79596 | 4893.973 |
| 157336 | 27.6149 | 0.769071 | 169.363 | 0.831525 | 349.499 | 0.743735 | 151.397 | 721.232 | 0.629201 | 98.5135 | 99.2266 | 0.913659 | 14.6395 | 141.734 | 75.1174 | 304.0676 | 15919.55 |
| 70274.4 | 15.8333 | 0.899337 | 56.2435 | 3.61769 | 800.855 | 0.396108 | 490.666 | 855.825 | 0.693609 | 505.661 | 965.09 | 0.855911 | 124.787 | 315.998 | 54.756 | 395.1515 | 36705.24 |
| 127365 | 22.8952 | 0.813915 | 89.9208 | 2.75579 | 815.52 | 0.584524 | 256.92 | 256.859 | 0.717471 | 451.51 | 403.731 | 0.659171 | 120.446 | 232.251 | 395.876 | 375.8996 | 27240.57 |
| 113867 | 16.6706 | 0.834108 | 97.0608 | 3.48551 | 912.417 | 0.434509 | 101.037 | 92.7921 | 0.844529 | 510.064 | 112.302 | 0.812475 | 53.4176 | 44.3322 | 466.727 | 255.2611 | 26279.66 |
| 63389.5 | 15.3082 | 0.909639 | 112.813 | 0.934619 | 647.77 | 0.493911 | 122.816 | 259.403 | 0.675616 | 132.301 | 528.319 | 0.476019 | 42.105 | 105.91 | 60.7464 | 418.1519 | 38943.35 |
| 127369 | 19.2378 | 0.813906 | 65.8373 | 0.567648 | 343.652 | 0.5558 | 306.933 | 305.204 | 0.923022 | 428.742 | 942.714 | 0.504016 | 40.6841 | 94.8162 | 171.467 | 412.152 | 24460.73 |
| 148863 | 14.0987 | 0.781741 | 46.301 | 2.03926 | 56.0851 | 0.175942 | 354.874 | 502.602 | 0.733672 | 88.7706 | 409.364 | 0.911799 | 142.923 | 283.626 | 56.606 | 610.3074 | 31760.61 |
| 74870 | 17.3512 | 0.892461 | 117.765 | 0.220134 | 831.409 | 0.491363 | 189.644 | 278.513 | 0.622088 | 470.337 | 235.471 | 0.968648 | 9.06891 | 71.0941 | 293.168 | 269.8858 | 25744.17 |
| 114115 | 31.8022 | 0.833751 | 147.36 | 1.93122 | 637.012 | 0.501405 | 300.86 | 26.6462 | 0.503858 | 284.392 | 782.928 | 0.839525 | 84.1771 | 61.7062 | 66.3911 | 430.6844 | 33099.86 |
| 71451.3 | 17.3049 | 0.897577 | 47.0438 | 1.0799 | 456.884 | 0.327155 | 63.382 | 101.12 | 0.654974 | 302.607 | 275.624 | 0.593919 | 70.6333 | 48.3169 | 65.876 | 428.6385 | 42055.94 |
| 31065.1 | 31.2061 | 0.958022 | 76.3745 | 1.42595 | 36.8787 | 0.273346 | 70.8369 | 186.794 | 0.882951 | 309.132 | 607.495 | 0.211272 | 36.5987 | 60.5472 | 124.634 | 670.934 | 46468.99 |
| 126327 | 16.5378 | 0.815464 | 70.7478 | 1.25919 | 407.053 | 0.414307 | 468.526 | 207.361 | 0.591634 | 437.561 | 904.315 | 0.763575 | 44.4385 | 199.848 | 294.408 | 428.7704 | 31020.91 |
| 174748 | 14.5549 | 0.743008 | 28.0139 | 0.508569 | 305.418 | 0.293635 | 308.156 | 374.285 | 0.712796 | 350.318 | 631.733 | 0.75193 | 48.2645 | 101.329 | 277.684 | 576.3262 | 37152.89 |
| 181452 | 32.1522 | 0.73299 | 82.3926 | 3.2556 | 866.512 | 0.237994 | 206.274 | 846.095 | 0.739404 | 387.57 | 774.085 | 0.942609 | 118.137 | 84.6697 | 245.287 | 799.1742 | 67786.38 |
| 168770 | 15.0381 | 0.751955 | 172.274 | 0.643084 | 101.798 | 0.687567 | 461.957 | 77.6211 | 0.196833 | 456.008 | 615.369 | 0.959418 | 60.4343 | 249.013 | 303.177 | 833.4238 | 39564 |
| 82098.2 | 22.024 | 0.881649 | 86.8083 | 1.32086 | 942.732 | 0.500546 | 411.765 | 61.7461 | 0.769367 | 368.339 | 733.845 | 0.427737 | 128.409 | 377.712 | 139.024 | 422.7491 | 41538.35 |
| 167636 | 20.1362 | 0.753653 | 93.8816 | 0.915098 | 206.575 | 0.490697 | 401.354 | 579.359 | 0.859633 | 313.16 | 547.733 | 0.592301 | 60.5192 | 155.673 | 126.586 | 421.3257 | 23014.61 |
| 136318 | 21.9526 | 0.800518 | 114.521 | 0.354776 | 984.435 | 0.438745 | 59.9016 | 718.134 | 0.410913 | 518.291 | 222.742 | 0.926396 | 15.6056 | 45.1391 | 304.141 | 652.1836 | 57242.93 |
| 191633 | 14.4641 | 0.717744 | 41.1299 | 1.25814 | 61.6724 | 0.496679 | 388.503 | 24.4418 | 0.460165 | 363.508 | 888.751 | 0.459955 | 3.54241 | 253.426 | 106.556 | 780.2868 | 36723.76 |
| 100000 | 32.7936 | 0.854872 | 34.9714 | 1.70768 | 619.858 | 0.409682 | 399.681 | 424.24 | 0.644741 | 150.375 | 229.164 | 0.569663 | 59.0574 | 323.213 | 142.745 | 510.6473 | 44953.55 |
| 92378.2 | 24.7367 | 0.866268 | 151.214 | 2.17039 | 251.699 | 0.621619 | 285.307 | 131.037 | 0.560092 | 248.182 | 171.586 | 0.672508 | 92.528 | 91.3239 | 143.367 | 287.0223 | 17613.36 |
| 123835 | 20.246 | 0.819195 | 106.511 | 0.960049 | 190.052 | 0.598477 | 493.134 | 881.703 | 0.584444 | 482.086 | 319.059 | 0.486545 | 24.0006 | 252.351 | 473.36 | 648.2526 | 35296.56 |
| 80050 | 14.3771 | 0.884708 | 84.4591 | 2.71602 | 228.655 | 0.225463 | 225.818 | 990.578 | 0.958719 | 506.178 | 536.101 | 0.34844 | 93.6418 | 90.1898 | 297.367 | 908.1774 | 66039.28 |
| 199177 | 18.2685 | 0.706457 | 20.517 | 1.708 | 368.247 | 0.251507 | 412.75 | 147.309 | 0.979566 | 397.219 | 213.309 | 0.482851 | 98.9031 | 225.71 | 126.434 | 793.0596 | 52916.71 |
| 44834.3 | 23.532 | 0.937409 | 149.428 | 0.987432 | 614.715 | 0.674213 | 291.058 | 970.02 | 0.991683 | 472.513 | 412.171 | 0.952458 | 98.5605 | 255.984 | 296.331 | 219.1956 | 14203.63 |
| 56193.4 | 19.9679 | 0.920409 | 28.3874 | 1.62245 | 65.6331 | 0.265519 | 77.1701 | 968.616 | 0.335758 | 252.473 | 132.555 | 0.594519 | 19.6129 | 64.0623 | 186.275 | 802.5259 | 53118.83 |
| 102448 | 25.8616 | 0.851201 | 150.285 | 2.50227 | 774.231 | 0.501347 | 386.295 | 646.046 | 0.951235 | 77.2273 | 896.575 | 0.410442 | 100.744 | 185.547 | 67.3734 | 570.7921 | 44204.26 |
| 113627 | 23.703 | 0.834473 | 121.55 | 3.54419 | 309.947 | 0.346249 | 216.332 | 918.932 | 0.581202 | 135.547 | 995.621 | 0.974797 | 97.602 | 121.403 | 48.1407 | 459.0583 | 31009.58 |
| 122891 | 31.9726 | 0.820618 | 36.2513 | 1.80163 | 987.843 | 0.489172 | 408.848 | 825.164 | 0.673355 | 449.171 | 277.407 | 0.885943 | 48.2814 | 336.625 | 401.837 | 363.6041 | 31470.52 |
| 166721 | 34.9019 | 0.755037 | 138.692 | 0.171003 | 585.269 | 0.339063 | 155.747 | 39.346 | 0.938722 | 175.454 | 818.819 | 0.749314 | 3.844 | 106.052 | 152.86 | 618.3953 | 41497.99 |
| 115073 | 28.2968 | 0.832312 | 87.194 | 0.74192 | 735.25 | 0.495578 | 234.177 | 997.247 | 0.880428 | 487.883 | 819.45 | 0.680084 | 70.0222 | 112.838 | 129.988 | 421.6794 | 30816.79 |
| 33959.3 | 24.2746 | 0.953683 | 116.467 | 0.757359 | 574.716 | 0.209091 | 313.115 | 741.905 | 0.425674 | 432.755 | 546.766 | 0.955964 | 26.4568 | 192.139 | 338.738 | 705.9549 | 82652.52 |
| 118451 | 22.4285 | 0.827252 | 153.838 | 1.05762 | 127.238 | 0.514016 | 429.732 | 857.137 | 0.294439 | 377.273 | 685.004 | 0.703315 | 33.5491 | 356.625 | 284.052 | 818.5273 | 44922.33 |
| 177597 | 18.9902 | 0.738748 | 46.3039 | 1.12202 | 797.78 | 0.384964 | 256.917 | 449.802 | 0.338803 | 184.431 | 470.397 | 0.905117 | 81.4994 | 249.929 | 90.3444 | 852.7563 | 71387.85 |
| 175122 | 33.8772 | 0.742465 | 120.806 | 1.41284 | 360.964 | 0.513071 | 326.052 | 166.936 | 0.863926 | 376.355 | 464.678 | 0.704244 | 80.3597 | 203.286 | 133.884 | 354.9838 | 20670.62 |
| 114882 | 22.7977 | 0.832593 | 54.5357 | 2.63789 | 214.786 | 0.342311 | 193.817 | 440.976 | 0.437363 | 392.368 | 58.1379 | 0.951263 | 92.216 | 81.7449 | 220.754 | 444.4369 | 29843.15 |
| 46634.9 | 14.7717 | 0.934709 | 134.366 | 1.67768 | 925.4 | 0.559974 | 419.079 | 63.3503 | 0.780701 | 441.808 | 88.2151 | 0.623428 | 103.142 | 372.171 | 99.6637 | 187.3783 | 19790.86 |
| 110795 | 23.0355 | 0.838709 | 29.7706 | 3.75629 | 753.255 | 0.428817 | 407.263 | 208.076 | 0.27867 | 373.099 | 577.019 | 0.623102 | 122.641 | 116.71 | 187.784 | 993.1673 | 93940.32 |
| 163764 | 30.6022 | 0.759456 | 118.546 | 0.694399 | 782.874 | 0.493518 | 391.581 | 567.308 | 0.493528 | 426.398 | 175.639 | 0.495375 | 12.8162 | 351.028 | 224.067 | 945.4289 | 69378.39 |
| 141420 | 25.4929 | 0.792886 | 71.4667 | 0.4027 | 12.328 | 0.374157 | 444.243 | 631.802 | 0.811777 | 159.293 | 94.6686 | 0.881104 | 20.8562 | 441.161 | 125.532 | 300.8451 | 14674.39 |
| 201232 | 17.8391 | 0.703382 | 40.2161 | 2.76035 | 699.079 | 0.330914 | 105.299 | 662.178 | 0.927839 | 373.699 | 101.367 | 0.877471 | 6.62716 | 97.4435 | 71.8192 | 446.4449 | 34263.67 |
| 166785 | 20.3848 | 0.754928 | 130.406 | 0.763199 | 870.723 | 0.46962 | 260.729 | 703.123 | 0.705773 | 409.189 | 447.831 | 0.786922 | 22.9482 | 75.5602 | 368.533 | 497.5291 | 37168.72 |
| 86548.5 | 28.06 | 0.874995 | 163.762 | 0.654672 | 495.985 | 0.664468 | 190.866 | 371.892 | 0.879111 | 441.383 | 982.206 | 0.879907 | 24.0743 | 147.274 | 329.551 | 243.5753 | 15316.73 |
| 53323.5 | 27.5455 | 0.924711 | 132.022 | 1.15082 | 959.446 | 0.342777 | 333.096 | 202.47 | 0.794509 | 149.744 | 242.986 | 0.581433 | 63.9978 | 48.7503 | 104.332 | 466.1803 | 56691.1 |
| 175013 | 28.0022 | 0.74262 | 61.565 | 2.30741 | 256.414 | 0.281518 | 342.953 | 228.523 | 0.683089 | 85.8739 | 549.559 | 0.719127 | 30.3272 | 124.742 | 75.6949 | 668.6606 | 40721.75 |
| 134752 | 30.9207 | 0.802869 | 125.06 | 2.85555 | 752.471 | 0.40685 | 329.164 | 606.899 | 0.367541 | 337.607 | 146.736 | 0.714489 | 163.931 | 193.34 | 95.992 | 848.9188 | 72921.14 |
| 166981 | 19.9927 | 0.754634 | 118.053 | 2.41276 | 288.364 | 0.32293 | 420.411 | 909.083 | 0.969131 | 224.037 | 910.206 | 0.416258 | 119.406 | 217.347 | 76.6667 | 849.9638 | 51405 |
| 162048 | 16.8168 | 0.762013 | 153.371 | 3.04696 | 748.894 | 0.322176 | 460.797 | 529.516 | 0.560891 | 154.092 | 244.738 | 0.952545 | 2.69634 | 445.208 | 135.378 | 619.7993 | 51957.86 |
| 104745 | 27.0129 | 0.847765 | 36.0173 | 1.30904 | 285.811 | 0.275644 | 476.48 | 637.201 | 0.315126 | 431.606 | 55.3228 | 0.816354 | 55.8764 | 440.422 | 240.506 | 888.3707 | 67531.37 |
| 92536.9 | 33.9448 | 0.866042 | 154.416 | 0.488371 | 589.717 | 0.213913 | 377.778 | 417.834 | 0.948385 | 402.489 | 454.984 | 0.962835 | 34.3488 | 207.391 | 306.284 | 852.3703 | 73553.73 |
| 57285.6 | 22.6307 | 0.918777 | 89.5193 | 3.46287 | 794.238 | 0.271088 | 264.959 | 708.061 | 0.332583 | 488.318 | 177.037 | 0.960284 | 120.347 | 168.398 | 79.7351 | 746.9568 | 92434.77 |
| 76761.6 | 24.1288 | 0.889636 | 69.9806 | 0.633697 | 588.729 | 0.324974 | 286.092 | 657.64 | 0.542809 | 249.102 | 962.828 | 0.51213 | 33.2821 | 81.8935 | 241.061 | 810.0987 | 77031.93 |
| 150734 | 15.5562 | 0.778942 | 119.448 | 2.6863 | 260.345 | 0.45921 | 401.675 | 523.843 | 0.811033 | 347.066 | 768.796 | 0.465546 | 40.6252 | 353.457 | 237.963 | 537.0906 | 31911.73 |
| 133564 | 21.5605 | 0.804639 | 167.715 | 3.05489 | 336.662 | 0.61897 | 218.279 | 240.129 | 0.256804 | 193.991 | 495.066 | 0.919467 | 83.4416 | 124.918 | 72.4254 | 571.895 | 33682.22 |
| 117607 | 23.6456 | 0.828517 | 151.267 | 2.73072 | 946.462 | 0.293608 | 185.735 | 460.359 | 0.93331 | 448.193 | 73.4049 | 0.587575 | 90.9595 | 87.27 | 364.105 | 628.7689 | 63219.34 |
| 69855 | 27.4312 | 0.899974 | 158.732 | 2.55989 | 900.628 | 0.444468 | 265.88 | 907.005 | 0.718552 | 324.943 | 311.952 | 0.520243 | 143.48 | 111.847 | 143.198 | 569.5123 | 53473.52 |
| 142922 | 17.4547 | 0.790633 | 49.354 | 2.894 | 382.192 | 0.436335 | 410.502 | 562.346 | 0.706907 | 160.579 | 53.132 | 0.612032 | 66.157 | 168.426 | 45.0471 | 434.4885 | 29684.23 |
| 57296.2 | 16.3052 | 0.918757 | 92.7463 | 0.248656 | 842.619 | 0.407503 | 255.886 | 156.473 | 0.672821 | 518.628 | 235.057 | 0.904346 | 7.02963 | 150.01 | 54.0444 | 274.5694 | 31055.58 |
| 194317 | 13.4434 | 0.713727 | 73.5346 | 0.701559 | 342.787 | 0.45329 | 321.951 | 344.925 | 0.2386 | 438.54 | 899.736 | 0.881225 | 5.31735 | 220.902 | 298.661 | 959.8337 | 58145.22 |
| 47561.1 | 32.5722 | 0.93334 | 42.8014 | 0.482625 | 587.833 | 0.454327 | 411.177 | 191.528 | 0.890789 | 271.371 | 614.913 | 0.150206 | 29.5623 | 375.808 | 111.893 | 902.7934 | 91981.49 |
| 88295.4 | 23.3553 | 0.872377 | 102.257 | 2.7446 | 409.078 | 0.531183 | 119.93 | 295.426 | 0.78343 | 315.353 | 67.2291 | 0.258371 | 76.6435 | 113.452 | 178.166 | 659.8914 | 46909.96 |
| 71860.5 | 16.275 | 0.896964 | 111.709 | 1.57322 | 283.928 | 0.193413 | 320.05 | 267.864 | 0.965601 | 186.286 | 496.075 | 0.474691 | 63.8525 | 229.262 | 66.0205 | 643.1126 | 54874.48 |
| 57428.3 | 15.8232 | 0.918559 | 18.0963 | 0.545766 | 489.204 | 0.202606 | 245.217 | 138.583 | 0.95384 | 284.351 | 745.347 | 0.845374 | 25.4098 | 95.9043 | 271.606 | 434.9803 | 45491.3 |
| 105527 | 16.7166 | 0.846587 | 32.6323 | 3.66811 | 169.024 | 0.232322 | 431.544 | 190.561 | 0.793324 | 177.021 | 80.6953 | 0.469422 | 131.462 | 91.5166 | 105.171 | 648.0555 | 44407.59 |
| 43921.3 | 13.0884 | 0.938768 | 129.762 | 0.699996 | 555.15 | 0.409108 | 383.266 | 360.355 | 0.783076 | 393.922 | 70.0678 | 0.26716 | 21.0273 | 172.891 | 118.547 | 701.1396 | 70560.55 |
| 199282 | 31.1491 | 0.706308 | 115.318 | 0.961476 | 418.278 | 0.3013 | 248.241 | 721.611 | 0.851122 | 351.051 | 37.3779 | 0.882878 | 58.3211 | 99.2065 | 317.254 | 575.0597 | 35993.91 |
| 100889 | 26.4512 | 0.853535 | 170.477 | 2.61712 | 875.925 | 0.595221 | 162.826 | 60.9418 | 0.733768 | 78.1067 | 305.853 | 0.2257 | 40.9298 | 148.148 | 64.4541 | 819.11 | 69564.5 |
| 45622.5 | 16.4536 | 0.936225 | 103.937 | 0.165457 | 250.346 | 0.491264 | 207.61 | 983.748 | 0.917105 | 230.13 | 59.8051 | 0.889414 | 9.56471 | 167.896 | 213.579 | 200.1443 | 13893.7 |
| 95532.4 | 19.3228 | 0.861544 | 128.865 | 2.07867 | 478.447 | 0.472857 | 466.362 | 486.654 | 0.959625 | 394.624 | 287.01 | 0.305417 | 96.9639 | 180.067 | 185.729 | 582.6394 | 44000.17 |
| 32598 | 30.8436 | 0.955727 | 96.2792 | 1.7495 | 407.118 | 0.370942 | 495.122 | 676.564 | 0.532432 | 303.286 | 472.311 | 0.957132 | 99.2799 | 359.666 | 271.883 | 290.8358 | 27522.77 |
| 186843 | 29.7463 | 0.724921 | 169.173 | 1.19806 | 287.26 | 0.413808 | 70.3504 | 778.843 | 0.559705 | 165.58 | 678.668 | 0.927164 | 78.1053 | 45.6273 | 47.1973 | 664.7723 | 36024.46 |
| 134147 | 30.4423 | 0.803773 | 115.629 | 2.23876 | 142.193 | 0.282996 | 461.629 | 845.974 | 0.667405 | 93.6043 | 559.325 | 0.511268 | 138.407 | 244.627 | 65.6214 | 867.3019 | 49848.64 |
| 134391 | 33.1572 | 0.803411 | 39.828 | 1.64771 | 644.466 | 0.544173 | 471.721 | 780.565 | 0.613457 | 477.661 | 134.772 | 0.386371 | 33.3119 | 60.3923 | 254.925 | 756.2795 | 53946.11 |
| 102721 | 13.7861 | 0.850785 | 96.136 | 1.12805 | 636.421 | 0.430055 | 99.2738 | 80.8628 | 0.980113 | 466.103 | 412.591 | 0.406478 | 47.7893 | 56.5186 | 432.601 | 415.1842 | 37655.83 |
| 50688.8 | 16.9979 | 0.928644 | 165.535 | 3.02732 | 980.555 | 0.600355 | 251.11 | 593.159 | 0.520726 | 286.301 | 454.959 | 0.774656 | 57.6966 | 240.461 | 257.571 | 321.2369 | 28133.76 |
| 85297.2 | 30.6567 | 0.87687 | 105.808 | 1.58905 | 546.968 | 0.204922 | 348.757 | 903.437 | 0.394537 | 191.54 | 41.7122 | 0.987175 | 111.18 | 318.768 | 160.615 | 883.0734 | 88141.84 |
| 78318.9 | 21.8087 | 0.887304 | 35.8232 | 1.99112 | 540.755 | 0.412865 | 249.865 | 546.456 | 0.710657 | 329.145 | 40.0666 | 0.444847 | 146.041 | 186.092 | 297.392 | 507.3071 | 45562.8 |
| 60619.2 | 33.4523 | 0.913801 | 47.3325 | 3.65553 | 536.969 | 0.292727 | 221.386 | 853.508 | 0.853539 | 481.078 | 264.726 | 0.839292 | 126.853 | 111.539 | 463.267 | 352.0102 | 33114.08 |
| 81463.6 | 20.507 | 0.882597 | 135.942 | 0.6892 | 404.888 | 0.63051 | 190.404 | 271.969 | 0.219537 | 286.419 | 499.982 | 0.501805 | 42.4557 | 176.9 | 131.207 | 899.7784 | 61365.58 |
| 107380 | 29.9176 | 0.843825 | 47.5056 | 1.88347 | 251.197 | 0.442568 | 485.25 | 662.641 | 0.819394 | 443.212 | 367.363 | 0.862831 | 163.278 | 245.154 | 394.433 | 268.5076 | 17086.88 |
| 156048 | 27.9915 | 0.770999 | 155.162 | 1.51766 | 224.517 | 0.527283 | 125.438 | 658.24 | 0.428525 | 96.0678 | 730.231 | 0.713419 | 65.044 | 109.323 | 82.102 | 685.8223 | 37174.59 |
| 113246 | 24.6109 | 0.835043 | 156.169 | 2.81623 | 64.0697 | 0.359101 | 315.238 | 972.844 | 0.646312 | 62.8973 | 718.547 | 0.381801 | 19.9366 | 180.198 | 55.8888 | 961.7684 | 51525.05 |
| 97770.5 | 19.3242 | 0.858195 | 27.2342 | 0.767707 | 613.234 | 0.495214 | 323.823 | 965.552 | 0.424922 | 274.312 | 469.676 | 0.896448 | 35.6153 | 265.078 | 49.975 | 425.4709 | 33847.95 |
| 30935.4 | 23.7313 | 0.958207 | 29.9316 | 2.72119 | 61.9607 | 0.217403 | 262.267 | 698.471 | 0.621191 | 66.6269 | 251.967 | 0.412768 | 137.004 | 84.7883 | 60.7168 | 659.7802 | 47744.29 |
| 83662.6 | 17.8259 | 0.879305 | 106.51 | 1.44984 | 720.074 | 0.450779 | 363.582 | 54.8048 | 0.16996 | 435.408 | 902.247 | 0.916842 | 96.6037 | 198.675 | 352.304 | 926.1184 | 91943.69 |
| 46512.7 | 13.3455 | 0.934891 | 41.6987 | 0.389711 | 607.187 | 0.449401 | 309.783 | 791.868 | 0.800858 | 324.739 | 922.493 | 0.56543 | 31.4296 | 272.656 | 114.778 | 395.2532 | 34302.22 |
| 110169 | 22.5394 | 0.839645 | 52.5325 | 3.1623 | 680.49 | 0.402003 | 448.081 | 666.619 | 0.330637 | 356.488 | 439.514 | 0.644498 | 34.0668 | 91.4143 | 53.7999 | 905.4477 | 82345.58 |
| 48567.3 | 22.1082 | 0.931822 | 52.2984 | 0.906508 | 24.3826 | 0.475456 | 241.884 | 749.729 | 0.767331 | 484.263 | 798.897 | 0.228624 | 27.0522 | 166.764 | 82.7775 | 699.7454 | 40509.65 |
| 162935 | 16.5166 | 0.760686 | 76.1173 | 2.47993 | 735.522 | 0.368826 | 190.501 | 57.4212 | 0.999357 | 153.72 | 747.213 | 0.472463 | 126.881 | 43.9638 | 79.8797 | 554.0022 | 46537.9 |
| 161565 | 25.6021 | 0.762741 | 82.6022 | 1.50328 | 170.737 | 0.449996 | 256.827 | 883.278 | 0.456122 | 334.446 | 445.119 | 0.728834 | 3.93356 | 185.224 | 299.113 | 614.2757 | 33558.9 |
| 159891 | 27.0598 | 0.765247 | 115.894 | 0.527262 | 935.456 | 0.497039 | 224.69 | 200.362 | 0.844916 | 288.311 | 12.3354 | 0.591523 | 32.0162 | 214.936 | 228.83 | 440.959 | 35487.47 |
| 52933.1 | 13.6477 | 0.925284 | 137.095 | 1.54342 | 137.414 | 0.118643 | 416.384 | 641.556 | 0.601381 | 289.459 | 624.591 | 0.893426 | 69.6567 | 375.751 | 223.824 | 935.2604 | 71811.72 |
| 88894.4 | 22.0694 | 0.871479 | 66.5134 | 0.235824 | 44.8471 | 0.501986 | 257.213 | 382.935 | 0.694793 | 451.399 | 932.47 | 0.210533 | 10.8326 | 202.182 | 47.1449 | 864.889 | 47555.57 |
| 83724.6 | 31.7579 | 0.879225 | 59.0186 | 0.770704 | 600.224 | 0.530833 | 384.389 | 778.434 | 0.499396 | 359.077 | 853.146 | 0.374427 | 69.8768 | 224.896 | 179.316 | 769.3637 | 57910.98 |
| 148727 | 33.7727 | 0.78196 | 76.9551 | 3.40694 | 558.411 | 0.560206 | 220.188 | 975.268 | 0.497215 | 386.005 | 839.585 | 0.817 | 48.6209 | 74.6401 | 271.563 | 507.2111 | 32464.99 |
| 105907 | 20.991 | 0.846021 | 89.9619 | 1.18271 | 712.057 | 0.449581 | 228.561 | 506.047 | 0.587139 | 280.674 | 756.639 | 0.897241 | 67.5332 | 101.14 | 47.6771 | 379.8485 | 32047.02 |
| 69054.4 | 27.5534 | 0.901172 | 122.996 | 2.13945 | 283.406 | 0.460873 | 222.936 | 48.4849 | 0.850852 | 474.189 | 87.2142 | 0.393313 | 132.157 | 206.949 | 458.632 | 319.8026 | 25398.82 |
| 53513.5 | 22.4967 | 0.924421 | 112.673 | 0.44931 | 125.493 | 0.13601 | 59.6972 | 552.973 | 0.483368 | 364.595 | 170.778 | 0.763523 | 38.2021 | 48.114 | 332.25 | 952.05 | 72109.19 |
| 59194.6 | 34.1433 | 0.915934 | 89.1102 | 1.54897 | 226.525 | 0.229999 | 96.7584 | 485.359 | 0.557296 | 307.622 | 447.931 | 0.963048 | 42.6945 | 50.4197 | 237.74 | 427.9408 | 34943.82 |
| 64112 | 23.6229 | 0.908563 | 103.073 | 1.87824 | 382.226 | 0.444971 | 353.891 | 390.691 | 0.355462 | 519.698 | 765.888 | 0.368336 | 157.956 | 47.3158 | 129.071 | 920.3978 | 78156.94 |
| 89493.1 | 23.855 | 0.870585 | 50.6325 | 1.6433 | 217.262 | 0.276575 | 474.304 | 897.48 | 0.712677 | 348.285 | 127.897 | 0.624725 | 143.367 | 388.783 | 246.043 | 527.7732 | 37333.94 |
| 161127 | 27.5211 | 0.763398 | 98.9046 | 0.45664 | 696.856 | 0.534582 | 181.76 | 557.5 | 0.757706 | 284.089 | 154.709 | 0.585306 | 37.839 | 114.908 | 136.857 | 477.7978 | 33112.97 |
| 182563 | 28.4467 | 0.731324 | 76.5503 | 1.55869 | 80.983 | 0.40637 | 263.835 | 276.541 | 0.373809 | 415.549 | 762.051 | 0.648249 | 56.2527 | 97.5964 | 112.596 | 910.9496 | 44430.5 |
| 62769.8 | 16.0016 | 0.910566 | 114.452 | 2.80392 | 246.425 | 0.393706 | 150.297 | 611.928 | 0.586064 | 422.832 | 107.876 | 0.289797 | 135.87 | 78.3496 | 279.296 | 790.6045 | 60859.94 |
| 185565 | 16.1147 | 0.726824 | 157.857 | 0.201069 | 578.987 | 0.460615 | 400.979 | 66.0086 | 0.582993 | 321.445 | 782.845 | 0.579834 | 6.03065 | 245.165 | 74.9315 | 874.4741 | 54606.47 |
| 86033.8 | 23.6911 | 0.875761 | 110.567 | 0.543003 | 35.9717 | 0.574949 | 485.387 | 800.65 | 0.317808 | 321.44 | 511.363 | 0.402516 | 39.9588 | 465.049 | 152.42 | 880.7508 | 47960.67 |
| 101570 | 17.4728 | 0.852509 | 156.946 | 1.7957 | 960.251 | 0.310904 | 164.383 | 7.52304 | 0.576211 | 190.545 | 383.164 | 0.67824 | 44.2731 | 63.4358 | 129.734 | 740.9979 | 79677.83 |
| 186688 | 24.5649 | 0.725148 | 39.2316 | 0.636921 | 579.55 | 0.18956 | 253.554 | 157.934 | 0.972396 | 237.909 | 924.111 | 0.769906 | 48.9899 | 131.372 | 216.141 | 913.819 | 71629.79 |
| 176105 | 29.6789 | 0.740989 | 164.138 | 0.145133 | 843.982 | 0.426113 | 223.006 | 429.567 | 0.549771 | 292.125 | 753.788 | 0.992154 | 2.93476 | 128.278 | 240.887 | 723.5906 | 49305.38 |
| 144185 | 15.9037 | 0.788742 | 36.3591 | 3.68971 | 51.1615 | 0.481291 | 392.003 | 353.24 | 0.815367 | 262.708 | 722.623 | 0.199902 | 32.8895 | 186.887 | 229.074 | 956.827 | 47972.85 |
| 170204 | 23.4406 | 0.749813 | 60.6607 | 2.74909 | 796.258 | 0.538271 | 323.883 | 860.431 | 0.607191 | 370.565 | 636.479 | 0.823382 | 64.5677 | 259.94 | 52.5909 | 445.6886 | 30765.4 |
| 94953.6 | 28.6069 | 0.862419 | 150.278 | 0.669935 | 71.0994 | 0.324828 | 156.25 | 847.24 | 0.867926 | 482.306 | 273.904 | 0.80146 | 13.5047 | 75.2082 | 325.077 | 397.4139 | 22227.66 |
| 125167 | 33.9268 | 0.817215 | 86.1517 | 1.78143 | 999.505 | 0.229233 | 356.451 | 734.587 | 0.633608 | 284.459 | 413.913 | 0.775566 | 137.93 | 176.596 | 255.759 | 929.2715 | 97833.77 |
| 145410 | 30.9546 | 0.78692 | 67.859 | 0.459587 | 187.116 | 0.483885 | 230.021 | 795.282 | 0.961277 | 222.441 | 275.922 | 0.38593 | 12.5419 | 162.437 | 118.889 | 585.7772 | 32328.88 |
| 164113 | 24.7929 | 0.758929 | 159.613 | 3.12248 | 213.779 | 0.50921 | 271.824 | 587.533 | 0.947825 | 423.624 | 914.419 | 0.326489 | 91.057 | 116.8 | 61.6338 | 760.3663 | 40753.16 |
| 120544 | 13.7053 | 0.824116 | 31.0701 | 1.82767 | 628.017 | 0.234715 | 438.92 | 132.562 | 0.896861 | 252.615 | 388.168 | 0.847005 | 42.746 | 81.5372 | 96.2368 | 459.7436 | 44478.82 |
| 31421.5 | 21.7562 | 0.957478 | 145.388 | 0.959393 | 799.351 | 0.486396 | 492.608 | 827.604 | 0.236556 | 425.669 | 540.735 | 0.784312 | 35.5503 | 444.443 | 261.138 | 692.3743 | 76483.26 |
| 62428.9 | 20.6268 | 0.911079 | 168.881 | 0.890509 | 717.931 | 0.197964 | 429.987 | 577.943 | 0.933518 | 269.453 | 551.152 | 0.559846 | 43.5028 | 131.773 | 108.367 | 863.2462 | 89735.64 |
| 199037 | 16.5332 | 0.706666 | 63.9164 | 0.961492 | 480.804 | 0.431027 | 398.649 | 456.909 | 0.429766 | 97.8636 | 18.627 | 0.921635 | 71.6977 | 92.8159 | 71.8835 | 556.6508 | 37189.47 |
| 171029 | 31.2002 | 0.748586 | 129.24 | 0.59968 | 457.867 | 0.483627 | 141.709 | 277.931 | 0.339088 | 111.197 | 185.063 | 0.977902 | 13.8463 | 95.0901 | 62.4693 | 681.2473 | 42363.51 |
| 81605.4 | 23.5504 | 0.882387 | 170.943 | 1.78328 | 618.656 | 0.172042 | 197.067 | 528.385 | 0.924904 | 219.528 | 504.424 | 0.737283 | 53.2487 | 82.0999 | 114.714 | 987.3522 | 94942.34 |
| 83617.3 | 31.0654 | 0.879385 | 67.8905 | 0.610597 | 578.179 | 0.283747 | 408.514 | 461.866 | 0.844832 | 275.347 | 79.6939 | 0.587176 | 19.8411 | 237.48 | 149.641 | 506.3213 | 49549.58 |
| 118957 | 33.613 | 0.826507 | 62.2006 | 1.95634 | 195.917 | 0.246907 | 143.254 | 953.039 | 0.671217 | 281.746 | 982.593 | 0.948535 | 110.903 | 109.841 | 161.185 | 561.7187 | 35057.44 |
| 37064.8 | 17.6511 | 0.94903 | 117.464 | 0.286409 | 152.493 | 0.593484 | 390.459 | 26.0514 | 0.28103 | 415.812 | 497.841 | 0.469638 | 20.4815 | 102.731 | 46.9369 | 526.6842 | 39220.89 |
| 168340 | 21.2097 | 0.7526 | 79.436 | 1.23616 | 253.289 | 0.503858 | 182.594 | 43.2739 | 0.882252 | 371.676 | 339.902 | 0.351255 | 113.69 | 89.3088 | 282.855 | 507.1399 | 29177.61 |
| 151866 | 28.015 | 0.777258 | 146.493 | 0.469579 | 55.8624 | 0.311857 | 164.351 | 384.277 | 0.733455 | 346.384 | 239.144 | 0.527231 | 7.31098 | 158.868 | 221.934 | 840.2736 | 41450.17 |
| 48446.3 | 14.8076 | 0.931998 | 161.309 | 0.176102 | 330.894 | 0.371457 | 214.004 | 746.489 | 0.993304 | 164.014 | 361.33 | 0.310283 | 15.2143 | 120.538 | 100.194 | 746.384 | 56407.76 |
| 61240.9 | 27.5747 | 0.912863 | 166.063 | 1.85027 | 970.082 | 0.359493 | 192.53 | 481.665 | 0.995749 | 501.894 | 958.805 | 0.662815 | 73.4354 | 151.652 | 136.794 | 444.5074 | 44134.47 |
| 119167 | 22.2356 | 0.826181 | 115.186 | 0.783098 | 994.994 | 0.521084 | 445.824 | 219.892 | 0.524502 | 517.986 | 29.1914 | 0.737607 | 37.9291 | 440.535 | 498.655 | 426.8266 | 39585.52 |
| 141924 | 31.9055 | 0.792138 | 96.9393 | 3.40609 | 311.209 | 0.497248 | 154.141 | 329.261 | 0.886601 | 142.71 | 469.144 | 0.48638 | 162.07 | 146.965 | 106.476 | 423.3443 | 25873.7 |
| 58886.1 | 19.4769 | 0.91638 | 172.344 | 1.18614 | 115.296 | 0.504193 | 192.734 | 912.301 | 0.519884 | 210.747 | 431.994 | 0.541143 | 68.7805 | 186.834 | 79.1618 | 523.2368 | 32413.94 |
| 127978 | 34.7816 | 0.81301 | 170.438 | 2.3886 | 88.5598 | 0.398898 | 452.442 | 514.559 | 0.890912 | 124.577 | 405.051 | 0.690116 | 103.835 | 175.519 | 110.912 | 415.6535 | 21965.59 |
| 187285 | 33.824 | 0.724264 | 68.8325 | 3.38876 | 239.686 | 0.656024 | 285.657 | 866.673 | 0.82381 | 215.258 | 259.26 | 0.769856 | 38.9169 | 173.581 | 121.82 | 362.0237 | 18137.4 |
| 192986 | 22.1603 | 0.715722 | 134.185 | 0.359454 | 772.437 | 0.40456 | 244.247 | 612.42 | 0.882308 | 424.303 | 568.429 | 0.513729 | 8.38444 | 115.867 | 239.9 | 810.8198 | 56166.45 |
| 111905 | 20.5296 | 0.837047 | 133.008 | 1.72993 | 395.5 | 0.187844 | 130.553 | 331.656 | 0.484763 | 504.621 | 65.5707 | 0.898648 | 127.65 | 50.6393 | 397.185 | 896.2945 | 74691.3 |
| 43269.8 | 34.0815 | 0.939763 | 140.492 | 0.628501 | 23.5086 | 0.681727 | 268.244 | 276.509 | 0.507153 | 287.961 | 424.061 | 0.994003 | 46.0476 | 225.918 | 239.383 | 192.9321 | 11627.32 |
| 192209 | 16.3991 | 0.716882 | 61.7526 | 1.16178 | 899.767 | 0.409314 | 488.263 | 269.465 | 0.605237 | 259.94 | 109.665 | 0.661091 | 22.8563 | 343.761 | 111.987 | 632.1346 | 54011.72 |
| 47057 | 16.4973 | 0.934078 | 73.3594 | 1.38355 | 71.6368 | 0.179917 | 436.631 | 466.435 | 0.6059 | 269.765 | 664.804 | 0.473078 | 33.6331 | 119.163 | 260.326 | 761.7701 | 53955.28 |
| 167829 | 21.7696 | 0.753366 | 95.2051 | 3.49198 | 384.641 | 0.249165 | 252.362 | 581.419 | 0.888861 | 292.033 | 618.222 | 0.679877 | 134.095 | 221.369 | 167.075 | 656.504 | 45265.25 |
| 93765 | 27.7314 | 0.864196 | 104.71 | 0.981233 | 196.116 | 0.305806 | 385.939 | 284.991 | 0.221338 | 513.841 | 328.511 | 0.910499 | 87.1451 | 66.1103 | 423.886 | 956.3112 | 66560.97 |
| 84524.7 | 19.5998 | 0.878016 | 94.3018 | 1.59695 | 941.988 | 0.475451 | 358.792 | 647.406 | 0.608409 | 213.493 | 466.813 | 0.575716 | 115.434 | 241.443 | 48.3547 | 492.3037 | 47525.74 |
| 32877.5 | 34.9001 | 0.955315 | 67.5806 | 0.398191 | 97.2338 | 0.510651 | 240.661 | 204.482 | 0.39086 | 175.826 | 414.299 | 0.903928 | 13.1027 | 185.107 | 166.1 | 218.26 | 15542.93 |
| 71983.8 | 25.2117 | 0.896786 | 70.5339 | 3.11356 | 421.583 | 0.420259 | 461.879 | 856.783 | 0.760601 | 508.252 | 395.592 | 0.657256 | 73.1896 | 452.48 | 337.308 | 360.0566 | 28248.75 |
| 59546.5 | 21.0894 | 0.915393 | 70.6133 | 2.02426 | 151.051 | 0.269018 | 71.2571 | 13.4983 | 0.90779 | 238.074 | 484.143 | 0.510024 | 29.6928 | 40.1036 | 139.673 | 350.5767 | 26925.84 |
| 161867 | 30.6813 | 0.762295 | 71.2526 | 0.322974 | 173.097 | 0.601306 | 453.821 | 760.511 | 0.696899 | 81.1834 | 429.802 | 0.992512 | 30.2623 | 143.131 | 51.0775 | 283.8737 | 14677.96 |
| 201098 | 22.9975 | 0.703585 | 34.7767 | 3.69181 | 616.86 | 0.367923 | 365.259 | 144.452 | 0.637408 | 369.778 | 641.818 | 0.535831 | 53.9665 | 193.382 | 361.311 | 849.6251 | 61926.97 |
| 58074.1 | 28.9259 | 0.917604 | 60.1205 | 0.987859 | 395.048 | 0.203737 | 109.256 | 210.454 | 0.856539 | 304.078 | 902.185 | 0.495654 | 6.50433 | 67.2085 | 131.671 | 667.2563 | 65233.15 |
| 145964 | 14.2532 | 0.786079 | 162.769 | 0.375536 | 741.182 | 0.357148 | 480.716 | 131.625 | 0.830404 | 514.579 | 960.271 | 0.46179 | 22.4486 | 213.585 | 395.651 | 896.8803 | 69275.98 |
| 74592.6 | 13.1053 | 0.892874 | 136.061 | 3.00265 | 361.427 | 0.477056 | 499.682 | 941.787 | 0.414763 | 493.732 | 664.742 | 0.683193 | 61.4861 | 391.7 | 311.386 | 514.3738 | 38270.61 |
| 74362.4 | 30.3677 | 0.893232 | 156.985 | 2.75326 | 9.03525 | 0.204169 | 280.82 | 690.81 | 0.841784 | 321.546 | 399.722 | 0.768732 | 125.574 | 245.827 | 188.829 | 474.1677 | 26208.51 |
| 150574 | 18.5874 | 0.779183 | 29.8056 | 2.18107 | 276.818 | 0.336533 | 335.661 | 119.892 | 0.372717 | 152.968 | 200.05 | 0.830882 | 154.152 | 295.57 | 75.6142 | 691.4884 | 45837.42 |
| 69242.9 | 19.6886 | 0.900883 | 170.977 | 0.758232 | 577.404 | 0.49681 | 239.737 | 143.512 | 0.492134 | 361.632 | 376.27 | 0.753499 | 43.6928 | 120.57 | 321.301 | 407.432 | 34620.92 |
| 109031 | 24.1546 | 0.84135 | 133.432 | 1.77947 | 867.048 | 0.527881 | 180.177 | 224.52 | 0.772273 | 384.074 | 115.275 | 0.261867 | 81.1061 | 125.875 | 356.198 | 772.3843 | 68257.1 |
| 123075 | 25.6594 | 0.820337 | 109.462 | 1.23968 | 630.414 | 0.564841 | 202.343 | 179.72 | 0.963456 | 250.149 | 745.622 | 0.960997 | 65.9114 | 88.582 | 196.043 | 219.3273 | 14897.95 |
| 195742 | 27.6859 | 0.711602 | 87.3399 | 1.43122 | 944.133 | 0.556407 | 407.33 | 533.852 | 0.46276 | 230.408 | 921.517 | 0.696228 | 18.87 | 250.583 | 116.592 | 692.9685 | 49359.45 |
| 148224 | 32.3127 | 0.782712 | 159.866 | 0.114696 | 833.709 | 0.671836 | 359.582 | 499.641 | 0.522874 | 313.798 | 414.946 | 0.443488 | 10.5388 | 150.292 | 248.731 | 894.8293 | 55640.8 |
| 100655 | 29.5072 | 0.853889 | 45.4237 | 0.475608 | 463.248 | 0.377724 | 254.375 | 889.139 | 0.899783 | 147.374 | 282.242 | 0.504488 | 8.25761 | 81.1995 | 73.8256 | 524.3734 | 39854.81 |
| 194515 | 24.4032 | 0.713436 | 117.202 | 2.68001 | 208.96 | 0.544756 | 285.643 | 917.539 | 0.293328 | 509.916 | 618.327 | 0.831592 | 34.3557 | 200.642 | 503.302 | 764.7879 | 39552.04 |
| 122671 | 28.8507 | 0.820944 | 71.8417 | 0.855677 | 710.168 | 0.382606 | 493.981 | 25.5483 | 0.885815 | 370.315 | 794.161 | 0.810026 | 14.1619 | 144.972 | 312.703 | 336.4015 | 29177.97 |
| 73780.2 | 31.5085 | 0.894105 | 74.6198 | 0.886992 | 113.4 | 0.244378 | 385.262 | 431.69 | 0.895236 | 355.876 | 85.2375 | 0.966824 | 8.94986 | 320.324 | 54.0856 | 299.4686 | 20142.89 |
| 75438.7 | 26.5436 | 0.891617 | 59.58 | 1.86907 | 143.156 | 0.326987 | 403.05 | 962.046 | 0.931392 | 447.008 | 670 | 0.811659 | 125.649 | 306.561 | 361.151 | 322.1643 | 20150.13 |
| 100533 | 31.6752 | 0.854074 | 124.508 | 2.90238 | 387.006 | 0.566632 | 440.02 | 894.861 | 0.697158 | 328.112 | 416.936 | 0.82878 | 36.637 | 417.894 | 229.406 | 296.585 | 18417.47 |
| 31951.6 | 34.5814 | 0.9567 | 162.385 | 1.22021 | 57.9119 | 0.510031 | 196.361 | 783.365 | 0.796286 | 130.375 | 636.744 | 0.874633 | 53.8124 | 146.364 | 119.958 | 226.856 | 13874.6 |
| 47203.8 | 19.0929 | 0.93386 | 58.5162 | 1.0222 | 2.79844 | 0.193151 | 213.441 | 547.79 | 0.336997 | 518.085 | 41.8101 | 0.759079 | 56.395 | 69.6047 | 398.159 | 676.3638 | 41493.22 |
| 119393 | 13.5422 | 0.825838 | 32.6466 | 0.31648 | 857.181 | 0.230204 | 143.869 | 577.183 | 0.612043 | 220.255 | 163.167 | 0.759532 | 24.2728 | 75.0858 | 82.0311 | 811.4081 | 88097.71 |
| 97993 | 30.7642 | 0.857873 | 145.485 | 0.705321 | 260.174 | 0.551792 | 248.174 | 806.946 | 0.86099 | 226.35 | 38.3343 | 0.704566 | 57.8619 | 91.635 | 93.0779 | 297.6185 | 18067.05 |
| 72690.2 | 20.278 | 0.895725 | 160.706 | 2.91979 | 24.1844 | 0.347631 | 367.439 | 812.924 | 0.731585 | 388.856 | 399.124 | 0.313745 | 89.8731 | 346.768 | 166.122 | 811.3274 | 45511.58 |
| 78781.2 | 14.1548 | 0.886607 | 36.3524 | 1.53121 | 519.486 | 0.474568 | 77.8331 | 336.671 | 0.848301 | 232.784 | 430.871 | 0.367336 | 10.1261 | 70.1249 | 175.607 | 445.4233 | 37724.2 |
| 115920 | 17.1268 | 0.831037 | 113.316 | 1.75146 | 109.416 | 0.190595 | 490.571 | 475.211 | 0.819312 | 227.379 | 964.924 | 0.454399 | 75.0074 | 152.843 | 225.25 | 965.2382 | 57500.7 |
| 82717.4 | 29.8177 | 0.88073 | 38.5278 | 1.53898 | 162.18 | 0.487618 | 432.823 | 468.983 | 0.45459 | 367.753 | 719.753 | 0.524924 | 61.8882 | 329.219 | 235.922 | 522.5535 | 33084.88 |
| 33581.1 | 33.3302 | 0.95426 | 171.379 | 0.149685 | 267.245 | 0.50511 | 146.19 | 339.078 | 0.577602 | 452.664 | 576.578 | 0.965305 | 11.1176 | 112.178 | 407.75 | 261.1047 | 19530.48 |
| 98439.1 | 17.2861 | 0.857194 | 23.264 | 0.973965 | 111.473 | 0.403125 | 193.955 | 952.958 | 0.380394 | 378.905 | 972.07 | 0.430845 | 54.1706 | 147.966 | 108.956 | 976.5636 | 57817.98 |
| 143085 | 18.9442 | 0.790389 | 127.438 | 0.807457 | 494.304 | 0.608143 | 270.169 | 686.928 | 0.841356 | 392.523 | 986.598 | 0.331401 | 62.3051 | 121.125 | 279.687 | 707.9364 | 42465.33 |
| 50463.8 | 17.8273 | 0.928981 | 108.203 | 0.223361 | 828.97 | 0.221219 | 476.381 | 196.344 | 0.469372 | 87.4969 | 309.246 | 0.909505 | 17.8312 | 425.326 | 73.9144 | 752.6271 | 94975.99 |
| 93599.5 | 25.359 | 0.864441 | 167.194 | 0.323805 | 847.499 | 0.691676 | 254.804 | 193.584 | 0.496691 | 186.535 | 660.656 | 0.560763 | 14.7034 | 120.153 | 142.363 | 507.1998 | 36887.7 |
| 132023 | 30.5575 | 0.806952 | 99.9194 | 0.516568 | 960.395 | 0.51639 | 458.373 | 671.645 | 0.622754 | 362.787 | 595.947 | 0.402885 | 6.06909 | 236.426 | 270.169 | 858.175 | 69790.41 |
| 118085 | 26.6719 | 0.827804 | 82.0902 | 1.02185 | 954.205 | 0.315389 | 353.928 | 151.229 | 0.694536 | 228.707 | 312.692 | 0.620619 | 93.2367 | 111.38 | 125.955 | 645.8401 | 69110.54 |
| 52644.2 | 30.6031 | 0.925731 | 78.9142 | 0.161911 | 14.2699 | 0.418276 | 354.708 | 84.1459 | 0.542478 | 220.661 | 942.91 | 0.705558 | 12.3826 | 218.832 | 191.461 | 326.5964 | 19332.11 |
| 115700 | 16.1351 | 0.831365 | 154.38 | 0.612293 | 821.28 | 0.663091 | 459.743 | 669.827 | 0.945775 | 444.366 | 310.885 | 0.393853 | 11.4959 | 112.503 | 222.019 | 492.682 | 33297.82 |
| 39092.3 | 32.4433 | 0.946012 | 75.499 | 0.320668 | 582.6 | 0.520698 | 252.832 | 852.198 | 0.908373 | 146.863 | 811.539 | 0.567632 | 21.1225 | 228.477 | 61.8155 | 344.0334 | 26956.86 |
| 69807.3 | 14.0635 | 0.900035 | 134.178 | 1.63483 | 524.043 | 0.277059 | 488.329 | 378.059 | 0.504446 | 407.669 | 562.829 | 0.823922 | 20.7155 | 77.4161 | 96.4074 | 586.4282 | 57298.11 |
| 193064 | 25.8573 | 0.715609 | 125.737 | 1.3366 | 902.674 | 0.565784 | 143.436 | 392.951 | 0.940101 | 264.724 | 834.719 | 0.846852 | 66.649 | 135.201 | 259.855 | 338.094 | 22470.36 |
| 145494 | 31.1887 | 0.786795 | 141.302 | 0.13221 | 279.151 | 0.545585 | 349.05 | 804.206 | 0.896326 | 177.762 | 614.455 | 0.364325 | 4.22357 | 55.0508 | 66.4949 | 806.4327 | 43974.39 |
| 74494 | 28.7034 | 0.893033 | 139.166 | 0.221343 | 278.732 | 0.340069 | 241.556 | 27.6359 | 0.469981 | 234.136 | 148.405 | 0.620778 | 1.86176 | 50.5315 | 103.35 | 669.4354 | 50838.71 |
| 73161.3 | 22.6805 | 0.895022 | 170.116 | 1.32318 | 716.494 | 0.46433 | 261.548 | 261.105 | 0.341914 | 471.477 | 764.809 | 0.95852 | 92.198 | 126.559 | 435.925 | 538.1194 | 48433.48 |
| 185264 | 14.8747 | 0.727274 | 67.4486 | 1.02422 | 452.448 | 0.547873 | 94.1846 | 403.071 | 0.658667 | 506.721 | 23.0397 | 0.396911 | 42.7327 | 82.8728 | 389.469 | 739.1509 | 43448.01 |
| 98362.4 | 26.965 | 0.857316 | 165.836 | 3.78679 | 948.173 | 0.798622 | 379.454 | 674.345 | 0.831025 | 479.682 | 959.057 | 0.608527 | 115.142 | 377.476 | 400.639 | 597.4604 | 35651.86 |
| 106095 | 25.6298 | 0.845745 | 32.2653 | 0.941417 | 48.0661 | 0.391115 | 140.245 | 993.934 | 0.740946 | 484.309 | 437.191 | 0.654643 | 72.2465 | 45.1392 | 444.077 | 420.6512 | 22543.59 |
| 194554 | 21.89 | 0.713377 | 47.3005 | 1.30011 | 109.645 | 0.468094 | 431.654 | 376.584 | 0.482824 | 311.066 | 270.031 | 0.530923 | 32.8682 | 162.75 | 237.919 | 747.5131 | 36755.39 |
| 156518 | 33.988 | 0.770303 | 154.227 | 0.338033 | 682.849 | 0.289962 | 399.043 | 137.975 | 0.641936 | 515.809 | 168.94 | 0.982091 | 1.08211 | 87.6915 | 264.294 | 730.7679 | 55183.74 |
| 50649.8 | 25.1584 | 0.928709 | 45.3104 | 1.16616 | 718.472 | 0.460345 | 374.46 | 895.769 | 0.41297 | 276.928 | 284.723 | 0.435697 | 32.8225 | 308.121 | 167.975 | 766.3276 | 78360.55 |
| 199736 | 22.1478 | 0.705623 | 80.2886 | 2.07604 | 867.114 | 0.511518 | 175.619 | 436.792 | 0.725968 | 390.794 | 815.251 | 0.59534 | 103.508 | 49.4138 | 202.316 | 563.9097 | 40231.7 |
| 52834.4 | 32.0993 | 0.925448 | 154.806 | 1.42003 | 860.205 | 0.29971 | 178.848 | 332.034 | 0.411833 | 215.867 | 459.386 | 0.867327 | 100.392 | 113.277 | 54.9376 | 708.9238 | 82524.41 |
| 46744.7 | 27.2532 | 0.934554 | 76.178 | 1.33131 | 507.74 | 0.440571 | 338.123 | 853.395 | 0.267264 | 371.332 | 895.99 | 0.72643 | 1.84585 | 310.778 | 51.8618 | 669.801 | 63917.6 |
| 143097 | 15.3306 | 0.790369 | 63.8858 | 0.814016 | 980.639 | 0.51279 | 265.627 | 171.276 | 0.459823 | 421.096 | 808.322 | 0.363675 | 46.8459 | 159.637 | 331.807 | 982.1948 | 83933.03 |
| 164510 | 31.1779 | 0.758341 | 119.984 | 1.34152 | 648.315 | 0.514465 | 187.97 | 794.571 | 0.916126 | 279.899 | 23.8272 | 0.392054 | 25.5531 | 106.383 | 121.621 | 679.8466 | 45311.48 |
| 73614.4 | 14.055 | 0.894338 | 73.1015 | 1.91873 | 430.902 | 0.377355 | 323.792 | 397.372 | 0.878895 | 394.419 | 305.635 | 0.642551 | 32.9239 | 66.8735 | 105.262 | 301.1002 | 26065.98 |
| 130222 | 25.7813 | 0.809642 | 167.084 | 0.463524 | 803.783 | 0.744387 | 455.039 | 843.348 | 0.626725 | 69.7942 | 258.425 | 0.699712 | 32.1379 | 195.311 | 68.9984 | 406.1679 | 24710.89 |
| 144654 | 18.8252 | 0.788041 | 133.835 | 1.30631 | 59.0824 | 0.351773 | 197.768 | 556.914 | 0.284587 | 203.47 | 999.814 | 0.986975 | 95.5045 | 165.754 | 148.537 | 853.6605 | 43292.31 |
| 132498 | 34.7349 | 0.806247 | 163.748 | 3.46416 | 722.833 | 0.388017 | 358.068 | 467.041 | 0.815637 | 298.279 | 346.752 | 0.816739 | 48.5178 | 342.843 | 161.022 | 426.2348 | 33994.32 |
| 121336 | 21.7568 | 0.822935 | 165.326 | 1.08837 | 262.169 | 0.24408 | 241.948 | 807.774 | 0.694426 | 502.29 | 920.877 | 0.733914 | 97.8373 | 215.98 | 361.776 | 815.7003 | 52273.85 |
| 103121 | 17.5724 | 0.850188 | 119.576 | 1.88703 | 481.808 | 0.488316 | 100.296 | 356.442 | 0.204728 | 178.827 | 774.29 | 0.679881 | 170.447 | 50.2322 | 65.4795 | 987.9262 | 77299.54 |
| 60364.1 | 18.3185 | 0.914167 | 145.871 | 1.49874 | 696.115 | 0.541086 | 491.363 | 395.532 | 0.46636 | 269.461 | 6.97073 | 0.659049 | 27.883 | 275.288 | 133.622 | 380.9946 | 36327.57 |
| 62245.9 | 21.2972 | 0.911354 | 51.6827 | 2.24139 | 383.348 | 0.525278 | 439.481 | 281.186 | 0.685666 | 453.961 | 432.506 | 0.513015 | 150.267 | 211.69 | 374.372 | 342.8783 | 25499.72 |
| 139216 | 21.5542 | 0.796181 | 51.9794 | 2.19852 | 701.124 | 0.378563 | 489.868 | 98.0511 | 0.928124 | 415.358 | 625.758 | 0.63666 | 75.3926 | 105.765 | 85.8329 | 408.0738 | 34874.54 |
| 201107 | 25.0229 | 0.703573 | 167.187 | 1.97266 | 658.02 | 0.345292 | 285.322 | 207.497 | 0.910474 | 93.3845 | 537.812 | 0.56192 | 5.36968 | 107.012 | 90.4071 | 774.5943 | 53262.31 |
| 149682 | 29.2866 | 0.780526 | 48.9524 | 0.367015 | 755.129 | 0.448169 | 306.895 | 490.179 | 0.514176 | 409.004 | 400.627 | 0.879985 | 19.7176 | 217.187 | 263.192 | 490.0686 | 39426.22 |
| 56112.3 | 24.902 | 0.920535 | 162.962 | 2.76574 | 273.51 | 0.596484 | 245.029 | 493.684 | 0.729873 | 391.779 | 449.404 | 0.494007 | 96.7238 | 99.2462 | 198.114 | 322.5576 | 21422.87 |
| 97578.1 | 13.7391 | 0.85848 | 100.026 | 0.265612 | 512.406 | 0.614611 | 480.029 | 618.762 | 0.956639 | 327.993 | 708.648 | 0.868346 | 14.6744 | 232.393 | 93.2085 | 238.1553 | 14808.13 |
| 82711.6 | 31.0296 | 0.88074 | 160.34 | 2.45961 | 484.899 | 0.222672 | 177.457 | 832.549 | 0.821032 | 191.357 | 723.558 | 0.699494 | 37.8893 | 77.4554 | 174.054 | 698.5261 | 59321.66 |
| 202998 | 23.0924 | 0.700742 | 135.551 | 1.92277 | 180.311 | 0.211663 | 420.058 | 203.486 | 0.681417 | 311.264 | 753.335 | 0.990352 | 91.425 | 265.507 | 68.9296 | 803.3239 | 43282.09 |
| 42009.9 | 15.0834 | 0.941629 | 158.689 | 1.64225 | 126.887 | 0.152829 | 493.721 | 675.22 | 0.871966 | 405.553 | 438.716 | 0.386095 | 58.6326 | 153.596 | 56.4803 | 997.1027 | 75623.48 |
| 83284.2 | 34.6826 | 0.879889 | 61.1737 | 1.531 | 340.311 | 0.202908 | 327.421 | 373.053 | 0.906019 | 324.382 | 353.346 | 0.579613 | 128.99 | 299.909 | 196.54 | 607.6888 | 51523.08 |
| 188579 | 19.1 | 0.722315 | 104.604 | 1.3212 | 206.618 | 0.322054 | 488.311 | 692.046 | 0.61713 | 357.714 | 213.965 | 0.762795 | 98.8776 | 442.594 | 100.277 | 638.0586 | 35773.07 |
| 96601.2 | 29.4254 | 0.859954 | 138.703 | 0.147796 | 939.162 | 0.504426 | 486.744 | 484.776 | 0.878676 | 278.848 | 241.912 | 0.954286 | 11.2005 | 320.824 | 143.947 | 280.2889 | 23376.44 |
| 48013.8 | 30.0457 | 0.932659 | 81.4572 | 3.08904 | 771.648 | 0.336823 | 376.511 | 183.308 | 0.77311 | 242.052 | 423.993 | 0.828232 | 164.944 | 262.376 | 105.152 | 297.0346 | 34863.81 |
| 78917 | 32.366 | 0.88642 | 136.914 | 0.957315 | 128.382 | 0.414106 | 147.964 | 229.771 | 0.977225 | 136.163 | 694.833 | 0.575329 | 11.5616 | 134.802 | 54.4479 | 324.3753 | 19887.86 |
| 168980 | 30.0681 | 0.75165 | 109.696 | 1.48865 | 962.385 | 0.539782 | 354.119 | 860.815 | 0.716364 | 202.003 | 859.514 | 0.707272 | 126.302 | 162.661 | 183.936 | 514.2426 | 36722.86 |
| 144908 | 28.7708 | 0.787669 | 147.763 | 1.53789 | 449.519 | 0.289289 | 489.884 | 277.601 | 0.791998 | 261.642 | 152.443 | 0.846109 | 95.8805 | 193.655 | 147.024 | 509.8575 | 36818.75 |
| 199904 | 25.7916 | 0.705373 | 103.475 | 1.75215 | 262.438 | 0.390942 | 119.836 | 279.661 | 0.732902 | 487.809 | 867.097 | 0.672008 | 123.04 | 92.7937 | 206.269 | 567.5825 | 31790.12 |
| 37634.8 | 24.0869 | 0.948183 | 67.827 | 1.92478 | 149.154 | 0.398129 | 312.667 | 324.431 | 0.640451 | 100.61 | 810.974 | 0.852952 | 174.127 | 145.167 | 96.1665 | 238.0916 | 17127.99 |
| 190274 | 23.5396 | 0.719782 | 114.89 | 3.71594 | 433.539 | 0.5876 | 307.17 | 114.92 | 0.97807 | 222.56 | 50.7614 | 0.785458 | 247.23 | 101.592 | 214.238 | 211.5603 | 11869.46 |
| 121334 | 19.3067 | 0.822936 | 32.2623 | 1.84074 | 854.916 | 0.365372 | 121.537 | 490.769 | 0.907592 | 321.805 | 493.211 | 0.922039 | 151.781 | 63.0147 | 167.97 | 333.6704 | 30521.4 |
| 116870 | 30.2835 | 0.829625 | 44.4559 | 0.363355 | 965.25 | 0.460904 | 256.478 | 232.751 | 0.407663 | 451.241 | 606.483 | 0.917735 | 24.2176 | 160.141 | 259.212 | 515.4276 | 49208.96 |
| 68654 | 21.798 | 0.901765 | 162.785 | 1.68907 | 283.684 | 0.641922 | 398.94 | 331.81 | 0.457369 | 474.03 | 526.242 | 0.579475 | 63.8651 | 301.619 | 188.668 | 403.5969 | 25935.56 |
| 101352 | 22.7721 | 0.852839 | 143.056 | 0.95397 | 325.129 | 0.429174 | 329.616 | 598.916 | 0.447142 | 193.714 | 433.928 | 0.75515 | 2.95525 | 294.73 | 63.3026 | 562.0358 | 38642.51 |
| 173681 | 31.6839 | 0.744618 | 37.5704 | 1.59012 | 380.748 | 0.507941 | 165.734 | 557.087 | 0.798622 | 185.96 | 888.351 | 0.417956 | 94.7936 | 151.218 | 180.891 | 678.424 | 39982.59 |
| 59748.8 | 26.8341 | 0.915095 | 147.566 | 0.758307 | 219.604 | 0.297929 | 368.737 | 807.226 | 0.710414 | 292.961 | 808.216 | 0.649309 | 60.5112 | 88.3079 | 151.534 | 548.373 | 39016.33 |
| 73923.6 | 17.7249 | 0.893877 | 121.228 | 1.00816 | 346.927 | 0.461351 | 487.114 | 963.916 | 0.727724 | 248.061 | 490.951 | 0.622686 | 31.2413 | 101.598 | 159.382 | 408.4148 | 28759.57 |
| 143017 | 28.6233 | 0.790499 | 67.8134 | 2.26463 | 105.338 | 0.253146 | 424.946 | 339.824 | 0.742295 | 350.475 | 187.366 | 0.574696 | 151.06 | 86.9624 | 231.959 | 681.7282 | 37761.09 |
| 58283.3 | 25.383 | 0.917287 | 161.019 | 1.44706 | 684.732 | 0.355207 | 145.619 | 235.58 | 0.847927 | 393.932 | 77.2547 | 0.424297 | 115.125 | 93.5075 | 109.477 | 553.7739 | 57447.28 |
| 185957 | 27.5611 | 0.726244 | 92.1766 | 0.690999 | 745.537 | 0.446195 | 315.494 | 469.231 | 0.605915 | 90.6156 | 515.643 | 0.766195 | 52.1356 | 200.316 | 45.2361 | 578.3442 | 41914.14 |
| 31313.2 | 13.1026 | 0.957634 | 80.0743 | 2.3712 | 181.038 | 0.287404 | 498.16 | 788.131 | 0.142315 | 403.058 | 657.743 | 0.895585 | 49.001 | 249.048 | 147.287 | 969.2753 | 87956.82 |
| 148576 | 21.426 | 0.782175 | 35.3072 | 2.71108 | 962.914 | 0.446601 | 197.21 | 456.674 | 0.481604 | 493.963 | 514.199 | 0.68567 | 103.724 | 45.9503 | 225.817 | 667.4749 | 59663.82 |
| 47141.4 | 28.9783 | 0.933963 | 142.51 | 2.06573 | 809.482 | 0.270726 | 68.0642 | 232.2 | 0.424928 | 347.502 | 335.983 | 0.736704 | 117.082 | 61.9315 | 156.925 | 780.1589 | 97390.67 |
| 172435 | 18.4389 | 0.746472 | 55.2323 | 0.444916 | 339.869 | 0.25854 | 468.342 | 102.401 | 0.488341 | 413.03 | 213.23 | 0.907959 | 5.06802 | 249.12 | 84.6183 | 718.5811 | 49775.75 |
| 41039.9 | 16.399 | 0.943081 | 135.747 | 0.325652 | 202.493 | 0.440109 | 409.797 | 11.1148 | 0.794052 | 386.546 | 392.112 | 0.576139 | 24.6157 | 64.2558 | 307.527 | 247.0672 | 19561.15 |
| 38485.5 | 31.3905 | 0.946918 | 70.5691 | 0.22393 | 160.061 | 0.533717 | 194.455 | 812.062 | 0.740178 | 413.065 | 143.908 | 0.667213 | 16.8913 | 183.792 | 108.502 | 237.991 | 15937.47 |
| 81932.7 | 13.0092 | 0.881891 | 48.4979 | 2.06067 | 175.892 | 0.47831 | 357.664 | 591.764 | 0.445037 | 468.971 | 980.068 | 0.46981 | 95.0139 | 166.198 | 58.9573 | 607.3722 | 38748.28 |
| 84838.1 | 28.4391 | 0.877555 | 44.6855 | 3.6721 | 409.827 | 0.251677 | 357.188 | 542.968 | 0.296701 | 214.943 | 249.688 | 0.824139 | 48.3608 | 240.985 | 193.566 | 990.5623 | 90604.56 |
| 117232 | 27.5488 | 0.82908 | 171.895 | 3.50017 | 519.5 | 0.479791 | 163.31 | 743.641 | 0.917312 | 433.683 | 393.815 | 0.746831 | 86.7587 | 124.449 | 429.167 | 344.4734 | 23604.83 |
| 107122 | 13.1266 | 0.8442 | 46.0287 | 0.560949 | 480.733 | 0.359356 | 332.243 | 124.214 | 0.603458 | 503.452 | 469.448 | 0.343592 | 42.6474 | 217.066 | 232.018 | 871.1521 | 76101.41 |
| 116929 | 26.7964 | 0.829534 | 29.0959 | 2.32774 | 910.346 | 0.461406 | 79.6242 | 937.089 | 0.749817 | 379.933 | 817.132 | 0.722611 | 70.1621 | 71.2313 | 117.462 | 465.1166 | 38409.01 |
| 53517 | 19.4811 | 0.924414 | 128.399 | 0.784362 | 368.769 | 0.402253 | 346.148 | 416.341 | 0.95428 | 285.827 | 889.084 | 0.493836 | 26.273 | 150.726 | 177.483 | 395.969 | 31128.84 |
| 47638.7 | 19.1705 | 0.933209 | 145.415 | 1.06615 | 114.197 | 0.504312 | 342.957 | 87.7479 | 0.610869 | 501.685 | 24.8598 | 0.315684 | 47.6539 | 266.598 | 165.009 | 448.1355 | 31742.59 |
| 132225 | 24.0359 | 0.806644 | 41.864 | 2.10064 | 75.6501 | 0.441557 | 136.2 | 824.15 | 0.25011 | 429.174 | 521.233 | 0.732106 | 162.148 | 55.3139 | 413.289 | 864.4029 | 45581.63 |
| 191242 | 23.9022 | 0.718333 | 90.0389 | 3.62949 | 402.364 | 0.686226 | 466.705 | 464.523 | 0.554281 | 333.053 | 832.664 | 0.927404 | 97.3397 | 404.196 | 292.988 | 523.6142 | 27259.67 |
| 178355 | 15.2872 | 0.737613 | 136.134 | 3.2305 | 948.555 | 0.434563 | 360.23 | 447.628 | 0.770927 | 374.617 | 837.43 | 0.392113 | 94.56 | 182.937 | 243.245 | 889.3114 | 72805.02 |
| 140905 | 19.909 | 0.793653 | 151.804 | 1.14759 | 563.414 | 0.428375 | 343.725 | 744.054 | 0.858479 | 349.725 | 477.058 | 0.987134 | 98.4369 | 219.783 | 181.652 | 360.188 | 24699.88 |
| 127015 | 21.1243 | 0.814437 | 53.3356 | 1.84688 | 798.256 | 0.319401 | 119.366 | 252.47 | 0.814278 | 231.893 | 310.385 | 0.428208 | 118.841 | 87.2618 | 165.16 | 773.2205 | 75428.88 |
| 201465 | 18.7726 | 0.703033 | 158.285 | 1.06276 | 612.451 | 0.559319 | 91.5663 | 379.489 | 0.493472 | 273.799 | 868.378 | 0.507572 | 51.574 | 65.545 | 66.0557 | 955.8032 | 57388.84 |
| 103295 | 18.9583 | 0.849929 | 41.4562 | 1.19398 | 45.0724 | 0.209643 | 292.653 | 790.37 | 0.407912 | 430.051 | 852.02 | 0.897071 | 84.0597 | 193.88 | 128.853 | 767.0965 | 42601.16 |
| 71475.6 | 22.26 | 0.897544 | 152.814 | 0.933403 | 381.781 | 0.436594 | 225.404 | 529.664 | 0.534098 | 503.783 | 849.666 | 0.894582 | 89.238 | 142.931 | 185.755 | 397.5322 | 29442.3 |
| 117390 | 32.3608 | 0.82885 | 52.8458 | 0.922925 | 414.779 | 0.326967 | 392.739 | 753.98 | 0.918073 | 93.8067 | 690.892 | 0.631468 | 72.5623 | 229.781 | 68.6075 | 509.9057 | 36780.57 |
| 146825 | 16.247 | 0.784792 | 125.708 | 1.41 | 116.225 | 0.474328 | 198.702 | 957.515 | 0.261094 | 458.945 | 856.036 | 0.932701 | 19.1373 | 191.179 | 409.566 | 751.4821 | 39709.69 |
| 100193 | 30.2486 | 0.854581 | 118.739 | 0.777904 | 846.438 | 0.441258 | 496.205 | 610.486 | 0.954545 | 420.193 | 274.909 | 0.305297 | 30.9684 | 118.977 | 252.695 | 792.5157 | 68908.28 |
| 97836.1 | 34.4549 | 0.858113 | 133.28 | 0.464828 | 254.632 | 0.230707 | 446.435 | 232.485 | 0.391014 | 183.187 | 340.439 | 0.991799 | 17.153 | 113.016 | 177.714 | 871.9761 | 61770.88 |
| 47550.2 | 18.7281 | 0.933341 | 163.726 | 1.6896 | 791.181 | 0.285355 | 254.085 | 784.273 | 0.721939 | 390.115 | 38.1969 | 0.525817 | 67.1408 | 44.6857 | 332.96 | 718.1452 | 80601 |
| 162666 | 14.452 | 0.761088 | 75.2968 | 1.3318 | 608.184 | 0.263587 | 400.208 | 344.498 | 0.610415 | 142.907 | 116.731 | 0.548913 | 53.6613 | 369.894 | 89.5476 | 999.3721 | 85800.86 |
| 90787.4 | 26.7085 | 0.868651 | 149.051 | 0.327445 | 743.078 | 0.48902 | 175.299 | 783.483 | 0.560005 | 197.675 | 185.986 | 0.43368 | 17.9955 | 130.861 | 89.8212 | 838.3089 | 68094.01 |
| 101796 | 15.4481 | 0.85217 | 95.0098 | 2.14551 | 37.256 | 0.396014 | 200.971 | 507.452 | 0.432445 | 469.257 | 360.052 | 0.518983 | 167.595 | 145.716 | 306.887 | 627.7217 | 34025.82 |
| 188124 | 32.1819 | 0.723007 | 62.1566 | 1.82426 | 192.855 | 0.471396 | 441.725 | 740 | 0.624619 | 140.823 | 822.822 | 0.601181 | 27.845 | 83.1969 | 125.03 | 660.7806 | 34556.94 |
| 61825.5 | 27.7296 | 0.911989 | 169.307 | 3.72821 | 206.302 | 0.635126 | 280.541 | 275.49 | 0.857722 | 265.178 | 383.869 | 0.798767 | 215.433 | 225.879 | 177.691 | 175.4729 | 10879.94 |
| 130334 | 19.8843 | 0.80947 | 120.724 | 1.65831 | 675.667 | 0.379596 | 431.392 | 397.106 | 0.773616 | 484.286 | 566.535 | 0.954387 | 93.7008 | 272.09 | 126.163 | 355.3852 | 29058.8 |
| 97672.9 | 25.386 | 0.858346 | 134.801 | 3.71399 | 112.163 | 0.447321 | 377.066 | 334.266 | 0.528526 | 414.196 | 402.007 | 0.469139 | 84.8434 | 118.948 | 335.86 | 546.4241 | 32454.11 |
| 103590 | 26.1738 | 0.849493 | 171.003 | 2.70548 | 631.019 | 0.411401 | 244.782 | 179.031 | 0.69845 | 322.121 | 50.0165 | 0.483693 | 127.158 | 209.617 | 128.041 | 591.8641 | 50560.54 |
| 38102.2 | 28.2398 | 0.947488 | 43.5452 | 1.56972 | 128.506 | 0.399521 | 336.538 | 548.098 | 0.910862 | 422.804 | 803.97 | 0.51648 | 43.4531 | 89.2278 | 370.332 | 315.6427 | 21355.02 |
| 70938.7 | 23.7764 | 0.898348 | 75.8371 | 2.09723 | 843.414 | 0.277644 | 128.569 | 809.853 | 0.644742 | 351.381 | 926.719 | 0.745454 | 85.8244 | 80.0902 | 122.375 | 639.71 | 69125.58 |
| 58366.5 | 20.5729 | 0.917158 | 66.9266 | 3.52556 | 307.141 | 0.602069 | 390.256 | 338.511 | 0.968714 | 370.187 | 104.779 | 0.927341 | 344.049 | 256.76 | 330.565 | 131.6557 | 9028.034 |
| 143899 | 16.6674 | 0.78917 | 29.9366 | 0.960848 | 973.978 | 0.185884 | 278.088 | 498.544 | 0.795042 | 246.477 | 745.779 | 0.987529 | 69.2048 | 44.5178 | 171.187 | 875.4919 | 91883.6 |
| 77751.7 | 15.6592 | 0.888148 | 34.9921 | 0.478448 | 316.659 | 0.458224 | 59.7206 | 765.643 | 0.961572 | 429.306 | 896.802 | 0.502546 | 45.3722 | 42.3715 | 360.257 | 401.7541 | 27063.31 |
| 51102.3 | 28.316 | 0.928035 | 160.085 | 0.661995 | 458.367 | 0.44246 | 468.378 | 66.9003 | 0.900614 | 364.46 | 869.805 | 0.219061 | 60.8839 | 183.62 | 317.327 | 751.0503 | 65743.67 |
| 52912.1 | 29.4373 | 0.925328 | 37.2555 | 3.43133 | 658.849 | 0.499558 | 364.01 | 885.359 | 0.448358 | 378.795 | 725.135 | 0.698008 | 95.6197 | 87.287 | 313.581 | 447.1598 | 38882.81 |
| 65979.6 | 31.4989 | 0.905778 | 70.8269 | 2.45725 | 415.61 | 0.191462 | 421.014 | 253.87 | 0.735809 | 158.925 | 810.816 | 0.688296 | 76.6853 | 201.321 | 155.809 | 631.8366 | 61131.21 |
| 169718 | 14.1278 | 0.750535 | 90.0854 | 1.59518 | 366.138 | 0.470261 | 169.766 | 509.995 | 0.378635 | 444.562 | 472.667 | 0.908277 | 132.267 | 78.1715 | 111.685 | 538.4223 | 33907.01 |
| 34022 | 13.5474 | 0.953581 | 21.7259 | 1.3839 | 55.0829 | 0.220002 | 336.342 | 223.2 | 0.670402 | 210.548 | 863.43 | 0.393203 | 119.814 | 309.144 | 140.044 | 595.072 | 42946.31 |
| 66303.3 | 30.6782 | 0.905292 | 156.19 | 1.66324 | 607.696 | 0.501841 | 382.903 | 390.561 | 0.450222 | 408.56 | 291.108 | 0.31659 | 77.4021 | 66.4202 | 286.776 | 970.8172 | 85879.19 |
| 59764.3 | 32.8526 | 0.91508 | 88.1574 | 1.37724 | 219.194 | 0.417267 | 323.466 | 231.69 | 0.706507 | 487.887 | 794.175 | 0.340127 | 109.989 | 231.629 | 176.415 | 528.3165 | 39291.06 |
| 52904.2 | 15.1886 | 0.925328 | 133.569 | 0.874317 | 776.282 | 0.512307 | 402.055 | 381.66 | 0.974368 | 312.212 | 0.491662 | 0.261362 | 24.8503 | 152.884 | 201.118 | 561.6132 | 54765.51 |
| 103924 | 28.9202 | 0.848996 | 76.3198 | 0.76905 | 576.169 | 0.170758 | 427.109 | 230.235 | 0.801919 | 406.858 | 113.128 | 0.754427 | 24.2926 | 352.143 | 206.261 | 721.6137 | 72514.09 |
| 128516 | 29.5171 | 0.812199 | 122.913 | 1.78012 | 715.165 | 0.35742 | 196.9 | 95.8455 | 0.879868 | 350.403 | 298.351 | 0.597172 | 71.2925 | 177.32 | 268.72 | 478.1143 | 42265.67 |
| 115202 | 22.4182 | 0.832114 | 36.2984 | 1.71592 | 321.772 | 0.48903 | 229.315 | 53.6723 | 0.557545 | 283.553 | 156.693 | 0.783337 | 120.738 | 148.812 | 269.405 | 287.4553 | 20110.06 |
| 68634.1 | 27.7856 | 0.901801 | 168.763 | 1.12493 | 419.35 | 0.472588 | 468.736 | 442.928 | 0.502233 | 246.655 | 327.39 | 0.831987 | 4.73289 | 241.886 | 226.498 | 383.3926 | 29744.28 |
| 131557 | 17.6342 | 0.807639 | 85.6226 | 3.32385 | 526.685 | 0.314526 | 248.377 | 984.689 | 0.404573 | 182.824 | 415.523 | 0.861931 | 48.3352 | 240.963 | 167.965 | 767.1215 | 62910.19 |
| 55425.9 | 13.8353 | 0.921554 | 64.216 | 1.29775 | 146.748 | 0.446999 | 211.156 | 45.0201 | 0.166695 | 302.683 | 142.767 | 0.621535 | 9.97313 | 92.8474 | 84.8959 | 785.9786 | 59641.04 |
| 48006.9 | 15.2874 | 0.932656 | 119.068 | 3.20415 | 74.3717 | 0.337425 | 151.632 | 997.034 | 0.694218 | 183.748 | 142.155 | 0.840486 | 109.537 | 137.508 | 82.4232 | 267.8204 | 17330.83 |
| 71296 | 22.3548 | 0.897812 | 165.41 | 2.50646 | 396.95 | 0.454803 | 203.242 | 559.718 | 0.570959 | 211.261 | 912.989 | 0.815028 | 156.676 | 177.177 | 164.102 | 391.932 | 28964.85 |
| 55428.4 | 13.3751 | 0.92155 | 97.1587 | 0.209694 | 386.285 | 0.610012 | 452.733 | 489.603 | 0.988912 | 336.626 | 377.102 | 0.186215 | 19.9729 | 78.6357 | 198.6 | 770.9183 | 52532.27 |
| 175349 | 29.4027 | 0.74212 | 139.285 | 3.65497 | 514.415 | 0.486417 | 370.125 | 858.756 | 0.471151 | 177.052 | 479.247 | 0.589301 | 25.3745 | 244.936 | 125.13 | 823.2889 | 53135.61 |
| 157091 | 20.5318 | 0.769433 | 144.961 | 3.54224 | 276.31 | 0.530388 | 433.78 | 314.631 | 0.573368 | 220.175 | 289.929 | 0.921255 | 49.782 | 128.992 | 171.137 | 316.5449 | 18441.56 |
| 43574 | 14.7833 | 0.939289 | 169.662 | 0.831661 | 511.367 | 0.559623 | 327.245 | 332.348 | 0.58619 | 298.941 | 39.4673 | 0.861744 | 62.627 | 58.1676 | 279.616 | 216.647 | 19173.43 |
| 127719 | 23.5967 | 0.813385 | 166.018 | 1.68481 | 66.4871 | 0.554623 | 150.446 | 107.686 | 0.766712 | 262.653 | 731.377 | 0.364359 | 57.3788 | 58.8321 | 238.634 | 561.4713 | 28767.55 |
| 96336.9 | 28.2056 | 0.860348 | 163.508 | 2.11704 | 574.565 | 0.635071 | 304.439 | 83.66 | 0.721359 | 95.5653 | 559.412 | 0.488306 | 104.316 | 148.904 | 89.6881 | 357.8652 | 25158.82 |
| 189892 | 14.5058 | 0.720348 | 72.5439 | 1.51485 | 784.03 | 0.520813 | 235.875 | 281.629 | 0.877179 | 195.433 | 845.08 | 0.851802 | 143.531 | 165.352 | 102.715 | 311.8268 | 20860.41 |
| 104449 | 18.5039 | 0.848202 | 87.1848 | 2.4984 | 673.784 | 0.276898 | 480.716 | 773.447 | 0.411396 | 296.261 | 594.683 | 0.726955 | 130.921 | 465.078 | 160.872 | 947.4626 | 93064.99 |
| 118197 | 33.816 | 0.827644 | 143.517 | 0.326155 | 357.665 | 0.79904 | 417.452 | 86.7638 | 0.973617 | 308.729 | 492.12 | 0.79447 | 25.9614 | 114.743 | 187.56 | 195.1236 | 10592.03 |
| 118858 | 18.1583 | 0.826641 | 133.245 | 0.994451 | 837.476 | 0.211338 | 108.326 | 712.523 | 0.841575 | 306.011 | 103.013 | 0.624099 | 84.2245 | 71.1034 | 261.466 | 924.953 | 91493.96 |
| 54786.9 | 33.8474 | 0.922529 | 97.0953 | 1.38224 | 817.248 | 0.443616 | 494.19 | 667.104 | 0.840502 | 297.617 | 359.921 | 0.759198 | 90.6361 | 451.881 | 218.913 | 286.0024 | 28040.54 |
| 81885 | 26.2378 | 0.881971 | 115.223 | 1.32488 | 304.733 | 0.23451 | 409.34 | 824.977 | 0.987416 | 301.476 | 779.761 | 0.635566 | 11.5603 | 82.6184 | 171.438 | 554.7258 | 41448.12 |
| 47857.7 | 16.5332 | 0.93288 | 94.8991 | 0.275236 | 595.611 | 0.386419 | 271.483 | 262.318 | 0.362067 | 238.291 | 319.983 | 0.750943 | 10.4297 | 235.169 | 213.824 | 543.969 | 58413.88 |
| 31798.4 | 26.3826 | 0.956918 | 64.1477 | 1.09835 | 541.391 | 0.489743 | 413.465 | 432.369 | 0.511038 | 345.844 | 141.954 | 0.819133 | 75.0309 | 223.241 | 138.833 | 226.1604 | 22115.2 |
| 76740.9 | 34.0079 | 0.889678 | 129.931 | 1.16047 | 600.979 | 0.48113 | 435.956 | 423.969 | 0.692998 | 420.32 | 185.092 | 0.800667 | 4.41932 | 216.951 | 287.339 | 288.4779 | 24613.02 |
| 37761.1 | 31.4111 | 0.948002 | 137.358 | 1.64133 | 121.531 | 0.547212 | 227.273 | 472.639 | 0.951694 | 489.972 | 74.2989 | 0.427671 | 109.852 | 186.753 | 205.612 | 255.1433 | 16963.71 |
| 93895.7 | 22.786 | 0.863996 | 86.1225 | 1.10892 | 335.987 | 0.253374 | 209.719 | 21.1458 | 0.818017 | 273.633 | 598.277 | 0.305247 | 39.4427 | 104.625 | 115.304 | 938.5424 | 79282.39 |
| 50950.9 | 29.2914 | 0.928263 | 88.3475 | 2.753 | 328.77 | 0.212365 | 453.61 | 956.592 | 0.978713 | 421.08 | 304.398 | 0.605161 | 105.292 | 368.136 | 103.312 | 500.8736 | 43782.53 |
| 97671 | 32.978 | 0.858358 | 38.4161 | 1.63216 | 924.133 | 0.341975 | 370.613 | 390.411 | 0.928169 | 70.477 | 927.826 | 0.764909 | 131.42 | 129.021 | 57.0003 | 423.982 | 40925.45 |
| 58718.5 | 32.2255 | 0.916644 | 56.9667 | 2.3961 | 465.55 | 0.36431 | 398.29 | 190.91 | 0.960112 | 51.1917 | 480.232 | 0.700947 | 125.058 | 144.692 | 47.6616 | 254.9373 | 23447.93 |
| 160168 | 20.5383 | 0.764828 | 123.539 | 1.91765 | 650.088 | 0.517054 | 381.382 | 116.107 | 0.75831 | 379.09 | 712.457 | 0.978809 | 53.1759 | 47.7895 | 163.142 | 282.6914 | 19786.35 |
| 94561.4 | 29.0382 | 0.863006 | 44.8389 | 0.212708 | 461.242 | 0.214092 | 486.89 | 575.624 | 0.671999 | 241.081 | 72.6457 | 0.562608 | 18.2478 | 438.332 | 48.4204 | 856.3872 | 78769.71 |
| 104534 | 23.4882 | 0.848078 | 158.81 | 1.33343 | 608.978 | 0.699125 | 426.014 | 954.501 | 0.901174 | 490.124 | 779.422 | 0.565122 | 28.0651 | 319.203 | 150.355 | 441.5573 | 25969.55 |
| 172320 | 24.9978 | 0.746648 | 91.5749 | 3.13428 | 533.786 | 0.503568 | 145.825 | 854.675 | 0.355661 | 316.501 | 93.3744 | 0.802458 | 144.594 | 112.579 | 270.038 | 670.0256 | 44733.3 |
| 34942.6 | 15.3751 | 0.952205 | 100.602 | 1.3708 | 156.664 | 0.19629 | 354.417 | 753.59 | 0.681985 | 488.101 | 887.811 | 0.935387 | 40.1115 | 65.7588 | 241.052 | 397.6397 | 31401.99 |
| 110990 | 15.0612 | 0.838413 | 151.709 | 1.85946 | 65.1107 | 0.371848 | 482.402 | 743.026 | 0.809066 | 262.529 | 499.404 | 0.762191 | 68.5908 | 80.5312 | 237.872 | 380.61 | 20594.36 |
| 82361.2 | 27.3603 | 0.88126 | 98.1032 | 1.32701 | 642.726 | 0.188298 | 134.019 | 487.007 | 0.985866 | 299.091 | 388.627 | 0.492807 | 83.8108 | 73.6662 | 237.068 | 838.7498 | 87792.69 |
| 133429 | 23.4618 | 0.804841 | 57.9998 | 1.49523 | 479.33 | 0.253633 | 79.551 | 273.425 | 0.720379 | 444.745 | 719.154 | 0.590292 | 42.8583 | 52.4275 | 246.354 | 771.9809 | 63056.53 |
| 159824 | 19.8759 | 0.765343 | 116.484 | 0.824748 | 157.595 | 0.481316 | 297.979 | 855.209 | 0.902877 | 270.981 | 468.795 | 0.955344 | 74.158 | 91.8467 | 106.452 | 304.7015 | 16143.69 |
| 49637.6 | 26.2992 | 0.930225 | 93.2665 | 3.09588 | 349.916 | 0.508452 | 294.815 | 972.279 | 0.439237 | 457.898 | 533.13 | 0.759099 | 63.2412 | 183.908 | 296.053 | 380.5115 | 27633.46 |
| 167017 | 22.5256 | 0.754581 | 99.3862 | 0.66441 | 290.641 | 0.528136 | 174.363 | 685.911 | 0.864998 | 292.399 | 155.576 | 0.360716 | 7.55369 | 163.834 | 245.12 | 657.7992 | 37167.71 |
| 103547 | 30.2305 | 0.849562 | 150.103 | 0.873524 | 479.014 | 0.378278 | 441.64 | 264.234 | 0.756627 | 186.604 | 794.367 | 0.370381 | 42.4671 | 290.836 | 81.1308 | 858.6997 | 65075.92 |
| 122862 | 13.1756 | 0.820648 | 75.1749 | 0.897897 | 873.707 | 0.335987 | 135.294 | 936.86 | 0.683538 | 433.997 | 420.529 | 0.651665 | 53.6494 | 50.5143 | 76.9147 | 658.6773 | 62734.62 |
| 89215.6 | 29.198 | 0.871005 | 161.494 | 2.5586 | 350.727 | 0.605746 | 348.113 | 766.105 | 0.800674 | 376.18 | 665.435 | 0.332525 | 108.604 | 57.2073 | 276.644 | 610.5411 | 37934.49 |
| 111373 | 24.1657 | 0.837845 | 88.6902 | 1.10077 | 141.409 | 0.40682 | 88.536 | 628.658 | 0.902645 | 458.098 | 321.506 | 0.325438 | 50.7445 | 82.9767 | 424.626 | 642.6881 | 37682.72 |
| 112054 | 27.6766 | 0.836829 | 92.6683 | 0.678069 | 459.913 | 0.210561 | 483.538 | 68.4725 | 0.404419 | 494.678 | 356.895 | 0.951133 | 59.9421 | 453.974 | 45.4009 | 919.0546 | 80279.25 |
| 157563 | 25.8846 | 0.76873 | 135.132 | 3.07337 | 670.068 | 0.360691 | 428.617 | 869.808 | 0.934682 | 106.582 | 527.289 | 0.777044 | 149.417 | 154.327 | 80.3016 | 474.266 | 35193.66 |
| 150558 | 23.8882 | 0.77921 | 85.7098 | 2.76186 | 992.895 | 0.519096 | 470.138 | 667.514 | 0.570714 | 442.54 | 131.649 | 0.674482 | 157.697 | 364.991 | 244.631 | 499.5836 | 41094.76 |
| 202161 | 26.999 | 0.701997 | 70.2866 | 0.114784 | 438.456 | 0.250698 | 240.085 | 579.78 | 0.599204 | 150.967 | 710.568 | 0.845281 | 2.36475 | 55.2596 | 64.8163 | 985.6951 | 63686.03 |
| 39591 | 15.213 | 0.945249 | 49.4617 | 0.811306 | 46.6452 | 0.492859 | 455.418 | 841.521 | 0.264904 | 322.754 | 968.742 | 0.873977 | 20.3224 | 441.74 | 239.179 | 422.2767 | 26301.63 |
| 189559 | 21.0822 | 0.72085 | 118.829 | 0.754035 | 189.079 | 0.556924 | 353.935 | 885.025 | 0.618067 | 343.29 | 781.984 | 0.85901 | 56.8901 | 191.853 | 167.156 | 451.8531 | 22995.33 |
| 148080 | 30.8178 | 0.782925 | 129.257 | 0.443908 | 500.54 | 0.479733 | 267.325 | 604.109 | 0.821261 | 103.216 | 789.374 | 0.910489 | 7.6043 | 81.9283 | 54.0142 | 380.9933 | 23955.99 |
| 127836 | 27.0336 | 0.813213 | 50.0937 | 1.91268 | 958.894 | 0.413418 | 405.173 | 589.734 | 0.883572 | 406.504 | 490.239 | 0.310464 | 90.0845 | 216.769 | 156.603 | 909.1265 | 82951.86 |
| 162211 | 22.8121 | 0.761773 | 160.034 | 2.07655 | 396.394 | 0.212547 | 445.598 | 178.05 | 0.707237 | 153.266 | 312.358 | 0.755238 | 120.997 | 188.304 | 99.5031 | 895.3398 | 62168.08 |
| 109659 | 27.0261 | 0.840413 | 146.938 | 0.883997 | 648.449 | 0.640931 | 308.203 | 929.532 | 0.525905 | 337.423 | 881.765 | 0.713299 | 45.5321 | 87.323 | 202.643 | 487.3303 | 31944.71 |
| 63169.6 | 15.5533 | 0.909968 | 111.767 | 1.05209 | 193.017 | 0.249797 | 460.77 | 481.138 | 0.51148 | 136.564 | 177.276 | 0.485292 | 21.2156 | 166.134 | 96.5386 | 812.8966 | 63677.93 |
| 38316.6 | 33.3949 | 0.947174 | 167.253 | 1.85342 | 328.005 | 0.363622 | 245.697 | 609.475 | 0.341193 | 261.931 | 350.042 | 0.523018 | 57.0051 | 237.721 | 75.5722 | 852.7879 | 75803.6 |
| 164247 | 34.8667 | 0.758739 | 41.541 | 0.294396 | 575.214 | 0.544495 | 132.98 | 690.612 | 0.810594 | 206.897 | 794.037 | 0.374269 | 23.0936 | 96.8656 | 73.6867 | 739.7175 | 47133.76 |
| 119115 | 15.7158 | 0.826254 | 128.944 | 0.881337 | 558.676 | 0.595985 | 380.816 | 352.49 | 0.771548 | 306.766 | 119.11 | 0.247635 | 30.8696 | 322 | 57.6334 | 738.2037 | 50834.18 |
| 41251.3 | 31.2515 | 0.94278 | 131.182 | 1.968 | 195.418 | 0.421513 | 410.523 | 931.446 | 0.797145 | 271.594 | 755.523 | 0.211085 | 79.898 | 224.265 | 87.985 | 946.522 | 66020.71 |
| 31017.7 | 24.8689 | 0.958085 | 52.7438 | 0.573272 | 483.361 | 0.464392 | 247.939 | 339.898 | 0.771758 | 167.294 | 50.1122 | 0.363755 | 28.6856 | 157.545 | 130.875 | 360.497 | 36595.12 |
| 67472.5 | 20.0032 | 0.903532 | 28.5595 | 0.917922 | 385.205 | 0.445468 | 479.197 | 261.895 | 0.19065 | 381.571 | 41.397 | 0.763596 | 11.5143 | 432.86 | 129.958 | 731.0365 | 66086.69 |
| 81258.8 | 24.5645 | 0.882907 | 82.8831 | 1.78091 | 787.233 | 0.362241 | 335.643 | 100.407 | 0.485039 | 276.12 | 910.587 | 0.866651 | 26.4939 | 107.922 | 79.3173 | 494.0327 | 51688.88 |
| 200674 | 27.9312 | 0.704223 | 137.102 | 3.16422 | 75.299 | 0.530177 | 90.0485 | 465.518 | 0.412842 | 511.159 | 795.406 | 0.755183 | 173.384 | 72.9236 | 196.781 | 659.2587 | 30792.47 |
| 148343 | 28.657 | 0.78253 | 140.649 | 1.62225 | 307.706 | 0.50702 | 373.058 | 374.127 | 0.608083 | 362.455 | 740.556 | 0.755707 | 23.9406 | 270.028 | 59.6675 | 452.0343 | 26579.55 |
| 199300 | 18.5148 | 0.706273 | 96.0339 | 1.92879 | 685.319 | 0.230832 | 197.472 | 606.52 | 0.764165 | 251.014 | 562.509 | 0.835735 | 28.9704 | 101.335 | 198.152 | 783.637 | 63263.08 |
| 122644 | 16.9249 | 0.820976 | 41.9655 | 3.60255 | 321.531 | 0.593267 | 452.407 | 278.146 | 0.845003 | 302.028 | 447.248 | 0.832271 | 146.192 | 166.867 | 193.487 | 243.1902 | 14350.71 |
| 100337 | 27.2023 | 0.854362 | 165.45 | 2.35649 | 716.248 | 0.258536 | 362.703 | 357.459 | 0.753506 | 403.413 | 923.251 | 0.673696 | 74.8134 | 264.297 | 186.863 | 747.136 | 69035.48 |
| 163317 | 32.5379 | 0.760127 | 167.181 | 1.97481 | 273.356 | 0.695636 | 416.549 | 682.781 | 0.829273 | 497.166 | 371.152 | 0.587702 | 139.32 | 185.393 | 299.872 | 403.1834 | 20751.2 |
| 98142.3 | 13.3729 | 0.857636 | 163.683 | 1.17942 | 295.189 | 0.207352 | 195.333 | 928.805 | 0.813701 | 264.443 | 201.076 | 0.674906 | 91.449 | 73.2358 | 164.908 | 755.7174 | 54502.35 |
| 148334 | 20.6784 | 0.782537 | 165.803 | 1.94061 | 20.94 | 0.302377 | 410.974 | 970.686 | 0.398484 | 498.323 | 44.7784 | 0.928323 | 64.1448 | 119.463 | 379.075 | 803.0786 | 38555.06 |
| 155601 | 20.8972 | 0.771663 | 29.5533 | 3.51036 | 27.135 | 0.448626 | 355.974 | 506.231 | 0.575175 | 345.148 | 289.426 | 0.892231 | 148.632 | 99.9927 | 130.959 | 347.0017 | 16805.35 |
| 176194 | 16.6428 | 0.740847 | 77.9563 | 1.50776 | 9.03351 | 0.23436 | 454.834 | 866.161 | 0.820459 | 471.133 | 243.547 | 0.870516 | 53.1759 | 354.314 | 451.163 | 509.7536 | 23574.77 |
| 71447.6 | 22.4734 | 0.897586 | 164.829 | 0.596984 | 258.673 | 0.605554 | 176.001 | 36.7771 | 0.796256 | 489.137 | 760.522 | 0.159864 | 17.3887 | 171.415 | 74.6162 | 862.3844 | 57794.04 |
| 53739.8 | 31.9693 | 0.924093 | 163.413 | 3.12276 | 664.894 | 0.361123 | 393.927 | 66.3274 | 0.463776 | 498.954 | 799.51 | 0.687131 | 161.094 | 126.57 | 122.727 | 582.1355 | 60833.39 |
| 136414 | 33.1193 | 0.800385 | 65.0899 | 3.01187 | 541.364 | 0.620564 | 493.164 | 798.696 | 0.931744 | 475.657 | 840.809 | 0.714211 | 209.878 | 124.249 | 128.691 | 373.699 | 21533.77 |
| 126483 | 19.1942 | 0.815232 | 127.056 | 3.58575 | 582.678 | 0.429527 | 331.589 | 475.515 | 0.702086 | 268.128 | 144.903 | 0.915281 | 113.38 | 52.2271 | 220.202 | 300.5946 | 24126.66 |
| 123304 | 17.4579 | 0.819987 | 40.9302 | 1.19017 | 889.971 | 0.329596 | 228.111 | 86.1415 | 0.531372 | 135.284 | 828.985 | 0.893011 | 31.0343 | 142.865 | 117.129 | 573.7622 | 58075.58 |
| 130772 | 16.9596 | 0.808812 | 118.128 | 3.73756 | 39.2953 | 0.420193 | 292.468 | 936.443 | 0.682937 | 479.588 | 818.422 | 0.825205 | 167.451 | 134.665 | 124.287 | 387.827 | 19822.17 |
| 132787 | 21.1215 | 0.8058 | 148.909 | 0.655718 | 982.976 | 0.32434 | 277.502 | 570.041 | 0.853344 | 339.379 | 251.302 | 0.690588 | 38.2048 | 213.328 | 120.236 | 634.8977 | 57635.78 |
| 187614 | 17.5488 | 0.723759 | 93.374 | 0.9957 | 824.49 | 0.285904 | 214.058 | 921.813 | 0.714948 | 428.105 | 833.951 | 0.820786 | 10.9097 | 125.805 | 401.637 | 757.0108 | 62290.49 |
| 58111.5 | 21.007 | 0.91754 | 48.0021 | 2.72222 | 488.168 | 0.430656 | 354.376 | 957.725 | 0.59333 | 255.333 | 870.637 | 0.455494 | 60.2707 | 163.347 | 71.5951 | 625.5786 | 52403.29 |
| 38119.7 | 32.3028 | 0.947467 | 128.158 | 0.695287 | 287.964 | 0.816504 | 380.6 | 727.178 | 0.748692 | 490.605 | 114.882 | 0.901595 | 54.8319 | 307.957 | 450.325 | 224.2631 | 13823.38 |
| 177318 | 20.0216 | 0.739165 | 63.4916 | 3.06575 | 344.343 | 0.202819 | 59.1552 | 225.747 | 0.799732 | 302.45 | 203.576 | 0.801426 | 123.701 | 49.4531 | 247.498 | 676.7302 | 46931.07 |
| 72653.1 | 28.4109 | 0.895788 | 85.87 | 2.07446 | 748.542 | 0.456445 | 296.203 | 95.4903 | 0.247947 | 304.432 | 439.948 | 0.994388 | 44.7018 | 101.499 | 63.3463 | 548.5324 | 57546.77 |
| 175137 | 32.9391 | 0.742441 | 111.269 | 0.740333 | 919.134 | 0.732572 | 339.434 | 13.9079 | 0.471729 | 324.108 | 464.643 | 0.846452 | 60.0241 | 305.582 | 218.025 | 486.6537 | 28729.54 |
| 123427 | 19.4673 | 0.819805 | 116.753 | 1.16878 | 73.6385 | 0.29094 | 182.735 | 684.032 | 0.708434 | 400.047 | 918.91 | 0.646904 | 22.3954 | 65.4352 | 311.334 | 616.7616 | 33375.71 |
| 146002 | 30.7769 | 0.786035 | 144.659 | 0.755324 | 153.043 | 0.620785 | 128.462 | 241.048 | 0.868453 | 118.332 | 493.024 | 0.600232 | 4.13663 | 101.726 | 97.2841 | 338.147 | 17531.48 |
| 107265 | 29.0423 | 0.843997 | 94.9356 | 1.67987 | 727.901 | 0.313671 | 389.942 | 930.918 | 0.388921 | 193.985 | 105.482 | 0.778278 | 39.9811 | 166.517 | 165.557 | 868.2811 | 84526.07 |
| 155774 | 20.7513 | 0.771404 | 119.63 | 2.39717 | 87.3719 | 0.227321 | 437.82 | 312.808 | 0.549732 | 278.243 | 203.6 | 0.988129 | 83.2725 | 376.33 | 269.803 | 605.7259 | 32273.75 |
| 141068 | 29.0473 | 0.793415 | 133.852 | 3.75912 | 45.1947 | 0.473093 | 297.71 | 554.072 | 0.881969 | 475.293 | 38.5101 | 0.540903 | 167.712 | 112.889 | 56.1503 | 373.4251 | 18728.96 |
| 129921 | 23.6728 | 0.81009 | 85.0162 | 1.75848 | 659.019 | 0.534787 | 140.875 | 286.358 | 0.437111 | 353.465 | 446.65 | 0.452046 | 145.465 | 102.256 | 73.5862 | 720.5516 | 51589.04 |
| 149808 | 30.9105 | 0.78034 | 134.671 | 0.550277 | 911.114 | 0.678216 | 398.539 | 133.88 | 0.268081 | 283.377 | 785.753 | 0.949617 | 23.1926 | 134.211 | 124.197 | 641.519 | 43319.3 |
| 125845 | 23.2474 | 0.81619 | 61.1335 | 2.44325 | 306.731 | 0.498241 | 419.914 | 116.054 | 0.639701 | 429.867 | 715.725 | 0.673893 | 89.3306 | 410.957 | 376.542 | 352.0497 | 22674.02 |
| 45057.5 | 14.7471 | 0.937069 | 149.909 | 3.28444 | 421.973 | 0.417127 | 413.165 | 96.9649 | 0.758505 | 273.662 | 714.451 | 0.566072 | 58.6886 | 397.678 | 243.401 | 311.5977 | 28763.81 |
| 37454.3 | 28.3849 | 0.948457 | 62.6875 | 2.2761 | 911.95 | 0.278013 | 172.76 | 9.72963 | 0.882105 | 298.676 | 709.661 | 0.524147 | 58.0015 | 114.517 | 298.489 | 497.3111 | 67965.17 |
| 84795.3 | 30.2167 | 0.877621 | 38.5025 | 3.71701 | 880.995 | 0.472915 | 298.505 | 581.489 | 0.470758 | 89.8466 | 611.819 | 0.76578 | 154.47 | 114.349 | 44.8348 | 477.8457 | 45406.91 |
| 106560 | 13.922 | 0.845041 | 60.9506 | 1.24164 | 505.516 | 0.169972 | 449.188 | 175.603 | 0.572131 | 440.229 | 636.93 | 0.932847 | 85.1255 | 270.336 | 209.028 | 778.8265 | 74987.88 |
| 154437 | 16.3519 | 0.773401 | 25.9375 | 0.407213 | 745.849 | 0.239041 | 236.491 | 152.684 | 0.749615 | 153.628 | 92.5697 | 0.578161 | 39.1976 | 224.879 | 137.181 | 864.1747 | 83300.52 |
| 84766.6 | 20.4789 | 0.877654 | 58.2491 | 1.86317 | 782.23 | 0.489099 | 87.2162 | 656.947 | 0.791241 | 152.848 | 164.035 | 0.84743 | 117.733 | 63.9004 | 122.165 | 247.1982 | 21719.41 |
| 126841 | 24.7228 | 0.8147 | 40.0955 | 1.0327 | 391.279 | 0.294531 | 193.806 | 207.758 | 0.637919 | 106.245 | 51.7393 | 0.478132 | 29.4337 | 65.9735 | 87.9123 | 796.9952 | 62654.75 |
| 87842.6 | 23.0853 | 0.873054 | 79.3824 | 3.23658 | 987.642 | 0.428573 | 134.164 | 158.285 | 0.417581 | 159.872 | 231.571 | 0.764481 | 60.7142 | 96.166 | 58.9386 | 524.6937 | 59226.8 |
| 114824 | 33.9819 | 0.832693 | 147.106 | 2.92895 | 757.188 | 0.462136 | 217.117 | 604.215 | 0.627118 | 493.245 | 123.578 | 0.799195 | 83.5039 | 184.778 | 363.97 | 410.9279 | 34140.16 |
| 88223.8 | 24.9566 | 0.872485 | 88.0781 | 1.66816 | 3.83922 | 0.373696 | 334.567 | 181.063 | 0.79744 | 78.781 | 478.156 | 0.969742 | 36.4782 | 212.968 | 52.6446 | 200.7906 | 10751.17 |
| 174912 | 30.0987 | 0.742774 | 102.283 | 1.14344 | 185.637 | 0.42003 | 491.193 | 64.7613 | 0.499533 | 255.424 | 949.254 | 0.59066 | 14.4285 | 269.43 | 109.781 | 767.1197 | 41476.96 |
| 121437 | 26.8024 | 0.822788 | 87.7272 | 0.967202 | 205.236 | 0.1553 | 231.453 | 423.999 | 0.945126 | 518.815 | 946.292 | 0.933793 | 26.9618 | 132.432 | 337.343 | 917.0912 | 60445.04 |
| 171192 | 23.9202 | 0.748336 | 85.9858 | 1.78787 | 531.364 | 0.546694 | 478.879 | 511.566 | 0.45511 | 437.035 | 340.373 | 0.777196 | 79.6863 | 76.2198 | 187.481 | 491.3202 | 31066.35 |
| 64471.1 | 30.8771 | 0.908034 | 85.4264 | 2.38345 | 962.484 | 0.315229 | 325.729 | 936.993 | 0.973326 | 405.889 | 316.585 | 0.346149 | 10.8886 | 245.924 | 213.376 | 868.5189 | 94537.97 |
| 31185 | 17.4879 | 0.957829 | 69.4133 | 1.16503 | 1.04572 | 0.411237 | 240.445 | 816.29 | 0.924399 | 149.793 | 152.371 | 0.789681 | 64.5838 | 161.033 | 146.203 | 178.0925 | 10615.63 |
| 41448.2 | 34.5565 | 0.94249 | 102.437 | 0.883639 | 780.575 | 0.500553 | 143.505 | 363.063 | 0.552511 | 375.079 | 158.026 | 0.313335 | 59.7845 | 121.885 | 61.1507 | 679.3989 | 73516.7 |
| 53400.8 | 26.3119 | 0.924594 | 161.088 | 0.646998 | 618.018 | 0.201283 | 423.721 | 263.977 | 0.835094 | 349.929 | 355.363 | 0.610027 | 58.0062 | 297.1 | 259.714 | 733.1277 | 78147.51 |
| 134766 | 26.243 | 0.802843 | 28.0627 | 1.37886 | 67.7349 | 0.423115 | 453.323 | 932.825 | 0.548406 | 392.513 | 435.592 | 0.950043 | 53.6186 | 317.362 | 150.16 | 385.7504 | 20139.59 |
| 70218.4 | 22.4886 | 0.899425 | 108.436 | 2.34877 | 50.7315 | 0.386054 | 401.773 | 991.58 | 0.198764 | 72.5907 | 169.053 | 0.768376 | 134.557 | 52.1941 | 61.2936 | 776.9108 | 46917.4 |
| 155173 | 14.9816 | 0.7723 | 40.1445 | 1.87282 | 55.8046 | 0.370972 | 357.578 | 71.6603 | 0.21453 | 338.054 | 579.787 | 0.920221 | 160.979 | 170.42 | 160.061 | 915.1108 | 45854.35 |
| 113883 | 21.8239 | 0.834087 | 141.611 | 1.01285 | 530.526 | 0.594423 | 421.929 | 57.4755 | 0.626327 | 182.135 | 443.928 | 0.742571 | 51.8174 | 68.1862 | 53.0025 | 302.0418 | 21156.17 |
| 54995.1 | 26.8629 | 0.922209 | 133.418 | 0.245819 | 110.171 | 0.34641 | 498.381 | 146.708 | 0.563561 | 217.203 | 312.883 | 0.331051 | 17.9912 | 292.607 | 212.127 | 827.0654 | 56796.84 |
| 125115 | 23.6217 | 0.817282 | 146.092 | 2.33844 | 399.325 | 0.189724 | 322.136 | 346.167 | 0.937148 | 339.661 | 791.51 | 0.530229 | 6.84566 | 152.118 | 107.023 | 943.0525 | 72602.21 |
| 110110 | 14.1293 | 0.839728 | 24.1654 | 0.250452 | 813.803 | 0.447327 | 114.555 | 155.699 | 0.717102 | 177.571 | 400.584 | 0.637078 | 14.6791 | 57.2469 | 106.468 | 378.1694 | 36223.6 |
| 171385 | 18.561 | 0.748044 | 150.802 | 1.35792 | 894.368 | 0.391149 | 338.128 | 142.737 | 0.903401 | 200.278 | 514.817 | 0.78582 | 27.0422 | 300.71 | 74.863 | 446.7712 | 35976.35 |
| 37633.2 | 19.1617 | 0.948181 | 80.8013 | 1.10709 | 763.549 | 0.26895 | 458.111 | 274.816 | 0.796023 | 259.929 | 377.652 | 0.899697 | 53.431 | 336.77 | 156.81 | 319.9181 | 40841.17 |
| 165144 | 23.2076 | 0.757384 | 32.6436 | 2.60183 | 592.668 | 0.43127 | 284.954 | 808.342 | 0.659376 | 246.983 | 352.537 | 0.96918 | 59.3798 | 47.213 | 164.535 | 394.6696 | 28166.31 |
| 48135 | 34.2826 | 0.932484 | 87.2291 | 1.43904 | 36.2583 | 0.160693 | 244.341 | 765.985 | 0.920384 | 285.794 | 499.935 | 0.763368 | 64.7091 | 47.7718 | 285.284 | 492.3805 | 30838.42 |
| 100724 | 32.2456 | 0.853789 | 123.309 | 1.49327 | 67.52 | 0.612488 | 427.177 | 109.186 | 0.866369 | 218.155 | 474.544 | 0.986846 | 123.121 | 131.842 | 87.2943 | 157.4326 | 8495.261 |
| 68227.9 | 27.051 | 0.902408 | 152.007 | 0.474064 | 471.564 | 0.630308 | 321.28 | 187.318 | 0.696058 | 333.174 | 41.8408 | 0.468453 | 2.27448 | 311.418 | 69.7859 | 328.8039 | 24950.32 |
| 138302 | 21.6433 | 0.797549 | 100.484 | 3.02762 | 64.3278 | 0.470442 | 164.187 | 292.102 | 0.312746 | 191.712 | 701.94 | 0.459306 | 132.865 | 64.9597 | 118.6 | 996.43 | 51129.74 |
| 70953.8 | 26.0708 | 0.898328 | 144.386 | 1.7826 | 34.5861 | 0.491273 | 227.362 | 430.625 | 0.941798 | 356.543 | 993.054 | 0.545394 | 105.091 | 175.874 | 50.6529 | 324.9875 | 18071.9 |
| 190451 | 30.7596 | 0.719523 | 91.1843 | 0.467412 | 472.185 | 0.638965 | 483.079 | 733.139 | 0.734939 | 384.431 | 184.6 | 0.878504 | 25.8154 | 440.457 | 90.3998 | 312.1764 | 17208.88 |
| 193052 | 29.3359 | 0.715629 | 104.125 | 1.85093 | 556.944 | 0.345612 | 151.48 | 217.08 | 0.449673 | 405.748 | 130.773 | 0.812081 | 89.2936 | 95.4888 | 68.6521 | 814.3544 | 58506.69 |
| 127384 | 32.329 | 0.813896 | 119.811 | 0.396141 | 771.953 | 0.575674 | 212.694 | 93.6106 | 0.982323 | 260.58 | 106.329 | 0.839721 | 27.191 | 133.154 | 211.706 | 200.523 | 15302.85 |
| 45213.3 | 31.9309 | 0.936852 | 134.169 | 3.45277 | 429.694 | 0.297232 | 427.06 | 111.82 | 0.714105 | 221.511 | 85.3214 | 0.503878 | 138.349 | 89.7262 | 149.244 | 450.8392 | 48031.91 |
| 49276.1 | 14.7924 | 0.930757 | 91.9314 | 0.987053 | 666.143 | 0.229747 | 201.273 | 502.169 | 0.792225 | 385.61 | 761.93 | 0.443666 | 57.1306 | 53.5983 | 77.1692 | 821.5175 | 94838.7 |
| 184912 | 29.0695 | 0.727809 | 56.3892 | 3.46083 | 256.296 | 0.545967 | 187.197 | 539.742 | 0.950855 | 87.685 | 683.602 | 0.435647 | 115.576 | 162.548 | 58.2699 | 527.5788 | 28151.91 |
| 58816.3 | 24.3539 | 0.916488 | 143.955 | 0.785595 | 857.554 | 0.3456 | 412.411 | 315.93 | 0.593064 | 336.344 | 597.046 | 0.915466 | 41.3197 | 372.497 | 71.8882 | 439.3378 | 47256.87 |
| 189164 | 28.0087 | 0.721445 | 92.5261 | 1.52398 | 248.733 | 0.636738 | 485.233 | 561.963 | 0.65939 | 394.918 | 848.756 | 0.636094 | 69.7985 | 318.209 | 388.093 | 574.0431 | 28863.63 |
| 42051.7 | 20.1677 | 0.94157 | 109.983 | 2.00917 | 346.941 | 0.374859 | 350.465 | 316.857 | 0.887394 | 140.256 | 842.843 | 0.747734 | 154.602 | 175.576 | 75.7866 | 255.5249 | 21262.4 |
| 120975 | 26.1194 | 0.823479 | 89.9171 | 2.62716 | 282.923 | 0.308722 | 423.236 | 357.137 | 0.525034 | 515.086 | 241.412 | 0.970443 | 39.6022 | 72.9133 | 279.804 | 448.1664 | 31787.08 |
| 164206 | 32.7766 | 0.758798 | 91.7665 | 1.38492 | 743.503 | 0.558224 | 137.206 | 866.778 | 0.711259 | 428.779 | 779.659 | 0.740685 | 121.178 | 74.1246 | 64.4094 | 453.2692 | 29874.18 |
| 64333.1 | 34.4826 | 0.908246 | 70.7076 | 2.37509 | 644.976 | 0.355344 | 430.877 | 189.752 | 0.49572 | 438.064 | 345.438 | 0.638926 | 133 | 423.822 | 343.089 | 542.5924 | 58048.1 |
| 113532 | 21.8871 | 0.834612 | 45.0379 | 0.296399 | 659.948 | 0.434411 | 472.545 | 830.972 | 0.896278 | 431.294 | 687.606 | 0.93222 | 14.089 | 108.22 | 294.829 | 307.603 | 23600.29 |
| 84582.4 | 22.3831 | 0.877931 | 132.423 | 1.18313 | 35.9823 | 0.722876 | 493.366 | 853.575 | 0.937128 | 477.507 | 195.838 | 0.965489 | 112.877 | 337.289 | 204.543 | 204.5858 | 10906.51 |
| 177404 | 29.3611 | 0.739045 | 141.98 | 1.33455 | 31.0535 | 0.440229 | 122.028 | 850.409 | 0.540802 | 360.964 | 823.968 | 0.509512 | 59.2897 | 73.2017 | 300.742 | 960.335 | 44734.36 |
| 148328 | 26.4401 | 0.78255 | 65.205 | 3.47491 | 566.262 | 0.192142 | 165.651 | 833 | 0.986124 | 462.76 | 892.655 | 0.570734 | 116.53 | 116.651 | 198.895 | 975.3898 | 79009.71 |
| 33655.5 | 34.5387 | 0.954151 | 104.817 | 3.23814 | 668.716 | 0.345455 | 338.343 | 742.482 | 0.544413 | 87.5061 | 20.8598 | 0.696366 | 111.866 | 110.362 | 83.2281 | 442.2266 | 51408.88 |
| 199597 | 30.8652 | 0.705837 | 167.194 | 1.53595 | 940.364 | 0.659872 | 343.275 | 256.591 | 0.630726 | 262.063 | 728.455 | 0.958359 | 147.991 | 175.355 | 243.468 | 393.6681 | 23969.21 |
| 112310 | 18.4994 | 0.836439 | 86.9524 | 1.49935 | 372.188 | 0.38866 | 216.338 | 557.076 | 0.267485 | 402.488 | 357.78 | 0.856794 | 116.486 | 212.973 | 304.784 | 742.7015 | 56780.84 |
| 36655.8 | 32.8293 | 0.949658 | 41.2849 | 1.09867 | 177.042 | 0.194708 | 277.903 | 776.981 | 0.549366 | 465.598 | 381.635 | 0.505455 | 105.152 | 227.517 | 203.599 | 793.6528 | 67775.08 |
| 103975 | 27.7957 | 0.848918 | 170.917 | 2.75119 | 506.873 | 0.487397 | 470.393 | 286.605 | 0.983207 | 152.569 | 133.253 | 0.539313 | 136.511 | 328.882 | 117.149 | 335.695 | 24859.05 |
| 174299 | 17.8573 | 0.743682 | 121.647 | 0.522068 | 533.86 | 0.426341 | 372.925 | 572.754 | 0.578972 | 454.307 | 122.32 | 0.59172 | 41.1497 | 172.829 | 150.71 | 754.5262 | 50789.39 |
| 127115 | 24.5495 | 0.81429 | 143.757 | 1.37579 | 920.042 | 0.494935 | 246.806 | 83.6291 | 0.869519 | 274.435 | 433.856 | 0.380743 | 101.316 | 206.292 | 95.7592 | 588.6333 | 50668.41 |
| 59989.7 | 26.4497 | 0.914734 | 37.6742 | 2.21713 | 66.7213 | 0.549898 | 499.975 | 527.462 | 0.885761 | 417.037 | 456.342 | 0.710579 | 31.6499 | 234.128 | 306.926 | 226.8183 | 13116.49 |
| 43198.6 | 28.0179 | 0.939862 | 97.1252 | 1.95364 | 6.85411 | 0.307446 | 430.549 | 385.428 | 0.867828 | 210.82 | 883.863 | 0.634593 | 63.0909 | 296.405 | 56.451 | 294.8083 | 17408.71 |
| 120733 | 27.7494 | 0.823843 | 138.726 | 0.629472 | 216.989 | 0.385181 | 187.45 | 778.356 | 0.406447 | 304.657 | 838.233 | 0.687812 | 47.8907 | 102.68 | 103.213 | 869.5946 | 52277.07 |
| 197637 | 28.6174 | 0.708768 | 44.9961 | 2.01062 | 227.979 | 0.352407 | 85.2631 | 168.51 | 0.797728 | 283.087 | 859.355 | 0.67555 | 127.959 | 49.1066 | 278.589 | 563.0293 | 31098.82 |
| 124406 | 23.4161 | 0.818342 | 107.619 | 0.413266 | 43.659 | 0.536266 | 465.455 | 722.087 | 0.769973 | 361.769 | 895.013 | 0.932367 | 1.381 | 361.129 | 114.73 | 299.5787 | 15333.54 |
| 95771.2 | 34.8353 | 0.861204 | 37.5081 | 1.66915 | 636.097 | 0.275809 | 405.138 | 551.25 | 0.602863 | 458.124 | 779.675 | 0.9089 | 105.348 | 190.212 | 283.661 | 562.9672 | 52309.51 |
| 54540.2 | 15.122 | 0.92288 | 87.2574 | 1.47067 | 515.96 | 0.426788 | 239.887 | 331.951 | 0.394117 | 178.122 | 349.307 | 0.589106 | 139.766 | 148.785 | 75.7753 | 519.0261 | 51840.37 |
| 115887 | 20.0764 | 0.831087 | 130.108 | 0.118647 | 537.599 | 0.220894 | 418.153 | 399.795 | 0.74994 | 465.357 | 61.0112 | 0.897391 | 4.67886 | 188.272 | 113.525 | 775.7534 | 63984.79 |
| 108077 | 31.6126 | 0.842785 | 166.79 | 1.5059 | 488.876 | 0.653418 | 199.147 | 512.49 | 0.963319 | 298.601 | 833.807 | 0.483835 | 121.754 | 72.5045 | 231.985 | 402.8282 | 24605.62 |
| 39549.8 | 25.2744 | 0.945318 | 35.0528 | 0.405258 | 300.259 | 0.303149 | 301.744 | 234.198 | 0.59241 | 261.173 | 815.685 | 0.689443 | 12.742 | 209.165 | 214.798 | 393.6602 | 36263.51 |
| 89659.6 | 26.4348 | 0.870338 | 158.824 | 0.985876 | 779.858 | 0.529411 | 247.494 | 241.167 | 0.938147 | 508.112 | 804.756 | 0.7526 | 40.7327 | 226.621 | 118.98 | 290.3356 | 22785.19 |
| 110189 | 20.9942 | 0.839615 | 135.83 | 1.40979 | 584.878 | 0.68644 | 359.549 | 311.562 | 0.994066 | 216.398 | 474.608 | 0.96298 | 14.6285 | 256.58 | 210.378 | 205.309 | 12668.34 |
| 48333.1 | 22.1698 | 0.932173 | 51.2617 | 0.355398 | 156.363 | 0.301091 | 157.54 | 990.729 | 0.536765 | 63.2071 | 95.9094 | 0.501953 | 2.54585 | 152.492 | 61.9818 | 602.7064 | 45142.13 |
| 56641.3 | 19.5114 | 0.919739 | 88.906 | 3.08412 | 214.908 | 0.149289 | 367.424 | 316.42 | 0.352533 | 383.344 | 905.032 | 0.976759 | 70.1572 | 298.754 | 117.216 | 895.3386 | 78305.06 |
| 156954 | 20.1451 | 0.769637 | 126.557 | 0.244366 | 283.155 | 0.714543 | 307.803 | 695.588 | 0.770885 | 492.11 | 159.672 | 0.620972 | 20.7511 | 68.3849 | 292.505 | 387.0262 | 19897.47 |
| 53510.3 | 24.9757 | 0.924428 | 47.2485 | 3.70483 | 302.817 | 0.3246 | 320.854 | 323.396 | 0.860461 | 368.281 | 766.718 | 0.486743 | 129.64 | 170.654 | 143.5 | 417.4041 | 35015.03 |
| 66362.6 | 27.2782 | 0.905199 | 108.504 | 1.55509 | 307.363 | 0.462951 | 436.611 | 591.291 | 0.644281 | 117.71 | 908.933 | 0.724528 | 77.0856 | 227.471 | 109.869 | 346.9187 | 24667.98 |
| 182901 | 24.0129 | 0.730815 | 111.275 | 2.36693 | 415.896 | 0.471542 | 95.1744 | 398.661 | 0.216117 | 380.198 | 243.585 | 0.922741 | 145.455 | 82.4162 | 149.292 | 954.6668 | 60633.56 |
| 120245 | 27.398 | 0.824573 | 124.883 | 1.80559 | 131.883 | 0.5693 | 403.442 | 196.582 | 0.911663 | 274.746 | 373.908 | 0.215749 | 163.118 | 302.58 | 183.276 | 654.8186 | 35768.42 |
| 85333.2 | 29.3232 | 0.876815 | 107.818 | 1.10502 | 16.4006 | 0.231578 | 287.023 | 584.078 | 0.992593 | 209.565 | 146.243 | 0.500433 | 21.8086 | 278.284 | 74.732 | 525.868 | 28677.26 |
| 147871 | 20.166 | 0.783228 | 135.944 | 2.71469 | 980.169 | 0.475765 | 205.449 | 30.7176 | 0.991171 | 291.125 | 178.838 | 0.568913 | 53.492 | 56.4692 | 165.935 | 347.193 | 31490.7 |
| 31463 | 32.4851 | 0.957428 | 101.906 | 2.67239 | 239.075 | 0.254135 | 315.035 | 82.855 | 0.860102 | 70.2057 | 338.701 | 0.44825 | 57.6075 | 202.724 | 64.7796 | 394.714 | 38518.77 |
| 40643.3 | 13.1917 | 0.943673 | 100.703 | 2.33391 | 387.108 | 0.380516 | 431.153 | 85.8543 | 0.820349 | 185.649 | 895.666 | 0.930213 | 17.8404 | 306.425 | 76.2189 | 207.9829 | 18419.49 |
| 98197.1 | 15.7467 | 0.857555 | 113.154 | 2.28688 | 723.957 | 0.467222 | 359.104 | 590.783 | 0.518422 | 423.821 | 600.526 | 0.69196 | 20.1135 | 344.871 | 205.496 | 482.7744 | 42572.76 |
| 71272.8 | 31.0493 | 0.897857 | 167.307 | 3.18864 | 358.314 | 0.49684 | 314.013 | 35.352 | 0.80534 | 211.848 | 706.482 | 0.873688 | 19.1883 | 121.971 | 130.908 | 216.2792 | 15842.7 |
| 125181 | 23.1913 | 0.817183 | 50.4234 | 1.63179 | 792.946 | 0.438609 | 285.885 | 127.924 | 0.793184 | 355.836 | 358.556 | 0.905732 | 33.755 | 259.946 | 114.728 | 272.4495 | 24530.32 |
| 105808 | 33.2026 | 0.846182 | 87.0659 | 0.937425 | 91.8568 | 0.241635 | 324.594 | 119.654 | 0.836021 | 479.629 | 389.497 | 0.695592 | 5.9651 | 143.226 | 346.252 | 442.7565 | 26283.54 |
| 104430 | 18.4828 | 0.848231 | 88.7709 | 2.60496 | 47.9863 | 0.126491 | 423.933 | 296.256 | 0.683242 | 488.721 | 575.199 | 0.703113 | 27.7011 | 310.292 | 332.773 | 885.1779 | 50268.19 |
| 108288 | 21.1527 | 0.842459 | 56.83 | 1.28633 | 669.305 | 0.375513 | 357.647 | 317.302 | 0.358797 | 477.513 | 777.857 | 0.620993 | 13.7426 | 66.6202 | 52.7038 | 904.2304 | 84422.93 |
| 195302 | 24.6357 | 0.712259 | 129.888 | 2.66357 | 364.579 | 0.467169 | 249.81 | 228.681 | 0.652266 | 256.606 | 790.362 | 0.733661 | 116.389 | 229.702 | 167.482 | 499.5271 | 29196.95 |
| 189077 | 13.439 | 0.721569 | 59.1815 | 0.966864 | 503.937 | 0.504416 | 71.1789 | 682.642 | 0.354517 | 193.416 | 996.5 | 0.679421 | 92.141 | 54.0053 | 112.988 | 831.5481 | 52665.74 |
| 86370.2 | 24.4967 | 0.875258 | 88.6054 | 1.29567 | 732.528 | 0.23418 | 72.9313 | 573.401 | 0.802312 | 99.0883 | 28.7706 | 0.590112 | 127.719 | 50.8544 | 66.1915 | 688.0347 | 74866.61 |
| 145218 | 18.3877 | 0.787198 | 72.9834 | 3.37369 | 617.202 | 0.600423 | 257.475 | 641.752 | 0.505846 | 503.727 | 892.958 | 0.597931 | 281.191 | 254.132 | 479.533 | 903.9015 | 56114.05 |
| 39831.7 | 22.0411 | 0.944894 | 167.517 | 2.57907 | 881.422 | 0.283771 | 156.145 | 194.466 | 0.941498 | 239.404 | 965.146 | 0.884601 | 14.5292 | 117.08 | 84.674 | 419.963 | 47412.4 |
| 182248 | 34.6389 | 0.731802 | 113.098 | 1.8621 | 102.279 | 0.233653 | 341.275 | 320.616 | 0.970871 | 92.5285 | 95.7388 | 0.922487 | 55.3609 | 83.5104 | 73.1301 | 623.9701 | 31751.17 |
| 34143.3 | 29.7068 | 0.953413 | 138.225 | 1.39395 | 54.5234 | 0.531087 | 157.625 | 984.965 | 0.133526 | 394.124 | 939.801 | 0.692715 | 88.9768 | 113.997 | 311.483 | 881.6964 | 58583.13 |
| 146115 | 25.9327 | 0.78586 | 30.4208 | 0.818049 | 295.73 | 0.32879 | 426.574 | 275.041 | 0.915011 | 358.958 | 893.66 | 0.699369 | 56.7328 | 269.65 | 314.713 | 440.4418 | 28419.18 |
| 47472.8 | 21.3892 | 0.933459 | 121.857 | 2.12401 | 663.245 | 0.605024 | 367.159 | 21.0221 | 0.924458 | 411.215 | 43.6852 | 0.954731 | 193.186 | 324.762 | 224.427 | 92.8076 | 8917.889 |
| 31325.5 | 32.4448 | 0.957634 | 126.462 | 1.75589 | 967.081 | 0.531756 | 224.562 | 852.074 | 0.619525 | 339.72 | 756.651 | 0.389732 | 110.741 | 143.297 | 134.706 | 605.7578 | 59408 |
| 172298 | 26.691 | 0.746682 | 126.611 | 3.36403 | 141.778 | 0.580842 | 148.223 | 246.767 | 0.274544 | 366.473 | 796.86 | 0.925156 | 156.072 | 130.205 | 166.107 | 653.3456 | 32221.41 |
| 110185 | 29.0536 | 0.839628 | 33.9616 | 1.8073 | 193.999 | 0.326981 | 456.35 | 357.869 | 0.929361 | 502.233 | 392.155 | 0.569878 | 61.2504 | 296.54 | 356.1 | 412.0037 | 26591.48 |
| 179119 | 33.4792 | 0.736483 | 163.99 | 1.50875 | 565.195 | 0.796716 | 466.006 | 921.663 | 0.857579 | 393.971 | 897.735 | 0.88203 | 128.867 | 402.116 | 144.327 | 370.2412 | 18781 |
| 79612.3 | 22.6197 | 0.885369 | 138.449 | 1.07127 | 160.742 | 0.370307 | 228.806 | 941.782 | 0.431578 | 200.486 | 386.387 | 0.933769 | 103.187 | 158.845 | 176.356 | 470.6441 | 30391.28 |
| 151336 | 28.4612 | 0.77805 | 77.7416 | 2.64815 | 286.261 | 0.261574 | 331.64 | 404.404 | 0.54879 | 123.222 | 651.842 | 0.93993 | 86.9065 | 245.685 | 100.184 | 645.312 | 42441.21 |
| 130409 | 24.5078 | 0.809362 | 107.997 | 0.429362 | 912.959 | 0.63402 | 339.962 | 317.603 | 0.671048 | 301.813 | 391.646 | 0.733317 | 41.7624 | 88.4355 | 281.521 | 324.1752 | 22504.41 |
| 177206 | 34.614 | 0.739347 | 148.189 | 0.89467 | 86.946 | 0.744862 | 316.325 | 616.826 | 0.918159 | 144.338 | 674.052 | 0.668412 | 66.131 | 56.1156 | 89.3834 | 358.4237 | 17058.51 |
| 84053.3 | 22.7366 | 0.878724 | 70.7993 | 1.29102 | 461.823 | 0.356887 | 246.846 | 418.037 | 0.605274 | 416.014 | 265.353 | 0.927973 | 98.9629 | 212.564 | 247.588 | 325.5518 | 28681.4 |
| 79780.6 | 29.5735 | 0.885124 | 105.231 | 1.81593 | 169.893 | 0.263955 | 115.315 | 258.797 | 0.697969 | 227.806 | 492.603 | 0.754814 | 71.1168 | 65.4277 | 151.318 | 410.3254 | 28939.38 |
| 35877.8 | 29.3307 | 0.950818 | 85.648 | 2.25505 | 209.556 | 0.159873 | 474.017 | 393.349 | 0.451146 | 448.909 | 900.323 | 0.958845 | 2.77589 | 326.96 | 285.753 | 617.7174 | 56897.92 |
| 180148 | 32.1102 | 0.734941 | 122.57 | 1.49521 | 193.17 | 0.215525 | 64.9113 | 305.576 | 0.834091 | 337.626 | 433.259 | 0.771727 | 75.3663 | 52.9118 | 52.1294 | 760.7135 | 42720.7 |
| 134141 | 14.0305 | 0.80377 | 162.761 | 1.58422 | 566.735 | 0.578009 | 368.997 | 915.894 | 0.584744 | 493.846 | 923.227 | 0.646807 | 57.3095 | 118.28 | 338.132 | 559.1348 | 35797.4 |
| 122266 | 16.4462 | 0.821541 | 28.488 | 3.58209 | 101.452 | 0.496342 | 453.777 | 596.392 | 0.249333 | 272.454 | 798.042 | 0.800567 | 94.6067 | 92.397 | 127.586 | 666.5551 | 36436.61 |
| 39978.4 | 28.3474 | 0.944681 | 113.76 | 0.33973 | 976.716 | 0.488879 | 196.112 | 201.309 | 0.681643 | 423.582 | 775.448 | 0.851385 | 20.5437 | 79.1894 | 217.01 | 281.8969 | 29787.55 |
| 34770.8 | 31.146 | 0.952477 | 103.181 | 0.388362 | 748.022 | 0.448881 | 374.05 | 509.132 | 0.910946 | 295.459 | 663.392 | 0.93624 | 19.8266 | 328.038 | 275.153 | 230.751 | 21747.99 |
| 133889 | 21.0468 | 0.804152 | 46.6712 | 1.92596 | 284.53 | 0.542234 | 303.534 | 101.695 | 0.923499 | 462.219 | 404.03 | 0.908563 | 42.0441 | 97.237 | 433.832 | 177.9192 | 10553.84 |
| 61183 | 31.3516 | 0.912955 | 119.361 | 3.47168 | 65.5828 | 0.597557 | 279 | 385.197 | 0.40074 | 457.182 | 737.912 | 0.854914 | 183.528 | 263.464 | 400.033 | 453.5335 | 26367.99 |
| 86096.9 | 20.2224 | 0.875664 | 135.932 | 0.142043 | 138.087 | 0.489403 | 138.511 | 161.998 | 0.513799 | 131.562 | 985.221 | 0.990676 | 2.39899 | 53.592 | 88.9227 | 349.0637 | 20671.05 |
| 57270.8 | 24.3894 | 0.918801 | 170.975 | 0.948218 | 632.998 | 0.287413 | 134.453 | 292.2 | 0.673936 | 485.202 | 636.727 | 0.895577 | 16.0914 | 110.815 | 476.096 | 468.1171 | 46089.42 |
| 122931 | 19.1125 | 0.820547 | 83.5029 | 0.914879 | 548.98 | 0.461522 | 498.971 | 359.705 | 0.529007 | 377.678 | 323.203 | 0.782767 | 8.15331 | 74.9139 | 203.516 | 408.4751 | 32284.73 |
| 48202.4 | 19.5169 | 0.932366 | 76.9471 | 0.816273 | 326.785 | 0.252632 | 424.419 | 788.335 | 0.30784 | 223.229 | 57.3823 | 0.841217 | 79.9662 | 299.821 | 161.441 | 710.4378 | 69943.05 |
| 115346 | 23.6817 | 0.8319 | 68.0499 | 1.12021 | 260.379 | 0.425823 | 186.007 | 763.827 | 0.56666 | 89.4165 | 422.523 | 0.875653 | 65.5296 | 99.622 | 50.3201 | 376.9498 | 24358.57 |
| 91602.2 | 13.4932 | 0.867422 | 99.2876 | 2.20793 | 613.108 | 0.492876 | 269.175 | 70.1099 | 0.800597 | 333.886 | 274.186 | 0.511462 | 125.98 | 127.402 | 86.8096 | 295.9333 | 25670.67 |
| 98600 | 24.372 | 0.856958 | 134.653 | 0.804317 | 94.1385 | 0.442047 | 441.344 | 314.081 | 0.805132 | 421.128 | 632.357 | 0.984998 | 44.5345 | 317.28 | 234.593 | 246.37 | 13942.39 |
| 149030 | 14.5299 | 0.781492 | 139.056 | 0.211637 | 931.325 | 0.678827 | 78.6128 | 3.70119 | 0.721246 | 290.812 | 551.584 | 0.311242 | 7.28587 | 72.623 | 83.5704 | 689.5788 | 47753.76 |
| 50696.7 | 27.6126 | 0.928641 | 129.047 | 1.92275 | 103.842 | 0.561649 | 319.596 | 298.441 | 0.307084 | 260.509 | 426.55 | 0.62104 | 74.7849 | 71.0798 | 191.188 | 455.3185 | 29410.41 |
| 31176.7 | 13.3657 | 0.957838 | 170.021 | 0.986417 | 27.421 | 0.575246 | 377.861 | 929.889 | 0.667105 | 212.523 | 907.882 | 0.585995 | 12.6376 | 160.288 | 62.2952 | 362.2068 | 21592.23 |
| 50651.4 | 19.9093 | 0.928702 | 135.517 | 1.15828 | 825.686 | 0.531999 | 473.491 | 717.16 | 0.697103 | 491.843 | 36.5978 | 0.842325 | 15.9837 | 299.44 | 372.946 | 241.3723 | 23244.48 |
| 34555.3 | 14.3246 | 0.952784 | 100.821 | 0.382794 | 766.213 | 0.340894 | 274.564 | 663.593 | 0.608569 | 400.711 | 519.759 | 0.440026 | 21.3389 | 191.638 | 171.999 | 740.174 | 85615.77 |
| 144465 | 13.531 | 0.788321 | 47.1114 | 0.487238 | 438.414 | 0.262286 | 154.276 | 465.494 | 0.846667 | 273.896 | 276.554 | 0.835835 | 33.7657 | 137.284 | 183.024 | 453.4585 | 35334.44 |
| 115674 | 18.9898 | 0.831406 | 137.217 | 0.21748 | 439.956 | 0.514951 | 116.863 | 768.6 | 0.735641 | 398.272 | 966.745 | 0.815427 | 12.0268 | 63.3139 | 82.2805 | 412.8427 | 26053.27 |
| 156120 | 23.562 | 0.770888 | 128.233 | 1.15892 | 281.135 | 0.594052 | 201.409 | 618.367 | 0.696767 | 260.135 | 392.262 | 0.327441 | 22.4562 | 120.611 | 159.042 | 776.984 | 42951.35 |
| 106806 | 23.8354 | 0.844678 | 154.546 | 1.43084 | 132.066 | 0.241539 | 123.07 | 990.552 | 0.947615 | 363.601 | 689.603 | 0.786142 | 73.723 | 73.5756 | 132.102 | 599.3532 | 35046.2 |
| 148209 | 20.7677 | 0.782723 | 24.7439 | 2.53055 | 180.403 | 0.147674 | 233.847 | 632.053 | 0.716271 | 340 | 215.353 | 0.770539 | 36.0872 | 68.2315 | 288.91 | 927.8571 | 58226.02 |
| 125838 | 29.9854 | 0.816206 | 167.819 | 1.32371 | 799.866 | 0.428476 | 351.361 | 930.547 | 0.702422 | 176.859 | 788.674 | 0.838288 | 115.733 | 154.364 | 92.9156 | 536.5721 | 40264.17 |
| 86318.5 | 20.507 | 0.875332 | 167.22 | 2.9155 | 223.156 | 0.493774 | 184.392 | 604.167 | 0.61596 | 196.996 | 158.039 | 0.990284 | 10.6648 | 151.963 | 49.0573 | 248.7214 | 16160.79 |
| 31959 | 21.8833 | 0.956674 | 166.105 | 0.399409 | 654.877 | 0.618708 | 373.782 | 307.228 | 0.544032 | 166.686 | 728.053 | 0.686301 | 27.3248 | 68.8729 | 148.528 | 314.7391 | 27303.23 |
| 144513 | 17.18 | 0.788252 | 167.692 | 2.20802 | 376.982 | 0.40602 | 93.2638 | 634.689 | 0.940781 | 196.042 | 786.754 | 0.761029 | 148.854 | 64.2124 | 49.0743 | 425.3177 | 26439.1 |
| 106244 | 31.6563 | 0.845527 | 60.5421 | 2.58387 | 724.392 | 0.207815 | 405.636 | 485.612 | 0.681889 | 62.1671 | 386.552 | 0.993771 | 148.035 | 58.0689 | 46.4593 | 628.975 | 63800.34 |
| 42992.8 | 17.9743 | 0.94016 | 77.6148 | 2.37959 | 824.227 | 0.353857 | 91.4632 | 683.44 | 0.775903 | 232.502 | 83.4523 | 0.964519 | 52.003 | 48.7044 | 211.269 | 257.9402 | 30216.61 |
| 37555 | 34.1704 | 0.948315 | 106.921 | 0.843326 | 107.905 | 0.448068 | 474.075 | 344.727 | 0.865595 | 377.717 | 306.723 | 0.366315 | 48.8551 | 277.067 | 56.1328 | 342.4867 | 23811.11 |
| 101022 | 23.1393 | 0.853333 | 61.5349 | 1.85793 | 735.725 | 0.195087 | 375.928 | 942.71 | 0.76644 | 455.153 | 748.574 | 0.899088 | 46.4034 | 83.7332 | 256.861 | 700.6265 | 70499.17 |
| 154565 | 16.9177 | 0.77321 | 106.162 | 1.87908 | 759.748 | 0.386143 | 57.8438 | 326.853 | 0.421324 | 373.018 | 48.3773 | 0.612548 | 30.6302 | 51.3707 | 280.215 | 885.1433 | 78119.13 |
| 81827.1 | 27.5231 | 0.882059 | 144.313 | 1.62561 | 415.48 | 0.548172 | 416.767 | 682.108 | 0.771698 | 503.169 | 382.274 | 0.86148 | 65.6207 | 308.592 | 332.437 | 248.586 | 17167.4 |
| 35287 | 18.0954 | 0.951691 | 124.48 | 0.349 | 895.842 | 0.46261 | 308.27 | 294.181 | 0.327684 | 388.722 | 137.408 | 0.544317 | 10.1247 | 279.545 | 189.307 | 730.5758 | 88728.71 |
| 61398.9 | 23.0324 | 0.912623 | 101.13 | 3.28112 | 110.687 | 0.471773 | 163.907 | 544.317 | 0.351062 | 490.157 | 186.635 | 0.692658 | 175.056 | 159.091 | 239.512 | 399.0273 | 26244.96 |
| 43156.7 | 23.9826 | 0.93992 | 80.2403 | 2.24836 | 947.757 | 0.38208 | 103.722 | 69.339 | 0.434961 | 433.753 | 387.297 | 0.756186 | 154.594 | 89.0684 | 80.9001 | 470.1202 | 62273.29 |
| 172932 | 21.705 | 0.74573 | 103.258 | 2.53763 | 406.831 | 0.265543 | 394.634 | 309.775 | 0.890198 | 67.8845 | 2.42885 | 0.589531 | 148.93 | 140.04 | 52.5397 | 658.2443 | 46991.06 |
| 78188.3 | 31.8565 | 0.887509 | 168.955 | 0.784605 | 702.52 | 0.681558 | 159.001 | 769.057 | 0.590358 | 424.053 | 350.082 | 0.718434 | 37.6082 | 146.321 | 372.934 | 353.5566 | 24828.88 |
| 74473.2 | 24.6542 | 0.89306 | 139.091 | 3.35976 | 277.717 | 0.393527 | 372.218 | 46.1776 | 0.975753 | 243.281 | 255.234 | 0.76744 | 61.6499 | 250.732 | 96.9362 | 189.5532 | 14872.73 |
| 43126.4 | 32.7815 | 0.939976 | 117.83 | 2.0958 | 639.417 | 0.42152 | 101.15 | 146.802 | 0.529322 | 54.0195 | 955.292 | 0.991488 | 104.498 | 73.0524 | 50.3032 | 304.8658 | 30204.81 |
| 151925 | 30.1599 | 0.777171 | 107.591 | 2.71894 | 200.504 | 0.584153 | 186.202 | 179.402 | 0.606223 | 279.092 | 685.336 | 0.90155 | 92.1588 | 139.326 | 93.989 | 304.3865 | 16078.15 |
| 49215 | 14.5445 | 0.930848 | 108.101 | 0.105576 | 423.094 | 0.61021 | 77.35 | 371.174 | 0.951033 | 495.847 | 854.019 | 0.971593 | 9.91761 | 43.4132 | 202.254 | 195.6289 | 13335.23 |
| 59901.6 | 29.7083 | 0.91487 | 141.804 | 0.976196 | 792.816 | 0.773196 | 285.449 | 575.089 | 0.85128 | 301.896 | 860.287 | 0.936325 | 38.1425 | 223.765 | 291.44 | 261.234 | 16369.12 |
| 131462 | 31.874 | 0.807793 | 144.378 | 3.52701 | 9.78745 | 0.471877 | 468.894 | 292.695 | 0.871415 | 195.839 | 315.392 | 0.945073 | 150.043 | 242.135 | 96.2963 | 215.4441 | 10670.87 |
| 92158 | 14.6309 | 0.866591 | 23.6272 | 1.03561 | 404.984 | 0.484858 | 344.783 | 55.8063 | 0.976287 | 186.67 | 282.181 | 0.850309 | 47.8294 | 159.647 | 65.2885 | 151.4194 | 11817.61 |
| 179166 | 30.7026 | 0.736409 | 121.972 | 3.15121 | 746.454 | 0.473034 | 145.529 | 825.459 | 0.855276 | 321.919 | 691.972 | 0.914738 | 23.0581 | 107.856 | 45.7775 | 384.1112 | 26411.88 |
| 50854.2 | 26.9617 | 0.928405 | 131.515 | 0.51967 | 411.285 | 0.440443 | 491.334 | 946.2 | 0.176604 | 456.465 | 898.085 | 0.895408 | 50.6467 | 60.3573 | 140.541 | 896.2507 | 76778.24 |
| 34360.5 | 15.0948 | 0.953075 | 141.392 | 3.69549 | 307.476 | 0.451869 | 199.798 | 999.765 | 0.424326 | 491.669 | 688.2 | 0.947603 | 174.06 | 165.856 | 215.637 | 330.7171 | 26269.55 |
| 150864 | 19.7388 | 0.77875 | 57.9927 | 2.74378 | 434.438 | 0.604305 | 213.301 | 52.0538 | 0.994933 | 416.967 | 366.311 | 0.866841 | 108.684 | 206.173 | 330.545 | 188.4921 | 11292.78 |
| 88339.7 | 22.7555 | 0.87231 | 90.7561 | 1.37774 | 347.748 | 0.368294 | 97.388 | 742.109 | 0.338409 | 316.805 | 601.714 | 0.794949 | 58.5639 | 73.5729 | 182.69 | 651.6998 | 51234.94 |
| 125865 | 16.4817 | 0.816155 | 81.6704 | 2.05219 | 52.0464 | 0.326607 | 349.3 | 596.721 | 0.884788 | 250.458 | 311.92 | 0.489334 | 140.272 | 316.786 | 229.72 | 505.1302 | 26692.21 |
| 70597.3 | 33.0452 | 0.89887 | 142.509 | 3.6374 | 436.11 | 0.308103 | 280.056 | 337.177 | 0.983268 | 347.81 | 236.082 | 0.391396 | 138.947 | 88.7612 | 312.807 | 559.3209 | 49743.76 |
| 50628.5 | 19.1489 | 0.928736 | 169.64 | 1.8659 | 325.99 | 0.183031 | 299.778 | 984.06 | 0.926605 | 365.951 | 472.775 | 0.812277 | 68.064 | 195.99 | 279.183 | 691.5157 | 58323.99 |
| 139560 | 16.9227 | 0.795663 | 109.829 | 1.85238 | 23.2429 | 0.451197 | 302.789 | 549.504 | 0.940131 | 207.034 | 894.587 | 0.415945 | 148.852 | 60.8559 | 86.0976 | 519.1373 | 25678.13 |
| 78263.4 | 27.4688 | 0.887392 | 159.552 | 0.665216 | 7.66267 | 0.596762 | 180.905 | 106.57 | 0.470197 | 504.32 | 96.6787 | 0.481799 | 12.8924 | 171.913 | 450.126 | 453.0432 | 24916.11 |
| 128008 | 19.255 | 0.81295 | 103.694 | 0.132738 | 540.001 | 0.609894 | 377.978 | 643.932 | 0.874356 | 467.033 | 533.962 | 0.425171 | 7.05948 | 151.104 | 78.0795 | 511.8403 | 32438.83 |
| 54685.5 | 28.1083 | 0.922673 | 94.8811 | 1.56694 | 872.502 | 0.294126 | 463.294 | 147.146 | 0.796882 | 360.045 | 469.227 | 0.42259 | 7.60313 | 438.615 | 337.582 | 672.0839 | 85430.12 |
| 68187.3 | 15.7932 | 0.90246 | 144.006 | 0.755986 | 814.405 | 0.5727 | 473.103 | 14.0868 | 0.555517 | 192.44 | 70.5593 | 0.580062 | 31.9705 | 301.991 | 132.404 | 342.4454 | 33680.91 |
| 149761 | 34.4004 | 0.780415 | 142.948 | 1.61347 | 966.755 | 0.871172 | 337.793 | 88.7769 | 0.970965 | 423.191 | 837.251 | 0.808648 | 48.3457 | 199.137 | 423.075 | 280.4226 | 15091.33 |
| 69172.1 | 24.2929 | 0.900992 | 87.4703 | 1.55314 | 950.56 | 0.383828 | 286.714 | 334.965 | 0.634813 | 83.1093 | 527.433 | 0.896306 | 112.904 | 99.5162 | 63.3344 | 355.8322 | 39714.85 |
| 49878.1 | 32.2801 | 0.929872 | 56.4299 | 0.867286 | 491.883 | 0.347132 | 479.55 | 779.846 | 0.771727 | 485.935 | 454.272 | 0.905225 | 3.3581 | 183.614 | 232.969 | 293.6677 | 26694.83 |
| 110367 | 28.4289 | 0.839354 | 35.3114 | 2.49502 | 804.451 | 0.49086 | 150.082 | 162.843 | 0.690028 | 233.072 | 813.88 | 0.748156 | 53.3161 | 118.093 | 137.225 | 352.9367 | 30200.94 |
| 149705 | 29.7955 | 0.780492 | 124.126 | 1.36671 | 512.666 | 0.607479 | 497.829 | 385.761 | 0.548973 | 407.073 | 658.261 | 0.86671 | 104.134 | 180.729 | 280.695 | 368.838 | 22628.67 |
| 158413 | 33.2201 | 0.767466 | 127.811 | 3.45986 | 823.278 | 0.197127 | 475.831 | 362.9 | 0.826442 | 178.037 | 578.714 | 0.857621 | 81.429 | 226.863 | 134.895 | 900.9593 | 83103.76 |
| 163320 | 26.443 | 0.760116 | 144.344 | 2.33506 | 561.01 | 0.535381 | 226.011 | 727.938 | 0.778266 | 375.273 | 395.079 | 0.84731 | 128.836 | 50.4153 | 218.272 | 353.1729 | 22410.5 |
| 142840 | 21.2678 | 0.790757 | 165.316 | 0.602133 | 775.436 | 0.64705 | 470.878 | 663.535 | 0.535763 | 59.34 | 238.401 | 0.773154 | 18.5251 | 231.101 | 51.0322 | 456.2092 | 29845.4 |
| 38285.3 | 23.6431 | 0.947209 | 66.7868 | 0.73883 | 666.74 | 0.318745 | 405.44 | 625.365 | 0.29704 | 136.481 | 800.562 | 0.868037 | 12.1802 | 209.465 | 63.6651 | 702.7967 | 83331.92 |
| 180965 | 30.0346 | 0.733716 | 72.2771 | 2.21271 | 77.7825 | 0.337153 | 306.835 | 715.363 | 0.727819 | 356.153 | 147.995 | 0.480079 | 76.0388 | 259.171 | 296.031 | 817.1924 | 40212.24 |
| 71920.5 | 26.9009 | 0.896882 | 53.3581 | 0.322294 | 660.793 | 0.482459 | 330.78 | 118.696 | 0.810491 | 515.586 | 628.768 | 0.589963 | 14.8179 | 217.956 | 477.136 | 292.6022 | 27180.54 |
| 67268.4 | 25.5131 | 0.903842 | 34.9427 | 2.07054 | 577.027 | 0.221478 | 127.125 | 561.399 | 0.865197 | 395.807 | 156.957 | 0.946184 | 66.3217 | 41.915 | 88.6398 | 426.0566 | 44917.88 |
| 92662.2 | 31.0265 | 0.86585 | 163.277 | 0.270119 | 241.512 | 0.424495 | 374.978 | 590.394 | 0.686821 | 262.269 | 290.454 | 0.700422 | 22.2923 | 96.7236 | 134.97 | 473.6771 | 29836.48 |
| 71458.6 | 29.6976 | 0.897577 | 111.106 | 1.88979 | 822.691 | 0.443811 | 109.819 | 621.232 | 0.499283 | 440.176 | 8.51797 | 0.857828 | 152.469 | 44.6292 | 277.441 | 373.8933 | 38539.3 |
| 83775.9 | 14.4419 | 0.879133 | 120.493 | 1.57984 | 57.833 | 0.467999 | 417.827 | 58.9784 | 0.731404 | 351.622 | 682.533 | 0.772405 | 31.0713 | 200.803 | 220.448 | 228.8188 | 13189.98 |
| 157022 | 16.1587 | 0.769533 | 141.931 | 2.59052 | 891.817 | 0.320498 | 480.764 | 697.737 | 0.592226 | 128.245 | 67.2434 | 0.903857 | 161.292 | 320.696 | 69.6306 | 623.8627 | 56489.88 |
| 44912.2 | 21.489 | 0.937291 | 151.089 | 3.34296 | 365.316 | 0.279541 | 347.252 | 534.797 | 0.518445 | 264.506 | 178.802 | 0.463376 | 52.6399 | 99.6255 | 108.494 | 780.741 | 75702.29 |
| 117500 | 20.1223 | 0.828674 | 140.621 | 1.72515 | 761.58 | 0.192815 | 424.042 | 127.005 | 0.575549 | 315.903 | 800.364 | 0.963238 | 100.708 | 54.7285 | 154.417 | 886.6657 | 87982.75 |
| 68325.3 | 17.6316 | 0.902254 | 90.8973 | 1.03291 | 730.576 | 0.227088 | 349.677 | 67.4823 | 0.678947 | 300.206 | 936.647 | 0.699393 | 70.4835 | 269.316 | 186.738 | 652.7162 | 75539.51 |
| 149762 | 21.7223 | 0.780401 | 65.1872 | 0.324245 | 599.123 | 0.493875 | 56.3037 | 48.5118 | 0.570698 | 263.038 | 661.797 | 0.374912 | 19.2684 | 49.2927 | 78.1164 | 804.0127 | 60208.51 |
| 61483.5 | 20.7845 | 0.912494 | 169.17 | 2.92393 | 659.852 | 0.531369 | 156.876 | 105.95 | 0.883085 | 503.535 | 221.584 | 0.290929 | 89.492 | 119.939 | 275.802 | 460.8631 | 43251.44 |
| 68343 | 13.1718 | 0.902225 | 28.9918 | 0.207377 | 399.082 | 0.43395 | 266.042 | 406.553 | 0.866159 | 237.479 | 955.312 | 0.744414 | 17.5554 | 129.706 | 191.625 | 278.117 | 21263.49 |
| 130075 | 14.7069 | 0.809855 | 47.2196 | 2.44883 | 725.235 | 0.281848 | 408.97 | 81.7468 | 0.6887 | 468.761 | 858.647 | 0.436791 | 58.1808 | 126.615 | 86.8499 | 984.1064 | 95523.03 |
| 115190 | 19.3112 | 0.832131 | 141.416 | 1.91994 | 40.1618 | 0.592378 | 157.756 | 901.34 | 0.49898 | 391.132 | 322.927 | 0.975034 | 166.66 | 79.4751 | 139.446 | 304.7923 | 15641.35 |
| 45035.1 | 15.2999 | 0.937103 | 111.271 | 0.199629 | 174.283 | 0.483368 | 330.463 | 542.977 | 0.811994 | 315.698 | 714.893 | 0.431786 | 3.06129 | 309.009 | 120.066 | 400.0631 | 27166.76 |
| 137900 | 25.9194 | 0.798152 | 100.901 | 0.181239 | 414.019 | 0.564974 | 377.261 | 467.751 | 0.726416 | 401.528 | 529.56 | 0.687167 | 3.96679 | 236.038 | 275.099 | 384.8304 | 23644.86 |
| 40091.9 | 17.3779 | 0.944501 | 112.596 | 2.57148 | 553.249 | 0.233412 | 254.383 | 218.159 | 0.541586 | 261.767 | 218.332 | 0.86841 | 104.976 | 76.8474 | 47.5984 | 460.7899 | 56555.33 |
| 119603 | 29.6435 | 0.825535 | 157.101 | 0.989954 | 396.707 | 0.629931 | 155.158 | 660.535 | 0.555488 | 260.044 | 979.366 | 0.470516 | 8.44277 | 146.4 | 95.2534 | 675.6974 | 40391.55 |
| 86044.8 | 26.045 | 0.875747 | 160.501 | 1.22735 | 205.157 | 0.190697 | 312.428 | 117.328 | 0.83063 | 286.316 | 683.146 | 0.648794 | 25.8777 | 215.418 | 115.262 | 699.4659 | 49344.47 |
| 172955 | 24.5331 | 0.745697 | 51.8011 | 0.771404 | 305.823 | 0.430427 | 492.777 | 3.8001 | 0.753387 | 363.868 | 729.549 | 0.952673 | 39.9098 | 367.541 | 361.574 | 311.6698 | 18853.76 |
| 147245 | 29.9085 | 0.784173 | 87.2052 | 3.25553 | 653.849 | 0.462474 | 409.546 | 699.81 | 0.934584 | 444.077 | 216.19 | 0.662247 | 89.1662 | 182.797 | 125.329 | 383.6725 | 28002.44 |
| 117212 | 14.859 | 0.829102 | 143.966 | 1.68921 | 820.192 | 0.535472 | 249.472 | 108.057 | 0.260179 | 369.942 | 415.858 | 0.622622 | 34.8365 | 221.894 | 131.195 | 927.771 | 80020.08 |
| 49506.7 | 18.7332 | 0.930414 | 66.4874 | 0.258563 | 92.9565 | 0.394394 | 394.802 | 517.847 | 0.767317 | 371.371 | 910.65 | 0.846584 | 23.8795 | 242.596 | 156.331 | 256.5209 | 16208.4 |
| 107698 | 30.6617 | 0.843352 | 55.0882 | 0.641122 | 678.241 | 0.382285 | 258.345 | 231.286 | 0.476053 | 387.674 | 533.928 | 0.97871 | 47.0887 | 165.256 | 85.1006 | 452.5876 | 41162.41 |
| 107238 | 17.1347 | 0.844027 | 69.2248 | 0.809254 | 248.724 | 0.292298 | 450.231 | 183.733 | 0.653232 | 198.587 | 712.64 | 0.55198 | 38.7812 | 99.2632 | 106.953 | 605.5831 | 43571.86 |
| 87644.4 | 18.4292 | 0.873347 | 67.713 | 0.371085 | 682.99 | 0.402261 | 387.838 | 196.55 | 0.834247 | 169.892 | 449.466 | 0.361646 | 19.7771 | 189.654 | 45.9263 | 585.4035 | 56808.75 |
| 56359.8 | 27.5527 | 0.920167 | 160.878 | 2.02328 | 949.541 | 0.460391 | 153.223 | 795.582 | 0.546766 | 401.082 | 97.2921 | 0.822601 | 58.0131 | 99.2313 | 324.362 | 397.4034 | 41143.36 |
| 92580.5 | 30.8575 | 0.865972 | 78.0876 | 2.19826 | 195.008 | 0.347841 | 148.987 | 214.311 | 0.355084 | 348.494 | 719.728 | 0.741347 | 118.56 | 112.948 | 85.622 | 647.5927 | 44308.77 |
| 63077 | 24.0466 | 0.910112 | 26.7845 | 2.29707 | 42.1079 | 0.442241 | 199.29 | 588.868 | 0.923948 | 284.562 | 877.133 | 0.228811 | 169.89 | 96.9274 | 149.924 | 669.3855 | 38444.37 |
| 115533 | 29.5301 | 0.831625 | 66.9307 | 0.676248 | 329.53 | 0.386259 | 443.804 | 26.3999 | 0.871831 | 127.084 | 681.002 | 0.856655 | 27.3089 | 231.024 | 112.979 | 272.0598 | 19133.28 |
| 66015.7 | 22.2523 | 0.905714 | 141.456 | 0.553627 | 238.277 | 0.645726 | 157.062 | 882.136 | 0.802674 | 419.068 | 901.736 | 0.524481 | 51.1538 | 118.487 | 180.656 | 392.1884 | 23256.81 |
| 110728 | 17.3902 | 0.838805 | 114.751 | 2.09907 | 926.581 | 0.273991 | 402.668 | 52.3427 | 0.984643 | 114.952 | 360.623 | 0.926343 | 19.876 | 289.764 | 76.4808 | 425.713 | 46707.93 |
| 52460.9 | 18.1521 | 0.925993 | 113.646 | 2.58095 | 567.881 | 0.494585 | 84.7233 | 866.224 | 0.988256 | 106.314 | 511.852 | 0.715669 | 124.764 | 53.5335 | 88.2036 | 261.411 | 19573.2 |
| 149684 | 21.1639 | 0.780517 | 54.9137 | 0.830502 | 714.576 | 0.400356 | 224.618 | 42.2752 | 0.717734 | 327.534 | 255.447 | 0.909892 | 38.8175 | 193.868 | 137.956 | 330.7933 | 28562.47 |
| 172833 | 31.4351 | 0.745887 | 61.5716 | 1.96823 | 952.544 | 0.601405 | 438.165 | 118.339 | 0.873793 | 268.399 | 321.22 | 0.942853 | 83.3166 | 98.9749 | 147.295 | 219.2506 | 14866.72 |
| 102212 | 29.2206 | 0.851557 | 161.007 | 1.07087 | 822.054 | 0.699774 | 166.704 | 344.857 | 0.664953 | 279.654 | 446.103 | 0.967346 | 84.8243 | 118.08 | 259.676 | 230.1897 | 15104.36 |
| 138950 | 25.1307 | 0.79658 | 170.174 | 2.43419 | 455.406 | 0.28254 | 95.1656 | 415.887 | 0.993442 | 181.604 | 50.8714 | 0.856649 | 63.1419 | 41.2322 | 59.4354 | 513.4361 | 37255.88 |
| 62885 | 23.5442 | 0.910399 | 24.0152 | 1.05223 | 341.229 | 0.404117 | 473.341 | 456.562 | 0.975336 | 124.516 | 82.3761 | 0.237436 | 62.4284 | 217.771 | 47.3831 | 636.1853 | 51746.37 |
| 67690 | 24.1332 | 0.90321 | 85.3777 | 1.99372 | 400.707 | 0.32305 | 477.299 | 630.602 | 0.722699 | 212.154 | 198.643 | 0.932037 | 129.8 | 62.167 | 60.1192 | 290.667 | 25445.14 |
| 66541.7 | 25.4018 | 0.904929 | 39.7076 | 2.627 | 214.463 | 0.486772 | 236.505 | 855.346 | 0.266296 | 504.795 | 588.186 | 0.51565 | 116.641 | 171.859 | 483.882 | 791.3444 | 55303.53 |
| 106282 | 33.7895 | 0.845474 | 101.221 | 2.61492 | 380.658 | 0.542841 | 149.928 | 499.255 | 0.352772 | 431.115 | 883.038 | 0.407619 | 140.704 | 60.184 | 320.851 | 925.5201 | 61950.26 |
| 59261.4 | 23.3282 | 0.915821 | 99.6069 | 1.43072 | 732.65 | 0.41044 | 242.09 | 590.303 | 0.921273 | 119.16 | 769.574 | 0.347927 | 81.0078 | 189.227 | 89.6061 | 606.7627 | 58190.26 |
| 112051 | 16.2122 | 0.836826 | 85.723 | 2.80837 | 190.261 | 0.460663 | 363.212 | 473.577 | 0.98718 | 254.315 | 856.276 | 0.170613 | 86.3889 | 64.1297 | 249.039 | 986.9659 | 59410.22 |
| 94749.1 | 22.6072 | 0.862719 | 77.1257 | 1.59363 | 947.266 | 0.334712 | 370.491 | 41.9102 | 0.395289 | 458.978 | 294.31 | 0.954334 | 35.8931 | 121.673 | 122.175 | 599.0603 | 69701.31 |
| 154664 | 25.8977 | 0.773068 | 75.659 | 0.971231 | 49.619 | 0.302896 | 387.395 | 980.24 | 0.325287 | 201.036 | 77.1086 | 0.959239 | 14.4872 | 66.6872 | 55.2211 | 805.2033 | 40154.32 |
| 170907 | 26.4433 | 0.748763 | 150.633 | 1.73104 | 841.837 | 0.720244 | 430.162 | 975.078 | 0.438732 | 351.298 | 209.221 | 0.929922 | 100.836 | 423.756 | 304.01 | 529.6234 | 30409.06 |
| 107436 | 33.8673 | 0.843747 | 109.292 | 0.521804 | 329.485 | 0.509597 | 497.776 | 681.16 | 0.73391 | 73.8656 | 599.101 | 0.783861 | 41.3467 | 76.6158 | 50.4374 | 349.2678 | 21985.99 |
| 203196 | 27.4712 | 0.700449 | 38.3055 | 3.76474 | 548.333 | 0.613713 | 344.816 | 889.366 | 0.668502 | 451.678 | 772.665 | 0.713811 | 252.165 | 219.182 | 165.641 | 531.8481 | 28800.43 |
| 187558 | 13.4356 | 0.723841 | 64.4426 | 3.55853 | 585.287 | 0.220481 | 243.027 | 605.642 | 0.790611 | 99.0186 | 787.297 | 0.745932 | 76.8701 | 195.226 | 90.5111 | 825.9734 | 64933.42 |
| 190692 | 14.4468 | 0.719151 | 98.8187 | 2.37832 | 138.503 | 0.180796 | 165.859 | 411.997 | 0.807066 | 156.591 | 488.26 | 0.619877 | 84.1834 | 74.1351 | 137.208 | 953.6271 | 52047.37 |
| 174002 | 33.8559 | 0.74414 | 58.1806 | 1.78959 | 878.701 | 0.593057 | 359.984 | 877.085 | 0.600485 | 140.511 | 183.561 | 0.381205 | 69.087 | 88.4027 | 111.076 | 886.2709 | 59572.44 |
| 95519.9 | 27.9674 | 0.861571 | 65.7623 | 0.133165 | 504.292 | 0.503169 | 366.949 | 839.376 | 0.386999 | 141.073 | 695.777 | 0.700809 | 11.4789 | 352.178 | 120.468 | 611.3064 | 45783.87 |
| 123246 | 32.0041 | 0.820087 | 35.8233 | 0.813395 | 933.667 | 0.445022 | 71.2377 | 158.694 | 0.475939 | 56.8589 | 440.745 | 0.584033 | 57.7038 | 52.8613 | 51.2305 | 706.1361 | 67181.82 |
| 84563.8 | 28.2687 | 0.877965 | 137.571 | 3.23738 | 697.784 | 0.424068 | 138.174 | 994.193 | 0.646469 | 259.313 | 368.333 | 0.437317 | 136.595 | 64.4321 | 238.306 | 738.6268 | 64174.85 |
| 71073.4 | 30.9187 | 0.898155 | 41.8291 | 0.465403 | 602.185 | 0.525184 | 184.081 | 879.935 | 0.851196 | 389.268 | 290.796 | 0.346462 | 32.2218 | 93.9574 | 257.87 | 554.7099 | 40926.5 |
| 83787.5 | 26.0439 | 0.879124 | 57.9481 | 0.548701 | 19.5112 | 0.426666 | 248.127 | 806.87 | 0.834334 | 110.167 | 406.657 | 0.645979 | 18.2464 | 44.7732 | 104.815 | 316.6418 | 17091.71 |
| 125110 | 30.6176 | 0.817296 | 50.2324 | 0.271543 | 186.854 | 0.371991 | 316.637 | 313.329 | 0.992884 | 134.993 | 37.8905 | 0.925293 | 11.9867 | 200.573 | 117.098 | 243.3575 | 15070.23 |
| 113223 | 33.0192 | 0.835087 | 71.3251 | 0.743679 | 773.492 | 0.511997 | 342.043 | 870.704 | 0.657477 | 471.507 | 9.67402 | 0.522973 | 34.1964 | 61.4652 | 201.049 | 538.5129 | 43534.1 |
| 201927 | 15.0638 | 0.70234 | 63.6914 | 1.28787 | 772.421 | 0.460935 | 144.921 | 897.508 | 0.521111 | 184.926 | 20.509 | 0.903949 | 61.0068 | 46.8466 | 79.6398 | 515.1791 | 38162.5 |
| 113839 | 28.4121 | 0.83416 | 140.933 | 0.768417 | 564.516 | 0.676565 | 205.087 | 903.785 | 0.839321 | 250.227 | 421.224 | 0.949613 | 17.5632 | 182.372 | 197.818 | 246.5951 | 14612.31 |
| 93927.8 | 27.7787 | 0.863953 | 102.319 | 3.72984 | 54.2619 | 0.619891 | 404.246 | 406.73 | 0.951138 | 374.778 | 665.163 | 0.744237 | 117.329 | 371.323 | 218.935 | 257.8022 | 13723.85 |
| 106787 | 23.3718 | 0.844706 | 111.2 | 0.670086 | 659.695 | 0.259873 | 497.51 | 788.069 | 0.876235 | 444.699 | 597.177 | 0.455425 | 34.1571 | 49.9223 | 54.0819 | 944.7701 | 83888.78 |
| 58621.3 | 29.0922 | 0.916785 | 152.051 | 2.81398 | 811.042 | 0.241345 | 466.625 | 712.106 | 0.976539 | 482.519 | 780.411 | 0.564867 | 73.987 | 253.957 | 55.1326 | 670.9849 | 71822.52 |
| 83861.7 | 14.6173 | 0.879005 | 63.1606 | 2.4103 | 221.918 | 0.407642 | 372.151 | 596.074 | 0.405951 | 460.441 | 968.471 | 0.612752 | 160.219 | 180.925 | 173.817 | 603.1169 | 41693.59 |
| 132300 | 26.2465 | 0.806533 | 171.046 | 2.4326 | 45.3842 | 0.656048 | 472.35 | 74.8222 | 0.858848 | 122.247 | 804.297 | 0.206295 | 119.75 | 162.249 | 121.134 | 740.9372 | 36524.98 |
| 120160 | 34.3529 | 0.824708 | 111.885 | 3.354 | 166.341 | 0.436855 | 354.593 | 579.884 | 0.331161 | 176.891 | 808.173 | 0.923085 | 43.4819 | 316.395 | 151.952 | 576.9654 | 33906.76 |
| 137166 | 22.5079 | 0.799249 | 101.33 | 3.6031 | 249.889 | 0.424363 | 477.589 | 870.12 | 0.585031 | 137.824 | 579.897 | 0.835157 | 138.392 | 271.092 | 59.9892 | 437.6416 | 26579.41 |
| 119647 | 15.1435 | 0.825458 | 56.4793 | 2.74458 | 790.072 | 0.295493 | 266.536 | 830.262 | 0.819492 | 394.655 | 480.788 | 0.846817 | 48.7692 | 181.859 | 234.374 | 478.9153 | 44982.65 |
| 52233.4 | 24.8259 | 0.926339 | 73.122 | 1.56029 | 425.202 | 0.485567 | 138.401 | 276.161 | 0.875471 | 499.719 | 466.723 | 0.798422 | 50.158 | 57.4308 | 191.352 | 182.6607 | 14981.63 |
| 173370 | 23.5822 | 0.745075 | 145.257 | 0.199142 | 171.629 | 0.597611 | 381.095 | 379.348 | 0.966549 | 517.074 | 982.866 | 0.23907 | 15.0078 | 100.721 | 117.416 | 988.9973 | 49151.1 |
| 114383 | 27.1319 | 0.833344 | 161.983 | 3.35353 | 166.658 | 0.408067 | 326.871 | 38.0145 | 0.680365 | 431.067 | 978.956 | 0.290286 | 115.194 | 60.8757 | 300.718 | 907.5074 | 54414.87 |
| 105813 | 23.1557 | 0.846163 | 167.625 | 1.48443 | 971.729 | 0.678678 | 362.499 | 881.021 | 0.990378 | 172.649 | 985.594 | 0.543796 | 73.4331 | 355.636 | 55.1972 | 420.5978 | 26434.56 |
| 45427.2 | 18.4679 | 0.936518 | 169.915 | 2.76187 | 90.1266 | 0.173813 | 312.493 | 585.294 | 0.644488 | 313.401 | 206.099 | 0.8689 | 0.781015 | 168.95 | 129.204 | 507.119 | 36582.29 |
| 115167 | 14.8178 | 0.832163 | 80.0613 | 1.41481 | 195.506 | 0.545547 | 252.521 | 943.115 | 0.981794 | 497.628 | 792.454 | 0.454677 | 90.9091 | 230.143 | 414.11 | 533.1239 | 29268.76 |
| 84703.6 | 24.2304 | 0.877752 | 84.3106 | 2.99992 | 800.043 | 0.413913 | 374.697 | 136.357 | 0.956077 | 425.205 | 859.403 | 0.402729 | 95.8259 | 296.597 | 243.773 | 483.7241 | 47970.64 |
| 143064 | 32.6041 | 0.790433 | 141.244 | 3.45686 | 820.237 | 0.59808 | 91.9706 | 392.251 | 0.61637 | 432.173 | 402.805 | 0.269424 | 156.432 | 52.2732 | 360.147 | 970.2228 | 67780.45 |
| 91383.7 | 14.8158 | 0.86775 | 153.895 | 1.67368 | 866.121 | 0.323034 | 168.36 | 380.785 | 0.797681 | 131.451 | 703.378 | 0.796536 | 63.5859 | 137.159 | 54.9014 | 474.5852 | 46584.75 |
| 143672 | 18.3694 | 0.789511 | 136.237 | 2.57784 | 71.8776 | 0.506526 | 87.6758 | 247.503 | 0.859915 | 81.1628 | 311.396 | 0.811545 | 118.666 | 55.6633 | 58.468 | 234.1578 | 12044.33 |
| 111873 | 19.03 | 0.837093 | 95.9031 | 3.17378 | 351.758 | 0.518537 | 426.79 | 557.67 | 0.49774 | 491.521 | 685.973 | 0.61012 | 26.5168 | 260.39 | 445.523 | 484.0881 | 31045.92 |
| 82563.7 | 17.4871 | 0.880949 | 57.9491 | 0.641306 | 117.004 | 0.357163 | 319.499 | 255.106 | 0.812195 | 337.79 | 396.334 | 0.597792 | 26.5503 | 120.251 | 298.492 | 313.3045 | 20164.37 |
| 43922.6 | 16.3802 | 0.938768 | 30.328 | 0.940031 | 251.901 | 0.542066 | 356.634 | 716.989 | 0.741518 | 469.704 | 764.945 | 0.49819 | 24.7364 | 186.994 | 404.067 | 465.7281 | 30827.63 |
| 47422.1 | 16.7816 | 0.933532 | 123.288 | 3.42294 | 358.751 | 0.289618 | 329.81 | 344.64 | 0.850367 | 165.948 | 723.593 | 0.77751 | 21.6899 | 312.787 | 46.8335 | 307.2958 | 27808.01 |
| 47903.3 | 29.8432 | 0.932824 | 79.2207 | 0.323599 | 659.66 | 0.374787 | 268.359 | 920.346 | 0.487852 | 398.764 | 192.304 | 0.835577 | 6.16875 | 76.6195 | 390.417 | 447.7456 | 46193.1 |
| 76222.7 | 32.9995 | 0.890452 | 39.086 | 0.57242 | 405.277 | 0.288926 | 131.557 | 38.9539 | 0.514256 | 448.049 | 843.642 | 0.82842 | 44.4532 | 64.0662 | 266.481 | 507.0155 | 45292.79 |
| 66884.2 | 34.6326 | 0.904429 | 84.0967 | 0.552801 | 630.9 | 0.397644 | 190.241 | 272.432 | 0.84345 | 342.96 | 55.227 | 0.362845 | 43.259 | 175.322 | 73.3181 | 539.4052 | 53726.19 |
| 45761.5 | 24.2058 | 0.936023 | 66.5522 | 0.118723 | 879.441 | 0.395755 | 489.122 | 379.112 | 0.882567 | 354.507 | 519.884 | 0.251739 | 8.83696 | 143.298 | 64.9705 | 822.5887 | 93177.31 |
| 84013.6 | 33.9144 | 0.878796 | 36.3209 | 2.15658 | 346.786 | 0.402647 | 273.026 | 765.274 | 0.404568 | 326.438 | 827.272 | 0.945087 | 25.5357 | 221.581 | 137.307 | 475.6435 | 35478.27 |
| 127478 | 20.5449 | 0.813743 | 171.535 | 1.20856 | 425.485 | 0.650153 | 164.508 | 718.672 | 0.989009 | 330.455 | 41.5512 | 0.413779 | 89.9608 | 118.651 | 262.779 | 461.6576 | 27036.39 |
| 115180 | 27.8103 | 0.832152 | 172.138 | 1.20685 | 716.193 | 0.261325 | 315.413 | 145.01 | 0.857523 | 480.369 | 912.167 | 0.739766 | 10.1394 | 275.833 | 131.436 | 677.8276 | 58277.08 |
| 69983.1 | 19.6115 | 0.899775 | 56.9328 | 1.54399 | 128.46 | 0.450142 | 463.813 | 461.943 | 0.431292 | 497.599 | 705.241 | 0.8312 | 20.2675 | 132.818 | 252.781 | 344.2888 | 22229.67 |
| 166796 | 25.5777 | 0.754914 | 129.358 | 2.1253 | 367.162 | 0.250341 | 47.8548 | 872.652 | 0.989952 | 106.542 | 393.659 | 0.838118 | 88.1708 | 41.0737 | 50.3858 | 646.5379 | 42191.1 |
| 50940.9 | 22.1716 | 0.928271 | 51.3606 | 1.74255 | 312.261 | 0.497982 | 235.77 | 404.067 | 0.982901 | 97.7071 | 500.441 | 0.12863 | 62.9645 | 59.8283 | 97.3923 | 908.0687 | 66022.2 |
| 86229.9 | 23.7061 | 0.875467 | 130.003 | 2.99982 | 120.106 | 0.251818 | 172.644 | 983.774 | 0.859366 | 290.871 | 192.38 | 0.944589 | 44.4839 | 76.541 | 247.12 | 374.8553 | 23505.52 |
| 152337 | 15.5143 | 0.776544 | 89.196 | 1.69883 | 812.345 | 0.208399 | 428.561 | 246.322 | 0.619605 | 268.318 | 314.948 | 0.916547 | 141.467 | 315.077 | 106.98 | 792.6532 | 79226.25 |
| 69098.4 | 34.696 | 0.901116 | 87.482 | 1.56503 | 171.906 | 0.139517 | 118.797 | 749.262 | 0.586022 | 84.085 | 170.107 | 0.716229 | 21.0214 | 73.6629 | 65.5505 | 885.2984 | 68066.79 |
| 43052.9 | 33.7582 | 0.940088 | 83.7776 | 1.27133 | 19.0325 | 0.352265 | 462.521 | 484.509 | 0.673844 | 317.89 | 259.888 | 0.227965 | 85.3001 | 278.542 | 120.329 | 765.1053 | 47235.45 |
| 40487.4 | 33.492 | 0.943926 | 85.0225 | 3.13986 | 131.318 | 0.428522 | 133.382 | 73.646 | 0.618677 | 255.883 | 54.895 | 0.846054 | 95.7118 | 126.891 | 198.391 | 155.7947 | 12323.69 |
| 62008.2 | 22.2086 | 0.91171 | 127.941 | 0.488646 | 824.72 | 0.618289 | 490.817 | 806.922 | 0.809066 | 392.232 | 149.487 | 0.264534 | 22.2616 | 107.368 | 49.5438 | 687.6876 | 54467.52 |
| 93626.7 | 28.2368 | 0.864404 | 100.914 | 0.975498 | 965.318 | 0.365015 | 154.702 | 404.35 | 0.80102 | 457.728 | 554.07 | 0.61604 | 13.3577 | 84.2769 | 54.0523 | 516.8035 | 53061.29 |
| 144934 | 31.1681 | 0.787634 | 109.947 | 1.70678 | 77.52 | 0.213385 | 430.137 | 358.485 | 0.8486 | 237.929 | 532.603 | 0.721988 | 103.05 | 178.305 | 144.061 | 622.7754 | 32985.82 |
| 112761 | 32.3251 | 0.835777 | 117.023 | 1.24177 | 0.280223 | 0.537358 | 382.789 | 369.051 | 0.806014 | 403.032 | 417.16 | 0.552076 | 56.1362 | 317.131 | 310.36 | 331.2543 | 16646.08 |
| 155229 | 20.447 | 0.772218 | 157.605 | 1.28505 | 124.789 | 0.658346 | 373.836 | 677.264 | 0.842167 | 119.781 | 880.47 | 0.607632 | 81.833 | 180.65 | 49.4262 | 407.3767 | 20410.99 |
| 133172 | 33.9053 | 0.805237 | 132.225 | 1.65409 | 348.954 | 0.485606 | 471.946 | 810.528 | 0.668972 | 266.942 | 979.417 | 0.940812 | 77.8226 | 49.8183 | 88.1557 | 401.4305 | 24228.75 |
| 88616.6 | 24.1378 | 0.871896 | 141.611 | 0.389437 | 979.363 | 0.580568 | 311.11 | 46.9433 | 0.435943 | 113.686 | 467.326 | 0.592401 | 31.3965 | 210.48 | 101.51 | 558.9123 | 50568.65 |
| 165477 | 21.803 | 0.756885 | 136.855 | 0.609221 | 248.732 | 0.624402 | 406.323 | 494.677 | 0.63773 | 344.32 | 461.706 | 0.902257 | 23.896 | 51.8784 | 297.655 | 330.5138 | 17504.34 |
| 104332 | 20.607 | 0.848378 | 152.804 | 1.49936 | 814.48 | 0.380623 | 387.493 | 466.339 | 0.644436 | 205.266 | 57.8176 | 0.816958 | 1.10552 | 108.019 | 192.571 | 456.7259 | 42841.28 |
| 127150 | 30.6862 | 0.814244 | 95.0896 | 1.28532 | 198.787 | 0.201196 | 170.376 | 53.9144 | 0.964388 | 154.718 | 543.787 | 0.391332 | 36.5083 | 59.7575 | 74.4549 | 932.2456 | 61277.05 |
| 170886 | 28.0508 | 0.748796 | 61.6601 | 2.12434 | 943.089 | 0.553102 | 205.722 | 466.058 | 0.998286 | 446.592 | 910.398 | 0.281507 | 143.169 | 116.695 | 114.903 | 790.309 | 56290.89 |
| 84605 | 14.8685 | 0.877893 | 172.686 | 1.30466 | 408.962 | 0.514223 | 170.517 | 188.778 | 0.937282 | 492.68 | 982.912 | 0.850775 | 125.872 | 48.1699 | 438.131 | 251.53 | 17034.89 |
| 134687 | 20.7208 | 0.802957 | 167.955 | 0.822453 | 689.457 | 0.689336 | 242.725 | 96.7398 | 0.781642 | 96.063 | 732.333 | 0.31009 | 15.1428 | 64.2216 | 58.4662 | 630.3944 | 40302.86 |
| 126599 | 22.2412 | 0.815061 | 67.6928 | 2.32254 | 827.785 | 0.200702 | 295.28 | 843.16 | 0.752989 | 466.307 | 312.88 | 0.961048 | 104.799 | 203.936 | 124.978 | 708.5159 | 71939.04 |
| 123653 | 22.5946 | 0.819468 | 69.3804 | 2.6542 | 317.431 | 0.446082 | 161.954 | 293.268 | 0.357777 | 129.077 | 278.571 | 0.53669 | 92.4604 | 123.636 | 124.879 | 785.9368 | 54193.13 |
| 116899 | 30.8163 | 0.829583 | 120.887 | 0.597007 | 758.409 | 0.311616 | 297.822 | 275.772 | 0.505992 | 161.316 | 38.8787 | 0.760574 | 26.5194 | 118.105 | 52.4334 | 771.421 | 71731.52 |
| 164730 | 21.3541 | 0.758003 | 75.4487 | 1.82581 | 183.682 | 0.246008 | 419.669 | 868.675 | 0.605471 | 326.535 | 680.014 | 0.908361 | 22.3078 | 229.429 | 208.816 | 670.3659 | 39087.82 |
| 153258 | 30.7526 | 0.775178 | 147.637 | 1.82706 | 493.359 | 0.418551 | 325.072 | 965.329 | 0.863913 | 370.873 | 833.015 | 0.425857 | 43.1323 | 280.246 | 137.139 | 850.8515 | 54854.97 |
| 196656 | 19.771 | 0.71023 | 151.717 | 2.08789 | 877.311 | 0.456397 | 254.166 | 741.559 | 0.869164 | 147.249 | 603.663 | 0.472272 | 153.106 | 190.245 | 119.309 | 772.737 | 54819.06 |
| 154964 | 34.3836 | 0.772629 | 146.748 | 2.24215 | 303.126 | 0.587613 | 288.719 | 626.616 | 0.391215 | 392.34 | 464.418 | 0.605965 | 77.0805 | 55.3431 | 57.0365 | 745.1055 | 41715.23 |
| 161082 | 32.924 | 0.763472 | 159.02 | 2.08301 | 510.615 | 0.340445 | 117.501 | 852.204 | 0.782977 | 338.646 | 360.037 | 0.951478 | 27.0126 | 55.6812 | 72.7582 | 514.0956 | 34517.55 |
| 119095 | 21.6722 | 0.826288 | 66.8945 | 1.94408 | 477.986 | 0.255749 | 223.956 | 491.321 | 0.744039 | 290.126 | 138.988 | 0.559459 | 55.0178 | 101.035 | 66.6501 | 717.7236 | 61369.11 |
| 38602.3 | 22.9498 | 0.946734 | 120.952 | 1.95909 | 425.723 | 0.387232 | 378.595 | 904.818 | 0.636992 | 432.232 | 688.989 | 0.284997 | 81.1499 | 61.6596 | 67.427 | 902.4241 | 80161.13 |
| 148533 | 25.5854 | 0.782242 | 131.516 | 0.839777 | 775.195 | 0.424402 | 497.574 | 270.552 | 0.928316 | 398.821 | 546.298 | 0.370184 | 0.806314 | 298.016 | 87.9177 | 766.4117 | 60264.8 |
| 85435.8 | 18.036 | 0.876652 | 27.4471 | 2.80214 | 481.167 | 0.515064 | 242.39 | 676.367 | 0.488929 | 405.3 | 70.5078 | 0.968378 | 146.546 | 232.865 | 79.5311 | 270.4441 | 20029.92 |
| 83887.9 | 31.12 | 0.87898 | 139.518 | 0.954413 | 470.826 | 0.309262 | 162.442 | 481.849 | 0.980465 | 195.512 | 877.281 | 0.37046 | 41.9671 | 128.723 | 185.532 | 789.0049 | 63599.51 |
| 38574.9 | 30.7825 | 0.946784 | 164.087 | 2.26701 | 34.1599 | 0.46737 | 340.893 | 78.4496 | 0.975895 | 329.471 | 692.497 | 0.337214 | 134.543 | 211.415 | 106.623 | 316.4277 | 20256.79 |
| 141860 | 26.1261 | 0.792227 | 147.828 | 2.25247 | 901.891 | 0.57088 | 180.245 | 403.79 | 0.903744 | 340.163 | 291.693 | 0.240661 | 162.958 | 51.1932 | 241.11 | 869.7153 | 65260.85 |
| 102140 | 13.5663 | 0.851653 | 35.7286 | 0.754769 | 506.437 | 0.453795 | 155.436 | 18.8396 | 0.782547 | 486.881 | 402.733 | 0.360404 | 59.7227 | 96.7816 | 188.338 | 480.2332 | 41048.15 |
| 109298 | 31.1694 | 0.840957 | 87.6379 | 1.72909 | 359.846 | 0.40858 | 78.2824 | 682.548 | 0.438285 | 381.237 | 760.389 | 0.808191 | 50.1725 | 73.5539 | 355.416 | 551.415 | 39160.14 |
| 135853 | 28.1875 | 0.801219 | 168.429 | 1.2814 | 159.198 | 0.36253 | 74.5777 | 648.781 | 0.381386 | 117.159 | 769.148 | 0.858677 | 16.3204 | 47.4753 | 71.6866 | 854.4852 | 47459.14 |
| 177845 | 20.6357 | 0.738379 | 33.3018 | 2.93321 | 637.334 | 0.402761 | 358.652 | 129.201 | 0.596336 | 182.908 | 57.3157 | 0.917913 | 3.6 | 123.197 | 84.3118 | 413.3257 | 32417.8 |
| 68612.6 | 18.6031 | 0.901825 | 96.5416 | 1.8356 | 41.1419 | 0.174827 | 150.888 | 155.809 | 0.419896 | 172.894 | 418.979 | 0.584109 | 71.3871 | 79.9954 | 155.826 | 937.9442 | 58638.64 |
| 166115 | 22.667 | 0.755932 | 134.485 | 2.14753 | 949.758 | 0.383437 | 316.356 | 233.448 | 0.938762 | 132.792 | 324.613 | 0.386844 | 13.9306 | 112.467 | 129.045 | 803.3986 | 70184.32 |
| 183097 | 20.3262 | 0.730519 | 87.3867 | 2.85031 | 322.477 | 0.239827 | 146.186 | 134.97 | 0.857586 | 213.307 | 865.223 | 0.505189 | 107.129 | 118.092 | 109.541 | 896.0387 | 58606.97 |
| 107916 | 27.5805 | 0.843021 | 166.886 | 3.04012 | 249.794 | 0.494186 | 114.064 | 372.993 | 0.512068 | 232.527 | 79.4981 | 0.614107 | 46.6889 | 108.209 | 107.4 | 486.0668 | 30845.48 |
| 42036.3 | 31.0583 | 0.941605 | 99.2081 | 2.19712 | 352.045 | 0.344842 | 173.66 | 180.848 | 0.542058 | 347.448 | 974.119 | 0.546185 | 14.6764 | 74.6932 | 160.194 | 494.8143 | 46331.5 |
| 115260 | 17.9707 | 0.832025 | 45.7733 | 2.60965 | 787.95 | 0.431254 | 440.042 | 857.037 | 0.926738 | 408.165 | 22.6657 | 0.793942 | 86.1707 | 254.661 | 363.33 | 305.2438 | 26307.12 |
| 48988.6 | 14.7954 | 0.931187 | 149.462 | 2.12476 | 188.784 | 0.246466 | 150.535 | 430.219 | 0.427458 | 506.808 | 671.511 | 0.975291 | 18.5319 | 129.981 | 348.136 | 501.4856 | 40017.71 |
| 77772 | 27.9205 | 0.888128 | 134.334 | 3.44509 | 407.449 | 0.174105 | 493.876 | 458.718 | 0.779426 | 325.106 | 854.648 | 0.917456 | 136.843 | 282.581 | 103.498 | 648.6987 | 57952.31 |
| 165203 | 21.8617 | 0.757295 | 56.8148 | 3.30728 | 603.369 | 0.308859 | 96.9677 | 361.898 | 0.920677 | 337.085 | 590.488 | 0.691617 | 136.547 | 68.6528 | 54.502 | 525.0247 | 40917.99 |
| 58188.4 | 31.4162 | 0.917436 | 120.437 | 1.73062 | 297.403 | 0.452801 | 120.993 | 978.701 | 0.215835 | 356.95 | 556.604 | 0.580132 | 85.1552 | 68.5977 | 262.282 | 977.5311 | 76884.96 |
| 163002 | 25.3349 | 0.760591 | 75.6146 | 0.573115 | 604.192 | 0.321786 | 296.606 | 882.368 | 0.733131 | 465.941 | 615.246 | 0.590986 | 48.7774 | 47.2304 | 172.581 | 802.2484 | 60496.62 |
| 37029.6 | 26.8675 | 0.949091 | 80.6951 | 0.681797 | 336.71 | 0.492759 | 233.539 | 219.173 | 0.961101 | 240.566 | 919.959 | 0.29344 | 50.396 | 146.3 | 137.165 | 392.8459 | 31984.15 |
| 113239 | 24.5129 | 0.835053 | 110.983 | 1.62702 | 573.93 | 0.553373 | 308.034 | 831.678 | 0.420203 | 450.136 | 390.225 | 0.594503 | 96.1796 | 219.227 | 359.138 | 589.9094 | 40339.02 |
| 45787.7 | 16.7004 | 0.935978 | 158.888 | 0.97762 | 154.754 | 0.367231 | 292.526 | 382.195 | 0.940824 | 440.566 | 420.216 | 0.979205 | 67.874 | 107.812 | 104.067 | 235.8109 | 16397.8 |
| 100186 | 22.1702 | 0.854584 | 122.445 | 0.644525 | 710.843 | 0.370973 | 196.688 | 488.73 | 0.565661 | 100.064 | 727.571 | 0.654465 | 43.1425 | 183.595 | 63.0214 | 667.0775 | 59178.13 |
| 80330.5 | 15.5619 | 0.884289 | 155.246 | 1.20405 | 746.565 | 0.598834 | 493.949 | 121.71 | 0.227208 | 480.396 | 420.492 | 0.664635 | 36.2789 | 390.586 | 91.3068 | 760.4526 | 66097.9 |
| 151817 | 31.9425 | 0.777335 | 135.276 | 0.377187 | 222.44 | 0.544745 | 350.091 | 365.568 | 0.908524 | 364.078 | 791.543 | 0.936087 | 13.2622 | 85.1438 | 340.438 | 306.2094 | 16428.46 |
| 197851 | 28.2032 | 0.708448 | 101.137 | 1.46204 | 206.758 | 0.590942 | 454.199 | 922.071 | 0.618328 | 122.097 | 213.107 | 0.449889 | 28.898 | 311.407 | 113.895 | 711.5069 | 35334.62 |
| 134368 | 30.0477 | 0.803443 | 122.956 | 1.62093 | 660.495 | 0.311075 | 464.054 | 2.83044 | 0.692932 | 359.571 | 378.691 | 0.831606 | 61.8143 | 249.794 | 114.937 | 510.1616 | 44243.25 |
| 33385.3 | 25.4112 | 0.954543 | 143.848 | 1.58483 | 978.893 | 0.622768 | 291.619 | 859.595 | 0.784966 | 514.863 | 147.754 | 0.289386 | 131.42 | 241.805 | 477.361 | 776.5218 | 64552.55 |
| 79011.7 | 34.4864 | 0.886281 | 131.716 | 0.193586 | 43.0802 | 0.179317 | 123.318 | 138.195 | 0.626911 | 169.675 | 330.597 | 0.712361 | 9.11759 | 51.4227 | 123.739 | 811.3459 | 47252.76 |
| 36579.1 | 14.9337 | 0.949756 | 170.124 | 2.42662 | 256.221 | 0.724339 | 299.032 | 139.275 | 0.77196 | 424.213 | 42.0418 | 0.7341 | 104.094 | 252.103 | 280.753 | 148.9852 | 10835.64 |
| 169820 | 28.4532 | 0.750392 | 66.5782 | 1.38371 | 3.87063 | 0.299568 | 398.044 | 517.107 | 0.596482 | 66.2776 | 633.117 | 0.776387 | 53.2326 | 301.42 | 46.071 | 631.1123 | 28965.1 |
| 199919 | 20.9124 | 0.705349 | 39.0246 | 2.08341 | 861.081 | 0.41497 | 414.332 | 647.57 | 0.546713 | 208.934 | 133.755 | 0.539192 | 23.6573 | 53.9987 | 100.891 | 934.0255 | 74241.13 |
| 79471.2 | 32.7469 | 0.885591 | 60.2891 | 0.150176 | 330.191 | 0.227007 | 236.061 | 308.816 | 0.582264 | 238.998 | 430.836 | 0.680818 | 8.64215 | 115.3 | 52.3987 | 710.0035 | 59719.22 |
| 61053.5 | 25.4303 | 0.913142 | 112.886 | 0.671292 | 449.696 | 0.442116 | 327.758 | 929.816 | 0.712078 | 496.178 | 29.5124 | 0.339701 | 46.4319 | 248.24 | 96.1502 | 702.8051 | 56706.39 |
| 43423.8 | 15.9127 | 0.939514 | 138.336 | 1.94765 | 942.158 | 0.563277 | 357.774 | 213.381 | 0.56141 | 156.479 | 685.766 | 0.523266 | 123.945 | 157.488 | 71.7318 | 381.9429 | 36776.62 |
| 153924 | 17.032 | 0.774169 | 129.888 | 3.49969 | 892.446 | 0.487397 | 119.476 | 491.969 | 0.860033 | 393.76 | 835.006 | 0.375885 | 106.119 | 73.5723 | 55.7736 | 696.7084 | 55237.37 |
| 126760 | 22.6128 | 0.814819 | 159.367 | 2.07 | 686.961 | 0.758334 | 487.334 | 390.256 | 0.580724 | 390.725 | 781.885 | 0.875233 | 200.168 | 385.511 | 248.915 | 419.7188 | 24194.62 |
| 146972 | 29.4625 | 0.784581 | 144.957 | 2.01174 | 796.654 | 0.32556 | 246.821 | 344.991 | 0.972519 | 505.425 | 943.671 | 0.457066 | 107.984 | 49.254 | 173.297 | 822.2908 | 67685.9 |
| 123659 | 17.893 | 0.819457 | 167.584 | 0.955929 | 684.197 | 0.517382 | 381.812 | 222.952 | 0.738061 | 168.783 | 779.035 | 0.954169 | 80.0735 | 316.231 | 70.1933 | 322.7198 | 23014.75 |
| 78924.2 | 25.4404 | 0.886401 | 70.1465 | 1.92683 | 614.56 | 0.52465 | 107.58 | 928.416 | 0.866695 | 135.829 | 320.439 | 0.43963 | 80.1572 | 89.4751 | 133.482 | 470.5614 | 33712.77 |
| 178687 | 22.8983 | 0.737119 | 134.081 | 1.11651 | 351.103 | 0.519357 | 427.559 | 778.436 | 0.745009 | 86.5176 | 543.314 | 0.643734 | 73.2767 | 377.681 | 67.7033 | 511.7918 | 28925.6 |
| 197988 | 33.9182 | 0.708249 | 75.2855 | 2.33274 | 179.844 | 0.367839 | 420.019 | 754.601 | 0.571884 | 275.345 | 856.223 | 0.771356 | 72.0465 | 335.342 | 185.647 | 725.2787 | 37841.87 |
| 161161 | 33.5169 | 0.763355 | 156.594 | 1.15378 | 990.099 | 0.608953 | 372.919 | 185.48 | 0.626734 | 231.645 | 867.535 | 0.57561 | 104.255 | 324.528 | 98.352 | 598.3996 | 41553.12 |
| 135706 | 22.6021 | 0.801433 | 83.829 | 0.738499 | 128.494 | 0.270853 | 201.127 | 988.981 | 0.899596 | 203.624 | 592.329 | 0.705016 | 6.47526 | 110.769 | 183.067 | 538.1118 | 30374.58 |
| 171081 | 24.2653 | 0.748502 | 147.382 | 1.59311 | 454.233 | 0.624697 | 126.301 | 36.88 | 0.843013 | 394.536 | 576.215 | 0.844694 | 152.798 | 105.421 | 290.26 | 253.859 | 14649.66 |
| 155440 | 27.9925 | 0.771908 | 86.0963 | 0.552048 | 519.831 | 0.51913 | 142.585 | 136.247 | 0.816912 | 483.776 | 680.039 | 0.638971 | 29.5018 | 108.9 | 326.166 | 373.371 | 24861.86 |
| 77050.7 | 33.9501 | 0.889215 | 92.1391 | 0.965833 | 859.695 | 0.371863 | 463.671 | 37.2845 | 0.449359 | 116.553 | 309.26 | 0.993428 | 38.6555 | 385.554 | 44.823 | 433.6842 | 48580.38 |
| 35394.8 | 19.1287 | 0.95153 | 65.1796 | 1.75345 | 251.276 | 0.340988 | 172.923 | 108.715 | 0.742403 | 436.63 | 117.248 | 0.621545 | 140.938 | 85.9128 | 286.704 | 236.7439 | 22770.51 |
| 123466 | 14.8411 | 0.819744 | 155.021 | 1.05923 | 356.033 | 0.474866 | 120.044 | 576.179 | 0.583645 | 400.57 | 389.184 | 0.967793 | 58.437 | 60.7585 | 247.898 | 363.0815 | 23372.63 |
| 201949 | 25.8348 | 0.702314 | 146.05 | 1.66099 | 979.835 | 0.428091 | 382.873 | 526.85 | 0.858911 | 308.783 | 782.812 | 0.870041 | 28.0352 | 170.88 | 251.434 | 493.3459 | 36142.87 |
| 36893.6 | 31.762 | 0.949301 | 126.869 | 1.25723 | 362.417 | 0.55337 | 455.223 | 481.724 | 0.73063 | 147.296 | 554.518 | 0.836644 | 83.7799 | 264.397 | 74.5585 | 203.1852 | 15266.19 |
| 37628 | 30.5773 | 0.9482 | 78.6525 | 3.22763 | 356.839 | 0.231802 | 422.359 | 102.564 | 0.657876 | 193.29 | 88.801 | 0.991554 | 151.84 | 295.315 | 186.248 | 284.1773 | 31256.48 |
| 86180.6 | 19.5728 | 0.875538 | 36.4238 | 3.52091 | 337.574 | 0.52511 | 240.418 | 665.144 | 0.697046 | 453.301 | 728.766 | 0.698399 | 179.188 | 155.797 | 279.168 | 340.3641 | 21610.13 |
| 166107 | 15.3924 | 0.755939 | 113.896 | 0.643602 | 973.734 | 0.226981 | 291.017 | 215.114 | 0.743901 | 255.426 | 298.472 | 0.75334 | 52.9249 | 248.682 | 125.1 | 901.7306 | 87676.65 |
| 185743 | 26.8894 | 0.726564 | 61.5647 | 2.0972 | 311.514 | 0.531798 | 221.382 | 176.693 | 0.935439 | 152.616 | 771.463 | 0.374117 | 82.2865 | 159.512 | 68.3633 | 552.1858 | 30984.26 |
| 97682.1 | 14.1488 | 0.858325 | 84.5507 | 0.110988 | 483.299 | 0.575941 | 202.584 | 567.357 | 0.981114 | 130.629 | 700.992 | 0.834292 | 4.43462 | 114.912 | 69.3997 | 243.5203 | 15982.54 |
| 118461 | 31.1522 | 0.827247 | 136.52 | 0.103803 | 497.591 | 0.276769 | 322.067 | 849.494 | 0.866428 | 229.593 | 495.335 | 0.582797 | 1.3611 | 44.0057 | 182.73 | 870.2183 | 62804.92 |
| 102463 | 25.9482 | 0.851179 | 105.412 | 0.945556 | 471.293 | 0.400903 | 322.312 | 538.133 | 0.913765 | 196.319 | 462.642 | 0.976752 | 84.0266 | 97.4296 | 76.8574 | 286.1416 | 21317.64 |
| 145936 | 15.5641 | 0.786122 | 133.823 | 1.34334 | 26.8429 | 0.474383 | 284.98 | 349.322 | 0.757369 | 289.493 | 912.092 | 0.805705 | 15.8325 | 144.228 | 175.46 | 345.4772 | 16996.06 |
| 140050 | 16.845 | 0.79493 | 127.677 | 1.18479 | 831.94 | 0.373193 | 371.493 | 566.218 | 0.589131 | 282.627 | 855.46 | 0.956639 | 23.8845 | 181.598 | 205.334 | 538.3833 | 45398.27 |
| 71431.6 | 30.4892 | 0.897618 | 73.8136 | 0.39845 | 772.086 | 0.583904 | 246.515 | 611.137 | 0.773338 | 165.936 | 395.947 | 0.977773 | 35.431 | 210.353 | 148.852 | 216.2651 | 16401.55 |
| 177717 | 31.0382 | 0.738577 | 148.094 | 1.36791 | 46.2897 | 0.506945 | 380.387 | 501.942 | 0.773028 | 516.124 | 164.26 | 0.511999 | 103.68 | 136.274 | 335.799 | 569.1429 | 26639.65 |
| 62663.9 | 18.0642 | 0.910726 | 160.529 | 0.858194 | 846.942 | 0.572198 | 247.277 | 168.084 | 0.62055 | 295.736 | 260.733 | 0.631528 | 34.0927 | 230.877 | 209.818 | 324.7309 | 30706.01 |
| 161662 | 22.9608 | 0.762594 | 154.262 | 1.47877 | 445.45 | 0.67994 | 365.215 | 896.798 | 0.970002 | 278.572 | 722.839 | 0.765468 | 22.9314 | 333.322 | 270.508 | 337.2388 | 18039.75 |
| 176148 | 17.2107 | 0.740916 | 130.109 | 1.90576 | 773.709 | 0.502318 | 249.861 | 904.015 | 0.722739 | 159.952 | 589.645 | 0.413295 | 71.1172 | 183.753 | 79.4384 | 840.3135 | 59029.61 |
| 63559.6 | 21.1801 | 0.909388 | 116.933 | 1.38127 | 501.698 | 0.308844 | 368.177 | 321.746 | 0.647982 | 301.903 | 112.152 | 0.631694 | 120.319 | 333.091 | 275.2 | 471.3422 | 47144.68 |
| 81762.1 | 27.5548 | 0.882157 | 135.35 | 0.119434 | 999.673 | 0.446493 | 232.184 | 550.012 | 0.338928 | 401.478 | 481.473 | 0.67928 | 9.10193 | 208.401 | 193.319 | 935.6762 | 90678.34 |
| 115715 | 30.5599 | 0.831355 | 38.225 | 1.43111 | 426.953 | 0.450888 | 356.981 | 771.811 | 0.604673 | 192.489 | 74.5275 | 0.572362 | 37.3891 | 323.153 | 68.3767 | 523.6586 | 37783.48 |
| 177729 | 28.3686 | 0.738556 | 43.4029 | 0.814241 | 281.467 | 0.350517 | 128.726 | 627.946 | 0.476636 | 232.974 | 50.5811 | 0.583933 | 64.2351 | 119.223 | 139.606 | 954.9767 | 57656.89 |
| 58439.9 | 18.035 | 0.917046 | 31.8557 | 1.56735 | 500.046 | 0.132772 | 303.352 | 611.784 | 0.977564 | 348.526 | 421.672 | 0.678046 | 47.5 | 265.821 | 246.347 | 838.2822 | 91472.34 |
| 115273 | 26.8538 | 0.832012 | 154.03 | 0.253364 | 496.839 | 0.513789 | 456.878 | 282.901 | 0.56014 | 165.869 | 829.257 | 0.584498 | 14.9191 | 447.181 | 165.206 | 634.0553 | 42583.88 |
| 69869.1 | 16.44 | 0.899943 | 88.3475 | 2.03068 | 617.767 | 0.423447 | 239.71 | 632.535 | 0.585189 | 491.014 | 9.67466 | 0.452367 | 48.3488 | 48.7273 | 215.655 | 576.2446 | 55726.15 |
| 80697.7 | 25.8242 | 0.883747 | 34.7719 | 3.03892 | 536.284 | 0.265313 | 184.184 | 365.167 | 0.609958 | 489.007 | 246.158 | 0.935434 | 26.1596 | 130.462 | 373.759 | 433.8245 | 43235.92 |
| 48699.1 | 23.7176 | 0.931626 | 157.402 | 1.36142 | 544.17 | 0.603268 | 495.38 | 857.709 | 0.328757 | 421.502 | 72.3664 | 0.490121 | 50.1827 | 406.339 | 96.8155 | 653.1437 | 54337.32 |
| 149134 | 17.1171 | 0.781337 | 103.834 | 1.38304 | 192.881 | 0.430362 | 158.405 | 258.398 | 0.995172 | 438.997 | 770.265 | 0.280808 | 114.881 | 137.666 | 126.391 | 702.2987 | 40265.01 |
| 155404 | 32.6887 | 0.771969 | 152.948 | 0.996694 | 497.957 | 0.723746 | 479.925 | 480.857 | 0.793485 | 391.855 | 557.816 | 0.641949 | 21.5699 | 187.819 | 103.446 | 363.2865 | 19564.47 |
| 134120 | 25.5129 | 0.80381 | 111.611 | 2.169 | 10.5355 | 0.413902 | 446.569 | 403.495 | 0.758473 | 184.245 | 441.442 | 0.746373 | 137.792 | 432.666 | 112.796 | 330.1863 | 16236.82 |
| 131409 | 19.7365 | 0.807861 | 85.8396 | 0.640604 | 250.143 | 0.407472 | 377.459 | 783.49 | 0.419586 | 321.711 | 526.693 | 0.642767 | 45.9669 | 363.59 | 64.2752 | 730.3532 | 45905.21 |
| 167508 | 29.0004 | 0.753851 | 89.7785 | 3.15679 | 431.898 | 0.261324 | 264.143 | 482.852 | 0.60195 | 473.956 | 697.813 | 0.95941 | 13.1142 | 61.2162 | 207.152 | 670.2489 | 47484.78 |
| 133098 | 22.1268 | 0.805335 | 164.09 | 0.615109 | 900.455 | 0.63162 | 444.635 | 652.396 | 0.839253 | 496.822 | 757.574 | 0.375712 | 26.7015 | 143.232 | 323.735 | 684.463 | 46338.95 |
| 145201 | 28.9881 | 0.787231 | 90.9137 | 2.24185 | 177.038 | 0.322131 | 197.903 | 570.839 | 0.733373 | 177.804 | 648.179 | 0.963536 | 57.6953 | 54.0265 | 77.4921 | 404.0739 | 23451.02 |
| 62174.5 | 30.0633 | 0.91147 | 85.99 | 3.11225 | 331.468 | 0.465867 | 112.113 | 1.09591 | 0.942822 | 504.976 | 288.826 | 0.192855 | 44.1696 | 71.2828 | 469.68 | 539.4015 | 46430.94 |
| 59074.1 | 30.0281 | 0.916109 | 166.112 | 0.323517 | 816.947 | 0.5215 | 80.1745 | 282.943 | 0.338555 | 354.977 | 465.946 | 0.720587 | 31.3468 | 58.4615 | 60.8585 | 635.4956 | 59185.04 |
| 73784.4 | 14.9218 | 0.894084 | 27.1443 | 2.15563 | 879.734 | 0.462385 | 499.09 | 986.011 | 0.71829 | 114.209 | 887.638 | 0.589115 | 119.278 | 267.978 | 108.647 | 489.3158 | 43610.81 |
| 108668 | 15.7274 | 0.841887 | 25.7972 | 2.98067 | 501.541 | 0.220894 | 250.315 | 147.686 | 0.654178 | 464.541 | 60.5292 | 0.685644 | 82.49 | 117.056 | 93.5786 | 672.9678 | 64337.52 |
| 64254.4 | 16.6049 | 0.908345 | 150.691 | 2.61559 | 431.571 | 0.398866 | 181.933 | 79.9061 | 0.949455 | 311.402 | 187.861 | 0.578681 | 167.635 | 90.5954 | 199.283 | 260.8881 | 23711.31 |
| 124479 | 20.0733 | 0.818231 | 87.8518 | 1.29502 | 899.472 | 0.37987 | 267.298 | 565.12 | 0.793203 | 414.157 | 450.782 | 0.35665 | 2.37233 | 65.4387 | 384.037 | 887.5311 | 84347.69 |
| 41552.2 | 24.8384 | 0.942322 | 132.946 | 1.42185 | 82.6875 | 0.201554 | 146.881 | 29.1498 | 0.67274 | 390.777 | 728.681 | 0.597344 | 19.5322 | 126.184 | 117.142 | 519.2897 | 38018.83 |
| 125833 | 23.506 | 0.816208 | 79.294 | 0.372923 | 990.411 | 0.459374 | 472.445 | 640.474 | 0.298928 | 153.259 | 351.449 | 0.744933 | 33.4735 | 84.1176 | 59.5258 | 909.4103 | 85298.81 |
| 139385 | 24.5802 | 0.79593 | 32.0723 | 0.838823 | 516.803 | 0.29479 | 391.499 | 880.036 | 0.994026 | 260.161 | 424.321 | 0.976722 | 8.63634 | 142.747 | 72.6304 | 480.006 | 35962.74 |
| 163432 | 18.2846 | 0.759944 | 44.3872 | 3.5856 | 809.149 | 0.404713 | 234.437 | 840.983 | 0.392993 | 513.933 | 288.866 | 0.885125 | 44.9979 | 189.666 | 245.695 | 710.5607 | 59998.95 |
| 78099.6 | 23.9017 | 0.887633 | 129.101 | 1.54024 | 986.551 | 0.455939 | 434.723 | 691.316 | 0.478067 | 175.869 | 9.36872 | 0.565183 | 97.2235 | 300.184 | 93.571 | 655.1266 | 68412.35 |
| 100018 | 25.1213 | 0.854837 | 51.1296 | 1.00687 | 577.191 | 0.411118 | 162.101 | 870.297 | 0.396352 | 330.723 | 26.5702 | 0.537188 | 93.7218 | 80.6305 | 274.666 | 840.4439 | 72822.55 |
| 112532 | 29.0223 | 0.836116 | 158.674 | 1.41765 | 545.231 | 0.683364 | 402.72 | 31.4205 | 0.945223 | 224.04 | 906.39 | 0.512703 | 90.0642 | 113.457 | 60.6393 | 307.7866 | 18623.71 |
| 182212 | 14.6738 | 0.73184 | 88.8693 | 3.18308 | 17.0319 | 0.523915 | 151.693 | 595.785 | 0.933538 | 432.712 | 563.785 | 0.877173 | 126.167 | 138.445 | 91.0776 | 260.7617 | 12354.1 |
| 48209.3 | 34.0072 | 0.932372 | 129.853 | 2.28593 | 136.816 | 0.281849 | 286.86 | 664.439 | 0.910374 | 354.237 | 12.654 | 0.43514 | 86.6333 | 122.403 | 292.382 | 489.1025 | 35037.26 |
| 169472 | 32.0122 | 0.750916 | 161.938 | 2.07309 | 747.847 | 0.558678 | 455.296 | 28.9609 | 0.738977 | 324.938 | 188.99 | 0.837474 | 167.378 | 326.656 | 115.623 | 325.2264 | 22269.14 |
| 148382 | 18.5412 | 0.782463 | 142.369 | 0.58244 | 609.81 | 0.235714 | 448.274 | 646.652 | 0.635695 | 400.142 | 23.1206 | 0.768593 | 3.64578 | 170.766 | 104.554 | 948.2831 | 76171.62 |
| 177684 | 28.1611 | 0.738625 | 128.005 | 2.33413 | 837.539 | 0.644161 | 217.377 | 463.552 | 0.759315 | 237.683 | 23.9992 | 0.827127 | 172.614 | 169.934 | 160.342 | 298.2159 | 18386.13 |
| 77526 | 27.5284 | 0.888495 | 149.295 | 2.93342 | 756.015 | 0.507751 | 456.37 | 143.362 | 0.528352 | 375.943 | 344.651 | 0.868918 | 47.9067 | 421.089 | 288.354 | 304.4698 | 28725.71 |
| 75572.7 | 20.5074 | 0.891412 | 169.172 | 1.52414 | 600.167 | 0.371883 | 346.133 | 802.888 | 0.676229 | 181.114 | 304.796 | 0.439041 | 88.9054 | 124.249 | 167.989 | 794.0197 | 68499.55 |
| 70848.7 | 26.028 | 0.898485 | 154.012 | 0.569265 | 18.5876 | 0.610881 | 219.29 | 285.498 | 0.279942 | 107.504 | 587.712 | 0.606969 | 9.85935 | 163.112 | 80.2897 | 604.108 | 33954.26 |
| 141905 | 26.1824 | 0.792161 | 45.2428 | 2.00621 | 842.271 | 0.491697 | 449.399 | 92.0194 | 0.893969 | 499.642 | 128.956 | 0.571037 | 40.8584 | 224.846 | 85.1239 | 340.6913 | 29582.05 |
| 52617.1 | 15.9412 | 0.925758 | 57.8238 | 3.7315 | 280.716 | 0.43181 | 141.444 | 384.83 | 0.926 | 194.288 | 117.449 | 0.214501 | 57.8637 | 113.215 | 166.999 | 603.2991 | 48474.68 |
| 98585.2 | 22.9699 | 0.856979 | 124.64 | 1.43143 | 37.602 | 0.218102 | 396.921 | 835.514 | 0.781933 | 390.237 | 470.282 | 0.68094 | 61.5908 | 107.931 | 233.948 | 597.2568 | 32633.23 |
| 64572.2 | 26.3543 | 0.907877 | 77.2542 | 0.195269 | 942.295 | 0.380042 | 350.654 | 600.439 | 0.34343 | 455.481 | 337.191 | 0.819483 | 18.0657 | 184.535 | 157.991 | 709.2033 | 80916.04 |
| 201610 | 19.1985 | 0.702817 | 151.872 | 0.531261 | 832.597 | 0.640706 | 388.628 | 643.347 | 0.875375 | 191.217 | 497.281 | 0.739588 | 43.3889 | 203.901 | 76.5339 | 399.3966 | 23856.36 |
| 76546.1 | 14.0519 | 0.889951 | 86.6292 | 1.73494 | 490.621 | 0.222252 | 126.423 | 79.47 | 0.52188 | 186.193 | 673.728 | 0.69286 | 102.025 | 76.7848 | 79.8211 | 739.3182 | 76037.6 |
| 147847 | 21.8231 | 0.783266 | 27.1668 | 3.69498 | 263.858 | 0.503276 | 406.841 | 941.642 | 0.517003 | 250.926 | 29.8338 | 0.571717 | 77.7159 | 186.788 | 208.877 | 584.4935 | 34419.14 |
| 199316 | 21.9293 | 0.706251 | 130.253 | 0.454261 | 847.881 | 0.47082 | 354.944 | 53.4154 | 0.826661 | 426.876 | 852.193 | 0.365951 | 38.6286 | 289.706 | 99.9424 | 928.7571 | 65724.35 |
| 71962.9 | 25.2773 | 0.896817 | 87.5713 | 1.43619 | 848.099 | 0.458975 | 354.076 | 232.091 | 0.653621 | 279.699 | 758.378 | 0.709315 | 10.3948 | 143.669 | 118.432 | 357.8489 | 35908.96 |
| 179385 | 33.8896 | 0.736085 | 138.962 | 0.138221 | 798.409 | 0.754572 | 182.203 | 359.658 | 0.20313 | 298.064 | 877.618 | 0.980377 | 2.21439 | 152.069 | 158.836 | 932.0535 | 52172.06 |
| 185588 | 25.3931 | 0.726795 | 112.907 | 1.09062 | 117.632 | 0.317057 | 419.157 | 188.394 | 0.737845 | 291.468 | 47.6202 | 0.702684 | 104.388 | 93.1293 | 221.655 | 560.3039 | 28581.62 |
| 95818.6 | 14.372 | 0.861113 | 96.0445 | 0.766002 | 573.673 | 0.307496 | 468.452 | 58.6491 | 0.801165 | 202.801 | 353.263 | 0.82134 | 41.6103 | 381.4 | 197.947 | 349.9383 | 33388.7 |
| 166099 | 21.8589 | 0.755955 | 157.925 | 0.145253 | 471.726 | 0.714387 | 451.631 | 742.726 | 0.738064 | 364.706 | 811.691 | 0.731333 | 9.3706 | 372.871 | 51.9581 | 436.5161 | 23292.22 |
| 69215.3 | 24.1345 | 0.900928 | 138.365 | 1.51329 | 124.07 | 0.276405 | 424.579 | 100.763 | 0.43626 | 193.126 | 163.617 | 0.965965 | 138.551 | 293.307 | 70.0918 | 433.3346 | 30113.45 |
| 158304 | 34.34 | 0.76763 | 132.358 | 1.97687 | 676.483 | 0.200918 | 268.903 | 705.994 | 0.863386 | 492.439 | 395.214 | 0.710975 | 59.5964 | 256.819 | 350.487 | 969.855 | 79739.34 |
| 135068 | 21.077 | 0.802387 | 112.829 | 1.79981 | 887.135 | 0.513901 | 349.146 | 228.075 | 0.825356 | 327.822 | 978.933 | 0.549254 | 22.2047 | 224.872 | 302.116 | 443.45 | 35916.52 |
| 139436 | 24.4166 | 0.795853 | 131.994 | 0.637297 | 821.892 | 0.610136 | 85.6637 | 4.44855 | 0.533938 | 342.295 | 154.402 | 0.977637 | 52.6503 | 49.9943 | 195.924 | 290.273 | 21756.45 |
| 174943 | 26.6205 | 0.742724 | 90.7881 | 1.80357 | 936.969 | 0.559351 | 139.265 | 17.4529 | 0.43513 | 454.97 | 483.428 | 0.830526 | 168.501 | 98.5686 | 268.64 | 478.0385 | 35250.12 |
| 58988.1 | 23.4141 | 0.91623 | 155.139 | 1.42131 | 241.494 | 0.207392 | 249.061 | 395.247 | 0.447656 | 424.114 | 508.791 | 0.96077 | 135.418 | 142.394 | 410.643 | 656.5856 | 53513.46 |
| 201889 | 30.9795 | 0.702408 | 69.1228 | 0.641643 | 879.339 | 0.511305 | 470.906 | 47.2921 | 0.616207 | 465.315 | 618.055 | 0.987337 | 47.2179 | 272.723 | 374.228 | 393.9518 | 28553.8 |
| 40602.7 | 16.7574 | 0.943736 | 80.6027 | 3.59506 | 74.9996 | 0.188782 | 463.281 | 450.46 | 0.669133 | 384.307 | 677.671 | 0.397453 | 150.981 | 424.711 | 366.409 | 752.6981 | 54820.99 |
| 79383.6 | 26.482 | 0.885714 | 69.9053 | 0.976462 | 589.187 | 0.243749 | 348.224 | 409.681 | 0.420498 | 515.897 | 603.905 | 0.778297 | 19.8422 | 209.863 | 324.921 | 844.021 | 87926.03 |
| 171655 | 34.244 | 0.747653 | 158.699 | 0.176938 | 893.122 | 0.554733 | 148.035 | 871.512 | 0.990516 | 164.81 | 109.355 | 0.71649 | 4.92229 | 76.2478 | 133.508 | 460.7521 | 29256.7 |
| 118851 | 22.6456 | 0.826654 | 149.924 | 2.13423 | 810.164 | 0.631974 | 467.745 | 749.5 | 0.787976 | 493.144 | 469.614 | 0.544848 | 166.853 | 240.485 | 393.582 | 443.86 | 28839.31 |
| 62196.6 | 29.9187 | 0.911436 | 159.706 | 2.33527 | 998.914 | 0.442353 | 403.6 | 183.907 | 0.951559 | 326.401 | 345.089 | 0.708488 | 130.482 | 272.435 | 201.104 | 275.2597 | 29475.83 |
| 193616 | 31.4 | 0.714788 | 158.96 | 0.843122 | 985.942 | 0.39256 | 316.87 | 657.622 | 0.897806 | 272.628 | 218.132 | 0.599947 | 37.1843 | 277.632 | 52.2583 | 764.4625 | 56281.13 |
| 44366.5 | 14.1912 | 0.938103 | 161.749 | 0.611915 | 245.916 | 0.366519 | 255.036 | 955.688 | 0.757325 | 364.804 | 26.3385 | 0.541578 | 11.2272 | 217.923 | 267.293 | 469.2166 | 35318.71 |
| 84219.4 | 14.2596 | 0.87847 | 26.4367 | 1.59889 | 676.896 | 0.398565 | 494.566 | 66.4743 | 0.323733 | 456.937 | 399.702 | 0.608865 | 120.153 | 395.534 | 249.476 | 772.8216 | 80410.58 |
| 36898.3 | 15.609 | 0.949278 | 40.5475 | 2.41593 | 746.521 | 0.396784 | 478.944 | 917.601 | 0.613668 | 69.2634 | 465.387 | 0.593088 | 160.361 | 288.675 | 69.0895 | 475.0652 | 50483.14 |
| 54064.2 | 25.7263 | 0.9236 | 87.4592 | 2.8622 | 44.7855 | 0.36739 | 184.761 | 165.662 | 0.139688 | 223.834 | 742.911 | 0.80653 | 28.2902 | 169.843 | 128.886 | 904.4382 | 58355.33 |
| 195306 | 24.6372 | 0.712253 | 155.719 | 1.99934 | 90.6268 | 0.625652 | 272.839 | 332.484 | 0.286291 | 463.968 | 975.137 | 0.849005 | 19.4986 | 212.325 | 234.265 | 754.1281 | 35093.11 |
| 174084 | 21.0215 | 0.744006 | 84.0345 | 1.8038 | 512.389 | 0.52297 | 123.926 | 718.815 | 0.660202 | 51.9156 | 446.129 | 0.476046 | 171.252 | 62.3756 | 47.3883 | 642.0838 | 40342.3 |
| 70381.7 | 19.2432 | 0.899178 | 73.1957 | 1.32407 | 445.825 | 0.40873 | 413.657 | 636.859 | 0.478984 | 519.143 | 161.871 | 0.782759 | 124.222 | 334.026 | 129.56 | 388.0245 | 34249.18 |
| 171336 | 32.2102 | 0.748127 | 99.2744 | 1.46603 | 349.017 | 0.628071 | 393.412 | 727.564 | 0.801402 | 401.585 | 80.0215 | 0.459412 | 127.969 | 311.964 | 248.248 | 567.4618 | 30125.97 |
| 103246 | 13.783 | 0.85 | 156.988 | 0.37895 | 203.564 | 0.245008 | 292.637 | 543.204 | 0.63511 | 177.333 | 143.575 | 0.726466 | 29.6537 | 84.3548 | 75.1672 | 730.8706 | 47634.06 |
| 152035 | 34.9422 | 0.777012 | 41.9712 | 2.24412 | 483.444 | 0.373221 | 58.3917 | 159.009 | 0.872795 | 72.2051 | 54.345 | 0.349431 | 61.6465 | 44.3036 | 55.0915 | 784.5133 | 57348.68 |
| 164407 | 18.6291 | 0.758484 | 27.0859 | 3.37074 | 792.917 | 0.42191 | 154.573 | 909.796 | 0.819752 | 251.585 | 156.633 | 0.324334 | 125.206 | 137.731 | 207.998 | 999.5609 | 78578.26 |
| 113477 | 22.9781 | 0.834696 | 117.254 | 1.54009 | 158.015 | 0.401886 | 230.349 | 760.786 | 0.817859 | 401.773 | 780.843 | 0.261319 | 123.736 | 194.622 | 129.017 | 983.0978 | 57492.24 |
| 84146.2 | 15.044 | 0.878579 | 63.7964 | 1.32976 | 487.102 | 0.488395 | 157.267 | 636.957 | 0.91531 | 462.103 | 929.115 | 0.386218 | 23.9153 | 59.5453 | 360.525 | 495.5756 | 36322.11 |
| 71357.5 | 16.4149 | 0.897716 | 138.943 | 0.267977 | 520.487 | 0.474565 | 300.082 | 264.955 | 0.937027 | 286.705 | 355.061 | 0.995257 | 9.16423 | 112.918 | 43.3355 | 222.5573 | 17656.26 |
| 56570.3 | 25.1525 | 0.91985 | 78.0514 | 1.11305 | 530.775 | 0.447061 | 270.164 | 630.591 | 0.96142 | 115.818 | 114.641 | 0.633421 | 92.3698 | 79.7242 | 53.6699 | 258.6979 | 22475.77 |
| 48275.6 | 25.4416 | 0.932262 | 140.282 | 0.828121 | 279.059 | 0.43719 | 462.839 | 657.43 | 0.757352 | 392.815 | 415.043 | 0.632439 | 51.4956 | 328.964 | 149.468 | 334.1412 | 24873.42 |
| 33461.6 | 17.1919 | 0.954422 | 81.3746 | 0.331192 | 218.806 | 0.296577 | 489.238 | 170.993 | 0.73209 | 344.436 | 194.158 | 0.951121 | 12.2495 | 312.373 | 167.814 | 200.8911 | 18372.48 |
| 40246 | 31.6736 | 0.944284 | 43.7506 | 1.45752 | 189.145 | 0.428299 | 268.408 | 521.258 | 0.48642 | 325.79 | 722.977 | 0.743042 | 28.7926 | 194.25 | 118.953 | 331.6851 | 24774.71 |
| 58710.4 | 31.4109 | 0.916655 | 32.7568 | 1.85956 | 794.938 | 0.358597 | 67.8495 | 125.336 | 0.615982 | 512.413 | 639.883 | 0.642103 | 171.543 | 56.0665 | 441.703 | 464.9979 | 52989.44 |
| 59777.2 | 16.8991 | 0.915045 | 79.1713 | 2.3195 | 105.211 | 0.294437 | 396.06 | 640.777 | 0.3788 | 161.069 | 493.414 | 0.99315 | 81.3788 | 135.173 | 126.873 | 423.9965 | 29213.34 |
| 63100.9 | 15.516 | 0.91007 | 41.9728 | 1.38036 | 560.568 | 0.298791 | 52.5504 | 150.564 | 0.90157 | 341.679 | 592.896 | 0.239593 | 84.5743 | 43.8284 | 330.14 | 895.3605 | 96180.22 |
| 150164 | 16.4122 | 0.779795 | 92.1792 | 2.53884 | 357.647 | 0.394935 | 294.103 | 537.341 | 0.715606 | 252.808 | 315.709 | 0.473405 | 1.05015 | 97.2465 | 61.7772 | 637.9554 | 42976.85 |
| 156840 | 29.8379 | 0.769816 | 85.6138 | 2.78481 | 28.2018 | 0.597988 | 231.754 | 726.147 | 0.48599 | 238.042 | 65.5647 | 0.947274 | 189.544 | 151.675 | 213.993 | 355.2042 | 16925.23 |
| 122839 | 32.504 | 0.820698 | 136.294 | 2.79457 | 382.863 | 0.492731 | 366.56 | 446.032 | 0.30387 | 286.642 | 950.516 | 0.682672 | 43.8709 | 168.543 | 271.418 | 817.4589 | 54823.35 |
| 102935 | 14.4807 | 0.850465 | 171.132 | 3.02726 | 461.372 | 0.256905 | 300.2 | 350.631 | 0.391989 | 178.065 | 32.3056 | 0.85869 | 65.6306 | 51.8526 | 135.874 | 873.621 | 74909.72 |
| 115873 | 31.8537 | 0.83112 | 54.9342 | 3.32116 | 151.999 | 0.543069 | 445.091 | 575.759 | 0.781295 | 143.312 | 450.151 | 0.411069 | 54.2427 | 61.1266 | 84.3804 | 478.8995 | 26711.36 |
| 153337 | 22.4094 | 0.775051 | 167.699 | 0.175016 | 950.086 | 0.405213 | 284.485 | 287.648 | 0.93606 | 399.722 | 570.26 | 0.718511 | 2.98917 | 104.324 | 318.262 | 553.1547 | 42060.77 |
| 59358.4 | 20.8418 | 0.915674 | 78.9647 | 1.30844 | 847.278 | 0.677761 | 315.133 | 605.997 | 0.825229 | 514.647 | 163.188 | 0.959782 | 125.059 | 270.01 | 341.31 | 211.7227 | 15992.6 |
| 184567 | 25.5162 | 0.728323 | 170.264 | 1.04237 | 224.918 | 0.716423 | 461.974 | 166.819 | 0.439883 | 454.166 | 309.788 | 0.422735 | 5.4226 | 109.898 | 82.2894 | 881.907 | 42763.23 |
| 87076.5 | 28.8385 | 0.874206 | 167.699 | 1.60957 | 685.271 | 0.360491 | 286.175 | 777.146 | 0.972182 | 350.317 | 686.386 | 0.63869 | 129.182 | 260.873 | 347.112 | 498.2171 | 40831.11 |
| 180112 | 21.3589 | 0.734987 | 130.108 | 2.6746 | 217.462 | 0.471668 | 266.183 | 846.99 | 0.60254 | 116.253 | 276.346 | 0.97822 | 23.7433 | 137.209 | 69.9235 | 383.2526 | 20893.57 |
| 110517 | 31.3173 | 0.839134 | 160.807 | 0.50009 | 618.584 | 0.720362 | 469.921 | 113.825 | 0.580447 | 94.8815 | 320.164 | 0.738266 | 25.7642 | 153.414 | 69.7761 | 307.9826 | 19875.05 |
| 37769.2 | 32.7248 | 0.947992 | 49.2717 | 1.88075 | 538.615 | 0.517143 | 494.722 | 743.152 | 0.281138 | 276.98 | 804.787 | 0.846905 | 69.9494 | 374.981 | 255.643 | 502.123 | 43329.49 |
| 167412 | 13.2675 | 0.753986 | 45.216 | 1.2176 | 417.777 | 0.350458 | 199.217 | 656.297 | 0.862605 | 459.613 | 278.609 | 0.755393 | 91.6028 | 63.8251 | 256.52 | 425.369 | 29171.1 |
| 91401.5 | 29.604 | 0.867735 | 127.232 | 2.36659 | 99.0597 | 0.479001 | 360.752 | 64.419 | 0.756112 | 104.796 | 858.659 | 0.699806 | 115.689 | 278.219 | 46.0944 | 274.6895 | 15952.88 |
| 80409.3 | 13.2185 | 0.88417 | 154.002 | 1.95806 | 886.474 | 0.56333 | 473.096 | 819.307 | 0.517468 | 191.213 | 202.043 | 0.959694 | 5.59899 | 367.494 | 158.093 | 311.6099 | 27332.51 |
| 74592 | 19.9611 | 0.892879 | 33.7516 | 2.75096 | 289.838 | 0.559036 | 415.557 | 570.313 | 0.857235 | 173.093 | 228.096 | 0.924808 | 186.207 | 206.232 | 154.016 | 185.4641 | 11872.43 |
| 184715 | 19.9661 | 0.728097 | 65.5273 | 0.62526 | 364.915 | 0.531434 | 302.72 | 586.103 | 0.246925 | 161.329 | 201.534 | 0.69554 | 34.3868 | 86.4437 | 71.729 | 962.9683 | 56615.04 |
| 108605 | 34.1147 | 0.841999 | 72.599 | 1.10316 | 244.87 | 0.141416 | 168.1 | 960.73 | 0.644811 | 280.933 | 183.881 | 0.983439 | 110.031 | 51.8783 | 198.359 | 954.7797 | 69354.48 |
| 114599 | 19.953 | 0.833015 | 23.7656 | 0.415157 | 806.896 | 0.383872 | 281.226 | 820.238 | 0.933561 | 501.015 | 54.4947 | 0.544145 | 13.2669 | 73.7847 | 98.971 | 499.7999 | 45039.9 |
| 147159 | 15.4305 | 0.784291 | 151.555 | 3.00146 | 945.169 | 0.280954 | 172.868 | 126.306 | 0.680481 | 297.16 | 308.596 | 0.892922 | 30.9218 | 133.913 | 143.456 | 605.0629 | 59747.97 |
| 120461 | 29.2426 | 0.824251 | 32.1493 | 2.57881 | 739.741 | 0.42568 | 396.103 | 2.73633 | 0.860597 | 446.117 | 96.1352 | 0.288805 | 88.46 | 124.369 | 277.731 | 709.5476 | 66050.58 |
| 83061.5 | 27.9159 | 0.880213 | 85.261 | 0.493628 | 539.716 | 0.421405 | 371.081 | 784.583 | 0.88956 | 131.992 | 356.088 | 0.748318 | 45.96 | 89.3325 | 131.948 | 323.5014 | 25666.06 |
| 121258 | 18.0703 | 0.82305 | 55.2533 | 0.916344 | 373.279 | 0.295428 | 385.956 | 298.576 | 0.922611 | 119.011 | 815.016 | 0.76329 | 54.8378 | 299.297 | 45.5045 | 399.5194 | 29652.92 |
| 83071.3 | 23.1828 | 0.880193 | 147.775 | 2.7776 | 221.882 | 0.481391 | 212.925 | 889.67 | 0.84217 | 124.827 | 511.585 | 0.6291 | 96.3934 | 95.4526 | 107.212 | 356.4462 | 22222.51 |
| 31046.9 | 34.66 | 0.958054 | 104.621 | 0.40977 | 620.866 | 0.24876 | 314.686 | 645.453 | 0.577988 | 429.759 | 689.759 | 0.699464 | 16.7461 | 158.974 | 282.513 | 645.8504 | 73554.84 |
| 62388.9 | 24.2141 | 0.911142 | 141.687 | 2.39512 | 947.793 | 0.505644 | 487.661 | 814.544 | 0.979382 | 302.31 | 485.482 | 0.644045 | 174.021 | 211.499 | 208.665 | 326.5863 | 28608.77 |
| 146467 | 34.7968 | 0.785344 | 131.753 | 1.83868 | 554.37 | 0.512982 | 203.624 | 699.08 | 0.405446 | 448.597 | 558.553 | 0.829922 | 14.8752 | 58.4305 | 367.948 | 615.6657 | 41489.59 |
| 172695 | 22.1751 | 0.746085 | 41.8587 | 0.483822 | 757.378 | 0.392845 | 401.16 | 344.583 | 0.718101 | 366.251 | 882.333 | 0.642519 | 13.7903 | 236.958 | 353.42 | 607.7694 | 48163.63 |
| 107389 | 30.865 | 0.843814 | 75.4271 | 0.999053 | 124.796 | 0.478116 | 428.647 | 106.998 | 0.919785 | 111.856 | 920.334 | 0.869292 | 44.5633 | 205.914 | 62.0256 | 223.2423 | 12723.01 |
| 80528.4 | 13.6822 | 0.883992 | 140.55 | 1.0063 | 65.8512 | 0.464119 | 91.657 | 403.602 | 0.303689 | 86.2792 | 474.628 | 0.814551 | 3.3113 | 50.6711 | 70.6548 | 517.412 | 30294.69 |
| 149461 | 31.6988 | 0.78086 | 84.9218 | 3.24282 | 281.55 | 0.317737 | 377.846 | 889.599 | 0.86276 | 395.904 | 145.397 | 0.621499 | 118.021 | 188.845 | 58.7118 | 572.5634 | 35870.24 |
| 142329 | 34.8764 | 0.791536 | 119.206 | 2.65938 | 951.169 | 0.52297 | 222.581 | 105.248 | 0.68554 | 122.344 | 44.0937 | 0.629642 | 66.9758 | 88.1079 | 97.2069 | 400.6561 | 34700.25 |
| 37892.9 | 21.7845 | 0.947794 | 102.554 | 2.86191 | 608.685 | 0.238301 | 231.532 | 312.341 | 0.661987 | 207.859 | 902.194 | 0.914073 | 153.939 | 212.93 | 150.74 | 427.1113 | 49010.59 |
| 116373 | 25.5692 | 0.830365 | 126.889 | 1.30979 | 150.388 | 0.60829 | 266.531 | 185.826 | 0.553801 | 498.16 | 747.987 | 0.635953 | 102.487 | 65.9105 | 232.75 | 385.631 | 20878.85 |
| 145159 | 30.4722 | 0.787296 | 144.515 | 3.22523 | 205.236 | 0.674295 | 314.499 | 345.871 | 0.820444 | 376.044 | 902.4 | 0.987078 | 320.179 | 196.421 | 203.394 | 268.0653 | 13848.87 |
| 191036 | 18.8389 | 0.718638 | 63.039 | 0.503959 | 864.155 | 0.25363 | 486.598 | 623.424 | 0.726013 | 470.907 | 117.516 | 0.660019 | 36.4606 | 50.7758 | 448.631 | 931.3547 | 83638.48 |
| 154609 | 23.5069 | 0.773148 | 89.0186 | 1.24265 | 845.619 | 0.22868 | 315.744 | 160.434 | 0.833584 | 478.46 | 234.345 | 0.687123 | 80.8533 | 109.665 | 295.42 | 748.0926 | 73766.86 |
| 156527 | 21.3184 | 0.770277 | 150.837 | 1.99956 | 81.1581 | 0.237667 | 438.929 | 967.304 | 0.604627 | 176.048 | 54.9254 | 0.808231 | 129.244 | 198.476 | 113.688 | 788.5418 | 40628.39 |
| 105002 | 22.8891 | 0.847377 | 114.766 | 1.21374 | 107.323 | 0.235467 | 150.34 | 58.4536 | 0.631195 | 260.398 | 713.398 | 0.469809 | 14.0206 | 136.882 | 131.666 | 880.9499 | 53677.38 |
| 138560 | 22.2622 | 0.797163 | 142.084 | 0.857074 | 802.21 | 0.359289 | 460.16 | 693.384 | 0.78709 | 165.975 | 740.436 | 0.477069 | 24.0852 | 51.7725 | 70.6248 | 895.5006 | 72631.62 |
| 35889.6 | 33.3279 | 0.950806 | 65.2459 | 1.77955 | 521.589 | 0.428026 | 457.421 | 440.409 | 0.654483 | 165.995 | 20.6654 | 0.57511 | 167.506 | 252.037 | 62.272 | 314.0989 | 32523.59 |
| 139524 | 31.327 | 0.795729 | 111.873 | 0.149744 | 414.191 | 0.703658 | 189.545 | 104.388 | 0.276618 | 475.006 | 277.563 | 0.704694 | 8.03441 | 127.724 | 67.8403 | 674.2449 | 38744.12 |
| 109617 | 32.9843 | 0.840482 | 115.022 | 1.81551 | 704.534 | 0.5262 | 158.529 | 798.571 | 0.756092 | 324.214 | 145.029 | 0.900248 | 4.91831 | 75.1038 | 272.225 | 276.6088 | 21323.57 |
| 197582 | 25.7828 | 0.708847 | 78.0229 | 2.88566 | 32.0334 | 0.354788 | 181.542 | 313.382 | 0.691761 | 507.275 | 395.913 | 0.980959 | 11.99 | 109.985 | 490.567 | 398.9877 | 18354.97 |
| 87343.4 | 18.8391 | 0.873798 | 32.4897 | 0.534292 | 409.391 | 0.482009 | 453.5 | 860.643 | 0.919555 | 413.507 | 516.067 | 0.771072 | 44.5974 | 344.479 | 373.674 | 272.0973 | 18846.79 |
| 87731.6 | 14.1295 | 0.873214 | 157.212 | 2.70341 | 990.559 | 0.441291 | 334.371 | 343.049 | 0.434479 | 140.877 | 835.586 | 0.616845 | 119.999 | 148.588 | 129.259 | 728.9157 | 73939.02 |
| 132802 | 33.732 | 0.80579 | 69.9306 | 3.43423 | 432.913 | 0.361709 | 210.018 | 398.682 | 0.652802 | 358.158 | 382.691 | 0.952908 | 136.327 | 81.3349 | 196.527 | 392.7596 | 28543.65 |
| 43957.4 | 18.503 | 0.938717 | 146.968 | 0.899039 | 589.769 | 0.460996 | 404.191 | 965.055 | 0.184562 | 485.541 | 516.057 | 0.743395 | 69.4371 | 346.299 | 264.323 | 964.8356 | 94963.54 |
| 104984 | 31.6137 | 0.847413 | 129.972 | 1.69913 | 467.038 | 0.504506 | 313.601 | 392.733 | 0.910644 | 265.239 | 260.174 | 0.187893 | 168.086 | 260.68 | 90.4119 | 965.7317 | 69230.29 |
| 86339 | 19.4512 | 0.875301 | 156.446 | 1.97322 | 29.4668 | 0.48611 | 459.094 | 884.803 | 0.673349 | 293.491 | 794.693 | 0.682718 | 109.526 | 45.3413 | 133.075 | 400.2246 | 21514.86 |
| 93259.1 | 13.1296 | 0.864943 | 161.679 | 2.54195 | 920.489 | 0.575354 | 337.53 | 470.628 | 0.789432 | 434.662 | 630.804 | 0.355145 | 164.28 | 136.702 | 66.689 | 579.0662 | 47491.53 |
| 176983 | 21.1579 | 0.739668 | 97.5427 | 1.86847 | 495.566 | 0.516268 | 357.123 | 378.204 | 0.438445 | 490.338 | 246.225 | 0.520257 | 81.9146 | 231.693 | 160.891 | 766.4992 | 49989.43 |
| 116174 | 13.6944 | 0.830655 | 61.5558 | 3.52873 | 386.029 | 0.277555 | 54.1023 | 864.187 | 0.955758 | 332.581 | 704.906 | 0.958947 | 160.847 | 42.3222 | 308.913 | 441.734 | 32053.18 |
| 190044 | 19.0462 | 0.720123 | 23.6632 | 1.73555 | 334.676 | 0.285236 | 413.026 | 985.705 | 0.912688 | 475.342 | 39.3025 | 0.774823 | 68.6869 | 369.739 | 413.04 | 526.9043 | 33240.28 |
| 97548.7 | 15.432 | 0.858525 | 153.234 | 0.717684 | 840.677 | 0.646215 | 287.971 | 601.293 | 0.605398 | 279.195 | 774.504 | 0.678066 | 68.5934 | 262.069 | 217.982 | 403.4915 | 29126.77 |
| 195169 | 19.9296 | 0.712454 | 137.035 | 0.714443 | 133.679 | 0.35663 | 336.468 | 235.623 | 0.562709 | 135.927 | 227.774 | 0.65797 | 41.7144 | 178.332 | 62.6656 | 808.6117 | 40409.81 |
| 179464 | 18.4934 | 0.735955 | 117.034 | 0.919006 | 934.692 | 0.402653 | 151.115 | 149.109 | 0.48803 | 240.754 | 679.573 | 0.719405 | 11.337 | 88.1628 | 55.2519 | 812.766 | 67983.65 |
| 80704.7 | 23.9992 | 0.883735 | 129.207 | 1.13576 | 800.086 | 0.456041 | 76.2197 | 723.333 | 0.32831 | 518.951 | 819.045 | 0.692149 | 108.842 | 52.5533 | 223.724 | 792.7182 | 74085.16 |
| 167845 | 18.2269 | 0.75334 | 160.917 | 0.278153 | 305.906 | 0.351463 | 262.856 | 258.894 | 0.941467 | 290.687 | 502.575 | 0.835283 | 3.48565 | 95.5243 | 179.706 | 521.8094 | 30187.07 |
| 72368.6 | 25.8367 | 0.896211 | 170.245 | 2.14752 | 579.875 | 0.612001 | 134.414 | 946.088 | 0.852325 | 196.838 | 697.165 | 0.648552 | 26.3967 | 124.237 | 107.22 | 347.346 | 23565.57 |
| 52350.6 | 16.5245 | 0.926157 | 112.936 | 1.71512 | 255.9 | 0.198559 | 457.734 | 331.007 | 0.493117 | 185.324 | 29.0817 | 0.564989 | 120.278 | 343.028 | 111.864 | 813.4074 | 75572.05 |
| 201249 | 31.1094 | 0.703366 | 109.955 | 2.82896 | 428.718 | 0.516872 | 205.138 | 12.7584 | 0.644358 | 222.612 | 216.043 | 0.469079 | 20.5287 | 153.229 | 167.725 | 640.3578 | 38339.17 |
| 31017 | 14.0088 | 0.958078 | 29.4084 | 0.33326 | 888.867 | 0.291351 | 305.323 | 145.059 | 0.350014 | 494.758 | 749.962 | 0.978756 | 21.3463 | 252.19 | 194.578 | 599.4218 | 83890.71 |
| 33591.5 | 33.8194 | 0.954245 | 35.5931 | 1.64515 | 440.357 | 0.387213 | 455.65 | 115.393 | 0.155853 | 402.288 | 991.384 | 0.95213 | 86.1448 | 227.196 | 332.795 | 772.9135 | 82583.15 |
| 179673 | 16.1071 | 0.73564 | 17.0909 | 3.26816 | 124.688 | 0.307308 | 148.4 | 818.589 | 0.647191 | 369.751 | 680.722 | 0.59018 | 21.2624 | 77.0074 | 124.95 | 791.3598 | 41838.31 |
| 179341 | 17.1453 | 0.736138 | 153.533 | 0.500764 | 247.64 | 0.639277 | 261.386 | 516.079 | 0.875371 | 501.477 | 36.9914 | 0.515773 | 25.5826 | 127.087 | 432.582 | 437.725 | 22413.55 |
| 34073.8 | 27.8827 | 0.953515 | 52.0076 | 1.3508 | 17.9483 | 0.487381 | 334.498 | 455.678 | 0.875213 | 86.9575 | 89.3267 | 0.574496 | 28.8087 | 191.956 | 49.1798 | 179.3337 | 11181.84 |
| 194301 | 27.9204 | 0.713758 | 99.3993 | 0.207809 | 436.809 | 0.521643 | 162.33 | 134.921 | 0.431783 | 513.939 | 472.419 | 0.554716 | 9.08384 | 90.5766 | 504.554 | 921.5969 | 53616.84 |
| 194436 | 15.937 | 0.71355 | 155.83 | 2.16522 | 0.916048 | 0.338962 | 324.246 | 77.8714 | 0.534613 | 223.32 | 696.831 | 0.844625 | 59.5112 | 49.615 | 137.826 | 652.8239 | 28710.21 |
| 96869.3 | 31.0963 | 0.859555 | 81.1749 | 1.39483 | 67.2634 | 0.231163 | 398.616 | 966.077 | 0.767423 | 100.394 | 698.669 | 0.761088 | 119.367 | 191.566 | 91.6099 | 527.807 | 30078.7 |
| 118896 | 22.8978 | 0.826587 | 115.164 | 0.156907 | 39.7089 | 0.427878 | 321.74 | 603.329 | 0.540415 | 361.506 | 526.533 | 0.546042 | 14.9833 | 51.259 | 309.607 | 691.4151 | 35520.68 |
| 179144 | 29.7359 | 0.736441 | 82.0358 | 0.749932 | 703.08 | 0.232127 | 478.802 | 637.528 | 0.948111 | 64.5888 | 590.517 | 0.698166 | 41.3605 | 291.509 | 57.5225 | 790.6802 | 63625.22 |
| 190805 | 32.6014 | 0.718995 | 68.4254 | 1.1896 | 136.874 | 0.469828 | 174.672 | 456.131 | 0.893652 | 157.915 | 10.6698 | 0.586974 | 86.9691 | 154.089 | 67.9189 | 424.0054 | 21299.73 |
| 108661 | 29.449 | 0.841909 | 65.0187 | 3.7737 | 157.171 | 0.472876 | 133.946 | 190.257 | 0.716853 | 250.719 | 728.879 | 0.346295 | 172.225 | 50.1311 | 202.331 | 569.7017 | 33991.97 |
| 39164.8 | 31.453 | 0.945902 | 163.607 | 2.40637 | 770.019 | 0.274828 | 116.06 | 867.666 | 0.721291 | 417.771 | 353.917 | 0.707156 | 86.0242 | 51.8971 | 55.8631 | 557.9854 | 62206.81 |
| 194491 | 28.161 | 0.713474 | 128.173 | 1.70149 | 872.16 | 0.316358 | 365.306 | 910.938 | 0.927579 | 408.346 | 211.978 | 0.525401 | 62.1703 | 80.8841 | 242.087 | 921.0976 | 71858.71 |
| 141930 | 22.9317 | 0.79212 | 66.8402 | 1.66365 | 916.776 | 0.391313 | 181.157 | 977.694 | 0.681504 | 402.844 | 940.523 | 0.951153 | 102.257 | 169.973 | 292.042 | 485.5522 | 40701.36 |
| 152790 | 29.2563 | 0.775875 | 171.35 | 1.08321 | 613.332 | 0.271582 | 231.558 | 968.569 | 0.743401 | 306.563 | 965.837 | 0.82438 | 25.1539 | 202.381 | 174.691 | 853.8598 | 60986.25 |
| 168182 | 30.2887 | 0.752844 | 126.686 | 0.512415 | 544.766 | 0.280327 | 353.555 | 338.131 | 0.845503 | 261.159 | 341.698 | 0.640986 | 4.0651 | 110.228 | 173.719 | 785.7342 | 56037.18 |
| 60532.9 | 29.8748 | 0.913926 | 39.5274 | 1.95648 | 773.625 | 0.302434 | 258.171 | 815.73 | 0.863432 | 426.729 | 656.214 | 0.850204 | 145.998 | 228.864 | 153.941 | 391.4105 | 39752.31 |
| 81488 | 23.5468 | 0.882563 | 116.311 | 1.87347 | 974.935 | 0.344685 | 297.325 | 597.609 | 0.591157 | 303.098 | 974.226 | 0.658384 | 16.6082 | 229.651 | 203.035 | 677.6241 | 72457.86 |
| 35714.7 | 19.1353 | 0.951052 | 69.6877 | 1.49837 | 22.6319 | 0.305881 | 103.295 | 310.33 | 0.754054 | 330.945 | 424.2 | 0.367875 | 20.047 | 79.4109 | 71.3998 | 426.6865 | 27859.47 |
| 48309.4 | 32.8767 | 0.932221 | 73.669 | 3.48639 | 869.871 | 0.418669 | 264.34 | 559.903 | 0.236848 | 115.155 | 981.464 | 0.806704 | 152.455 | 86.3095 | 87.4085 | 805.7154 | 93000.37 |
| 94590.9 | 30.5796 | 0.862964 | 105.292 | 2.84799 | 209.292 | 0.4843 | 319.009 | 992.831 | 0.821854 | 398.561 | 426.252 | 0.858851 | 148.569 | 220.127 | 168.633 | 272.7207 | 16493.79 |
| 43981.5 | 17.7534 | 0.938681 | 29.4427 | 3.41586 | 81.8049 | 0.375607 | 105.383 | 800.571 | 0.294059 | 307.058 | 799.868 | 0.794507 | 129.353 | 73.0575 | 170.134 | 500.5324 | 33913.5 |
| 68345.8 | 33.7996 | 0.90224 | 99.4658 | 0.96069 | 245.555 | 0.367489 | 408.46 | 323.182 | 0.726802 | 93.1547 | 793.929 | 0.507859 | 12.2816 | 307.97 | 64.6557 | 468.3674 | 34438.76 |
| 165725 | 21.948 | 0.756515 | 129.434 | 1.07534 | 500.962 | 0.521048 | 150.584 | 724.439 | 0.3397 | 506.397 | 173.227 | 0.862862 | 26.4781 | 112.787 | 50.0979 | 670.5308 | 43217.62 |
| 118394 | 31.1031 | 0.827346 | 101.104 | 1.06711 | 757.207 | 0.40637 | 389.48 | 31.3141 | 0.537699 | 316.18 | 597.107 | 0.465163 | 52.1951 | 240.067 | 283.194 | 822.2732 | 74905.76 |
| 58510.5 | 18.9066 | 0.916941 | 32.1572 | 2.86362 | 638.67 | 0.448139 | 320.646 | 67.4181 | 0.353933 | 152.57 | 223.822 | 0.767676 | 159.812 | 240.826 | 88.8712 | 417.5091 | 44995.07 |
| 84820.8 | 31.16 | 0.877584 | 149.483 | 2.19709 | 715.197 | 0.222736 | 87.7747 | 401.119 | 0.674105 | 104.426 | 12.8645 | 0.808152 | 112.955 | 77.1788 | 57.5123 | 667.4894 | 70162.49 |
| 135149 | 18.3708 | 0.802264 | 148.542 | 1.2018 | 263.586 | 0.398597 | 451.662 | 276.063 | 0.463346 | 506.378 | 348.534 | 0.556575 | 59.2947 | 258.911 | 414.865 | 826.5236 | 51477.34 |
| 109365 | 26.6534 | 0.840852 | 127.231 | 1.12953 | 630.539 | 0.498897 | 206.451 | 558.695 | 0.939055 | 230.125 | 190.503 | 0.834507 | 87.7137 | 141.483 | 201.471 | 253.2539 | 19135.39 |
| 160737 | 16.7728 | 0.763975 | 30.6505 | 0.210837 | 123.393 | 0.522474 | 361.185 | 135.335 | 0.858879 | 257.013 | 750.785 | 0.70966 | 19.7432 | 174.367 | 62.4551 | 280.1775 | 14496.23 |
| 77884.5 | 22.6232 | 0.887954 | 119.995 | 1.00271 | 799.684 | 0.518989 | 360.799 | 26.4054 | 0.870932 | 191.28 | 527.601 | 0.885213 | 65.8624 | 346.36 | 147.517 | 196.7232 | 17995.32 |
| 177326 | 29.4473 | 0.739162 | 71.0003 | 3.34677 | 272.235 | 0.537843 | 404.633 | 524.898 | 0.446675 | 360.607 | 562.65 | 0.755886 | 83.1802 | 97.7738 | 111.996 | 552.0906 | 30495.64 |
| 172712 | 15.8472 | 0.746057 | 17.598 | 0.610281 | 462.7 | 0.273521 | 464.567 | 965.818 | 0.521406 | 168.526 | 860.993 | 0.861114 | 44.6454 | 71.769 | 81.7096 | 826.0398 | 59586.14 |
| 69607.9 | 27.6854 | 0.900344 | 80.5695 | 1.19512 | 24.4678 | 0.35439 | 204.311 | 312.073 | 0.517375 | 69.084 | 577.774 | 0.439652 | 41.2507 | 135.713 | 62.8612 | 583.3205 | 33745.4 |
| 117430 | 25.0529 | 0.828782 | 162.701 | 0.438807 | 573.167 | 0.49477 | 241.936 | 170.68 | 0.732083 | 289.412 | 495.207 | 0.536276 | 17.0757 | 181.487 | 193.546 | 533.2685 | 37931 |
| 45851.8 | 18.321 | 0.935883 | 53.4893 | 2.2078 | 540.15 | 0.442255 | 184.85 | 697.445 | 0.531633 | 286.397 | 889.002 | 0.442892 | 155.339 | 88.6698 | 220.311 | 600.6195 | 55256.68 |
| 175855 | 32.6097 | 0.741365 | 144.724 | 2.15454 | 756.011 | 0.630285 | 339.334 | 628.124 | 0.838621 | 112.364 | 65.5166 | 0.862193 | 101.179 | 247.909 | 55.6024 | 281.5177 | 17748.46 |
| 64261.9 | 23.9016 | 0.908339 | 118.898 | 0.559632 | 750.136 | 0.610784 | 462.671 | 671.181 | 0.821908 | 253.919 | 288.416 | 0.203698 | 50.9507 | 300.442 | 162.758 | 864.348 | 65115.83 |
| 50489 | 27.5199 | 0.928952 | 148.692 | 2.03652 | 344.045 | 0.233502 | 209.999 | 329.504 | 0.522803 | 95.0096 | 201.144 | 0.820338 | 117.128 | 116.981 | 83.9641 | 544.4245 | 51559.48 |
| 43489.1 | 28.2641 | 0.939427 | 74.7077 | 1.8333 | 732.886 | 0.222475 | 410.233 | 41.8574 | 0.944924 | 431.389 | 532.899 | 0.674517 | 32.7682 | 331.575 | 249.376 | 432.0399 | 55679.07 |
| 62508.9 | 34.9229 | 0.910976 | 103.007 | 1.65005 | 381.819 | 0.43851 | 115.431 | 307.675 | 0.795307 | 317.013 | 847.804 | 0.341837 | 128.789 | 69.8165 | 123.875 | 535.2351 | 43107.46 |
| 142837 | 19.2075 | 0.790761 | 56.6341 | 2.70697 | 520.822 | 0.168426 | 258.647 | 641.465 | 0.953797 | 479.677 | 395.113 | 0.677062 | 81.8856 | 32.925 | 216.55 | 857.3478 | 72644.27 |
| 185494 | 25.8601 | 0.726936 | 124.523 | 1.91321 | 842.459 | 0.628233 | 346.21 | 618.896 | 0.412061 | 446.958 | 70.2918 | 0.871453 | 187.597 | 246.786 | 138.839 | 531.4005 | 32776.59 |
| 166877 | 14.5913 | 0.754787 | 55.3768 | 1.57767 | 811.012 | 0.270796 | 93.1003 | 704.257 | 0.919829 | 372.928 | 865.017 | 0.682711 | 111.116 | 74.0524 | 238.459 | 686.9333 | 59307.9 |
| 107097 | 27.9716 | 0.844247 | 60.6454 | 1.22504 | 120.382 | 0.191277 | 199.522 | 109.944 | 0.79638 | 348.686 | 49.1049 | 0.614395 | 9.90509 | 138.122 | 109.537 | 608.2781 | 38802.55 |
| 51567.8 | 25.3654 | 0.927335 | 160.416 | 1.54915 | 905.357 | 0.808427 | 483.486 | 228.598 | 0.625039 | 518.382 | 501.465 | 0.861062 | 38.3511 | 370.272 | 469.635 | 282.025 | 20019.21 |
| 141938 | 23.622 | 0.792109 | 165.642 | 0.24527 | 652.307 | 0.374113 | 131.126 | 509.103 | 0.815489 | 87.6646 | 135.565 | 0.644995 | 10.9747 | 112.692 | 81.5093 | 653.6666 | 47086.51 |
| 160471 | 28.1965 | 0.764381 | 103.345 | 2.44617 | 639.553 | 0.482119 | 326.415 | 4.20022 | 0.202887 | 363.926 | 339.858 | 0.969883 | 43.0725 | 54.9556 | 174.996 | 915.8488 | 69518.1 |
| 78733.4 | 31.8835 | 0.886694 | 105.767 | 2.3784 | 280.995 | 0.233349 | 304.202 | 417.011 | 0.929303 | 233.72 | 809.536 | 0.385138 | 135.653 | 104.034 | 148.115 | 771.9507 | 60711.32 |
| 145698 | 29.5642 | 0.786488 | 160.75 | 1.24686 | 811.87 | 0.686613 | 218.551 | 11.3724 | 0.179236 | 481.197 | 919.867 | 0.860497 | 22.9886 | 143.586 | 197.893 | 981.5453 | 64585.49 |
| 115536 | 31.6026 | 0.831623 | 148.858 | 2.12926 | 967.604 | 0.641818 | 278.166 | 790.283 | 0.739203 | 404.82 | 425.108 | 0.340194 | 19.8534 | 256.47 | 371.935 | 723.611 | 49963.59 |
| 120567 | 14.1637 | 0.824081 | 52.3252 | 2.39959 | 103.046 | 0.390271 | 158.47 | 378.575 | 0.797887 | 360.776 | 539.573 | 0.563535 | 107.798 | 69.064 | 338.865 | 398.5044 | 22538.55 |
| 162445 | 23.5281 | 0.761423 | 138.075 | 2.10214 | 835.555 | 0.235137 | 251.85 | 71.2628 | 0.859648 | 505.893 | 349.077 | 0.711323 | 68.342 | 214.033 | 485.789 | 754.6572 | 69376.5 |
| 153796 | 15.5217 | 0.774361 | 56.835 | 1.07178 | 761.923 | 0.324201 | 345.007 | 2.34633 | 0.855193 | 394.163 | 119.116 | 0.850834 | 73.941 | 216.307 | 361.179 | 362.0829 | 34113.76 |
| 66106.5 | 27.716 | 0.905583 | 64.0439 | 1.03724 | 393.443 | 0.507167 | 232.717 | 622.393 | 0.411527 | 480.645 | 61.6984 | 0.276281 | 30.0093 | 124.189 | 386.65 | 956.7536 | 75435.55 |
| 194373 | 22.6722 | 0.713648 | 45.5728 | 0.395319 | 93.7543 | 0.388689 | 236.16 | 584.99 | 0.698278 | 259.134 | 674.19 | 0.475469 | 12.4054 | 230.012 | 67.2521 | 776.6601 | 38212.12 |
| 194578 | 26.2645 | 0.713344 | 115.902 | 3.28087 | 80.4348 | 0.431138 | 169.725 | 351.962 | 0.307913 | 269.354 | 25.2538 | 0.993322 | 57.7653 | 129.342 | 209.246 | 663.4909 | 31680.55 |
| 196579 | 27.573 | 0.710351 | 158.798 | 1.24044 | 470.956 | 0.321477 | 469.724 | 769.226 | 0.752752 | 502.045 | 227.856 | 0.717058 | 31.5935 | 243.552 | 112.294 | 798.2926 | 49787.9 |
| 150179 | 18.3738 | 0.779774 | 128.5 | 0.449832 | 948.881 | 0.580606 | 468.946 | 288.537 | 0.905604 | 261.074 | 961.474 | 0.830829 | 41.7052 | 198.477 | 85.4876 | 320.815 | 22632.41 |
| 201736 | 15.8381 | 0.702627 | 64.525 | 1.06581 | 71.4925 | 0.459676 | 424.224 | 669.681 | 0.950771 | 101.485 | 217.365 | 0.70923 | 30.5266 | 69.2105 | 85.5127 | 346.7944 | 16690.38 |
| 70524.7 | 18.6794 | 0.898964 | 85.083 | 1.17568 | 334.796 | 0.476192 | 359.126 | 931.124 | 0.923591 | 339.424 | 363.68 | 0.953777 | 26.4233 | 230.856 | 215.743 | 212.0493 | 14587.17 |
| 91228.4 | 21.5748 | 0.867986 | 31.0226 | 0.276064 | 111.435 | 0.229624 | 488.452 | 748.587 | 0.906429 | 335.78 | 826.139 | 0.87839 | 23.0551 | 203.672 | 45.1482 | 437.9817 | 26803.64 |
| 54632.4 | 26.1985 | 0.922751 | 45.3388 | 3.72034 | 60.7715 | 0.404941 | 235.842 | 819.556 | 0.785851 | 381.084 | 942.469 | 0.775717 | 131.788 | 114.976 | 243.126 | 296.1505 | 17444.02 |
| 103429 | 17.9271 | 0.849727 | 42.126 | 1.17561 | 597.096 | 0.380606 | 186.529 | 285.114 | 0.284722 | 214.406 | 782.841 | 0.855632 | 13.2808 | 67.7568 | 92.2846 | 764.6611 | 69960.33 |
| 103467 | 18.3371 | 0.849671 | 164.624 | 1.14982 | 98.905 | 0.197458 | 439.305 | 546.997 | 0.78319 | 413.205 | 2.83848 | 0.812158 | 93.1577 | 243.527 | 248.845 | 644.6489 | 38058.07 |
| 195253 | 34.37 | 0.712342 | 123.082 | 1.52655 | 814.974 | 0.523658 | 360.864 | 793.705 | 0.53068 | 446.479 | 190.261 | 0.577749 | 52.0558 | 157.815 | 318.228 | 825.2414 | 55950.2 |
| 69229.9 | 31.2185 | 0.900914 | 111.363 | 1.87913 | 391.565 | 0.191475 | 316.527 | 205.099 | 0.643748 | 250.334 | 702.987 | 0.835529 | 147.375 | 212.785 | 172.548 | 596.1372 | 55841.7 |
| 60444.1 | 15.9297 | 0.914046 | 128.38 | 1.09676 | 644.311 | 0.268898 | 82.9657 | 522.807 | 0.612371 | 182.491 | 402.013 | 0.797702 | 23.532 | 52.1847 | 178.232 | 541.6864 | 57565.38 |
| 55883.9 | 27.9589 | 0.92088 | 82.9469 | 1.25924 | 123.694 | 0.551515 | 415.038 | 586.004 | 0.861234 | 311.847 | 656.23 | 0.737639 | 100.969 | 125.654 | 136.635 | 251.4831 | 14870.37 |
| 40413.7 | 21.5844 | 0.944022 | 34.8915 | 0.391772 | 768.414 | 0.439916 | 396.466 | 193.93 | 0.482212 | 81.8335 | 879.229 | 0.574938 | 13.4895 | 174.525 | 53.7012 | 481.9485 | 54871.99 |
| 148798 | 22.3181 | 0.781843 | 154.497 | 0.73496 | 775.536 | 0.554152 | 400.174 | 366.797 | 0.282152 | 150.334 | 158.403 | 0.966183 | 42.6324 | 266.225 | 120.289 | 703.5767 | 50897.97 |
| 176129 | 32.0429 | 0.740956 | 125.82 | 0.187756 | 32.9158 | 0.727573 | 129.184 | 295.181 | 0.594738 | 273.385 | 113.456 | 0.824953 | 16.4266 | 47.8668 | 51.8557 | 329.379 | 15110.63 |
| 203422 | 13.1112 | 0.700103 | 26.7118 | 0.431942 | 96.8818 | 0.453207 | 270.926 | 737.535 | 0.453431 | 326.397 | 123.937 | 0.799155 | 41.0739 | 88.5286 | 194.466 | 558.9363 | 27174.44 |
| 41804.1 | 22.5233 | 0.941943 | 166.23 | 2.44818 | 860.313 | 0.247972 | 460.821 | 42.3054 | 0.443772 | 502.606 | 981.59 | 0.870972 | 138.26 | 54.4367 | 161.332 | 753.8065 | 94355.37 |
| 103465 | 31.3859 | 0.849686 | 63.3496 | 1.7595 | 105.366 | 0.342375 | 100.361 | 413.36 | 0.793861 | 264.436 | 786.673 | 0.769623 | 134.759 | 71.0759 | 166.058 | 358.9559 | 20858.67 |
| 185219 | 32.026 | 0.727353 | 116.179 | 2.69628 | 289.442 | 0.377151 | 193.117 | 397.417 | 0.433787 | 58.778 | 280.892 | 0.842091 | 124.971 | 125.332 | 47.2574 | 713.0273 | 41946.59 |
| 61394.7 | 17.9775 | 0.912625 | 141.912 | 0.332344 | 191.729 | 0.494451 | 430.199 | 426.659 | 0.504481 | 150.385 | 418.518 | 0.64209 | 12.1715 | 298.446 | 114.428 | 409.2483 | 27782.64 |
| 82176.8 | 18.2134 | 0.881528 | 36.5772 | 2.42212 | 785.852 | 0.495839 | 353.839 | 22.9744 | 0.455461 | 147.442 | 482.807 | 0.35465 | 61.5218 | 65.3852 | 63.6263 | 734.9259 | 72796.86 |
| 202107 | 19.0812 | 0.702073 | 124.232 | 3.03109 | 439.865 | 0.425934 | 380.364 | 512.491 | 0.570475 | 133.109 | 0.724178 | 0.558676 | 24.499 | 160.663 | 128.892 | 754.3862 | 48140.22 |
| 60685.3 | 33.4772 | 0.913703 | 123.95 | 1.23737 | 946.316 | 0.448035 | 432.086 | 732.308 | 0.666928 | 464.627 | 45.0208 | 0.660226 | 116.733 | 103.674 | 144.922 | 414.8314 | 43024.85 |
| 103713 | 19.9186 | 0.849304 | 109.646 | 1.46763 | 665.133 | 0.50717 | 486.914 | 373.115 | 0.169507 | 489.201 | 711.324 | 0.963467 | 74.7919 | 114.309 | 430.868 | 856.2285 | 73240.66 |
| 39235.2 | 25.9022 | 0.94579 | 83.2582 | 1.23401 | 397.539 | 0.375467 | 407.306 | 959.538 | 0.407348 | 461.409 | 735.471 | 0.410586 | 90.5517 | 245.344 | 73.4587 | 867.5274 | 80394.85 |
| 149553 | 25.5004 | 0.780716 | 98.7846 | 3.54904 | 691.908 | 0.420513 | 345.301 | 822.164 | 0.397719 | 274.902 | 498.036 | 0.635801 | 66.1215 | 208.431 | 140.59 | 907.8326 | 72367.48 |
| 66543.5 | 26.9606 | 0.904928 | 125.331 | 3.25468 | 359.531 | 0.565429 | 337.345 | 433.465 | 0.546098 | 407.078 | 519.257 | 0.445179 | 305.751 | 312.052 | 356.863 | 636.4047 | 43933.17 |